|  | University of Southampton · Department of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	04src0010

Empirical formula 	C5H10Se0.50Sn

Formula weight 	228.30

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Tetragonal

Space group 	P(4

Unit cell dimensions	a = 10.60340(10) Å	( = 90°

b = 10.60340(10) Å	( = 90°

c = 6.3943(2) Å	(  = 90°

Volume	718.92(2) Å3

Z	4

Density (calculated)	2.109 Mg / m3

Absorption coefficient	5.969 mm(1

F(000)	428

Crystal	block; colourless

Crystal size	0.40 ( 0.28 ( 0.14 mm3

( range for data collection	3.72 ( 27.49°

Index ranges	(13 ( h ( 13, (13 ( k ( 13, (8 ( l ( 8

Reflections collected	9987

Independent reflections	1655 [Rint = 0.1240]

Completeness to ( = 27.49°	99.2 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.4887 and 0.1987

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	1655 / 0 / 65

Goodness-of-fit on F2	1.191

Final R indices [F2 > 2((F2)]	R1 = 0.0369, wR2 = 0.0886

R indices (all data)	R1 = 0.0369, wR2 = 0.0887

Absolute structure parameter	0.13(2)

Extinction coefficient	0.024(2)

Largest diff. peak and hole	1.841 and (1.771 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	4109(5)	9106(5)	1640(9)	27(1)	1

C2	4525(5)	9532(5)	3550(9)	26(1)	1

C3	2446(6)	7461(6)	(2172(11)	32(1)	1

C4	1016(6)	8384(6)	2531(12)	35(1)	1

C5	3390(6)	6015(6)	2536(12)	35(1)	1

Se1	5000	10000	(401(1)	25(1)	1

Sn1	2706(1)	7706(1)	1117(1)	23(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(C2	1.375(8)

C1(Se1	1.869(6)

C1(Sn1	2.129(5)

C2(C2i	1.414(10)

C2(H2	0.9500

C3(Sn1	2.137(7)

C3(H3A	0.9800

C3(H3B	0.9800

C3(H3C	0.9800

C4(Sn1	2.132(6)

C4(H4A	0.9800

C4(H4B	0.9800

C4(H4C	0.9800

C5(Sn1	2.137(7)

C5(H5A	0.9800

C5(H5B	0.9800

C5(H5C	0.9800

Se1(C1i	1.869(6)

C2(C1(Se1	107.0(4)

C2(C1(Sn1	126.4(4)

Se1(C1(Sn1	126.7(3)

C1(C2(C2i	117.3(3)

C1(C2(H2	121.3

C2i(C2(H2	121.3

Sn1(C3(H3A	109.5

Sn1(C3(H3B	109.5

H3A(C3(H3B	109.5

Sn1(C3(H3C	109.5

H3A(C3(H3C	109.5

H3B(C3(H3C	109.5

Sn1(C4(H4A	109.5

Sn1(C4(H4B	109.5

H4A(C4(H4B	109.5

Sn1(C4(H4C	109.5

H4A(C4(H4C	109.5

H4B(C4(H4C	109.5

Sn1(C5(H5A	109.5

Sn1(C5(H5B	109.5

H5A(C5(H5B	109.5

Sn1(C5(H5C	109.5

H5A(C5(H5C	109.5

H5B(C5(H5C	109.5

C1i(Se1(C1	91.4(3)

C1(Sn1(C4	106.6(2)

C1(Sn1(C3	109.3(2)

C4(Sn1(C3	110.5(3)

C1(Sn1(C5	106.3(2)

C4(Sn1(C5	112.8(3)

C3(Sn1(C5	111.1(3)

Symmetry transformations used to generate equivalent atoms:

(i) (x+1,(y+2,z

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	21(3) 	24(3)	35(3) 	1(2)	(3(2) 	(3(2)

C2	28(3) 	24(3)	27(3) 	2(2)	4(2) 	(8(2)

C3	26(3) 	29(3)	41(3) 	(9(3)	(4(3) 	0(2)

C4	30(3) 	36(3)	40(4) 	(6(3)	7(3) 	2(2)

C5	37(3) 	27(3)	41(4) 	5(3)	(3(3) 	(1(2)

Se1	25(1) 	25(1)	26(1) 	0	0 	(5(1)

Sn1	20(1) 	20(1)	30(1) 	0(1)	0(1) 	(2(1)