|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	04src0821   (HJ EDTT Butyl)

Empirical formula 	C10H12Br2S3

Formula weight 	388.20

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/n

Unit cell dimensions	a = 7.974(8) Å	( = 90°

b = 24.103(19) Å	( = 118.41(5)°

c = 7.837(7) Å	(  = 90°

Volume	1325(2) Å3

Z	4

Density (calculated)	1.946 Mg / m3

Absorption coefficient	6.558 mm(1

F(000)	760

Crystal	slab; colourless

Crystal size	0.38 ( 0.14 ( 0.05 mm3

( range for data collection	2.90 ( 27.49°

Index ranges	(9 ( h ( 10, (30 ( k ( 31, (9 ( l ( 10

Reflections collected	10463

Independent reflections	3000 [Rint = 0.0887]

Completeness to ( = 27.49°	98.6 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.7351 and 0.1896

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	3000 / 0 / 137

Goodness-of-fit on F2	1.041

Final R indices [F2 > 2((F2)]	R1 = 0.0806, wR2 = 0.1863

R indices (all data)	R1 = 0.1188, wR2 = 0.2070

Largest diff. peak and hole	1.393 and (1.026 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C10	15494(14)	1649(4)	3513(14)	35(2)	1

C7	12744(14)	1699(4)	6511(14)	32(2)	1

C8	13516(15)	1470(4)	5217(15)	37(2)	1

C6	9265(14)	1241(4)	8822(14)	33(2)	1

C9	14775(16)	1888(5)	4892(15)	41(2)	1

C5	11400(30)	1329(6)	6820(30)	94(7)	1

C1	8526(15)	1375(4)	10009(14)	32(2)	1

C2	7590(16)	458(4)	8674(15)	39(2)	1

C3	8722(14)	696(4)	8016(13)	32(2)	1

C4	10950(40)	857(9)	6360(50)	224(19)	1

S1	7161(4)	858(1)	10226(4)	36(1)	1

S2	9369(4)	374(1)	6428(4)	41(1)	1

S3	10724(4)	1711(1)	8411(4)	36(1)	1

Br1	8831(2)	2063(1)	11229(2)	39(1)	1

Br2	6465(2)	(248(1)	7942(2)	48(1)	1

Table 3. Bond lengths [Å] and angles [°].

C10(C9	1.556(13)

C10(H10A	0.9800

C10(H10B	0.9800

C10(H10C	0.9800

C7(C5	1.503(14)

C7(C8	1.517(12)

C7(H7A	0.9900

C7(H7B	0.9900

C8(C9	1.527(14)

C8(H8A	0.9900

C8(H8B	0.9900

C6(C1	1.357(12)

C6(C3	1.431(14)

C6(S3	1.760(10)

C9(H9A	0.9900

C9(H9B	0.9900

C5(C4	1.19(2)

C5(S3	1.825(12)

C1(S1	1.716(10)

C1(Br1	1.869(9)

C2(C3	1.361(13)

C2(S1	1.709(10)

C2(Br2	1.882(10)

C3(S2	1.741(9)

C4(S2	1.737(15)

C4(H4	0.9500

C9(C10(H10A	109.5

C9(C10(H10B	109.5

H10A(C10(H10B	109.5

C9(C10(H10C	109.5

H10A(C10(H10C	109.5

H10B(C10(H10C	109.5

C5(C7(C8	116.1(9)

C5(C7(H7A	108.3

C8(C7(H7A	108.3

C5(C7(H7B	108.3

C8(C7(H7B	108.3

H7A(C7(H7B	107.4

C7(C8(C9	112.3(9)

C7(C8(H8A	109.1

C9(C8(H8A	109.1

C7(C8(H8B	109.1

C9(C8(H8B	109.1

H8A(C8(H8B	107.9

C1(C6(C3	112.5(8)

C1(C6(S3	120.8(8)

C3(C6(S3	126.7(6)

C8(C9(C10	111.1(9)

C8(C9(H9A	109.4

C10(C9(H9A	109.4

C8(C9(H9B	109.4

C10(C9(H9B	109.4

H9A(C9(H9B	108.0

C4(C5(C7	130.4(12)

C4(C5(S3	123.2(10)

C7(C5(S3	105.9(8)

C6(C1(S1	113.4(7)

C6(C1(Br1	124.7(7)

S1(C1(Br1	121.8(5)

C3(C2(S1	115.1(8)

C3(C2(Br2	124.9(8)

S1(C2(Br2	120.0(5)

C2(C3(C6	109.6(8)

C2(C3(S2	123.9(8)

C6(C3(S2	126.4(7)

C5(C4(S2	138.0(13)

C5(C4(H4	111.0

S2(C4(H4	111.0

C2(S1(C1	89.3(5)

C3(S2(C4	101.0(6)

C6(S3(C5	103.5(5)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C10	34(5) 	41(6)	32(5) 	(1(4)	17(4) 	0(4)

C7	42(6) 	24(5)	39(5) 	0(4)	27(5) 	(4(4)

C8	45(6) 	33(6)	44(6) 	10(5)	31(5) 	6(5)

C6	40(6) 	35(6)	36(5) 	3(4)	28(5) 	4(4)

C9	50(7) 	42(6)	41(6) 	3(5)	29(5) 	(1(5)

C5	143(14) 	66(10)	164(16) 	(65(10)	146(14) 	(66(10)

C1	51(6) 	15(5)	44(5) 	(1(4)	34(5) 	2(4)

C2	52(7) 	29(6)	49(6) 	(15(5)	34(6) 	(19(5)

C3	35(5) 	41(6)	28(5) 	7(4)	20(4) 	8(4)

C4	380(40) 	125(17)	410(40) 	(180(20)	390(40) 	(180(20)

S1	44(2) 	36(1)	42(1) 	5(1)	31(1) 	0(1)

S2	59(2) 	32(1)	51(2) 	(11(1)	42(1) 	(10(1)

S3	51(2) 	26(1)	48(1) 	(5(1)	37(1) 	(6(1)

Br1	56(1) 	31(1)	45(1) 	0(1)	38(1) 	5(1)

Br2	64(1) 	40(1)	53(1) 	(6(1)	39(1) 	(18(1)