|  | University of Southampton · Department of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	00src148

Empirical formula 	C33H30ClNO3P2Pt

Formula weight 	781.06

Temperature 	150(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/c

Unit cell dimensions	a = 10.647(2) Å	( = 90°

b = 17.517(4) Å	( = 105.06(3)°

c = 16.715(3) Å	(  = 90°

Volume	3010.3(10) Å3

Z	4

Density (calculated)	1.723 Mg / m3

Absorption coefficient	4.892 mm(1

F(000)	1536

Crystal	plate; colourless

Crystal size	0.40 ( 0.10 ( 0.03 mm3

( range for data collection	3.01 ( 27.47°

Index ranges	(13 ( h ( 13, (22 ( k ( 22, (19 ( l ( 21

Reflections collected	34591

Independent reflections	6881 [Rint = 0.0603]

Completeness to ( = 27.47°	99.7 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.8875 and 0.2450

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	6881 / 0 / 373

Goodness-of-fit on F2	0.871

Final R indices [F2 > 2((F2)]	R1 = 0.0363, wR2 = 0.1003

R indices (all data)	R1 = 0.0423, wR2 = 0.1076

Extinction coefficient	0.00081(19)

Largest diff. peak and hole	3.063 and (2.924 e Å(3

Diffractometer: Enraf Nonius KappaCCD area detector (( scans and ( scans to fill Ewald sphere). Data collection and cell

refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography,

part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing,

Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Program used to solve structure:

SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Program used to refine structure: SHELXL97 (G. M. Sheldrick

(1997), University of Göttingen, Germany).

Further information:  http://www.soton.ac.uk/~xservice/strat.htm

Special details:

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

Pt1	7339(1)	1536(1)	2423(1)	17(1)	1

Cl1	5110(1)	1352(1)	2330(1)	25(1)	1

P1	9367(1)	1703(1)	2389(1)	19(1)	1

P2	7278(1)	2488(1)	3347(1)	19(1)	1

O1	8432(3)	(813(2)	(779(2)	28(1)	1

O2	7235(3)	(1597(1)	(220(2)	28(1)	1

O3	8723(3)	2797(2)	3754(2)	26(1)	1

N1	9495(3)	1194(2)	1573(2)	23(1)	1

C1	7361(4)	717(2)	1541(2)	19(1)	1

C2	6388(3)	195(2)	1211(2)	20(1)	1

C3	6499(3)	(358(2)	627(2)	22(1)	1

C4	7594(3)	(365(2)	327(2)	20(1)	1

C5	7792(3)	(928(2)	(288(2)	21(1)	1

C6	7442(4)	(2200(2)	(767(3)	31(1)	1

C7	8593(3)	156(2)	633(2)	20(1)	1

C8	8485(3)	679(2)	1238(2)	19(1)	1

C9	9844(3)	2665(2)	2184(2)	20(1)	1

C10	9233(4)	2992(2)	1418(2)	27(1)	1

C11	9492(4)	3745(3)	1259(3)	34(1)	1

C12	10380(4)	4167(2)	1854(3)	34(1)	1

C13	10982(4)	3845(3)	2605(3)	30(1)	1

C14	10722(4)	3099(2)	2781(2)	25(1)	1

C15	10653(4)	1395(2)	3272(2)	22(1)	1

C16	10372(4)	1146(2)	3997(2)	29(1)	1

C17	11372(4)	904(3)	4664(2)	36(1)	1

C18	12646(4)	921(3)	4613(3)	37(1)	1

C19	12927(4)	1171(3)	3896(3)	34(1)	1

C20	11937(4)	1405(3)	3228(3)	30(1)	1

C21	8995(5)	3403(2)	4355(3)	34(1)	1

C22	6606(3)	2266(2)	4212(2)	22(1)	1

C23	6147(4)	2833(2)	4645(2)	25(1)	1

C24	5717(4)	2647(3)	5337(2)	29(1)	1

C25	5751(4)	1903(3)	5598(2)	28(1)	1

C26	6204(4)	1322(3)	5169(2)	27(1)	1

C27	6634(4)	1515(2)	4477(2)	22(1)	1

C28	6368(4)	3311(2)	2858(2)	25(1)	1

C29	5021(5)	3327(3)	2691(3)	31(1)	1

C30	4327(5)	3934(3)	2247(3)	41(1)	1

C31	4983(6)	4526(3)	1996(3)	50(1)	1

C32	6298(6)	4517(3)	2161(3)	50(1)	1

C33	7006(5)	3909(3)	2588(3)	37(1)	1

Table 3. Bond lengths [Å] and angles [°].

Pt1(C1	2.062(3)

Pt1(P1	2.1951(11)

Pt1(P2	2.2855(10)

Pt1(Cl1	2.3590(11)

P1(N1	1.663(3)

P1(C15	1.816(4)

P1(C9	1.818(4)

P2(O3	1.606(3)

P2(C28	1.809(4)

P2(C22	1.814(3)

O1(C5	1.211(5)

O2(C5	1.331(5)

O2(C6	1.452(4)

O3(C21	1.439(5)

N1(C8	1.404(4)

C1(C2	1.385(5)

C1(C8	1.417(5)

C2(C3	1.402(5)

C3(C4	1.384(5)

C4(C7	1.394(5)

C4(C5	1.479(5)

C7(C8	1.390(5)

C9(C10	1.399(5)

C9(C14	1.402(5)

C10(C11	1.388(6)

C11(C12	1.393(6)

C12(C13	1.373(6)

C13(C14	1.384(6)

C15(C20	1.388(6)

C15(C16	1.392(5)

C16(C17	1.392(6)

C17(C18	1.381(6)

C18(C19	1.381(6)

C19(C20	1.382(6)

C22(C27	1.387(5)

C22(C23	1.390(5)

C23(C24	1.389(5)

C24(C25	1.371(6)

C25(C26	1.401(6)

C26(C27	1.391(5)

C28(C33	1.386(6)

C28(C29	1.388(7)

C29(C30	1.393(7)

C30(C31	1.376(7)

C31(C32	1.356(8)

C32(C33	1.391(7)

C1(Pt1(P1	83.08(11)

C1(Pt1(P2	176.98(10)

P1(Pt1(P2	96.97(4)

C1(Pt1(Cl1	93.20(11)

P1(Pt1(Cl1	174.84(3)

P2(Pt1(Cl1	86.57(4)

N1(P1(C15	107.62(18)

N1(P1(C9	104.84(16)

C15(P1(C9	103.87(18)

N1(P1(Pt1	103.94(12)

C15(P1(Pt1	118.55(13)

C9(P1(Pt1	116.96(12)

O3(P2(C28	105.35(18)

O3(P2(C22	105.51(15)

C28(P2(C22	104.74(17)

O3(P2(Pt1	109.90(10)

C28(P2(Pt1	112.48(13)

C22(P2(Pt1	117.91(13)

C5(O2(C6	116.2(3)

C21(O3(P2	122.8(3)

C8(N1(P1	117.0(2)

C2(C1(C8	116.2(3)

C2(C1(Pt1	126.7(3)

C8(C1(Pt1	117.2(3)

C1(C2(C3	122.9(3)

C4(C3(C2	119.4(3)

C3(C4(C7	119.7(3)

C3(C4(C5	122.9(3)

C7(C4(C5	117.3(3)

O1(C5(O2	123.1(4)

O1(C5(C4	124.5(3)

O2(C5(C4	112.3(3)

C8(C7(C4	120.0(3)

C7(C8(N1	121.0(3)

C7(C8(C1	121.8(3)

N1(C8(C1	117.2(3)

C10(C9(C14	119.7(4)

C10(C9(P1	117.7(3)

C14(C9(P1	122.4(3)

C11(C10(C9	119.8(4)

C10(C11(C12	120.0(4)

C13(C12(C11	120.2(4)

C12(C13(C14	120.7(4)

C13(C14(C9	119.6(4)

C20(C15(C16	119.2(4)

C20(C15(P1	119.8(3)

C16(C15(P1	120.9(3)

C15(C16(C17	119.9(4)

C18(C17(C16	120.2(4)

C17(C18(C19	119.8(4)

C18(C19(C20	120.2(4)

C19(C20(C15	120.5(4)

C27(C22(C23	119.5(3)

C27(C22(P2	118.5(3)

C23(C22(P2	121.8(3)

C24(C23(C22	120.1(4)

C25(C24(C23	120.1(4)

C24(C25(C26	120.8(4)

C27(C26(C25	118.7(4)

C22(C27(C26	120.8(3)

C33(C28(C29	119.2(4)

C33(C28(P2	119.9(4)

C29(C28(P2	120.8(3)

C28(C29(C30	120.0(5)

C31(C30(C29	119.8(5)

C32(C31(C30	120.6(4)

C31(C32(C33	120.5(5)

C28(C33(C32	120.0(5)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

Pt1	16(1) 	20(1)	15(1) 	(1(1)	6(1) 	0(1)

Cl1	18(1) 	32(1)	27(1) 	(3(1)	9(1) 	(1(1)

P1	17(1) 	23(1)	17(1) 	(4(1)	6(1) 	(2(1)

P2	19(1) 	24(1)	17(1) 	(3(1)	7(1) 	(1(1)

O1	25(1) 	35(2)	28(1) 	(8(1)	14(1) 	(5(1)

O2	33(2) 	23(2)	32(2) 	(9(1)	13(1) 	(5(1)

O3	21(1) 	36(2)	24(1) 	(9(1)	9(1) 	(3(1)

N1	20(2) 	25(2)	27(2) 	(10(1)	13(1) 	(7(1)

C1	21(2) 	21(2)	16(2) 	2(1)	7(1) 	3(1)

C2	15(2) 	25(2)	22(2) 	(1(1)	6(1) 	1(1)

C3	19(2) 	26(2)	19(2) 	(2(1)	0(1) 	(4(2)

C4	18(2) 	26(2)	15(2) 	(3(1)	3(1) 	1(1)

C5	16(2) 	23(2)	21(2) 	(3(2)	0(1) 	(2(1)

C6	32(2) 	25(2)	37(2) 	(12(2)	9(2) 	0(2)

C7	20(2) 	25(2)	17(2) 	1(1)	9(1) 	0(1)

C8	18(2) 	21(2)	16(2) 	2(1)	4(1) 	(4(1)

C9	19(2) 	24(2)	21(2) 	(5(1)	10(1) 	(1(1)

C10	21(2) 	30(2)	29(2) 	(1(2)	6(2) 	(5(2)

C11	34(2) 	37(3)	30(2) 	6(2)	6(2) 	(1(2)

C12	40(2) 	25(2)	41(2) 	(2(2)	19(2) 	(7(2)

C13	31(2) 	30(2)	30(2) 	(9(2)	11(2) 	(12(2)

C14	29(2) 	26(2)	21(2) 	(4(2)	7(2) 	(4(2)

C15	21(2) 	22(2)	22(2) 	(2(2)	5(2) 	0(2)

C16	26(2) 	35(2)	28(2) 	(3(2)	7(2) 	2(2)

C17	40(2) 	44(3)	20(2) 	4(2)	4(2) 	5(2)

C18	35(2) 	42(3)	28(2) 	(3(2)	(1(2) 	8(2)

C19	22(2) 	43(3)	36(2) 	(5(2)	5(2) 	3(2)

C20	25(2) 	34(2)	30(2) 	(3(2)	9(2) 	1(2)

C21	33(3) 	45(3)	23(2) 	(14(2)	8(2) 	(11(2)

C22	20(2) 	32(2)	16(2) 	(2(1)	7(1) 	0(2)

C23	27(2) 	27(2)	22(2) 	0(2)	9(2) 	3(2)

C24	24(2) 	46(3)	19(2) 	(2(2)	7(2) 	4(2)

C25	22(2) 	46(3)	17(2) 	3(2)	6(2) 	(2(2)

C26	28(2) 	29(2)	22(2) 	3(2)	5(2) 	(4(2)

C27	20(2) 	27(2)	17(2) 	(1(1)	4(2) 	0(1)

C28	34(2) 	24(2)	20(2) 	(2(2)	11(2) 	4(2)

C29	37(3) 	35(2)	23(2) 	(2(2)	9(2) 	11(2)

C30	48(3) 	44(3)	29(2) 	(7(2)	7(2) 	23(2)

C31	88(4) 	28(2)	26(2) 	(2(2)	4(2) 	22(3)

C32	89(4) 	26(2)	31(2) 	1(2)	8(3) 	(9(3)

C33	53(3) 	33(2)	29(2) 	(2(2)	16(2) 	(7(2)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H1	10151	1244	1367	27	1

H2	5626	212	1385	24	1

H3	5843	(716	443	27	1

H6A	7129	(2036	(1333	47	1

H6B	6980	(2649	(680	47	1

H6C	8354	(2312	(652	47	1

H7	9330	155	433	24	1

H10	8654	2705	1018	32	1

H11	9074	3967	755	41	1

H12	10565	4669	1742	40	1

H13	11570	4132	2999	36	1

H14	11128	2887	3293	30	1

H16	9516	1141	4036	35	1

H17	11181	730	5145	43	1

H18	13313	765	5062	44	1

H19	13784	1183	3861	41	1

H20	12133	1570	2746	35	1

H21A	8286	3760	4238	50	1

H21B	9780	3660	4329	50	1

H21C	9100	3194	4900	50	1

H23	6127	3339	4471	30	1

H24	5405	3027	5624	35	1

H25	5471	1783	6065	34	1

H26	6218	817	5343	32	1

H27	6943	1135	4189	26	1

H29	4582	2933	2875	37	1

H30	3423	3938	2121	49	1

H31	4520	4936	1710	59	1

H32	6731	4920	1987	60	1

H33	7908	3903	2693	45	1