|  | University of Southampton · Department of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	01src054

Empirical formula 	C20.50H18.50Cl1.50N2PPdS

Formula weight 	515.48

Temperature 	150(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P(1

Unit cell dimensions	a = 9.7364(19) Å	( = 90.42(3)°

b = 13.149(3) Å	( = 99.76(3)°

c = 15.993(3) Å	(  = 91.45(3)°

Volume	2017.0(7) Å3

Z	4

Density (calculated)	1.698 Mg / m3

Absorption coefficient	1.310 mm(1

F(000)	1032

Crystal	block; colourless

Crystal size	0.08 ( 0.05 ( 0.03 mm3

( range for data collection	3.00 ( 27.45°

Index ranges	(12 ( h ( 12, (16 ( k ( 17, (20 ( l ( 20

Reflections collected	29638

Independent reflections	8956 [Rint = 0.0932]

Completeness to ( = 27.45°	97.2 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9618 and 0.9024

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	8956 / 7 / 498

Goodness-of-fit on F2	0.973

Final R indices [F2 > 2((F2)]	R1 = 0.0483, wR2 = 0.0854

R indices (all data)	R1 = 0.1139, wR2 = 0.1028

Largest diff. peak and hole	1.070 and (1.169 e Å(3

Diffractometer: Enraf Nonius KappaCCD area detector (( scans and ( scans to fill Ewald sphere). Data collection and cell

refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography,

part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing,

Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Program used to solve structure:

SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Program used to refine structure: SHELXL97 (G. M. Sheldrick

(1997), University of Göttingen, Germany).

Further information:  http://www.soton.ac.uk/~xservice/strat.htm

Special details:

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C01	5672(9)	5065(8)	4708(7)	186(8)	0.80

C20	(2841(5)	(3039(4)	230(3)	30(1)	1

C14	(4281(5)	(4160(4)	1849(3)	25(1)	1

C15	(5306(5)	(4469(4)	1162(3)	28(1)	1

C16	(6686(5)	(4245(4)	1146(3)	31(1)	1

C17	(7088(5)	(3706(4)	1814(3)	34(1)	1

C18	(6076(6)	(3407(4)	2493(3)	35(1)	1

C19	(4705(5)	(3623(4)	2515(3)	27(1)	1

C8	(2132(5)	(5408(3)	1295(3)	22(1)	1

C9	(2975(5)	(6279(4)	1267(3)	27(1)	1

C10	(2596(5)	(7158(4)	883(3)	29(1)	1

C11	(1388(5)	(7178(4)	551(3)	29(1)	1

C12	(523(5)	(6325(4)	591(3)	31(1)	1

C13	(896(5)	(5445(4)	962(3)	28(1)	1

C7	(620(5)	(3586(4)	3108(3)	25(1)	1

C4	765(5)	(2219(4)	3099(3)	23(1)	1

C3	1379(5)	(1363(4)	2802(3)	27(1)	1

C2	2342(5)	(790(4)	3363(3)	34(1)	1

C1	2715(5)	(1064(4)	4207(3)	35(1)	1

C6	2175(5)	(1948(4)	4498(3)	29(1)	1

C5	1202(5)	(2516(3)	3936(3)	24(1)	1

C21	5460(5)	1760(4)	3498(3)	32(1)	1

C22	5701(5)	(20(4)	1871(3)	24(1)	1

C23	4873(5)	711(4)	1439(3)	27(1)	1

C24	3792(5)	433(4)	801(3)	34(1)	1

C25	3514(5)	(577(4)	594(3)	34(1)	1

C26	4342(6)	(1313(4)	1015(3)	38(1)	1

C27	5445(5)	(1041(4)	1654(3)	34(1)	1

C28	7339(5)	(542(4)	3511(3)	25(1)	1

C29	6178(6)	(1028(4)	3738(3)	34(1)	1

C30	6310(6)	(1615(4)	4464(3)	42(2)	1

C31	7589(6)	(1711(4)	4968(3)	41(2)	1

C32	8754(6)	(1225(4)	4748(3)	39(1)	1

C33	8635(5)	(654(4)	4025(3)	33(1)	1

C34	9498(5)	1083(4)	2249(3)	24(1)	1

C35	10496(5)	2597(4)	2666(3)	27(1)	1

C36	10725(5)	3518(4)	3098(3)	34(1)	1

C37	11889(6)	4098(4)	3010(4)	42(2)	1

C38	12837(6)	3761(4)	2516(4)	41(2)	1

C39	12614(5)	2853(4)	2086(3)	33(1)	1

C40	11448(5)	2266(4)	2175(3)	27(1)	1

N2	(1652(4)	(4297(3)	2819(2)	23(1)	1

N1	(284(4)	(2848(3)	2635(2)	22(1)	1

N3	8573(4)	286(3)	2193(2)	28(1)	1

N4	9356(4)	1916(3)	2690(2)	26(1)	1

P1	(2454(1)	(4219(1)	1796(1)	23(1)	1

P2	7159(1)	390(1)	2673(1)	25(1)	1

S1	274(1)	(3624(1)	4147(1)	28(1)	1

S2	10933(1)	1063(1)	1733(1)	30(1)	1

Cl1	(688(1)	(1300(1)	823(1)	28(1)	1

Cl01	7113(4)	5785(3)	4812(2)	42(1)	0.40

Cl02	4281(3)	5897(2)	4597(2)	77(1)	0.80

Cl2	7468(2)	3664(1)	3656(1)	46(1)	1

Pd1	(1521(1)	(2837(1)	1367(1)	22(1)	1

Pd2	7358(1)	1959(1)	3128(1)	26(1)	1

Table 3. Bond lengths [Å] and angles [°].

C01(Cl01	1.657(12)

C01(Cl02i	1.687(10)

C01(Cl02	1.7488(12)

C20(Pd1	2.053(4)

C14(C19	1.398(6)

C14(C15	1.403(6)

C14(P1	1.798(5)

C15(C16	1.380(7)

C16(C17	1.393(7)

C17(C18	1.385(7)

C18(C19	1.367(7)

C8(C9	1.387(6)

C8(C13	1.397(6)

C8(P1	1.810(5)

C9(C10	1.391(7)

C10(C11	1.371(7)

C11(C12	1.379(7)

C12(C13	1.382(6)

C7(N1	1.303(6)

C7(N2	1.374(5)

C7(S1	1.742(5)

C4(C3	1.386(6)

C4(C5	1.395(6)

C4(N1	1.404(5)

C3(C2	1.386(6)

C2(C1	1.390(7)

C1(C6	1.380(7)

C6(C5	1.390(6)

C5(S1	1.760(5)

C21(Pd2	2.045(5)

C22(C23	1.383(7)

C22(C27	1.390(6)

C22(P2	1.812(5)

C23(C24	1.376(6)

C24(C25	1.374(7)

C25(C26	1.380(7)

C26(C27	1.388(7)

C28(C29	1.387(7)

C28(C33	1.396(7)

C28(P2	1.811(5)

C29(C30	1.389(7)

C30(C31	1.373(7)

C31(C32	1.385(8)

C32(C33	1.374(7)

C34(N4	1.321(6)

C34(N3	1.356(6)

C34(S2	1.739(5)

C35(C36	1.384(7)

C35(C40	1.388(7)

C35(N4	1.415(6)

C36(C37	1.377(7)

C37(C38	1.390(7)

C38(C39	1.367(7)

C39(C40	1.384(7)

C40(S2	1.754(5)

N2(P1	1.695(4)

N1(Pd1	2.176(4)

N3(P2	1.695(4)

N4(Pd2	2.179(4)

P1(Pd1	2.1777(14)

P2(Pd2	2.1764(14)

Cl1(Pd1	2.3834(14)

Cl02(C01i	1.687(10)

Cl2(Pd2	2.3829(15)

Cl01(C01(Cl02i	114.9(5)

Cl01(C01(Cl02	106.4(6)

Cl02i(C01(Cl02	119.3(6)

C19(C14(C15	118.0(5)

C19(C14(P1	119.5(4)

C15(C14(P1	121.5(4)

C16(C15(C14	120.8(5)

C15(C16(C17	120.4(5)

C18(C17(C16	118.7(5)

C19(C18(C17	121.4(5)

C18(C19(C14	120.8(4)

C9(C8(C13	119.1(4)

C9(C8(P1	124.7(4)

C13(C8(P1	116.1(3)

C8(C9(C10	119.4(5)

C11(C10(C9	120.8(4)

C10(C11(C12	120.5(5)

C11(C12(C13	119.2(5)

C12(C13(C8	121.0(4)

N1(C7(N2	122.4(4)

N1(C7(S1	117.1(3)

N2(C7(S1	120.5(4)

C3(C4(C5	119.2(4)

C3(C4(N1	126.3(4)

C5(C4(N1	114.6(4)

C4(C3(C2	118.7(5)

C3(C2(C1	121.5(5)

C6(C1(C2	120.3(5)

C1(C6(C5	118.0(5)

C6(C5(C4	122.1(5)

C6(C5(S1	127.8(4)

C4(C5(S1	110.0(3)

C23(C22(C27	119.7(4)

C23(C22(P2	118.6(4)

C27(C22(P2	121.6(4)

C24(C23(C22	120.4(5)

C25(C24(C23	120.3(5)

C24(C25(C26	119.8(5)

C25(C26(C27	120.4(5)

C26(C27(C22	119.4(5)

C29(C28(C33	118.8(5)

C29(C28(P2	121.0(4)

C33(C28(P2	119.4(4)

C28(C29(C30	120.3(5)

C31(C30(C29	120.2(5)

C30(C31(C32	119.9(5)

C33(C32(C31	120.2(5)

C32(C33(C28	120.5(5)

N4(C34(N3	122.1(4)

N4(C34(S2	116.4(3)

N3(C34(S2	121.5(4)

C36(C35(C40	119.9(4)

C36(C35(N4	125.4(5)

C40(C35(N4	114.7(4)

C37(C36(C35	118.5(5)

C36(C37(C38	121.2(5)

C39(C38(C37	120.5(5)

C38(C39(C40	118.5(5)

C39(C40(C35	121.3(5)

C39(C40(S2	128.4(4)

C35(C40(S2	110.2(4)

C7(N2(P1	117.6(3)

C7(N1(C4	110.2(4)

C7(N1(Pd1	114.1(3)

C4(N1(Pd1	135.6(3)

C34(N3(P2	118.5(3)

C34(N4(C35	109.9(4)

C34(N4(Pd2	113.0(3)

C35(N4(Pd2	136.7(3)

N2(P1(C14	104.9(2)

N2(P1(C8	105.8(2)

C14(P1(C8	109.1(2)

N2(P1(Pd1	102.79(14)

C14(P1(Pd1	115.28(16)

C8(P1(Pd1	117.56(16)

N3(P2(C28	106.5(2)

N3(P2(C22	104.5(2)

C28(P2(C22	107.7(2)

N3(P2(Pd2	102.14(14)

C28(P2(Pd2	113.97(15)

C22(P2(Pd2	120.55(17)

C7(S1(C5	88.1(2)

C34(S2(C40	88.8(2)

C01i(Cl02(C01	60.7(6)

C20(Pd1(N1	170.65(17)

C20(Pd1(P1	87.64(15)

N1(Pd1(P1	83.01(11)

C20(Pd1(Cl1	88.10(15)

N1(Pd1(Cl1	101.24(11)

P1(Pd1(Cl1	175.07(5)

C21(Pd2(P2	87.80(15)

C21(Pd2(N4	170.97(17)

P2(Pd2(N4	83.24(11)

C21(Pd2(Cl2	89.24(15)

P2(Pd2(Cl2	177.02(5)

N4(Pd2(Cl2	99.71(11)

Symmetry transformations used to generate equivalent atoms:

(i) (x+1,(y+1,(z+1

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C01	280(20) 	157(13)	164(13) 	(74(11)	183(14) 	(78(14)

C20	34(3) 	36(3)	21(3) 	3(2)	1(2) 	6(2)

C14	27(3) 	23(3)	25(3) 	3(2)	2(2) 	0(2)

C15	31(3) 	29(3)	26(3) 	(1(2)	6(2) 	2(2)

C16	30(3) 	34(3)	29(3) 	0(3)	1(2) 	(1(2)

C17	24(3) 	30(3)	47(3) 	5(3)	5(3) 	4(2)

C18	42(4) 	31(3)	32(3) 	(3(3)	9(3) 	4(3)

C19	24(3) 	26(3)	30(3) 	(7(2)	4(2) 	2(2)

C8	29(3) 	22(3)	15(2) 	0(2)	3(2) 	3(2)

C9	29(3) 	27(3)	23(3) 	1(2)	2(2) 	2(2)

C10	40(3) 	18(3)	30(3) 	0(2)	7(3) 	(4(2)

C11	40(3) 	22(3)	24(3) 	5(2)	2(2) 	11(2)

C12	27(3) 	38(3)	31(3) 	1(3)	10(2) 	13(3)

C13	28(3) 	25(3)	31(3) 	(2(2)	2(2) 	1(2)

C7	22(3) 	25(3)	27(3) 	(7(2)	5(2) 	2(2)

C4	18(3) 	24(3)	26(3) 	(1(2)	3(2) 	8(2)

C3	24(3) 	26(3)	30(3) 	3(2)	(1(2) 	5(2)

C2	27(3) 	27(3)	44(3) 	3(3)	(1(3) 	(4(2)

C1	27(3) 	33(3)	41(3) 	(7(3)	(7(3) 	(4(3)

C6	32(3) 	30(3)	24(3) 	(2(2)	(3(2) 	4(2)

C5	19(3) 	22(3)	30(3) 	(1(2)	0(2) 	5(2)

C21	27(3) 	42(3)	30(3) 	(3(3)	9(2) 	6(3)

C22	22(3) 	27(3)	26(3) 	6(2)	11(2) 	5(2)

C23	25(3) 	25(3)	31(3) 	3(2)	6(2) 	0(2)

C24	32(3) 	39(3)	30(3) 	7(3)	2(2) 	6(3)

C25	30(3) 	44(4)	27(3) 	(5(3)	(1(2) 	(4(3)

C26	44(4) 	27(3)	44(3) 	(6(3)	9(3) 	(4(3)

C27	37(3) 	25(3)	38(3) 	0(3)	3(3) 	2(2)

C28	25(3) 	25(3)	27(3) 	(4(2)	5(2) 	6(2)

C29	37(3) 	29(3)	35(3) 	2(3)	6(3) 	3(3)

C30	44(4) 	43(4)	43(3) 	14(3)	17(3) 	6(3)

C31	53(4) 	38(3)	34(3) 	11(3)	7(3) 	23(3)

C32	31(3) 	51(4)	34(3) 	0(3)	1(3) 	16(3)

C33	31(3) 	32(3)	37(3) 	4(3)	5(3) 	9(2)

C34	19(3) 	30(3)	23(3) 	11(2)	6(2) 	7(2)

C35	29(3) 	26(3)	26(3) 	7(2)	3(2) 	0(2)

C36	32(3) 	27(3)	43(3) 	2(3)	11(3) 	2(2)

C37	49(4) 	28(3)	50(4) 	1(3)	10(3) 	(3(3)

C38	37(3) 	33(3)	52(4) 	10(3)	9(3) 	(6(3)

C39	30(3) 	33(3)	40(3) 	12(3)	13(3) 	4(3)

C40	32(3) 	23(3)	25(3) 	7(2)	2(2) 	1(2)

N2	25(2) 	22(2)	21(2) 	4(2)	3(2) 	(2(2)

N1	21(2) 	22(2)	22(2) 	(2(2)	2(2) 	(3(2)

N3	26(2) 	24(2)	37(2) 	(6(2)	14(2) 	1(2)

N4	29(2) 	24(2)	25(2) 	(2(2)	7(2) 	4(2)

P1	24(1) 	22(1)	22(1) 	(2(1)	2(1) 	1(1)

P2	23(1) 	25(1)	26(1) 	(1(1)	4(1) 	2(1)

S1	31(1) 	29(1)	23(1) 	2(1)	(1(1) 	0(1)

S2	30(1) 	29(1)	32(1) 	2(1)	11(1) 	4(1)

Cl1	35(1) 	24(1)	26(1) 	1(1)	7(1) 	0(1)

Cl01	44(2) 	36(2)	42(2) 	(7(2)	3(2) 	(7(2)

Cl02	87(2) 	68(2)	76(2) 	13(1)	16(1) 	(14(1)

Cl2	65(1) 	25(1)	57(1) 	0(1)	36(1) 	0(1)

Pd1	24(1) 	20(1)	20(1) 	0(1)	2(1) 	2(1)

Pd2	28(1) 	25(1)	25(1) 	0(1)	7(1) 	4(1)