|  | University of Southampton · Department of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	01src103

Empirical formula 	C21H20ClN2PPdS

Formula weight 	505.27

Temperature 	150(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P(1

Unit cell dimensions	a = 7.7501(16) Å	( = 83.37(3)°

b = 9.3637(19) Å	( = 79.63(3)°

c = 14.660(3) Å	(  = 88.23(3)°

Volume	1039.5(4) Å3

Z	2

Density (calculated)	1.614 Mg / m3

Absorption coefficient	1.207 mm(1

F(000)	508

Crystal	block; pale yellow

Crystal size	0.28 ( 0.18 ( 0.18 mm3

( range for data collection	2.79 ( 27.48°

Index ranges	(10 ( h ( 10, (11 ( k ( 12, (19 ( l ( 18

Reflections collected	15539

Independent reflections	4662 [Rint = 0.0496]

Completeness to ( = 27.48°	98.1 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.8120 and 0.7286

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	4662 / 0 / 247

Goodness-of-fit on F2	1.040

Final R indices [F2 > 2((F2)]	R1 = 0.0321, wR2 = 0.0809

R indices (all data)	R1 = 0.0369, wR2 = 0.0839

Extinction coefficient	0.0083(14)

Largest diff. peak and hole	0.650 and (1.093 e Å(3

Diffractometer: Enraf Nonius KappaCCD area detector (( scans and ( scans to fill Ewald sphere). Data collection and cell

refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography,

part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing,

Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Program used to solve structure:

SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Program used to refine structure: SHELXL97 (G. M. Sheldrick

(1997), University of Göttingen, Germany).

Further information:  http://www.soton.ac.uk/~xservice/strat.htm

Special details:

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	2740(4)	8896(3)	346(2)	35(1)	1

C2	4088(3)	7809(3)	(14(2)	29(1)	1

C3	4037(4)	7239(3)	(846(2)	36(1)	1

C4	5334(4)	6313(3)	(1236(2)	39(1)	1

C5	6796(4)	5969(3)	(835(2)	33(1)	1

C6	6871(3)	6550(3)	(15(2)	29(1)	1

C7	5506(3)	7376(3)	427(2)	26(1)	1

C8	7368(3)	7411(3)	1425(2)	28(1)	1

C9	7204(3)	7773(3)	4064(2)	30(1)	1

C10	6843(7)	6328(4)	4300(3)	71(1)	1

C11	7323(8)	5604(4)	5088(4)	86(2)	1

C12	8117(5)	6310(4)	5666(3)	52(1)	1

C13	8450(4)	7750(4)	5449(2)	41(1)	1

C14	7992(4)	8486(3)	4644(2)	34(1)	1

C15	7421(3)	10428(3)	2878(2)	28(1)	1

C16	6294(4)	11467(3)	3257(2)	37(1)	1

C17	6881(5)	12866(4)	3225(2)	51(1)	1

C18	8576(6)	13210(4)	2800(3)	60(1)	1

C19	9690(5)	12192(5)	2421(3)	57(1)	1

C20	9127(4)	10787(4)	2459(2)	41(1)	1

C21	2804(4)	8456(3)	3918(2)	37(1)	1

N1	5787(3)	7781(2)	1283(1)	25(1)	1

N2	7997(3)	7745(3)	2178(2)	36(1)	1

P1	6627(1)	8614(1)	2982(1)	25(1)	1

S1	8612(1)	6411(1)	605(1)	31(1)	1

Cl1	1711(1)	6694(1)	2425(1)	31(1)	1

Pd1	4118(1)	8085(1)	2633(1)	24(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(C2	1.505(4)

C2(C3	1.394(4)

C2(C7	1.400(4)

C3(C4	1.394(5)

C4(C5	1.380(4)

C5(C6	1.388(4)

C6(C7	1.398(4)

C6(S1	1.750(3)

C7(N1	1.407(3)

C8(N1	1.309(3)

C8(N2	1.355(3)

C8(S1	1.743(3)

C9(C14	1.373(4)

C9(C10	1.382(4)

C9(P1	1.811(3)

C10(C11	1.375(5)

C11(C12	1.369(6)

C12(C13	1.370(5)

C13(C14	1.394(4)

C15(C16	1.384(4)

C15(C20	1.388(4)

C15(P1	1.805(3)

C16(C17	1.393(4)

C17(C18	1.379(6)

C18(C19	1.364(6)

C19(C20	1.391(5)

C21(Pd1	2.035(3)

N1(Pd1	2.204(2)

N2(P1	1.701(2)

P1(Pd1	2.1824(8)

Cl1(Pd1	2.3909(9)

C3(C2(C7	116.2(3)

C3(C2(C1	121.0(2)

C7(C2(C1	122.7(2)

C2(C3(C4	122.6(3)

C5(C4(C3	121.1(3)

C4(C5(C6	116.7(3)

C5(C6(C7	122.7(2)

C5(C6(S1	127.0(2)

C7(C6(S1	110.28(18)

C6(C7(C2	120.3(2)

C6(C7(N1	113.8(2)

C2(C7(N1	125.7(2)

N1(C8(N2	122.4(2)

N1(C8(S1	116.16(19)

N2(C8(S1	121.44(19)

C14(C9(C10	119.0(3)

C14(C9(P1	123.7(2)

C10(C9(P1	117.3(2)

C11(C10(C9	120.4(3)

C12(C11(C10	120.7(3)

C11(C12(C13	119.5(3)

C12(C13(C14	120.1(3)

C9(C14(C13	120.2(3)

C16(C15(C20	119.9(3)

C16(C15(P1	118.2(2)

C20(C15(P1	121.9(2)

C15(C16(C17	119.9(3)

C18(C17(C16	119.6(4)

C19(C18(C17	120.8(3)

C18(C19(C20	120.2(3)

C15(C20(C19	119.7(3)

C8(N1(C7	110.7(2)

C8(N1(Pd1	108.86(16)

C7(N1(Pd1	135.47(16)

C8(N2(P1	117.87(17)

N2(P1(C15	106.76(13)

N2(P1(C9	101.69(12)

C15(P1(C9	104.29(12)

N2(P1(Pd1	99.27(8)

C15(P1(Pd1	123.34(9)

C9(P1(Pd1	118.56(9)

C8(S1(C6	88.64(12)

C21(Pd1(P1	91.90(9)

C21(Pd1(N1	173.89(10)

P1(Pd1(N1	82.07(6)

C21(Pd1(Cl1	89.77(9)

P1(Pd1(Cl1	160.12(3)

N1(Pd1(Cl1	96.22(6)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	32(1) 	34(1)	41(2) 	5(1)	(15(1) 	(2(1)

C2	29(1) 	28(1)	30(1) 	6(1)	(10(1) 	(9(1)

C3	40(2) 	41(2)	29(1) 	5(1)	(17(1) 	(12(1)

C4	51(2) 	44(2)	25(1) 	(2(1)	(12(1) 	(13(1)

C5	41(2) 	32(1)	25(1) 	(5(1)	(4(1) 	(7(1)

C6	30(1) 	30(1)	27(1) 	(2(1)	(8(1) 	(6(1)

C7	28(1) 	24(1)	25(1) 	(1(1)	(7(1) 	(7(1)

C8	21(1) 	34(1)	31(1) 	(10(1)	(6(1) 	2(1)

C9	30(1) 	26(1)	36(1) 	(6(1)	(12(1) 	3(1)

C10	119(4) 	27(2)	84(3) 	(1(2)	(67(3) 	(9(2)

C11	142(5) 	27(2)	104(4) 	16(2)	(79(3) 	(14(2)

C12	58(2) 	45(2)	54(2) 	12(2)	(26(2) 	3(2)

C13	46(2) 	47(2)	33(1) 	0(1)	(15(1) 	1(1)

C14	37(2) 	34(1)	31(1) 	(2(1)	(10(1) 	(3(1)

C15	31(1) 	33(1)	23(1) 	0(1)	(11(1) 	(5(1)

C16	45(2) 	31(1)	37(2) 	(6(1)	(10(1) 	(3(1)

C17	77(3) 	31(2)	53(2) 	(6(1)	(31(2) 	(7(2)

C18	86(3) 	43(2)	61(2) 	15(2)	(48(2) 	(29(2)

C19	52(2) 	66(2)	53(2) 	23(2)	(24(2) 	(31(2)

C20	35(2) 	52(2)	37(2) 	5(1)	(10(1) 	(10(1)

C21	32(1) 	43(2)	34(1) 	(9(1)	0(1) 	1(1)

N1	21(1) 	30(1)	26(1) 	(7(1)	(6(1) 	0(1)

N2	21(1) 	55(2)	40(1) 	(25(1)	(14(1) 	11(1)

P1	22(1) 	29(1)	28(1) 	(9(1)	(9(1) 	2(1)

S1	25(1) 	39(1)	33(1) 	(15(1)	(6(1) 	4(1)

Cl1	22(1) 	33(1)	41(1) 	(3(1)	(12(1) 	(2(1)

Pd1	19(1) 	26(1)	28(1) 	(6(1)	(7(1) 	2(1)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H1A	2222	9377	(172	52	1

H1B	3302	9611	631	52	1

H1C	1818	8409	814	52	1

H3	3081	7491	(1160	43	1

H4	5210	5911	(1787	47	1

H5	7705	5364	(1108	39	1

H10	6260	5832	3916	85	1

H11	7101	4604	5233	103	1

H12	8434	5806	6212	62	1

H13	8995	8247	5849	49	1

H14	8226	9484	4496	40	1

H16	5122	11227	3538	44	1

H17	6119	13579	3494	61	1

H18	8973	14166	2772	72	1

H19	10854	12444	2129	68	1

H20	9907	10077	2201	50	1

H21A	3648	8567	4328	55	1

H21B	2036	7643	4182	55	1

H21C	2096	9337	3863	55	1

H2	9079	7519	2249	43	1