|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement details.

Identification code 	2009src1151

Empirical formula 	C19H17FeNO

Formula weight 	331.19

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/c

Unit cell dimensions	a = 6.0028(2) Å	( = 90°

b = 21.5130(12) Å	( = 93.010(3)°

c = 11.3488(5) Å	(  = 90°

Volume	1463.54(11) Å3

Z	4

Density (calculated)	1.503 Mg / m3

Absorption coefficient	1.031 mm(1

F(000)	688

Crystal	block; brown

Crystal size	0.31 ( 0.15 ( 0.15 mm3

( range for data collection	3.36 ( 27.48°

Index ranges	(7 ( h ( 6, (27 ( k ( 27, (14 ( l ( 14

Reflections collected	16999

Independent reflections	3347 [Rint = 0.0823]

Completeness to ( = 27.48°	99.8 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.8607 and 0.7406

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	3347 / 1 / 202

Goodness-of-fit on F2	1.046

Final R indices [F2 > 2((F2)]	R1 = 0.0505, wR2 = 0.1146

R indices (all data)	R1 = 0.0713, wR2 = 0.1253

Largest diff. peak and hole	0.622 and (0.736 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SADABS (Sheldrick, G. M. (2007). SADABS. Version 2007/2. Bruker AXS Inc., Madison, Wisconsin, USA.). Structure solution: SHELXS97 (Sheldrick, G.M. (2008). Acta Cryst. A64, 112-122.). Structure refinement: SHELXL97 (G Sheldrick, G.M. (2008). Acta Cryst. A64, 112-122.). Graphics: CAMERON (Watkin, D. M., Pearce, L. & Prout, C. K. (1993). Chemical Crystallography Lab, University of Oxford)

Special details:

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	829(5)	3171(1)	6050(3)	25(1)	1

C2	3026(6)	2986(2)	6416(3)	32(1)	1

C3	4268(5)	3536(2)	6725(3)	34(1)	1

C4	2837(5)	4050(2)	6536(3)	27(1)	1

C5	727(5)	3822(2)	6124(2)	22(1)	1

C6	2215(5)	3361(1)	3265(2)	21(1)	1

C7	4247(5)	3056(2)	3628(2)	23(1)	1

C8	5839(5)	3520(1)	3995(3)	24(1)	1

C9	4775(4)	4108(1)	3854(2)	21(1)	1

C10	2534(4)	4016(1)	3400(2)	18(1)	1

C11	869(5)	4521(1)	3116(2)	18(1)	1

C12	510(4)	4655(1)	1782(2)	18(1)	1

C13	2657(5)	4823(1)	1191(2)	20(1)	1

C14	1050(4)	4021(1)	124(2)	18(1)	1

C15	672(5)	3569(1)	(729(2)	21(1)	1

C16	(1262(5)	3213(1)	(662(3)	24(1)	1

C17	(2733(5)	3309(2)	221(3)	24(1)	1

C18	(2305(5)	3770(2)	1081(3)	22(1)	1

C19	(394(4)	4123(1)	1027(2)	16(1)	1

N1	2839(4)	4445(1)	235(2)	19(1)	1

O1	3997(3)	5230(1)	1510(2)	25(1)	1

Fe1	3114(1)	3564(1)	4993(1)	17(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(C5	1.406(4)

C1(C2	1.418(5)

C1(Fe1	2.052(3)

C1(H1	0.9500

C2(C3	1.432(5)

C2(Fe1	2.040(3)

C2(H2	0.9500

C3(C4	1.410(5)

C3(Fe1	2.050(3)

C3(H3	0.9500

C4(C5	1.415(4)

C4(Fe1	2.053(3)

C4(H4	0.9500

C5(Fe1	2.050(3)

C5(H5	0.9500

C6(C7	1.427(4)

C6(C10	1.429(4)

C6(Fe1	2.054(3)

C6(H6	0.9500

C7(C8	1.429(4)

C7(Fe1	2.042(3)

C7(H7	0.9500

C8(C9	1.423(4)

C8(Fe1	2.041(3)

C8(H8	0.9500

C9(C10	1.429(4)

C9(Fe1	2.042(3)

C9(H9	0.9500

C10(C11	1.500(4)

C10(Fe1	2.066(3)

C11(C12	1.545(4)

C11(H11A	0.9900

C11(H11B	0.9900

C12(C19	1.514(4)

C12(C13	1.527(4)

C12(H12	1.0000

C13(O1	1.231(3)

C13(N1	1.364(4)

C14(C15	1.383(4)

C14(C19	1.394(4)

C14(N1	1.410(4)

C15(C16	1.396(4)

C15(H15	0.9500

C16(C17	1.385(4)

C16(H16	0.9500

C17(C18	1.406(4)

C17(H17	0.9500

C18(C19	1.379(4)

C18(H18	0.9500

N1(H1N	0.953(17)

C5(C1(C2	107.7(3)

C5(C1(Fe1	69.88(16)

C2(C1(Fe1	69.29(17)

C5(C1(H1	126.1

C2(C1(H1	126.1

Fe1(C1(H1	126.3

C1(C2(C3	107.8(3)

C1(C2(Fe1	70.16(17)

C3(C2(Fe1	69.86(18)

C1(C2(H2	126.1

C3(C2(H2	126.1

Fe1(C2(H2	125.4

C4(C3(C2	107.8(3)

C4(C3(Fe1	70.05(17)

C2(C3(Fe1	69.16(17)

C4(C3(H3	126.1

C2(C3(H3	126.1

Fe1(C3(H3	126.3

C3(C4(C5	107.8(3)

C3(C4(Fe1	69.75(18)

C5(C4(Fe1	69.70(17)

C3(C4(H4	126.1

C5(C4(H4	126.1

Fe1(C4(H4	126.0

C1(C5(C4	108.9(3)

C1(C5(Fe1	70.03(16)

C4(C5(Fe1	69.97(17)

C1(C5(H5	125.5

C4(C5(H5	125.5

Fe1(C5(H5	126.1

C7(C6(C10	108.4(3)

C7(C6(Fe1	69.15(16)

C10(C6(Fe1	70.16(15)

C7(C6(H6	125.8

C10(C6(H6	125.8

Fe1(C6(H6	126.4

C6(C7(C8	108.1(3)

C6(C7(Fe1	70.08(16)

C8(C7(Fe1	69.47(17)

C6(C7(H7	125.9

C8(C7(H7	125.9

Fe1(C7(H7	126.1

C9(C8(C7	107.4(3)

C9(C8(Fe1	69.67(16)

C7(C8(Fe1	69.55(16)

C9(C8(H8	126.3

C7(C8(H8	126.3

Fe1(C8(H8	126.1

C8(C9(C10	109.0(3)

C8(C9(Fe1	69.54(17)

C10(C9(Fe1	70.54(16)

C8(C9(H9	125.5

C10(C9(H9	125.5

Fe1(C9(H9	126.0

C6(C10(C9	107.1(2)

C6(C10(C11	127.4(3)

C9(C10(C11	125.5(3)

C6(C10(Fe1	69.26(15)

C9(C10(Fe1	68.76(15)

C11(C10(Fe1	127.51(19)

C10(C11(C12	113.8(2)

C10(C11(H11A	108.8

C12(C11(H11A	108.8

C10(C11(H11B	108.8

C12(C11(H11B	108.8

H11A(C11(H11B	107.7

C19(C12(C13	102.4(2)

C19(C12(C11	116.1(2)

C13(C12(C11	113.4(2)

C19(C12(H12	108.2

C13(C12(H12	108.2

C11(C12(H12	108.2

O1(C13(N1	125.4(3)

O1(C13(C12	126.3(3)

N1(C13(C12	108.3(2)

C15(C14(C19	122.7(3)

C15(C14(N1	127.9(3)

C19(C14(N1	109.4(2)

C14(C15(C16	117.0(3)

C14(C15(H15	121.5

C16(C15(H15	121.5

C17(C16(C15	121.4(3)

C17(C16(H16	119.3

C15(C16(H16	119.3

C16(C17(C18	120.5(3)

C16(C17(H17	119.8

C18(C17(H17	119.8

C19(C18(C17	118.6(3)

C19(C18(H18	120.7

C17(C18(H18	120.7

C18(C19(C14	119.8(3)

C18(C19(C12	131.7(3)

C14(C19(C12	108.5(2)

C13(N1(C14	111.4(2)

C13(N1(H1N	124.5(18)

C14(N1(H1N	124.1(18)

C2(Fe1(C8	117.79(12)

C2(Fe1(C7	107.33(13)

C8(Fe1(C7	40.97(12)

C2(Fe1(C9	152.12(13)

C8(Fe1(C9	40.79(12)

C7(Fe1(C9	68.51(12)

C2(Fe1(C3	40.99(14)

C8(Fe1(C3	106.91(12)

C7(Fe1(C3	127.05(13)

C9(Fe1(C3	118.16(13)

C2(Fe1(C5	67.77(12)

C8(Fe1(C5	165.33(13)

C7(Fe1(C5	153.10(13)

C9(Fe1(C5	128.41(12)

C3(Fe1(C5	67.67(12)

C2(Fe1(C1	40.55(13)

C8(Fe1(C1	152.33(12)

C7(Fe1(C1	118.84(13)

C9(Fe1(C1	165.95(12)

C3(Fe1(C1	68.28(13)

C5(Fe1(C1	40.09(12)

C2(Fe1(C4	68.24(14)

C8(Fe1(C4	126.89(12)

C7(Fe1(C4	164.75(12)

C9(Fe1(C4	108.15(12)

C3(Fe1(C4	40.20(13)

C5(Fe1(C4	40.34(12)

C1(Fe1(C4	67.99(12)

C2(Fe1(C6	127.57(13)

C8(Fe1(C6	68.76(12)

C7(Fe1(C6	40.77(11)

C9(Fe1(C6	68.28(12)

C3(Fe1(C6	165.45(14)

C5(Fe1(C6	119.88(12)

C1(Fe1(C6	108.70(12)

C4(Fe1(C6	153.30(13)

C2(Fe1(C10	165.64(13)

C8(Fe1(C10	68.84(11)

C7(Fe1(C10	68.62(11)

C9(Fe1(C10	40.71(11)

C3(Fe1(C10	152.33(13)

C5(Fe1(C10	109.20(11)

C1(Fe1(C10	128.20(11)

C4(Fe1(C10	119.25(12)

C6(Fe1(C10	40.58(11)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	33(2) 	27(2)	16(1) 	(1(1)	7(1) 	(8(1)

C2	52(2) 	30(2)	14(2) 	12(1)	12(1) 	16(2)

C3	24(2) 	67(3)	11(2) 	6(2)	0(1) 	1(2)

C4	41(2) 	30(2)	11(1) 	(5(1)	6(1) 	(11(1)

C5	26(2) 	27(2)	14(1) 	0(1)	6(1) 	5(1)

C6	26(2) 	24(2)	11(1) 	(2(1)	0(1) 	2(1)

C7	33(2) 	25(2)	13(1) 	(1(1)	3(1) 	11(1)

C8	21(2) 	37(2)	14(1) 	5(1)	3(1) 	7(1)

C9	19(1) 	32(2)	11(1) 	1(1)	4(1) 	(3(1)

C10	21(1) 	24(2)	9(1) 	2(1)	2(1) 	2(1)

C11	24(2) 	21(2)	10(1) 	0(1)	2(1) 	0(1)

C12	21(1) 	19(1)	14(1) 	2(1)	(1(1) 	2(1)

C13	25(2) 	23(2)	11(1) 	7(1)	(3(1) 	1(1)

C14	20(1) 	18(1)	15(1) 	6(1)	(1(1) 	1(1)

C15	26(2) 	24(2)	12(1) 	1(1)	4(1) 	2(1)

C16	32(2) 	22(2)	17(1) 	0(1)	(1(1) 	(3(1)

C17	24(2) 	29(2)	20(2) 	2(1)	0(1) 	(8(1)

C18	18(1) 	32(2)	16(1) 	3(1)	2(1) 	0(1)

C19	19(1) 	20(1)	10(1) 	4(1)	(2(1) 	2(1)

N1	21(1) 	25(1)	12(1) 	0(1)	4(1) 	(4(1)

O1	31(1) 	30(1)	15(1) 	2(1)	(1(1) 	(11(1)

Fe1	20(1) 	22(1)	8(1) 	1(1)	1(1) 	1(1)