|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	2005src0805 / CROIN

Empirical formula 	C28H28Cl2Mo2N4O6S2

Formula weight 	843.44

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	C2/c

Unit cell dimensions	a = 22.361(5) Å	( = 90°

b = 11.409(2) Å	( = 128.22(3)°

c = 15.609(3) Å	(  = 90°

Volume	3128.5(11) Å3

Z	4

Density (calculated)	1.791 Mg / m3

Absorption coefficient	1.155 mm(1

F(000)	1688

Crystal	Block; Red

Crystal size	0.12 ( 0.07 ( 0.04 mm3

( range for data collection	3.11 ( 27.48°

Index ranges	(28 ( h ( 28, (14 ( k ( 14, (20 ( l ( 20

Reflections collected	21247

Independent reflections	3586 [Rint = 0.0527]

Completeness to ( = 27.48°	99.7 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9553 and 0.8738

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	3586 / 0 / 201

Goodness-of-fit on F2	1.058

Final R indices [F2 > 2((F2)]	R1 = 0.0365, wR2 = 0.0875

R indices (all data)	R1 = 0.0469, wR2 = 0.0929

Largest diff. peak and hole	1.412 and (0.850 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SADABS Version 2.10. (G. M. Sheldrick (2003)) Bruker AXS Inc., Madison, Wisconsin, USA. Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP3 for Windows (L. J. Farrugia, J. Appl. Crystallogr. 1997, 30, 565).

Special details:

All hydrogen atoms were fixed.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	945(2)	(4029(3)	5713(3)	19(1)	1

C2	1528(2)	(3878(3)	6832(3)	20(1)	1

C3	1840(2)	(2796(3)	7234(3)	20(1)	1

C4	1551(2)	(1831(3)	6513(3)	18(1)	1

C5	952(2)	(2046(3)	5406(2)	16(1)	1

C6	578(2)	(1083(3)	4659(2)	16(1)	1

C7	815(2)	69(3)	5034(3)	18(1)	1

C8	376(2)	986(3)	4288(3)	19(1)	1

C9	(256(2)	714(3)	3257(3)	20(1)	1

C10	(440(2)	(470(3)	2943(3)	19(1)	1

C11	1810(2)	(661(3)	6860(3)	20(1)	1

C12	1461(2)	259(3)	6160(3)	21(1)	1

N1	665(2)	(3142(2)	5010(2)	16(1)	1

N2	(25(2)	(1354(2)	3615(2)	16(1)	1

O1	(110(1)	(4814(2)	3389(2)	20(1)	1

O2	(780(1)	(2971(2)	1665(2)	18(1)	1

Cl1	(1247(1)	(3090(1)	3145(1)	22(1)	1

Mo1	(134(1)	(3352(1)	3191(1)	15(1)	1

C21	2510(2)	(900(4)	4948(4)	42(1)	1

C22	3407(2)	1016(4)	5547(4)	39(1)	1

O21	1915(2)	1171(2)	4077(2)	34(1)	1

S21	2500(1)	638(1)	5177(1)	28(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(N1	1.331(4)

C1(C2	1.401(5)

C1(H1	0.9500

C2(C3	1.364(5)

C2(H2	0.9500

C3(C4	1.413(5)

C3(H3	0.9500

C4(C5	1.406(4)

C4(C11	1.421(5)

C5(N1	1.366(4)

C5(C6	1.436(4)

C6(N2	1.360(4)

C6(C7	1.402(5)

C7(C8	1.415(4)

C7(C12	1.442(5)

C8(C9	1.368(5)

C8(H8	0.9500

C9(C10	1.409(5)

C9(H9	0.9500

C10(N2	1.332(4)

C10(H10	0.9500

C11(C12	1.360(5)

C11(H11	0.9500

C12(H12	0.9500

N1(Mo1	2.244(3)

N2(Mo1	2.344(3)

O1(Mo1	1.692(2)

O2(Mo1	1.921(2)

O2(Mo1i	1.961(2)

Cl1(Mo1	2.4651(10)

Mo1(O2i	1.961(2)

Mo1(Mo1i	2.5687(7)

C21(S21	1.794(4)

C21(H21A	0.9800

C21(H21B	0.9800

C21(H21C	0.9800

C22(S21	1.784(4)

C22(H22A	0.9800

C22(H22B	0.9800

C22(H22C	0.9800

O21(S21	1.499(3)

N1(C1(C2	122.3(3)

N1(C1(H1	118.8

C2(C1(H1	118.8

C3(C2(C1	120.1(3)

C3(C2(H2	120.0

C1(C2(H2	120.0

C2(C3(C4	119.2(3)

C2(C3(H3	120.4

C4(C3(H3	120.4

C5(C4(C3	117.4(3)

C5(C4(C11	119.1(3)

C3(C4(C11	123.4(3)

N1(C5(C4	122.7(3)

N1(C5(C6	117.3(3)

C4(C5(C6	119.9(3)

N2(C6(C7	123.5(3)

N2(C6(C5	116.5(3)

C7(C6(C5	119.9(3)

C6(C7(C8	117.3(3)

C6(C7(C12	119.0(3)

C8(C7(C12	123.6(3)

C9(C8(C7	119.1(3)

C9(C8(H8	120.4

C7(C8(H8	120.4

C8(C9(C10	119.6(3)

C8(C9(H9	120.2

C10(C9(H9	120.2

N2(C10(C9	122.7(3)

N2(C10(H10	118.6

C9(C10(H10	118.6

C12(C11(C4	121.5(3)

C12(C11(H11	119.3

C4(C11(H11	119.3

C11(C12(C7	120.5(3)

C11(C12(H12	119.8

C7(C12(H12	119.8

C1(N1(C5	118.2(3)

C1(N1(Mo1	124.2(2)

C5(N1(Mo1	117.0(2)

C10(N2(C6	117.5(3)

C10(N2(Mo1	127.9(2)

C6(N2(Mo1	114.3(2)

Mo1(O2(Mo1i	82.86(9)

O1(Mo1(O2	111.36(10)

O1(Mo1(O2i	106.55(10)

O2(Mo1(O2i	91.39(10)

O1(Mo1(N1	87.89(10)

O2(Mo1(N1	160.76(10)

O2i(Mo1(N1	82.82(10)

O1(Mo1(N2	157.12(10)

O2(Mo1(N2	89.85(10)

O2i(Mo1(N2	80.42(9)

N1(Mo1(N2	71.13(9)

O1(Mo1(Cl1	92.36(8)

O2(Mo1(Cl1	87.95(8)

O2i(Mo1(Cl1	159.87(7)

N1(Mo1(Cl1	91.26(8)

N2(Mo1(Cl1	79.46(7)

O1(Mo1(Mo1i	99.01(7)

O2(Mo1(Mo1i	49.25(7)

O2i(Mo1(Mo1i	47.89(7)

N1(Mo1(Mo1i	130.28(7)

N2(Mo1(Mo1i	101.51(6)

Cl1(Mo1(Mo1i	136.96(4)

S21(C21(H21A	109.5

S21(C21(H21B	109.5

H21A(C21(H21B	109.5

S21(C21(H21C	109.5

H21A(C21(H21C	109.5

H21B(C21(H21C	109.5

S21(C22(H22A	109.5

S21(C22(H22B	109.5

H22A(C22(H22B	109.5

S21(C22(H22C	109.5

H22A(C22(H22C	109.5

H22B(C22(H22C	109.5

O21(S21(C22	106.52(19)

O21(S21(C21	106.15(19)

C22(S21(C21	98.6(2)

Symmetry transformations used to generate equivalent atoms:

(i) (x,y,(z+1/2

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	22(2) 	16(2)	23(2) 	1(1)	16(1) 	1(1)

C2	21(2) 	21(2)	17(2) 	4(1)	11(1) 	6(1)

C3	17(2) 	23(2)	19(2) 	(1(1)	10(1) 	1(1)

C4	15(2) 	24(2)	19(2) 	(1(1)	12(1) 	1(1)

C5	16(2) 	16(2)	17(2) 	(1(1)	11(1) 	(1(1)

C6	15(2) 	16(2)	18(2) 	0(1)	12(1) 	1(1)

C7	20(2) 	19(2)	22(2) 	2(1)	16(1) 	3(1)

C8	23(2) 	15(2)	27(2) 	(1(1)	19(2) 	0(1)

C9	22(2) 	20(2)	23(2) 	5(1)	17(2) 	4(1)

C10	16(2) 	22(2)	19(2) 	3(1)	11(1) 	3(1)

C11	15(2) 	24(2)	19(2) 	(5(1)	10(1) 	(4(1)

C12	18(2) 	20(2)	23(2) 	(5(1)	12(1) 	(5(1)

N1	17(1) 	16(1)	18(1) 	(2(1)	12(1) 	(2(1)

N2	17(1) 	17(1)	17(1) 	(1(1)	12(1) 	(1(1)

O1	19(1) 	19(1)	21(1) 	(2(1)	12(1) 	(1(1)

O2	16(1) 	19(1)	17(1) 	1(1)	9(1) 	0(1)

Cl1	21(1) 	18(1)	30(1) 	(2(1)	18(1) 	(1(1)

Mo1	16(1) 	14(1)	15(1) 	(1(1)	9(1) 	(1(1)

C21	24(2) 	30(2)	46(2) 	12(2)	10(2) 	5(2)

C22	26(2) 	39(2)	47(2) 	1(2)	21(2) 	3(2)

O21	29(1) 	33(2)	24(1) 	5(1)	9(1) 	9(1)

S21	22(1) 	40(1)	20(1) 	4(1)	13(1) 	6(1)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H1	742	(4792	5447	22	1

H2	1707	(4530	7311	24	1

H3	2246	(2694	7989	24	1

H8	518	1781	4501	23	1

H9	(569	1320	2755	24	1

H10	(879	(645	2222	23	1

H11	2236	(519	7598	24	1

H12	1644	1033	6414	25	1

H21A	2037	(1260	4734	62	1

H21B	2945	(1269	5619	62	1

H21C	2552	(1013	4365	62	1

H22A	3418	824	4945	58	1

H22B	3805	574	6198	58	1

H22C	3496	1858	5702	58	1