|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	04src1115

Empirical formula 	C24H28Cl3N12O16Zn2

Formula weight 	977.67

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/c

Unit cell dimensions	a = 20.502(4) Å	( = 90°

b = 11.575(2) Å	( = 107.67(2)°

c = 15.431(3) Å	(  = 90°

Volume	3489.2(12) Å3

Z	4

Density (calculated)	1.861 Mg / m3

Absorption coefficient	1.697 mm(1

F(000)	1980

Crystal	Plate; Yellow

Crystal size	0.16 ( 0.14 ( 0.03 mm3

( range for data collection	2.92 ( 27.48°

Index ranges	(26 ( h ( 26, (14 ( k ( 15, (19 ( l ( 19

Reflections collected	37319

Independent reflections	7835 [Rint = 0.1064]

Completeness to ( = 27.48°	98.1 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9509 and 0.7730

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	7835 / 18 / 546

Goodness-of-fit on F2	1.148

Final R indices [F2 > 2((F2)]	R1 = 0.0821, wR2 = 0.1963

R indices (all data)	R1 = 0.1130, wR2 = 0.2127

Largest diff. peak and hole	1.075 and (0.771 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP3 for Windows (L. J. Farrugia, J. Appl. Crystallogr. 1997, 30, 565).

Special details:

All hydrogen atoms were fixed.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	908(4)	3837(7)	1337(5)	28(2)	1

C2	210(4)	3999(7)	934(5)	30(2)	1

C3	(196(4)	3060(7)	592(5)	30(2)	1

C4	104(4)	1969(7)	691(5)	29(2)	1

C5	795(4)	1866(6)	1110(5)	23(2)	1

C6	1158(4)	736(6)	1231(5)	22(1)	1

C7	2098(4)	(955(6)	859(5)	23(2)	1

C8	2498(3)	(2062(6)	1094(5)	24(2)	1

C9	2415(4)	(2983(7)	498(5)	28(2)	1

C10	2806(4)	(3962(7)	800(5)	27(2)	1

C11	3261(4)	(3996(7)	1658(5)	25(2)	1

C12	3322(4)	(3032(7)	2199(5)	26(2)	1

C13	3820(4)	(2931(6)	3146(5)	24(2)	1

C14	4299(4)	(3760(7)	3559(5)	27(2)	1

C15	4742(4)	(3521(7)	4389(5)	29(2)	1

C16	4702(4)	(2467(7)	4813(5)	28(2)	1

C17	4207(3)	(1695(6)	4365(5)	23(2)	1

C18	4114(3)	(529(6)	4696(5)	23(1)	1

C19	3202(4)	1806(7)	3679(5)	25(2)	1

C20	3054(4)	3018(6)	3807(5)	24(2)	1

C21	3371(4)	3615(7)	4616(5)	27(2)	1

C22	3234(4)	4759(7)	4690(5)	28(2)	1

C23	2799(4)	5298(7)	3939(6)	30(2)	1

C24	2481(4)	4678(7)	3160(5)	27(2)	1

N1	1194(3)	2790(6)	1441(4)	26(1)	1

N2	803(3)	(212(6)	1202(4)	26(1)	1

N3	1820(3)	814(5)	1357(4)	23(1)	1

N4	2202(3)	(224(5)	1538(4)	22(1)	1

N5	1666(3)	(827(6)	33(4)	25(1)	1

N6	2950(3)	(2086(5)	1935(4)	21(1)	1

N7	3764(3)	(1938(5)	3539(4)	24(1)	1

N8	4425(3)	(212(6)	5543(4)	26(1)	1

N9	3712(3)	132(5)	4071(4)	24(1)	1

N10	3619(3)	1249(5)	4350(4)	24(1)	1

N11	2919(3)	1373(5)	2867(3)	14(1)	1

N12	2610(3)	3535(5)	3101(4)	25(1)	1

O1	2698(3)	3122(5)	1171(4)	28(1)	1

O11	3803(3)	(60(5)	2052(4)	27(1)	1

O12	2332(3)	(825(5)	3463(4)	28(1)	1

Zn1	2218(1)	2378(1)	2004(1)	22(1)	1

Zn2	3072(1)	(510(1)	2786(1)	22(1)	1

O31	1587(3)	7160(5)	3325(4)	41(2)	1

O32	719(3)	5923(5)	2518(4)	44(2)	1

O33	1252(4)	7152(7)	1734(5)	57(2)	1

O34	534(3)	7916(6)	2482(5)	47(2)	1

Cl31	1010(1)	7039(2)	2499(1)	28(1)	1

O41	1460(3)	418(5)	4658(4)	39(1)	1

O42	1855(3)	2303(6)	4498(4)	45(2)	1

O43	699(3)	1876(6)	3934(5)	44(2)	1

O44	1453(4)	1109(7)	3218(4)	57(2)	1

Cl41	1362(1)	1418(2)	4078(1)	31(1)	1

O51	5029(3)	1986(6)	2974(4)	42(2)	1

O52	4945(3)	3709(5)	2154(4)	42(2)	1

O53	4062(3)	2362(6)	1740(4)	40(1)	1

O54	4260(3)	3428(5)	3105(4)	36(1)	1

Cl51	4579(1)	2880(2)	2510(1)	24(1)	1

O61	616(3)	4362(5)	3895(4)	33(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(N1	1.335(10)

C1(C2	1.388(11)

C1(H1	0.9500

C2(C3	1.373(11)

C2(H2	0.9500

C3(C4	1.393(11)

C3(H3	0.9500

C4(C5	1.372(10)

C4(H4	0.9500

C5(N1	1.349(9)

C5(C6	1.489(10)

C6(N2	1.311(9)

C6(N3	1.314(9)

C7(N4	1.313(9)

C7(N5	1.322(9)

C7(C8	1.505(10)

C8(N6	1.346(9)

C8(C9	1.384(11)

C9(C10	1.384(11)

C9(H9	0.9500

C10(C11	1.370(10)

C10(H10	0.9500

C11(C12	1.376(11)

C11(H11	0.9500

C12(N6	1.325(10)

C12(C13	1.512(10)

C13(N7	1.321(10)

C13(C14	1.382(10)

C14(C15	1.356(11)

C14(H14	0.9500

C15(C16	1.399(11)

C15(H15	0.9500

C16(C17	1.372(10)

C16(H16	0.9500

C17(N7	1.351(9)

C17(C18	1.476(10)

C18(N9	1.309(9)

C18(N8	1.321(9)

C19(N10	1.296(10)

C19(N11	1.311(9)

C19(C20	1.461(11)

C20(N12	1.332(9)

C20(C21	1.402(11)

C21(C22	1.366(11)

C21(H21	0.9500

C22(C23	1.379(11)

C22(H22	0.9500

C23(C24	1.383(11)

C23(H23	0.9500

C24(N12	1.357(10)

C24(H24	0.9500

N1(Zn1	2.070(6)

N2(H2A	0.8800

N2(H2B	0.8800

N3(N4	1.415(8)

N3(Zn1	2.109(6)

N4(Zn2	2.216(6)

N5(H5A	0.8800

N5(H5B	0.8800

N6(Zn2	2.217(6)

N7(Zn2	2.258(6)

N8(H8A	0.8800

N8(H8B	0.8800

N9(N10	1.394(9)

N9(Zn2	2.151(6)

N11(Zn1	2.008(5)

N11(Zn2	2.210(5)

N12(Zn1	2.116(6)

O1(Zn1	2.032(5)

O1(H1A	0.841(19)

O1(H1B	0.847(19)

O11(Zn2	2.198(5)

O11(H11A	0.848(19)

O11(H11B	0.85(2)

O12(Zn2	2.117(5)

O12(H12A	0.845(19)

O12(H12B	0.84(2)

O31(Cl31	1.459(6)

O32(Cl31	1.428(6)

O33(Cl31	1.420(7)

O34(Cl31	1.403(7)

O41(Cl41	1.440(6)

O42(Cl41	1.446(7)

O43(Cl41	1.412(6)

O44(Cl41	1.440(6)

O51(Cl51	1.426(6)

O52(Cl51	1.427(6)

O53(Cl51	1.460(6)

O54(Cl51	1.428(6)

O61(H61A	0.84(2)

O61(H61B	0.84(2)

N1(C1(C2	122.1(7)

N1(C1(H1	118.9

C2(C1(H1	118.9

C3(C2(C1	119.2(7)

C3(C2(H2	120.4

C1(C2(H2	120.4

C2(C3(C4	118.6(7)

C2(C3(H3	120.7

C4(C3(H3	120.7

C5(C4(C3	119.3(7)

C5(C4(H4	120.3

C3(C4(H4	120.3

N1(C5(C4	122.0(7)

N1(C5(C6	115.2(6)

C4(C5(C6	122.8(7)

N2(C6(N3	127.0(7)

N2(C6(C5	118.7(6)

N3(C6(C5	114.4(6)

N4(C7(N5	126.6(7)

N4(C7(C8	114.3(6)

N5(C7(C8	119.0(6)

N6(C8(C9	122.3(7)

N6(C8(C7	114.6(6)

C9(C8(C7	123.2(7)

C8(C9(C10	117.7(7)

C8(C9(H9	121.1

C10(C9(H9	121.1

C11(C10(C9	120.2(7)

C11(C10(H10	119.9

C9(C10(H10	119.9

C10(C11(C12	118.2(7)

C10(C11(H11	120.9

C12(C11(H11	120.9

N6(C12(C11	123.1(7)

N6(C12(C13	112.9(6)

C11(C12(C13	124.0(7)

N7(C13(C14	122.7(7)

N7(C13(C12	112.6(6)

C14(C13(C12	124.7(7)

C15(C14(C13	118.2(7)

C15(C14(H14	120.9

C13(C14(H14	120.9

C14(C15(C16	120.2(7)

C14(C15(H15	119.9

C16(C15(H15	119.9

C17(C16(C15	118.2(7)

C17(C16(H16	120.9

C15(C16(H16	120.9

N7(C17(C16	121.5(7)

N7(C17(C18	113.4(6)

C16(C17(C18	125.1(7)

N9(C18(N8	125.1(7)

N9(C18(C17	113.4(6)

N8(C18(C17	121.5(7)

N10(C19(N11	124.5(7)

N10(C19(C20	118.9(7)

N11(C19(C20	116.5(7)

N12(C20(C21	121.6(7)

N12(C20(C19	116.1(7)

C21(C20(C19	122.3(7)

C22(C21(C20	120.1(7)

C22(C21(H21	120.0

C20(C21(H21	120.0

C21(C22(C23	117.7(7)

C21(C22(H22	121.1

C23(C22(H22	121.1

C22(C23(C24	120.6(7)

C22(C23(H23	119.7

C24(C23(H23	119.7

N12(C24(C23	121.0(7)

N12(C24(H24	119.5

C23(C24(H24	119.5

C1(N1(C5	118.7(6)

C1(N1(Zn1	127.8(5)

C5(N1(Zn1	113.4(5)

C6(N2(H2A	120.0

C6(N2(H2B	120.0

H2A(N2(H2B	120.0

C6(N3(N4	117.1(6)

C6(N3(Zn1	111.3(5)

N4(N3(Zn1	121.6(4)

C7(N4(N3	116.4(6)

C7(N4(Zn2	119.3(5)

N3(N4(Zn2	123.3(4)

C7(N5(H5A	120.0

C7(N5(H5B	120.0

H5A(N5(H5B	120.0

C12(N6(C8	118.5(6)

C12(N6(Zn2	123.2(5)

C8(N6(Zn2	118.3(5)

C13(N7(C17	119.2(6)

C13(N7(Zn2	122.0(5)

C17(N7(Zn2	118.1(5)

C18(N8(H8A	120.0

C18(N8(H8B	120.0

H8A(N8(H8B	120.0

C18(N9(N10	115.3(6)

C18(N9(Zn2	123.3(5)

N10(N9(Zn2	120.2(4)

C19(N10(N9	109.5(6)

C19(N11(Zn1	115.6(5)

C19(N11(Zn2	113.7(5)

Zn1(N11(Zn2	128.2(2)

C20(N12(C24	118.9(7)

C20(N12(Zn1	111.6(5)

C24(N12(Zn1	129.5(5)

Zn1(O1(H1A	129(4)

Zn1(O1(H1B	125(4)

H1A(O1(H1B	106(4)

Zn2(O11(H11A	113(3)

Zn2(O11(H11B	114(3)

H11A(O11(H11B	103(4)

Zn2(O12(H12A	119(4)

Zn2(O12(H12B	122(4)

H12A(O12(H12B	106(4)

N11(Zn1(O1	106.2(2)

N11(Zn1(N1	147.4(2)

O1(Zn1(N1	105.1(2)

N11(Zn1(N3	85.0(2)

O1(Zn1(N3	104.9(2)

N1(Zn1(N3	78.5(2)

N11(Zn1(N12	79.3(2)

O1(Zn1(N12	95.7(2)

N1(Zn1(N12	106.3(2)

N3(Zn1(N12	157.0(2)

O12(Zn2(N9	86.1(2)

O12(Zn2(O11	175.8(2)

N9(Zn2(O11	94.1(2)

O12(Zn2(N11	90.4(2)

N9(Zn2(N11	70.4(2)

O11(Zn2(N11	85.7(2)

O12(Zn2(N4	87.0(2)

N9(Zn2(N4	148.7(2)

O11(Zn2(N4	90.7(2)

N11(Zn2(N4	79.1(2)

O12(Zn2(N6	100.5(2)

N9(Zn2(N6	139.2(2)

O11(Zn2(N6	82.0(2)

N11(Zn2(N6	148.5(2)

N4(Zn2(N6	72.1(2)

O12(Zn2(N7	92.9(2)

N9(Zn2(N7	70.5(2)

O11(Zn2(N7	91.1(2)

N11(Zn2(N7	140.4(2)

N4(Zn2(N7	140.4(2)

N6(Zn2(N7	69.0(2)

O34(Cl31(O33	109.6(5)

O34(Cl31(O32	111.2(4)

O33(Cl31(O32	110.7(4)

O34(Cl31(O31	108.8(4)

O33(Cl31(O31	108.8(4)

O32(Cl31(O31	107.6(4)

O43(Cl41(O41	110.2(4)

O43(Cl41(O44	109.6(4)

O41(Cl41(O44	109.9(4)

O43(Cl41(O42	108.2(4)

O41(Cl41(O42	110.1(4)

O44(Cl41(O42	108.7(5)

O51(Cl51(O52	110.2(4)

O51(Cl51(O54	110.6(4)

O52(Cl51(O54	110.3(4)

O51(Cl51(O53	108.1(4)

O52(Cl51(O53	107.4(4)

O54(Cl51(O53	110.2(4)

H61A(O61(H61B	108(5)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	29(4) 	25(4)	29(4) 	5(3)	7(3) 	6(3)

C2	34(4) 	28(4)	28(4) 	(1(3)	8(3) 	4(3)

C3	26(4) 	38(4)	26(4) 	5(3)	9(3) 	5(3)

C4	23(4) 	31(4)	29(4) 	0(3)	6(3) 	(2(3)

C5	27(4) 	27(4)	19(4) 	0(3)	12(3) 	(1(3)

C6	24(3) 	27(4)	15(3) 	(4(3)	6(3) 	0(3)

C7	20(3) 	28(4)	21(4) 	(5(3)	7(3) 	(3(3)

C8	20(3) 	26(4)	25(4) 	(1(3)	7(3) 	2(3)

C9	28(4) 	31(4)	25(4) 	(3(3)	7(3) 	(2(3)

C10	31(4) 	27(4)	25(4) 	(4(3)	9(3) 	1(3)

C11	27(4) 	26(4)	22(4) 	(1(3)	6(3) 	3(3)

C12	24(3) 	32(4)	22(4) 	0(3)	8(3) 	(3(3)

C13	25(3) 	29(4)	16(3) 	2(3)	5(3) 	(3(3)

C14	23(3) 	26(4)	31(4) 	(1(3)	8(3) 	0(3)

C15	28(4) 	28(4)	29(4) 	9(3)	8(3) 	3(3)

C16	29(4) 	29(4)	23(4) 	1(3)	6(3) 	(2(3)

C17	20(3) 	31(4)	19(4) 	(1(3)	6(3) 	(2(3)

C18	21(3) 	27(4)	20(4) 	(3(3)	7(3) 	(2(3)

C19	26(4) 	31(4)	20(4) 	(7(3)	8(3) 	(6(3)

C20	20(3) 	25(4)	29(4) 	6(3)	9(3) 	(1(3)

C21	26(4) 	35(4)	20(4) 	1(3)	8(3) 	(2(3)

C22	31(4) 	33(4)	21(4) 	(5(3)	11(3) 	(4(3)

C23	34(4) 	26(4)	32(4) 	(1(3)	14(3) 	0(3)

C24	27(4) 	30(4)	26(4) 	(2(3)	10(3) 	1(3)

N1	24(3) 	30(3)	26(3) 	(4(3)	10(3) 	(2(3)

N2	27(3) 	29(3)	26(3) 	2(3)	13(3) 	4(3)

N3	22(3) 	23(3)	23(3) 	(1(2)	6(2) 	(2(2)

N4	21(3) 	22(3)	21(3) 	(5(2)	6(2) 	1(2)

N5	29(3) 	29(3)	16(3) 	(3(2)	4(2) 	5(3)

N6	21(3) 	22(3)	20(3) 	0(2)	6(2) 	1(2)

N7	24(3) 	28(3)	20(3) 	4(3)	7(2) 	0(3)

N8	29(3) 	28(3)	21(3) 	3(3)	5(3) 	1(3)

N9	25(3) 	28(3)	19(3) 	0(3)	4(2) 	0(3)

N10	26(3) 	26(3)	18(3) 	(2(2)	2(2) 	(2(3)

N11	17(3) 	16(3)	6(2) 	0(2)	(2(2) 	1(2)

N12	24(3) 	29(3)	24(3) 	(2(3)	9(2) 	(1(3)

O1	29(3) 	29(3)	25(3) 	(1(2)	9(2) 	0(2)

O11	26(3) 	31(3)	27(3) 	(1(2)	11(2) 	(3(2)

O12	28(3) 	35(3)	23(3) 	2(2)	11(2) 	3(3)

Zn1	21(1) 	25(1)	20(1) 	0(1)	4(1) 	1(1)

Zn2	22(1) 	26(1)	17(1) 	0(1)	4(1) 	0(1)

O31	43(3) 	34(3)	36(3) 	11(3)	0(3) 	(8(3)

O32	54(4) 	29(3)	45(4) 	1(3)	9(3) 	(10(3)

O33	63(5) 	77(5)	41(4) 	(3(4)	31(4) 	(15(4)

O34	52(4) 	38(4)	50(4) 	4(3)	12(3) 	13(3)

Cl31	32(1) 	29(1)	22(1) 	2(1)	6(1) 	(3(1)

O41	43(3) 	40(3)	33(3) 	4(3)	10(3) 	4(3)

O42	38(3) 	61(4)	34(3) 	6(3)	7(3) 	(10(3)

O43	28(3) 	43(4)	60(4) 	(5(3)	13(3) 	5(3)

O44	86(5) 	64(5)	23(3) 	4(3)	20(3) 	36(4)

Cl41	27(1) 	43(1)	22(1) 	(2(1)	6(1) 	6(1)

O51	59(4) 	48(4)	20(3) 	9(3)	14(3) 	20(3)

O52	40(3) 	43(3)	46(4) 	3(3)	18(3) 	(15(3)

O53	30(3) 	52(4)	34(3) 	(10(3)	3(2) 	(4(3)

O54	41(3) 	38(3)	36(3) 	(5(3)	21(3) 	5(3)

Cl51	24(1) 	27(1)	22(1) 	3(1)	6(1) 	1(1)

O61	33(3) 	36(3)	30(3) 	(2(3)	11(2) 	(4(3)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H1	1191	4493	1544	34	1

H2	16	4749	897	36	1

H3	(672	3153	293	36	1

H4	(166	1304	471	34	1

H9	2100	(2944	(97	34	1

H10	2758	(4613	410	33	1

H11	3528	(4667	1874	30	1

H14	4317	(4478	3268	32	1

H15	5080	(4072	4684	34	1

H16	5009	(2291	5395	33	1

H21	3682	3223	5113	32	1

H22	3433	5170	5240	33	1

H23	2716	6104	3957	36	1

H24	2167	5056	2658	33	1

H2A	1008	(889	1271	32	1

H2B	359	(173	1114	32	1

H5A	1412	(200	(105	30	1

H5B	1631	(1368	(379	30	1

H8A	4369	493	5723	32	1

H8B	4688	(705	5928	32	1

H1A	2580(100)	3700(200)	800(200)	400(200)	1

H1B	3080(30)	2920(90)	1130(80)	90(50)	1

H11A	3900(30)	650(20)	2080(40)	12(18)	1

H11B	4189(17)	(380(50)	2270(50)	50(30)	1

H12A	2070(40)	(280(40)	3510(60)	60(30)	1

H12B	2090(40)	(1430(50)	3360(70)	90(50)	1

H61A	540(80)	3650(30)	3830(70)	120(60)	1

H61B	690(40)	4610(60)	3420(30)	20(20)	1