|  | University of Southampton · School of Chemistry # EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	04src1115

Empirical formula 	C24H28Cl3N12O16Zn2

Formula weight 	977.67

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/c

Unit cell dimensions	a = 20.502(4) Å	a = 90°

b = 11.575(2) Å	b = 107.67(2)°

c = 15.431(3) Å	g  = 90°

Volume	3489.2(12) Å3

Z	4

Density (calculated)	1.861 Mg / m3

Absorption coefficient	1.697 mm-1

F(000)	1980

Crystal	Plate; Yellow

Crystal size	0.16 ´ 0.14 ´ 0.03 mm3

q range for data collection	2.92 - 27.48°

Index ranges	-26 £ h £ 26, -14 £ k £ 15, -19 £ l £ 19

Reflections collected	37319

Independent reflections	7835 [Rint = 0.1064]

Completeness to q = 27.48°	98.1 %

Absorption correction	Semi-empirical from equivalents

Max. and min. transmission	0.9509 and 0.7730

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	7835 / 18 / 546

Goodness-of-fit on F2	1.148

Final R indices [F2 > 2s(F2)]	R1 = 0.0821, wR2 = 0.1963

R indices (all data)	R1 = 0.1130, wR2 = 0.2127

Largest diff. peak and hole	1.075 and -0.771 e Å-3

Diffractometer: Nonius KappaCCD area detector (f scans and w scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307-326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33-37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421-426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467-473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP3 for Windows (L. J. Farrugia, J. Appl. Crystallogr. 1997, 30, 565).

Special details:

All hydrogen atoms were fixed.

Table 2. Atomic coordinates [´ 104], equivalent isotropic displacement parameters [Å2 ´ 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	908(4)	3837(7)	1337(5)	28(2)	1

C2	210(4)	3999(7)	934(5)	30(2)	1

C3	-196(4)	3060(7)	592(5)	30(2)	1

C4	104(4)	1969(7)	691(5)	29(2)	1

C5	795(4)	1866(6)	1110(5)	23(2)	1

C6	1158(4)	736(6)	1231(5)	22(1)	1

C7	2098(4)	-955(6)	859(5)	23(2)	1

C8	2498(3)	-2062(6)	1094(5)	24(2)	1

C9	2415(4)	-2983(7)	498(5)	28(2)	1

C10	2806(4)	-3962(7)	800(5)	27(2)	1

C11	3261(4)	-3996(7)	1658(5)	25(2)	1

C12	3322(4)	-3032(7)	2199(5)	26(2)	1

C13	3820(4)	-2931(6)	3146(5)	24(2)	1

C14	4299(4)	-3760(7)	3559(5)	27(2)	1

C15	4742(4)	-3521(7)	4389(5)	29(2)	1

C16	4702(4)	-2467(7)	4813(5)	28(2)	1

C17	4207(3)	-1695(6)	4365(5)	23(2)	1

C18	4114(3)	-529(6)	4696(5)	23(1)	1

C19	3202(4)	1806(7)	3679(5)	25(2)	1

C20	3054(4)	3018(6)	3807(5)	24(2)	1

C21	3371(4)	3615(7)	4616(5)	27(2)	1

C22	3234(4)	4759(7)	4690(5)	28(2)	1

C23	2799(4)	5298(7)	3939(6)	30(2)	1

C24	2481(4)	4678(7)	3160(5)	27(2)	1

N1	1194(3)	2790(6)	1441(4)	26(1)	1

N2	803(3)	-212(6)	1202(4)	26(1)	1

N3	1820(3)	814(5)	1357(4)	23(1)	1

N4	2202(3)	-224(5)	1538(4)	22(1)	1

N5	1666(3)	-827(6)	33(4)	25(1)	1

N6	2950(3)	-2086(5)	1935(4)	21(1)	1

N7	3764(3)	-1938(5)	3539(4)	24(1)	1

N8	4425(3)	-212(6)	5543(4)	26(1)	1

N9	3712(3)	132(5)	4071(4)	24(1)	1

N10	3619(3)	1249(5)	4350(4)	24(1)	1

N11	2919(3)	1373(5)	2867(3)	14(1)	1

N12	2610(3)	3535(5)	3101(4)	25(1)	1

O1	2698(3)	3122(5)	1171(4)	28(1)	1

O11	3803(3)	-60(5)	2052(4)	27(1)	1

O12	2332(3)	-825(5)	3463(4)	28(1)	1

Zn1	2218(1)	2378(1)	2004(1)	22(1)	1

Zn2	3072(1)	-510(1)	2786(1)	22(1)	1

O31	1587(3)	7160(5)	3325(4)	41(2)	1

O32	719(3)	5923(5)	2518(4)	44(2)	1

O33	1252(4)	7152(7)	1734(5)	57(2)	1

O34	534(3)	7916(6)	2482(5)	47(2)	1

Cl31	1010(1)	7039(2)	2499(1)	28(1)	1

O41	1460(3)	418(5)	4658(4)	39(1)	1

O42	1855(3)	2303(6)	4498(4)	45(2)	1

O43	699(3)	1876(6)	3934(5)	44(2)	1

O44	1453(4)	1109(7)	3218(4)	57(2)	1

Cl41	1362(1)	1418(2)	4078(1)	31(1)	1

O51	5029(3)	1986(6)	2974(4)	42(2)	1

O52	4945(3)	3709(5)	2154(4)	42(2)	1

O53	4062(3)	2362(6)	1740(4)	40(1)	1

O54	4260(3)	3428(5)	3105(4)	36(1)	1

Cl51	4579(1)	2880(2)	2510(1)	24(1)	1

O61	616(3)	4362(5)	3895(4)	33(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1-N1	1.335(10)

C1-C2	1.388(11)

C1-H1	0.9500

C2-C3	1.373(11)

C2-H2	0.9500

C3-C4	1.393(11)

C3-H3	0.9500

C4-C5	1.372(10)

C4-H4	0.9500

C5-N1	1.349(9)

C5-C6	1.489(10)

C6-N2	1.311(9)

C6-N3	1.314(9)

C7-N4	1.313(9)

C7-N5	1.322(9)

C7-C8	1.505(10)

C8-N6	1.346(9)

C8-C9	1.384(11)

C9-C10	1.384(11)

C9-H9	0.9500

C10-C11	1.370(10)

C10-H10	0.9500

C11-C12	1.376(11)

C11-H11	0.9500

C12-N6	1.325(10)

C12-C13	1.512(10)

C13-N7	1.321(10)

C13-C14	1.382(10)

C14-C15	1.356(11)

C14-H14	0.9500

C15-C16	1.399(11)

C15-H15	0.9500

C16-C17	1.372(10)

C16-H16	0.9500

C17-N7	1.351(9)

C17-C18	1.476(10)

C18-N9	1.309(9)

C18-N8	1.321(9)

C19-N10	1.296(10)

C19-N11	1.311(9)

C19-C20	1.461(11)

C20-N12	1.332(9)

C20-C21	1.402(11)

C21-C22	1.366(11)

C21-H21	0.9500

C22-C23	1.379(11)

C22-H22	0.9500

C23-C24	1.383(11)

C23-H23	0.9500

C24-N12	1.357(10)

C24-H24	0.9500

N1-Zn1	2.070(6)

N2-H2A	0.8800

N2-H2B	0.8800

N3-N4	1.415(8)

N3-Zn1	2.109(6)

N4-Zn2	2.216(6)

N5-H5A	0.8800

N5-H5B	0.8800

N6-Zn2	2.217(6)

N7-Zn2	2.258(6)

N8-H8A	0.8800

N8-H8B	0.8800

N9-N10	1.394(9)

N9-Zn2	2.151(6)

N11-Zn1	2.008(5)

N11-Zn2	2.210(5)

N12-Zn1	2.116(6)

O1-Zn1	2.032(5)

O1-H1A	0.841(19)

O1-H1B	0.847(19)

O11-Zn2	2.198(5)

O11-H11A	0.848(19)

O11-H11B	0.85(2)

O12-Zn2	2.117(5)

O12-H12A	0.845(19)

O12-H12B	0.84(2)

O31-Cl31	1.459(6)

O32-Cl31	1.428(6)

O33-Cl31	1.420(7)

O34-Cl31	1.403(7)

O41-Cl41	1.440(6)

O42-Cl41	1.446(7)

O43-Cl41	1.412(6)

O44-Cl41	1.440(6)

O51-Cl51	1.426(6)

O52-Cl51	1.427(6)

O53-Cl51	1.460(6)

O54-Cl51	1.428(6)

O61-H61A	0.84(2)

O61-H61B	0.84(2)

N1-C1-C2	122.1(7)

N1-C1-H1	118.9

C2-C1-H1	118.9

C3-C2-C1	119.2(7)

C3-C2-H2	120.4

C1-C2-H2	120.4

C2-C3-C4	118.6(7)

C2-C3-H3	120.7

C4-C3-H3	120.7

C5-C4-C3	119.3(7)

C5-C4-H4	120.3

C3-C4-H4	120.3

N1-C5-C4	122.0(7)

N1-C5-C6	115.2(6)

C4-C5-C6	122.8(7)

N2-C6-N3	127.0(7)

N2-C6-C5	118.7(6)

N3-C6-C5	114.4(6)

N4-C7-N5	126.6(7)

N4-C7-C8	114.3(6)

N5-C7-C8	119.0(6)

N6-C8-C9	122.3(7)

N6-C8-C7	114.6(6)

C9-C8-C7	123.2(7)

C8-C9-C10	117.7(7)

C8-C9-H9	121.1

C10-C9-H9	121.1

C11-C10-C9	120.2(7)

C11-C10-H10	119.9

C9-C10-H10	119.9

C10-C11-C12	118.2(7)

C10-C11-H11	120.9

C12-C11-H11	120.9

N6-C12-C11	123.1(7)

N6-C12-C13	112.9(6)

C11-C12-C13	124.0(7)

N7-C13-C14	122.7(7)

N7-C13-C12	112.6(6)

C14-C13-C12	124.7(7)

C15-C14-C13	118.2(7)

C15-C14-H14	120.9

C13-C14-H14	120.9

C14-C15-C16	120.2(7)

C14-C15-H15	119.9

C16-C15-H15	119.9

C17-C16-C15	118.2(7)

C17-C16-H16	120.9

C15-C16-H16	120.9

N7-C17-C16	121.5(7)

N7-C17-C18	113.4(6)

C16-C17-C18	125.1(7)

N9-C18-N8	125.1(7)

N9-C18-C17	113.4(6)

N8-C18-C17	121.5(7)

N10-C19-N11	124.5(7)

N10-C19-C20	118.9(7)

N11-C19-C20	116.5(7)

N12-C20-C21	121.6(7)

N12-C20-C19	116.1(7)

C21-C20-C19	122.3(7)

C22-C21-C20	120.1(7)

C22-C21-H21	120.0

C20-C21-H21	120.0

C21-C22-C23	117.7(7)

C21-C22-H22	121.1

C23-C22-H22	121.1

C22-C23-C24	120.6(7)

C22-C23-H23	119.7

C24-C23-H23	119.7

N12-C24-C23	121.0(7)

N12-C24-H24	119.5

C23-C24-H24	119.5

C1-N1-C5	118.7(6)

C1-N1-Zn1	127.8(5)

C5-N1-Zn1	113.4(5)

C6-N2-H2A	120.0

C6-N2-H2B	120.0

H2A-N2-H2B	120.0

C6-N3-N4	117.1(6)

C6-N3-Zn1	111.3(5)

N4-N3-Zn1	121.6(4)

C7-N4-N3	116.4(6)

C7-N4-Zn2	119.3(5)

N3-N4-Zn2	123.3(4)

C7-N5-H5A	120.0

C7-N5-H5B	120.0

H5A-N5-H5B	120.0

C12-N6-C8	118.5(6)

C12-N6-Zn2	123.2(5)

C8-N6-Zn2	118.3(5)

C13-N7-C17	119.2(6)

C13-N7-Zn2	122.0(5)

C17-N7-Zn2	118.1(5)

C18-N8-H8A	120.0

C18-N8-H8B	120.0

H8A-N8-H8B	120.0

C18-N9-N10	115.3(6)

C18-N9-Zn2	123.3(5)

N10-N9-Zn2	120.2(4)

C19-N10-N9	109.5(6)

C19-N11-Zn1	115.6(5)

C19-N11-Zn2	113.7(5)

Zn1-N11-Zn2	128.2(2)

C20-N12-C24	118.9(7)

C20-N12-Zn1	111.6(5)

C24-N12-Zn1	129.5(5)

Zn1-O1-H1A	129(4)

Zn1-O1-H1B	125(4)

H1A-O1-H1B	106(4)

Zn2-O11-H11A	113(3)

Zn2-O11-H11B	114(3)

H11A-O11-H11B	103(4)

Zn2-O12-H12A	119(4)

Zn2-O12-H12B	122(4)

H12A-O12-H12B	106(4)

N11-Zn1-O1	106.2(2)

N11-Zn1-N1	147.4(2)

O1-Zn1-N1	105.1(2)

N11-Zn1-N3	85.0(2)

O1-Zn1-N3	104.9(2)

N1-Zn1-N3	78.5(2)

N11-Zn1-N12	79.3(2)

O1-Zn1-N12	95.7(2)

N1-Zn1-N12	106.3(2)

N3-Zn1-N12	157.0(2)

O12-Zn2-N9	86.1(2)

O12-Zn2-O11	175.8(2)

N9-Zn2-O11	94.1(2)

O12-Zn2-N11	90.4(2)

N9-Zn2-N11	70.4(2)

O11-Zn2-N11	85.7(2)

O12-Zn2-N4	87.0(2)

N9-Zn2-N4	148.7(2)

O11-Zn2-N4	90.7(2)

N11-Zn2-N4	79.1(2)

O12-Zn2-N6	100.5(2)

N9-Zn2-N6	139.2(2)

O11-Zn2-N6	82.0(2)

N11-Zn2-N6	148.5(2)

N4-Zn2-N6	72.1(2)

O12-Zn2-N7	92.9(2)

N9-Zn2-N7	70.5(2)

O11-Zn2-N7	91.1(2)

N11-Zn2-N7	140.4(2)

N4-Zn2-N7	140.4(2)

N6-Zn2-N7	69.0(2)

O34-Cl31-O33	109.6(5)

O34-Cl31-O32	111.2(4)

O33-Cl31-O32	110.7(4)

O34-Cl31-O31	108.8(4)

O33-Cl31-O31	108.8(4)

O32-Cl31-O31	107.6(4)

O43-Cl41-O41	110.2(4)

O43-Cl41-O44	109.6(4)

O41-Cl41-O44	109.9(4)

O43-Cl41-O42	108.2(4)

O41-Cl41-O42	110.1(4)

O44-Cl41-O42	108.7(5)

O51-Cl51-O52	110.2(4)

O51-Cl51-O54	110.6(4)

O52-Cl51-O54	110.3(4)

O51-Cl51-O53	108.1(4)

O52-Cl51-O53	107.4(4)

O54-Cl51-O53	110.2(4)

H61A-O61-H61B	108(5)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2´ 103]. The anisotropic displacement

factor exponent takes the form: -2p 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	29(4) 	25(4)	29(4) 	5(3)	7(3) 	6(3)

C2	34(4) 	28(4)	28(4) 	-1(3)	8(3) 	4(3)

C3	26(4) 	38(4)	26(4) 	5(3)	9(3) 	5(3)

C4	23(4) 	31(4)	29(4) 	0(3)	6(3) 	-2(3)

C5	27(4) 	27(4)	19(4) 	0(3)	12(3) 	-1(3)

C6	24(3) 	27(4)	15(3) 	-4(3)	6(3) 	0(3)

C7	20(3) 	28(4)	21(4) 	-5(3)	7(3) 	-3(3)

C8	20(3) 	26(4)	25(4) 	-1(3)	7(3) 	2(3)

C9	28(4) 	31(4)	25(4) 	-3(3)	7(3) 	-2(3)

C10	31(4) 	27(4)	25(4) 	-4(3)	9(3) 	1(3)

C11	27(4) 	26(4)	22(4) 	-1(3)	6(3) 	3(3)

C12	24(3) 	32(4)	22(4) 	0(3)	8(3) 	-3(3)

C13	25(3) 	29(4)	16(3) 	2(3)	5(3) 	-3(3)

C14	23(3) 	26(4)	31(4) 	-1(3)	8(3) 	0(3)

C15	28(4) 	28(4)	29(4) 	9(3)	8(3) 	3(3)

C16	29(4) 	29(4)	23(4) 	1(3)	6(3) 	-2(3)

C17	20(3) 	31(4)	19(4) 	-1(3)	6(3) 	-2(3)

C18	21(3) 	27(4)	20(4) 	-3(3)	7(3) 	-2(3)

C19	26(4) 	31(4)	20(4) 	-7(3)	8(3) 	-6(3)

C20	20(3) 	25(4)	29(4) 	6(3)	9(3) 	-1(3)

C21	26(4) 	35(4)	20(4) 	1(3)	8(3) 	-2(3)

C22	31(4) 	33(4)	21(4) 	-5(3)	11(3) 	-4(3)

C23	34(4) 	26(4)	32(4) 	-1(3)	14(3) 	0(3)

C24	27(4) 	30(4)	26(4) 	-2(3)	10(3) 	1(3)

N1	24(3) 	30(3)	26(3) 	-4(3)	10(3) 	-2(3)

N2	27(3) 	29(3)	26(3) 	2(3)	13(3) 	4(3)

N3	22(3) 	23(3)	23(3) 	-1(2)	6(2) 	-2(2)

N4	21(3) 	22(3)	21(3) 	-5(2)	6(2) 	1(2)

N5	29(3) 	29(3)	16(3) 	-3(2)	4(2) 	5(3)

N6	21(3) 	22(3)	20(3) 	0(2)	6(2) 	1(2)

N7	24(3) 	28(3)	20(3) 	4(3)	7(2) 	0(3)

N8	29(3) 	28(3)	21(3) 	3(3)	5(3) 	1(3)

N9	25(3) 	28(3)	19(3) 	0(3)	4(2) 	0(3)

N10	26(3) 	26(3)	18(3) 	-2(2)	2(2) 	-2(3)

N11	17(3) 	16(3)	6(2) 	0(2)	-2(2) 	1(2)

N12	24(3) 	29(3)	24(3) 	-2(3)	9(2) 	-1(3)

O1	29(3) 	29(3)	25(3) 	-1(2)	9(2) 	0(2)

O11	26(3) 	31(3)	27(3) 	-1(2)	11(2) 	-3(2)

O12	28(3) 	35(3)	23(3) 	2(2)	11(2) 	3(3)

Zn1	21(1) 	25(1)	20(1) 	0(1)	4(1) 	1(1)

Zn2	22(1) 	26(1)	17(1) 	0(1)	4(1) 	0(1)

O31	43(3) 	34(3)	36(3) 	11(3)	0(3) 	-8(3)

O32	54(4) 	29(3)	45(4) 	1(3)	9(3) 	-10(3)

O33	63(5) 	77(5)	41(4) 	-3(4)	31(4) 	-15(4)

O34	52(4) 	38(4)	50(4) 	4(3)	12(3) 	13(3)

Cl31	32(1) 	29(1)	22(1) 	2(1)	6(1) 	-3(1)

O41	43(3) 	40(3)	33(3) 	4(3)	10(3) 	4(3)

O42	38(3) 	61(4)	34(3) 	6(3)	7(3) 	-10(3)

O43	28(3) 	43(4)	60(4) 	-5(3)	13(3) 	5(3)

O44	86(5) 	64(5)	23(3) 	4(3)	20(3) 	36(4)

Cl41	27(1) 	43(1)	22(1) 	-2(1)	6(1) 	6(1)

O51	59(4) 	48(4)	20(3) 	9(3)	14(3) 	20(3)

O52	40(3) 	43(3)	46(4) 	3(3)	18(3) 	-15(3)

O53	30(3) 	52(4)	34(3) 	-10(3)	3(2) 	-4(3)

O54	41(3) 	38(3)	36(3) 	-5(3)	21(3) 	5(3)

Cl51	24(1) 	27(1)	22(1) 	3(1)	6(1) 	1(1)

O61	33(3) 	36(3)	30(3) 	-2(3)	11(2) 	-4(3)

Table 5. Hydrogen coordinates [´ 104] and isotropic displacement parameters [Å2 ´ 103].

Atom 	x	y	z	Ueq	S.o.f.

H1	1191	4493	1544	34	1

H2	16	4749	897	36	1

H3	-672	3153	293	36	1

H4	-166	1304	471	34	1

H9	2100	-2944	-97	34	1

H10	2758	-4613	410	33	1

H11	3528	-4667	1874	30	1

H14	4317	-4478	3268	32	1

H15	5080	-4072	4684	34	1

H16	5009	-2291	5395	33	1

H21	3682	3223	5113	32	1

H22	3433	5170	5240	33	1

H23	2716	6104	3957	36	1

H24	2167	5056	2658	33	1

H2A	1008	-889	1271	32	1

H2B	359	-173	1114	32	1

H5A	1412	-200	-105	30	1

H5B	1631	-1368	-379	30	1

H8A	4369	493	5723	32	1

H8B	4688	-705	5928	32	1

H1A	2580(100)	3700(200)	800(200)	400(200)	1

H1B	3080(30)	2920(90)	1130(80)	90(50)	1

H11A	3900(30)	650(20)	2080(40)	12(18)	1

H11B	4189(17)	-380(50)	2270(50)	50(30)	1

H12A	2070(40)	-280(40)	3510(60)	60(30)	1

H12B	2090(40)	-1430(50)	3360(70)	90(50)	1

H61A	540(80)	3650(30)	3830(70)	120(60)	1

H61B	690(40)	4610(60)	3420(30)	20(20)	1