|  | University of Southampton · School of Chemistry # EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	04src1116

Empirical formula 	C26H35Cl3Mn2N13O21.50

Formula weight 	1089.90

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P-1

Unit cell dimensions	a = 9.1978(8) Å	a = 88.34(2)°

b = 12.711(4) Å	b = 80.737(12)°

c = 18.081(5) Å	g  = 86.262(14)°

Volume	2081.7(8) Å3

Z	2

Density (calculated)	1.739 Mg / m3

Absorption coefficient	0.898 mm-1

F(000)	1110

Crystal	Slab; Orange

Crystal size	0.24 ´ 0.10 ´ 0.04 mm3

q range for data collection	3.18 - 27.48°

Index ranges	-11 £ h £ 11, -16 £ k £ 16, -23 £ l £ 23

Reflections collected	39474

Independent reflections	9493 [Rint = 0.0750]

Completeness to q = 27.48°	99.4 %

Absorption correction	Semi-empirical from equivalents

Max. and min. transmission	0.9650 and 0.8133

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	9493 / 632 / 664

Goodness-of-fit on F2	1.047

Final R indices [F2 > 2s(F2)]	R1 = 0.0943, wR2 = 0.2176

R indices (all data)	R1 = 0.1575, wR2 = 0.2472

Largest diff. peak and hole	1.719 and -1.605 e Å-3

Diffractometer: Nonius KappaCCD area detector (f scans and w scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307-326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33-37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421-426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467-473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP3 for Windows (L. J. Farrugia, J. Appl. Crystallogr. 1997, 30, 565).

Special details:

All hydrogen atoms were fixed.

There was some disordered solvent, including a half occupied water molecule.

Table 2. Atomic coordinates [´ 104], equivalent isotropic displacement parameters [Å2 ´ 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	660(7)	9807(6)	2291(4)	43(2)	1

C2	1194(8)	10503(7)	1738(5)	52(2)	1

C3	2210(8)	10150(6)	1150(5)	47(2)	1

C4	2689(8)	9100(6)	1137(4)	42(2)	1

C5	2116(7)	8448(6)	1720(4)	36(1)	1

C6	2577(7)	7312(6)	1749(4)	34(1)	1

C7	2029(7)	4968(5)	1779(3)	31(1)	1

C8	2743(7)	3915(5)	1918(4)	32(1)	1

C9	3177(8)	3162(6)	1377(4)	41(2)	1

C10	3965(8)	2263(6)	1564(4)	45(2)	1

C11	4263(8)	2103(6)	2290(4)	40(2)	1

C12	3767(7)	2885(5)	2800(4)	31(1)	1

C13	4021(7)	2832(5)	3601(4)	30(1)	1

C14	4664(7)	1972(5)	3936(4)	33(1)	1

C15	4782(7)	2018(5)	4679(4)	34(1)	1

C16	4259(7)	2933(5)	5083(3)	30(1)	1

C17	3648(6)	3757(5)	4712(3)	25(1)	1

C18	3005(6)	4776(5)	5054(3)	25(1)	1

C19	919(7)	6816(5)	4464(3)	29(1)	1

C20	-45(7)	7789(5)	4683(4)	31(1)	1

C21	-307(8)	8158(5)	5402(4)	37(2)	1

C22	-1220(8)	9066(6)	5554(4)	43(2)	1

C23	-1840(7)	9553(5)	4982(5)	43(2)	1

C24	-1519(7)	9153(5)	4282(4)	40(2)	1

N1	1095(6)	8786(5)	2279(3)	37(1)	1

N2	3894(6)	6991(5)	1379(3)	47(2)	1

N3	1634(6)	6712(4)	2136(3)	30(1)	1

N4	2200(6)	5672(4)	2260(3)	30(1)	1

N5	1380(7)	5147(5)	1181(3)	43(2)	1

N6	3029(5)	3769(4)	2623(3)	27(1)	1

N7	3525(5)	3710(4)	3981(3)	24(1)	1

N8	3343(5)	5063(4)	5711(3)	29(1)	1

N9	2139(5)	5311(4)	4669(3)	27(1)	1

N10	1408(5)	6236(4)	4986(3)	27(1)	1

N12	-631(6)	8270(4)	4118(3)	34(1)	1

O1	1156(5)	6598(4)	3755(2)	32(1)	1

O2	-1952(5)	8237(4)	2554(3)	46(1)	1

O3	-1332(5)	6139(5)	3073(3)	55(2)	1

O4	153(5)	4366(4)	3617(2)	31(1)	1

O5	4538(5)	5914(4)	3296(3)	34(1)	1

Mn1	-39(1)	7509(1)	2998(1)	33(1)	1

Mn2	2383(1)	5087(1)	3449(1)	26(1)	1

O11	3080(8)	8524(7)	3843(4)	93(2)	1

O12	4823(10)	8062(5)	2837(6)	111(3)	1

O13	3721(9)	9748(5)	2914(4)	79(2)	1

O14	5376(7)	9234(6)	3693(4)	83(2)	1

Cl11	4247(2)	8900(1)	3322(1)	37(1)	1

O21	7069(8)	6836(7)	724(7)	128(4)	1

O22	9233(10)	6245(6)	61(4)	94(3)	1

O23	8436(10)	7993(6)	-5(4)	94(2)	1

O24	9242(9)	7281(5)	1052(4)	82(2)	1

Cl21	8491(2)	7106(1)	467(1)	38(1)	1

O31	-221(6)	12697(5)	2708(4)	69(2)	1

O32	-2674(6)	13348(5)	3039(4)	63(2)	1

O33	-1961(10)	12395(9)	1952(5)	130(3)	1

O34	-2104(9)	11516(6)	2957(7)	133(4)	1

Cl33	-1736(2)	12574(2)	2652(1)	59(1)	1

C41	7970(20)	190(11)	1065(12)	168(7)	1

N41	6603(13)	-188(9)	999(5)	96(3)	1

O41	5932(10)	328(8)	574(4)	111(3)	1

O42	6225(11)	-1041(9)	1355(5)	129(4)	1

O71	6818(12)	5597(12)	2274(7)	68(4)	0.50

C51	7230(20)	3436(17)	403(11)	73(5)	0.50

N51	6091(12)	4354(10)	471(8)	54(3)	0.50

O51	6097(11)	4554(13)	-201(8)	165(9)	0.50

O52	5616(13)	4725(9)	1081(7)	61(3)	0.50

C61	7163(17)	4176(14)	789(9)	47(3)	0.50

N61	7013(12)	4751(9)	1484(6)	36(2)	0.50

O61	5785(11)	4988(8)	1808(6)	42(2)	0.50

O62	8138(11)	4992(9)	1693(6)	49(3)	0.50

Table 3. Bond lengths [Å] and angles [°].

C1-N1	1.333(9)

C1-C2	1.368(10)

C1-H1	0.9500

C2-C3	1.364(12)

C2-H2	0.9500

C3-C4	1.377(11)

C3-H3	0.9500

C4-C5	1.380(9)

C4-H4	0.9500

C5-N1	1.325(9)

C5-C6	1.479(10)

C6-N3	1.298(8)

C6-N2	1.331(9)

C7-N4	1.300(8)

C7-N5	1.324(8)

C7-C8	1.485(10)

C8-N6	1.347(8)

C8-C9	1.383(10)

C9-C10	1.376(11)

C9-H9	0.9500

C10-C11	1.389(10)

C10-H10	0.9500

C11-C12	1.381(10)

C11-H11	0.9500

C12-N6	1.332(8)

C12-C13	1.502(9)

C13-N7	1.343(8)

C13-C14	1.380(9)

C14-C15	1.369(9)

C14-H14	0.9500

C15-C16	1.407(9)

C15-H15	0.9500

C16-C17	1.366(8)

C16-H16	0.9500

C17-N7	1.348(7)

C17-C18	1.497(9)

C18-N9	1.290(7)

C18-N8	1.342(8)

C19-O1	1.299(7)

C19-N10	1.300(8)

C19-C20	1.498(9)

C20-N12	1.344(8)

C20-C21	1.375(10)

C21-C22	1.390(9)

C21-H21	0.9500

C22-C23	1.374(11)

C22-H22	0.9500

C23-C24	1.358(11)

C23-H23	0.9500

C24-N12	1.355(9)

C24-H24	0.9500

N1-Mn1	2.252(5)

N2-H2A	0.8800

N2-H2B	0.8800

N3-N4	1.414(7)

N3-Mn1	2.222(6)

N4-Mn2	2.284(5)

N5-H5A	0.8800

N5-H5B	0.8800

N6-Mn2	2.264(5)

N7-Mn2	2.253(5)

N8-H8A	0.8800

N8-H8B	0.8800

N9-N10	1.405(7)

N9-Mn2	2.204(5)

N12-Mn1	2.242(6)

O1-Mn1	2.156(4)

O1-Mn2	2.201(5)

O2-Mn1	2.190(5)

O2-H2WA	0.838(18)

O2-H2WB	0.829(18)

O3-Mn1	2.161(5)

O3-H3WA	0.839(18)

O3-H3WB	0.841(19)

O4-Mn2	2.274(4)

O4-H4WA	0.819(18)

O4-H4WB	0.824(18)

O5-Mn2	2.278(5)

O5-H5WA	0.831(19)

O5-H5WB	0.842(19)

O11-Cl11	1.409(6)

O12-Cl11	1.419(7)

O13-Cl11	1.393(5)

O14-Cl11	1.417(6)

O21-Cl21	1.378(8)

O22-Cl21	1.411(7)

O23-Cl21	1.397(7)

O24-Cl21	1.383(6)

O31-Cl33	1.431(6)

O32-Cl33	1.392(6)

O33-Cl33	1.344(8)

O34-Cl33	1.477(9)

C41-N41	1.401(19)

C41-H41A	0.9800

C41-H41B	0.9800

C41-H41C	0.9800

N41-O41	1.214(11)

N41-O42	1.283(14)

O71-H71A	0.84(2)

O71-H71B	0.84(2)

C51-N51	1.51(2)

C51-H51A	0.9800

C51-H51B	0.9800

C51-H51C	0.9800

N51-O52	1.217(17)

N51-O51	1.23(2)

C61-N61	1.45(2)

C61-H61A	0.9800

C61-H61B	0.9800

C61-H61C	0.9800

N61-O61	1.208(14)

N61-O62	1.217(14)

N1-C1-C2	122.4(7)

N1-C1-H1	118.8

C2-C1-H1	118.8

C3-C2-C1	119.4(8)

C3-C2-H2	120.3

C1-C2-H2	120.3

C2-C3-C4	118.8(7)

C2-C3-H3	120.6

C4-C3-H3	120.6

C3-C4-C5	118.5(7)

C3-C4-H4	120.7

C5-C4-H4	120.7

N1-C5-C4	122.6(7)

N1-C5-C6	115.6(6)

C4-C5-C6	121.8(7)

N3-C6-N2	125.7(7)

N3-C6-C5	116.0(6)

N2-C6-C5	118.3(6)

N4-C7-N5	125.4(6)

N4-C7-C8	113.8(5)

N5-C7-C8	120.7(6)

N6-C8-C9	121.6(6)

N6-C8-C7	113.8(6)

C9-C8-C7	124.5(6)

C10-C9-C8	118.5(7)

C10-C9-H9	120.8

C8-C9-H9	120.8

C9-C10-C11	120.4(7)

C9-C10-H10	119.8

C11-C10-H10	119.8

C12-C11-C10	117.4(7)

C12-C11-H11	121.3

C10-C11-H11	121.3

N6-C12-C11	122.8(6)

N6-C12-C13	113.6(6)

C11-C12-C13	123.6(6)

N7-C13-C14	121.9(6)

N7-C13-C12	113.3(5)

C14-C13-C12	124.9(6)

C15-C14-C13	118.7(6)

C15-C14-H14	120.7

C13-C14-H14	120.7

C14-C15-C16	119.9(6)

C14-C15-H15	120.1

C16-C15-H15	120.1

C17-C16-C15	118.2(6)

C17-C16-H16	120.9

C15-C16-H16	120.9

N7-C17-C16	122.0(6)

N7-C17-C18	112.5(5)

C16-C17-C18	125.5(6)

N9-C18-N8	125.4(6)

N9-C18-C17	114.5(5)

N8-C18-C17	120.1(5)

O1-C19-N10	124.8(6)

O1-C19-C20	116.3(5)

N10-C19-C20	118.8(6)

N12-C20-C21	122.8(6)

N12-C20-C19	114.5(6)

C21-C20-C19	122.7(6)

C20-C21-C22	118.7(6)

C20-C21-H21	120.6

C22-C21-H21	120.6

C23-C22-C21	118.7(7)

C23-C22-H22	120.6

C21-C22-H22	120.6

C24-C23-C22	119.4(6)

C24-C23-H23	120.3

C22-C23-H23	120.3

N12-C24-C23	123.1(6)

N12-C24-H24	118.5

C23-C24-H24	118.5

C5-N1-C1	118.2(6)

C5-N1-Mn1	115.2(5)

C1-N1-Mn1	125.6(5)

C6-N2-H2A	120.0

C6-N2-H2B	120.0

H2A-N2-H2B	120.0

C6-N3-N4	114.4(5)

C6-N3-Mn1	116.1(5)

N4-N3-Mn1	120.7(4)

C7-N4-N3	117.2(5)

C7-N4-Mn2	117.1(4)

N3-N4-Mn2	119.9(4)

C7-N5-H5A	120.0

C7-N5-H5B	120.0

H5A-N5-H5B	120.0

C12-N6-C8	119.3(6)

C12-N6-Mn2	121.8(4)

C8-N6-Mn2	118.8(4)

C13-N7-C17	119.4(5)

C13-N7-Mn2	122.0(4)

C17-N7-Mn2	118.5(4)

C18-N8-H8A	120.0

C18-N8-H8B	120.0

H8A-N8-H8B	120.0

C18-N9-N10	117.4(5)

C18-N9-Mn2	119.7(4)

N10-N9-Mn2	119.8(3)

C19-N10-N9	109.3(5)

C20-N12-C24	117.2(6)

C20-N12-Mn1	115.9(4)

C24-N12-Mn1	126.8(5)

C19-O1-Mn1	119.4(4)

C19-O1-Mn2	116.2(4)

Mn1-O1-Mn2	122.9(2)

Mn1-O2-H2WA	121(3)

Mn1-O2-H2WB	127(3)

H2WA-O2-H2WB	109(3)

Mn1-O3-H3WA	122(3)

Mn1-O3-H3WB	112(3)

H3WA-O3-H3WB	107(3)

Mn2-O4-H4WA	118(3)

Mn2-O4-H4WB	117(3)

H4WA-O4-H4WB	111(3)

Mn2-O5-H5WA	112(3)

Mn2-O5-H5WB	109(3)

H5WA-O5-H5WB	107(3)

O1-Mn1-O3	83.24(19)

O1-Mn1-O2	157.76(18)

O3-Mn1-O2	82.0(2)

O1-Mn1-N3	82.58(17)

O3-Mn1-N3	89.6(2)

O2-Mn1-N3	113.8(2)

O1-Mn1-N12	73.50(18)

O3-Mn1-N12	105.2(2)

O2-Mn1-N12	94.5(2)

N3-Mn1-N12	149.81(19)

O1-Mn1-N1	119.19(18)

O3-Mn1-N1	148.3(2)

O2-Mn1-N1	81.29(19)

N3-Mn1-N1	73.0(2)

N12-Mn1-N1	102.7(2)

O1-Mn2-N9	69.80(17)

O1-Mn2-N7	140.23(17)

N9-Mn2-N7	70.46(18)

O1-Mn2-N6	149.68(17)

N9-Mn2-N6	138.28(19)

N7-Mn2-N6	69.25(18)

O1-Mn2-O4	86.58(17)

N9-Mn2-O4	89.47(17)

N7-Mn2-O4	94.42(17)

N6-Mn2-O4	83.27(17)

O1-Mn2-O5	89.71(17)

N9-Mn2-O5	89.53(18)

N7-Mn2-O5	88.62(16)

N6-Mn2-O5	99.84(18)

O4-Mn2-O5	176.27(17)

O1-Mn2-N4	82.90(17)

N9-Mn2-N4	152.34(19)

N7-Mn2-N4	136.51(19)

N6-Mn2-N4	69.33(19)

O4-Mn2-N4	93.40(17)

O5-Mn2-N4	85.84(17)

O13-Cl11-O11	109.6(5)

O13-Cl11-O14	109.0(4)

O11-Cl11-O14	110.6(4)

O13-Cl11-O12	110.4(5)

O11-Cl11-O12	107.8(5)

O14-Cl11-O12	109.4(6)

O21-Cl21-O24	111.6(6)

O21-Cl21-O23	108.5(6)

O24-Cl21-O23	111.6(5)

O21-Cl21-O22	107.4(6)

O24-Cl21-O22	107.6(4)

O23-Cl21-O22	110.0(5)

O33-Cl33-O32	115.9(5)

O33-Cl33-O31	113.5(5)

O32-Cl33-O31	112.1(4)

O33-Cl33-O34	95.8(7)

O32-Cl33-O34	110.5(5)

O31-Cl33-O34	107.5(5)

N41-C41-H41A	109.5

N41-C41-H41B	109.5

H41A-C41-H41B	109.5

N41-C41-H41C	109.5

H41A-C41-H41C	109.5

H41B-C41-H41C	109.5

O41-N41-O42	127.5(13)

O41-N41-C41	114.1(14)

O42-N41-C41	118.3(12)

H71A-O71-H71B	107(3)

O52-N51-O51	140.2(13)

O52-N51-C51	120.2(13)

O51-N51-C51	98.9(12)

N61-C61-H61A	109.5

N61-C61-H61B	109.5

H61A-C61-H61B	109.5

N61-C61-H61C	109.5

H61A-C61-H61C	109.5

H61B-C61-H61C	109.5

O61-N61-O62	123.9(12)

O61-N61-C61	118.4(12)

O62-N61-C61	117.6(12)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2´ 103]. The anisotropic displacement

factor exponent takes the form: -2p 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	28(4) 	42(4)	56(4) 	13(3)	-2(3) 	3(3)

C2	37(4) 	49(4)	67(5) 	24(4)	-8(3) 	0(3)

C3	34(4) 	52(4)	54(4) 	25(4)	-8(3) 	-6(3)

C4	39(4) 	46(4)	41(4) 	20(3)	-8(3) 	-7(3)

C5	29(3) 	47(4)	35(3) 	14(3)	-9(3) 	-8(3)

C6	20(3) 	52(4)	32(3) 	13(3)	-7(2) 	-1(3)

C7	26(3) 	45(3)	23(3) 	7(3)	-7(2) 	-11(3)

C8	25(3) 	44(3)	28(3) 	1(3)	-5(2) 	-9(3)

C9	37(4) 	59(4)	29(3) 	-2(3)	-6(3) 	-8(3)

C10	43(4) 	53(4)	38(4) 	-13(3)	-5(3) 	5(3)

C11	37(4) 	44(4)	39(4) 	-8(3)	-5(3) 	7(3)

C12	26(3) 	38(3)	29(3) 	4(2)	-5(2) 	-9(3)

C13	25(3) 	34(3)	32(3) 	4(2)	-7(2) 	-4(2)

C14	28(3) 	33(3)	35(3) 	0(3)	-2(3) 	5(3)

C15	33(3) 	31(3)	38(4) 	7(3)	-8(3) 	1(3)

C16	29(3) 	37(3)	25(3) 	6(2)	-7(2) 	-1(3)

C17	20(3) 	28(3)	27(3) 	5(2)	-5(2) 	-5(2)

C18	19(3) 	32(3)	25(3) 	8(2)	-3(2) 	-3(2)

C19	24(3) 	36(3)	26(3) 	6(2)	0(2) 	1(2)

C20	24(3) 	33(3)	34(3) 	11(2)	1(2) 	0(2)

C21	38(4) 	34(4)	35(3) 	11(3)	4(3) 	8(3)

C22	40(4) 	34(4)	48(4) 	0(3)	13(3) 	2(3)

C23	27(3) 	28(4)	67(5) 	7(3)	3(3) 	9(3)

C24	24(3) 	36(4)	56(4) 	16(3)	-1(3) 	3(3)

N1	25(3) 	44(3)	40(3) 	16(2)	-7(2) 	0(2)

N2	32(3) 	58(4)	46(4) 	26(3)	5(3) 	-2(3)

N3	25(2) 	42(3)	25(3) 	8(2)	-7(2) 	-4(2)

N4	27(3) 	38(3)	22(2) 	5(2)	-4(2) 	3(2)

N5	56(4) 	41(3)	38(3) 	8(3)	-25(3) 	-12(3)

N6	20(2) 	39(3)	23(2) 	3(2)	-3(2) 	-4(2)

N7	18(2) 	29(2)	26(2) 	5(2)	-6(2) 	-2(2)

N8	26(3) 	33(3)	29(3) 	3(2)	-10(2) 	1(2)

N9	25(3) 	33(3)	23(2) 	4(2)	-3(2) 	4(2)

N10	23(3) 	34(3)	23(2) 	5(2)	0(2) 	6(2)

N12	23(3) 	37(3)	39(3) 	14(2)	1(2) 	3(2)

O1	30(2) 	43(2)	21(2) 	9(2)	-2(2) 	7(2)

O2	30(2) 	59(3)	51(3) 	23(3)	-14(2) 	-1(2)

O3	21(2) 	55(3)	89(4) 	37(3)	-11(2) 	-7(2)

O4	26(2) 	43(3)	23(2) 	5(2)	-1(2) 	-3(2)

O5	39(2) 	28(2)	38(3) 	6(2)	-17(2) 	-5(2)

Mn1	22(1) 	42(1)	33(1) 	16(1)	-3(1) 	2(1)

Mn2	22(1) 	34(1)	22(1) 	5(1)	-5(1) 	2(1)

O11	65(4) 	132(7)	82(5) 	5(4)	8(3) 	-53(4)

O12	117(6) 	33(3)	162(8) 	-22(4)	43(5) 	8(4)

O13	130(6) 	36(3)	87(5) 	2(3)	-73(4) 	11(3)

O14	58(4) 	96(5)	110(5) 	60(4)	-58(4) 	-47(4)

Cl11	31(1) 	35(1)	45(1) 	9(1)	-9(1) 	3(1)

O21	48(4) 	100(7)	231(11) 	20(6)	-8(5) 	-11(4)

O22	146(7) 	67(4)	75(5) 	-36(4)	-54(4) 	48(5)

O23	153(7) 	64(4)	59(4) 	15(3)	-21(4) 	22(4)

O24	118(6) 	55(4)	89(5) 	-20(3)	-75(5) 	18(4)

Cl21	43(1) 	39(1)	36(1) 	-1(1)	-17(1) 	2(1)

O31	36(3) 	84(5)	91(5) 	-40(4)	-9(3) 	-11(3)

O32	42(3) 	61(4)	85(4) 	-27(3)	-2(3) 	-10(3)

O33	96(6) 	188(9)	119(6) 	-93(6)	-59(5) 	40(6)

O34	72(5) 	61(4)	248(10) 	-14(6)	34(6) 	-9(4)

Cl33	34(1) 	92(2)	53(1) 	-22(1)	-8(1) 	-10(1)

C41	199(13) 	84(9)	259(19) 	-97(11)	-145(13) 	8(8)

N41	118(7) 	107(7)	60(6) 	-16(5)	-27(5) 	51(6)

O41	123(6) 	153(8)	45(4) 	1(4)	-15(4) 	81(6)

O42	114(7) 	160(9)	99(7) 	44(6)	0(5) 	40(6)

O71	32(6) 	117(11)	57(7) 	-8(7)	-14(5) 	-2(7)

C51	62(12) 	89(14)	57(11) 	-26(9)	19(8) 	7(8)

N51	50(8) 	53(8)	54(7) 	-10(6)	14(6) 	-17(6)

O51	330(30) 	110(15)	88(8) 	42(10)	-118(15) 	-86(14)

O52	57(7) 	49(7)	78(7) 	-19(6)	-18(6) 	15(5)

C61	36(8) 	60(10)	44(8) 	-3(6)	-4(6) 	-9(7)

N61	33(5) 	32(6)	41(6) 	1(5)	-2(4) 	-4(5)

O61	38(5) 	47(6)	39(6) 	-1(4)	3(4) 	-1(4)

O62	42(5) 	59(7)	48(6) 	0(5)	-14(5) 	-8(5)

Table 5. Hydrogen coordinates [´ 104] and isotropic displacement parameters [Å2 ´ 103].

Atom 	x	y	z	Ueq	S.o.f.

H1	-46	10061	2699	52	1

H2	860	11226	1764	62	1

H3	2579	10619	756	56	1

H4	3398	8831	735	50	1

H9	2936	3262	887	50	1

H10	4308	1750	1195	54	1

H11	4787	1479	2429	48	1

H14	5018	1361	3656	39	1

H15	5216	1434	4922	41	1

H16	4328	2977	5600	36	1

H21	129	7799	5788	45	1

H22	-1412	9344	6045	52	1

H23	-2487	10165	5075	51	1

H24	-1936	9509	3890	48	1

H2A	4190	6319	1386	57	1

H2B	4469	7451	1129	57	1

H5A	1022	5785	1083	52	1

H5B	1307	4627	880	52	1

H8A	2963	5662	5913	35	1

H8B	3945	4653	5941	35	1

H2WA	-2010(50)	8210(60)	2097(12)	39	1

H2WB	-2790(30)	8360(60)	2790(20)	39	1

H3WA	-1030(50)	5560(20)	3240(30)	39	1

H3WB	-2200(30)	6260(30)	3290(30)	39	1

H4WA	0(60)	3940(40)	3310(20)	39	1

H4WB	-180(60)	4170(50)	4047(13)	39	1

H5WA	5070(50)	5780(40)	2890(20)	39	1

H5WB	4340(50)	6571(16)	3300(30)	39	1

H41A	8219	737	681	252	1

H41B	8733	-391	998	252	1

H41C	7922	488	1563	252	1

H71A	6860(130)	4930(20)	2260(100)	102	0.50

H71B	7000(300)	5820(120)	1830(40)	102	0.50

H51A	7199	3073	890	109	0.50

H51B	8211	3694	240	109	0.50

H51C	7010	2943	33	109	0.50

H61A	6638	3527	879	70	0.50

H61B	8211	3999	608	70	0.50

H61C	6743	4616	413	70	0.50