|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	05src0038

Empirical formula 	C75H72BClF16N4O3Ru

Formula weight 	1528.70

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	C2/c

Unit cell dimensions	a = 18.253(3) Å	( = 90°

b = 23.128(7) Å	( = 102.535(19)°

c = 16.974(5) Å	(  = 90°

Volume	6995(3) Å3

Z	4

Density (calculated)	1.452 Mg / m3

Absorption coefficient	0.356 mm(1

F(000)	3136

Crystal	Block; Colourless

Crystal size	0.25 ( 0.16 ( 0.11 mm3

( range for data collection	3.02 ( 27.48°

Index ranges	(23 ( h ( 23, (29 ( k ( 30, (21 ( l ( 21

Reflections collected	39833

Independent reflections	7833 [Rint = 0.0659]

Completeness to ( = 27.48°	97.4 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9619 and 0.9162

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	7833 / 791 / 640

Goodness-of-fit on F2	1.035

Final R indices [F2 > 2((F2)]	R1 = 0.0663, wR2 = 0.1484

R indices (all data)	R1 = 0.0953, wR2 = 0.1658

Largest diff. peak and hole	0.756 and (0.983 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP3 for Windows (L. J. Farrugia, J. Appl. Crystallogr. 1997, 30, 565).

Special details:

All hydrogen atoms were fixed.

The anion was completely disordered over two main positions.

The anions (Cl- and CO-) around the ruthenium were also disordered, with the best (sensible fitting) ratio of 1:3.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	(370(5)	7681(5)	6717(6)	42(2)	0.8676(15)

O1	(725(2)	7389(2)	6235(3)	51(1)	0.8676(15)

Cl1	210(4)	8892(3)	8564(6)	70(2)	0.3676(15)

C2	145(9)	8923(7)	8138(8)	98(5)	0.6324(15)

O2	231(8)	9075(6)	8713(9)	112(5)	0.6324(15)

Cl2	(556(8)	7608(7)	6482(9)	43(3)	0.1324(15)

Ru1	0	8234(1)	7500	35(1)	1

C11	1134(2)	8233(2)	7308(2)	36(1)	1

C12	2190(2)	7957(2)	6908(3)	54(1)	1

C13	2368(2)	8412(2)	7389(3)	49(1)	1

C14	1050(2)	7411(2)	6318(2)	39(1)	1

C15	1035(2)	6851(2)	6612(2)	37(1)	1

C16	619(2)	6451(2)	6084(2)	38(1)	1

C17	264(2)	6605(2)	5303(2)	42(1)	1

C18	345(2)	7151(2)	5022(2)	46(1)	1

C19	753(2)	7569(2)	5520(3)	45(1)	1

C20	1502(2)	6665(2)	7421(2)	42(1)	1

C21	1116(2)	6229(2)	7865(3)	52(1)	1

C22	2248(2)	6414(2)	7284(3)	55(1)	1

C23	893(3)	8150(2)	5172(3)	59(1)	1

C24	182(4)	8439(3)	4707(5)	112(3)	1

C25	1446(3)	8077(2)	4615(3)	63(1)	1

C26	1720(2)	9093(2)	8117(3)	46(1)	1

C27	1535(3)	9617(2)	7714(3)	56(1)	1

C28	1498(3)	10093(2)	8198(4)	73(1)	1

C29	1664(4)	10048(3)	9022(4)	86(2)	1

C30	1898(3)	9542(3)	9400(4)	78(2)	1

C31	1934(3)	9036(2)	8950(3)	55(1)	1

C32	1437(3)	9670(2)	6812(3)	63(1)	1

C33	2211(4)	9793(3)	6615(4)	87(2)	1

C34	880(4)	10139(2)	6432(4)	95(2)	1

C35	2245(3)	8484(2)	9361(3)	61(1)	1

C36	3101(3)	8519(3)	9597(3)	76(2)	1

C37	1932(4)	8329(3)	10113(4)	93(2)	1

N11	1438(2)	7848(1)	6860(2)	43(1)	1

N12	1725(2)	8581(1)	7629(2)	39(1)	1

F51	5915(5)	8680(3)	7021(5)	44(2)	0.50

B51	5283(4)	8705(4)	7388(4)	34(2)	0.50

C61	5527(5)	9063(5)	8237(7)	23(2)	0.50

C62	6135(6)	8855(5)	8808(7)	35(3)	0.50

C63	6413(6)	9103(5)	9550(7)	34(2)	0.50

C64	6096(6)	9584(5)	9772(6)	39(3)	0.50

C65	5488(7)	9811(6)	9238(8)	49(3)	0.50

C66	5226(7)	9559(6)	8503(8)	39(3)	0.50

F62	6491(5)	8369(5)	8656(10)	41(2)	0.50

F63	7010(6)	8876(6)	10075(5)	51(2)	0.50

F64	6345(4)	9845(3)	10485(4)	59(2)	0.50

F65	5167(8)	10287(5)	9467(9)	76(4)	0.50

F66	4625(8)	9830(7)	8051(10)	47(3)	0.50

C71	5000	8048(2)	7500	46(1)	1

C72	5287(4)	7537(4)	7344(2)	71(3)	0.50

C73	5000	7007(3)	7500	89(2)	1

C74	4430(5)	6975(4)	7863(5)	80(2)	0.50

C75	4050(7)	7470(6)	7977(7)	78(5)	0.50

C76	4394(4)	7981(3)	7905(4)	45(2)	0.50

F72	5944(4)	7549(4)	7067(5)	82(3)	0.50

F73	5418(5)	6520(3)	7410(5)	110(3)	0.50

F74	4137(5)	6463(3)	7999(5)	114(3)	0.50

F75	3487(3)	7424(3)	8372(3)	88(2)	0.50

F76	4025(5)	8453(3)	8082(5)	49(2)	0.50

C81	4654(6)	9011(5)	6666(6)	28(2)	0.50

C82	3976(6)	8814(5)	6232(7)	34(3)	0.50

C83	3521(6)	9116(5)	5622(7)	38(3)	0.50

C84	3735(6)	9639(5)	5402(6)	41(3)	0.50

C85	4401(7)	9868(6)	5826(9)	44(3)	0.50

C86	4842(8)	9559(6)	6430(9)	38(3)	0.50

F82	3725(5)	8286(5)	6388(9)	36(2)	0.50

F83	2890(6)	8863(6)	5195(5)	52(2)	0.50

F84	3329(4)	9914(3)	4751(4)	64(2)	0.50

F85	4608(7)	10396(5)	5634(8)	57(3)	0.50

F86	5501(8)	9779(9)	6835(11)	52(3)	0.50

Table 3. Bond lengths [Å] and angles [°].

C1(O1	1.148(7)

C1(Ru1	1.862(7)

Cl1(Ru1	2.329(5)

C2(O2	1.016(16)

C2(Ru1	1.913(13)

Cl2(Ru1	2.314(14)

Ru1(C1i	1.862(7)

Ru1(C2i	1.913(13)

Ru1(C11	2.163(3)

Ru1(C11i	2.163(3)

Ru1(Cl2i	2.314(14)

Ru1(Cl1i	2.329(5)

C11(N12	1.361(4)

C11(N11	1.366(5)

C12(C13	1.329(6)

C12(N11	1.380(5)

C12(H12	0.9500

C13(N12	1.379(5)

C13(H13	0.9500

C14(C15	1.390(5)

C14(C19	1.394(6)

C14(N11	1.444(5)

C15(C16	1.392(5)

C15(C20	1.513(5)

C16(C17	1.390(5)

C16(H16	0.9500

C17(C18	1.368(6)

C17(H17	0.9500

C18(C19	1.390(6)

C18(H18	0.9500

C19(C23	1.513(6)

C20(C21	1.520(6)

C20(C22	1.544(5)

C20(H20	1.0000

C21(H21A	0.9800

C21(H21B	0.9800

C21(H21C	0.9800

C22(H22A	0.9800

C22(H22B	0.9800

C22(H22C	0.9800

C23(C24	1.519(8)

C23(C25	1.534(6)

C23(H23	1.0000

C24(H24A	0.9800

C24(H24B	0.9800

C24(H24C	0.9800

C25(H25A	0.9800

C25(H25B	0.9800

C25(H25C	0.9800

C26(C31	1.388(6)

C26(C27	1.398(6)

C26(N12	1.447(5)

C27(C28	1.382(7)

C27(C32	1.507(7)

C28(C29	1.369(9)

C28(H28	0.9500

C29(C30	1.359(9)

C29(H29	0.9500

C30(C31	1.408(7)

C30(H30	0.9500

C31(C35	1.505(7)

C32(C34	1.530(7)

C32(C33	1.548(7)

C32(H32	1.0000

C33(H33A	0.9800

C33(H33B	0.9800

C33(H33C	0.9800

C34(H34A	0.9800

C34(H34B	0.9800

C34(H34C	0.9800

C35(C36	1.530(7)

C35(C37	1.548(7)

C35(H35	1.0000

C36(H36A	0.9800

C36(H36B	0.9800

C36(H36C	0.9800

C37(H37A	0.9800

C37(H37B	0.9800

C37(H37C	0.9800

F51(B51	1.425(11)

B51(C71	1.630(9)

B51(C61	1.639(14)

B51(C81	1.647(14)

C61(C66	1.389(11)

C61(C62	1.391(10)

C62(F62	1.351(10)

C62(C63	1.376(10)

C63(C64	1.345(11)

C63(F63	1.356(10)

C64(F64	1.341(10)

C64(C65	1.376(11)

C65(F65	1.344(10)

C65(C66	1.366(11)

C66(F66	1.347(10)

C71(C72	1.342(9)

C71(C76	1.432(7)

C72(C73	1.379(9)

C72(F72	1.381(11)

C73(C74	1.322(10)

C73(F73	1.389(9)

C74(F74	1.340(10)

C74(C75	1.375(13)

C75(F75	1.348(13)

C75(C76	1.356(12)

C76(F76	1.349(11)

C81(C82	1.373(11)

C81(C86	1.394(11)

C82(F82	1.351(10)

C82(C83	1.370(10)

C83(C84	1.346(11)

C83(F83	1.354(10)

C84(F84	1.349(10)

C84(C85	1.378(10)

C85(F85	1.340(10)

C85(C86	1.359(11)

C86(F86	1.350(10)

O1(C1(Ru1	167.2(9)

O2(C2(Ru1	143.6(18)

C1i(Ru1(C1	93.2(8)

C1i(Ru1(C2	100.6(7)

C1(Ru1(C2	163.8(6)

C1i(Ru1(C2i	163.8(6)

C1(Ru1(C2i	100.6(7)

C2(Ru1(C2i	67.2(10)

C1i(Ru1(C11	84.0(3)

C1(Ru1(C11	95.9(3)

C2(Ru1(C11	93.8(5)

C2i(Ru1(C11	86.3(5)

C1i(Ru1(C11i	95.9(3)

C1(Ru1(C11i	84.0(3)

C2(Ru1(C11i	86.3(5)

C2i(Ru1(C11i	93.8(5)

C11(Ru1(C11i	179.86(19)

C1i(Ru1(Cl2	97.7(3)

C1(Ru1(Cl2	5.5(7)

C2(Ru1(Cl2	158.3(7)

C2i(Ru1(Cl2	96.6(7)

C11(Ru1(Cl2	99.5(4)

C11i(Ru1(Cl2	80.4(4)

C1i(Ru1(Cl2i	5.5(7)

C1(Ru1(Cl2i	97.7(3)

C2(Ru1(Cl2i	96.6(7)

C2i(Ru1(Cl2i	158.3(7)

C11(Ru1(Cl2i	80.4(4)

C11i(Ru1(Cl2i	99.5(4)

Cl2(Ru1(Cl2i	102.4(9)

C1i(Ru1(Cl1	85.5(5)

C1(Ru1(Cl1	167.2(4)

C2(Ru1(Cl1	15.7(6)

C2i(Ru1(Cl1	82.8(6)

C11(Ru1(Cl1	96.67(19)

C11i(Ru1(Cl1	83.43(19)

Cl2(Ru1(Cl1	163.7(4)

Cl2i(Ru1(Cl1	81.8(5)

C1i(Ru1(Cl1i	167.2(4)

C1(Ru1(Cl1i	85.5(5)

C2(Ru1(Cl1i	82.8(6)

C2i(Ru1(Cl1i	15.7(6)

C11(Ru1(Cl1i	83.43(19)

C11i(Ru1(Cl1i	96.67(19)

Cl2(Ru1(Cl1i	81.8(5)

Cl2i(Ru1(Cl1i	163.7(4)

Cl1(Ru1(Cl1i	98.5(5)

N12(C11(N11	103.0(3)

N12(C11(Ru1	129.8(3)

N11(C11(Ru1	127.1(2)

C13(C12(N11	106.8(3)

C13(C12(H12	126.6

N11(C12(H12	126.6

C12(C13(N12	107.1(3)

C12(C13(H13	126.4

N12(C13(H13	126.4

C15(C14(C19	123.9(4)

C15(C14(N11	118.0(4)

C19(C14(N11	118.0(4)

C14(C15(C16	116.0(4)

C14(C15(C20	122.6(3)

C16(C15(C20	121.1(3)

C17(C16(C15	121.3(4)

C17(C16(H16	119.4

C15(C16(H16	119.4

C18(C17(C16	120.4(4)

C18(C17(H17	119.8

C16(C17(H17	119.8

C17(C18(C19	120.9(4)

C17(C18(H18	119.5

C19(C18(H18	119.5

C18(C19(C14	116.9(4)

C18(C19(C23	119.6(4)

C14(C19(C23	123.3(4)

C15(C20(C21	114.1(3)

C15(C20(C22	108.1(3)

C21(C20(C22	110.1(3)

C15(C20(H20	108.1

C21(C20(H20	108.1

C22(C20(H20	108.1

C20(C21(H21A	109.5

C20(C21(H21B	109.5

H21A(C21(H21B	109.5

C20(C21(H21C	109.5

H21A(C21(H21C	109.5

H21B(C21(H21C	109.5

C20(C22(H22A	109.5

C20(C22(H22B	109.5

H22A(C22(H22B	109.5

C20(C22(H22C	109.5

H22A(C22(H22C	109.5

H22B(C22(H22C	109.5

C19(C23(C24	113.3(4)

C19(C23(C25	109.4(4)

C24(C23(C25	109.3(5)

C19(C23(H23	108.2

C24(C23(H23	108.2

C25(C23(H23	108.2

C23(C24(H24A	109.5

C23(C24(H24B	109.5

H24A(C24(H24B	109.5

C23(C24(H24C	109.5

H24A(C24(H24C	109.5

H24B(C24(H24C	109.5

C23(C25(H25A	109.5

C23(C25(H25B	109.5

H25A(C25(H25B	109.5

C23(C25(H25C	109.5

H25A(C25(H25C	109.5

H25B(C25(H25C	109.5

C31(C26(C27	124.5(4)

C31(C26(N12	118.0(4)

C27(C26(N12	117.5(4)

C28(C27(C26	115.9(5)

C28(C27(C32	121.9(5)

C26(C27(C32	122.0(4)

C29(C28(C27	121.2(6)

C29(C28(H28	119.4

C27(C28(H28	119.4

C30(C29(C28	121.7(5)

C30(C29(H29	119.2

C28(C29(H29	119.2

C29(C30(C31	120.4(5)

C29(C30(H30	119.8

C31(C30(H30	119.8

C26(C31(C30	115.9(5)

C26(C31(C35	123.2(4)

C30(C31(C35	120.7(5)

C27(C32(C34	114.1(5)

C27(C32(C33	108.7(4)

C34(C32(C33	109.4(5)

C27(C32(H32	108.2

C34(C32(H32	108.2

C33(C32(H32	108.2

C32(C33(H33A	109.5

C32(C33(H33B	109.5

H33A(C33(H33B	109.5

C32(C33(H33C	109.5

H33A(C33(H33C	109.5

H33B(C33(H33C	109.5

C32(C34(H34A	109.5

C32(C34(H34B	109.5

H34A(C34(H34B	109.5

C32(C34(H34C	109.5

H34A(C34(H34C	109.5

H34B(C34(H34C	109.5

C31(C35(C36	109.7(4)

C31(C35(C37	114.2(4)

C36(C35(C37	109.6(4)

C31(C35(H35	107.7

C36(C35(H35	107.7

C37(C35(H35	107.7

C35(C36(H36A	109.5

C35(C36(H36B	109.5

H36A(C36(H36B	109.5

C35(C36(H36C	109.5

H36A(C36(H36C	109.5

H36B(C36(H36C	109.5

C35(C37(H37A	109.5

C35(C37(H37B	109.5

H37A(C37(H37B	109.5

C35(C37(H37C	109.5

H37A(C37(H37C	109.5

H37B(C37(H37C	109.5

C11(N11(C12	111.6(3)

C11(N11(C14	127.4(3)

C12(N11(C14	120.7(3)

C11(N12(C13	111.5(3)

C11(N12(C26	127.6(3)

C13(N12(C26	120.7(3)

F51(B51(C71	108.6(6)

F51(B51(C61	108.3(6)

C71(B51(C61	113.6(5)

F51(B51(C81	101.1(6)

C71(B51(C81	107.5(6)

C61(B51(C81	116.7(5)

C66(C61(C62	111.8(9)

C66(C61(B51	130.7(9)

C62(C61(B51	117.5(9)

F62(C62(C63	115.1(10)

F62(C62(C61	119.9(10)

C63(C62(C61	125.0(10)

C64(C63(F63	118.0(10)

C64(C63(C62	120.4(10)

F63(C63(C62	121.7(9)

F64(C64(C63	123.0(9)

F64(C64(C65	119.3(9)

C63(C64(C65	117.7(9)

F65(C65(C66	121.7(11)

F65(C65(C64	117.5(11)

C66(C65(C64	120.8(10)

F66(C66(C65	113.7(11)

F66(C66(C61	122.0(11)

C65(C66(C61	124.3(10)

C72(C71(C76	112.0(6)

C72(C71(B51	130.6(5)

C76(C71(B51	117.0(5)

C71(C72(C73	124.3(7)

C71(C72(F72	117.0(7)

C73(C72(F72	118.5(7)

C74(C73(C72	120.7(7)

C74(C73(F73	120.8(7)

C72(C73(F73	117.3(5)

C73(C74(F74	121.0(10)

C73(C74(C75	119.3(9)

F74(C74(C75	118.7(10)

F75(C75(C76	122.2(10)

F75(C75(C74	117.7(11)

C76(C75(C74	117.2(10)

F76(C76(C75	114.9(8)

F76(C76(C71	119.7(6)

C75(C76(C71	123.9(8)

C82(C81(C86	113.4(10)

C82(C81(B51	131.2(10)

C86(C81(B51	115.4(9)

F82(C82(C83	115.7(10)

F82(C82(C81	120.0(10)

C83(C82(C81	124.3(10)

C84(C83(F83	120.2(9)

C84(C83(C82	120.2(9)

F83(C83(C82	119.3(9)

C83(C84(F84	120.7(9)

C83(C84(C85	118.4(9)

F84(C84(C85	120.7(9)

F85(C85(C86	120.7(10)

F85(C85(C84	119.1(10)

C86(C85(C84	120.2(10)

F86(C86(C85	120.1(12)

F86(C86(C81	116.4(12)

C85(C86(C81	123.5(11)

Symmetry transformations used to generate equivalent atoms:

(i) (x,y,(z+3/2

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	25(4) 	65(4)	33(5) 	(4(3)	1(3) 	(2(3)

O1	32(2) 	67(3)	54(3) 	(15(2)	10(2) 	(5(2)

Cl1	52(3) 	71(3)	101(5) 	(56(3)	49(4) 	(34(2)

C2	86(8) 	123(10)	97(8) 	(73(8)	48(8) 	(25(6)

O2	77(6) 	178(14)	85(6) 	(36(7)	29(4) 	(49(9)

Cl2	35(8) 	53(8)	39(11) 	(5(5)	5(6) 	(2(6)

Ru1	29(1) 	31(1)	47(1) 	0	15(1) 	0

C11	29(2) 	34(2)	48(2) 	(2(2)	13(2) 	(2(1)

C12	33(2) 	48(2)	88(3) 	(19(2)	29(2) 	(8(2)

C13	34(2) 	45(2)	74(3) 	(17(2)	25(2) 	(12(2)

C14	22(2) 	38(2)	59(2) 	(10(2)	14(2) 	0(1)

C15	25(2) 	36(2)	48(2) 	(10(2)	9(1) 	(1(1)

C16	35(2) 	29(2)	51(2) 	(6(2)	11(2) 	(2(2)

C17	33(2) 	49(2)	45(2) 	(6(2)	11(2) 	(4(2)

C18	40(2) 	56(2)	44(2) 	3(2)	15(2) 	4(2)

C19	39(2) 	42(2)	59(2) 	2(2)	23(2) 	5(2)

C20	32(2) 	43(2)	49(2) 	(10(2)	4(2) 	2(2)

C21	48(2) 	59(3)	46(2) 	(1(2)	3(2) 	1(2)

C22	39(2) 	55(3)	67(3) 	(1(2)	5(2) 	15(2)

C23	69(3) 	44(2)	76(3) 	5(2)	39(2) 	1(2)

C24	100(5) 	79(4)	175(7) 	66(5)	68(5) 	41(4)

C25	67(3) 	53(3)	75(3) 	6(2)	32(3) 	(8(2)

C26	36(2) 	49(2)	58(2) 	(16(2)	23(2) 	(13(2)

C27	56(3) 	40(2)	80(3) 	(9(2)	33(2) 	(12(2)

C28	76(3) 	49(3)	103(4) 	(19(3)	39(3) 	(8(2)

C29	93(4) 	66(3)	106(4) 	(38(3)	37(4) 	(9(3)

C30	80(4) 	93(4)	67(3) 	(29(3)	31(3) 	(4(3)

C31	52(2) 	62(3)	60(3) 	(15(2)	29(2) 	(12(2)

C32	77(3) 	38(2)	80(3) 	6(2)	30(3) 	(3(2)

C33	106(4) 	74(4)	100(4) 	5(3)	62(4) 	(16(3)

C34	116(5) 	49(3)	125(5) 	24(3)	37(4) 	12(3)

C35	51(3) 	85(3)	49(2) 	(6(2)	19(2) 	(13(2)

C36	59(3) 	118(5)	49(3) 	8(3)	7(2) 	(13(3)

C37	84(4) 	135(6)	70(4) 	15(4)	41(3) 	(13(4)

N11	28(2) 	37(2)	68(2) 	(12(2)	17(2) 	(3(1)

N12	32(2) 	38(2)	52(2) 	(8(1)	18(1) 	(6(1)

F51	25(3) 	56(5)	53(3) 	10(3)	15(2) 	21(3)

B51	25(3) 	43(4)	36(4) 	2(3)	10(3) 	(3(3)

C61	23(5) 	25(4)	26(3) 	6(3)	17(3) 	(12(3)

C62	29(5) 	39(6)	39(6) 	(1(5)	13(4) 	1(4)

C63	31(5) 	41(5)	32(5) 	4(3)	9(3) 	(5(4)

C64	50(7) 	34(5)	33(4) 	0(3)	11(4) 	(9(4)

C65	75(8) 	35(6)	38(5) 	(4(4)	15(4) 	12(5)

C66	37(7) 	43(8)	38(6) 	8(5)	7(4) 	6(5)

F62	30(5) 	47(5)	48(4) 	0(3)	11(4) 	6(4)

F63	30(4) 	73(4)	46(5) 	(6(4)	1(3) 	6(3)

F64	74(5) 	56(4)	44(3) 	(16(3)	6(3) 	(3(4)

F65	135(12) 	42(5)	56(4) 	5(4)	32(6) 	39(6)

F66	48(5) 	42(4)	49(5) 	9(4)	9(4) 	9(4)

C71	40(3) 	35(3)	57(3) 	0	(1(2) 	0

C72	86(7) 	50(4)	77(7) 	2(5)	17(5) 	13(4)

C73	105(6) 	36(4)	107(7) 	0	(16(5) 	0

C74	92(7) 	48(5)	74(7) 	18(5)	(38(4) 	(27(4)

C75	79(12) 	57(6)	93(14) 	(13(8)	5(9) 	(48(6)

C76	42(4) 	46(4)	42(4) 	16(3)	(4(3) 	(13(3)

F72	65(6) 	61(5)	109(9) 	(19(5)	(1(5) 	26(4)

F73	107(6) 	52(4)	139(7) 	4(4)	(46(6) 	23(4)

F74	107(6) 	53(4)	148(8) 	22(4)	(49(5) 	(42(4)

F75	81(4) 	104(5)	71(4) 	38(3)	(3(3) 	(56(3)

F76	36(3) 	58(5)	57(4) 	(9(4)	15(3) 	(23(3)

C81	22(5) 	38(4)	30(4) 	(5(3)	19(3) 	10(3)

C82	27(4) 	33(6)	44(7) 	4(5)	12(4) 	5(4)

C83	20(4) 	48(5)	47(7) 	7(4)	10(4) 	1(4)

C84	31(5) 	44(5)	46(6) 	6(4)	3(4) 	10(3)

C85	44(5) 	31(5)	54(7) 	4(5)	6(4) 	(2(4)

C86	29(6) 	41(7)	44(7) 	(8(5)	13(4) 	(3(5)

F82	27(5) 	38(4)	46(3) 	7(3)	13(4) 	(4(3)

F83	28(4) 	60(4)	60(6) 	10(5)	(6(4) 	(9(3)

F84	59(4) 	53(4)	69(5) 	25(3)	(14(3) 	4(3)

F85	76(5) 	43(4)	47(5) 	8(4)	(1(4) 	(15(4)

F86	40(4) 	64(6)	52(5) 	(22(4)	9(4) 	(21(4)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H12	2517	7747	6648	64	1

H13	2848	8589	7540	59	1

H16	577	6065	6262	46	1

H17	(37	6331	4963	50	1

H18	120	7244	4478	55	1

H20	1619	7017	7768	51	1

H21A	628	6381	7916	78	1

H21B	1429	6159	8403	78	1

H21C	1044	5865	7561	78	1

H22A	2148	6059	6965	82	1

H22B	2580	6328	7807	82	1

H22C	2491	6698	6995	82	1

H23	1128	8410	5627	71	1

H24A	(76	8178	4280	169	1

H24B	312	8799	4464	169	1

H24C	(149	8526	5075	169	1

H25A	1913	7906	4920	94	1

H25B	1552	8455	4405	94	1

H25C	1225	7822	4165	94	1

H28	1355	10457	7954	88	1

H29	1614	10379	9337	103	1

H30	2038	9529	9973	93	1

H32	1252	9290	6564	76	1

H33A	2378	10182	6801	131	1

H33B	2170	9767	6031	131	1

H33C	2577	9508	6889	131	1

H34A	402	10080	6595	143	1

H34B	799	10117	5843	143	1

H34C	1083	10520	6615	143	1

H35	2109	8162	8963	73	1

H36A	3298	8616	9120	114	1

H36B	3305	8145	9812	114	1

H36C	3250	8818	10009	114	1

H37A	2071	8632	10522	139	1

H37B	2143	7959	10334	139	1

H37C	1384	8299	9958	139	1