|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	2009src1292

Empirical formula 	C4H10La2O14P2

Formula weight 	621.88

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P(1

Unit cell dimensions	a = 9.0460(3) Å	( = 108.166(2)°

b = 9.0502(3) Å	( = 110.482(2)°

c = 9.8341(3) Å	(  = 91.492(2)°

Volume	708.30(4) Å3

Z	2

Density (calculated)	2.916 Mg / m3

Absorption coefficient	6.248 mm(1

F(000)	580

Crystal	plate; colourless

Crystal size	0.08 ( 0.08 ( 0.02 mm3

( range for data collection	3.14 ( 27.48°

Index ranges	(11 ( h ( 11, (11 ( k ( 11, (12 ( l ( 12

Reflections collected	16163

Independent reflections	3241 [Rint = 0.0406]

Completeness to ( = 27.48°	99.8 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.8852 and 0.6348

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	3241 / 0 / 227

Goodness-of-fit on F2	1.062

Final R indices [F2 > 2((F2)]	R1 = 0.0256, wR2 = 0.0620

R indices (all data)	R1 = 0.0284, wR2 = 0.0638

Largest diff. peak and hole	1.240 and (1.535 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP3 for Windows (L. J. Farrugia, J. Appl. Crystallogr. 1997, 30, 565).

Special details:

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

La2	3680(1)	3650(1)	778(1)	7(1)	1

La1	5694(1)	2147(1)	4808(1)	7(1)	1

P1	7081(1)	5330(1)	4627(1)	8(1)	1

P2	5765(1)	1893(1)	8108(1)	8(1)	1

C1	8411(4)	5185(4)	3585(4)	9(1)	1

O2	5458(3)	4327(3)	3524(3)	9(1)	1

O13	9735(4)	9017(3)	6763(4)	19(1)	1

O11	7121(4)	1268(3)	2899(3)	15(1)	1

O1	7793(3)	4566(3)	5846(3)	9(1)	1

O3	6925(3)	7051(3)	5271(3)	11(1)	1

O8	6378(3)	4906(3)	1152(3)	10(1)	1

O6	4576(3)	1879(3)	8885(3)	11(1)	1

O4	5140(3)	693(3)	6443(3)	10(1)	1

O7	8588(3)	6519(3)	1867(3)	15(1)	1

O5	6239(3)	3463(3)	7974(3)	11(1)	1

C3	7552(4)	1286(4)	9219(4)	11(1)	1

C2	7766(4)	5589(4)	2135(4)	10(1)	1

C4	7336(4)	(391(4)	9202(4)	9(1)	1

O10	6227(3)	(1402(3)	8083(3)	13(1)	1

O9	8243(3)	(773(3)	10292(3)	17(1)	1

O12	8478(3)	1600(4)	6229(3)	15(1)	1

O17	992(3)	4048(3)	1115(3)	18(1)	1

Table 3. Bond lengths [Å] and angles [°].

La2(O6i	2.440(3)

La2(O2	2.477(2)

La2(O5ii	2.503(2)

La2(O8	2.520(3)

La2(O17	2.586(3)

La2(O10iii	2.602(3)

La2(O8iv	2.607(3)

La2(O7iv	2.645(3)

La2(O9iii	2.772(3)

La2(C2iv	3.008(3)

La2(C4iii	3.075(3)

La1(O4iii	2.443(2)

La1(O3ii	2.479(3)

La1(O4	2.534(2)

La1(O1	2.544(3)

La1(O12	2.563(3)

La1(O11	2.577(3)

La1(O10iii	2.616(3)

La1(O2	2.630(2)

La1(O5	2.818(2)

La1(P1	3.1924(9)

La1(P2	3.3030(9)

P1(O3	1.519(3)

P1(O1	1.527(2)

P1(O2	1.535(3)

P1(C1	1.817(4)

P2(O6	1.523(3)

P2(O5	1.531(3)

P2(O4	1.546(3)

P2(C3	1.815(4)

C1(C2	1.504(5)

C1(H4A	0.9900

C1(H4B	0.9900

O13(H13A	0.92(6)

O13(H13B	0.80(7)

O11(H11B	0.81(7)

O11(H11A	0.87(6)

O3(La1ii	2.479(3)

O8(C2	1.277(4)

O8(La2iv	2.607(3)

O6(La2v	2.440(3)

O4(La1iii	2.443(2)

O7(C2	1.255(5)

O7(La2iv	2.645(3)

O5(La2ii	2.503(2)

C3(C4	1.520(5)

C3(H1A	0.9900

C3(H1B	0.9900

C2(La2iv	3.008(3)

C4(O9	1.253(4)

C4(O10	1.268(4)

C4(La2iii	3.075(3)

O10(La2iii	2.602(3)

O10(La1iii	2.616(3)

O9(La2iii	2.772(3)

O12(H12A	0.87(7)

O12(H12B	0.85(7)

O6i(La2(O2	116.16(9)

O6i(La2(O5ii	139.37(8)

O2(La2(O5ii	73.82(8)

O6i(La2(O8	72.22(8)

O2(La2(O8	71.41(8)

O5ii(La2(O8	74.93(8)

O6i(La2(O17	136.51(9)

O2(La2(O17	99.23(9)

O5ii(La2(O17	72.35(9)

O8(La2(O17	147.28(9)

O6i(La2(O10iii	86.34(8)

O2(La2(O10iii	64.35(8)

O5ii(La2(O10iii	129.42(8)

O8(La2(O10iii	114.31(8)

O17(La2(O10iii	87.17(9)

O6i(La2(O8iv	74.67(8)

O2(La2(O8iv	129.24(8)

O5ii(La2(O8iv	70.30(8)

O8(La2(O8iv	65.46(9)

O17(La2(O8iv	102.67(9)

O10iii(La2(O8iv	160.21(8)

O6i(La2(O7iv	77.89(9)

O2(La2(O7iv	165.78(9)

O5ii(La2(O7iv	94.14(8)

O8(La2(O7iv	113.37(8)

O17(La2(O7iv	69.34(9)

O10iii(La2(O7iv	121.54(8)

O8iv(La2(O7iv	49.57(8)

O6i(La2(O9iii	74.29(9)

O2(La2(O9iii	111.05(8)

O5ii(La2(O9iii	142.03(9)

O8(La2(O9iii	143.02(9)

O17(La2(O9iii	69.70(9)

O10iii(La2(O9iii	47.83(8)

O8iv(La2(O9iii	119.40(8)

O7iv(La2(O9iii	73.72(8)

O6i(La2(C2iv	73.95(9)

O2(La2(C2iv	152.57(9)

O5ii(La2(C2iv	82.52(9)

O8(La2(C2iv	89.38(9)

O17(La2(C2iv	86.32(9)

O10iii(La2(C2iv	143.05(9)

O8iv(La2(C2iv	25.01(9)

O7iv(La2(C2iv	24.59(9)

O9iii(La2(C2iv	96.11(9)

O6i(La2(C4iii	77.19(9)

O2(La2(C4iii	88.17(9)

O5ii(La2(C4iii	143.35(9)

O8(La2(C4iii	129.62(9)

O17(La2(C4iii	79.67(9)

O10iii(La2(C4iii	24.00(9)

O8iv(La2(C4iii	140.46(8)

O7iv(La2(C4iii	97.69(9)

O9iii(La2(C4iii	24.04(8)

C2iv(La2(C4iii	119.26(9)

O4iii(La1(O3ii	99.02(8)

O4iii(La1(O4	63.98(9)

O3ii(La1(O4	81.19(8)

O4iii(La1(O1	150.35(8)

O3ii(La1(O1	110.13(8)

O4(La1(O1	124.65(8)

O4iii(La1(O12	88.24(9)

O3ii(La1(O12	152.04(9)

O4(La1(O12	77.85(9)

O1(La1(O12	68.59(9)

O4iii(La1(O11	74.33(9)

O3ii(La1(O11	137.11(9)

O4(La1(O11	127.93(9)

O1(La1(O11	80.52(9)

O12(La1(O11	70.84(9)

O4iii(La1(O10iii	68.15(8)

O3ii(La1(O10iii	71.44(9)

O4(La1(O10iii	119.17(8)

O1(La1(O10iii	115.66(8)

O12(La1(O10iii	135.53(9)

O11(La1(O10iii	66.78(9)

O4iii(La1(O2	128.64(8)

O3ii(La1(O2	77.21(8)

O4(La1(O2	156.45(8)

O1(La1(O2	56.56(8)

O12(La1(O2	118.81(9)

O11(La1(O2	75.25(9)

O10iii(La1(O2	62.12(8)

O4iii(La1(O5	117.90(8)

O3ii(La1(O5	78.11(8)

O4(La1(O5	54.20(8)

O1(La1(O5	74.76(7)

O12(La1(O5	74.67(8)

O11(La1(O5	143.00(9)

O10iii(La1(O5	149.55(8)

O2(La1(O5	111.38(7)

O4iii(La1(P1	146.95(6)

O3ii(La1(P1	95.20(6)

O4(La1(P1	148.27(6)

O1(La1(P1	28.07(6)

O12(La1(P1	93.00(7)

O11(La1(P1	74.94(7)

O10iii(La1(P1	88.69(6)

O2(La1(P1	28.55(6)

O5(La1(P1	94.13(5)

O4iii(La1(P2	90.38(6)

O3ii(La1(P2	80.37(6)

O4(La1(P2	26.81(6)

O1(La1(P2	99.46(6)

O12(La1(P2	72.57(7)

O11(La1(P2	140.54(7)

O10iii(La1(P2	140.57(6)

O2(La1(P2	137.29(6)

O5(La1(P2	27.53(5)

P1(La1(P2	121.46(2)

O4iii(La1(La1iii	32.64(6)

O3ii(La1(La1iii	89.93(6)

O4(La1(La1iii	31.34(6)

O1(La1(La1iii	147.59(5)

O12(La1(La1iii	81.71(7)

O11(La1(La1iii	102.28(7)

O10iii(La1(La1iii	94.43(6)

O2(La1(La1iii	155.74(6)

O5(La1(La1iii	85.39(5)

P1(La1(La1iii	174.638(19)

P2(La1(La1iii	57.869(16)

O3(P1(O1	114.64(14)

O3(P1(O2	111.66(15)

O1(P1(O2	106.43(14)

O3(P1(C1	108.30(16)

O1(P1(C1	106.39(15)

O2(P1(C1	109.20(16)

O3(P1(La1	134.34(11)

O1(P1(La1	51.64(10)

O2(P1(La1	54.93(10)

C1(P1(La1	117.34(12)

O6(P2(O5	116.58(15)

O6(P2(O4	111.74(15)

O5(P2(O4	105.61(14)

O6(P2(C3	106.76(16)

O5(P2(C3	108.48(16)

O4(P2(C3	107.31(16)

O6(P2(La1	136.99(11)

O5(P2(La1	58.31(10)

O4(P2(La1	47.65(9)

C3(P2(La1	115.27(13)

C2(C1(P1	114.8(3)

C2(C1(H4A	108.6

P1(C1(H4A	108.6

C2(C1(H4B	108.6

P1(C1(H4B	108.6

H4A(C1(H4B	107.5

P1(O2(La2	137.75(14)

P1(O2(La1	96.52(12)

La2(O2(La1	118.74(10)

H13A(O13(H13B	101(6)

La1(O11(H11B	128(5)

La1(O11(H11A	103(4)

H11B(O11(H11A	107(6)

P1(O1(La1	100.29(12)

P1(O3(La1ii	120.84(14)

C2(O8(La2	145.3(2)

C2(O8(La2iv	95.3(2)

La2(O8(La2iv	114.54(9)

P2(O6(La2v	140.31(15)

P2(O4(La1iii	137.15(14)

P2(O4(La1	105.55(12)

La1iii(O4(La1	116.02(9)

C2(O7(La2iv	94.1(2)

P2(O5(La2ii	139.92(14)

P2(O5(La1	94.16(11)

La2ii(O5(La1	121.16(9)

C4(C3(P2	114.9(3)

C4(C3(H1A	108.5

P2(C3(H1A	108.5

C4(C3(H1B	108.5

P2(C3(H1B	108.5

H1A(C3(H1B	107.5

O7(C2(O8	120.8(3)

O7(C2(C1	121.2(3)

O8(C2(C1	117.9(3)

O7(C2(La2iv	61.30(19)

O8(C2(La2iv	59.65(18)

C1(C2(La2iv	177.3(3)

O9(C4(O10	120.1(3)

O9(C4(C3	120.3(3)

O10(C4(C3	119.6(3)

O9(C4(La2iii	64.34(19)

O10(C4(La2iii	56.60(18)

C3(C4(La2iii	169.6(3)

C4(O10(La2iii	99.4(2)

C4(O10(La1iii	145.2(2)

La2iii(O10(La1iii	114.78(10)

C4(O9(La2iii	91.6(2)

La1(O12(H12A	121(4)

La1(O12(H12B	127(4)

H12A(O12(H12B	112(6)

Symmetry transformations used to generate equivalent atoms:

(i) x,y,z(1    (ii) (x+1,(y+1,(z+1    (iii) (x+1,(y,(z+1

(iv)  (x+1,(y+1,(z    (v) x,y,z+1

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

La2	10(1) 	6(1)	4(1) 	1(1)	2(1) 	1(1)

La1	10(1) 	6(1)	5(1) 	1(1)	3(1) 	0(1)

P1	9(1) 	8(1)	5(1) 	2(1)	2(1) 	1(1)

P2	11(1) 	6(1)	5(1) 	1(1)	4(1) 	1(1)

C1	5(2) 	14(2)	9(2) 	10(1)	0(1) 	1(1)

O2	10(1) 	10(1)	7(1) 	2(1)	3(1) 	(1(1)

O13	17(2) 	17(2)	15(2) 	0(1)	2(1) 	(2(1)

O11	14(2) 	16(2)	14(1) 	1(1)	10(1) 	0(1)

O1	11(1) 	11(1)	7(1) 	4(1)	3(1) 	1(1)

O3	11(1) 	7(1)	11(1) 	2(1)	3(1) 	0(1)

O8	10(1) 	12(1)	7(1) 	1(1)	2(1) 	(1(1)

O6	15(1) 	8(1)	12(1) 	2(1)	7(1) 	2(1)

O4	16(1) 	8(1)	6(1) 	1(1)	5(1) 	1(1)

O7	14(1) 	17(1)	13(1) 	7(1)	4(1) 	(3(1)

O5	15(1) 	9(1)	9(1) 	3(1)	6(1) 	1(1)

C3	10(2) 	11(2)	10(2) 	3(1)	1(1) 	(2(1)

C2	12(2) 	9(2)	8(2) 	1(1)	6(1) 	4(1)

C4	13(2) 	7(2)	5(2) 	0(1)	5(1) 	1(1)

O10	18(1) 	9(1)	9(1) 	2(1)	2(1) 	(1(1)

O9	19(2) 	13(1)	13(1) 	6(1)	(1(1) 	(1(1)

O12	14(1) 	11(1)	17(1) 	5(1)	2(1) 	1(1)

O17	14(1) 	18(1)	15(1) 	(3(1)	7(1) 	(1(1)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H4A	9426	5894	4284	10(10)	1

H4B	8657	4097	3311	18(12)	1

H1A	8390	1399	8811	27(13)	1

H1B	7939	2009	10303	19(12)	1

H13A	8750(70)	8440(60)	6480(60)	28(14)	1

H11B	8070(90)	1290(80)	3090(70)	47(19)	1

H12A	8660(70)	650(80)	6140(70)	46(18)	1

H11A	6670(70)	300(70)	2360(60)	30(15)	1

H12B	9330(80)	2270(80)	6750(80)	51(19)	1

H13B	10110(80)	9150(80)	7670(80)	49(19)	1