|  | University of Southampton · Department of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	s92

Empirical formula 	C20H30Cl2CoN6O8

Formula weight 	612.3

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	C2/c

Unit cell dimensions	a = 19.0985(6) Å

b = 8.5350(3) Å	( = 115.6480(10)°

c = 16.7990(7) Å

Volume	2468.52(16) Å3

Z	4

Density (calculated)	1.648 Mg / m3

Absorption coefficient	0.971 mm(1

F(000)	1268

Crystal	Red Block

Crystal size	0.10 ( 0.10 ( 0.10 mm3

( range for data collection	3.21 ( 25.03°

Index ranges	(22 ( h ( 22, (10 ( k ( 10, (18 ( l ( 19

Reflections collected	6548

Independent reflections	2151 [Rint = 0.0414]

Completeness to ( = 25.03°	98.5 %

Max. and min. transmission	0.9091 and 0.9091

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	2151 / 0 / 228

Goodness-of-fit on F2	1.004

Final R indices [F2 > 2((F2)]	R1 = 0.0359, wR2 = 0.0819

R indices (all data)	R1 = 0.0508, wR2 = 0.0885

Largest diff. peak and hole	0.300 and (0.552 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details: All hydrogen atoms were located from the difference map and fully refined.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	(1241(1)	5227(3)	649(2)	15(1)	1

C2	(1713(2)	5852(4)	(171(2)	19(1)	1

C3	(2117(2)	4891(3)	(885(2)	20(1)	1

C4	(2052(2)	3275(3)	(789(2)	20(1)	1

C5	(1590(2)	2636(3)	24(2)	18(1)	1

C6	(1184(1)	3601(3)	745(2)	15(1)	1

C7	1500(2)	5995(3)	2667(2)	19(1)	1

C8	383(2)	6441(3)	1178(2)	18(1)	1

C9	(283(2)	7329(3)	1231(2)	18(1)	1

C10	(1317(2)	7041(3)	1725(2)	18(1)	1

N1	776(1)	5385(3)	1945(2)	16(1)	1

N2	(797(1)	6220(2)	1413(1)	14(1)	1

N3	(690(1)	2954(3)	1604(2)	17(1)	1

O1	510(1)	12110(3)	874(1)	35(1)	1

O2	775(2)	10438(3)	2063(2)	54(1)	1

O3	1473(2)	10189(3)	1198(2)	61(1)	1

O4	1680(1)	12334(2)	2143(1)	33(1)	1

Cl1	1118(1)	11246(1)	1564(1)	24(1)	1

Co1	0	4698(1)	2500	13(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(C2	1.386(4)

C1(C6	1.396(4)

C1(N2	1.464(3)

C2(C3	1.380(4)

C3(C4	1.388(4)

C4(C5	1.378(4)

C5(C6	1.391(4)

C6(N3	1.449(3)

C7(N1	1.484(3)

C7(C10i	1.507(4)

C8(N1	1.483(3)

C8(C9	1.515(4)

C9(N2	1.487(3)

C10(N2	1.485(3)

C10(C7i	1.507(4)

N1(Co1	2.146(2)

N2(Co1	2.221(2)

N3(Co1	2.121(2)

O1(Cl1	1.438(2)

O2(Cl1	1.443(2)

O3(Cl1	1.418(2)

O4(Cl1	1.4349(19)

Co1(N3i	2.121(2)

Co1(N1i	2.146(2)

Co1(N2i	2.221(2)

C2(C1(C6	118.8(2)

C2(C1(N2	122.0(2)

C6(C1(N2	119.2(2)

C3(C2(C1	120.9(3)

C2(C3(C4	120.1(3)

C5(C4(C3	119.7(3)

C4(C5(C6	120.3(3)

C5(C6(C1	120.2(2)

C5(C6(N3	121.2(2)

C1(C6(N3	118.6(2)

N1(C7(C10i	110.8(2)

N1(C8(C9	112.0(2)

N2(C9(C8	109.8(2)

N2(C10(C7i	110.3(2)

C8(N1(C7	116.1(2)

C8(N1(Co1	111.02(17)

C7(N1(Co1	108.34(16)

C1(N2(C10	111.07(19)

C1(N2(C9	111.9(2)

C10(N2(C9	112.0(2)

C1(N2(Co1	108.25(14)

C10(N2(Co1	108.12(15)

C9(N2(Co1	105.23(14)

C6(N3(Co1	112.08(16)

O3(Cl1(O4	110.35(14)

O3(Cl1(O1	110.35(14)

O4(Cl1(O1	108.72(12)

O3(Cl1(O2	111.69(17)

O4(Cl1(O2	108.03(14)

O1(Cl1(O2	107.58(15)

N3(Co1(N3i	90.89(12)

N3(Co1(N1	102.55(9)

N3i(Co1(N1	99.58(10)

N3(Co1(N1i	99.58(10)

N3i(Co1(N1i	102.55(10)

N1(Co1(N1i	148.27(13)

N3(Co1(N2i	171.08(8)

N3i(Co1(N2i	80.37(8)

N1(Co1(N2i	80.88(8)

N1i(Co1(N2i	80.72(8)

N3(Co1(N2	80.37(8)

N3i(Co1(N2	171.08(8)

N1(Co1(N2	80.72(8)

N1i(Co1(N2	80.88(8)

N2i(Co1(N2	108.41(10)

Symmetry transformations used to generate equivalent atoms:

(i) (x,y,(z+1/2

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	14(1) 	19(1)	14(1) 	(1(1)	7(1) 	1(1)

C2	18(2) 	18(2)	19(2) 	2(1)	7(1) 	3(1)

C3	17(2) 	30(2)	12(2) 	1(1)	5(1) 	1(1)

C4	15(1) 	29(2)	16(2) 	(7(1)	7(1) 	(5(1)

C5	17(1) 	20(2)	19(2) 	(4(1)	9(1) 	(2(1)

C6	12(1) 	20(1)	13(1) 	0(1)	6(1) 	0(1)

C7	13(1) 	25(2)	19(2) 	4(1)	7(1) 	(4(1)

C8	19(2) 	21(2)	15(2) 	1(1)	6(1) 	(4(1)

C9	20(1) 	15(1)	16(2) 	3(1)	6(1) 	(2(1)

C10	17(1) 	19(2)	17(1) 	(3(1)	5(1) 	4(1)

N1	18(1) 	16(1)	16(1) 	(3(1)	8(1) 	1(1)

N2	15(1) 	13(1)	13(1) 	(2(1)	5(1) 	0(1)

N3	16(1) 	16(1)	18(1) 	1(1)	5(1) 	2(1)

O1	26(1) 	52(2)	19(1) 	3(1)	3(1) 	8(1)

O2	84(2) 	30(1)	59(2) 	10(1)	41(2) 	(12(1)

O3	50(2) 	63(2)	64(2) 	(35(1)	19(1) 	19(1)

O4	26(1) 	26(1)	33(1) 	(7(1)	1(1) 	0(1)

Cl1	27(1) 	20(1)	21(1) 	(4(1)	7(1) 	1(1)

Co1	13(1) 	13(1)	12(1) 	0	5(1) 	0

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H9A	(88(14)	8090(30)	1720(17)	15(7)	1

H7A	1803(15)	5050(30)	2993(17)	16(7)	1

H5	(1540(14)	1560(30)	102(17)	14(7)	1

H10B	(1823(14)	7350(30)	1216(16)	12(6)	1

H10A	(1043(14)	7950(30)	2039(16)	11(6)	1

H6B	(981(19)	2510(40)	1830(20)	35(9)	1

H7B	1780(15)	6520(30)	2433(16)	12(7)	1

H8B	743(15)	7190(30)	1116(16)	13(7)	1

H8A	190(15)	5820(30)	643(18)	17(7)	1

H4	(2319(15)	2600(30)	(1265(18)	17(7)	1

H6A	(398(18)	2280(30)	1562(19)	25(9)	1

H9B	(591(15)	7900(30)	660(18)	21(7)	1

H3	(2387(16)	5340(30)	(1401(19)	25(8)	1

H1	889(15)	4710(30)	1749(17)	9(8)	1

H2	(1758(16)	6800(30)	(259(18)	24(8)	1

Table 6. Hydrogen bonds [Å and °].

D(H···A	d(D(H)	d(H···A)	d(D···A)	((DHA)

N3(H6B...O2ii	0.88(3)	2.47(3)	3.157(3)	135(3)

N3(H6B...O4ii	0.88(3)	2.60(3)	3.424(3)	155(3)

N3(H6A...O1iii	0.83(3)	2.47(3)	3.116(3)	136(3)

N3(H6A...O2iii	0.83(3)	2.56(3)	3.342(4)	158(3)

N1(H1...O4iii	0.74(3)	2.44(3)	3.063(3)	142(3)

N1(H1...O1iii	0.74(3)	2.58(3)	3.243(3)	149(3)

Symmetry transformations used to generate equivalent atoms:

(i) (x,y,(z+1/2    (ii) (x,y(1,(z+1/2    (iii) x,y(1,z