|  | University of Southampton · Department of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	02src425

Empirical formula 	C34H32Cl2N4PdS4

Formula weight 	802.18

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P(1

Unit cell dimensions	a = 6.2568(3) Å	( = 100.823(2)°

b = 11.4708(5) Å	( = 94.201(2)°

c = 12.9370(9) Å	(  = 105.230(2)°

Volume	872.56(8) Å3

Z	1

Density (calculated)	1.527 Mg / m3

Absorption coefficient	0.955 mm(1

F(000)	408

Crystal	Needle; Pale

Crystal size	0.20 ( 0.03 ( 0.02 mm3

( range for data collection	3.37 ( 25.03°

Index ranges	(7 ( h ( 7, (13 ( k ( 13, (15 ( l ( 15

Reflections collected	11258

Independent reflections	3047 [Rint = 0.0734]

Completeness to ( = 25.03°	98.3 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9812 and 0.8320

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	3047 / 20 / 226

Goodness-of-fit on F2	1.025

Final R indices [F2 > 2((F2)]	R1 = 0.0463, wR2 = 0.1021

R indices (all data)	R1 = 0.0648, wR2 = 0.1083

Extinction coefficient	0.0061(18)

Largest diff. peak and hole	0.774 and (0.510 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

The thiophene rings are both disordered.

All hydrogen atoms are fixed.

There is a molecule of acetonitrile in the asymmetric unit that is disordered over two sites.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

Pd1	(5000	0	5000	16(1)	1

Cl1	(2449(2)	(275(1)	3868(1)	24(1)	1

N1	(4058(5)	1859(3)	5044(3)	15(1)	1

C2	(5010(7)	2292(4)	4279(3)	16(1)	1

C3	(4350(7)	3546(4)	4265(3)	19(1)	1

C5	(1849(7)	3911(4)	5841(4)	18(1)	1

C7	(6796(7)	1370(4)	3461(4)	20(1)	1

C4	(2777(7)	4362(4)	5054(4)	20(1)	1

C6	(2480(7)	2653(4)	5824(3)	18(1)	1

C12	(1476(7)	2104(4)	6642(4)	20(1)	1

C8	(7850(40)	1960(30)	2704(19)	17(2)	0.681(4)

C9	(7623(19)	2158(11)	1640(13)	28(1)	0.681(4)

C10	(9180(20)	2809(13)	1325(13)	34(2)	0.681(4)

C11	(10490(20)	2985(12)	2093(7)	34(2)	0.681(4)

S1	(10067(6)	2524(3)	3101(2)	28(1)	0.681(4)

C28	(8260(90)	1920(80)	2800(40)	17(2)	0.319(4)

C29	(10050(50)	2500(30)	2812(17)	28(1)	0.319(4)

C30	(10320(50)	2990(30)	1818(18)	34(2)	0.319(4)

C31	(8780(50)	2690(30)	1220(30)	34(2)	0.319(4)

S6	(7215(9)	2102(6)	1618(7)	28(1)	0.319(4)

C13	360(30)	3060(40)	7400(30)	20(5)	0.680(4)

C14	455(17)	3717(10)	8432(9)	31(1)	0.680(4)

C15	2363(15)	4526(13)	8887(14)	34(1)	0.680(4)

C16	4000(30)	4516(12)	8258(7)	34(1)	0.680(4)

S2	3039(5)	3471(3)	7049(2)	31(1)	0.680(4)

C33	530(70)	2950(90)	7420(70)	20(5)	0.320(4)

C34	2760(40)	3440(30)	7286(19)	31(1)	0.320(4)

C35	3990(60)	4370(30)	8006(17)	34(1)	0.320(4)

C36	2880(30)	4660(30)	8840(30)	34(1)	0.320(4)

S7	(34(8)	3813(5)	8568(5)	31(1)	0.320(4)

C1A	(2228(14)	(605(9)	1135(6)	36(2)	0.686(7)

C2A	(4830(30)	(907(11)	1010(8)	67(3)	0.686(7)

N1A	(6395(15)	(1073(9)	891(7)	61(3)	0.686(7)

C1B	(1380(30)	(1075(19)	1131(16)	36(2)	0.314(7)

C2B	(4180(60)	(1500(20)	829(19)	67(3)	0.314(7)

N1B	(5840(30)	(2203(18)	592(15)	61(3)	0.314(7)

Table 3. Bond lengths [Å] and angles [°].

Pd1(N1i	2.046(3)

Pd1(N1	2.046(3)

Pd1(Cl1i	2.2857(10)

Pd1(Cl1	2.2857(10)

N1(C2	1.354(5)

N1(C6	1.364(5)

C2(C3	1.392(6)

C2(C7	1.508(6)

C3(C4	1.377(6)

C3(H3	0.9500

C5(C4	1.383(6)

C5(C6	1.387(6)

C5(H5	0.9500

C7(C8	1.496(10)

C7(C28	1.54(2)

C7(H7A	0.9900

C7(H7B	0.9900

C4(H4	0.9500

C6(C12	1.508(6)

C12(C13	1.500(11)

C12(C33	1.53(3)

C12(H12A	0.9900

C12(H12B	0.9900

C8(C9	1.45(2)

C8(S1	1.749(15)

C9(C10	1.454(13)

C9(H9	0.9500

C10(C11	1.349(11)

C10(H10	0.9500

C11(S1	1.527(9)

C11(H11	0.9500

C28(C29	1.44(3)

C28(S6	1.74(3)

C29(C30	1.52(2)

C29(H29	0.9500

C30(C31	1.353(16)

C30(H30	0.9500

C31(S6	1.439(17)

C31(H31	0.9500

C13(C14	1.39(3)

C13(S2	1.74(2)

C14(C15	1.321(15)

C14(H14	0.9500

C15(C16	1.355(11)

C15(H15	0.9500

C16(S2	1.739(8)

C16(H16	0.9500

C33(C34	1.40(3)

C33(S7	1.74(3)

C34(C35	1.30(2)

C34(H34	0.9500

C35(C36	1.358(17)

C35(H35	0.9500

C36(S7	1.802(16)

C36(H36	0.9500

C1A(C2A	1.560(18)

C1A(H1A1	0.9800

C1A(H1A2	0.9800

C1A(H1A3	0.9800

C2A(N1A	0.945(15)

C1B(C2B	1.68(4)

C1B(H1B1	0.9800

C1B(H1B2	0.9800

C1B(H1B3	0.9800

C2B(N1B	1.12(3)

N1i(Pd1(N1	180.0

N1i(Pd1(Cl1i	90.17(10)

N1(Pd1(Cl1i	89.83(10)

N1i(Pd1(Cl1	89.83(10)

N1(Pd1(Cl1	90.17(10)

Cl1i(Pd1(Cl1	180.00(4)

C2(N1(C6	120.2(3)

C2(N1(Pd1	119.0(3)

C6(N1(Pd1	120.7(3)

N1(C2(C3	120.5(4)

N1(C2(C7	117.5(4)

C3(C2(C7	122.1(4)

C4(C3(C2	120.0(4)

C4(C3(H3	120.0

C2(C3(H3	120.0

C4(C5(C6	120.2(4)

C4(C5(H5	119.9

C6(C5(H5	119.9

C8(C7(C2	113.1(15)

C8(C7(C28	10.9(18)

C2(C7(C28	116(3)

C8(C7(H7A	109.0

C2(C7(H7A	109.0

C28(C7(H7A	116.2

C8(C7(H7B	109.0

C2(C7(H7B	109.0

C28(C7(H7B	98.4

H7A(C7(H7B	107.8

C3(C4(C5	118.9(4)

C3(C4(H4	120.6

C5(C4(H4	120.6

N1(C6(C5	120.1(4)

N1(C6(C12	117.3(4)

C5(C6(C12	122.6(4)

C13(C12(C6	112(2)

C13(C12(C33	7(7)

C6(C12(C33	118(6)

C13(C12(H12A	109.3

C6(C12(H12A	109.3

C33(C12(H12A	109.1

C13(C12(H12B	109.3

C6(C12(H12B	109.3

C33(C12(H12B	102.9

H12A(C12(H12B	107.9

C9(C8(C7	136.9(13)

C9(C8(S1	105.9(6)

C7(C8(S1	117.0(10)

C8(C9(C10	110.5(12)

C8(C9(H9	124.7

C10(C9(H9	124.7

C11(C10(C9	110.2(15)

C11(C10(H10	124.9

C9(C10(H10	124.9

C10(C11(S1	117.7(14)

C10(C11(H11	121.2

S1(C11(H11	121.2

C11(S1(C8	95.6(7)

C29(C28(C7	145(3)

C29(C28(S6	104.0(12)

C7(C28(S6	110.4(19)

C28(C29(C30	111(2)

C28(C29(H29	124.3

C30(C29(H29	124.3

C31(C30(C29	106(3)

C31(C30(H30	127.2

C29(C30(H30	127.2

C30(C31(S6	121(3)

C30(C31(H31	119.6

S6(C31(H31	119.6

C31(S6(C28	98.0(17)

C14(C13(C12	133.1(19)

C14(C13(S2	106.9(8)

C12(C13(S2	119.9(15)

C15(C14(C13	118.2(14)

C15(C14(H14	120.9

C13(C14(H14	120.9

C14(C15(C16	111.5(16)

C14(C15(H15	124.2

C16(C15(H15	124.2

C15(C16(S2	112.1(14)

C15(C16(H16	124.0

S2(C16(H16	124.0

C13(S2(C16	91.1(8)

C34(C33(C12	131(5)

C34(C33(S7	108.7(14)

C12(C33(S7	117(2)

C35(C34(C33	118(2)

C35(C34(H34	120.8

C33(C34(H34	120.8

C34(C35(C36	112(3)

C34(C35(H35	124.0

C36(C35(H35	124.0

C35(C36(S7	111(3)

C35(C36(H36	124.3

S7(C36(H36	124.3

C33(S7(C36	88.8(15)

N1A(C2A(C1A	176.3(13)

N1B(C2B(C1B	153(3)

Symmetry transformations used to generate equivalent atoms:

(i) (x(1,(y,(z+1

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

Pd1	13(1) 	12(1)	20(1) 	3(1)	1(1) 	4(1)

Cl1	22(1) 	20(1)	31(1) 	5(1)	11(1) 	8(1)

N1	11(2) 	19(2)	17(2) 	6(2)	1(1) 	7(2)

C2	13(2) 	16(2)	20(2) 	4(2)	5(2) 	5(2)

C3	17(2) 	19(2)	23(2) 	7(2)	0(2) 	9(2)

C5	14(2) 	15(2)	24(2) 	2(2)	(1(2) 	2(2)

C7	18(2) 	17(2)	25(2) 	3(2)	(2(2) 	7(2)

C4	20(2) 	17(2)	25(2) 	6(2)	6(2) 	4(2)

C6	11(2) 	19(2)	21(2) 	(1(2)	3(2) 	3(2)

C12	18(2) 	16(2)	24(2) 	3(2)	(1(2) 	2(2)

C8	8(9) 	13(3)	25(5) 	3(3)	(2(4) 	(3(7)

C9	23(1) 	26(1)	34(1) 	8(1)	(2(1) 	9(1)

C10	39(4) 	27(2)	34(4) 	14(3)	(9(4) 	6(2)

C11	39(4) 	27(2)	34(4) 	14(3)	(9(4) 	6(2)

S1	23(1) 	26(1)	34(1) 	8(1)	(2(1) 	9(1)

C28	8(9) 	13(3)	25(5) 	3(3)	(2(4) 	(3(7)

C29	23(1) 	26(1)	34(1) 	8(1)	(2(1) 	9(1)

C30	39(4) 	27(2)	34(4) 	14(3)	(9(4) 	6(2)

C31	39(4) 	27(2)	34(4) 	14(3)	(9(4) 	6(2)

S6	23(1) 	26(1)	34(1) 	8(1)	(2(1) 	9(1)

C13	18(3) 	17(8)	27(3) 	7(5)	(4(4) 	7(5)

C14	23(1) 	29(1)	39(1) 	6(1)	(1(1) 	6(1)

C15	34(3) 	23(3)	37(4) 	(2(2)	(19(4) 	3(3)

C16	34(3) 	23(3)	37(4) 	(2(2)	(19(4) 	3(3)

S2	23(1) 	29(1)	39(1) 	6(1)	(1(1) 	6(1)

C33	18(3) 	17(8)	27(3) 	7(5)	(4(4) 	7(5)

C34	23(1) 	29(1)	39(1) 	6(1)	(1(1) 	6(1)

C35	34(3) 	23(3)	37(4) 	(2(2)	(19(4) 	3(3)

C36	34(3) 	23(3)	37(4) 	(2(2)	(19(4) 	3(3)

S7	23(1) 	29(1)	39(1) 	6(1)	(1(1) 	6(1)

C1A	35(6) 	40(6)	10(3) 	(13(3)	2(4) 	(12(3)

C2A	128(12) 	41(8)	32(5) 	15(6)	25(6) 	15(7)

N1A	37(4) 	67(5)	62(5) 	25(4)	(24(4) 	(15(4)

C1B	35(6) 	40(6)	10(3) 	(13(3)	2(4) 	(12(3)

C2B	128(12) 	41(8)	32(5) 	15(6)	25(6) 	15(7)

N1B	37(4) 	67(5)	62(5) 	25(4)	(24(4) 	(15(4)