|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	04src0851    (MEB 7.16A)

Empirical formula 	C55H44Cl4O6P2Pd

Formula weight 	1111.04

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21

Unit cell dimensions	a = 11.268(3) Å	( = 90°

b = 20.164(3) Å	( = 109.820(15)°

c = 11.420(3) Å	(  = 90°

Volume	2441.1(9) Å3

Z	2

Density (calculated)	1.512 Mg / m3

Absorption coefficient	0.717 mm(1

F(000)	1132

Crystal	shard; colourless

Crystal size	0.18 ( 0.08 ( 0.02 mm3

( range for data collection	2.98 ( 27.50°

Index ranges	(14 ( h ( 14, (26 ( k ( 26, (14 ( l ( 14

Reflections collected	25786

Independent reflections	10212 [Rint = 0.0669]

Completeness to ( = 27.50°	96.2 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9858 and 0.8818

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	10212 / 7 / 621

Goodness-of-fit on F2	1.069

Final R indices [F2 > 2((F2)]	R1 = 0.1121, wR2 = 0.3015

R indices (all data)	R1 = 0.1245, wR2 = 0.3115

Absolute structure parameter	0.18(7)

Extinction coefficient	0.030(3)

Largest diff. peak and hole	2.478 and (1.793 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Split crystal? Hence poor R factor. Can't get better dataset. Molecule of chloroform present.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	2499(11)	9344(9)	8399(10)	30(2)	1

C2	2678(13)	8932(6)	9403(12)	27(3)	1

C3	3845(13)	8869(6)	10379(13)	30(3)	1

C4	4900(20)	9265(8)	10350(20)	73(7)	1

C5	4768(14)	9681(6)	9321(11)	30(3)	1

C6	3590(11)	9707(6)	8374(12)	25(2)	1

C7	3979(17)	8369(7)	11411(16)	43(4)	1

C8	3720(20)	7663(9)	10912(19)	57(5)	1

C9	5360(18)	8341(7)	12296(17)	46(4)	1

C10	3155(15)	8543(8)	12162(15)	40(3)	1

C11	5887(13)	10072(6)	9263(11)	29(3)	1

C12	7092(14)	9928(7)	10469(15)	41(3)	1

C13	5643(14)	10809(7)	9237(14)	37(3)	1

C14	6289(14)	9872(7)	8200(13)	35(3)	1

C15	(1495(12)	7877(7)	7526(12)	33(3)	1

C16	(1965(16)	7681(7)	6242(14)	38(3)	1

C17	(3272(14)	7616(6)	5733(13)	36(3)	1

C18	(4064(14)	7731(6)	6392(13)	33(3)	1

C19	(5444(13)	7720(7)	5808(14)	37(3)	1

C20	(6175(14)	7869(7)	6448(13)	37(3)	1

C21	(5705(15)	8040(7)	7673(17)	44(4)	1

C22	(4410(14)	8045(6)	8259(13)	33(3)	1

C23	(3620(12)	7903(6)	7615(13)	29(3)	1

C24	(2249(14)	7964(6)	8245(12)	32(3)	1

C25	(1638(13)	8189(7)	9555(14)	35(3)	1

C26	(1807(14)	7800(6)	10561(13)	33(3)	1

C27	(2466(14)	7185(6)	10388(15)	36(3)	1

C28	(2552(13)	6860(7)	11399(15)	39(3)	1

C29	(2084(14)	7152(7)	12615(14)	35(3)	1

C30	(1451(16)	7720(8)	12784(16)	43(4)	1

C31	(1271(14)	8069(6)	11816(12)	32(3)	1

C32	(575(14)	8659(7)	11965(14)	35(3)	1

C33	(295(13)	8955(7)	11059(14)	37(3)	1

C34	(849(13)	8710(6)	9844(14)	33(3)	1

C35	3513(15)	9769(6)	4720(13)	34(3)	1

C36	4662(13)	9437(5)	5112(13)	33(3)	1

C37	5551(16)	9613(8)	4670(15)	44(4)	1

C38	5379(12)	10137(7)	3854(13)	31(3)	1

C39	6406(15)	10375(7)	3430(15)	39(3)	1

C40	6252(15)	10929(6)	2694(14)	38(3)	1

C41	5097(17)	11302(6)	2408(15)	40(4)	1

C42	4158(16)	11089(8)	2809(16)	41(3)	1

C43	4245(15)	10504(7)	3528(14)	36(3)	1

C44	3195(14)	10283(6)	3892(12)	32(3)	1

C45	1994(13)	10626(6)	3583(14)	32(3)	1

C46	1276(15)	10750(6)	2226(14)	36(3)	1

C47	1613(16)	10499(6)	1230(14)	38(3)	1

C48	984(15)	10655(7)	59(14)	38(3)	1

C49	(100(20)	11081(9)	(278(16)	55(5)	1

C50	(519(19)	11327(10)	663(18)	56(5)	1

C51	152(13)	11158(8)	1916(13)	36(3)	1

C52	(304(16)	11349(8)	2815(15)	48(4)	1

C53	257(14)	11164(6)	4051(14)	34(3)	1

C54	1410(13)	10796(6)	4336(12)	29(3)	1

C55	2530(20)	6416(8)	4063(15)	54(5)	1

O1	1589(10)	8564(4)	9376(9)	35(2)	1

O2	3425(9)	10088(5)	7302(9)	32(2)	1

O3	(194(9)	7987(5)	7996(9)	32(2)	1

O4	(625(9)	9045(4)	8855(8)	28(2)	1

O5	2568(10)	9486(4)	5133(8)	38(3)	1

O6	2040(9)	10695(5)	5652(9)	31(2)	1

P1	330(3)	8722(2)	8273(3)	30(1)	1

P2	2160(3)	9945(2)	6156(3)	28(1)	1

Cl1	(886(3)	9218(2)	5139(3)	40(1)	1

Cl2	1544(5)	7119(2)	3466(5)	65(1)	1

Cl3	3745(5)	6359(2)	3493(5)	58(1)	1

Cl4	1557(5)	5691(2)	3700(4)	53(1)	1

Pd1	906(1)	9344(1)	6928(1)	29(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(C2	1.374(19)

C1(C6	1.440(19)

C1(Pd1	2.001(11)

C2(C3	1.412(19)

C2(O1	1.425(16)

C3(C4	1.44(2)

C3(C7	1.52(2)

C4(C5	1.41(2)

C4(H4	0.9500

C5(C6	1.400(18)

C5(C11	1.51(2)

C6(O2	1.403(16)

C7(C10	1.50(2)

C7(C8	1.52(2)

C7(C9	1.54(3)

C8(H8A	0.9800

C8(H8B	0.9800

C8(H8C	0.9800

C9(H9A	0.9800

C9(H9B	0.9800

C9(H9C	0.9800

C10(H10A	0.9800

C10(H10B	0.9800

C10(H10C	0.9800

C11(C14	1.49(2)

C11(C13	1.510(18)

C11(C12	1.599(18)

C12(H12A	0.9800

C12(H12B	0.9800

C12(H12C	0.9800

C13(H13A	0.9800

C13(H13B	0.9800

C13(H13C	0.9800

C14(H14A	0.9800

C14(H14B	0.9800

C14(H14C	0.9800

C15(C24	1.38(2)

C15(O3	1.398(16)

C15(C16	1.435(19)

C16(C17	1.39(2)

C16(H16	0.9500

C17(C18	1.37(2)

C17(H17	0.9500

C18(C23	1.36(2)

C18(C19	1.47(2)

C19(C20	1.31(2)

C19(H19	0.9500

C20(C21	1.36(2)

C20(H20	0.9500

C21(C22	1.38(2)

C21(H21	0.9500

C22(C23	1.36(2)

C22(H22	0.9500

C23(C24	1.471(19)

C24(C25	1.490(19)

C25(C34	1.344(19)

C25(C26	1.45(2)

C26(C27	1.424(17)

C26(C31	1.458(18)

C27(C28	1.36(2)

C27(H27	0.9500

C28(C29	1.43(2)

C28(H28	0.9500

C29(C30	1.33(2)

C29(H29	0.9500

C30(C31	1.38(2)

C30(H30	0.9500

C31(C32	1.403(19)

C32(C33	1.32(2)

C32(H32	0.9500

C33(C34	1.40(2)

C33(H33	0.9500

C34(O4	1.410(17)

C35(C44	1.366(18)

C35(C36	1.39(2)

C35(O5	1.422(18)

C36(C37	1.31(2)

C36(H36	0.9500

C37(C38	1.38(2)

C37(H37	0.9500

C38(C43	1.41(2)

C38(C39	1.48(2)

C39(C40	1.37(2)

C39(H39	0.9500

C40(C41	1.44(2)

C40(H40	0.9500

C41(C42	1.36(2)

C41(H41	0.9500

C42(C43	1.42(2)

C42(H42	0.9500

C43(C44	1.45(2)

C44(C45	1.452(18)

C45(C54	1.29(2)

C45(C46	1.51(2)

C46(C47	1.41(2)

C46(C51	1.45(2)

C47(C48	1.32(2)

C47(H47	0.9500

C48(C49	1.43(3)

C48(H48	0.9500

C49(C50	1.40(3)

C49(H49	0.9500

C50(C51	1.41(2)

C50(H50	0.9500

C51(C52	1.35(2)

C52(C53	1.39(2)

C52(H52	0.9500

C53(C54	1.43(2)

C53(H53	0.9500

C54(O6	1.443(15)

C55(Cl3	1.71(2)

C55(Cl2	1.79(2)

C55(Cl4	1.789(17)

C55(H55	1.0000

O1(P1	1.578(12)

O2(P2	1.601(10)

O3(P1	1.588(10)

O4(P1	1.583(10)

O5(P2	1.672(12)

O6(P2	1.609(10)

P1(Pd1	2.242(4)

P2(Pd1	2.256(4)

Cl1(Pd1	2.349(3)

C2(C1(C6	116.1(10)

C2(C1(Pd1	122.5(11)

C6(C1(Pd1	120.8(9)

C1(C2(C3	123.1(12)

C1(C2(O1	114.5(12)

C3(C2(O1	122.4(12)

C2(C3(C4	119.1(15)

C2(C3(C7	119.5(12)

C4(C3(C7	121.4(15)

C5(C4(C3	120(2)

C5(C4(H4	120.1

C3(C4(H4	120.1

C6(C5(C4	118.0(16)

C6(C5(C11	122.3(11)

C4(C5(C11	119.8(15)

C5(C6(O2	120.4(11)

C5(C6(C1	123.9(11)

O2(C6(C1	115.7(10)

C10(C7(C3	111.6(13)

C10(C7(C8	110.9(14)

C3(C7(C8	111.9(13)

C10(C7(C9	108.4(14)

C3(C7(C9	110.2(13)

C8(C7(C9	103.4(13)

C7(C8(H8A	109.5

C7(C8(H8B	109.5

H8A(C8(H8B	109.5

C7(C8(H8C	109.5

H8A(C8(H8C	109.5

H8B(C8(H8C	109.5

C7(C9(H9A	109.5

C7(C9(H9B	109.5

H9A(C9(H9B	109.5

C7(C9(H9C	109.5

H9A(C9(H9C	109.5

H9B(C9(H9C	109.5

C7(C10(H10A	109.5

C7(C10(H10B	109.5

H10A(C10(H10B	109.5

C7(C10(H10C	109.5

H10A(C10(H10C	109.5

H10B(C10(H10C	109.5

C14(C11(C5	112.6(11)

C14(C11(C13	110.7(11)

C5(C11(C13	111.5(12)

C14(C11(C12	104.4(12)

C5(C11(C12	110.2(11)

C13(C11(C12	107.0(11)

C11(C12(H12A	109.5

C11(C12(H12B	109.5

H12A(C12(H12B	109.5

C11(C12(H12C	109.5

H12A(C12(H12C	109.5

H12B(C12(H12C	109.5

C11(C13(H13A	109.5

C11(C13(H13B	109.5

H13A(C13(H13B	109.5

C11(C13(H13C	109.5

H13A(C13(H13C	109.5

H13B(C13(H13C	109.5

C11(C14(H14A	109.5

C11(C14(H14B	109.5

H14A(C14(H14B	109.5

C11(C14(H14C	109.5

H14A(C14(H14C	109.5

H14B(C14(H14C	109.5

C24(C15(O3	122.0(11)

C24(C15(C16	123.8(13)

O3(C15(C16	114.3(13)

C17(C16(C15	115.0(14)

C17(C16(H16	122.5

C15(C16(H16	122.5

C18(C17(C16	123.3(14)

C18(C17(H17	118.4

C16(C17(H17	118.4

C23(C18(C17	121.8(14)

C23(C18(C19	115.7(14)

C17(C18(C19	122.4(14)

C20(C19(C18	120.9(14)

C20(C19(H19	119.6

C18(C19(H19	119.6

C19(C20(C21	122.2(15)

C19(C20(H20	118.9

C21(C20(H20	118.9

C20(C21(C22	118.5(16)

C20(C21(H21	120.7

C22(C21(H21	120.7

C23(C22(C21	120.8(14)

C23(C22(H22	119.6

C21(C22(H22	119.6

C18(C23(C22	121.9(13)

C18(C23(C24	118.9(13)

C22(C23(C24	119.2(12)

C15(C24(C23	117.1(12)

C15(C24(C25	118.0(12)

C23(C24(C25	124.6(13)

C34(C25(C26	118.7(13)

C34(C25(C24	121.7(14)

C26(C25(C24	119.3(12)

C27(C26(C25	124.1(12)

C27(C26(C31	118.8(13)

C25(C26(C31	117.0(11)

C28(C27(C26	119.1(14)

C28(C27(H27	120.5

C26(C27(H27	120.4

C27(C28(C29	121.1(13)

C27(C28(H28	119.5

C29(C28(H28	119.5

C30(C29(C28	119.8(14)

C30(C29(H29	120.1

C28(C29(H29	120.1

C29(C30(C31	122.6(15)

C29(C30(H30	118.7

C31(C30(H30	118.7

C30(C31(C32	124.2(13)

C30(C31(C26	118.3(13)

C32(C31(C26	117.5(12)

C33(C32(C31	124.1(13)

C33(C32(H32	118.0

C31(C32(H32	118.0

C32(C33(C34	118.1(13)

C32(C33(H33	121.0

C34(C33(H33	121.0

C25(C34(C33	123.6(14)

C25(C34(O4	117.5(13)

C33(C34(O4	118.9(12)

C44(C35(C36	125.8(14)

C44(C35(O5	118.9(13)

C36(C35(O5	114.8(11)

C37(C36(C35	119.7(13)

C37(C36(H36	120.2

C35(C36(H36	120.2

C36(C37(C38	121.0(15)

C36(C37(H37	119.5

C38(C37(H37	119.5

C37(C38(C43	119.2(14)

C37(C38(C39	121.6(14)

C43(C38(C39	118.8(13)

C40(C39(C38	120.9(15)

C40(C39(H39	119.5

C38(C39(H39	119.5

C39(C40(C41	118.7(14)

C39(C40(H40	120.7

C41(C40(H40	120.7

C42(C41(C40	120.4(14)

C42(C41(H41	119.8

C40(C41(H41	119.8

C41(C42(C43	123.2(15)

C41(C42(H42	118.4

C43(C42(H42	118.4

C38(C43(C42	117.8(13)

C38(C43(C44	121.1(13)

C42(C43(C44	121.1(13)

C35(C44(C43	112.5(13)

C35(C44(C45	122.3(14)

C43(C44(C45	124.5(12)

C54(C45(C44	127.3(13)

C54(C45(C46	115.0(12)

C44(C45(C46	117.4(12)

C47(C46(C51	117.3(14)

C47(C46(C45	125.0(14)

C51(C46(C45	117.7(13)

C48(C47(C46	122.2(15)

C48(C47(H47	118.9

C46(C47(H47	118.9

C47(C48(C49	122.0(15)

C47(C48(H48	119.0

C49(C48(H48	119.0

C50(C49(C48	118.9(16)

C50(C49(H49	120.6

C48(C49(H49	120.6

C49(C50(C51	119.1(19)

C49(C50(H50	120.4

C51(C50(H50	120.4

C52(C51(C50	119.3(15)

C52(C51(C46	120.2(13)

C50(C51(C46	120.4(16)

C51(C52(C53	122.5(15)

C51(C52(H52	118.8

C53(C52(H52	118.8

C52(C53(C54	115.8(15)

C52(C53(H53	122.1

C54(C53(H53	122.1

C45(C54(C53	127.7(13)

C45(C54(O6	118.3(12)

C53(C54(O6	113.3(12)

Cl3(C55(Cl2	112.5(9)

Cl3(C55(Cl4	111.4(10)

Cl2(C55(Cl4	107.9(11)

Cl3(C55(H55	108.3

Cl2(C55(H55	108.3

Cl4(C55(H55	108.3

C2(O1(P1	116.5(8)

C6(O2(P2	115.6(8)

C15(O3(P1	119.7(9)

C34(O4(P1	118.1(8)

C35(O5(P2	115.1(8)

C54(O6(P2	117.2(8)

O1(P1(O4	107.6(5)

O1(P1(O3	98.2(5)

O4(P1(O3	102.0(5)

O1(P1(Pd1	105.6(4)

O4(P1(Pd1	117.0(3)

O3(P1(Pd1	124.0(4)

O2(P2(O6	93.8(5)

O2(P2(O5	106.9(5)

O6(P2(O5	106.3(5)

O2(P2(Pd1	106.2(4)

O6(P2(Pd1	131.1(4)

O5(P2(Pd1	109.4(3)

C1(Pd1(P1	79.1(4)

C1(Pd1(P2	79.9(4)

P1(Pd1(P2	158.95(13)

C1(Pd1(Cl1	173.0(5)

P1(Pd1(Cl1	99.93(13)

P2(Pd1(Cl1	100.70(13)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	25(5) 	30(5)	27(5) 	3(7)	1(4) 	16(7)

C2	32(7) 	18(5)	34(6) 	(4(5)	14(5) 	2(4)

C3	38(7) 	14(5)	34(7) 	(9(5)	7(6) 	(9(5)

C4	124(17) 	19(7)	129(17) 	17(9)	109(16) 	18(9)

C5	52(8) 	16(5)	16(5) 	1(4)	4(5) 	1(5)

C6	22(6) 	18(5)	28(6) 	(4(4)	(1(5) 	(5(4)

C7	60(10) 	26(7)	47(9) 	5(6)	25(8) 	(2(6)

C8	76(13) 	38(9)	59(11) 	19(8)	26(10) 	22(8)

C9	70(11) 	15(6)	56(10) 	4(6)	24(8) 	1(6)

C10	40(8) 	36(7)	40(8) 	13(6)	8(7) 	18(6)

C11	30(7) 	20(6)	22(6) 	13(5)	(12(5) 	7(5)

C12	30(7) 	30(7)	49(8) 	2(6)	(4(6) 	7(6)

C13	33(7) 	27(7)	39(8) 	1(6)	(2(6) 	(7(5)

C14	41(8) 	24(6)	35(7) 	1(5)	6(6) 	(13(5)

C15	14(6) 	41(7)	29(6) 	(10(5)	(11(5) 	1(5)

C16	52(9) 	26(7)	28(7) 	5(5)	4(6) 	8(6)

C17	43(8) 	17(6)	34(7) 	16(5)	(3(6) 	4(5)

C18	48(8) 	11(5)	37(7) 	5(5)	12(6) 	6(5)

C19	27(7) 	34(7)	37(7) 	8(6)	(5(6) 	1(5)

C20	37(8) 	35(7)	28(7) 	5(5)	(3(6) 	(8(6)

C21	43(9) 	18(6)	68(10) 	(6(6)	16(8) 	0(6)

C22	41(8) 	18(5)	32(7) 	0(5)	3(6) 	1(5)

C23	29(7) 	17(5)	34(7) 	(3(5)	2(5) 	(6(5)

C24	41(8) 	19(5)	32(7) 	(4(5)	5(6) 	(16(5)

C25	26(7) 	33(7)	45(8) 	(18(6)	11(6) 	(4(5)

C26	50(8) 	18(6)	31(7) 	(11(5)	13(6) 	(11(5)

C27	37(8) 	21(6)	49(8) 	(6(6)	15(6) 	(8(5)

C28	25(7) 	33(7)	50(9) 	9(6)	(1(6) 	2(5)

C29	42(8) 	25(6)	38(7) 	11(5)	12(6) 	7(5)

C30	54(10) 	36(8)	42(8) 	4(6)	18(7) 	15(7)

C31	40(8) 	23(6)	23(6) 	1(5)	(2(5) 	3(5)

C32	37(8) 	36(7)	34(7) 	(15(6)	13(6) 	(9(6)

C33	23(7) 	40(8)	40(8) 	(4(6)	2(6) 	(5(5)

C34	35(7) 	17(5)	50(8) 	(2(5)	19(6) 	(3(5)

C35	45(8) 	23(6)	33(7) 	7(5)	12(6) 	5(5)

C36	42(7) 	6(5)	50(7) 	3(5)	14(6) 	3(5)

C37	48(9) 	33(7)	41(8) 	3(6)	0(7) 	2(6)

C38	22(6) 	30(6)	35(7) 	(3(5)	3(5) 	(11(5)

C39	37(8) 	28(7)	44(8) 	(1(6)	7(6) 	(6(5)

C40	50(9) 	13(5)	45(8) 	(12(5)	10(7) 	(13(5)

C41	70(11) 	18(6)	44(8) 	(4(5)	33(8) 	(11(6)

C42	50(9) 	34(7)	46(9) 	3(6)	26(7) 	7(6)

C43	44(8) 	34(7)	36(7) 	2(6)	21(6) 	4(6)

C44	51(9) 	17(6)	26(6) 	0(5)	12(6) 	13(5)

C45	32(7) 	19(6)	43(8) 	13(5)	11(6) 	10(5)

C46	47(8) 	14(5)	41(8) 	0(5)	10(6) 	(7(5)

C47	63(10) 	14(5)	40(8) 	(2(5)	21(7) 	(6(6)

C48	47(9) 	30(7)	35(7) 	(10(6)	12(6) 	(12(6)

C49	76(13) 	47(9)	35(8) 	3(7)	11(8) 	(32(9)

C50	54(11) 	56(10)	55(10) 	1(8)	15(8) 	(29(8)

C51	32(7) 	41(7)	31(7) 	21(6)	7(6) 	4(6)

C52	51(10) 	40(8)	41(8) 	24(7)	2(7) 	3(7)

C53	40(8) 	22(6)	39(8) 	12(5)	11(6) 	4(5)

C54	39(7) 	16(5)	25(6) 	4(4)	4(5) 	(5(5)

C55	86(13) 	32(8)	30(8) 	3(6)	3(8) 	(19(9)

O1	53(6) 	14(4)	41(5) 	(3(4)	23(5) 	(6(4)

O2	32(5) 	28(5)	29(5) 	4(4)	3(4) 	(2(4)

O3	33(5) 	23(4)	36(5) 	5(4)	8(4) 	3(4)

O4	41(5) 	11(4)	33(5) 	5(3)	15(4) 	7(3)

O5	42(5) 	19(5)	30(4) 	12(3)	(17(4) 	(12(3)

O6	35(5) 	25(4)	31(5) 	5(4)	10(4) 	6(4)

P1	32(2) 	24(2)	32(2) 	1(1)	7(1) 	(3(1)

P2	33(2) 	16(1)	32(2) 	(1(1)	9(1) 	(2(1)

Cl1	38(2) 	37(2)	36(2) 	(1(1)	1(1) 	1(1)

Cl2	62(3) 	33(2)	76(3) 	(6(2)	(7(2) 	5(2)

Cl3	81(3) 	41(2)	65(3) 	(9(2)	44(3) 	(6(2)

Cl4	67(3) 	35(2)	49(2) 	0(2)	11(2) 	(13(2)

Pd1	33(1) 	21(1)	31(1) 	3(1)	7(1) 	2(1)