|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	04src0896r

Empirical formula 	C53H48Cl3F6O3P4PdSb

Formula weight 	1305.29

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/c

Unit cell dimensions	a = 12.677(4) Å	( = 90°

b = 26.381(11) Å	( = 95.89(3)°

c = 16.334(5) Å	(  = 90°

Volume	5434(3) Å3

Z	4

Density (calculated)	1.596 Mg / m3

Absorption coefficient	1.156 mm(1

F(000)	2608

Crystal	Block; Yellow

Crystal size	0.17 ( 0.08 ( 0.06 mm3

( range for data collection	2.94 ( 27.48°

Index ranges	(16 ( h ( 16, (34 ( k ( 34, (20 ( l ( 21

Reflections collected	46944

Independent reflections	12362 [Rint = 0.0919]

Completeness to ( = 27.48°	99.2 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9339 and 0.8277

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	12362 / 225 / 753

Goodness-of-fit on F2	1.042

Final R indices [F2 > 2((F2)]	R1 = 0.0951, wR2 = 0.2105

R indices (all data)	R1 = 0.1514, wR2 = 0.2409

Largest diff. peak and hole	1.181 and (1.523 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP3 for Windows (L. J. Farrugia, J. Appl. Crystallogr. 1997, 30, 565).

Special details:

All hydrogen atoms were fixed.

There is a molecule of chloroform in the asymmetric unit which is disordered over 4 main sites.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

Pd1	6996(1)	3495(1)	757(1)	27(1)	1

C1	6834(6)	4327(3)	1962(6)	35(2)	1

C2	7016(6)	4239(3)	1173(5)	30(2)	1

C3	7310(6)	4660(3)	717(6)	33(2)	1

C4	7463(7)	5131(3)	1082(6)	41(2)	1

C5	7304(7)	5193(4)	1894(6)	43(2)	1

C6	6973(7)	4790(3)	2344(6)	42(2)	1

C7	4635(7)	3171(4)	2726(6)	40(2)	1

C8	4704(8)	3498(4)	3368(7)	51(3)	1

C9	4053(9)	3421(5)	4008(7)	65(3)	1

C10	3375(8)	3018(5)	3967(7)	61(3)	1

C11	3310(8)	2702(4)	3310(8)	59(3)	1

C12	3943(7)	2768(4)	2688(7)	47(3)	1

C13	7991(7)	3059(3)	2993(5)	36(2)	1

C14	8657(7)	2699(4)	2743(6)	43(2)	1

C15	9727(7)	2718(5)	3027(7)	58(3)	1

C16	10085(8)	3093(5)	3576(7)	59(3)	1

C17	9415(9)	3456(4)	3815(7)	60(3)	1

C18	8345(8)	3444(3)	3532(5)	38(2)	1

O1	6518(5)	3930(2)	2446(4)	36(1)	1

O2	5205(4)	3231(2)	2042(4)	36(1)	1

O3	6908(4)	3022(2)	2728(4)	33(1)	1

P1	6406(2)	3386(1)	2009(2)	30(1)	1

C21	9196(6)	2814(3)	506(6)	32(2)	1

C22	8326(6)	2534(3)	(27(6)	36(2)	1

C23	6162(6)	2636(3)	(711(5)	33(2)	1

C24	6241(6)	3131(3)	(1171(5)	35(2)	1

C25	9854(6)	3713(3)	1417(5)	31(2)	1

C26	9642(7)	4124(3)	1888(6)	37(2)	1

C27	10398(7)	4309(3)	2470(6)	39(2)	1

C28	11379(7)	4081(4)	2596(6)	44(2)	1

C29	11590(6)	3671(4)	2157(6)	40(2)	1

C30	10862(6)	3483(4)	1556(6)	41(2)	1

C31	9317(5)	3779(3)	(318(5)	29(2)	1

C32	9462(6)	3507(3)	(1022(6)	34(2)	1

C33	9745(7)	3751(4)	(1720(6)	40(2)	1

C34	9873(7)	4259(4)	(1724(6)	43(2)	1

C35	9734(7)	4530(3)	(1021(6)	43(2)	1

C36	9459(6)	4304(3)	(312(6)	39(2)	1

C37	6628(6)	2135(3)	856(5)	32(2)	1

C38	5576(7)	2084(4)	1016(6)	43(2)	1

C39	5270(8)	1664(4)	1446(7)	51(3)	1

C40	5990(8)	1291(4)	1716(6)	46(2)	1

C41	7043(8)	1351(4)	1576(7)	52(3)	1

C42	7364(7)	1761(3)	1160(6)	41(2)	1

C43	4507(6)	3588(3)	(493(6)	36(2)	1

C44	3838(6)	3626(3)	(1214(6)	40(2)	1

C45	2764(7)	3543(3)	(1204(6)	40(2)	1

C46	2365(7)	3432(5)	(498(7)	60(3)	1

C47	3025(9)	3380(7)	225(9)	110(7)	1

C48	4087(7)	3473(5)	196(7)	73(4)	1

C49	6101(6)	4239(3)	(1048(5)	35(2)	1

C50	5421(7)	4644(3)	(924(6)	42(2)	1

C51	5624(7)	5108(4)	(1266(7)	50(3)	1

C52	6453(7)	5189(4)	(1704(7)	54(3)	1

C53	7139(7)	4790(4)	(1826(6)	46(2)	1

C54	6973(7)	4318(3)	(1488(6)	38(2)	1

P21	8872(2)	3482(1)	608(1)	29(1)	1

P22	7006(2)	2672(1)	268(1)	30(1)	1

P23	5942(2)	3654(1)	(497(1)	30(1)	1

F1	1496(6)	2202(3)	469(5)	91(2)	1

F2	2849(7)	1608(6)	1319(10)	202(7)	1

F3	1320(9)	2025(4)	2028(5)	129(4)	1

F4	1292(7)	1050(3)	1754(5)	98(3)	1

F5	(26(5)	1654(3)	907(6)	102(3)	1

F6	1497(7)	1211(3)	201(5)	100(3)	1

Sb1	1420(1)	1618(1)	1116(1)	52(1)	1

C61	1682(9)	4956(5)	4725(6)	99(4)	0.367(3)

Cl61	810(8)	5345(4)	4131(7)	76(3)	0.367(3)

Cl62	1829(11)	5184(5)	5726(6)	109(4)	0.367(3)

Cl63	2878(9)	4933(5)	4302(7)	98(3)	0.367(3)

C66	1470(14)	5003(8)	4906(10)	98(5)	0.185(5)

Cl66	1068(14)	5455(6)	4174(13)	77(6)	0.185(5)

Cl67	892(18)	5125(8)	5803(12)	97(6)	0.185(5)

Cl68	2840(14)	5008(10)	5099(13)	120(4)	0.185(5)

C71	3470(14)	4918(4)	4960(6)	94(4)	0.381(6)

Cl71	3610(10)	5539(3)	5302(5)	100(4)	0.381(6)

Cl72	3752(12)	4864(3)	3950(5)	96(4)	0.381(6)

Cl73	4269(13)	4522(4)	5595(6)	114(4)	0.381(6)

C76	2520(40)	4857(13)	4810(30)	99(4)	0.068(6)

Cl76	2360(40)	5431(14)	5300(30)	110(6)	0.068(6)

Cl77	2980(60)	4970(20)	3860(20)	91(7)	0.068(6)

Cl78	3430(60)	4485(18)	5410(30)	93(6)	0.068(6)

Table 3. Bond lengths [Å] and angles [°].

Pd1(C2	2.077(8)

Pd1(P1	2.267(3)

Pd1(P22	2.313(2)

Pd1(P23	2.365(2)

Pd1(P21	2.416(2)

C1(C2	1.353(12)

C1(C6	1.375(12)

C1(O1	1.395(10)

C2(C3	1.407(12)

C3(C4	1.384(12)

C3(H3	0.9500

C4(C5	1.372(13)

C4(H4	0.9500

C5(C6	1.382(13)

C5(H5	0.9500

C6(H6	0.9500

C7(C8	1.353(14)

C7(C12	1.376(13)

C7(O2	1.401(11)

C8(C9	1.411(14)

C8(H8	0.9500

C9(C10	1.364(17)

C9(H9	0.9500

C10(C11	1.354(16)

C10(H10	0.9500

C11(C12	1.369(14)

C11(H11	0.9500

C12(H12	0.9500

C13(C14	1.363(13)

C13(C18	1.387(12)

C13(O3	1.400(9)

C14(C15	1.389(12)

C14(H14	0.9500

C15(C16	1.381(16)

C15(H15	0.9500

C16(C17	1.363(17)

C16(H16	0.9500

C17(C18	1.388(14)

C17(H17	0.9500

C18(H18	0.9500

O1(P1	1.602(6)

O2(P1	1.584(6)

O3(P1	1.597(6)

C21(C22	1.524(11)

C21(P21	1.821(8)

C21(H21A	0.9900

C21(H21B	0.9900

C22(P22	1.825(9)

C22(H22A	0.9900

C22(H22B	0.9900

C23(C24	1.515(12)

C23(P22	1.833(8)

C23(H23A	0.9900

C23(H23B	0.9900

C24(P23	1.830(9)

C24(H24A	0.9900

C24(H24B	0.9900

C25(C26	1.372(12)

C25(C30	1.413(11)

C25(P21	1.825(8)

C26(C27	1.369(12)

C26(H26	0.9500

C27(C28	1.378(12)

C27(H27	0.9500

C28(C29	1.340(13)

C28(H28	0.9500

C29(C30	1.370(12)

C29(H29	0.9500

C30(H30	0.9500

C31(C32	1.383(12)

C31(C36	1.396(12)

C31(P21	1.842(8)

C32(C33	1.389(12)

C32(H32	0.9500

C33(C34	1.348(13)

C33(H33	0.9500

C34(C35	1.379(13)

C34(H34	0.9500

C35(C36	1.379(13)

C35(H35	0.9500

C36(H36	0.9500

C37(C38	1.393(11)

C37(C42	1.412(12)

C37(P22	1.805(9)

C38(C39	1.387(13)

C38(H38	0.9500

C39(C40	1.382(14)

C39(H39	0.9500

C40(C41	1.386(13)

C40(H40	0.9500

C41(C42	1.363(14)

C41(H41	0.9500

C42(H42	0.9500

C43(C48	1.328(14)

C43(C44	1.383(13)

C43(P23	1.828(8)

C44(C45	1.380(11)

C44(H44	0.9500

C45(C46	1.339(14)

C45(H45	0.9500

C46(C47	1.383(17)

C46(H46	0.9500

C47(C48	1.373(14)

C47(H47	0.9500

C48(H48	0.9500

C49(C54	1.394(12)

C49(C50	1.401(12)

C49(P23	1.808(9)

C50(C51	1.379(13)

C50(H50	0.9500

C51(C52	1.348(13)

C51(H51	0.9500

C52(C53	1.392(13)

C52(H52	0.9500

C53(C54	1.388(12)

C53(H53	0.9500

C54(H54	0.9500

F1(Sb1	1.876(8)

F2(Sb1	1.809(8)

F3(Sb1	1.852(8)

F4(Sb1	1.842(8)

F5(Sb1	1.832(6)

F6(Sb1	1.850(8)

C61(Cl63	1.731(8)

C61(Cl61	1.731(8)

C61(Cl62	1.734(8)

C61(H61	1.0000

C66(Cl66	1.730(12)

C66(Cl68	1.733(9)

C66(Cl67	1.733(9)

C66(H66	1.0000

C71(Cl73	1.727(9)

C71(Cl72	1.730(8)

C71(Cl71	1.733(9)

C71(H71	1.0000

C76(Cl78	1.734(9)

C76(Cl76	1.734(12)

C76(Cl77	1.735(9)

C76(H76	1.0000

C2(Pd1(P1	79.5(3)

C2(Pd1(P22	178.4(2)

P1(Pd1(P22	101.95(8)

C2(Pd1(P23	95.9(2)

P1(Pd1(P23	126.48(8)

P22(Pd1(P23	83.73(8)

C2(Pd1(P21	93.8(2)

P1(Pd1(P21	120.55(8)

P22(Pd1(P21	84.90(7)

P23(Pd1(P21	112.94(8)

C2(C1(C6	123.9(9)

C2(C1(O1	119.9(8)

C6(C1(O1	116.1(8)

C1(C2(C3	116.7(8)

C1(C2(Pd1	118.4(6)

C3(C2(Pd1	124.5(6)

C4(C3(C2	120.9(9)

C4(C3(H3	119.6

C2(C3(H3	119.6

C5(C4(C3	119.8(9)

C5(C4(H4	120.1

C3(C4(H4	120.1

C4(C5(C6	120.3(9)

C4(C5(H5	119.8

C6(C5(H5	119.8

C1(C6(C5	118.3(9)

C1(C6(H6	120.9

C5(C6(H6	120.9

C8(C7(C12	121.2(10)

C8(C7(O2	123.3(9)

C12(C7(O2	115.4(9)

C7(C8(C9	119.1(11)

C7(C8(H8	120.4

C9(C8(H8	120.4

C10(C9(C8	119.3(11)

C10(C9(H9	120.3

C8(C9(H9	120.3

C11(C10(C9	120.3(10)

C11(C10(H10	119.9

C9(C10(H10	119.9

C10(C11(C12	121.2(11)

C10(C11(H11	119.4

C12(C11(H11	119.4

C11(C12(C7	118.9(11)

C11(C12(H12	120.5

C7(C12(H12	120.5

C14(C13(C18	122.1(8)

C14(C13(O3	118.4(8)

C18(C13(O3	119.4(8)

C13(C14(C15	119.2(10)

C13(C14(H14	120.4

C15(C14(H14	120.4

C16(C15(C14	119.2(11)

C16(C15(H15	120.4

C14(C15(H15	120.4

C17(C16(C15	121.1(9)

C17(C16(H16	119.4

C15(C16(H16	119.4

C16(C17(C18	120.3(11)

C16(C17(H17	119.8

C18(C17(H17	119.8

C13(C18(C17	118.0(10)

C13(C18(H18	121.0

C17(C18(H18	121.0

C1(O1(P1	115.9(5)

C7(O2(P1	129.2(6)

C13(O3(P1	119.3(5)

O2(P1(O3	97.6(3)

O2(P1(O1	105.0(3)

O3(P1(O1	101.6(3)

O2(P1(Pd1	118.0(3)

O3(P1(Pd1	126.5(2)

O1(P1(Pd1	105.5(2)

C22(C21(P21	111.3(6)

C22(C21(H21A	109.4

P21(C21(H21A	109.4

C22(C21(H21B	109.4

P21(C21(H21B	109.4

H21A(C21(H21B	108.0

C21(C22(P22	112.5(6)

C21(C22(H22A	109.1

P22(C22(H22A	109.1

C21(C22(H22B	109.1

P22(C22(H22B	109.1

H22A(C22(H22B	107.8

C24(C23(P22	109.0(6)

C24(C23(H23A	109.9

P22(C23(H23A	109.9

C24(C23(H23B	109.9

P22(C23(H23B	109.9

H23A(C23(H23B	108.3

C23(C24(P23	108.8(6)

C23(C24(H24A	109.9

P23(C24(H24A	109.9

C23(C24(H24B	109.9

P23(C24(H24B	109.9

H24A(C24(H24B	108.3

C26(C25(C30	118.4(8)

C26(C25(P21	120.8(6)

C30(C25(P21	120.7(7)

C27(C26(C25	120.6(8)

C27(C26(H26	119.7

C25(C26(H26	119.7

C26(C27(C28	120.3(9)

C26(C27(H27	119.9

C28(C27(H27	119.9

C29(C28(C27	120.0(9)

C29(C28(H28	120.0

C27(C28(H28	120.0

C28(C29(C30	121.3(9)

C28(C29(H29	119.4

C30(C29(H29	119.4

C29(C30(C25	119.4(9)

C29(C30(H30	120.3

C25(C30(H30	120.3

C32(C31(C36	119.5(8)

C32(C31(P21	122.6(6)

C36(C31(P21	117.8(7)

C31(C32(C33	120.7(8)

C31(C32(H32	119.7

C33(C32(H32	119.7

C34(C33(C32	120.3(9)

C34(C33(H33	119.8

C32(C33(H33	119.8

C33(C34(C35	119.0(9)

C33(C34(H34	120.5

C35(C34(H34	120.5

C34(C35(C36	122.7(9)

C34(C35(H35	118.6

C36(C35(H35	118.6

C35(C36(C31	117.8(9)

C35(C36(H36	121.1

C31(C36(H36	121.1

C38(C37(C42	118.5(8)

C38(C37(P22	119.2(7)

C42(C37(P22	122.3(7)

C39(C38(C37	119.7(9)

C39(C38(H38	120.2

C37(C38(H38	120.2

C40(C39(C38	121.3(9)

C40(C39(H39	119.3

C38(C39(H39	119.3

C39(C40(C41	118.9(9)

C39(C40(H40	120.6

C41(C40(H40	120.6

C42(C41(C40	120.9(10)

C42(C41(H41	119.5

C40(C41(H41	119.5

C41(C42(C37	120.6(9)

C41(C42(H42	119.7

C37(C42(H42	119.7

C48(C43(C44	118.3(8)

C48(C43(P23	120.7(7)

C44(C43(P23	120.9(7)

C45(C44(C43	119.9(9)

C45(C44(H44	120.1

C43(C44(H44	120.1

C46(C45(C44	120.3(9)

C46(C45(H45	119.8

C44(C45(H45	119.8

C45(C46(C47	120.6(9)

C45(C46(H46	119.7

C47(C46(H46	119.7

C48(C47(C46	117.5(12)

C48(C47(H47	121.2

C46(C47(H47	121.2

C43(C48(C47	123.4(11)

C43(C48(H48	118.3

C47(C48(H48	118.3

C54(C49(C50	119.6(8)

C54(C49(P23	121.2(7)

C50(C49(P23	118.5(7)

C51(C50(C49	118.3(9)

C51(C50(H50	120.8

C49(C50(H50	120.8

C52(C51(C50	122.9(9)

C52(C51(H51	118.5

C50(C51(H51	118.5

C51(C52(C53	119.2(9)

C51(C52(H52	120.4

C53(C52(H52	120.4

C54(C53(C52	120.0(8)

C54(C53(H53	120.0

C52(C53(H53	120.0

C53(C54(C49	119.9(9)

C53(C54(H54	120.0

C49(C54(H54	120.1

C21(P21(C25	104.3(4)

C21(P21(C31	104.2(4)

C25(P21(C31	102.0(4)

C21(P21(Pd1	104.9(3)

C25(P21(Pd1	121.8(3)

C31(P21(Pd1	117.6(2)

C37(P22(C22	106.5(4)

C37(P22(C23	105.1(4)

C22(P22(C23	103.2(4)

C37(P22(Pd1	122.8(3)

C22(P22(Pd1	108.4(3)

C23(P22(Pd1	109.0(3)

C49(P23(C43	104.2(4)

C49(P23(C24	107.7(4)

C43(P23(C24	101.4(4)

C49(P23(Pd1	120.0(3)

C43(P23(Pd1	117.0(3)

C24(P23(Pd1	104.7(3)

F2(Sb1(F5	177.8(5)

F2(Sb1(F4	91.7(6)

F5(Sb1(F4	90.2(4)

F2(Sb1(F6	90.2(6)

F5(Sb1(F6	90.9(4)

F4(Sb1(F6	90.0(4)

F2(Sb1(F3	90.6(6)

F5(Sb1(F3	88.3(5)

F4(Sb1(F3	90.0(4)

F6(Sb1(F3	179.1(4)

F2(Sb1(F1	90.4(6)

F5(Sb1(F1	87.8(3)

F4(Sb1(F1	177.9(3)

F6(Sb1(F1	90.6(4)

F3(Sb1(F1	89.4(4)

Cl63(C61(Cl61	109.3(6)

Cl63(C61(Cl62	111.9(6)

Cl61(C61(Cl62	108.9(6)

Cl63(C61(H61	108.9

Cl61(C61(H61	108.9

Cl62(C61(H61	108.9

Cl66(C66(Cl68	109.8(8)

Cl66(C66(Cl67	109.6(8)

Cl68(C66(Cl67	110.4(7)

Cl66(C66(H66	109.0

Cl68(C66(H66	109.0

Cl67(C66(H66	109.0

Cl73(C71(Cl72	110.9(6)

Cl73(C71(Cl71	110.2(7)

Cl72(C71(Cl71	111.2(7)

Cl73(C71(H71	108.2

Cl72(C71(H71	108.2

Cl71(C71(H71	108.2

Cl78(C76(Cl76	109.6(8)

Cl78(C76(Cl77	109.9(7)

Cl76(C76(Cl77	109.7(8)

Cl78(C76(H76	109.2

Cl76(C76(H76	109.2

Cl77(C76(H76	109.2

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

Pd1	21(1) 	33(1)	28(1) 	0(1)	8(1) 	(1(1)

C1	32(4) 	37(5)	36(6) 	1(4)	8(4) 	8(4)

C2	26(4) 	34(4)	31(5) 	(1(4)	6(4) 	5(3)

C3	28(4) 	33(4)	38(6) 	(2(4)	2(4) 	2(3)

C4	35(5) 	34(5)	54(7) 	5(4)	1(4) 	1(4)

C5	46(5) 	41(5)	43(6) 	(2(4)	9(5) 	10(4)

C6	47(5) 	44(5)	35(6) 	(9(4)	7(4) 	7(4)

C7	34(5) 	54(6)	34(6) 	8(4)	12(4) 	10(4)

C8	35(5) 	76(7)	44(7) 	(2(6)	15(5) 	4(5)

C9	47(6) 	113(10)	40(7) 	(4(6)	27(5) 	22(6)

C10	38(5) 	97(9)	54(8) 	40(7)	35(5) 	24(6)

C11	47(6) 	59(7)	77(9) 	16(6)	32(6) 	7(5)

C12	36(5) 	49(5)	60(7) 	18(5)	26(5) 	5(4)

C13	32(4) 	46(5)	28(5) 	7(4)	4(4) 	(4(4)

C14	32(4) 	61(6)	37(6) 	11(5)	11(4) 	0(4)

C15	30(5) 	82(8)	63(8) 	34(6)	12(5) 	10(5)

C16	33(5) 	95(9)	48(7) 	27(6)	(9(5) 	(26(6)

C17	57(7) 	69(7)	50(7) 	25(6)	(18(6) 	(26(6)

C18	52(5) 	41(5)	20(5) 	4(4)	1(4) 	(11(4)

O1	44(3) 	36(3)	29(4) 	1(3)	11(3) 	2(3)

O2	26(3) 	52(4)	33(4) 	7(3)	9(3) 	(5(3)

O3	26(3) 	43(3)	30(3) 	7(3)	6(2) 	(3(2)

P1	26(1) 	37(1)	30(1) 	1(1)	11(1) 	0(1)

C21	25(4) 	35(4)	36(5) 	7(4)	9(4) 	(2(3)

C22	35(4) 	37(5)	37(6) 	3(4)	9(4) 	(4(4)

C23	25(4) 	48(5)	28(5) 	(1(4)	6(3) 	(5(3)

C24	27(4) 	52(5)	28(5) 	0(4)	7(4) 	3(4)

C25	23(4) 	44(5)	26(5) 	3(4)	2(3) 	(4(3)

C26	30(4) 	38(5)	43(6) 	5(4)	5(4) 	(1(4)

C27	40(5) 	37(5)	39(6) 	1(4)	1(4) 	(8(4)

C28	39(5) 	45(5)	48(7) 	5(5)	(2(4) 	(14(4)

C29	23(4) 	65(6)	33(6) 	8(5)	(1(4) 	(8(4)

C30	25(4) 	54(5)	48(6) 	(9(5)	17(4) 	(2(4)

C31	16(3) 	42(5)	30(5) 	6(4)	13(3) 	0(3)

C32	24(4) 	46(5)	34(5) 	2(4)	12(4) 	2(4)

C33	33(4) 	56(6)	34(6) 	(2(4)	16(4) 	0(4)

C34	35(5) 	55(6)	40(6) 	9(5)	12(4) 	(3(4)

C35	40(5) 	37(5)	51(7) 	9(4)	6(5) 	(11(4)

C36	31(4) 	51(5)	36(6) 	6(4)	13(4) 	(10(4)

C37	30(4) 	34(4)	32(5) 	(9(4)	7(4) 	(5(3)

C38	32(4) 	56(6)	42(6) 	8(5)	18(4) 	(4(4)

C39	36(5) 	70(7)	49(7) 	2(5)	15(5) 	(21(5)

C40	54(6) 	41(5)	45(6) 	9(5)	12(5) 	(12(5)

C41	49(6) 	46(6)	64(8) 	(7(5)	15(5) 	(1(5)

C42	30(4) 	46(5)	48(6) 	(9(5)	5(4) 	(2(4)

C43	21(4) 	45(5)	42(6) 	(1(4)	5(4) 	(2(3)

C44	26(4) 	40(5)	55(7) 	7(4)	8(4) 	(2(3)

C45	32(4) 	39(5)	46(6) 	1(4)	(1(4) 	(7(4)

C46	23(4) 	108(9)	52(7) 	7(7)	9(5) 	10(5)

C47	30(6) 	240(20)	61(9) 	40(11)	22(6) 	(2(8)

C48	23(5) 	155(13)	40(7) 	18(7)	(2(5) 	3(6)

C49	24(4) 	48(5)	31(5) 	5(4)	(2(4) 	2(4)

C50	28(4) 	48(5)	51(6) 	9(5)	9(4) 	(7(4)

C51	32(5) 	50(6)	69(8) 	16(5)	7(5) 	5(4)

C52	37(5) 	52(6)	75(8) 	37(6)	15(5) 	3(4)

C53	39(5) 	59(6)	44(6) 	8(5)	17(4) 	(11(4)

C54	34(4) 	48(5)	31(5) 	3(4)	4(4) 	1(4)

P21	22(1) 	37(1)	29(1) 	(1(1)	8(1) 	(2(1)

P22	23(1) 	36(1)	32(1) 	(4(1)	10(1) 	(3(1)

P23	22(1) 	41(1)	30(1) 	0(1)	7(1) 	(1(1)

F1	82(5) 	96(5)	103(6) 	3(5)	57(5) 	(13(4)

F2	38(5) 	289(17)	268(17) 	(37(12)	(34(7) 	22(7)

F3	170(10) 	143(8)	71(6) 	(42(6)	5(6) 	19(7)

F4	133(7) 	100(6)	65(5) 	27(4)	32(5) 	57(5)

F5	41(4) 	100(6)	166(9) 	42(6)	10(4) 	11(4)

F6	148(8) 	95(6)	61(5) 	(11(4)	31(5) 	16(5)

Sb1	30(1) 	87(1)	40(1) 	(4(1)	10(1) 	10(1)

C61	126(9) 	99(9)	70(8) 	(23(8)	2(8) 	15(9)

Cl61	95(7) 	63(6)	64(5) 	(7(4)	(23(5) 	(36(6)

Cl62	172(10) 	94(6)	56(5) 	(14(5)	(9(6) 	8(8)

Cl63	118(6) 	101(6)	73(7) 	(7(6)	(1(6) 	(12(5)

C66	133(9) 	97(9)	62(8) 	(21(8)	7(8) 	15(9)

Cl66	79(10) 	73(10)	75(10) 	(1(8)	(17(8) 	(68(8)

Cl67	139(14) 	74(10)	89(10) 	(6(9)	58(11) 	32(11)

Cl68	133(8) 	129(9)	98(9) 	(18(8)	16(8) 	14(9)

C71	116(10) 	93(8)	73(8) 	(26(8)	8(8) 	21(9)

Cl71	178(10) 	63(5)	53(6) 	(11(4)	(14(6) 	6(6)

Cl72	171(10) 	67(5)	46(5) 	(14(4)	(11(6) 	(2(6)

Cl73	183(12) 	87(6)	68(6) 	4(5)	(11(7) 	18(7)

C76	125(9) 	100(8)	70(8) 	(21(7)	4(8) 	15(9)

Cl76	162(12) 	95(10)	71(10) 	(16(9)	6(10) 	18(10)

Cl77	143(15) 	77(13)	47(10) 	(29(10)	(21(12) 	(27(13)

Cl78	121(13) 	91(11)	66(11) 	(11(10)	3(12) 	7(11)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H3	7405	4619	151	40	1

H4	7678	5410	772	49	1

H5	7422	5515	2149	52	1

H6	6845	4832	2903	50	1

H8	5184	3775	3388	61	1

H9	4086	3648	4461	78	1

H10	2947	2959	4402	73	1

H11	2816	2430	3281	71	1

H12	3905	2539	2237	56	1

H14	8392	2437	2379	51	1

H15	10208	2476	2845	70	1

H16	10810	3099	3791	71	1

H17	9682	3719	4177	72	1

H18	7869	3692	3703	46	1

H21A	9873	2782	256	38	1

H21B	9293	2656	1058	38	1

H22A	8457	2165	19	43	1

H22B	8355	2632	(610	43	1

H23A	6395	2352	(1045	40	1

H23B	5417	2575	(607	40	1

H24A	5732	3131	(1674	42	1

H24B	6965	3171	(1339	42	1

H26	8965	4281	1811	44	1

H27	10246	4597	2788	47	1

H28	11905	4214	2994	53	1

H29	12257	3507	2265	49	1

H30	11034	3199	1236	50	1

H32	9367	3150	(1027	41	1

H33	9850	3560	(2198	48	1

H34	10056	4427	(2204	52	1

H35	9833	4887	(1026	51	1

H36	9368	4499	165	47	1

H38	5069	2335	832	51	1

H39	4552	1632	1556	61	1

H40	5767	1000	1994	55	1

H41	7548	1101	1772	63	1

H42	8091	1796	1074	49	1

H44	4116	3709	(1715	48	1

H45	2307	3564	(1701	48	1

H46	1622	3389	(493	72	1

H47	2755	3284	724	131	1

H48	4544	3454	694	88	1

H50	4835	4601	(612	50	1

H51	5158	5382	(1190	60	1

H52	6568	5515	(1927	65	1

H53	7720	4842	(2140	56	1

H54	7453	4048	(1556	45	1

H61	1377	4606	4726	119	0.367(3)

H66	1236	4661	4693	117	0.185(5)

H71	2716	4814	4987	113	0.381(6)

H76	1826	4677	4729	118	0.068(6)