|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	03src0783

Empirical formula 	C22H20F5NO4Pt

Formula weight 	652.48

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/n

Unit cell dimensions	a = 14.5057(3) Å	( = 90°

b = 11.5897(3) Å	( = 102.3040(10)°

c = 26.1769(6) Å	(  = 90°

Volume	4299.69(17) Å3

Z	8

Density (calculated)	2.016 Mg / m3

Absorption coefficient	6.600 mm(1

F(000)	2512

Crystal	Cone; Red

Crystal size	0.50 ( 0.40 ( 0.10 mm3

( range for data collection	2.94 ( 27.48°

Index ranges	(18 ( h ( 18, (15 ( k ( 14, (33 ( l ( 33

Reflections collected	49351

Independent reflections	9804 [Rint = 0.0798]

Completeness to ( = 27.48°	99.5 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.5582 and 0.1370

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	9804 / 0 / 601

Goodness-of-fit on F2	1.053

Final R indices [F2 > 2((F2)]	R1 = 0.0355, wR2 = 0.0762

R indices (all data)	R1 = 0.0502, wR2 = 0.0819

Largest diff. peak and hole	2.231 and (1.678 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

All hydrogen atoms were fixed.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

Pt1	6134(1)	1819(1)	2266(1)	14(1)	1

Pt2	1145(1)	66(1)	2144(1)	14(1)	1

C1	5927(4)	1551(5)	2975(2)	16(1)	1

C2	5826(3)	377(5)	3091(2)	19(1)	1

C3	5670(4)	39(5)	3579(2)	23(1)	1

C4	5629(4)	851(5)	3949(2)	24(1)	1

C5	5755(4)	2024(5)	3841(2)	23(1)	1

C6	5890(4)	2371(5)	3352(2)	17(1)	1

C7	5874(3)	(378(5)	2665(2)	18(1)	1

C8	6028(3)	(593(5)	1783(2)	18(1)	1

C9	5512(4)	(249(5)	1296(2)	21(1)	1

C10	5531(4)	(906(5)	862(2)	23(1)	1

C11	6078(4)	(1902(5)	901(2)	23(1)	1

C12	6607(4)	(2235(5)	1386(2)	20(1)	1

C13	6578(3)	(1572(5)	1826(2)	18(1)	1

C14	5961(5)	3933(6)	4175(2)	33(2)	1

C15	6510(5)	(3581(6)	490(2)	37(2)	1

N1	5980(3)	103(4)	2232(2)	18(1)	1

O1	5726(3)	2760(4)	4241(2)	29(1)	1

O2	6043(3)	(2492(4)	449(2)	30(1)	1

C21	6243(4)	2665(5)	402(2)	26(1)	1

C22	7057(4)	2835(5)	865(2)	24(1)	1

C23	6742(4)	2952(5)	1386(2)	21(1)	1

C24	6792(4)	4022(5)	1623(2)	22(1)	1

C25	6518(3)	4265(5)	2098(2)	17(1)	1

C26	6523(4)	5479(5)	2282(2)	23(1)	1

C27	6443(4)	5653(5)	2840(2)	22(1)	1

O21	6457(3)	2006(3)	1531(1)	21(1)	1

O22	6250(2)	3510(3)	2393(1)	18(1)	1

F21	5778(3)	1705(3)	439(1)	44(1)	1

F22	5668(3)	3551(3)	355(1)	37(1)	1

F23	6576(3)	2605(4)	(40(1)	44(1)	1

F24	7654(3)	1940(4)	885(1)	42(1)	1

F25	7526(3)	3794(4)	760(1)	39(1)	1

C31	982(4)	351(5)	2857(2)	16(1)	1

C32	897(4)	1526(5)	2975(2)	19(1)	1

C33	790(4)	1877(5)	3472(2)	22(1)	1

C34	771(4)	1057(5)	3847(2)	25(1)	1

C35	877(4)	(105(5)	3735(2)	20(1)	1

C36	967(4)	(470(5)	3243(2)	18(1)	1

C37	907(3)	2261(5)	2543(2)	18(1)	1

C38	1005(4)	2452(5)	1649(2)	20(1)	1

C39	437(4)	2125(5)	1170(2)	21(1)	1

C40	451(4)	2764(5)	726(2)	23(1)	1

C41	1024(4)	3723(5)	753(2)	21(1)	1

C42	1594(4)	4050(5)	1225(2)	20(1)	1

C43	1585(4)	3406(5)	1675(2)	19(1)	1

C44	1015(5)	(2045(5)	4052(2)	28(1)	1

C45	1491(5)	5339(6)	311(2)	37(2)	1

N31	979(3)	1779(4)	2103(2)	16(1)	1

O31	894(3)	(850(4)	4144(2)	28(1)	1

O32	979(3)	4301(4)	294(1)	30(1)	1

C51	2497(4)	(144(6)	604(2)	30(1)	1

C52	1726(4)	(992(5)	666(2)	27(1)	1

C53	1571(4)	(1093(5)	1223(2)	19(1)	1

C54	1665(4)	(2153(5)	1467(2)	21(1)	1

C55	1520(4)	(2372(5)	1974(2)	17(1)	1

C56	1574(3)	(3602(5)	2159(2)	16(1)	1

C57	1503(4)	(3773(5)	2728(2)	24(1)	1

O51	1351(3)	(126(3)	1388(1)	21(1)	1

O52	1326(2)	(1623(3)	2283(1)	17(1)	1

F51	2254(3)	916(3)	669(2)	51(1)	1

F52	3272(3)	(375(5)	951(2)	76(2)	1

F53	2686(3)	(218(3)	130(2)	44(1)	1

F54	921(3)	(628(4)	342(1)	43(1)	1

F55	1943(4)	(2012(3)	476(2)	57(1)	1

Table 3. Bond lengths [Å] and angles [°].

Pt1(C1	1.969(5)

Pt1(O22	1.988(4)

Pt1(N1	2.001(5)

Pt1(O21	2.084(3)

Pt2(C31	1.959(5)

Pt2(O52	1.998(4)

Pt2(N31	2.001(4)

Pt2(O51	2.077(4)

C1(C6	1.379(7)

C1(C2	1.408(8)

C2(C3	1.401(7)

C2(C7	1.431(8)

C3(C4	1.360(8)

C3(H3	0.9500

C4(C5	1.408(8)

C4(H4	0.9500

C5(O1	1.360(7)

C5(C6	1.394(7)

C6(H6	0.9500

C7(N1	1.303(7)

C7(H7	0.9500

C8(C13	1.377(8)

C8(C9	1.393(7)

C8(N1	1.438(7)

C9(C10	1.372(8)

C9(H9	0.9500

C10(C11	1.392(8)

C10(H10	0.9500

C11(O2	1.359(7)

C11(C12	1.389(8)

C12(C13	1.394(7)

C12(H12	0.9500

C13(H13	0.9500

C14(O1	1.421(8)

C14(H14A	0.9800

C14(H14B	0.9800

C14(H14C	0.9800

C15(O2	1.426(7)

C15(H15A	0.9800

C15(H15B	0.9800

C15(H15C	0.9800

C21(F22	1.312(7)

C21(F21	1.316(7)

C21(F23	1.347(6)

C21(C22	1.514(8)

C22(F24	1.346(7)

C22(F25	1.361(7)

C22(C23	1.534(7)

C23(O21	1.259(7)

C23(C24	1.381(8)

C24(C25	1.413(7)

C24(H24	0.9500

C25(O22	1.282(6)

C25(C26	1.487(8)

C26(C27	1.502(8)

C26(H26A	0.9900

C26(H26B	0.9900

C27(H27A	0.9800

C27(H27B	0.9800

C27(H27C	0.9800

C31(C36	1.390(7)

C31(C32	1.407(8)

C32(C33	1.405(7)

C32(C37	1.418(8)

C33(C34	1.371(8)

C33(H33	0.9500

C34(C35	1.394(8)

C34(H34	0.9500

C35(O31	1.371(7)

C35(C36	1.389(7)

C36(H36	0.9500

C37(N31	1.303(7)

C37(H37	0.9500

C38(C43	1.381(8)

C38(C39	1.397(7)

C38(N31	1.430(7)

C39(C40	1.382(8)

C39(H39	0.9500

C40(C41	1.380(8)

C40(H40	0.9500

C41(O32	1.366(6)

C41(C42	1.384(7)

C42(C43	1.398(7)

C42(H42	0.9500

C43(H43	0.9500

C44(O31	1.423(7)

C44(H44A	0.9800

C44(H44B	0.9800

C44(H44C	0.9800

C45(O32	1.410(7)

C45(H45A	0.9800

C45(H45B	0.9800

C45(H45C	0.9800

C51(F51	1.299(7)

C51(F52	1.313(7)

C51(F53	1.330(7)

C51(C52	1.523(9)

C52(F55	1.345(7)

C52(F54	1.355(7)

C52(C53	1.526(7)

C53(O51	1.266(6)

C53(C54	1.379(8)

C54(C55	1.409(7)

C54(H54	0.9500

C55(O52	1.258(6)

C55(C56	1.503(7)

C56(C57	1.526(7)

C56(H56A	0.9900

C56(H56B	0.9900

C57(H57A	0.9800

C57(H57B	0.9800

C57(H57C	0.9800

C1(Pt1(O22	91.26(18)

C1(Pt1(N1	81.2(2)

O22(Pt1(N1	172.44(16)

C1(Pt1(O21	174.90(18)

O22(Pt1(O21	91.40(14)

N1(Pt1(O21	96.16(16)

C31(Pt2(O52	91.75(19)

C31(Pt2(N31	81.1(2)

O52(Pt2(N31	172.73(15)

C31(Pt2(O51	176.21(19)

O52(Pt2(O51	91.62(14)

N31(Pt2(O51	95.47(16)

C6(C1(C2	119.4(5)

C6(C1(Pt1	127.1(4)

C2(C1(Pt1	113.5(4)

C3(C2(C1	120.7(5)

C3(C2(C7	125.7(5)

C1(C2(C7	113.5(5)

C4(C3(C2	119.7(5)

C4(C3(H3	120.2

C2(C3(H3	120.2

C3(C4(C5	119.9(5)

C3(C4(H4	120.0

C5(C4(H4	120.0

O1(C5(C6	124.0(5)

O1(C5(C4	115.1(5)

C6(C5(C4	120.8(5)

C1(C6(C5	119.4(5)

C1(C6(H6	120.3

C5(C6(H6	120.3

N1(C7(C2	116.8(5)

N1(C7(H7	121.6

C2(C7(H7	121.6

C13(C8(C9	119.9(5)

C13(C8(N1	121.5(5)

C9(C8(N1	118.5(5)

C10(C9(C8	119.9(5)

C10(C9(H9	120.1

C8(C9(H9	120.1

C9(C10(C11	120.7(5)

C9(C10(H10	119.7

C11(C10(H10	119.7

O2(C11(C12	124.5(5)

O2(C11(C10	115.9(5)

C12(C11(C10	119.5(5)

C11(C12(C13	119.6(5)

C11(C12(H12	120.2

C13(C12(H12	120.2

C8(C13(C12	120.4(5)

C8(C13(H13	119.8

C12(C13(H13	119.8

O1(C14(H14A	109.5

O1(C14(H14B	109.5

H14A(C14(H14B	109.5

O1(C14(H14C	109.5

H14A(C14(H14C	109.5

H14B(C14(H14C	109.5

O2(C15(H15A	109.5

O2(C15(H15B	109.5

H15A(C15(H15B	109.5

O2(C15(H15C	109.5

H15A(C15(H15C	109.5

H15B(C15(H15C	109.5

C7(N1(C8	120.4(5)

C7(N1(Pt1	114.8(4)

C8(N1(Pt1	124.7(3)

C5(O1(C14	117.3(5)

C11(O2(C15	116.8(5)

F22(C21(F21	110.0(5)

F22(C21(F23	107.3(5)

F21(C21(F23	107.7(5)

F22(C21(C22	110.2(5)

F21(C21(C22	112.0(5)

F23(C21(C22	109.5(5)

F24(C22(F25	107.0(5)

F24(C22(C21	108.4(5)

F25(C22(C21	106.4(5)

F24(C22(C23	110.2(5)

F25(C22(C23	111.4(5)

C21(C22(C23	113.2(5)

O21(C23(C24	129.5(5)

O21(C23(C22	111.8(5)

C24(C23(C22	118.7(5)

C23(C24(C25	125.2(5)

C23(C24(H24	117.4

C25(C24(H24	117.4

O22(C25(C24	124.9(5)

O22(C25(C26	115.6(5)

C24(C25(C26	119.5(5)

C25(C26(C27	116.6(5)

C25(C26(H26A	108.1

C27(C26(H26A	108.1

C25(C26(H26B	108.1

C27(C26(H26B	108.1

H26A(C26(H26B	107.3

C26(C27(H27A	109.5

C26(C27(H27B	109.5

H27A(C27(H27B	109.5

C26(C27(H27C	109.5

H27A(C27(H27C	109.5

H27B(C27(H27C	109.5

C23(O21(Pt1	121.5(3)

C25(O22(Pt1	126.7(3)

C36(C31(C32	119.2(5)

C36(C31(Pt2	126.8(4)

C32(C31(Pt2	113.9(4)

C33(C32(C31	121.0(5)

C33(C32(C37	125.9(5)

C31(C32(C37	113.0(5)

C34(C33(C32	119.0(5)

C34(C33(H33	120.5

C32(C33(H33	120.5

C33(C34(C35	120.0(5)

C33(C34(H34	120.0

C35(C34(H34	120.0

O31(C35(C36	122.9(5)

O31(C35(C34	115.4(5)

C36(C35(C34	121.7(5)

C35(C36(C31	119.0(5)

C35(C36(H36	120.5

C31(C36(H36	120.5

N31(C37(C32	117.6(5)

N31(C37(H37	121.2

C32(C37(H37	121.2

C43(C38(C39	119.9(5)

C43(C38(N31	121.2(5)

C39(C38(N31	118.8(5)

C40(C39(C38	119.7(5)

C40(C39(H39	120.1

C38(C39(H39	120.1

C41(C40(C39	120.4(5)

C41(C40(H40	119.8

C39(C40(H40	119.8

O32(C41(C40	115.8(5)

O32(C41(C42	123.9(5)

C40(C41(C42	120.3(5)

C41(C42(C43	119.7(5)

C41(C42(H42	120.2

C43(C42(H42	120.2

C38(C43(C42	120.0(5)

C38(C43(H43	120.0

C42(C43(H43	120.0

O31(C44(H44A	109.5

O31(C44(H44B	109.5

H44A(C44(H44B	109.5

O31(C44(H44C	109.5

H44A(C44(H44C	109.5

H44B(C44(H44C	109.5

O32(C45(H45A	109.5

O32(C45(H45B	109.5

H45A(C45(H45B	109.5

O32(C45(H45C	109.5

H45A(C45(H45C	109.5

H45B(C45(H45C	109.5

C37(N31(C38	121.5(5)

C37(N31(Pt2	114.2(4)

C38(N31(Pt2	124.2(3)

C35(O31(C44	117.6(4)

C41(O32(C45	117.7(4)

F51(C51(F52	108.6(6)

F51(C51(F53	107.4(5)

F52(C51(F53	108.3(5)

F51(C51(C52	111.8(5)

F52(C51(C52	109.6(5)

F53(C51(C52	111.0(5)

F55(C52(F54	106.3(5)

F55(C52(C51	107.1(5)

F54(C52(C51	106.7(5)

F55(C52(C53	112.2(5)

F54(C52(C53	109.9(5)

C51(C52(C53	114.3(5)

O51(C53(C54	129.6(5)

O51(C53(C52	110.9(5)

C54(C53(C52	119.5(5)

C53(C54(C55	125.3(5)

C53(C54(H54	117.4

C55(C54(H54	117.4

O52(C55(C54	125.4(5)

O52(C55(C56	116.8(4)

C54(C55(C56	117.8(5)

C55(C56(C57	115.3(4)

C55(C56(H56A	108.4

C57(C56(H56A	108.4

C55(C56(H56B	108.4

C57(C56(H56B	108.4

H56A(C56(H56B	107.5

C56(C57(H57A	109.5

C56(C57(H57B	109.5

H57A(C57(H57B	109.5

C56(C57(H57C	109.5

H57A(C57(H57C	109.5

H57B(C57(H57C	109.5

C53(O51(Pt2	121.2(3)

C55(O52(Pt2	126.7(3)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

Pt1	14(1) 	12(1)	17(1) 	1(1)	3(1) 	(1(1)

Pt2	15(1) 	11(1)	17(1) 	(1(1)	4(1) 	1(1)

C1	17(3) 	15(3)	16(2) 	2(2)	1(2) 	1(2)

C2	10(2) 	20(3)	24(3) 	2(2)	0(2) 	1(2)

C3	19(3) 	25(3)	24(3) 	8(2)	2(2) 	(1(2)

C4	23(3) 	29(3)	19(3) 	6(2)	4(2) 	1(2)

C5	18(3) 	28(3)	21(3) 	(2(2)	0(2) 	2(2)

C6	16(3) 	15(3)	19(3) 	1(2)	2(2) 	2(2)

C7	13(2) 	15(3)	25(3) 	3(2)	0(2) 	(5(2)

C8	12(2) 	13(3)	27(3) 	0(2)	2(2) 	(8(2)

C9	23(3) 	12(3)	26(3) 	1(2)	0(2) 	(1(2)

C10	33(3) 	15(3)	18(3) 	3(2)	(1(2) 	(2(2)

C11	29(3) 	21(3)	21(3) 	(2(2)	7(2) 	(3(2)

C12	18(3) 	14(3)	28(3) 	(1(2)	4(2) 	2(2)

C13	13(2) 	17(3)	22(3) 	0(2)	(1(2) 	(5(2)

C14	32(3) 	37(4)	30(3) 	(7(3)	6(3) 	(3(3)

C15	57(4) 	24(3)	28(3) 	(8(3)	5(3) 	9(3)

N1	15(2) 	17(2)	21(2) 	1(2)	0(2) 	1(2)

O1	35(2) 	34(3)	19(2) 	(5(2)	7(2) 	1(2)

O2	43(3) 	24(2)	21(2) 	(4(2)	3(2) 	7(2)

C21	36(3) 	25(3)	17(3) 	(1(2)	5(2) 	1(3)

C22	25(3) 	24(3)	28(3) 	3(2)	13(2) 	1(2)

C23	18(3) 	23(3)	21(3) 	3(2)	5(2) 	(2(2)

C24	24(3) 	18(3)	23(3) 	3(2)	5(2) 	(4(2)

C25	4(2) 	19(3)	26(3) 	3(2)	(3(2) 	(1(2)

C26	18(3) 	15(3)	35(3) 	0(2)	1(2) 	(5(2)

C27	16(3) 	9(3)	41(3) 	(1(2)	7(2) 	0(2)

O21	28(2) 	17(2)	17(2) 	1(2)	6(2) 	(3(2)

O22	20(2) 	12(2)	21(2) 	3(2)	5(2) 	(2(2)

F21	62(3) 	36(2)	30(2) 	(2(2)	1(2) 	(19(2)

F22	36(2) 	37(2)	38(2) 	0(2)	6(2) 	12(2)

F23	58(3) 	51(3)	26(2) 	5(2)	19(2) 	15(2)

F24	40(2) 	56(3)	33(2) 	9(2)	18(2) 	24(2)

F25	42(2) 	47(2)	34(2) 	2(2)	19(2) 	(18(2)

C31	15(2) 	17(3)	16(2) 	(3(2)	4(2) 	(2(2)

C32	14(3) 	19(3)	24(3) 	(5(2)	4(2) 	(1(2)

C33	19(3) 	21(3)	28(3) 	(11(2)	8(2) 	(1(2)

C34	24(3) 	29(3)	21(3) 	(3(2)	5(2) 	4(3)

C35	16(3) 	21(3)	22(3) 	1(2)	5(2) 	2(2)

C36	19(3) 	16(3)	19(3) 	(4(2)	6(2) 	0(2)

C37	13(2) 	18(3)	22(3) 	(4(2)	3(2) 	0(2)

C38	23(3) 	15(3)	20(3) 	2(2)	3(2) 	10(2)

C39	20(3) 	11(3)	28(3) 	(4(2)	(1(2) 	(2(2)

C40	30(3) 	15(3)	21(3) 	(4(2)	(2(2) 	1(2)

C41	25(3) 	17(3)	20(3) 	0(2)	4(2) 	2(2)

C42	22(3) 	14(3)	24(3) 	(1(2)	7(2) 	1(2)

C43	17(3) 	20(3)	20(3) 	0(2)	5(2) 	4(2)

C44	42(4) 	20(3)	25(3) 	7(2)	13(3) 	0(3)

C45	54(4) 	31(4)	25(3) 	5(3)	6(3) 	(19(3)

N31	13(2) 	12(2)	22(2) 	(2(2)	2(2) 	(2(2)

O31	38(2) 	28(2)	20(2) 	3(2)	9(2) 	2(2)

O32	48(3) 	21(2)	18(2) 	3(2)	2(2) 	(5(2)

C51	32(3) 	28(4)	33(3) 	4(3)	13(3) 	2(3)

C52	38(3) 	16(3)	30(3) 	(1(2)	14(3) 	1(3)

C53	18(3) 	19(3)	22(3) 	(4(2)	7(2) 	(2(2)

C54	21(3) 	17(3)	26(3) 	(4(2)	7(2) 	3(2)

C55	14(2) 	11(3)	25(3) 	(3(2)	4(2) 	(4(2)

C56	9(2) 	14(3)	25(3) 	(3(2)	5(2) 	(1(2)

C57	20(3) 	29(3)	22(3) 	5(2)	1(2) 	0(3)

O51	30(2) 	14(2)	19(2) 	(1(2)	7(2) 	2(2)

O52	17(2) 	11(2)	22(2) 	(2(1)	4(1) 	4(1)

F51	78(3) 	23(2)	64(3) 	(6(2)	43(2) 	(16(2)

F52	24(2) 	128(5)	73(3) 	50(3)	6(2) 	(8(3)

F53	63(3) 	33(2)	49(2) 	7(2)	40(2) 	1(2)

F54	37(2) 	72(3)	18(2) 	3(2)	4(2) 	(15(2)

F55	116(4) 	23(2)	50(2) 	(6(2)	59(3) 	(3(2)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H3	5592	(754	3652	28	1

H4	5516	628	4279	28	1

H6	5956	3166	3279	20	1

H7	5830	(1192	2697	22	1

H9	5148	439	1263	25	1

H10	5167	(679	531	28	1

H12	6985	(2910	1416	24	1

H13	6939	(1796	2158	21	1

H14A	6610	3981	4124	49	1

H14B	5908	4374	4487	49	1

H14C	5528	4253	3869	49	1

H15A	7184	(3472	636	55	1

H15B	6426	(3931	142	55	1

H15C	6240	(4089	719	55	1

H24	7031	4643	1452	26	1

H26A	5993	5891	2054	28	1

H26B	7114	5847	2235	28	1

H27A	5841	5338	2889	33	1

H27B	6471	6480	2921	33	1

H27C	6965	5256	3073	33	1

H33	732	2672	3548	26	1

H34	687	1280	4183	30	1

H36	1017	(1268	3170	21	1

H37	863	3075	2573	21	1

H39	42	1465	1150	25	1

H40	65	2543	401	28	1

H42	1990	4708	1242	24	1

H43	1977	3624	2000	23	1

H44A	506	(2309	3766	42	1

H44B	995	(2484	4369	42	1

H44C	1625	(2167	3956	42	1

H45A	1293	5874	557	55	1

H45B	1370	5687	(39	55	1

H45C	2167	5178	426	55	1

H54	1842	(2788	1279	25	1

H56A	2178	(3935	2112	19	1

H56B	1059	(4043	1934	19	1

H57A	2019	(3357	2957	36	1

H57B	1549	(4597	2813	36	1

H57C	897	(3473	2778	36	1