|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	04src0173

Empirical formula 	C9H6Cl3Cu3NSe

Formula weight 	504.08

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/c

Unit cell dimensions	a = 3.7872(3) Å	( = 90°

b = 14.5657(11) Å	( = 91.700(3)°

c = 22.444(2) Å	(  = 90°

Volume	1237.51(18) Å3

Z	4

Density (calculated)	2.706 Mg / m3

Absorption coefficient	8.666 mm(1

F(000)	956

Crystal	Needle; Light Brown

Crystal size	0.22 ( 0.05 ( 0.02 mm3

( range for data collection	2.94 ( 27.42°

Index ranges	(4 ( h ( 4, (18 ( k ( 18, (29 ( l ( 29

Reflections collected	11352

Independent reflections	2739 [Rint = 0.0929]

Completeness to ( = 27.42°	97.7 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.8458 and 0.2515

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	2739 / 0 / 154

Goodness-of-fit on F2	1.154

Final R indices [F2 > 2((F2)]	R1 = 0.0877, wR2 = 0.1610

R indices (all data)	R1 = 0.1417, wR2 = 0.1764

Largest diff. peak and hole	1.939 and (0.880 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

All hydrogen atoms were fixed.

The structure contains infinite tapes of copper and chloride ions bounded by aromatic rings.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	2030(30)	812(9)	2863(5)	28(3)	1

C2	3350(30)	744(10)	2304(5)	31(3)	1

C3	4260(30)	(114(10)	2084(6)	34(3)	1

C4	3960(30)	(890(9)	2401(5)	30(3)	1

C5	2400(30)	(860(10)	2974(6)	34(3)	1

C6	1470(30)	15(10)	3217(5)	32(3)	1

C7	(310(30)	(682(8)	4085(5)	24(3)	1

C8	430(40)	(1560(9)	3870(6)	36(3)	1

C9	1860(30)	(1640(10)	3320(7)	36(3)	1

N1	160(30)	75(7)	3775(4)	27(2)	1

Cl1	(5058(8)	1687(2)	4712(1)	30(1)	1

Cl2	(4857(9)	3747(2)	5733(2)	37(1)	1

Cl3	(10007(9)	6125(2)	5762(2)	41(1)	1

Cu1	(385(5)	1248(1)	4206(1)	38(1)	1

Cu2	(4890(5)	3272(1)	4720(1)	51(1)	1

Cu3	(9840(5)	4610(1)	5613(1)	46(1)	1

Se1	692(4)	1975(1)	3163(1)	29(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(C2	1.367(16)

C1(C6	1.427(18)

C1(Se1	1.897(13)

C2(C3	1.392(19)

C2(H2	0.9500

C3(C4	1.342(18)

C3(H3	0.9500

C4(C5	1.431(18)

C4(H4	0.9500

C5(C9	1.394(19)

C5(C6	1.435(19)

C6(N1	1.365(15)

C7(N1	1.318(15)

C7(C8	1.397(18)

C7(H7	0.9500

C8(C9	1.369(19)

C8(H8	0.9500

C9(H9	0.9500

N1(Cu1	1.977(10)

Cl1(Cu1	2.225(3)

Cl1(Cu2	2.310(4)

Cl1(Cu1i	2.373(3)

Cl2(Cu3	2.276(4)

Cl2(Cu3ii	2.300(4)

Cl2(Cu2	2.376(4)

Cl3(Cu3	2.234(4)

Cl3(Cu2iii	2.345(4)

Cl3(Cu2iv	2.356(4)

Cu1(Cl1ii	2.373(3)

Cu1(Se1	2.613(2)

Cu2(Cl3iii	2.345(4)

Cu2(Cl3iv	2.356(4)

Cu3(Cl2i	2.300(4)

Cu3(Cu3iv	2.977(4)

C2(C1(C6	121.1(12)

C2(C1(Se1	120.0(10)

C6(C1(Se1	118.9(9)

C1(C2(C3	119.5(13)

C1(C2(H2	120.3

C3(C2(H2	120.3

C4(C3(C2	122.8(12)

C4(C3(H3	118.6

C2(C3(H3	118.6

C3(C4(C5	119.7(12)

C3(C4(H4	120.1

C5(C4(H4	120.1

C9(C5(C4	123.2(13)

C9(C5(C6	118.1(12)

C4(C5(C6	118.7(12)

N1(C6(C1	121.6(12)

N1(C6(C5	120.4(12)

C1(C6(C5	118.0(11)

N1(C7(C8	123.5(11)

N1(C7(H7	118.2

C8(C7(H7	118.2

C9(C8(C7	118.6(12)

C9(C8(H8	120.7

C7(C8(H8	120.7

C8(C9(C5	120.1(13)

C8(C9(H9	119.9

C5(C9(H9	119.9

C7(N1(C6	119.3(11)

C7(N1(Cu1	116.6(8)

C6(N1(Cu1	123.4(9)

Cu1(Cl1(Cu2	105.63(14)

Cu1(Cl1(Cu1i	110.86(14)

Cu2(Cl1(Cu1i	107.22(14)

Cu3(Cl2(Cu3ii	111.69(16)

Cu3(Cl2(Cu2	93.82(14)

Cu3ii(Cl2(Cu2	91.59(14)

Cu3(Cl3(Cu2iii	105.91(16)

Cu3(Cl3(Cu2iv	109.00(16)

Cu2iii(Cl3(Cu2iv	107.31(15)

N1(Cu1(Cl1	126.4(3)

N1(Cu1(Cl1ii	111.6(3)

Cl1(Cu1(Cl1ii	110.86(14)

N1(Cu1(Se1	83.7(3)

Cl1(Cu1(Se1	119.24(11)

Cl1ii(Cu1(Se1	99.58(10)

Cl1(Cu2(Cl3iii	113.09(14)

Cl1(Cu2(Cl3iv	110.28(14)

Cl3iii(Cu2(Cl3iv	107.31(15)

Cl1(Cu2(Cl2	107.33(14)

Cl3iii(Cu2(Cl2	110.55(15)

Cl3iv(Cu2(Cl2	108.19(15)

Cl3(Cu3(Cl2	123.69(15)

Cl3(Cu3(Cl2i	119.66(15)

Cl2(Cu3(Cl2i	111.69(16)

Cl3(Cu3(Cu3iv	76.14(12)

Cl2(Cu3(Cu3iv	109.34(13)

Cl2i(Cu3(Cu3iv	107.81(13)

C1(Se1(Cu1	90.4(4)

Symmetry transformations used to generate equivalent atoms:

(i) x(1,y,z    (ii) x+1,y,z    (iii) (x(1,(y+1,(z+1    (iv)  (x(2,(y+1,(z+1

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	21(7) 	35(7)	26(6) 	(10(6)	(5(5) 	(7(6)

C2	20(7) 	47(8)	24(6) 	(2(6)	(5(5) 	6(6)

C3	25(7) 	58(9)	21(6) 	(4(6)	0(5) 	(8(7)

C4	19(7) 	41(8)	30(7) 	(13(6)	1(5) 	3(6)

C5	28(8) 	40(8)	34(7) 	(7(6)	(6(6) 	1(7)

C6	19(7) 	54(9)	21(6) 	(4(6)	(9(5) 	(2(6)

C7	18(6) 	29(7)	25(6) 	5(5)	(2(5) 	(2(5)

C8	45(9) 	29(7)	34(8) 	13(6)	(15(7) 	(3(7)

C9	18(7) 	36(8)	53(9) 	0(7)	(15(6) 	1(6)

N1	29(6) 	27(6)	24(5) 	(2(4)	(1(4) 	(2(5)

Cl1	25(2) 	37(2)	27(2) 	2(1)	2(1) 	(1(1)

Cl2	35(2) 	34(2)	43(2) 	(12(2)	3(2) 	0(2)

Cl3	32(2) 	36(2)	55(2) 	14(2)	1(2) 	0(2)

Cu1	44(1) 	38(1)	31(1) 	(2(1)	7(1) 	3(1)

Cu2	50(1) 	55(1)	47(1) 	9(1)	3(1) 	2(1)

Cu3	41(1) 	49(1)	48(1) 	8(1)	5(1) 	3(1)

Se1	31(1) 	28(1)	27(1) 	3(1)	5(1) 	1(1)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H2	3637	1278	2068	37	1

H3	5143	(153	1693	41	1

H4	4773	(1456	2246	36	1

H7	(1189	(629	4476	29	1

H8	(59	(2089	4101	43	1

H9	2488	(2228	3173	43	1