|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	2005src1629

Empirical formula 	C43H35Br2Cl9Fe2N4Ni

Formula weight 	1257.03

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P(1

Unit cell dimensions	a = 12.605(5) Å	( = 89.829(5)°

b = 12.979(5) Å	( = 86.600(5)°

c = 16.011(5) Å	(  = 64.693(5)°

Volume	2363.1(15) Å3

Z	2

Density (calculated)	1.767 Mg / m3

Absorption coefficient	3.237 mm(1

F(000)	1248

Crystal	Block; Orange

Crystal size	0.25 ( 0.20 ( 0.15 mm3

( range for data collection	4.85 ( 27.14°

Index ranges	(16 ( h ( 15, (16 ( k ( 16, (20 ( l ( 20

Reflections collected	35380

Independent reflections	35386 [Rint = 0.0000]

Completeness to ( = 27.14°	89.2 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.6424 and 0.4983

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	35386 / 0 / 551

Goodness-of-fit on F2	1.097

Final R indices [F2 > 2((F2)]	R1 = 0.1109, wR2 = 0.2258

R indices (all data)	R1 = 0.2071, wR2 = 0.2874

Largest diff. peak and hole	1.550 and (1.543 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SADABS Version 2.10. (G. M. Sheldrick (2003)) Bruker AXS Inc., Madison, Wisconsin, USA. Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP3 for Windows (L. J. Farrugia, J. Appl. Crystallogr. 1997, 30, 565).

Special details:

All hydrogen atoms were fixed.

The crystals were twinned (180( about -1 0 0 direct axis) at 41.4%

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

Ni1	4472(1)	(52(1)	2527(1)	17(1)	1

Br1	2518(1)	918(1)	3466(1)	26(1)	1

Br2	3929(1)	(1448(1)	1673(1)	22(1)	1

C1	2645(8)	1600(7)	1457(5)	23(2)	1

C2	2191(8)	2244(8)	773(5)	26(2)	1

C3	2987(9)	2235(9)	120(5)	31(2)	1

C4	4172(9)	1637(8)	222(5)	25(2)	1

C5	4569(7)	1043(8)	939(5)	22(2)	1

C6	5800(8)	382(8)	1089(5)	21(2)	1

C7	6675(8)	603(8)	652(5)	26(2)	1

C8	7826(8)	(13(9)	857(6)	31(2)	1

C9	8088(8)	(845(8)	1429(5)	27(2)	1

C10	7189(7)	(1074(8)	1827(5)	21(2)	1

C11	7474(7)	(2021(8)	2392(5)	23(2)	1

C12	7029(9)	(2862(8)	2411(6)	29(2)	1

C13	7554(8)	(3606(8)	3060(6)	34(2)	1

C14	8319(9)	(3262(9)	3441(6)	35(2)	1

C15	8314(8)	(2287(8)	3026(6)	30(2)	1

C16	9326(11)	(4622(11)	1109(7)	53(3)	1

C17	9772(11)	(5300(11)	1812(8)	58(3)	1

C18	10502(10)	(4899(10)	2199(7)	50(3)	1

C19	10519(8)	(3966(10)	1751(6)	39(3)	1

C20	9761(8)	(3768(9)	1076(6)	36(2)	1

N1	3773(6)	1047(6)	1566(4)	19(2)	1

N2	6053(6)	(428(6)	1680(4)	18(2)	1

Fe1	8828(1)	(3640(1)	2203(1)	28(1)	1

C21	4609(8)	(1930(7)	3667(5)	20(2)	1

C22	4884(8)	(2588(8)	4370(5)	23(2)	1

C23	5601(8)	(2422(7)	4926(5)	25(2)	1

C24	5991(8)	(1599(8)	4772(5)	23(2)	1

C25	5691(7)	(958(8)	4051(5)	20(2)	1

C26	6046(7)	(53(7)	3846(5)	17(2)	1

C27	6987(7)	5(7)	4229(5)	20(2)	1

C28	7341(8)	832(8)	3984(6)	28(2)	1

C29	6737(8)	1601(8)	3410(5)	26(2)	1

C30	5746(7)	1555(7)	3090(5)	20(2)	1

C31	5036(8)	2443(7)	2522(5)	18(2)	1

C32	5511(8)	2913(8)	1880(5)	26(2)	1

C33	4548(10)	3717(9)	1464(5)	33(2)	1

C34	3507(8)	3781(7)	1859(5)	23(2)	1

C35	3806(8)	2975(8)	2501(5)	25(2)	1

C36	5377(11)	4966(9)	3110(6)	40(3)	1

C37	4459(12)	5740(9)	2687(7)	49(3)	1

C38	3409(12)	5815(10)	3140(7)	55(3)	1

C39	3722(11)	5058(10)	3805(7)	47(3)	1

C40	4958(10)	4554(9)	3806(6)	39(3)	1

N21	4989(6)	(1143(6)	3502(4)	18(2)	1

N22	5424(6)	706(6)	3284(4)	17(2)	1

Fe21	4430(1)	4177(1)	2699(1)	24(1)	1

C41	2439(9)	(3884(9)	(60(6)	39(3)	1

Cl41	3170(3)	(3305(3)	518(2)	55(1)	1

Cl42	1465(3)	(2851(3)	(697(2)	67(1)	1

Cl43	3458(3)	(5056(3)	(710(2)	59(1)	1

C51	883(9)	(154(9)	2177(6)	38(3)	1

Cl51	824(3)	(516(4)	1125(2)	76(1)	1

Cl52	782(3)	(1179(3)	2823(2)	78(1)	1

Cl53	(289(3)	1183(3)	2434(2)	67(1)	1

C61	(297(10)	2766(10)	4315(7)	44(3)	1

Cl61	(301(4)	2009(4)	5224(2)	93(1)	1

Cl62	162(4)	3828(3)	4494(3)	90(1)	1

Cl63	(1726(3)	3380(3)	3970(2)	65(1)	1

Table 3. Bond lengths [Å] and angles [°].

Ni1(N21	2.047(7)

Ni1(N1	2.062(7)

Ni1(N2	2.214(6)

Ni1(N22	2.253(6)

Ni1(Br2	2.6078(14)

Ni1(Br1	2.6135(15)

C1(N1	1.312(11)

C1(C2	1.373(12)

C1(H1	0.9500

C2(C3	1.403(12)

C2(H2	0.9500

C3(C4	1.378(13)

C3(H3	0.9500

C4(C5	1.376(12)

C4(H4	0.9500

C5(N1	1.376(10)

C5(C6	1.451(12)

C6(N2	1.359(10)

C6(C7	1.402(11)

C7(C8	1.383(13)

C7(H7	0.9500

C8(C9	1.357(13)

C8(H8	0.9500

C9(C10	1.406(11)

C9(H9	0.9500

C10(N2	1.349(11)

C10(C11	1.453(12)

C11(C12	1.424(12)

C11(C15	1.444(12)

C11(Fe1	2.073(9)

C12(C13	1.407(13)

C12(Fe1	2.056(10)

C12(H12	0.9500

C13(C14	1.393(13)

C13(Fe1	2.035(9)

C13(H13	0.9500

C14(C15	1.425(14)

C14(Fe1	2.042(9)

C14(H14	0.9500

C15(Fe1	2.045(10)

C15(H15	0.9500

C16(C17	1.416(16)

C16(C20	1.432(14)

C16(Fe1	2.070(10)

C16(H16	0.9500

C17(C18	1.406(16)

C17(Fe1	2.043(12)

C17(H17	0.9500

C18(C19	1.413(16)

C18(Fe1	2.043(11)

C18(H18	0.9500

C19(C20	1.435(13)

C19(Fe1	2.073(9)

C19(H19	0.9500

C20(Fe1	2.062(9)

C20(H20	0.9500

C21(N21	1.320(10)

C21(C22	1.379(11)

C21(H21	0.9500

C22(C23	1.385(11)

C22(H22	0.9500

C23(C24	1.370(11)

C23(H23	0.9500

C24(C25	1.394(11)

C24(H24	0.9500

C25(N21	1.374(10)

C25(C26	1.455(11)

C26(N22	1.346(10)

C26(C27	1.397(11)

C27(C28	1.375(12)

C27(H27	0.9500

C28(C29	1.361(13)

C28(H28	0.9500

C29(C30	1.402(11)

C29(H29	0.9500

C30(N22	1.355(10)

C30(C31	1.472(12)

C31(C35	1.404(13)

C31(C32	1.422(11)

C31(Fe21	2.059(8)

C32(C33	1.419(14)

C32(Fe21	2.039(9)

C32(H32	0.9500

C33(C34	1.391(13)

C33(Fe21	2.046(8)

C33(H33	0.9500

C34(C35	1.413(12)

C34(Fe21	2.031(8)

C34(H34	0.9500

C35(Fe21	2.058(7)

C35(H35	0.9500

C36(C37	1.379(16)

C36(C40	1.405(13)

C36(Fe21	2.012(9)

C36(H36	0.9500

C37(C38	1.436(17)

C37(Fe21	2.044(10)

C37(H37	0.9500

C38(C39	1.402(16)

C38(Fe21	2.058(11)

C38(H38	0.9500

C39(C40	1.409(16)

C39(Fe21	2.047(10)

C39(H39	0.9500

C40(Fe21	2.060(9)

C40(H40	0.9500

C41(Cl41	1.723(10)

C41(Cl42	1.754(11)

C41(Cl43	1.796(11)

C41(H41	1.0000

C51(Cl52	1.726(11)

C51(Cl53	1.762(11)

C51(Cl51	1.764(10)

C51(H51	1.0000

C61(Cl62	1.738(10)

C61(Cl63	1.753(11)

C61(Cl61	1.754(11)

C61(H61	1.0000

N21(Ni1(N1	173.7(2)

N21(Ni1(N2	107.1(3)

N1(Ni1(N2	78.4(3)

N21(Ni1(N22	77.6(2)

N1(Ni1(N22	106.7(2)

N2(Ni1(N22	79.6(2)

N21(Ni1(Br2	92.42(17)

N1(Ni1(Br2	84.43(17)

N2(Ni1(Br2	91.26(15)

N22(Ni1(Br2	163.66(18)

N21(Ni1(Br1	83.24(19)

N1(Ni1(Br1	91.86(19)

N2(Ni1(Br1	165.66(19)

N22(Ni1(Br1	93.36(17)

Br2(Ni1(Br1	98.33(5)

N1(C1(C2	124.3(8)

N1(C1(H1	117.8

C2(C1(H1	117.8

C1(C2(C3	117.6(8)

C1(C2(H2	121.2

C3(C2(H2	121.2

C4(C3(C2	118.3(8)

C4(C3(H3	120.9

C2(C3(H3	120.9

C3(C4(C5	121.1(8)

C3(C4(H4	119.5

C5(C4(H4	119.5

N1(C5(C4	119.7(8)

N1(C5(C6	115.9(7)

C4(C5(C6	124.4(8)

N2(C6(C7	122.2(8)

N2(C6(C5	117.2(7)

C7(C6(C5	120.6(8)

C8(C7(C6	117.9(8)

C8(C7(H7	121.1

C6(C7(H7	121.1

C9(C8(C7	120.1(8)

C9(C8(H8	119.9

C7(C8(H8	119.9

C8(C9(C10	120.2(9)

C8(C9(H9	119.9

C10(C9(H9	119.9

N2(C10(C9	120.5(8)

N2(C10(C11	119.1(7)

C9(C10(C11	120.4(8)

C12(C11(C15	107.9(8)

C12(C11(C10	127.6(7)

C15(C11(C10	124.5(7)

C12(C11(Fe1	69.2(5)

C15(C11(Fe1	68.4(5)

C10(C11(Fe1	126.3(6)

C13(C12(C11	107.4(8)

C13(C12(Fe1	69.1(5)

C11(C12(Fe1	70.5(5)

C13(C12(H12	126.3

C11(C12(H12	126.3

Fe1(C12(H12	125.7

C14(C13(C12	109.5(8)

C14(C13(Fe1	70.3(5)

C12(C13(Fe1	70.7(5)

C14(C13(H13	125.3

C12(C13(H13	125.3

Fe1(C13(H13	125.3

C13(C14(C15	108.7(9)

C13(C14(Fe1	69.7(5)

C15(C14(Fe1	69.7(5)

C13(C14(H14	125.7

C15(C14(H14	125.7

Fe1(C14(H14	126.5

C14(C15(C11	106.5(8)

C14(C15(Fe1	69.5(6)

C11(C15(Fe1	70.5(5)

C14(C15(H15	126.8

C11(C15(H15	126.8

Fe1(C15(H15	124.8

C17(C16(C20	108.0(10)

C17(C16(Fe1	68.8(6)

C20(C16(Fe1	69.4(6)

C17(C16(H16	126.0

C20(C16(H16	126.0

Fe1(C16(H16	127.3

C16(C17(C18	108.1(11)

C16(C17(Fe1	70.9(7)

C18(C17(Fe1	69.9(7)

C16(C17(H17	125.9

C18(C17(H17	125.9

Fe1(C17(H17	124.9

C19(C18(C17	109.1(11)

C19(C18(Fe1	71.1(6)

C17(C18(Fe1	69.9(7)

C19(C18(H18	125.4

C17(C18(H18	125.4

Fe1(C18(H18	125.2

C18(C19(C20	107.4(9)

C18(C19(Fe1	68.8(6)

C20(C19(Fe1	69.3(5)

C18(C19(H19	126.3

C20(C19(H19	126.3

Fe1(C19(H19	127.2

C16(C20(C19	107.3(10)

C16(C20(Fe1	70.0(5)

C19(C20(Fe1	70.1(5)

C16(C20(H20	126.3

C19(C20(H20	126.3

Fe1(C20(H20	125.1

C1(N1(C5	118.9(7)

C1(N1(Ni1	124.8(5)

C5(N1(Ni1	115.6(6)

C10(N2(C6	118.9(7)

C10(N2(Ni1	128.2(5)

C6(N2(Ni1	109.6(6)

C13(Fe1(C17	107.0(4)

C13(Fe1(C18	121.0(4)

C17(Fe1(C18	40.2(5)

C13(Fe1(C14	40.0(4)

C17(Fe1(C14	119.7(5)

C18(Fe1(C14	104.4(4)

C13(Fe1(C15	68.3(4)

C17(Fe1(C15	154.8(5)

C18(Fe1(C15	119.4(4)

C14(Fe1(C15	40.8(4)

C13(Fe1(C12	40.2(4)

C17(Fe1(C12	124.5(4)

C18(Fe1(C12	158.3(4)

C14(Fe1(C12	67.8(4)

C15(Fe1(C12	68.9(4)

C13(Fe1(C20	161.1(4)

C17(Fe1(C20	68.3(5)

C18(Fe1(C20	68.0(4)

C14(Fe1(C20	158.5(4)

C15(Fe1(C20	123.9(4)

C12(Fe1(C20	126.3(4)

C13(Fe1(C19	156.4(4)

C17(Fe1(C19	67.8(5)

C18(Fe1(C19	40.2(4)

C14(Fe1(C19	120.9(4)

C15(Fe1(C19	106.0(4)

C12(Fe1(C19	161.2(4)

C20(Fe1(C19	40.6(4)

C13(Fe1(C16	124.2(4)

C17(Fe1(C16	40.3(5)

C18(Fe1(C16	67.5(5)

C14(Fe1(C16	156.9(4)

C15(Fe1(C16	162.1(5)

C12(Fe1(C16	111.3(4)

C20(Fe1(C16	40.5(4)

C19(Fe1(C16	67.7(4)

C13(Fe1(C11	67.5(4)

C17(Fe1(C11	162.0(4)

C18(Fe1(C11	157.5(4)

C14(Fe1(C11	67.9(4)

C15(Fe1(C11	41.0(3)

C12(Fe1(C11	40.4(3)

C20(Fe1(C11	111.0(4)

C19(Fe1(C11	124.2(4)

C16(Fe1(C11	127.5(5)

N21(C21(C22	123.2(7)

N21(C21(H21	118.4

C22(C21(H21	118.4

C21(C22(C23	118.4(7)

C21(C22(H22	120.8

C23(C22(H22	120.8

C24(C23(C22	119.3(8)

C24(C23(H23	120.3

C22(C23(H23	120.3

C23(C24(C25	120.1(7)

C23(C24(H24	120.0

C25(C24(H24	120.0

N21(C25(C24	119.8(7)

N21(C25(C26	116.4(7)

C24(C25(C26	123.8(7)

N22(C26(C27	122.9(7)

N22(C26(C25	116.9(7)

C27(C26(C25	120.2(8)

C28(C27(C26	118.6(8)

C28(C27(H27	120.7

C26(C27(H27	120.7

C29(C28(C27	119.5(7)

C29(C28(H28	120.2

C27(C28(H28	120.2

C28(C29(C30	119.5(8)

C28(C29(H29	120.3

C30(C29(H29	120.3

N22(C30(C29	121.8(8)

N22(C30(C31	118.7(7)

C29(C30(C31	119.4(7)

C35(C31(C32	107.8(8)

C35(C31(C30	127.9(7)

C32(C31(C30	124.4(8)

C35(C31(Fe21	70.0(5)

C32(C31(Fe21	68.9(5)

C30(C31(Fe21	126.5(5)

C33(C32(C31	107.0(8)

C33(C32(Fe21	69.9(5)

C31(C32(Fe21	70.4(5)

C33(C32(H32	126.5

C31(C32(H32	126.5

Fe21(C32(H32	124.8

C34(C33(C32	108.8(8)

C34(C33(Fe21	69.5(5)

C32(C33(Fe21	69.4(5)

C34(C33(H33	125.6

C32(C33(H33	125.6

Fe21(C33(H33	127.1

C33(C34(C35	107.8(8)

C33(C34(Fe21	70.6(5)

C35(C34(Fe21	70.8(4)

C33(C34(H34	126.1

C35(C34(H34	126.1

Fe21(C34(H34	124.1

C31(C35(C34	108.5(7)

C31(C35(Fe21	70.1(4)

C34(C35(Fe21	68.8(4)

C31(C35(H35	125.8

C34(C35(H35	125.8

Fe21(C35(H35	126.9

C37(C36(C40	110.9(11)

C37(C36(Fe21	71.4(6)

C40(C36(Fe21	71.7(5)

C37(C36(H36	124.5

C40(C36(H36	124.5

Fe21(C36(H36	124.0

C36(C37(C38	105.4(10)

C36(C37(Fe21	68.9(6)

C38(C37(Fe21	70.1(6)

C36(C37(H37	127.3

C38(C37(H37	127.3

Fe21(C37(H37	125.4

C39(C38(C37	109.1(11)

C39(C38(Fe21	69.6(7)

C37(C38(Fe21	69.0(6)

C39(C38(H38	125.5

C37(C38(H38	125.5

Fe21(C38(H38	127.6

C38(C39(C40	107.4(10)

C38(C39(Fe21	70.5(6)

C40(C39(Fe21	70.4(6)

C38(C39(H39	126.3

C40(C39(H39	126.3

Fe21(C39(H39	124.4

C36(C40(C39	107.1(10)

C36(C40(Fe21	68.0(5)

C39(C40(Fe21	69.5(6)

C36(C40(H40	126.5

C39(C40(H40	126.5

Fe21(C40(H40	127.6

C21(N21(C25	119.2(7)

C21(N21(Ni1	124.0(5)

C25(N21(Ni1	116.5(5)

C26(N22(C30	117.4(6)

C26(N22(Ni1	109.3(5)

C30(N22(Ni1	129.4(5)

C36(Fe21(C34	155.5(4)

C36(Fe21(C32	107.1(4)

C34(Fe21(C32	68.3(3)

C36(Fe21(C37	39.7(4)

C34(Fe21(C37	120.2(4)

C32(Fe21(C37	120.4(4)

C36(Fe21(C33	121.0(4)

C34(Fe21(C33	39.9(4)

C32(Fe21(C33	40.7(4)

C37(Fe21(C33	104.8(4)

C36(Fe21(C39	67.7(4)

C34(Fe21(C39	124.6(4)

C32(Fe21(C39	160.0(4)

C37(Fe21(C39	68.8(4)

C33(Fe21(C39	158.8(5)

C36(Fe21(C35	162.2(4)

C34(Fe21(C35	40.4(3)

C32(Fe21(C35	67.7(4)

C37(Fe21(C35	157.8(5)

C33(Fe21(C35	67.0(3)

C39(Fe21(C35	110.9(4)

C36(Fe21(C31	125.2(4)

C34(Fe21(C31	68.0(3)

C32(Fe21(C31	40.6(3)

C37(Fe21(C31	158.2(4)

C33(Fe21(C31	67.6(4)

C39(Fe21(C31	125.4(4)

C35(Fe21(C31	39.9(4)

C36(Fe21(C38	66.8(5)

C34(Fe21(C38	107.8(4)

C32(Fe21(C38	157.7(4)

C37(Fe21(C38	41.0(5)

C33(Fe21(C38	122.3(5)

C39(Fe21(C38	39.9(4)

C35(Fe21(C38	124.5(5)

C31(Fe21(C38	160.2(4)

C36(Fe21(C40	40.3(4)

C34(Fe21(C40	161.8(4)

C32(Fe21(C40	123.5(4)

C37(Fe21(C40	68.0(4)

C33(Fe21(C40	157.9(4)

C39(Fe21(C40	40.1(5)

C35(Fe21(C40	127.1(4)

C31(Fe21(C40	111.0(4)

C38(Fe21(C40	66.7(5)

Cl41(C41(Cl42	110.4(6)

Cl41(C41(Cl43	110.8(6)

Cl42(C41(Cl43	108.9(5)

Cl41(C41(H41	108.9

Cl42(C41(H41	108.9

Cl43(C41(H41	108.9

Cl52(C51(Cl53	110.0(6)

Cl52(C51(Cl51	109.7(5)

Cl53(C51(Cl51	109.2(6)

Cl52(C51(H51	109.3

Cl53(C51(H51	109.3

Cl51(C51(H51	109.3

Cl62(C61(Cl63	109.5(7)

Cl62(C61(Cl61	111.8(6)

Cl63(C61(Cl61	108.4(6)

Cl62(C61(H61	109.0

Cl63(C61(H61	109.0

Cl61(C61(H61	109.0

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

Ni1	17(1) 	20(1)	13(1) 	(2(1)	(1(1) 	(9(1)

Br1	20(1) 	38(1)	19(1) 	(3(1)	0(1) 	(11(1)

Br2	27(1) 	27(1)	17(1) 	(2(1)	(2(1) 	(16(1)

C1	26(5) 	18(5)	23(5) 	(1(4)	(5(4) 	(6(4)

C2	14(4) 	33(6)	31(5) 	(11(4)	(4(4) 	(8(4)

C3	43(6) 	35(6)	20(5) 	3(4)	(9(4) 	(21(6)

C4	44(6) 	23(5)	14(4) 	(2(4)	(1(4) 	(19(5)

C5	25(5) 	23(5)	20(4) 	(5(4)	(4(4) 	(12(5)

C6	28(5) 	23(5)	14(4) 	(2(4)	(6(4) 	(11(5)

C7	33(6) 	26(5)	28(5) 	2(4)	(2(4) 	(21(5)

C8	20(5) 	47(7)	32(5) 	3(5)	5(4) 	(19(5)

C9	27(5) 	23(5)	25(5) 	3(4)	(2(4) 	(5(5)

C10	12(4) 	30(5)	21(4) 	(2(4)	3(3) 	(8(4)

C11	18(5) 	25(5)	26(5) 	(6(4)	3(4) 	(10(4)

C12	28(5) 	18(5)	31(5) 	(5(4)	8(4) 	(2(5)

C13	25(5) 	18(5)	50(6) 	3(5)	11(5) 	(1(5)

C14	31(6) 	40(7)	25(5) 	3(5)	7(4) 	(7(5)

C15	18(5) 	26(6)	38(5) 	(2(4)	(11(4) 	(1(5)

C16	56(8) 	56(8)	32(6) 	(25(6)	22(6) 	(15(7)

C17	44(7) 	43(8)	54(8) 	(5(6)	16(6) 	11(6)

C18	31(6) 	48(8)	34(6) 	1(5)	3(5) 	19(6)

C19	18(5) 	56(8)	36(6) 	(6(5)	5(4) 	(9(5)

C20	27(5) 	36(6)	34(5) 	2(5)	5(4) 	(3(5)

N1	24(4) 	22(4)	12(3) 	(13(3)	7(3) 	(13(4)

N2	20(4) 	21(4)	14(3) 	(9(3)	1(3) 	(11(4)

Fe1	22(1) 	26(1)	28(1) 	(1(1)	1(1) 	(2(1)

C21	27(5) 	18(5)	19(4) 	(4(4)	(1(4) 	(13(4)

C22	35(5) 	28(6)	11(4) 	(7(4)	5(4) 	(18(5)

C23	32(5) 	17(5)	20(4) 	15(4)	(5(4) 	(6(4)

C24	30(5) 	28(5)	13(4) 	(1(4)	(1(4) 	(14(5)

C25	21(5) 	25(5)	14(4) 	(7(4)	(2(3) 	(9(4)

C26	24(5) 	15(5)	11(4) 	(9(3)	7(3) 	(8(4)

C27	11(4) 	17(5)	25(5) 	3(4)	(10(3) 	2(4)

C28	15(5) 	36(6)	40(5) 	(7(4)	(9(4) 	(16(5)

C29	25(5) 	24(5)	34(5) 	(3(4)	(9(4) 	(15(5)

C30	23(5) 	21(5)	16(4) 	(5(4)	5(4) 	(9(4)

C31	29(5) 	16(5)	17(4) 	0(3)	0(4) 	(19(4)

C32	29(5) 	23(5)	25(5) 	(3(4)	(5(4) 	(11(5)

C33	61(7) 	36(6)	16(5) 	4(4)	(6(4) 	(33(6)

C34	18(5) 	11(5)	33(5) 	(1(4)	(7(4) 	2(4)

C35	32(5) 	30(6)	24(5) 	(4(4)	(4(4) 	(25(5)

C36	64(8) 	34(6)	36(6) 	3(5)	(2(5) 	(35(6)

C37	92(10) 	22(6)	40(6) 	5(5)	(19(7) 	(29(7)

C38	67(9) 	26(7)	57(8) 	(24(6)	(14(7) 	(5(6)

C39	68(9) 	29(7)	45(7) 	(12(5)	9(6) 	(21(7)

C40	67(8) 	32(6)	28(5) 	5(4)	(19(5) 	(30(6)

N21	20(4) 	24(4)	9(3) 	(6(3)	1(3) 	(10(4)

N22	17(4) 	17(4)	12(3) 	0(3)	4(3) 	(4(3)

Fe21	32(1) 	18(1)	24(1) 	(1(1)	(5(1) 	(11(1)

C41	42(6) 	43(7)	29(5) 	7(5)	6(5) 	(15(6)

Cl41	61(2) 	49(2)	58(2) 	(1(1)	(19(2) 	(24(2)

Cl42	62(2) 	69(2)	77(2) 	22(2)	(33(2) 	(33(2)

Cl43	58(2) 	68(2)	57(2) 	(17(2)	8(2) 	(34(2)

C51	28(6) 	45(7)	47(6) 	(7(5)	(8(5) 	(20(6)

Cl51	36(2) 	141(4)	43(2) 	(24(2)	2(1) 	(33(2)

Cl52	73(2) 	88(3)	91(3) 	36(2)	(13(2) 	(51(2)

Cl53	41(2) 	64(2)	82(2) 	(16(2)	(16(2) 	(7(2)

C61	38(6) 	55(8)	46(6) 	(2(6)	(11(5) 	(25(6)

Cl61	80(3) 	108(4)	68(2) 	31(2)	0(2) 	(18(3)

Cl62	97(3) 	57(2)	127(3) 	(11(2)	(44(3) 	(38(2)

Cl63	42(2) 	47(2)	96(2) 	(4(2)	(27(2) 	(9(2)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H1	2107	1552	1879	28	1

H2	1368	2679	744	32	1

H3	2716	2631	(381	37	1

H4	4725	1634	(209	31	1

H7	6484	1158	230	32	1

H8	8434	147	596	38	1

H9	8881	(1274	1562	33	1

H12	6479	(2911	2051	34	1

H13	7409	(4244	3214	41	1

H14	8769	(3618	3902	43	1

H15	8773	(1891	3143	37	1

H16	8825	(4718	726	63	1

H17	9608	(5917	1992	69	1

H18	10917	(5206	2683	61	1

H19	10953	(3546	1874	47	1

H20	9582	(3179	680	44	1

H21	4123	(2048	3284	25	1

H22	4588	(3141	4470	28	1

H23	5820	(2875	5408	30	1

H24	6466	(1464	5157	28	1

H27	7374	(516	4649	24	1

H28	8003	866	4215	34	1

H29	6984	2166	3226	31	1

H32	6319	2725	1753	31	1

H33	4605	4141	993	40	1

H34	2734	4278	1721	28	1

H35	3266	2819	2859	30	1

H36	6185	4742	2953	48	1

H37	4510	6139	2199	59	1

H38	2628	6300	3010	66	1

H39	3197	4911	4184	57	1

H40	5420	4033	4201	47	1

H41	1980	(4168	332	47	1

H51	1646	(110	2249	46	1

H61	245	2223	3872	53	1