|  | University of Southampton · Department of Chemistry # EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	01SOT025

Empirical formula 	C52H44N4O6S2

C48H32N4O4 . 2(CH3)2SO

Formula weight 	885.03

Temperature 	150(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/c

Unit cell dimensions	a = 16.4380(3) Å

b = 7.82380(10) Å	 = 109.970(3)°

c = 18.1280(3) Å

Volume	2191.22(6) Å3

Z	2

Density (calculated)	1.341 Mg / m3

Absorption coefficient	0.179 mm1

F(000)	928

Crystal	Colourless hexagonal prism

Crystal size	0.15  0.10  0.08 mm3

 range for data collection	2.92  25.02°

Index ranges	19  h  19, 9  k  9, 20  l  21

Reflections collected	12475

Independent reflections	3848 [Rint = 0.1479]

Completeness to  = 25.02°	99.4 %

Max. and min. transmission	0.9858 and 0.9736

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	3848 / 0 / 290

Goodness-of-fit on F2	0.947

Final R indices [F2 > 2(F2)]	R1 = 0.0580, wR2 = 0.1088

R indices (all data)	R1 = 0.1481, wR2 = 0.1363

Extinction coefficient	0.0032(8)

Largest diff. peak and hole	0.315 and 0.313 e Å3

Diffractometer: Nonius KappaCCD area detector ( scans and  scans to fill Ewald sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 3337; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:  All hydrogen atoms were placed in idealised positions and refined using a riding model.

Table 2. Atomic coordinates [ 104], equivalent isotropic displacement parameters [Å2  103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	474(2)	10144(5)	879(2)	36(1)	1

C2	374(3)	11618(5)	1313(2)	40(1)	1

C3	636(2)	11684(5)	1958(2)	36(1)	1

C4	989(2)	10262(5)	2162(2)	38(1)	1

C5	1096(2)	8775(5)	1724(2)	35(1)	1

C6	824(2)	8697(4)	1080(2)	24(1)	1

C7	992(2)	7134(4)	591(2)	26(1)	1

C8	1815(2)	6296(5)	263(2)	26(1)	1

C9	2641(2)	6900(5)	340(2)	29(1)	1

C10	2876(2)	8605(5)	224(2)	32(1)	1

C11	3638(3)	9188(5)	300(2)	41(1)	1

C12	4173(3)	8052(6)	499(2)	43(1)	1

C13	3955(3)	6366(6)	616(2)	43(1)	1

C14	3192(2)	5771(5)	535(2)	36(1)	1

C15	1724(2)	4932(4)	168(2)	26(1)	1

C16	2427(2)	3756(5)	659(2)	27(1)	1

C17	3501(2)	3543(4)	1993(2)	27(1)	1

C18	3535(2)	3623(5)	2767(2)	35(1)	1

C19	4224(3)	2892(5)	3358(2)	41(1)	1

C20	4876(3)	2074(5)	3179(2)	44(1)	1

C21	4846(3)	2008(5)	2410(3)	41(1)	1

C22	4168(2)	2741(5)	1815(2)	34(1)	1

C23	419(2)	6198(4)	338(2)	24(1)	1

C24	513(2)	3636(5)	511(2)	27(1)	1

C25	1821(3)	21(5)	2281(2)	44(1)	1

C26	3052(3)	1090(6)	1749(3)	61(1)	1

N1	868(2)	4845(4)	133(2)	26(1)	1

N2	2789(2)	4315(4)	1408(2)	28(1)	1

O1	2668(2)	2535(3)	369(2)	40(1)	1

O2	969(2)	2546(3)	931(2)	35(1)	1

O3	1793(2)	3104(3)	1745(2)	44(1)	1

S1	1922(1)	1310(1)	1521(1)	38(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1C6	1.374(5)

C1C2	1.374(5)

C2C3	1.379(5)

C3C4	1.363(5)

C4C5	1.386(5)

C5C6	1.387(5)

C6C7	1.479(5)

C7C23	1.389(5)

C7C8	1.438(5)

C8C15	1.360(5)

C8C9	1.488(5)

C9C10	1.385(5)

C9C14	1.394(5)

C10C11	1.383(5)

C11C12	1.383(5)

C12C13	1.364(5)

C13C14	1.392(5)

C15N1	1.389(4)

C15C16	1.508(5)

C16O1	1.219(4)

C16N2	1.356(4)

C17C18	1.387(5)

C17C22	1.394(5)

C17N2	1.418(4)

C18C19	1.389(5)

C19C20	1.378(5)

C20C21	1.379(5)

C21C22	1.384(5)

C23N1	1.401(4)

C23C24i	1.461(5)

C24O2	1.216(4)

C24N1	1.407(4)

C24C23i	1.461(5)

C25S1	1.780(4)

C26S1	1.768(4)

O3S1	1.497(3)

C6C1C2	121.3(4)

C1C2C3	120.4(4)

C4C3C2	119.1(4)

C3C4C5	120.8(4)

C4C5C6	120.4(4)

C1C6C5	118.1(3)

C1C6C7	122.1(3)

C5C6C7	119.5(3)

C23C7C8	105.7(3)

C23C7C6	128.7(3)

C8C7C6	125.5(3)

C15C8C7	108.8(3)

C15C8C9	125.8(3)

C7C8C9	125.2(3)

C10C9C14	118.5(3)

C10C9C8	120.5(3)

C14C9C8	121.0(3)

C11C10C9	121.1(4)

C10C11C12	119.5(4)

C13C12C11	120.4(4)

C12C13C14	120.3(4)

C13C14C9	120.1(4)

C8C15N1	108.7(3)

C8C15C16	127.3(3)

N1C15C16	123.8(3)

O1C16N2	126.0(3)

O1C16C15	121.3(3)

N2C16C15	112.4(3)

C18C17C22	119.5(3)

C18C17N2	118.3(3)

C22C17N2	122.2(3)

C17C18C19	120.2(4)

C20C19C18	120.2(4)

C19C20C21	119.6(4)

C20C21C22	120.9(4)

C21C22C17	119.6(4)

C7C23N1	109.0(3)

C7C23C24i	131.4(3)

N1C23C24i	119.6(3)

O2C24N1	120.4(3)

O2C24C23i	125.1(3)

N1C24C23i	114.5(3)

C15N1C23	107.8(3)

C15N1C24	126.4(3)

C23N1C24	125.8(3)

C16N2C17	125.4(3)

O3S1C26	105.21(19)

O3S1C25	106.20(17)

C26S1C25	97.5(2)

Symmetry transformations used to generate equivalent atoms:

(i) x,y+1,z

Table 4. Anisotropic displacement parameters [Å2 103]. The anisotropic displacement

factor exponent takes the form: 2 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	37(3) 	33(3)	43(2) 	3(2)	22(2) 	4(2)

C2	41(3) 	30(3)	52(3) 	4(2)	20(2) 	5(2)

C3	29(3) 	35(3)	41(2) 	11(2)	8(2) 	2(2)

C4	32(3) 	48(3)	33(2) 	8(2)	12(2) 	2(2)

C5	27(2) 	39(3)	37(2) 	1(2)	10(2) 	5(2)

C6	16(2) 	24(2)	29(2) 	0(2)	4(2) 	4(2)

C7	25(2) 	24(2)	28(2) 	1(2)	7(2) 	1(2)

C8	22(2) 	26(2)	31(2) 	2(2)	9(2) 	0(2)

C9	21(2) 	31(2)	34(2) 	3(2)	6(2) 	0(2)

C10	23(2) 	36(2)	35(2) 	0(2)	9(2) 	3(2)

C11	32(3) 	44(3)	43(2) 	3(2)	10(2) 	13(2)

C12	24(3) 	62(3)	45(3) 	2(2)	13(2) 	7(2)

C13	32(3) 	51(3)	50(3) 	3(2)	18(2) 	9(2)

C14	29(3) 	37(3)	39(2) 	3(2)	9(2) 	2(2)

C15	18(2) 	24(2)	34(2) 	1(2)	6(2) 	1(2)

C16	20(2) 	23(2)	38(2) 	5(2)	8(2) 	2(2)

C17	18(2) 	23(2)	35(2) 	0(2)	2(2) 	1(2)

C18	31(3) 	34(2)	39(2) 	0(2)	13(2) 	4(2)

C19	39(3) 	44(3)	37(2) 	4(2)	7(2) 	4(2)

C20	31(3) 	43(3)	47(3) 	5(2)	3(2) 	9(2)

C21	24(3) 	40(3)	53(3) 	2(2)	7(2) 	7(2)

C22	28(3) 	35(2)	40(2) 	1(2)	13(2) 	2(2)

C23	18(2) 	19(2)	32(2) 	2(2)	3(2) 	2(2)

C24	23(2) 	23(2)	31(2) 	2(2)	5(2) 	1(2)

C25	50(3) 	38(3)	42(2) 	1(2)	11(2) 	5(2)

C26	43(3) 	56(3)	95(4) 	12(3)	39(3) 	14(3)

N1	17(2) 	26(2)	31(2) 	4(1)	2(1) 	4(2)

N2	20(2) 	26(2)	35(2) 	1(2)	5(2) 	6(1)

O1	33(2) 	34(2)	44(2) 	8(1)	2(1) 	10(1)

O2	21(2) 	33(2)	46(2) 	15(1)	5(1) 	4(1)

O3	39(2) 	32(2)	70(2) 	2(1)	30(2) 	3(1)

S1	38(1) 	36(1)	41(1) 	0(1)	13(1) 	6(1)

Table 5. Hydrogen coordinates [ 104] and isotropic displacement parameters [Å2  103].

Atom 	x	y	z	Ueq	S.o.f.

H1	297	10124	432	43	1

H2	122	12598	1168	47	1

H3	572	12705	2255	43	1

H4	1164	10290	2610	45	1

H5	1357	7803	1866	42	1

H10	2507	9388	89	38	1

H11	3792	10360	215	49	1

H12	4695	8448	555	52	1

H13	4326	5595	754	52	1

H14	3047	4593	611	43	1

H18	3086	4180	2894	41	1

H19	4247	2956	3888	49	1

H20	5342	1559	3582	53	1

H21	5298	1451	2287	49	1

H22	4157	2697	1288	41	1

H25A	1213	64	2246	66	1

H25B	2020	1177	2223	66	1

H25C	2173	445	2792	66	1

H26A	3236	1766	1379	91	1

H26B	3352	1498	2285	91	1

H26C	3193	116	1710	91	1

H2A	2564	5233	1543	34	1

Table 6. Hydrogen bonds [Å and °].

DH···A	d(DH)	d(H···A)	d(D···A)	(DHA)

N2H2A...O3ii	0.88	1.94	2.795(4)	164.9

N2H2A...S1ii	0.88	2.90	3.741(3)	160.6

Symmetry transformations used to generate equivalent atoms:

(i) x,y+1,z    (ii) x,y+1,z