|  | University of Southampton · School of Chemistry # EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	2005src1568   (384/1)

Empirical formula 	C24H32O

Formula weight 	336.50

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/c

Unit cell dimensions	a = 11.5027(3) Å	a = 90°

b = 13.7029(2) Å	b = 101.0000(10)°

c = 27.1787(7) Å	g  = 90°

Volume	4205.21(17) Å3

Z	8

Density (calculated)	1.063 Mg / m3

Absorption coefficient	0.062 mm-1

F(000)	1472

Crystal	block; colourless

Crystal size	0.40 ´ 0.40 ´ 0.30 mm3

q range for data collection	2.97 - 27.50°

Index ranges	-14 £ h £ 14, -17 £ k £ 17, -33 £ l £ 35

Reflections collected	52713

Independent reflections	9622 [Rint = 0.0662]

Completeness to q = 27.50°	99.6 %

Absorption correction	Semi-empirical from equivalents

Max. and min. transmission	0.9815 and 0.9754

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	9622 / 0 / 463

Goodness-of-fit on F2	1.016

Final R indices [F2 > 2s(F2)]	R1 = 0.0515, wR2 = 0.1109

R indices (all data)	R1 = 0.1035, wR2 = 0.1335

Largest diff. peak and hole	0.221 and -0.198 e Å-3

Diffractometer: Nonius KappaCCD area detector (f scans and w scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307-326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33-37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421-426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467-473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Chirality: C1=R, C9=R, C25=R, C33=R.

Table 2. Atomic coordinates [´ 104], equivalent isotropic displacement parameters [Å2 ´ 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	5241(1)	7782(1)	341(1)	22(1)	1

C2	3945(1)	7720(1)	380(1)	22(1)	1

C3	3075(1)	7907(1)	-40(1)	28(1)	1

C4	1883(1)	7813(1)	-20(1)	32(1)	1

C5	1555(1)	7535(1)	422(1)	33(1)	1

C6	2407(2)	7364(1)	843(1)	32(1)	1

C7	3603(1)	7452(1)	823(1)	27(1)	1

C8	5536(1)	6998(1)	-10(1)	25(1)	1

C9	6843(1)	6921(1)	-63(1)	23(1)	1

C10	6927(1)	6259(1)	-525(1)	26(1)	1

C11	6373(2)	6786(1)	-995(1)	32(1)	1

C12	5419(2)	6515(2)	-1317(1)	46(1)	1

C13	8198(1)	5914(1)	-543(1)	31(1)	1

C14	8180(2)	5170(1)	-964(1)	43(1)	1

C15	9046(2)	6742(1)	-601(1)	42(1)	1

C16	7660(1)	6653(1)	431(1)	24(1)	1

C17	7672(1)	5721(1)	654(1)	30(1)	1

C18	6916(2)	4870(1)	422(1)	42(1)	1

C19	8429(2)	5543(1)	1109(1)	36(1)	1

C20	9196(2)	6241(1)	1357(1)	35(1)	1

C21	10000(2)	6031(2)	1854(1)	54(1)	1

C22	9184(1)	7148(1)	1134(1)	30(1)	1

C23	8427(1)	7373(1)	685(1)	24(1)	1

C24	8457(1)	8410(1)	496(1)	31(1)	1

C25	5286(1)	9518(1)	-1196(1)	24(1)	1

C26	6630(1)	9525(1)	-1102(1)	25(1)	1

C27	7204(2)	9158(1)	-1470(1)	32(1)	1

C28	8429(2)	9174(1)	-1410(1)	39(1)	1

C29	9096(2)	9560(1)	-977(1)	39(1)	1

C30	8542(2)	9927(1)	-609(1)	37(1)	1

C31	7310(1)	9907(1)	-671(1)	29(1)	1

C32	4782(1)	10294(1)	-1577(1)	26(1)	1

C33	3457(1)	10202(1)	-1816(1)	25(1)	1

C34	3055(1)	11130(1)	-2132(1)	25(1)	1

C35	1834(1)	11024(1)	-2486(1)	32(1)	1

C36	814(2)	10913(2)	-2205(1)	46(1)	1

C37	1591(2)	11875(1)	-2852(1)	45(1)	1

C38	3066(1)	11995(1)	-1792(1)	31(1)	1

C39	3516(2)	12858(1)	-1856(1)	42(1)	1

C40	3194(1)	9215(1)	-2079(1)	24(1)	1

C41	3598(1)	8964(1)	-2520(1)	27(1)	1

C42	4244(2)	9660(1)	-2810(1)	33(1)	1

C43	3388(1)	8032(1)	-2723(1)	34(1)	1

C44	2771(2)	7327(1)	-2512(1)	38(1)	1

C45	2550(2)	6331(1)	-2751(1)	59(1)	1

C46	2373(2)	7578(1)	-2080(1)	36(1)	1

C47	2571(1)	8498(1)	-1860(1)	29(1)	1

C48	2106(2)	8681(1)	-1383(1)	42(1)	1

O1	5508(1)	8713(1)	143(1)	24(1)	1

O2	4814(1)	9699(1)	-752(1)	26(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1-O1	1.4404(17)

C1-C8	1.517(2)

C1-C2	1.518(2)

C2-C7	1.384(2)

C2-C3	1.392(2)

C3-C4	1.388(2)

C4-C5	1.379(2)

C5-C6	1.378(2)

C6-C7	1.392(2)

C8-C9	1.541(2)

C9-C16	1.530(2)

C9-C10	1.565(2)

C10-C11	1.500(2)

C10-C13	1.546(2)

C11-C12	1.320(2)

C13-C15	1.523(2)

C13-C14	1.531(2)

C16-C17	1.413(2)

C16-C23	1.414(2)

C17-C19	1.392(2)

C17-C18	1.518(2)

C19-C20	1.385(3)

C20-C22	1.381(2)

C20-C21	1.512(2)

C22-C23	1.392(2)

C23-C24	1.514(2)

C25-O2	1.4345(18)

C25-C26	1.518(2)

C25-C32	1.521(2)

C26-C31	1.382(2)

C26-C27	1.393(2)

C27-C28	1.387(2)

C28-C29	1.383(3)

C29-C30	1.378(3)

C30-C31	1.395(2)

C32-C33	1.543(2)

C33-C40	1.533(2)

C33-C34	1.556(2)

C34-C38	1.502(2)

C34-C35	1.550(2)

C35-C37	1.524(2)

C35-C36	1.525(2)

C38-C39	1.316(2)

C40-C41	1.409(2)

C40-C47	1.413(2)

C41-C43	1.393(2)

C41-C42	1.517(2)

C43-C44	1.386(3)

C44-C46	1.381(3)

C44-C45	1.512(2)

C46-C47	1.395(2)

C47-C48	1.514(2)

O1-C1-C8	107.68(12)

O1-C1-C2	111.00(11)

C8-C1-C2	110.18(12)

C7-C2-C3	118.91(14)

C7-C2-C1	121.48(14)

C3-C2-C1	119.58(14)

C4-C3-C2	120.70(16)

C5-C4-C3	119.78(16)

C6-C5-C4	120.09(15)

C5-C6-C7	120.17(16)

C2-C7-C6	120.34(16)

C1-C8-C9	116.55(12)

C16-C9-C8	112.35(13)

C16-C9-C10	116.28(12)

C8-C9-C10	109.04(12)

C11-C10-C13	111.76(14)

C11-C10-C9	108.78(12)

C13-C10-C9	113.92(13)

C12-C11-C10	126.46(17)

C15-C13-C14	109.65(14)

C15-C13-C10	113.86(14)

C14-C13-C10	110.44(14)

C17-C16-C23	117.85(15)

C17-C16-C9	123.20(14)

C23-C16-C9	118.93(13)

C19-C17-C16	119.53(15)

C19-C17-C18	116.54(15)

C16-C17-C18	123.92(15)

C20-C19-C17	122.92(16)

C22-C20-C19	117.16(16)

C22-C20-C21	121.03(18)

C19-C20-C21	121.79(17)

C20-C22-C23	122.38(16)

C22-C23-C16	120.12(15)

C22-C23-C24	117.05(14)

C16-C23-C24	122.82(14)

O2-C25-C26	113.27(13)

O2-C25-C32	107.18(12)

C26-C25-C32	110.70(12)

C31-C26-C27	118.44(15)

C31-C26-C25	122.53(14)

C27-C26-C25	119.00(14)

C28-C27-C26	121.36(17)

C29-C28-C27	119.50(17)

C30-C29-C28	119.87(16)

C29-C30-C31	120.42(17)

C26-C31-C30	120.41(16)

C25-C32-C33	116.57(13)

C40-C33-C32	111.04(12)

C40-C33-C34	116.85(13)

C32-C33-C34	109.32(12)

C38-C34-C35	110.86(12)

C38-C34-C33	109.72(13)

C35-C34-C33	113.85(13)

C37-C35-C36	109.87(15)

C37-C35-C34	111.37(14)

C36-C35-C34	113.10(14)

C39-C38-C34	125.74(17)

C41-C40-C47	117.73(14)

C41-C40-C33	123.06(14)

C47-C40-C33	119.13(14)

C43-C41-C40	119.95(15)

C43-C41-C42	115.94(15)

C40-C41-C42	124.09(14)

C44-C43-C41	122.67(16)

C46-C44-C43	117.14(16)

C46-C44-C45	122.25(17)

C43-C44-C45	120.62(18)

C44-C46-C47	122.43(16)

C46-C47-C40	120.09(16)

C46-C47-C48	117.48(15)

C40-C47-C48	122.43(15)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2´ 103]. The anisotropic displacement

factor exponent takes the form: -2p 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	21(1) 	23(1)	22(1) 	3(1)	4(1) 	-1(1)

C2	21(1) 	21(1)	24(1) 	-1(1)	4(1) 	1(1)

C3	25(1) 	35(1)	25(1) 	2(1)	6(1) 	1(1)

C4	23(1) 	38(1)	34(1) 	0(1)	2(1) 	2(1)

C5	20(1) 	37(1)	43(1) 	0(1)	11(1) 	-1(1)

C6	30(1) 	36(1)	32(1) 	4(1)	13(1) 	-1(1)

C7	26(1) 	29(1)	25(1) 	2(1)	5(1) 	0(1)

C8	20(1) 	25(1)	29(1) 	-3(1)	2(1) 	-1(1)

C9	20(1) 	22(1)	27(1) 	-2(1)	4(1) 	1(1)

C10	24(1) 	24(1)	30(1) 	-4(1)	6(1) 	0(1)

C11	35(1) 	34(1)	28(1) 	-5(1)	5(1) 	5(1)

C12	44(1) 	58(1)	34(1) 	-10(1)	1(1) 	9(1)

C13	29(1) 	35(1)	30(1) 	-2(1)	8(1) 	6(1)

C14	41(1) 	39(1)	52(1) 	-12(1)	17(1) 	4(1)

C15	30(1) 	55(1)	45(1) 	-14(1)	12(1) 	-6(1)

C16	18(1) 	29(1)	25(1) 	-1(1)	7(1) 	3(1)

C17	28(1) 	29(1)	35(1) 	3(1)	9(1) 	4(1)

C18	46(1) 	29(1)	51(1) 	8(1)	10(1) 	-2(1)

C19	35(1) 	39(1)	36(1) 	12(1)	11(1) 	10(1)

C20	27(1) 	52(1)	27(1) 	4(1)	5(1) 	14(1)

C21	50(1) 	74(2)	34(1) 	6(1)	-1(1) 	21(1)

C22	20(1) 	43(1)	26(1) 	-8(1)	5(1) 	4(1)

C23	17(1) 	31(1)	27(1) 	-4(1)	7(1) 	2(1)

C24	25(1) 	32(1)	36(1) 	-7(1)	3(1) 	-5(1)

C25	26(1) 	24(1)	21(1) 	-2(1)	5(1) 	-1(1)

C26	27(1) 	17(1)	29(1) 	3(1)	4(1) 	0(1)

C27	32(1) 	30(1)	35(1) 	-5(1)	8(1) 	-2(1)

C28	36(1) 	33(1)	51(1) 	-2(1)	19(1) 	1(1)

C29	25(1) 	30(1)	62(1) 	3(1)	9(1) 	1(1)

C30	29(1) 	31(1)	46(1) 	-1(1)	-2(1) 	0(1)

C31	28(1) 	27(1)	32(1) 	-1(1)	3(1) 	2(1)

C32	25(1) 	28(1)	23(1) 	0(1)	2(1) 	-2(1)

C33	24(1) 	30(1)	21(1) 	-1(1)	6(1) 	-1(1)

C34	24(1) 	32(1)	21(1) 	0(1)	6(1) 	2(1)

C35	27(1) 	39(1)	27(1) 	-6(1)	1(1) 	6(1)

C36	27(1) 	66(1)	44(1) 	-12(1)	5(1) 	1(1)

C37	46(1) 	49(1)	36(1) 	1(1)	-5(1) 	15(1)

C38	26(1) 	37(1)	28(1) 	-4(1)	3(1) 	5(1)

C39	38(1) 	36(1)	50(1) 	-6(1)	3(1) 	2(1)

C40	20(1) 	31(1)	21(1) 	0(1)	-1(1) 	2(1)

C41	21(1) 	35(1)	24(1) 	-2(1)	0(1) 	3(1)

C42	36(1) 	42(1)	25(1) 	-2(1)	11(1) 	5(1)

C43	23(1) 	44(1)	34(1) 	-12(1)	2(1) 	5(1)

C44	22(1) 	36(1)	52(1) 	-11(1)	2(1) 	1(1)

C45	40(1) 	45(1)	95(2) 	-28(1)	19(1) 	-7(1)

C46	25(1) 	35(1)	47(1) 	2(1)	5(1) 	-6(1)

C47	23(1) 	36(1)	28(1) 	1(1)	1(1) 	-3(1)

C48	44(1) 	49(1)	35(1) 	2(1)	13(1) 	-16(1)

O1	26(1) 	23(1)	25(1) 	0(1)	8(1) 	0(1)

O2	29(1) 	28(1)	22(1) 	2(1)	5(1) 	3(1)