|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	05src0194    (CS13)

Empirical formula 	C22H8F10N2Zn

Formula weight 	555.67

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/c

Unit cell dimensions	a = 8.0151(8) Å	( = 90°

b = 15.5644(14) Å	( = 102.337(5)°

c = 16.6592(10) Å	(  = 90°

Volume	2030.2(3) Å3

Z	4

Density (calculated)	1.818 Mg / m3

Absorption coefficient	1.315 mm(1

F(000)	1096

Crystal	block; colourless

Crystal size	0.20 ( 0.20 ( 0.20 mm3

( range for data collection	2.91 ( 27.50°

Index ranges	(10 ( h ( 10, (18 ( k ( 20, (21 ( l ( 20

Reflections collected	28500

Independent reflections	4632 [Rint = 0.0366]

Completeness to ( = 27.50°	99.4 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.7790 and 0.7790

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	4632 / 0 / 317

Goodness-of-fit on F2	1.021

Final R indices [F2 > 2((F2)]	R1 = 0.0271, wR2 = 0.0832

R indices (all data)	R1 = 0.0303, wR2 = 0.0866

Extinction coefficient	0.0067(11)

Largest diff. peak and hole	0.380 and (0.401 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	(542(2)	9639(1)	2639(1)	19(1)	1

C2	(902(2)	10115(1)	3281(1)	22(1)	1

C3	(2022(2)	10796(1)	3183(1)	26(1)	1

C4	(2842(2)	11034(1)	2402(1)	26(1)	1

C5	(2516(2)	10590(1)	1734(1)	25(1)	1

C6	(1386(2)	9911(1)	1873(1)	22(1)	1

C7	(397(2)	7455(1)	2993(1)	19(1)	1

C8	(610(2)	7219(1)	3763(1)	22(1)	1

C9	(1571(2)	6531(1)	3922(1)	25(1)	1

C10	(2383(2)	6030(1)	3274(1)	24(1)	1

C11	(2228(2)	6236(1)	2488(1)	23(1)	1

C12	(1250(2)	6933(1)	2369(1)	21(1)	1

C13	3424(2)	8802(1)	4439(1)	25(1)	1

C14	5033(2)	8862(1)	4942(1)	30(1)	1

C15	6442(2)	8808(1)	4591(1)	31(1)	1

C16	6200(2)	8694(1)	3749(1)	26(1)	1

C17	4547(2)	8636(1)	3277(1)	19(1)	1

C18	4168(2)	8509(1)	2374(1)	19(1)	1

C19	5433(2)	8466(1)	1922(1)	25(1)	1

C20	4968(2)	8340(1)	1080(1)	29(1)	1

C21	3269(2)	8250(1)	713(1)	27(1)	1

C22	2063(2)	8300(1)	1199(1)	23(1)	1

N1	3179(2)	8686(1)	3626(1)	20(1)	1

N2	2503(2)	8429(1)	2012(1)	19(1)	1

F1	(151(1)	9900(1)	4068(1)	33(1)	1

F2	(2340(2)	11234(1)	3832(1)	40(1)	1

F3	(3947(1)	11690(1)	2287(1)	38(1)	1

F4	(3314(2)	10824(1)	976(1)	40(1)	1

F5	(1149(1)	9481(1)	1197(1)	34(1)	1

F6	(1169(1)	7112(1)	1577(1)	30(1)	1

F7	(3048(1)	5750(1)	1855(1)	33(1)	1

F8	(3339(1)	5358(1)	3401(1)	35(1)	1

F9	(1752(2)	6350(1)	4686(1)	39(1)	1

F10	118(1)	7709(1)	4424(1)	30(1)	1

Zn1	847(1)	8547(1)	2807(1)	18(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(C6	1.379(2)

C1(C2	1.380(2)

C1(Zn1	2.0180(15)

C2(F1	1.3628(18)

C2(C3	1.376(2)

C3(F2	1.3471(19)

C3(C4	1.376(2)

C4(F3	1.337(2)

C4(C5	1.382(2)

C5(F4	1.3390(19)

C5(C6	1.379(2)

C6(F5	1.3575(18)

C7(C12	1.380(2)

C7(C8	1.380(2)

C7(Zn1	2.0274(16)

C8(F10	1.3633(18)

C8(C9	1.378(2)

C9(F9	1.341(2)

C9(C10	1.377(2)

C10(F8	1.3403(19)

C10(C11	1.379(2)

C11(F7	1.3495(18)

C11(C12	1.376(2)

C12(F6	1.3641(18)

C13(N1	1.338(2)

C13(C14	1.383(2)

C14(C15	1.381(3)

C15(C16	1.387(3)

C16(C17	1.391(2)

C17(N1	1.348(2)

C17(C18	1.484(2)

C18(N2	1.348(2)

C18(C19	1.387(2)

C19(C20	1.387(3)

C20(C21	1.375(3)

C21(C22	1.389(2)

C22(N2	1.340(2)

N1(Zn1	2.0766(13)

N2(Zn1	2.0738(13)

C6(C1(C2	114.16(14)

C6(C1(Zn1	122.30(11)

C2(C1(Zn1	123.08(11)

F1(C2(C3	116.52(14)

F1(C2(C1	119.33(14)

C3(C2(C1	124.13(15)

F2(C3(C2	121.65(16)

F2(C3(C4	119.20(15)

C2(C3(C4	119.16(15)

F3(C4(C3	120.60(15)

F3(C4(C5	119.94(16)

C3(C4(C5	119.46(15)

F4(C5(C6	122.05(15)

F4(C5(C4	119.31(15)

C6(C5(C4	118.64(15)

F5(C6(C5	116.28(14)

F5(C6(C1	119.25(14)

C5(C6(C1	124.44(15)

C12(C7(C8	113.83(14)

C12(C7(Zn1	124.02(11)

C8(C7(Zn1	121.83(11)

F10(C8(C9	116.09(14)

F10(C8(C7	119.07(14)

C9(C8(C7	124.80(15)

F9(C9(C8	121.54(15)

F9(C9(C10	119.82(15)

C8(C9(C10	118.63(15)

F8(C10(C9	120.51(15)

F8(C10(C11	120.17(15)

C9(C10(C11	119.31(15)

F7(C11(C12	121.73(15)

F7(C11(C10	118.94(15)

C12(C11(C10	119.32(15)

F6(C12(C11	116.56(14)

F6(C12(C7	119.31(14)

C11(C12(C7	124.11(15)

N1(C13(C14	122.62(16)

C15(C14(C13	118.69(16)

C14(C15(C16	119.09(15)

C15(C16(C17	119.34(16)

N1(C17(C16	121.17(15)

N1(C17(C18	115.81(13)

C16(C17(C18	123.02(15)

N2(C18(C19	121.44(16)

N2(C18(C17	115.75(14)

C19(C18(C17	122.80(14)

C18(C19(C20	119.09(16)

C21(C20(C19	119.36(16)

C20(C21(C22	118.80(16)

N2(C22(C21	122.14(15)

C13(N1(C17	119.09(14)

C13(N1(Zn1	126.58(11)

C17(N1(Zn1	114.33(10)

C22(N2(C18	119.17(14)

C22(N2(Zn1	126.37(11)

C18(N2(Zn1	114.45(11)

C1(Zn1(C7	116.88(6)

C1(Zn1(N2	113.31(6)

C7(Zn1(N2	115.22(6)

C1(Zn1(N1	113.33(6)

C7(Zn1(N1	112.95(6)

N2(Zn1(N1	79.62(5)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	16(1) 	19(1)	22(1) 	(1(1)	5(1) 	(2(1)

C2	21(1) 	26(1)	20(1) 	1(1)	5(1) 	(3(1)

C3	27(1) 	23(1)	30(1) 	(7(1)	14(1) 	(2(1)

C4	21(1) 	16(1)	41(1) 	1(1)	9(1) 	1(1)

C5	25(1) 	24(1)	25(1) 	4(1)	2(1) 	(1(1)

C6	22(1) 	23(1)	20(1) 	(4(1)	6(1) 	(1(1)

C7	14(1) 	21(1)	22(1) 	1(1)	4(1) 	2(1)

C8	20(1) 	24(1)	19(1) 	(2(1)	0(1) 	1(1)

C9	25(1) 	30(1)	20(1) 	5(1)	5(1) 	0(1)

C10	21(1) 	20(1)	31(1) 	3(1)	3(1) 	(1(1)

C11	20(1) 	22(1)	25(1) 	(4(1)	(2(1) 	2(1)

C12	19(1) 	24(1)	19(1) 	2(1)	3(1) 	4(1)

C13	22(1) 	31(1)	22(1) 	(2(1)	3(1) 	(3(1)

C14	26(1) 	37(1)	23(1) 	(1(1)	(2(1) 	(4(1)

C15	19(1) 	36(1)	32(1) 	1(1)	(4(1) 	(3(1)

C16	16(1) 	28(1)	32(1) 	2(1)	4(1) 	(1(1)

C17	17(1) 	16(1)	25(1) 	3(1)	4(1) 	(1(1)

C18	18(1) 	16(1)	24(1) 	3(1)	6(1) 	1(1)

C19	18(1) 	24(1)	34(1) 	3(1)	10(1) 	0(1)

C20	28(1) 	32(1)	32(1) 	0(1)	17(1) 	(1(1)

C21	33(1) 	28(1)	23(1) 	(1(1)	12(1) 	(1(1)

C22	22(1) 	26(1)	21(1) 	1(1)	6(1) 	0(1)

N1	17(1) 	24(1)	19(1) 	1(1)	3(1) 	(1(1)

N2	17(1) 	20(1)	20(1) 	2(1)	6(1) 	1(1)

F1	39(1) 	42(1)	18(1) 	1(1)	6(1) 	4(1)

F2	48(1) 	38(1)	38(1) 	(13(1)	20(1) 	6(1)

F3	30(1) 	22(1)	59(1) 	(1(1)	7(1) 	7(1)

F4	43(1) 	42(1)	29(1) 	10(1)	(3(1) 	10(1)

F5	41(1) 	41(1)	19(1) 	(7(1)	4(1) 	10(1)

F6	33(1) 	37(1)	18(1) 	1(1)	5(1) 	(2(1)

F7	33(1) 	30(1)	31(1) 	(7(1)	(6(1) 	(5(1)

F8	33(1) 	26(1)	46(1) 	6(1)	5(1) 	(9(1)

F9	49(1) 	44(1)	24(1) 	9(1)	11(1) 	(12(1)

F10	34(1) 	34(1)	20(1) 	(4(1)	3(1) 	(9(1)

Zn1	14(1) 	22(1)	17(1) 	0(1)	3(1) 	0(1)