|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	2005src0377  (DP3-143)

Empirical formula 	C22H8Cl2F10N4Ti

Formula weight 	637.12

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	C2/c

Unit cell dimensions	a = 14.034(3) Å	( = 90°

b = 7.5893(15) Å	( = 104.38(3)°

c = 22.296(5) Å	(  = 90°

Volume	2300.3(8) Å3

Z	4

Density (calculated)	1.840 Mg / m3

Absorption coefficient	0.707 mm(1

F(000)	1256

Crystal	block; black

Crystal size	0.30 ( 0.20 ( 0.10 mm3

( range for data collection	3.41 ( 27.50°

Index ranges	(18 ( h ( 18, (9 ( k ( 9, (28 ( l ( 28

Reflections collected	16052

Independent reflections	2637 [Rint = 0.0319]

Completeness to ( = 27.50°	99.7 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9326 and 0.8158

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	2637 / 0 / 194

Goodness-of-fit on F2	1.012

Final R indices [F2 > 2((F2)]	R1 = 0.0315, wR2 = 0.0879

R indices (all data)	R1 = 0.0404, wR2 = 0.0953

Extinction coefficient	0.0010(5)

Largest diff. peak and hole	0.273 and (0.465 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	6154(1)	2516(2)	6715(1)	19(1)	1

C2	6309(1)	2726(2)	6126(1)	24(1)	1

C3	5616(1)	1659(2)	5735(1)	25(1)	1

C4	5070(1)	836(2)	6090(1)	24(1)	1

C5	3464(1)	3318(2)	7708(1)	19(1)	1

C6	3469(1)	3575(2)	6660(1)	19(1)	1

C7	3969(1)	4786(2)	6386(1)	22(1)	1

C8	3595(1)	5349(2)	5786(1)	29(1)	1

C9	2712(2)	4700(3)	5446(1)	31(1)	1

C10	2196(1)	3505(2)	5703(1)	29(1)	1

C11	2570(1)	2968(2)	6310(1)	23(1)	1

N1	5387(1)	1339(2)	6694(1)	19(1)	1

N2	3883(1)	2916(2)	7264(1)	18(1)	1

F1	4827(1)	5445(1)	6708(1)	29(1)	1

F2	4090(1)	6528(2)	5533(1)	44(1)	1

F3	2346(1)	5246(2)	4860(1)	45(1)	1

F4	1340(1)	2862(2)	5373(1)	39(1)	1

F5	2047(1)	1828(1)	6554(1)	31(1)	1

Cl1	3850(1)	(1088(1)	7013(1)	27(1)	1

Ti1	5000	845(1)	7500	17(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(N1	1.390(2)

C1(C2	1.392(2)

C1(C5i	1.404(2)

C2(C3	1.394(3)

C3(C4	1.381(3)

C4(N1	1.364(2)

C5(N2	1.307(2)

C5(C1i	1.404(2)

C6(C7	1.387(2)

C6(C11	1.388(2)

C6(N2	1.418(2)

C7(F1	1.336(2)

C7(C8	1.377(3)

C8(F2	1.339(2)

C8(C9	1.374(3)

C9(F3	1.345(2)

C9(C10	1.372(3)

C10(F4	1.335(2)

C10(C11	1.386(2)

C11(F5	1.336(2)

N1(Ti1	2.0372(14)

N2(Ti1	2.1895(14)

Cl1(Ti1	2.2505(7)

Ti1(N1i	2.0372(14)

Ti1(N2i	2.1895(14)

Ti1(Cl1i	2.2505(7)

N1(C1(C2	110.05(14)

N1(C1(C5i	115.21(14)

C2(C1(C5i	134.49(15)

C1(C2(C3	106.03(15)

C4(C3(C2	107.65(16)

N1(C4(C3	110.38(15)

N2(C5(C1i	116.85(14)

C7(C6(C11	117.44(15)

C7(C6(N2	121.29(14)

C11(C6(N2	121.20(15)

F1(C7(C8	118.75(15)

F1(C7(C6	119.83(15)

C8(C7(C6	121.41(16)

F2(C8(C9	119.88(16)

F2(C8(C7	120.20(18)

C9(C8(C7	119.92(17)

F3(C9(C10	119.70(18)

F3(C9(C8	120.05(18)

C10(C9(C8	120.25(16)

F4(C10(C9	120.50(16)

F4(C10(C11	120.07(17)

C9(C10(C11	119.44(17)

F5(C11(C10	118.43(15)

F5(C11(C6	120.05(14)

C10(C11(C6	121.51(16)

C4(N1(C1	105.88(13)

C4(N1(Ti1	136.56(12)

C1(N1(Ti1	117.54(11)

C5(N2(C6	118.78(13)

C5(N2(Ti1	114.54(11)

C6(N2(Ti1	125.54(10)

N1(Ti1(N1i	158.77(8)

N1(Ti1(N2i	75.41(5)

N1i(Ti1(N2i	89.28(5)

N1(Ti1(N2	89.28(5)

N1i(Ti1(N2	75.41(5)

N2i(Ti1(N2	88.22(7)

N1(Ti1(Cl1	90.61(4)

N1i(Ti1(Cl1	103.27(4)

N2i(Ti1(Cl1	165.59(4)

N2(Ti1(Cl1	88.12(4)

N1(Ti1(Cl1i	103.27(4)

N1i(Ti1(Cl1i	90.61(4)

N2i(Ti1(Cl1i	88.12(4)

N2(Ti1(Cl1i	165.59(4)

Cl1(Ti1(Cl1i	98.67(4)

Symmetry transformations used to generate equivalent atoms:

(i) (x+1,y,(z+3/2

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	16(1) 	21(1)	21(1) 	(1(1)	6(1) 	0(1)

C2	26(1) 	27(1)	22(1) 	1(1)	9(1) 	(1(1)

C3	27(1) 	30(1)	19(1) 	(1(1)	6(1) 	4(1)

C4	21(1) 	27(1)	22(1) 	(5(1)	4(1) 	1(1)

C5	16(1) 	19(1)	22(1) 	(2(1)	5(1) 	0(1)

C6	20(1) 	18(1)	17(1) 	(1(1)	5(1) 	5(1)

C7	22(1) 	21(1)	25(1) 	1(1)	8(1) 	5(1)

C8	36(1) 	26(1)	29(1) 	9(1)	17(1) 	9(1)

C9	42(1) 	33(1)	18(1) 	6(1)	7(1) 	17(1)

C10	28(1) 	30(1)	23(1) 	(7(1)	(3(1) 	8(1)

C11	23(1) 	22(1)	23(1) 	(1(1)	5(1) 	2(1)

N1	16(1) 	21(1)	19(1) 	(3(1)	6(1) 	(1(1)

N2	16(1) 	18(1)	18(1) 	1(1)	4(1) 	0(1)

F1	21(1) 	24(1)	42(1) 	6(1)	8(1) 	0(1)

F2	51(1) 	43(1)	45(1) 	25(1)	25(1) 	10(1)

F3	58(1) 	54(1)	21(1) 	11(1)	5(1) 	21(1)

F4	36(1) 	42(1)	30(1) 	(9(1)	(11(1) 	6(1)

F5	23(1) 	31(1)	35(1) 	5(1)	0(1) 	(6(1)

Cl1	19(1) 	24(1)	39(1) 	(10(1)	10(1) 	(5(1)

Ti1	13(1) 	18(1)	20(1) 	0	6(1) 	0