|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	2005src0721

Empirical formula 	C44H18B2F30LiO4P

Formula weight 	1240.11

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P(1

Unit cell dimensions	a = 12.465(13) Å	( = 62.10(13)°

b = 14.37(3) Å	( = 84.68(10)°

c = 14.461(14) Å	(  = 89.27(10)°

Volume	2279(5) Å3

Z	2

Density (calculated)	1.807 Mg / m3

Absorption coefficient	0.230 mm(1

F(000)	1224

Crystal	Cut Blade; Colourless

Crystal size	0.14 ( 0.05 ( 0.02 mm3

( range for data collection	3.09 ( 27.48°

Index ranges	(16 ( h ( 16, (18 ( k ( 18, (18 ( l ( 18

Reflections collected	42972

Independent reflections	10370 [Rint = 0.1233]

Completeness to ( = 27.48°	99.3 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9954 and 0.9685

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	10370 / 0 / 739

Goodness-of-fit on F2	1.086

Final R indices [F2 > 2((F2)]	R1 = 0.0920, wR2 = 0.1375

R indices (all data)	R1 = 0.1822, wR2 = 0.1623

Largest diff. peak and hole	0.631 and (0.355 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SADABS Version 2.10. (G. M. Sheldrick (2003)) Bruker AXS Inc., Madison, Wisconsin, USA. Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP3 for Windows (L. J. Farrugia, J. Appl. Crystallogr. 1997, 30, 565).

Special details:

All hydrogen atoms were fixed.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	7402(3)	7021(3)	1971(3)	26(1)	1

C2	6594(3)	7667(3)	2064(3)	25(1)	1

C3	5816(4)	8084(4)	1387(4)	32(1)	1

C4	5802(4)	7859(4)	559(4)	37(1)	1

C5	6558(4)	7209(4)	439(4)	34(1)	1

C6	7322(4)	6789(4)	1147(3)	28(1)	1

C7	7489(3)	5571(3)	3911(3)	26(1)	1

C8	7051(3)	5636(4)	4796(3)	27(1)	1

C9	6335(4)	4906(4)	5585(4)	30(1)	1

C10	6013(4)	4039(4)	5511(4)	32(1)	1

C11	6398(4)	3930(4)	4642(4)	32(1)	1

C12	7104(4)	4694(4)	3862(3)	29(1)	1

C13	8845(3)	7322(3)	3186(3)	24(1)	1

C14	8917(3)	8414(3)	2572(3)	26(1)	1

C15	9463(4)	9075(4)	2828(4)	29(1)	1

C16	10004(4)	8654(4)	3718(4)	34(1)	1

C17	9972(4)	7588(4)	4349(4)	33(1)	1

C18	9401(4)	6960(3)	4074(3)	28(1)	1

C19	10362(3)	6867(3)	336(3)	26(1)	1

C20	9686(4)	7719(3)	(34(3)	29(1)	1

C21	9182(4)	8067(4)	(942(4)	30(1)	1

C22	9353(4)	7569(4)	(1550(4)	35(1)	1

C23	10017(4)	6726(4)	(1231(4)	35(1)	1

C24	10494(4)	6385(3)	(306(4)	30(1)	1

C25	11829(4)	5610(3)	1657(3)	27(1)	1

C26	11873(4)	4574(4)	2429(3)	28(1)	1

C27	12740(4)	3948(4)	2504(4)	32(1)	1

C28	13646(4)	4344(4)	1807(4)	35(1)	1

C29	13661(4)	5362(4)	1024(4)	37(1)	1

C30	12767(4)	5954(4)	973(4)	32(1)	1

C31	11434(3)	7436(3)	1582(3)	25(1)	1

C32	11791(4)	8416(4)	747(3)	29(1)	1

C33	12357(4)	9158(4)	856(4)	32(1)	1

C34	12591(4)	8970(4)	1836(4)	32(1)	1

C35	12269(4)	8014(4)	2700(4)	30(1)	1

C36	11732(4)	7285(3)	2545(3)	28(1)	1

B1	8231(4)	6505(4)	2888(4)	27(1)	1

B2	10872(4)	6478(4)	1465(4)	28(1)	1

F2	6569(2)	7912(2)	2864(2)	31(1)	1

F3	5082(2)	8726(2)	1516(2)	42(1)	1

F4	5048(2)	8288(2)	(128(2)	51(1)	1

F5	6557(2)	6992(2)	(368(2)	45(1)	1

F6	8005(2)	6121(2)	995(2)	34(1)	1

F8	7286(2)	6481(2)	4939(2)	34(1)	1

F9	5947(2)	5031(2)	6425(2)	42(1)	1

F10	5332(2)	3305(2)	6272(2)	45(1)	1

F11	6069(2)	3101(2)	4543(2)	44(1)	1

F12	7398(2)	4545(2)	3016(2)	37(1)	1

F14	8400(2)	8914(2)	1699(2)	30(1)	1

F15	9454(2)	10128(2)	2224(2)	41(1)	1

F16	10557(2)	9299(2)	3953(2)	48(1)	1

F17	10511(2)	7173(2)	5212(2)	41(1)	1

F18	9399(2)	5914(2)	4740(2)	32(1)	1

F20	9486(2)	8246(2)	523(2)	34(1)	1

F21	8527(2)	8887(2)	(1236(2)	41(1)	1

F22	8890(3)	7905(2)	(2454(2)	52(1)	1

F23	10218(3)	6234(2)	(1827(2)	50(1)	1

F24	11118(2)	5532(2)	(55(2)	38(1)	1

F26	11034(2)	4100(2)	3179(2)	34(1)	1

F27	12715(2)	2941(2)	3281(2)	41(1)	1

F28	14509(2)	3740(2)	1896(2)	51(1)	1

F29	14540(2)	5782(2)	316(2)	52(1)	1

F30	12829(2)	6946(2)	141(2)	40(1)	1

F32	11644(2)	8677(2)	(265(2)	37(1)	1

F33	12717(2)	10068(2)	9(2)	42(1)	1

F34	13136(2)	9697(2)	1966(2)	42(1)	1

F35	12503(2)	7830(2)	3665(2)	39(1)	1

F36	11495(2)	6347(2)	3416(2)	32(1)	1

P1	9552(1)	5806(1)	2548(1)	25(1)	1

C41	4880(5)	9598(4)	3398(4)	45(1)	1

C42	4479(5)	10701(4)	2943(4)	51(2)	1

C43	6042(4)	11915(4)	2145(4)	42(1)	1

C44	6765(4)	12516(4)	2475(4)	44(1)	1

C45	8081(4)	11276(4)	3433(5)	55(2)	1

C46	8092(4)	10350(5)	4506(5)	54(2)	1

C47	7043(4)	8980(4)	4446(4)	40(1)	1

C48	5932(4)	8478(4)	4819(4)	36(1)	1

Li41	5914(7)	10778(7)	4373(6)	37(2)	1

O41	5120(2)	9276(2)	4469(2)	35(1)	1

O42	5252(3)	11378(3)	3032(3)	46(1)	1

O43	7125(3)	11825(3)	3481(3)	46(1)	1

O44	7096(3)	9736(3)	4828(3)	43(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(C6	1.392(6)

C1(C2	1.401(6)

C1(B1	1.641(7)

C2(F2	1.355(5)

C2(C3	1.368(6)

C3(F3	1.352(6)

C3(C4	1.381(7)

C4(F4	1.355(6)

C4(C5	1.375(7)

C5(F5	1.342(5)

C5(C6	1.380(7)

C6(F6	1.355(5)

C7(C8	1.388(6)

C7(C12	1.389(7)

C7(B1	1.663(7)

C8(F8	1.364(6)

C8(C9	1.383(7)

C9(F9	1.354(5)

C9(C10	1.368(7)

C10(F10	1.344(6)

C10(C11	1.381(7)

C11(F11	1.337(6)

C11(C12	1.391(7)

C12(F12	1.355(5)

C13(C18	1.389(6)

C13(C14	1.394(7)

C13(B1	1.646(7)

C14(F14	1.347(5)

C14(C15	1.376(7)

C15(F15	1.349(6)

C15(C16	1.378(7)

C16(F16	1.344(5)

C16(C17	1.367(7)

C17(F17	1.347(5)

C17(C18	1.373(7)

C18(F18	1.353(6)

C19(C24	1.392(7)

C19(C20	1.393(7)

C19(B2	1.647(7)

C20(F20	1.347(5)

C20(C21	1.377(7)

C21(F21	1.344(5)

C21(C22	1.373(7)

C22(F22	1.348(5)

C22(C23	1.375(7)

C23(F23	1.352(6)

C23(C24	1.382(7)

C24(F24	1.361(6)

C25(C26	1.386(7)

C25(C30	1.390(7)

C25(B2	1.661(7)

C26(F26	1.361(5)

C26(C27	1.376(7)

C27(F27	1.353(6)

C27(C28	1.373(7)

C28(F28	1.350(5)

C28(C29	1.367(7)

C29(F29	1.357(6)

C29(C30	1.380(7)

C30(F30	1.367(6)

C31(C36	1.392(6)

C31(C32	1.403(7)

C31(B2	1.637(8)

C32(F32	1.359(5)

C32(C33	1.362(7)

C33(F33	1.351(6)

C33(C34	1.373(7)

C34(F34	1.347(6)

C34(C35	1.388(7)

C35(F35	1.353(5)

C35(C36	1.363(7)

C36(F36	1.358(6)

B1(P1	2.057(6)

B2(P1	2.058(6)

P1(H1A	1.3000

P1(H1B	1.3000

C41(O41	1.455(6)

C41(C42	1.504(8)

C41(H41A	0.9900

C41(H41B	0.9900

C42(O42	1.435(7)

C42(H42A	0.9900

C42(H42B	0.9900

C43(O42	1.439(6)

C43(C44	1.507(7)

C43(H43A	0.9900

C43(H43B	0.9900

C44(O43	1.437(6)

C44(H44A	0.9900

C44(H44B	0.9900

C45(O43	1.436(6)

C45(C46	1.500(8)

C45(H45A	0.9900

C45(H45B	0.9900

C46(O44	1.440(6)

C46(H46A	0.9900

C46(H46B	0.9900

C47(O44	1.435(6)

C47(C48	1.501(7)

C47(H47A	0.9900

C47(H47B	0.9900

C48(O41	1.455(6)

C48(H48A	0.9900

C48(H48B	0.9900

Li41(O42	1.974(9)

Li41(O41i	1.988(9)

Li41(O44	2.011(9)

Li41(O43	2.022(10)

Li41(O41	2.325(10)

Li41(Li41i	3.008(18)

O41(Li41i	1.988(9)

C6(C1(C2	114.1(4)

C6(C1(B1	126.5(4)

C2(C1(B1	118.9(4)

F2(C2(C3	116.7(4)

F2(C2(C1	119.2(4)

C3(C2(C1	124.2(4)

F3(C3(C2	120.4(4)

F3(C3(C4	120.5(4)

C2(C3(C4	119.1(5)

F4(C4(C5	121.0(5)

F4(C4(C3	119.4(5)

C5(C4(C3	119.6(5)

F5(C5(C4	120.0(4)

F5(C5(C6	120.3(5)

C4(C5(C6	119.7(5)

F6(C6(C5	115.7(4)

F6(C6(C1	121.0(4)

C5(C6(C1	123.3(4)

C8(C7(C12	112.9(4)

C8(C7(B1	126.1(4)

C12(C7(B1	120.3(4)

F8(C8(C9	113.6(4)

F8(C8(C7	120.8(4)

C9(C8(C7	125.5(5)

F9(C9(C10	119.4(4)

F9(C9(C8	121.6(4)

C10(C9(C8	119.0(4)

F10(C10(C9	120.6(5)

F10(C10(C11	120.4(5)

C9(C10(C11	118.9(4)

F11(C11(C10	119.8(4)

F11(C11(C12	120.4(5)

C10(C11(C12	119.8(5)

F12(C12(C7	120.5(4)

F12(C12(C11	115.6(4)

C7(C12(C11	123.8(5)

C18(C13(C14	113.4(4)

C18(C13(B1	121.6(4)

C14(C13(B1	124.9(4)

F14(C14(C15	114.3(4)

F14(C14(C13	122.0(4)

C15(C14(C13	123.6(4)

F15(C15(C14	120.4(4)

F15(C15(C16	120.0(4)

C14(C15(C16	119.6(4)

F16(C16(C17	120.9(5)

F16(C16(C15	119.5(4)

C17(C16(C15	119.6(5)

F17(C17(C16	119.8(5)

F17(C17(C18	121.3(4)

C16(C17(C18	118.8(4)

F18(C18(C17	115.5(4)

F18(C18(C13	119.6(4)

C17(C18(C13	124.9(4)

C24(C19(C20	113.5(4)

C24(C19(B2	126.0(4)

C20(C19(B2	120.5(4)

F20(C20(C21	116.3(4)

F20(C20(C19	119.2(4)

C21(C20(C19	124.5(5)

F21(C21(C22	119.8(4)

F21(C21(C20	120.8(4)

C22(C21(C20	119.4(4)

F22(C22(C21	120.8(4)

F22(C22(C23	120.2(5)

C21(C22(C23	119.0(4)

F23(C23(C22	120.2(4)

F23(C23(C24	119.7(4)

C22(C23(C24	120.0(5)

F24(C24(C23	115.2(4)

F24(C24(C19	121.3(4)

C23(C24(C19	123.6(4)

C26(C25(C30	112.4(4)

C26(C25(B2	130.4(4)

C30(C25(B2	117.2(4)

F26(C26(C27	115.0(4)

F26(C26(C25	121.0(4)

C27(C26(C25	124.0(5)

F27(C27(C28	119.3(4)

F27(C27(C26	120.2(4)

C28(C27(C26	120.5(4)

F28(C28(C29	120.6(5)

F28(C28(C27	120.6(4)

C29(C28(C27	118.8(4)

F29(C29(C28	120.7(4)

F29(C29(C30	120.8(4)

C28(C29(C30	118.6(5)

F30(C30(C29	114.8(4)

F30(C30(C25	119.4(4)

C29(C30(C25	125.8(4)

C36(C31(C32	112.9(4)

C36(C31(B2	121.2(4)

C32(C31(B2	125.5(4)

F32(C32(C33	114.2(4)

F32(C32(C31	121.5(4)

C33(C32(C31	124.2(4)

F33(C33(C32	121.0(4)

F33(C33(C34	119.2(4)

C32(C33(C34	119.7(4)

F34(C34(C33	120.9(4)

F34(C34(C35	119.8(4)

C33(C34(C35	119.3(5)

F35(C35(C36	122.1(4)

F35(C35(C34	119.2(4)

C36(C35(C34	118.7(4)

F36(C36(C35	115.4(4)

F36(C36(C31	119.5(4)

C35(C36(C31	125.1(4)

C1(B1(C13	116.7(4)

C1(B1(C7	104.3(4)

C13(B1(C7	112.8(4)

C1(B1(P1	115.8(3)

C13(B1(P1	99.5(3)

C7(B1(P1	107.7(3)

C31(B2(C19	113.6(4)

C31(B2(C25	105.1(4)

C19(B2(C25	112.8(4)

C31(B2(P1	111.7(3)

C19(B2(P1	102.8(3)

C25(B2(P1	110.9(3)

B1(P1(B2	129.8(2)

B1(P1(H1A	104.8

B2(P1(H1A	104.8

B1(P1(H1B	104.8

B2(P1(H1B	104.8

H1A(P1(H1B	105.8

O41(C41(C42	108.4(4)

O41(C41(H41A	110.0

C42(C41(H41A	110.0

O41(C41(H41B	110.0

C42(C41(H41B	110.0

H41A(C41(H41B	108.4

O42(C42(C41	109.5(5)

O42(C42(H42A	109.8

C41(C42(H42A	109.8

O42(C42(H42B	109.8

C41(C42(H42B	109.8

H42A(C42(H42B	108.2

O42(C43(C44	104.7(4)

O42(C43(H43A	110.8

C44(C43(H43A	110.8

O42(C43(H43B	110.8

C44(C43(H43B	110.8

H43A(C43(H43B	108.9

O43(C44(C43	110.1(4)

O43(C44(H44A	109.6

C43(C44(H44A	109.6

O43(C44(H44B	109.6

C43(C44(H44B	109.6

H44A(C44(H44B	108.2

O43(C45(C46	105.6(5)

O43(C45(H45A	110.6

C46(C45(H45A	110.6

O43(C45(H45B	110.6

C46(C45(H45B	110.6

H45A(C45(H45B	108.7

O44(C46(C45	111.5(5)

O44(C46(H46A	109.3

C45(C46(H46A	109.3

O44(C46(H46B	109.3

C45(C46(H46B	109.3

H46A(C46(H46B	108.0

O44(C47(C48	105.5(4)

O44(C47(H47A	110.6

C48(C47(H47A	110.6

O44(C47(H47B	110.6

C48(C47(H47B	110.6

H47A(C47(H47B	108.8

O41(C48(C47	110.5(4)

O41(C48(H48A	109.6

C47(C48(H48A	109.6

O41(C48(H48B	109.6

C47(C48(H48B	109.6

H48A(C48(H48B	108.1

O42(Li41(O41i	111.1(4)

O42(Li41(O44	127.9(4)

O41i(Li41(O44	115.3(4)

O42(Li41(O43	82.9(4)

O41i(Li41(O43	130.9(5)

O44(Li41(O43	84.3(4)

O42(Li41(O41	79.0(3)

O41i(Li41(O41	91.9(4)

O44(Li41(O41	77.1(3)

O43(Li41(O41	137.2(4)

O42(Li41(Li41i	95.2(4)

O41i(Li41(Li41i	50.6(3)

O44(Li41(Li41i	96.3(4)

O43(Li41(Li41i	177.9(5)

O41(Li41(Li41i	41.3(2)

C41(O41(C48	112.9(4)

C41(O41(Li41i	125.8(4)

C48(O41(Li41i	113.9(4)

C41(O41(Li41	104.0(4)

C48(O41(Li41	105.7(3)

Li41i(O41(Li41	88.1(4)

C42(O42(C43	116.4(4)

C42(O42(Li41	115.5(4)

C43(O42(Li41	111.6(4)

C45(O43(C44	114.4(4)

C45(O43(Li41	109.8(4)

C44(O43(Li41	108.7(4)

C47(O44(C46	114.4(4)

C47(O44(Li41	112.9(4)

C46(O44(Li41	106.1(4)

Symmetry transformations used to generate equivalent atoms:

(i) (x+1,(y+2,(z+1

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	25(2) 	27(3)	20(2) 	(6(2)	4(2) 	(9(2)

C2	23(2) 	26(2)	19(2) 	(5(2)	1(2) 	(5(2)

C3	25(3) 	30(3)	33(3) 	(9(2)	3(2) 	(4(2)

C4	35(3) 	42(3)	26(3) 	(7(2)	(6(2) 	(7(2)

C5	35(3) 	40(3)	23(3) 	(12(2)	2(2) 	(13(2)

C6	27(3) 	28(3)	25(2) 	(11(2)	6(2) 	(8(2)

C7	25(2) 	24(3)	23(2) 	(6(2)	(2(2) 	0(2)

C8	25(2) 	27(3)	26(3) 	(11(2)	(2(2) 	2(2)

C9	25(3) 	38(3)	24(3) 	(12(2)	3(2) 	3(2)

C10	28(3) 	29(3)	27(3) 	(3(2)	3(2) 	(6(2)

C11	32(3) 	24(3)	33(3) 	(7(2)	(2(2) 	(4(2)

C12	31(3) 	30(3)	23(2) 	(10(2)	1(2) 	(1(2)

C13	23(2) 	24(2)	20(2) 	(8(2)	4(2) 	(2(2)

C14	25(2) 	29(3)	20(2) 	(9(2)	2(2) 	1(2)

C15	29(3) 	25(3)	31(3) 	(11(2)	5(2) 	(7(2)

C16	36(3) 	35(3)	36(3) 	(23(2)	2(2) 	(10(2)

C17	26(3) 	40(3)	25(3) 	(9(2)	(2(2) 	(3(2)

C18	26(3) 	23(3)	26(3) 	(6(2)	0(2) 	3(2)

C19	22(2) 	23(2)	23(2) 	(4(2)	5(2) 	(8(2)

C20	31(3) 	25(3)	26(3) 	(10(2)	5(2) 	(6(2)

C21	27(3) 	24(3)	31(3) 	(6(2)	(2(2) 	(1(2)

C22	41(3) 	37(3)	21(2) 	(7(2)	(6(2) 	(6(2)

C23	45(3) 	30(3)	28(3) 	(13(2)	(2(2) 	(5(2)

C24	28(3) 	23(3)	27(3) 	(5(2)	5(2) 	(4(2)

C25	30(3) 	26(3)	23(2) 	(10(2)	(3(2) 	0(2)

C26	31(3) 	31(3)	22(2) 	(12(2)	(1(2) 	0(2)

C27	39(3) 	29(3)	24(2) 	(8(2)	(5(2) 	3(2)

C28	34(3) 	33(3)	41(3) 	(18(2)	(7(2) 	13(2)

C29	30(3) 	36(3)	41(3) 	(17(3)	5(2) 	1(2)

C30	39(3) 	26(3)	25(3) 	(7(2)	3(2) 	3(2)

C31	24(2) 	23(2)	22(2) 	(7(2)	3(2) 	2(2)

C32	32(3) 	31(3)	20(2) 	(8(2)	(1(2) 	(1(2)

C33	36(3) 	22(3)	29(3) 	(3(2)	(8(2) 	2(2)

C34	30(3) 	27(3)	38(3) 	(15(2)	(6(2) 	1(2)

C35	26(3) 	32(3)	26(3) 	(11(2)	(5(2) 	5(2)

C36	30(3) 	23(3)	26(3) 	(7(2)	(1(2) 	1(2)

B1	28(3) 	26(3)	22(3) 	(9(2)	6(2) 	2(2)

B2	30(3) 	26(3)	18(3) 	(4(2)	5(2) 	(3(2)

F2	32(2) 	32(2)	28(1) 	(14(1)	(1(1) 	2(1)

F3	32(2) 	48(2)	41(2) 	(16(1)	(6(1) 	7(1)

F4	44(2) 	66(2)	35(2) 	(15(2)	(17(1) 	4(2)

F5	44(2) 	66(2)	32(2) 	(27(2)	(3(1) 	(8(2)

F6	35(2) 	39(2)	30(2) 	(19(1)	4(1) 	(4(1)

F8	39(2) 	33(2)	30(2) 	(15(1)	3(1) 	(1(1)

F9	43(2) 	51(2)	28(2) 	(18(1)	9(1) 	(8(1)

F10	40(2) 	45(2)	33(2) 	(6(1)	10(1) 	(16(1)

F11	47(2) 	34(2)	45(2) 	(17(1)	6(1) 	(16(1)

F12	42(2) 	38(2)	35(2) 	(22(1)	9(1) 	(14(1)

F14	35(2) 	24(1)	25(1) 	(6(1)	(4(1) 	0(1)

F15	53(2) 	23(2)	41(2) 	(10(1)	(3(1) 	(7(1)

F16	55(2) 	45(2)	50(2) 	(26(2)	(10(2) 	(13(2)

F17	42(2) 	51(2)	27(2) 	(14(1)	(8(1) 	(5(1)

F18	37(2) 	27(2)	25(1) 	(7(1)	(4(1) 	1(1)

F20	38(2) 	31(2)	30(2) 	(13(1)	(1(1) 	4(1)

F21	40(2) 	37(2)	38(2) 	(10(1)	(10(1) 	10(1)

F22	67(2) 	52(2)	39(2) 	(20(2)	(23(2) 	6(2)

F23	72(2) 	50(2)	39(2) 	(31(2)	(13(2) 	8(2)

F24	49(2) 	28(2)	37(2) 	(15(1)	(7(1) 	7(1)

F26	38(2) 	29(2)	26(1) 	(5(1)	3(1) 	3(1)

F27	51(2) 	29(2)	33(2) 	(5(1)	(9(1) 	11(1)

F28	39(2) 	51(2)	56(2) 	(21(2)	(5(2) 	18(2)

F29	37(2) 	50(2)	57(2) 	(19(2)	14(2) 	2(1)

F30	40(2) 	31(2)	34(2) 	(5(1)	13(1) 	(2(1)

F32	43(2) 	31(2)	26(1) 	(4(1)	(2(1) 	(9(1)

F33	49(2) 	27(2)	34(2) 	(1(1)	(6(1) 	(12(1)

F34	46(2) 	31(2)	50(2) 	(18(1)	(16(1) 	(2(1)

F35	44(2) 	38(2)	33(2) 	(14(1)	(10(1) 	(1(1)

F36	38(2) 	26(1)	22(1) 	(4(1)	(2(1) 	(2(1)

P1	29(1) 	21(1)	22(1) 	(7(1)	3(1) 	(2(1)

C41	60(4) 	46(3)	40(3) 	(26(3)	(19(3) 	8(3)

C42	57(4) 	51(4)	41(3) 	(19(3)	(9(3) 	(5(3)

C43	60(4) 	36(3)	23(3) 	(11(2)	7(2) 	(4(3)

C44	45(3) 	34(3)	40(3) 	(8(3)	6(3) 	(6(3)

C45	34(3) 	53(4)	74(4) 	(29(3)	0(3) 	(1(3)

C46	38(3) 	62(4)	68(4) 	(35(4)	(14(3) 	1(3)

C47	35(3) 	39(3)	39(3) 	(15(3)	2(2) 	7(2)

C48	41(3) 	31(3)	31(3) 	(10(2)	(2(2) 	5(2)

Li41	37(5) 	45(5)	31(5) 	(20(4)	4(4) 	3(4)

O41	35(2) 	37(2)	30(2) 	(14(2)	(2(2) 	2(2)

O42	51(2) 	44(2)	31(2) 	(8(2)	(2(2) 	(16(2)

O43	41(2) 	44(2)	50(2) 	(22(2)	1(2) 	1(2)

O44	34(2) 	49(2)	49(2) 	(23(2)	(8(2) 	4(2)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H1A	9155	5115	2321	30	1

H1B	9952	5268	3441	30	1

H41A	4323	9114	3396	54	1

H41B	5537	9574	2970	54	1

H42A	4367	10958	2194	61	1

H42B	3779	10707	3325	61	1

H43A	5693	12401	1514	50	1

H43B	6457	11406	1988	50	1

H44A	7395	12826	1945	53	1

H44B	6367	13098	2516	53	1

H45A	8732	11738	3258	65	1

H45B	8060	11038	2894	65	1

H46A	8698	9899	4501	65	1

H46B	8210	10603	5020	65	1

H47A	7597	8446	4733	48	1

H47B	7160	9331	3669	48	1

H48A	5826	7978	4540	43	1

H48B	5851	8078	5596	43	1