|  | University of Southampton · Department of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	02src455

Empirical formula 	C34H34O2S2

Formula weight 	538.73

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	C2/c

Unit cell dimensions	a = 21.0182(4) Å	( = 90°

b = 5.48710(10) Å	( = 91.0170(10)°

c = 24.2168(5) Å	(  = 90°

Volume	2792.46(9) Å3

Z	4

Density (calculated)	1.281 Mg / m3

Absorption coefficient	0.221 mm(1

F(000)	1144

Crystal	Block; Colourless

Crystal size	0.40 ( 0.35 ( 0.20 mm3

( range for data collection	3.37 ( 25.03°

Index ranges	(24 ( h ( 24, (6 ( k ( 6, (28 ( l ( 28

Reflections collected	8799

Independent reflections	2457 [Rint = 0.0375]

Completeness to ( = 25.03°	99.6 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9572 and 0.9169

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	2457 / 0 / 240

Goodness-of-fit on F2	1.054

Final R indices [F2 > 2((F2)]	R1 = 0.0343, wR2 = 0.0856

R indices (all data)	R1 = 0.0402, wR2 = 0.0889

Largest diff. peak and hole	0.307 and (0.313 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

S1	1814(1)	8283(1)	3945(1)	26(1)	1

O1	1299(1)	2726(2)	5249(1)	32(1)	1

C3	1209(1)	6707(3)	4852(1)	22(1)	1

C2	1806(1)	6135(3)	4529(1)	22(1)	1

C16	3017(1)	8236(3)	3518(1)	25(1)	1

C11	2442(1)	7022(3)	3554(1)	23(1)	1

C6	432(1)	3488(3)	6082(1)	24(1)	1

C1	2425(1)	6261(3)	4872(1)	23(1)	1

C4	1042(1)	4707(3)	5257(1)	22(1)	1

C15	3498(1)	7304(3)	3191(1)	28(1)	1

C12	2358(1)	4845(3)	3267(1)	26(1)	1

C5	534(1)	5201(3)	5670(1)	21(1)	1

C14	3414(1)	5151(3)	2898(1)	25(1)	1

C13	2837(1)	3928(3)	2944(1)	28(1)	1

C9	(315(1)	7632(4)	6041(1)	32(1)	1

C10	159(1)	7296(3)	5654(1)	27(1)	1

C7	(36(1)	3848(4)	6468(1)	31(1)	1

C17	3929(1)	4159(4)	2533(1)	34(1)	1

C8	(410(1)	5919(4)	6445(1)	32(1)	1

Table 3. Bond lengths [Å] and angles [°].

S1(C11	1.7767(17)

S1(C2	1.8426(17)

O1(C4	1.214(2)

C3(C4	1.517(2)

C3(C2	1.523(2)

C3(H3B	0.993(19)

C3(H3A	1.000(19)

C2(C1	1.532(2)

C2(H2	0.992(18)

C16(C11	1.385(2)

C16(C15	1.391(2)

C16(H16	0.94(2)

C11(C12	1.392(2)

C6(C7	1.383(3)

C6(C5	1.391(2)

C6(H6	0.92(2)

C1(C1i	1.525(3)

C1(H1B	0.985(18)

C1(H1A	0.971(18)

C4(C5	1.499(2)

C15(C14	1.388(3)

C15(H15	0.97(2)

C12(C13	1.381(2)

C12(H12	0.96(2)

C5(C10	1.394(2)

C14(C13	1.393(3)

C14(C17	1.510(2)

C13(H13	0.94(2)

C9(C8	1.375(3)

C9(C10	1.392(3)

C9(H9	0.94(2)

C10(H10	0.92(2)

C7(C8	1.383(3)

C7(H7	0.95(2)

C17(H17B	0.94(3)

C17(H17A	0.95(2)

C17(H17C	1.01(3)

C8(H8	0.96(2)

C11(S1(C2	100.23(8)

C4(C3(C2	112.64(14)

C4(C3(H3B	111.1(10)

C2(C3(H3B	110.1(10)

C4(C3(H3A	104.6(11)

C2(C3(H3A	110.4(11)

H3B(C3(H3A	107.8(15)

C3(C2(C1	114.35(14)

C3(C2(S1	106.39(11)

C1(C2(S1	111.54(12)

C3(C2(H2	108.0(10)

C1(C2(H2	108.8(10)

S1(C2(H2	107.5(10)

C11(C16(C15	120.11(17)

C11(C16(H16	119.2(11)

C15(C16(H16	120.7(11)

C16(C11(C12	119.00(16)

C16(C11(S1	120.20(14)

C12(C11(S1	120.77(13)

C7(C6(C5	120.61(17)

C7(C6(H6	120.3(12)

C5(C6(H6	119.1(12)

C1i(C1(C2	115.38(17)

C1i(C1(H1B	111.6(11)

C2(C1(H1B	107.0(10)

C1i(C1(H1A	110.8(10)

C2(C1(H1A	106.5(10)

H1B(C1(H1A	105.0(14)

O1(C4(C5	119.68(15)

O1(C4(C3	121.92(15)

C5(C4(C3	118.38(14)

C14(C15(C16	121.21(17)

C14(C15(H15	119.6(12)

C16(C15(H15	119.1(12)

C13(C12(C11	120.55(16)

C13(C12(H12	120.4(11)

C11(C12(H12	119.0(11)

C6(C5(C10	118.84(16)

C6(C5(C4	118.48(15)

C10(C5(C4	122.68(15)

C15(C14(C13	118.15(16)

C15(C14(C17	121.42(17)

C13(C14(C17	120.42(17)

C12(C13(C14	120.96(17)

C12(C13(H13	119.1(12)

C14(C13(H13	120.0(12)

C8(C9(C10	120.26(18)

C8(C9(H9	120.1(12)

C10(C9(H9	119.6(12)

C9(C10(C5	120.15(17)

C9(C10(H10	121.1(12)

C5(C10(H10	118.7(12)

C8(C7(C6	120.09(18)

C8(C7(H7	119.1(14)

C6(C7(H7	120.7(14)

C14(C17(H17B	110.0(15)

C14(C17(H17A	111.3(13)

H17B(C17(H17A	107(2)

C14(C17(H17C	110.6(14)

H17B(C17(H17C	111(2)

H17A(C17(H17C	107.0(19)

C9(C8(C7	120.04(17)

C9(C8(H8	119.5(12)

C7(C8(H8	120.5(12)

Symmetry transformations used to generate equivalent atoms:

(i) (x+1/2,(y+3/2,(z+1

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

S1	23(1) 	33(1)	21(1) 	5(1)	2(1) 	6(1)

O1	33(1) 	23(1)	40(1) 	0(1)	10(1) 	4(1)

C3	19(1) 	23(1)	24(1) 	(1(1)	0(1) 	1(1)

C2	23(1) 	23(1)	21(1) 	1(1)	1(1) 	2(1)

C16	27(1) 	25(1)	23(1) 	(1(1)	(1(1) 	(2(1)

C11	23(1) 	27(1)	17(1) 	5(1)	(1(1) 	2(1)

C6	20(1) 	24(1)	29(1) 	1(1)	(1(1) 	(1(1)

C1	19(1) 	27(1)	22(1) 	5(1)	2(1) 	4(1)

C4	19(1) 	21(1)	24(1) 	(2(1)	(3(1) 	(2(1)

C15	22(1) 	35(1)	26(1) 	1(1)	1(1) 	(4(1)

C12	25(1) 	29(1)	25(1) 	2(1)	(2(1) 	(6(1)

C5	17(1) 	21(1)	24(1) 	(2(1)	(3(1) 	(3(1)

C14	26(1) 	31(1)	18(1) 	4(1)	(3(1) 	5(1)

C13	33(1) 	26(1)	24(1) 	(2(1)	(2(1) 	1(1)

C9	23(1) 	31(1)	43(1) 	(7(1)	6(1) 	4(1)

C10	26(1) 	23(1)	33(1) 	3(1)	2(1) 	(1(1)

C7	26(1) 	39(1)	28(1) 	2(1)	2(1) 	(8(1)

C17	32(1) 	46(1)	24(1) 	(1(1)	3(1) 	9(1)

C8	23(1) 	41(1)	33(1) 	(7(1)	7(1) 	(6(1)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H1B	2769(8)	5710(30)	4632(7)	23(4)	1

H3B	1256(9)	8300(30)	5042(7)	26(5)	1

H2	1760(8)	4470(30)	4374(7)	20(4)	1

H3A	831(9)	6820(30)	4597(8)	29(5)	1

H1A	2394(8)	5020(30)	5155(7)	21(4)	1

H10	231(9)	8440(40)	5383(9)	36(5)	1

H16	3073(9)	9720(40)	3707(8)	28(5)	1

H6	685(9)	2110(40)	6098(8)	31(5)	1

H13	2768(9)	2470(40)	2751(8)	31(5)	1

H12	1958(9)	3990(40)	3294(8)	32(5)	1

H8	(735(10)	6190(40)	6715(8)	39(6)	1

H9	(569(10)	9050(40)	6026(8)	39(6)	1

H15	3902(10)	8130(40)	3183(8)	38(5)	1

H7	(112(11)	2670(40)	6745(9)	46(6)	1

H17B	3995(11)	2500(50)	2608(10)	59(7)	1

H17A	3811(10)	4280(40)	2155(10)	47(6)	1

H17C	4334(12)	5110(50)	2585(10)	64(7)	1