|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	2005src1337

Empirical formula 	C14H8CuN4S2

Formula weight 	359.90

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Orthorhombic

Space group 	Pbcn

Unit cell dimensions	a = 7.52250(10) Å	( = 90°

b = 24.7605(7) Å	( = 90°

c = 7.5372(2) Å	(  = 90°

Volume	1403.89(6) Å3

Z	4

Density (calculated)	1.703 Mg / m3

Absorption coefficient	1.849 mm(1

F(000)	724

Crystal	Needle; Dark Brown

Crystal size	0.24 ( 0.03 ( 0.02 mm3

( range for data collection	3.16 ( 27.47°

Index ranges	(9 ( h ( 9, (30 ( k ( 32, (9 ( l ( 9

Reflections collected	19394

Independent reflections	1608 [Rint = 0.0395]

Completeness to ( = 27.47°	99.6 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9640 and 0.6653

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	1608 / 0 / 96

Goodness-of-fit on F2	1.200

Final R indices [F2 > 2((F2)]	R1 = 0.0291, wR2 = 0.0689

R indices (all data)	R1 = 0.0341, wR2 = 0.0717

Largest diff. peak and hole	0.416 and (0.335 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SADABS Version 2.10. (G. M. Sheldrick (2003)) Bruker AXS Inc., Madison, Wisconsin, USA. Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP3 for Windows (L. J. Farrugia, J. Appl. Crystallogr. 1997, 30, 565).

Special details:

All hydrogen atoms were fixed.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	(779(3)	(1041(1)	2036(3)	17(1)	1

C2	(1611(3)	(1542(1)	1559(3)	19(1)	1

C11	879(3)	1305(1)	2946(3)	17(1)	1

C12	1777(3)	1772(1)	3421(3)	21(1)	1

C13	3403(3)	1730(1)	4277(3)	23(1)	1

C14	4078(3)	1222(1)	4643(3)	24(1)	1

C15	3114(3)	775(1)	4123(3)	21(1)	1

N1	(2304(3)	(1936(1)	1157(3)	26(1)	1

N11	1553(2)	809(1)	3293(2)	17(1)	1

S1	(1838(1)	(451(1)	1384(1)	19(1)	1

Cu1	0	187(1)	2500	16(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(C1i	1.365(4)

C1(C2	1.435(3)

C1(S1	1.736(2)

C2(N1	1.147(3)

C11(N11	1.354(3)

C11(C12	1.386(3)

C11(C11i	1.484(4)

C12(C13	1.386(3)

C12(H12	0.9500

C13(C14	1.383(3)

C13(H13	0.9500

C14(C15	1.380(3)

C14(H14	0.9500

C15(N11	1.333(3)

C15(H15	0.9500

N11(Cu1	2.0229(18)

S1(Cu1	2.2609(6)

Cu1(N11i	2.0229(18)

Cu1(S1i	2.2609(6)

C1i(C1(C2	120.19(12)

C1i(C1(S1	122.62(7)

C2(C1(S1	117.19(16)

N1(C2(C1	178.5(2)

N11(C11(C12	121.6(2)

N11(C11(C11i	114.91(12)

C12(C11(C11i	123.48(13)

C11(C12(C13	119.2(2)

C11(C12(H12	120.4

C13(C12(H12	120.4

C14(C13(C12	118.9(2)

C14(C13(H13	120.5

C12(C13(H13	120.5

C15(C14(C13	118.7(2)

C15(C14(H14	120.7

C13(C14(H14	120.7

N11(C15(C14	123.0(2)

N11(C15(H15	118.5

C14(C15(H15	118.5

C15(N11(C11	118.51(18)

C15(N11(Cu1	126.83(15)

C11(N11(Cu1	114.65(14)

C1(S1(Cu1	101.67(7)

N11(Cu1(N11i	80.87(10)

N11(Cu1(S1	174.00(5)

N11i(Cu1(S1	93.93(5)

N11(Cu1(S1i	93.93(5)

N11i(Cu1(S1i	174.00(5)

S1(Cu1(S1i	91.41(3)

Symmetry transformations used to generate equivalent atoms:

(i) (x,y,(z+1/2

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	19(1) 	12(1)	19(1) 	0(1)	(1(1) 	(1(1)

C2	19(1) 	16(1)	24(1) 	1(1)	(2(1) 	3(1)

C11	20(1) 	14(1)	16(1) 	0(1)	0(1) 	1(1)

C12	25(1) 	13(1)	26(1) 	0(1)	(1(1) 	(1(1)

C13	26(1) 	17(1)	27(1) 	(2(1)	(2(1) 	(5(1)

C14	20(1) 	21(1)	30(1) 	(1(1)	(5(1) 	(2(1)

C15	20(1) 	17(1)	25(1) 	0(1)	(5(1) 	2(1)

N1	27(1) 	17(1)	32(1) 	0(1)	(6(1) 	(2(1)

N11	18(1) 	12(1)	21(1) 	(1(1)	(1(1) 	0(1)

S1	20(1) 	12(1)	26(1) 	0(1)	(6(1) 	0(1)

Cu1	17(1) 	10(1)	23(1) 	0	(4(1) 	0

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H12	1285	2116	3162	25	1

H13	4043	2045	4608	28	1

H14	5182	1182	5240	28	1

H15	3585	427	4368	25	1