|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	04src0949_90    (H3OFe(24))

Empirical formula 	H6Fe3O15S2

Formula weight 	477.72

Temperature 	90(2) K

Wavelength 	0.71073 Å

Crystal system 	Rhombohedral

Space group 	R(3

Unit cell dimensions	a = 7.3218(10) Å	( = 90°

b = 7.3218(10) Å	( = 90°

c = 16.881(3) Å	(  = 120°

Volume	783.7(2) Å3

Z	3

Density (calculated)	3.037 Mg / m3

Absorption coefficient	4.603 mm(1

F(000)	708

Crystal	cube; orange

Crystal size	0.08 ( 0.08 ( 0.08 mm3

( range for data collection	3.43 ( 27.47°

Index ranges	(9 ( h ( 9, (9 ( k ( 9, (21 ( l ( 19

Reflections collected	3462

Independent reflections	252 [Rint = 0.0246]

Completeness to ( = 27.47°	100.0 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.7096 and 0.7096

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	252 / 0 / 27

Goodness-of-fit on F2	1.218

Final R indices [F2 > 2((F2)]	R1 = 0.0197, wR2 = 0.0516

R indices (all data)	R1 = 0.0201, wR2 = 0.0524

Extinction coefficient	0.0049(7)

Largest diff. peak and hole	0.510 and (0.499 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

Fe1	3333	1667	1667	6(1)	1

S1	6667	3333	248(1)	4(1)	1

O1	4471(3)	2236(2)	542(1)	7(1)	1

O2	1275(2)	(1275(2)	1352(1)	10(1)	1

O3	6667	3333	(614(2)	8(1)	1

O4	0	0	0	23(1)	1

Table 3. Bond lengths [Å] and angles [°].

Fe1(O2i	1.9865(8)

Fe1(O2ii	1.9865(8)

Fe1(O2	1.9865(8)

Fe1(O2iii	1.9865(8)

Fe1(O1	2.0311(17)

Fe1(O1iii	2.0311(17)

S1(O3	1.454(3)

S1(O1iv	1.4783(18)

S1(O1v	1.4783(18)

S1(O1	1.4783(18)

O2(Fe1vi	1.9865(8)

O2i(Fe1(O2ii	180.0

O2i(Fe1(O2	90.35(11)

O2ii(Fe1(O2	89.65(11)

O2i(Fe1(O2iii	89.65(11)

O2ii(Fe1(O2iii	90.35(11)

O2(Fe1(O2iii	180.0

O2i(Fe1(O1	90.95(6)

O2ii(Fe1(O1	89.06(6)

O2(Fe1(O1	89.06(6)

O2iii(Fe1(O1	90.95(6)

O2i(Fe1(O1iii	89.06(6)

O2ii(Fe1(O1iii	90.94(6)

O2(Fe1(O1iii	90.94(6)

O2iii(Fe1(O1iii	89.05(6)

O1(Fe1(O1iii	180.0

O3(S1(O1iv	109.65(7)

O3(S1(O1v	109.65(7)

O1iv(S1(O1v	109.29(8)

O3(S1(O1	109.65(7)

O1iv(S1(O1	109.29(8)

O1v(S1(O1	109.29(8)

S1(O1(Fe1	130.45(11)

Fe1vi(O2(Fe1	134.27(10)

Symmetry transformations used to generate equivalent atoms:

(i) y+2/3,(x+y+1/3,(z+1/3    (ii) (y,x(y,z    (iii) (x+2/3,(y+1/3,(z+1/3

(iv)  (y+1,x(y,z    (v) (x+y+1,(x+1,z    (vi) (x+y,(x,z

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

Fe1	5(1) 	7(1)	6(1) 	1(1)	1(1) 	3(1)

S1	5(1) 	5(1)	2(1) 	0	0 	3(1)

O1	5(1) 	10(1)	5(1) 	0(1)	1(1) 	2(1)

O2	5(1) 	5(1)	19(1) 	(4(1)	4(1) 	2(1)

O3	12(1) 	12(1)	1(1) 	0	0 	6(1)

O4	26(2) 	26(2)	18(3) 	0	0 	13(1)