|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	04src0951_295    (KFe)

Empirical formula 	H6Fe3KO14S2

Formula weight 	500.82

Temperature 	295(2) K

Wavelength 	0.71073 Å

Crystal system 	Rombohedral

Space group 	R(3m

Unit cell dimensions	a = 7.3003(10) Å	( = 90°

b = 7.3003(10) Å	( = 90°

c = 17.216(3) Å	(  = 120°

Volume	794.6(2) Å3

Z	3

Density (calculated)	3.140 Mg / m3

Absorption coefficient	4.924 mm(1

F(000)	741

Crystal	cube; orange

Crystal size	0.05 ( 0.05 ( 0.05 mm3

( range for data collection	4.00 ( 27.49°

Index ranges	(9 ( h ( 9, (9 ( k ( 8, (22 ( l ( 19

Reflections collected	2190

Independent reflections	252 [Rint = 0.0320]

Completeness to ( = 27.49°	98.8 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.7908 and 0.7908

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	252 / 0 / 27

Goodness-of-fit on F2	1.090

Final R indices [F2 > 2((F2)]	R1 = 0.0230, wR2 = 0.0603

R indices (all data)	R1 = 0.0241, wR2 = 0.0609

Extinction coefficient	0.0021(6)

Largest diff. peak and hole	0.499 and (0.521 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

Fe1	3333	1667	1667	8(1)	1

S1	6667	3333	251(1)	7(1)	1

O1	1270(2)	(1270(2)	1356(1)	10(1)	1

O2	4464(3)	2232(2)	543(1)	11(1)	1

O3	6667	3333	(595(2)	12(1)	1

K1	0	0	0	18(1)	1

Table 3. Bond lengths [Å] and angles [°].

Fe1(O1i	1.9802(9)

Fe1(O1ii	1.9802(9)

Fe1(O1	1.9802(9)

Fe1(O1iii	1.9802(9)

Fe1(O2	2.063(2)

Fe1(O2iii	2.063(2)

Fe1(K1	3.5601(4)

Fe1(K1iv	3.5601(4)

S1(O3	1.457(4)

S1(O2v	1.480(2)

S1(O2vi	1.480(2)

S1(O2	1.480(2)

O1(Fe1vii	1.9802(9)

O1(K1	2.833(2)

O2(K1	2.973(2)

K1(O1ii	2.833(2)

K1(O1viii	2.833(2)

K1(O1vii	2.833(2)

K1(O1ix	2.833(2)

K1(O1(x) 	2.833(2)

K1(O2ix	2.973(2)

K1(O2(x) 	2.973(2)

K1(O2ii	2.973(2)

K1(O2vii	2.973(2)

K1(O2viii	2.973(2)

O1i(Fe1(O1ii	180.0

O1i(Fe1(O1	90.82(14)

O1ii(Fe1(O1	89.18(14)

O1i(Fe1(O1iii	89.18(14)

O1ii(Fe1(O1iii	90.82(14)

O1(Fe1(O1iii	180.0

O1i(Fe1(O2	91.43(7)

O1ii(Fe1(O2	88.57(7)

O1(Fe1(O2	88.57(7)

O1iii(Fe1(O2	91.43(7)

O1i(Fe1(O2iii	88.57(7)

O1ii(Fe1(O2iii	91.43(7)

O1(Fe1(O2iii	91.43(7)

O1iii(Fe1(O2iii	88.57(7)

O2(Fe1(O2iii	180.0

O1i(Fe1(K1	127.43(7)

O1ii(Fe1(K1	52.57(7)

O1(Fe1(K1	52.57(7)

O1iii(Fe1(K1	127.43(7)

O2(Fe1(K1	56.57(6)

O2iii(Fe1(K1	123.43(6)

O1i(Fe1(K1iv	52.57(7)

O1ii(Fe1(K1iv	127.43(7)

O1(Fe1(K1iv	127.43(7)

O1iii(Fe1(K1iv	52.57(7)

O2(Fe1(K1iv	123.43(6)

O2iii(Fe1(K1iv	56.57(6)

K1(Fe1(K1iv	180.0

O3(S1(O2v	109.81(9)

O3(S1(O2vi	109.81(9)

O2v(S1(O2vi	109.13(9)

O3(S1(O2	109.81(9)

O2v(S1(O2	109.13(9)

O2vi(S1(O2	109.13(9)

Fe1vii(O1(Fe1	134.34(12)

Fe1vii(O1(K1	93.71(7)

Fe1(O1(K1	93.71(7)

S1(O2(Fe1	130.09(13)

S1(O2(K1	141.86(12)

Fe1(O2(K1	88.05(7)

O1ii(K1(O1viii	180.00(11)

O1ii(K1(O1vii	58.77(8)

O1viii(K1(O1vii	121.23(8)

O1ii(K1(O1	58.77(8)

O1viii(K1(O1	121.23(8)

O1vii(K1(O1	58.77(8)

O1ii(K1(O1ix	121.23(8)

O1viii(K1(O1ix	58.77(8)

O1vii(K1(O1ix	121.23(8)

O1(K1(O1ix	180.00(7)

O1ii(K1(O1(x) 	121.23(8)

O1viii(K1(O1(x) 	58.77(8)

O1vii(K1(O1(x) 	180.00(17)

O1(K1(O1(x) 	121.23(8)

O1ix(K1(O1(x) 	58.77(8)

O1ii(K1(O2	58.13(3)

O1viii(K1(O2	121.87(3)

O1vii(K1(O2	106.19(6)

O1(K1(O2	58.13(3)

O1ix(K1(O2	121.87(3)

O1(x) (K1(O2	73.81(6)

O1ii(K1(O2ix	121.87(3)

O1viii(K1(O2ix	58.13(3)

O1vii(K1(O2ix	73.81(6)

O1(K1(O2ix	121.87(3)

O1ix(K1(O2ix	58.13(3)

O1(x) (K1(O2ix	106.19(6)

O2(K1(O2ix	180.00(9)

O1ii(K1(O2(x) 	73.81(6)

O1viii(K1(O2(x) 	106.19(6)

O1vii(K1(O2(x) 	121.87(3)

O1(K1(O2(x) 	121.87(3)

O1ix(K1(O2(x) 	58.13(3)

O1(x) (K1(O2(x) 	58.13(3)

O2(K1(O2(x) 	69.41(4)

O2ix(K1(O2(x) 	110.59(4)

O1ii(K1(O2ii	58.13(3)

O1viii(K1(O2ii	121.87(3)

O1vii(K1(O2ii	58.13(3)

O1(K1(O2ii	106.19(6)

O1ix(K1(O2ii	73.81(6)

O1(x) (K1(O2ii	121.87(3)

O2(K1(O2ii	110.59(4)

O2ix(K1(O2ii	69.41(4)

O2(x) (K1(O2ii	69.41(4)

O1ii(K1(O2vii	106.19(6)

O1viii(K1(O2vii	73.81(6)

O1vii(K1(O2vii	58.13(3)

O1(K1(O2vii	58.13(3)

O1ix(K1(O2vii	121.87(3)

O1(x) (K1(O2vii	121.87(3)

O2(K1(O2vii	110.59(4)

O2ix(K1(O2vii	69.41(4)

O2(x) (K1(O2vii	180.0

O2ii(K1(O2vii	110.59(4)

O1ii(K1(O2viii	121.87(3)

O1viii(K1(O2viii	58.13(3)

O1vii(K1(O2viii	121.87(3)

O1(K1(O2viii	73.81(6)

O1ix(K1(O2viii	106.19(6)

O1(x) (K1(O2viii	58.13(3)

O2(K1(O2viii	69.41(4)

O2ix(K1(O2viii	110.59(4)

O2(x) (K1(O2viii	110.59(4)

O2ii(K1(O2viii	180.00(8)

O2vii(K1(O2viii	69.41(4)

Symmetry transformations used to generate equivalent atoms:

(i) y+2/3,(x+y+1/3,(z+1/3    (ii) (y,x(y,z    (iii) (x+2/3,(y+1/3,(z+1/3

(iv)  x+2/3,y+1/3,z+1/3    (v) (y+1,x(y,z    (vi) (x+y+1,(x+1,z

(vii) (x+y,(x,z    (viii) y,(x+y,(z    (xi) (x,(y,(z    (x)  x(y,x,(z

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

Fe1	5(1) 	7(1)	10(1) 	0(1)	0(1) 	3(1)

S1	7(1) 	7(1)	6(1) 	0	0 	4(1)

O1	8(1) 	8(1)	14(1) 	(2(1)	2(1) 	4(1)

O2	7(1) 	14(1)	11(1) 	1(1)	2(1) 	3(1)

O3	16(1) 	16(1)	4(2) 	0	0 	8(1)

K1	22(1) 	22(1)	10(1) 	0	0 	11(1)