|  | University of Southampton · Department of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	02SRC630

Empirical formula 	C16H34N2O2

Formula weight 	286.45

Temperature 	120(2) K

Wavelength 	0.71069 Å

Crystal system 	Monoclininc

Space group 	C2/c

Unit cell dimensions	a = 25.225(5) Å

b = 6.279(5) Å	( = 94.662(5)°

c = 10.921(5) Å

Volume	1724.0(16) Å3

Z	4

Density (calculated)	1.104 Mg / m3

Absorption coefficient	0.072 mm(1

F(000)	640

## Crystal	Colourless Block

Crystal size	0.10 ( 0.03 ( 0.03 mm3

( range for data collection	3.24 ( 23.25°

Index ranges	(25 ( h ( 27, (6 ( k ( 6, (12 ( l ( 12

Reflections collected	5130

Independent reflections	1223 [Rint = 0.0538]

Completeness to ( = 23.25°	99.5 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9978 and 0.9929

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	1223 / 60 / 96

Goodness-of-fit on F2	1.841

Final R indices [F2 > 2((F2)]	R1 = 0.1400, wR2 = 0.4541

R indices (all data)	R1 = 0.1944, wR2 = 0.4999

Extinction coefficient	0.004(8)

Largest diff. peak and hole	0.578 and (0.369 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:  All hydrogen atoms were placed in idealised positions and refined using a riding model.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

N1	9677(3)	1217(17)	785(8)	126(4)	1

O1	9378(2)	3549(10)	2885(6)	101(3)	1

C1	8028(4)	2700(20)	1205(10)	125(4)	1

C2	8306(3)	2454(15)	3427(8)	87(3)	1

C3	8426(3)	5797(16)	2294(9)	96(3)	1

C4	8446(3)	3416(13)	2210(7)	73(3)	1

C5	9010(4)	2740(30)	1942(12)	147(6)	1

C6	9151(5)	1960(40)	1045(18)	237(11)	1

C7	9705(4)	(1100(20)	797(9)	129(5)	1

C8	10232(5)	(1923(19)	438(11)	127(5)	1

Table 3. Bond lengths [Å] and angles [°].

N1(C8i	1.443(17)

N1(C6	1.456(15)

N1(C7	1.458(14)

O1(C5	1.423(10)

C1(C4	1.527(11)

C2(C4	1.528(12)

C3(C4	1.499(12)

C4(C5	1.533(13)

C5(C6	1.177(16)

C7(C8	1.507(15)

C8(N1i	1.443(17)

C8i(N1(C6	107.3(12)

C8i(N1(C7	107.7(7)

C6(N1(C7	111.2(14)

C3(C4(C1	108.1(8)

C3(C4(C2	109.2(7)

C1(C4(C2	108.3(8)

C3(C4(C5	109.0(9)

C1(C4(C5	112.3(7)

C2(C4(C5	109.9(9)

C6(C5(O1	121.8(10)

C6(C5(C4	128.5(10)

O1(C5(C4	108.9(7)

C5(C6(N1	129.7(12)

N1(C7(C8	112.5(11)

N1i(C8(C7	110.2(8)

Symmetry transformations used to generate equivalent atoms:

(i) (x+2,(y,(z

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

N1	75(5) 	194(9)	104(7) 	(99(6)	(25(4) 	65(5)

O1	54(4) 	153(6)	95(5) 	(43(4)	3(3) 	2(3)

C1	61(6) 	218(11)	95(7) 	(62(7)	3(5) 	(4(6)

C2	61(5) 	107(7)	92(7) 	(3(5)	7(4) 	3(4)

C3	63(6) 	137(9)	86(6) 	12(5)	4(4) 	(3(5)

C4	54(5) 	108(7)	59(5) 	(24(4)	13(3) 	0(4)

C5	51(6) 	273(14)	119(8) 	(126(9)	12(5) 	1(7)

C6	77(8) 	430(20)	198(15) 	(212(17)	(29(9) 	87(11)

C7	85(7) 	218(13)	81(7) 	(71(8)	(18(5) 	37(8)

C8	112(8) 	165(9)	94(8) 	(78(7)	(47(6) 	63(7)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H1	9611	2624	3074	151	1

H1A	7674	3128	1426	187	1

H1B	8041	1150	1120	187	1

H1C	8100	3372	425	187	1

H2A	8557	2973	4093	130	1

H2B	8328	898	3382	130	1

H2C	7944	2873	3586	130	1

H3A	8067	6241	2468	143	1

H3B	8514	6420	1514	143	1

H3C	8682	6286	2956	143	1

H5	8980	1336	2361	177	1

H6A	9048	2991	382	284	1

H6B	8916	712	888	284	1

H7A	9417	(1679	222	155	1

H7B	9646	(1621	1631	155	1

H8A	10522	(1397	1028	152	1

H8B	10234	(3499	467	152	1