|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	2005src1438 / NDC90

Empirical formula 	C45H27BF24FeO3

Formula weight 	1138.33

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/c

Unit cell dimensions	a = 12.1544(3) Å	( = 90°

b = 19.3432(5) Å	( = 104.4350(10)°

c = 20.2595(3) Å	(  = 90°

Volume	4612.74(18) Å3

Z	4

Density (calculated)	1.639 Mg / m3

Absorption coefficient	0.465 mm(1

F(000)	2272

Crystal	Blade; Light Yellow

Crystal size	0.22 ( 0.16 ( 0.02 mm3

( range for data collection	2.96 ( 27.48°

Index ranges	(15 ( h ( 15, (25 ( k ( 25, (26 ( l ( 26

Reflections collected	56541

Independent reflections	10558 [Rint = 0.0523]

Completeness to ( = 27.48°	99.8 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9908 and 0.9046

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	10558 / 793 / 701

Goodness-of-fit on F2	1.027

Final R indices [F2 > 2((F2)]	R1 = 0.0483, wR2 = 0.1061

R indices (all data)	R1 = 0.0672, wR2 = 0.1150

Largest diff. peak and hole	0.574 and (0.550 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SADABS Version 2.10. (G. M. Sheldrick (2003)) Bruker AXS Inc., Madison, Wisconsin, USA. Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP3 for Windows (L. J. Farrugia, J. Appl. Crystallogr. 1997, 30, 565).

Special details:

All hydrogen atoms were fixed

One of the trifluoromethyl groups was disordered over two positions.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	5667(2)	9560(1)	2090(1)	25(1)	1

C2	6273(2)	8930(1)	2095(1)	23(1)	1

C3	6460(2)	8632(1)	2757(1)	22(1)	1

C4	6015(2)	9099(1)	3173(1)	22(1)	1

C5	5510(2)	9663(1)	2763(1)	25(1)	1

C6	5340(3)	10057(2)	1507(2)	42(1)	1

C7	6707(3)	8650(2)	1518(1)	39(1)	1

C8	7128(2)	7988(1)	2998(2)	38(1)	1

C9	6140(2)	9027(2)	3925(1)	34(1)	1

C10	4984(3)	10280(1)	3013(2)	44(1)	1

C11	3377(2)	9196(2)	2031(1)	35(1)	1

C12	4395(2)	8094(2)	1684(1)	38(1)	1

C13	4239(2)	8234(1)	2974(1)	27(1)	1

O11	2567(2)	9499(1)	1823(1)	56(1)	1

O12	4213(2)	7699(1)	1259(1)	59(1)	1

O13	4000(2)	7928(1)	3395(1)	37(1)	1

Fe1	4706(1)	8742(1)	2347(1)	21(1)	1

C21	(1402(2)	7409(1)	158(1)	17(1)	1

C22	(2232(2)	7872(1)	(178(1)	18(1)	1

C23	(3366(2)	7823(1)	(140(1)	20(1)	1

C24	(3706(2)	7311(1)	239(1)	19(1)	1

C25	(2887(2)	6845(1)	586(1)	18(1)	1

C26	(1768(2)	6894(1)	545(1)	18(1)	1

C27	(4204(2)	8339(1)	(518(1)	25(1)	1

C28	(3252(2)	6298(1)	1006(1)	24(1)	1

C31	356(2)	6743(1)	(167(1)	17(1)	1

C32	(362(2)	6215(1)	(481(1)	17(1)	1

C33	25(2)	5637(1)	(767(1)	17(1)	1

C34	1168(2)	5562(1)	(740(1)	19(1)	1

C35	1906(2)	6080(1)	(430(1)	20(1)	1

C36	1511(2)	6660(1)	(161(1)	19(1)	1

C37	(803(2)	5112(1)	(1136(1)	20(1)	1

C38	3149(2)	5980(1)	(369(1)	30(1)	1

C41	604(2)	7512(1)	980(1)	18(1)	1

C42	1358(2)	7032(1)	1358(1)	21(1)	1

C43	1776(2)	7093(1)	2067(1)	23(1)	1

C44	1453(2)	7638(1)	2416(1)	25(1)	1

C45	713(2)	8130(1)	2047(1)	23(1)	1

C46	303(2)	8067(1)	1349(1)	22(1)	1

C47	2609(2)	6572(1)	2445(1)	30(1)	1

C48	348(2)	8707(1)	2430(1)	33(1)	1

C51	235(2)	8095(1)	(279(1)	20(1)	1

C52	1010(2)	8623(1)	(26(1)	27(1)	1

C53	1211(2)	9163(1)	(435(1)	36(1)	1

C54	633(2)	9205(1)	(1112(1)	34(1)	1

C55	(136(2)	8691(1)	(1380(1)	27(1)	1

C56	(313(2)	8144(1)	(976(1)	21(1)	1

C57	2050(3)	9715(2)	(133(2)	58(1)	1

C58	(827(2)	8737(1)	(2102(1)	34(1)	1

B21	(44(2)	7441(1)	165(1)	18(1)	1

F21	(3943(1)	8982(1)	(308(1)	44(1)	1

F22	(4276(2)	8332(1)	(1186(1)	48(1)	1

F23	(5258(1)	8229(1)	(459(1)	50(1)	1

F24	(3714(2)	6569(1)	1485(1)	52(1)	1

F25	(4038(1)	5879(1)	626(1)	49(1)	1

F26	(2418(1)	5889(1)	1333(1)	30(1)	1

F31	(1459(1)	5363(1)	(1722(1)	36(1)	1

F32	(1533(1)	4904(1)	(777(1)	32(1)	1

F33	(310(1)	4544(1)	(1295(1)	37(1)	1

F34	3360(1)	5739(1)	(945(1)	47(1)	1

F35	3605(1)	5517(1)	112(1)	54(1)	1

F36	3747(1)	6561(1)	(219(1)	41(1)	1

F41	2437(2)	5939(1)	2190(1)	53(1)	1

F42	3682(1)	6727(1)	2427(1)	42(1)	1

F43	2641(2)	6543(1)	3108(1)	54(1)	1

F44	(214(2)	8478(1)	2874(1)	60(1)	1

F45	(316(2)	9168(1)	2030(1)	64(1)	1

F46	1223(2)	9067(1)	2801(1)	49(1)	1

F51A	2991(2)	9457(2)	284(2)	84(1)	0.855(6)

F52A	1672(3)	10136(2)	272(2)	94(1)	0.855(6)

F53A	2410(4)	10072(2)	(588(1)	120(2)	0.855(6)

F51B	2253(16)	9821(10)	484(6)	68(5)	0.145(6)

F52B	1669(11)	10348(5)	(422(8)	50(4)	0.145(6)

F53B	2999(11)	9638(9)	(308(11)	77(5)	0.145(6)

F54	(415(2)	9167(1)	(2475(1)	107(1)	1

F55	(1888(2)	8923(1)	(2136(1)	81(1)	1

F56	(939(2)	8135(1)	(2425(1)	53(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(C2	1.422(3)

C1(C5	1.438(3)

C1(C6	1.498(3)

C1(Fe1	2.108(2)

C2(C3	1.425(3)

C2(C7	1.498(3)

C2(Fe1	2.122(2)

C3(C4	1.432(3)

C3(C8	1.500(3)

C3(Fe1	2.097(2)

C4(C5	1.415(3)

C4(C9	1.500(3)

C4(Fe1	2.116(2)

C5(C10	1.500(3)

C5(Fe1	2.104(2)

C6(H6A	0.9800

C6(H6B	0.9800

C6(H6C	0.9800

C7(H7A	0.9800

C7(H7B	0.9800

C7(H7C	0.9800

C8(H8A	0.9800

C8(H8B	0.9800

C8(H8C	0.9800

C9(H9A	0.9800

C9(H9B	0.9800

C9(H9C	0.9800

C10(H10A	0.9800

C10(H10B	0.9800

C10(H10C	0.9800

C11(O11	1.132(3)

C11(Fe1	1.810(3)

C12(O12	1.131(3)

C12(Fe1	1.807(3)

C13(O13	1.133(3)

C13(Fe1	1.806(3)

C21(C22	1.393(3)

C21(C26	1.406(3)

C21(B21	1.648(3)

C22(C23	1.402(3)

C22(H22	0.9500

C23(C24	1.378(3)

C23(C27	1.494(3)

C24(C25	1.395(3)

C24(H24	0.9500

C25(C26	1.386(3)

C25(C28	1.493(3)

C26(H26	0.9500

C27(F21	1.328(3)

C27(F23	1.333(3)

C27(F22	1.334(3)

C28(F26	1.326(3)

C28(F25	1.340(3)

C28(F24	1.342(3)

C31(C32	1.391(3)

C31(C36	1.411(3)

C31(B21	1.635(3)

C32(C33	1.393(3)

C32(H32	0.9500

C33(C34	1.384(3)

C33(C37	1.493(3)

C34(C35	1.387(3)

C34(H34	0.9500

C35(C36	1.384(3)

C35(C38	1.497(3)

C36(H36	0.9500

C37(F33	1.329(3)

C37(F32	1.341(2)

C37(F31	1.344(3)

C38(F36	1.331(3)

C38(F35	1.337(3)

C38(F34	1.341(3)

C41(C42	1.392(3)

C41(C46	1.408(3)

C41(B21	1.649(3)

C42(C43	1.403(3)

C42(H42	0.9500

C43(C44	1.379(3)

C43(C47	1.497(3)

C44(C45	1.394(3)

C44(H44	0.9500

C45(C46	1.381(3)

C45(C48	1.489(3)

C46(H46	0.9500

C47(F41	1.325(3)

C47(F43	1.336(3)

C47(F42	1.347(3)

C48(F45	1.332(3)

C48(F44	1.333(3)

C48(F46	1.336(3)

C51(C52	1.397(3)

C51(C56	1.406(3)

C51(B21	1.636(3)

C52(C53	1.393(3)

C52(H52	0.9500

C53(C54	1.380(4)

C53(C57	1.497(4)

C54(C55	1.379(3)

C54(H54	0.9500

C55(C56	1.388(3)

C55(C58	1.497(3)

C56(H56	0.9500

C57(F51B	1.230(12)

C57(F53B	1.297(12)

C57(F52A	1.318(5)

C57(F53A	1.311(4)

C57(F51A	1.338(5)

C57(F52B	1.386(11)

C58(F54	1.303(3)

C58(F55	1.324(3)

C58(F56	1.326(3)

C2(C1(C5	107.6(2)

C2(C1(C6	126.2(2)

C5(C1(C6	126.0(2)

C2(C1(Fe1	70.89(13)

C5(C1(Fe1	69.89(13)

C6(C1(Fe1	128.48(18)

C1(C2(C3	108.4(2)

C1(C2(C7	125.9(2)

C3(C2(C7	125.6(2)

C1(C2(Fe1	69.83(13)

C3(C2(Fe1	69.31(12)

C7(C2(Fe1	129.59(17)

C2(C3(C4	107.64(19)

C2(C3(C8	126.1(2)

C4(C3(C8	125.8(2)

C2(C3(Fe1	71.20(13)

C4(C3(Fe1	70.87(12)

C8(C3(Fe1	128.88(17)

C5(C4(C3	108.23(19)

C5(C4(C9	125.9(2)

C3(C4(C9	125.7(2)

C5(C4(Fe1	69.93(13)

C3(C4(Fe1	69.40(12)

C9(C4(Fe1	129.75(16)

C4(C5(C1	108.1(2)

C4(C5(C10	125.0(2)

C1(C5(C10	126.8(2)

C4(C5(Fe1	70.89(13)

C1(C5(Fe1	70.19(13)

C10(C5(Fe1	127.88(18)

C1(C6(H6A	109.5

C1(C6(H6B	109.5

H6A(C6(H6B	109.5

C1(C6(H6C	109.5

H6A(C6(H6C	109.5

H6B(C6(H6C	109.5

C2(C7(H7A	109.5

C2(C7(H7B	109.5

H7A(C7(H7B	109.5

C2(C7(H7C	109.5

H7A(C7(H7C	109.5

H7B(C7(H7C	109.5

C3(C8(H8A	109.5

C3(C8(H8B	109.5

H8A(C8(H8B	109.5

C3(C8(H8C	109.5

H8A(C8(H8C	109.5

H8B(C8(H8C	109.5

C4(C9(H9A	109.5

C4(C9(H9B	109.5

H9A(C9(H9B	109.5

C4(C9(H9C	109.5

H9A(C9(H9C	109.5

H9B(C9(H9C	109.5

C5(C10(H10A	109.5

C5(C10(H10B	109.5

H10A(C10(H10B	109.5

C5(C10(H10C	109.5

H10A(C10(H10C	109.5

H10B(C10(H10C	109.5

O11(C11(Fe1	177.4(3)

O12(C12(Fe1	178.2(3)

O13(C13(Fe1	176.0(2)

C13(Fe1(C12	95.82(12)

C13(Fe1(C11	95.93(11)

C12(Fe1(C11	94.04(13)

C13(Fe1(C3	97.66(10)

C12(Fe1(C3	103.14(11)

C11(Fe1(C3	156.82(11)

C13(Fe1(C5	112.00(10)

C12(Fe1(C5	151.08(11)

C11(Fe1(C5	90.89(11)

C3(Fe1(C5	66.60(9)

C13(Fe1(C1	150.83(10)

C12(Fe1(C1	111.29(11)

C11(Fe1(C1	92.81(11)

C3(Fe1(C1	66.61(9)

C5(Fe1(C1	39.92(9)

C13(Fe1(C4	85.82(9)

C12(Fe1(C4	142.27(11)

C11(Fe1(C4	123.37(11)

C3(Fe1(C4	39.73(9)

C5(Fe1(C4	39.17(9)

C1(Fe1(C4	66.26(9)

C13(Fe1(C2	136.15(10)

C12(Fe1(C2	88.53(11)

C11(Fe1(C2	127.35(11)

C3(Fe1(C2	39.48(9)

C5(Fe1(C2	66.19(9)

C1(Fe1(C2	39.28(9)

C4(Fe1(C2	65.93(9)

C22(C21(C26	115.89(19)

C22(C21(B21	125.55(19)

C26(C21(B21	118.49(18)

C21(C22(C23	122.1(2)

C21(C22(H22	119.0

C23(C22(H22	119.0

C24(C23(C22	121.0(2)

C24(C23(C27	120.3(2)

C22(C23(C27	118.7(2)

C23(C24(C25	118.01(19)

C23(C24(H24	121.0

C25(C24(H24	121.0

C26(C25(C24	120.8(2)

C26(C25(C28	121.25(19)

C24(C25(C28	117.92(19)

C25(C26(C21	122.2(2)

C25(C26(H26	118.9

C21(C26(H26	118.9

F21(C27(F23	106.2(2)

F21(C27(F22	106.5(2)

F23(C27(F22	105.61(19)

F21(C27(C23	112.53(18)

F23(C27(C23	113.3(2)

F22(C27(C23	112.20(19)

F26(C28(F25	105.80(19)

F26(C28(F24	106.16(19)

F25(C28(F24	106.54(19)

F26(C28(C25	114.11(18)

F25(C28(C25	111.83(19)

F24(C28(C25	111.87(19)

C32(C31(C36	115.43(19)

C32(C31(B21	125.33(18)

C36(C31(B21	119.23(18)

C31(C32(C33	122.76(19)

C31(C32(H32	118.6

C33(C32(H32	118.6

C34(C33(C32	120.50(19)

C34(C33(C37	119.56(19)

C32(C33(C37	119.87(18)

C33(C34(C35	118.2(2)

C33(C34(H34	120.9

C35(C34(H34	120.9

C36(C35(C34	121.00(19)

C36(C35(C38	120.9(2)

C34(C35(C38	118.1(2)

C35(C36(C31	122.1(2)

C35(C36(H36	118.9

C31(C36(H36	118.9

F33(C37(F32	106.46(18)

F33(C37(F31	106.77(18)

F32(C37(F31	105.07(17)

F33(C37(C33	113.26(18)

F32(C37(C33	112.78(18)

F31(C37(C33	111.93(17)

F36(C38(F35	107.2(2)

F36(C38(F34	106.3(2)

F35(C38(F34	105.5(2)

F36(C38(C35	113.1(2)

F35(C38(C35	111.9(2)

F34(C38(C35	112.3(2)

C42(C41(C46	116.0(2)

C42(C41(B21	125.47(19)

C46(C41(B21	118.22(19)

C41(C42(C43	121.8(2)

C41(C42(H42	119.1

C43(C42(H42	119.1

C44(C43(C42	120.8(2)

C44(C43(C47	119.6(2)

C42(C43(C47	119.5(2)

C43(C44(C45	118.3(2)

C43(C44(H44	120.8

C45(C44(H44	120.8

C46(C45(C44	120.6(2)

C46(C45(C48	121.4(2)

C44(C45(C48	117.9(2)

C45(C46(C41	122.3(2)

C45(C46(H46	118.8

C41(C46(H46	118.8

F41(C47(F43	108.4(2)

F41(C47(F42	104.8(2)

F43(C47(F42	104.5(2)

F41(C47(C43	113.7(2)

F43(C47(C43	112.9(2)

F42(C47(C43	111.9(2)

F45(C48(F44	107.3(2)

F45(C48(F46	105.6(2)

F44(C48(F46	105.3(2)

F45(C48(C45	113.4(2)

F44(C48(C45	111.9(2)

F46(C48(C45	112.6(2)

C52(C51(C56	115.3(2)

C52(C51(B21	125.2(2)

C56(C51(B21	119.48(19)

C53(C52(C51	122.1(2)

C53(C52(H52	118.9

C51(C52(H52	118.9

C54(C53(C52	121.0(2)

C54(C53(C57	119.4(2)

C52(C53(C57	119.7(2)

C55(C54(C53	118.4(2)

C55(C54(H54	120.8

C53(C54(H54	120.8

C54(C55(C56	120.5(2)

C54(C55(C58	120.1(2)

C56(C55(C58	119.4(2)

C55(C56(C51	122.6(2)

C55(C56(H56	118.7

C51(C56(H56	118.7

F51B(C57(F53B	109.3(11)

F52A(C57(F53A	109.9(4)

F52A(C57(F51A	102.3(3)

F53A(C57(F51A	105.0(4)

F51B(C57(F52B	104.1(10)

F53B(C57(F52B	102.2(10)

F51B(C57(C53	118.5(7)

F53B(C57(C53	111.6(7)

F52A(C57(C53	112.8(3)

F53A(C57(C53	113.6(3)

F51A(C57(C53	112.3(3)

F52B(C57(C53	109.6(5)

F54(C58(F55	107.8(3)

F54(C58(F56	106.3(2)

F55(C58(F56	103.5(2)

F54(C58(C55	113.7(2)

F55(C58(C55	111.6(2)

F56(C58(C55	113.2(2)

C31(B21(C51	106.78(17)

C31(B21(C21	111.37(17)

C51(B21(C21	111.63(17)

C31(B21(C41	111.36(17)

C51(B21(C41	111.92(17)

C21(B21(C41	103.88(17)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	26(1) 	21(1)	27(1) 	4(1)	5(1) 	(3(1)

C2	25(1) 	22(1)	24(1) 	(2(1)	10(1) 	(4(1)

C3	18(1) 	23(1)	26(1) 	2(1)	6(1) 	(2(1)

C4	17(1) 	28(1)	20(1) 	(2(1)	4(1) 	(5(1)

C5	24(1) 	21(1)	33(1) 	(5(1)	10(1) 	(3(1)

C6	48(2) 	33(2)	42(2) 	16(1)	7(1) 	(1(1)

C7	49(2) 	40(2)	36(2) 	(8(1)	25(1) 	(4(1)

C8	31(1) 	34(1)	51(2) 	14(1)	12(1) 	11(1)

C9	28(1) 	50(2)	23(1) 	(4(1)	6(1) 	(12(1)

C10	50(2) 	28(1)	61(2) 	(12(1)	24(2) 	1(1)

C11	26(1) 	42(2)	35(1) 	8(1)	6(1) 	(1(1)

C12	36(1) 	45(2)	34(2) 	(7(1)	8(1) 	(12(1)

C13	23(1) 	24(1)	31(1) 	(4(1)	0(1) 	(6(1)

O11	29(1) 	71(2)	66(2) 	26(1)	7(1) 	16(1)

O12	65(2) 	65(2)	49(1) 	(33(1)	20(1) 	(27(1)

O13	43(1) 	34(1)	33(1) 	2(1)	9(1) 	(14(1)

Fe1	20(1) 	21(1)	21(1) 	0(1)	3(1) 	(1(1)

C21	18(1) 	15(1)	17(1) 	(3(1)	3(1) 	(1(1)

C22	22(1) 	15(1)	17(1) 	(2(1)	3(1) 	(1(1)

C23	19(1) 	19(1)	19(1) 	(3(1)	1(1) 	2(1)

C24	14(1) 	21(1)	21(1) 	(5(1)	4(1) 	(1(1)

C25	21(1) 	16(1)	18(1) 	(2(1)	6(1) 	(2(1)

C26	17(1) 	17(1)	19(1) 	0(1)	2(1) 	1(1)

C27	24(1) 	21(1)	28(1) 	1(1)	1(1) 	2(1)

C28	20(1) 	25(1)	29(1) 	2(1)	8(1) 	0(1)

C31	18(1) 	19(1)	16(1) 	2(1)	4(1) 	(2(1)

C32	15(1) 	20(1)	15(1) 	2(1)	4(1) 	0(1)

C33	17(1) 	19(1)	16(1) 	2(1)	3(1) 	(2(1)

C34	20(1) 	18(1)	21(1) 	2(1)	7(1) 	1(1)

C35	16(1) 	24(1)	21(1) 	2(1)	7(1) 	(2(1)

C36	16(1) 	21(1)	20(1) 	0(1)	4(1) 	(4(1)

C37	20(1) 	19(1)	21(1) 	0(1)	6(1) 	0(1)

C38	20(1) 	30(1)	42(2) 	0(1)	10(1) 	(3(1)

C41	17(1) 	18(1)	21(1) 	(1(1)	7(1) 	(5(1)

C42	19(1) 	21(1)	22(1) 	0(1)	5(1) 	(3(1)

C43	19(1) 	25(1)	23(1) 	3(1)	2(1) 	(6(1)

C44	23(1) 	32(1)	20(1) 	(3(1)	2(1) 	(7(1)

C45	22(1) 	27(1)	23(1) 	(5(1)	8(1) 	(5(1)

C46	19(1) 	23(1)	23(1) 	(2(1)	4(1) 	(2(1)

C47	33(1) 	27(1)	26(1) 	0(1)	(2(1) 	(2(1)

C48	37(1) 	37(1)	27(1) 	(8(1)	9(1) 	(2(1)

C51	21(1) 	19(1)	21(1) 	(1(1)	8(1) 	(2(1)

C52	29(1) 	30(1)	21(1) 	(2(1)	3(1) 	(12(1)

C53	44(2) 	34(1)	30(1) 	(2(1)	7(1) 	(23(1)

C54	45(2) 	29(1)	29(1) 	4(1)	10(1) 	(15(1)

C55	32(1) 	26(1)	22(1) 	1(1)	7(1) 	(6(1)

C56	22(1) 	21(1)	21(1) 	(1(1)	5(1) 	(6(1)

C57	80(2) 	53(2)	38(2) 	1(1)	10(2) 	(48(2)

C58	44(2) 	30(1)	25(1) 	4(1)	6(1) 	(8(1)

B21	17(1) 	18(1)	18(1) 	(1(1)	4(1) 	(2(1)

F21	49(1) 	17(1)	53(1) 	(2(1)	(13(1) 	7(1)

F22	59(1) 	52(1)	25(1) 	4(1)	(2(1) 	26(1)

F23	23(1) 	47(1)	80(1) 	22(1)	9(1) 	11(1)

F24	73(1) 	39(1)	64(1) 	16(1)	56(1) 	15(1)

F25	41(1) 	45(1)	51(1) 	19(1)	(10(1) 	(26(1)

F26	28(1) 	29(1)	33(1) 	12(1)	7(1) 	2(1)

F31	39(1) 	30(1)	27(1) 	6(1)	(11(1) 	(12(1)

F32	32(1) 	32(1)	34(1) 	(4(1)	14(1) 	(15(1)

F33	26(1) 	27(1)	57(1) 	(19(1)	7(1) 	(1(1)

F34	29(1) 	54(1)	65(1) 	(21(1)	28(1) 	(5(1)

F35	22(1) 	59(1)	79(1) 	29(1)	6(1) 	10(1)

F36	19(1) 	37(1)	69(1) 	(11(1)	14(1) 	(9(1)

F41	55(1) 	23(1)	61(1) 	1(1)	(24(1) 	(1(1)

F42	28(1) 	34(1)	57(1) 	0(1)	(2(1) 	4(1)

F43	61(1) 	66(1)	31(1) 	19(1)	4(1) 	16(1)

F44	73(1) 	54(1)	72(1) 	(24(1)	55(1) 	(14(1)

F45	88(2) 	53(1)	43(1) 	(18(1)	2(1) 	36(1)

F46	55(1) 	50(1)	45(1) 	(28(1)	16(1) 	(16(1)

F51A	59(2) 	93(2)	86(2) 	(11(2)	(9(2) 	(52(2)

F52A	104(3) 	57(2)	111(3) 	(43(2)	10(2) 	(37(2)

F53A	166(4) 	139(4)	46(2) 	10(2)	10(2) 	(134(3)

F51B	75(9) 	80(9)	46(5) 	(8(5)	10(5) 	(42(7)

F52B	46(6) 	27(5)	66(8) 	0(5)	(10(5) 	(29(4)

F53B	51(6) 	81(8)	103(10) 	(29(7)	25(6) 	(27(5)

F54	146(2) 	123(2)	31(1) 	35(1)	(17(1) 	(99(2)

F55	72(1) 	125(2)	35(1) 	(5(1)	(8(1) 	56(1)

F56	70(1) 	52(1)	28(1) 	(8(1)	(4(1) 	5(1)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H6A	5972	10375	1517	63	1

H6B	4670	10321	1545	63	1

H6C	5164	9801	1076	63	1

H7A	7456	8848	1537	58	1

H7B	6180	8774	1084	58	1

H7C	6768	8146	1556	58	1

H8A	7001	7651	2625	58	1

H8B	6880	7791	3382	58	1

H8C	7938	8101	3143	58	1

H9A	6804	9290	4172	50	1

H9B	6240	8539	4054	50	1

H9C	5457	9206	4041	50	1

H10A	4552	10129	3336	67	1

H10B	4474	10513	2626	67	1

H10C	5583	10601	3241	67	1

H22	(2023	8233	(441	22	1

H24	(4474	7276	263	23	1

H26	(1230	6569	786	21	1

H32	(1150	6249	(502	20	1

H34	1439	5166	(928	23	1

H36	2035	7013	33	23	1

H42	1596	6653	1130	25	1

H44	1728	7675	2897	30	1

H46	(200	8411	1110	26	1

H52	1414	8613	441	33	1

H54	761	9579	(1388	41	1

H56	(824	7787	(1178	25	1