|  | University of Southampton · Department of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	03SRC0515 ( GRDaT

Empirical formula 	C65H54FeP4

Formula weight 	1014.81

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P-1

Unit cell dimensions	a = 10.99210(10) Å	( = 70.6060(10)°

b = 15.0127(2) Å	( = 79.0650(10)°

c = 17.1197(2) Å	(  = 85.9430(10)°

Volume	2616.33(5) Å3

Z	2

Density (calculated)	1.288 Mg / m3

Absorption coefficient	0.452 mm(1

F(000)	1060

Crystal	Orange Block

Crystal size	0.30 ( 0.20 ( 0.15 mm3

( range for data collection	3.17 ( 25.03°

Index ranges	(13 ( h ( 11, (17 ( k ( 17, (20 ( l ( 20

Reflections collected	17566

Independent reflections	9187 [Rint = 0.0266]

Completeness to ( = 25.03°	99.5 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9353 and 0.8764

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	9187 / 90 / 673

Goodness-of-fit on F2	0.926

Final R indices [F2 > 2((F2)]	R1 = 0.0381, wR2 = 0.1038

R indices (all data)	R1 = 0.0443, wR2 = 0.1090

Largest diff. peak and hole	0.660 and (0.501 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:  All hydrogen atoms were placed in idealised positions and refined using a riding model. Contains a disordered toluene.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C59A	8305(5)	8966(3)	3424(3)	65(2)	0.50

C60A	7261(5)	9024(3)	3060(3)	86(4)	0.50

C61A	6521(4)	8236(4)	3273(3)	53(2)	0.50

C62A	6825(5)	7390(3)	3850(4)	67(3)	0.50

C63A	7868(5)	7331(3)	4214(4)	70(3)	0.50

C64A	8608(4)	8120(4)	4001(3)	106(4)	0.50

C65A	9101(6)	9854(4)	3207(5)	57(2)	0.50

C59B	7449(4)	8149(3)	3623(3)	66(2)	0.50

C60B	7541(5)	9077(3)	3085(3)	49(2)	0.50

C61B	8567(6)	9612(3)	3004(4)	81(3)	0.50

C62B	9502(5)	9219(5)	3463(4)	83(3)	0.50

C63B	9410(5)	8291(5)	4002(4)	112(4)	0.50

C64B	8384(5)	7756(4)	4082(4)	101(4)	0.50

C65B	6335(9)	7503(7)	3755(8)	96(4)	0.50

C1	7518(2)	3016(1)	1560(1)	20(1)	1

C2	8325(2)	2572(1)	2147(1)	19(1)	1

C3	9426(2)	3123(1)	1922(1)	19(1)	1

C4	9280(2)	3928(1)	1204(1)	20(1)	1

C5	8119(2)	3864(1)	986(1)	20(1)	1

C6	7056(2)	5181(1)	2185(1)	21(1)	1

C7	6171(2)	4435(2)	2560(1)	22(1)	1

C8	6587(2)	3772(2)	3270(1)	21(1)	1

C9	7747(2)	4088(1)	3343(1)	20(1)	1

C10	8032(2)	4957(1)	2667(1)	20(1)	1

C11	5277(2)	2168(2)	2593(1)	23(1)	1

C12	4239(2)	2632(2)	2889(2)	26(1)	1

C13	3701(2)	2330(2)	3736(2)	32(1)	1

C14	4200(2)	1568(2)	4296(2)	35(1)	1

C15	5215(2)	1088(2)	4008(2)	33(1)	1

C16	5742(2)	1375(2)	3164(2)	28(1)	1

C17	6398(2)	1568(2)	1224(1)	24(1)	1

C18	5402(2)	1032(2)	1235(2)	33(1)	1

C19	5599(2)	212(2)	1027(2)	39(1)	1

C20	6791(2)	(86(2)	797(2)	34(1)	1

C21	7783(2)	444(2)	769(2)	33(1)	1

C22	7590(2)	1265(2)	986(1)	28(1)	1

C23	11811(2)	3732(2)	1820(1)	21(1)	1

C24	11757(2)	4481(2)	2141(1)	26(1)	1

C25	12532(2)	5254(2)	1741(2)	31(1)	1

C26	13378(2)	5286(2)	1020(1)	28(1)	1

C27	13437(2)	4549(2)	696(1)	27(1)	1

C28	12657(2)	3782(2)	1090(1)	24(1)	1

C29	11330(2)	1818(1)	1942(1)	21(1)	1

C30	11045(2)	1807(2)	1183(1)	28(1)	1

C31	11413(2)	1058(2)	887(2)	32(1)	1

C32	12070(2)	307(2)	1344(2)	34(1)	1

C33	12363(2)	309(2)	2093(2)	35(1)	1

C34	11995(2)	1059(2)	2389(2)	28(1)	1

C35	5604(2)	6811(1)	1574(1)	23(1)	1

C36	5065(2)	7480(2)	946(2)	29(1)	1

C37	3999(2)	7966(2)	1151(2)	36(1)	1

C38	3449(2)	7787(2)	1979(2)	36(1)	1

C39	3964(2)	7124(2)	2608(2)	35(1)	1

C40	5031(2)	6639(2)	2407(2)	30(1)	1

C41	8268(2)	6857(2)	1213(1)	24(1)	1

C42	8193(2)	7540(2)	1600(2)	30(1)	1

C43	9254(3)	8013(2)	1576(2)	42(1)	1

C44	10389(2)	7796(2)	1168(2)	45(1)	1

C45	10477(2)	7116(2)	782(2)	42(1)	1

C46	9424(2)	6654(2)	800(2)	34(1)	1

C47	8095(2)	4217(2)	4883(1)	25(1)	1

C48	6984(3)	4723(2)	4884(2)	40(1)	1

C49	6579(3)	5165(2)	5484(2)	47(1)	1

C50	7286(3)	5115(2)	6082(2)	40(1)	1

C51	8389(3)	4621(2)	6086(2)	40(1)	1

C52	8796(2)	4181(2)	5486(2)	33(1)	1

C53	8099(2)	2411(2)	4691(1)	26(1)	1

C54	7001(2)	2236(2)	5272(2)	38(1)	1

C55	6608(3)	1318(2)	5706(2)	49(1)	1

C56	7295(3)	569(2)	5567(2)	46(1)	1

C57	8371(3)	731(2)	4989(2)	53(1)	1

C58	8783(3)	1651(2)	4552(2)	43(1)	1

P1	6005(1)	2664(1)	1481(1)	21(1)	1

P2	10779(1)	2736(1)	2422(1)	20(1)	1

P3	6955(1)	6160(1)	1224(1)	23(1)	1

P4	8737(1)	3603(1)	4123(1)	22(1)	1

Fe1	7856(1)	3891(1)	2195(1)	17(1)	1

Table 3. Bond lengths [Å] and angles [°].

C59A(C60A	1.3900

C59A(C64A	1.3900

C59A(C65A	1.547(5)

C60A(C61A	1.3900

C61A(C62A	1.3900

C62A(C63A	1.3900

C63A(C64A	1.3900

C59B(C60B	1.3900

C59B(C64B	1.3900

C59B(C65B	1.553(6)

C60B(C61B	1.3900

C61B(C62B	1.3900

C62B(C63B	1.3900

C63B(C64B	1.3900

C1(C2	1.432(3)

C1(C5	1.437(3)

C1(P1	1.822(2)

C1(Fe1	2.054(2)

C2(C3	1.432(3)

C2(Fe1	2.035(2)

C3(C4	1.434(3)

C3(P2	1.820(2)

C3(Fe1	2.072(2)

C4(C5	1.414(3)

C4(Fe1	2.067(2)

C5(Fe1	2.048(2)

C6(C10	1.430(3)

C6(C7	1.433(3)

C6(P3	1.822(2)

C6(Fe1	2.066(2)

C7(C8	1.422(3)

C7(Fe1	2.043(2)

C8(C9	1.432(3)

C8(Fe1	2.052(2)

C9(C10	1.434(3)

C9(P4	1.814(2)

C9(Fe1	2.064(2)

C10(Fe1	2.054(2)

C11(C12	1.396(3)

C11(C16	1.402(3)

C11(P1	1.839(2)

C12(C13	1.391(3)

C13(C14	1.383(4)

C14(C15	1.386(4)

C15(C16	1.383(3)

C17(C22	1.388(3)

C17(C18	1.399(3)

C17(P1	1.842(2)

C18(C19	1.383(3)

C19(C20	1.382(4)

C20(C21	1.379(4)

C21(C22	1.392(3)

C23(C28	1.392(3)

C23(C24	1.399(3)

C23(P2	1.833(2)

C24(C25	1.390(3)

C25(C26	1.387(3)

C26(C27	1.385(3)

C27(C28	1.386(3)

C29(C34	1.390(3)

C29(C30	1.399(3)

C29(P2	1.840(2)

C30(C31	1.386(3)

C31(C32	1.386(3)

C32(C33	1.380(4)

C33(C34	1.388(3)

C35(C40	1.391(3)

C35(C36	1.398(3)

C35(P3	1.835(2)

C36(C37	1.386(3)

C37(C38	1.376(4)

C38(C39	1.382(4)

C39(C40	1.383(3)

C41(C42	1.385(3)

C41(C46	1.398(3)

C41(P3	1.835(2)

C42(C43	1.394(3)

C43(C44	1.383(4)

C44(C45	1.377(4)

C45(C46	1.381(4)

C47(C52	1.386(3)

C47(C48	1.391(3)

C47(P4	1.843(2)

C48(C49	1.390(4)

C49(C50	1.378(4)

C50(C51	1.375(4)

C51(C52	1.387(3)

C53(C58	1.384(4)

C53(C54	1.390(3)

C53(P4	1.845(2)

C54(C55	1.385(4)

C55(C56	1.371(4)

C56(C57	1.368(4)

C57(C58	1.395(4)

C60A(C59A(C64A	120.0

C60A(C59A(C65A	119.8(4)

C64A(C59A(C65A	120.2(4)

C59A(C60A(C61A	120.0

C62A(C61A(C60A	120.0

C61A(C62A(C63A	120.0

C64A(C63A(C62A	120.0

C63A(C64A(C59A	120.0

C60B(C59B(C64B	120.0

C60B(C59B(C65B	123.5(4)

C64B(C59B(C65B	116.5(4)

C61B(C60B(C59B	120.0

C62B(C61B(C60B	120.0

C63B(C62B(C61B	120.0

C62B(C63B(C64B	120.0

C63B(C64B(C59B	120.0

C2(C1(C5	106.91(18)

C2(C1(P1	130.61(16)

C5(C1(P1	122.48(15)

C2(C1(Fe1	68.82(11)

C5(C1(Fe1	69.28(11)

P1(C1(Fe1	126.54(11)

C1(C2(C3	108.69(18)

C1(C2(Fe1	70.18(11)

C3(C2(Fe1	70.98(11)

C2(C3(C4	107.28(17)

C2(C3(P2	123.11(15)

C4(C3(P2	129.24(16)

C2(C3(Fe1	68.22(11)

C4(C3(Fe1	69.55(11)

P2(C3(Fe1	132.66(11)

C5(C4(C3	108.35(18)

C5(C4(Fe1	69.16(11)

C3(C4(Fe1	69.90(11)

C4(C5(C1	108.75(18)

C4(C5(Fe1	70.65(11)

C1(C5(Fe1	69.70(11)

C10(C6(C7	107.02(18)

C10(C6(P3	128.50(16)

C7(C6(P3	124.32(16)

C10(C6(Fe1	69.24(11)

C7(C6(Fe1	68.73(11)

P3(C6(Fe1	123.48(11)

C8(C7(C6	108.54(19)

C8(C7(Fe1	70.02(12)

C6(C7(Fe1	70.45(12)

C7(C8(C9	108.46(19)

C7(C8(Fe1	69.33(12)

C9(C8(Fe1	70.09(11)

C8(C9(C10	107.00(18)

C8(C9(P4	131.10(16)

C10(C9(P4	121.85(16)

C8(C9(Fe1	69.18(11)

C10(C9(Fe1	69.24(11)

P4(C9(Fe1	128.65(11)

C6(C10(C9	108.97(18)

C6(C10(Fe1	70.13(11)

C9(C10(Fe1	70.00(11)

C12(C11(C16	118.5(2)

C12(C11(P1	118.04(17)

C16(C11(P1	123.44(17)

C13(C12(C11	120.7(2)

C14(C13(C12	120.1(2)

C13(C14(C15	119.9(2)

C16(C15(C14	120.3(2)

C15(C16(C11	120.5(2)

C22(C17(C18	118.3(2)

C22(C17(P1	125.25(17)

C18(C17(P1	116.39(17)

C19(C18(C17	120.9(2)

C20(C19(C18	120.3(2)

C21(C20(C19	119.6(2)

C20(C21(C22	120.4(2)

C17(C22(C21	120.6(2)

C28(C23(C24	118.3(2)

C28(C23(P2	124.99(16)

C24(C23(P2	116.64(16)

C25(C24(C23	120.7(2)

C26(C25(C24	120.1(2)

C27(C26(C25	119.7(2)

C26(C27(C28	120.2(2)

C27(C28(C23	120.9(2)

C34(C29(C30	118.2(2)

C34(C29(P2	117.95(17)

C30(C29(P2	123.72(16)

C31(C30(C29	120.8(2)

C30(C31(C32	120.1(2)

C33(C32(C31	119.8(2)

C32(C33(C34	120.2(2)

C33(C34(C29	121.0(2)

C40(C35(C36	118.2(2)

C40(C35(P3	124.89(17)

C36(C35(P3	116.75(17)

C37(C36(C35	120.8(2)

C38(C37(C36	120.1(2)

C37(C38(C39	119.9(2)

C38(C39(C40	120.3(2)

C39(C40(C35	120.8(2)

C42(C41(C46	118.7(2)

C42(C41(P3	124.66(17)

C46(C41(P3	116.64(18)

C41(C42(C43	120.3(2)

C44(C43(C42	120.0(3)

C45(C44(C43	120.3(2)

C44(C45(C46	119.7(2)

C45(C46(C41	121.0(2)

C52(C47(C48	118.2(2)

C52(C47(P4	116.68(17)

C48(C47(P4	125.06(18)

C49(C48(C47	120.7(2)

C50(C49(C48	120.1(3)

C51(C50(C49	119.8(2)

C50(C51(C52	120.2(2)

C47(C52(C51	121.0(2)

C58(C53(C54	118.6(2)

C58(C53(P4	117.70(19)

C54(C53(P4	123.63(18)

C55(C54(C53	120.4(3)

C56(C55(C54	120.5(3)

C57(C56(C55	119.6(3)

C56(C57(C58	120.5(3)

C53(C58(C57	120.2(3)

C1(P1(C11	102.18(9)

C1(P1(C17	101.41(10)

C11(P1(C17	100.17(10)

C3(P2(C23	99.73(9)

C3(P2(C29	97.95(9)

C23(P2(C29	103.81(10)

C6(P3(C41	98.96(10)

C6(P3(C35	101.42(10)

C41(P3(C35	103.24(10)

C9(P4(C47	100.11(10)

C9(P4(C53	102.65(10)

C47(P4(C53	100.58(10)

C2(Fe1(C7	130.10(8)

C2(Fe1(C5	68.73(8)

C7(Fe1(C5	113.15(8)

C2(Fe1(C8	108.66(8)

C7(Fe1(C8	40.65(8)

C5(Fe1(C8	145.43(8)

C2(Fe1(C1	41.00(8)

C7(Fe1(C1	105.80(8)

C5(Fe1(C1	41.02(8)

C8(Fe1(C1	113.78(8)

C2(Fe1(C10	149.63(8)

C7(Fe1(C10	68.38(8)

C5(Fe1(C10	131.57(8)

C8(Fe1(C10	68.28(8)

C1(Fe1(C10	169.15(8)

C2(Fe1(C9	116.76(8)

C7(Fe1(C9	68.66(8)

C5(Fe1(C9	171.75(8)

C8(Fe1(C9	40.73(8)

C1(Fe1(C9	147.11(8)

C10(Fe1(C9	40.76(8)

C2(Fe1(C6	168.74(8)

C7(Fe1(C6	40.82(8)

C5(Fe1(C6	107.02(8)

C8(Fe1(C6	68.51(8)

C1(Fe1(C6	129.13(8)

C10(Fe1(C6	40.63(8)

C9(Fe1(C6	68.75(8)

C2(Fe1(C4	68.47(8)

C7(Fe1(C4	145.88(8)

C5(Fe1(C4	40.18(8)

C8(Fe1(C4	173.22(8)

C1(Fe1(C4	68.44(8)

C10(Fe1(C4	110.84(8)

C9(Fe1(C4	134.33(8)

C6(Fe1(C4	115.53(8)

C2(Fe1(C3	40.80(8)

C7(Fe1(C3	170.52(8)

C5(Fe1(C3	68.18(8)

C8(Fe1(C3	133.39(8)

C1(Fe1(C3	68.68(8)

C10(Fe1(C3	118.33(8)

C9(Fe1(C3	111.45(8)

C6(Fe1(C3	148.60(8)

C4(Fe1(C3	40.55(8)

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C59A	81(5) 	88(6)	37(4) 	(38(4)	(21(4) 	39(5)

C60A	75(6) 	104(9)	102(8) 	(76(7)	12(5) 	(21(5)

C61A	49(4) 	61(4)	58(4) 	(29(3)	(13(3) 	8(3)

C62A	110(8) 	37(4)	37(4) 	(9(3)	27(5) 	(8(5)

C63A	34(4) 	60(5)	108(7) 	(30(4)	12(4) 	(4(3)

C64A	144(11) 	95(7)	67(7) 	(37(5)	28(7) 	11(8)

C65A	47(4) 	59(5)	62(5) 	(9(4)	(16(3) 	(10(3)

C59B	76(5) 	67(5)	30(3) 	(1(3)	9(3) 	42(4)

C60B	70(5) 	37(4)	34(4) 	(3(3)	(21(4) 	24(3)

C61B	103(8) 	70(6)	62(6) 	(14(4)	(13(5) 	12(5)

C62B	68(5) 	110(7)	96(6) 	(62(6)	(28(5) 	19(5)

C63B	78(6) 	112(8)	151(10) 	(38(7)	(31(7) 	(28(6)

C64B	83(7) 	149(10)	54(6) 	(11(6)	(34(5) 	67(7)

C65B	81(7) 	123(10)	106(8) 	(66(8)	(4(6) 	(33(6)

C1	23(1) 	18(1)	21(1) 	(11(1)	(4(1) 	2(1)

C2	23(1) 	16(1)	21(1) 	(9(1)	(5(1) 	3(1)

C3	21(1) 	18(1)	20(1) 	(10(1)	(4(1) 	3(1)

C4	22(1) 	18(1)	19(1) 	(8(1)	(1(1) 	1(1)

C5	27(1) 	19(1)	15(1) 	(8(1)	(5(1) 	4(1)

C6	28(1) 	18(1)	21(1) 	(11(1)	(4(1) 	5(1)

C7	21(1) 	22(1)	25(1) 	(12(1)	(4(1) 	4(1)

C8	24(1) 	21(1)	20(1) 	(9(1)	(1(1) 	1(1)

C9	25(1) 	19(1)	18(1) 	(10(1)	(3(1) 	1(1)

C10	24(1) 	19(1)	20(1) 	(9(1)	(3(1) 	0(1)

C11	23(1) 	22(1)	27(1) 	(11(1)	(6(1) 	(4(1)

C12	22(1) 	28(1)	35(1) 	(15(1)	(9(1) 	(1(1)

C13	26(1) 	37(1)	41(1) 	(23(1)	1(1) 	(3(1)

C14	38(1) 	37(1)	30(1) 	(11(1)	2(1) 	(14(1)

C15	36(1) 	28(1)	32(1) 	(3(1)	(4(1) 	(8(1)

C16	24(1) 	23(1)	35(1) 	(7(1)	(4(1) 	(4(1)

C17	30(1) 	22(1)	22(1) 	(9(1)	(8(1) 	1(1)

C18	30(1) 	34(1)	42(1) 	(22(1)	(6(1) 	(1(1)

C19	42(2) 	34(1)	47(2) 	(21(1)	(6(1) 	(9(1)

C20	52(2) 	22(1)	34(1) 	(16(1)	(7(1) 	0(1)

C21	38(1) 	29(1)	35(1) 	(15(1)	(5(1) 	6(1)

C22	32(1) 	25(1)	29(1) 	(11(1)	(7(1) 	(1(1)

C23	20(1) 	23(1)	23(1) 	(8(1)	(10(1) 	3(1)

C24	30(1) 	27(1)	25(1) 	(14(1)	(4(1) 	0(1)

C25	38(1) 	27(1)	37(1) 	(19(1)	(10(1) 	(1(1)

C26	30(1) 	27(1)	29(1) 	(7(1)	(11(1) 	(5(1)

C27	23(1) 	33(1)	25(1) 	(9(1)	(5(1) 	(1(1)

C28	26(1) 	24(1)	25(1) 	(12(1)	(7(1) 	2(1)

C29	20(1) 	18(1)	25(1) 	(6(1)	(4(1) 	1(1)

C30	32(1) 	25(1)	30(1) 	(11(1)	(10(1) 	9(1)

C31	33(1) 	33(1)	34(1) 	(19(1)	(7(1) 	5(1)

C32	37(1) 	21(1)	44(2) 	(17(1)	(1(1) 	3(1)

C33	38(1) 	22(1)	43(2) 	(8(1)	(10(1) 	10(1)

C34	31(1) 	23(1)	28(1) 	(6(1)	(8(1) 	4(1)

C35	26(1) 	15(1)	31(1) 	(10(1)	(10(1) 	1(1)

C36	33(1) 	22(1)	34(1) 	(9(1)	(13(1) 	1(1)

C37	35(1) 	23(1)	52(2) 	(9(1)	(20(1) 	8(1)

C38	27(1) 	23(1)	63(2) 	(20(1)	(9(1) 	5(1)

C39	34(1) 	31(1)	42(2) 	(18(1)	1(1) 	2(1)

C40	35(1) 	24(1)	32(1) 	(11(1)	(7(1) 	6(1)

C41	29(1) 	20(1)	18(1) 	0(1)	(3(1) 	4(1)

C42	29(1) 	31(1)	30(1) 	(10(1)	(3(1) 	(1(1)

C43	47(2) 	41(2)	40(2) 	(13(1)	(9(1) 	(10(1)

C44	30(1) 	51(2)	45(2) 	(1(1)	(5(1) 	(11(1)

C45	29(1) 	38(2)	44(2) 	3(1)	2(1) 	5(1)

C46	38(1) 	23(1)	29(1) 	0(1)	3(1) 	7(1)

C47	32(1) 	23(1)	21(1) 	(8(1)	(3(1) 	(3(1)

C48	46(2) 	48(2)	33(1) 	(22(1)	(14(1) 	15(1)

C49	54(2) 	50(2)	42(2) 	(24(1)	(10(1) 	21(1)

C50	60(2) 	35(1)	28(1) 	(18(1)	1(1) 	(1(1)

C51	50(2) 	48(2)	32(1) 	(22(1)	(9(1) 	(5(1)

C52	32(1) 	40(1)	31(1) 	(18(1)	(4(1) 	(3(1)

C53	34(1) 	25(1)	21(1) 	(6(1)	(10(1) 	(1(1)

C54	40(1) 	33(1)	39(2) 	(11(1)	(2(1) 	(5(1)

C55	47(2) 	49(2)	46(2) 	(7(1)	(4(1) 	(19(1)

C56	62(2) 	30(1)	43(2) 	4(1)	(26(1) 	(12(1)

C57	71(2) 	25(1)	60(2) 	(6(1)	(21(2) 	9(1)

C58	51(2) 	28(1)	43(2) 	(7(1)	(4(1) 	4(1)

P1	23(1) 	21(1)	24(1) 	(10(1)	(8(1) 	2(1)

P2	21(1) 	20(1)	20(1) 	(8(1)	(6(1) 	3(1)

P3	32(1) 	19(1)	20(1) 	(8(1)	(7(1) 	6(1)

P4	26(1) 	23(1)	19(1) 	(8(1)	(5(1) 	1(1)

Fe1	20(1) 	15(1)	18(1) 	(7(1)	(5(1) 	2(1)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H60A	7054	9602	2666	103	0.50

H61A	5808	8276	3024	64	0.50

H62A	6319	6851	3995	81	0.50

H63A	8075	6753	4608	84	0.50

H64A	9321	8080	4250	128	0.50

H65A	9466	10056	2607	86	0.50

H65B	9763	9704	3543	86	0.50

H65C	8579	10363	3333	86	0.50

H60B	6902	9346	2771	59	0.50

H61B	8630	10246	2636	97	0.50

H62B	10203	9584	3408	100	0.50

H63B	10049	8023	4315	134	0.50

H64B	8321	7122	4450	122	0.50

H65D	5791	7461	4290	145	0.50

H65E	6640	6871	3764	145	0.50

H65F	5870	7769	3293	145	0.50

H2	8158	2005	2608	23	1

H4	9864	4419	923	23	1

H5	7790	4309	535	24	1

H7	5430	4390	2366	26	1

H8	6167	3215	3635	25	1

H10	8751	5325	2558	24	1

H12	3896	3160	2508	31	1

H13	2989	2648	3930	39	1

H14	3847	1373	4877	42	1

H15	5551	560	4392	40	1

H16	6424	1032	2970	33	1

H18	4578	1234	1387	39	1

H19	4913	(148	1043	46	1

H20	6926	(651	658	41	1

H21	8603	248	602	40	1

H22	8281	1620	971	33	1

H24	11183	4462	2637	31	1

H25	12483	5760	1962	37	1

H26	13913	5811	749	34	1

H27	14016	4569	201	33	1

H28	12700	3284	859	28	1

H30	10594	2320	866	34	1

H31	11215	1060	370	38	1

H32	12317	(209	1144	40	1

H33	12817	(203	2405	42	1

H34	12200	1054	2906	33	1

H36	5434	7602	373	35	1

H37	3648	8423	719	43	1

H38	2717	8119	2119	44	1

H39	3584	7000	3179	42	1

H40	5376	6183	2844	36	1

H42	7416	7687	1884	36	1

H43	9198	8483	1840	50	1

H44	11112	8117	1153	55	1

H45	11258	6966	505	51	1

H46	9487	6191	527	41	1

H48	6496	4766	4469	48	1

H49	5814	5501	5482	57	1

H50	7013	5420	6490	48	1

H51	8874	4580	6501	48	1

H52	9565	3851	5488	39	1

H54	6517	2749	5373	45	1

H55	5857	1207	6102	59	1

H56	7025	(59	5869	55	1

H57	8840	214	4885	64	1

H58	9537	1756	4158	51	1