|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement details.

Identification code 	2009src1289

Empirical formula 	C4H11Nd2O14P2

Formula weight 	633.55

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P(1

Unit cell dimensions	a = 8.9198(3) Å	( = 107.751(2)°

b = 8.9196(2) Å	( = 110.1650(10)°

c = 9.7074(3) Å	(  = 91.715(2)°

Volume	682.55(3) Å3

Z	2

Density (calculated)	3.088 Mg / m3

Absorption coefficient	7.832 mm(1

F(000)	594

Crystal	plate; colourless

Crystal size	0.06 ( 0.05 ( 0.01 mm3

( range for data collection	3.18 ( 27.48°

Index ranges	(11 ( h ( 11, (11 ( k ( 10, (12 ( l ( 12

Reflections collected	11744

Independent reflections	3118 [Rint = 0.0332]

Completeness to ( = 27.48°	99.3 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9258 and 0.6508

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	3118 / 0 / 227

Goodness-of-fit on F2	1.089

Final R indices [F2 > 2((F2)]	R1 = 0.0214, wR2 = 0.0470

R indices (all data)	R1 = 0.0237, wR2 = 0.0486

Largest diff. peak and hole	0.643 and (0.659 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SADABS (Sheldrick, G. M. (2007). SADABS. Version 2007/2. Bruker AXS Inc., Madison, Wisconsin, USA.). Structure solution: SHELXS97 (Sheldrick, G.M. (2008). Acta Cryst. A64, 112-122.). Structure refinement: SHELXL97 (G Sheldrick, G.M. (2008). Acta Cryst. A64, 112-122.). Graphics: CAMERON (Watkin, D. M., Pearce, L. & Prout, C. K. (1993). Chemical Crystallography Lab, University of Oxford)

Special details:

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

Nd1	8693(1)	3646(1)	5779(1)	5(1)	1

Nd2	10682(1)	2104(1)	9761(1)	6(1)	1

P1	12038(1)	5297(1)	9589(1)	6(1)	1

P2	10762(1)	1921(1)	13104(1)	6(1)	1

C4	12358(4)	(373(4)	14228(4)	7(1)	1

O1	10425(3)	4246(3)	8471(3)	8(1)	1

O3	12751(3)	4508(3)	10812(3)	7(1)	1

O6	10143(3)	711(3)	11435(3)	7(1)	1

O7	11231(3)	3508(3)	12953(3)	9(1)	1

O2	11852(3)	7026(3)	10232(3)	9(1)	1

O4	11368(3)	4901(3)	6120(3)	8(1)	1

O8	9552(3)	1891(3)	13890(3)	9(1)	1

O1W	12106(4)	1269(3)	7898(3)	12(1)	1

O2W	13423(4)	1582(4)	11192(3)	14(1)	1

C3	12571(4)	1315(4)	14232(4)	9(1)	1

C1	13413(4)	5209(4)	8577(4)	9(1)	1

C2	12766(4)	5596(4)	7107(4)	6(1)	1

O5	13595(3)	6529(3)	6813(3)	11(1)	1

O9	11240(3)	(1410(3)	13087(3)	11(1)	1

O10	13254(3)	(776(3)	15322(3)	14(1)	1

O3W	15287(4)	1016(4)	8251(4)	17(1)	1

O4W	6072(3)	4004(3)	6163(4)	16(1)	1

Table 3. Bond lengths [Å] and angles [°].

Nd1(O8i	2.385(2)

Nd1(O1	2.412(2)

Nd1(O7ii	2.447(2)

Nd1(O4	2.475(2)

Nd1(O4W	2.506(3)

Nd1(O4iii	2.544(2)

Nd1(O9iv	2.548(2)

Nd1(O5iii	2.592(3)

Nd1(O10iv	2.738(3)

Nd1(C2iii	2.948(3)

Nd1(C4iv	3.037(3)

Nd2(O6iv	2.391(2)

Nd2(O2ii	2.413(3)

Nd2(O6	2.481(2)

Nd2(O3	2.485(2)

Nd2(O2W	2.499(3)

Nd2(O1W	2.501(3)

Nd2(O1	2.561(2)

Nd2(O9iv	2.567(2)

Nd2(O7	2.822(2)

Nd2(P1	3.1348(9)

Nd2(P2	3.2756(9)

P1(O2	1.515(3)

P1(O3	1.525(2)

P1(O1	1.533(3)

P1(C1	1.806(4)

P2(O8	1.525(3)

P2(O7	1.528(3)

P2(O6	1.541(3)

P2(C3	1.814(4)

C4(O10	1.249(4)

C4(O9	1.279(4)

C4(C3	1.510(5)

C4(Nd1iv	3.037(3)

O6(Nd2iv	2.391(2)

O7(Nd1ii	2.447(2)

O2(Nd2ii	2.413(3)

O4(C2	1.275(4)

O4(Nd1iii	2.544(2)

O8(Nd1v	2.385(2)

O1W(H1W	0.83(6)

O1W(H2W	0.78(6)

O2W(H3W	0.84(6)

O2W(H4W	0.72(5)

C3(H3A	0.9900

C3(H3B	0.9900

C1(C2	1.494(5)

C1(H1A	0.9900

C1(H1B	0.9900

C2(O5	1.256(4)

C2(Nd1iii	2.948(3)

O5(Nd1iii	2.592(3)

O9(Nd1iv	2.548(2)

O9(Nd2iv	2.567(2)

O10(Nd1iv	2.738(3)

O3W(H5W	0.80(6)

O3W(H6W	0.88(6)

O4W(H7W	0.70(5)

O8i(Nd1(O1	116.34(9)

O8i(Nd1(O7ii	140.58(8)

O1(Nd1(O7ii	74.04(8)

O8i(Nd1(O4	72.66(8)

O1(Nd1(O4	72.55(8)

O7ii(Nd1(O4	75.36(8)

O8i(Nd1(O4W	136.17(9)

O1(Nd1(O4W	98.09(9)

O7ii(Nd1(O4W	72.31(9)

O4(Nd1(O4W	147.67(9)

O8i(Nd1(O4iii	74.97(8)

O1(Nd1(O4iii	130.28(8)

O7ii(Nd1(O4iii	71.03(8)

O4(Nd1(O4iii	65.20(9)

O4W(Nd1(O4iii	103.63(9)

O8i(Nd1(O9iv	86.65(8)

O1(Nd1(O9iv	63.29(8)

O7ii(Nd1(O9iv	128.21(8)

O4(Nd1(O9iv	115.06(8)

O4W(Nd1(O9iv	85.58(9)

O4iii(Nd1(O9iv	160.74(8)

O8i(Nd1(O5iii	77.99(9)

O1(Nd1(O5iii	165.67(9)

O7ii(Nd1(O5iii	94.94(8)

O4(Nd1(O5iii	114.13(8)

O4W(Nd1(O5iii	69.36(9)

O4iii(Nd1(O5iii	50.60(8)

O9iv(Nd1(O5iii	120.50(8)

O8i(Nd1(O10iv	73.48(9)

O1(Nd1(O10iv	110.87(8)

O7ii(Nd1(O10iv	141.50(9)

O4(Nd1(O10iv	143.14(8)

O4W(Nd1(O10iv	69.19(9)

O4iii(Nd1(O10iv	118.56(8)

O9iv(Nd1(O10iv	48.58(8)

O5iii(Nd1(O10iv	71.98(8)

O8i(Nd1(C2iii	73.80(9)

O1(Nd1(C2iii	154.10(9)

O7ii(Nd1(C2iii	83.56(9)

O4(Nd1(C2iii	89.53(9)

O4W(Nd1(C2iii	87.06(10)

O4iii(Nd1(C2iii	25.50(9)

O9iv(Nd1(C2iii	142.61(9)

O5iii(Nd1(C2iii	25.15(9)

O10iv(Nd1(C2iii	94.73(9)

O8i(Nd1(C4iv	76.75(9)

O1(Nd1(C4iv	87.68(9)

O7ii(Nd1(C4iv	142.61(9)

O4(Nd1(C4iv	130.27(9)

O4W(Nd1(C4iv	78.56(10)

O4iii(Nd1(C4iv	140.06(9)

O9iv(Nd1(C4iv	24.53(9)

O5iii(Nd1(C4iv	96.23(9)

O10iv(Nd1(C4iv	24.29(8)

C2iii(Nd1(C4iv	118.21(9)

O6iv(Nd2(O2ii	100.66(8)

O6iv(Nd2(O6	64.55(10)

O2ii(Nd2(O6	80.90(8)

O6iv(Nd2(O3	151.16(8)

O2ii(Nd2(O3	107.99(8)

O6(Nd2(O3	122.74(8)

O6iv(Nd2(O2W	88.49(10)

O2ii(Nd2(O2W	149.89(9)

O6(Nd2(O2W	77.30(9)

O3(Nd2(O2W	68.33(9)

O6iv(Nd2(O1W	75.33(9)

O2ii(Nd2(O1W	138.54(9)

O6(Nd2(O1W	129.13(9)

O3(Nd2(O1W	80.96(9)

O2W(Nd2(O1W	71.48(10)

O6iv(Nd2(O1	128.86(8)

O2ii(Nd2(O1	76.47(8)

O6(Nd2(O1	155.50(8)

O3(Nd2(O1	57.65(8)

O2W(Nd2(O1	119.54(9)

O1W(Nd2(O1	75.12(9)

O6iv(Nd2(O9iv	69.39(8)

O2ii(Nd2(O9iv	72.34(9)

O6(Nd2(O9iv	120.28(8)

O3(Nd2(O9iv	116.11(8)

O2W(Nd2(O9iv	137.14(9)

O1W(Nd2(O9iv	67.66(9)

O1(Nd2(O9iv	61.06(8)

O6iv(Nd2(O7	118.71(7)

O2ii(Nd2(O7	76.08(8)

O6(Nd2(O7	54.40(7)

O3(Nd2(O7	72.63(7)

O2W(Nd2(O7	74.39(9)

O1W(Nd2(O7	142.64(9)

O1(Nd2(O7	110.14(7)

O9iv(Nd2(O7	148.38(8)

O6iv(Nd2(P1	148.24(6)

O2ii(Nd2(P1	93.48(6)

O6(Nd2(P1	146.54(6)

O3(Nd2(P1	28.63(6)

O2W(Nd2(P1	93.37(7)

O1W(Nd2(P1	75.27(7)

O1(Nd2(P1	29.06(6)

O9iv(Nd2(P1	88.46(6)

O7(Nd2(P1	92.17(5)

O6iv(Nd2(P2	90.95(6)

O2ii(Nd2(P2	79.18(6)

O6(Nd2(P2	26.79(6)

O3(Nd2(P2	97.49(6)

O2W(Nd2(P2	71.98(7)

O1W(Nd2(P2	141.14(7)

O1(Nd2(P2	136.27(6)

O9iv(Nd2(P2	141.04(6)

O7(Nd2(P2	27.76(5)

P1(Nd2(P2	119.75(2)

O6iv(Nd2(Nd2iv	32.95(6)

O2ii(Nd2(Nd2iv	90.69(6)

O6(Nd2(Nd2iv	31.61(6)

O3(Nd2(Nd2iv	146.53(5)

O2W(Nd2(Nd2iv	81.51(7)

O1W(Nd2(Nd2iv	103.48(7)

O1(Nd2(Nd2iv	155.81(6)

O9iv(Nd2(Nd2iv	95.70(6)

O7(Nd2(Nd2iv	85.88(5)

P1(Nd2(Nd2iv	174.842(18)

P2(Nd2(Nd2iv	58.130(16)

O2(P1(O3	114.97(14)

O2(P1(O1	112.41(14)

O3(P1(O1	105.43(14)

O2(P1(C1	107.87(16)

O3(P1(C1	106.30(15)

O1(P1(C1	109.62(16)

O2(P1(Nd2	134.20(11)

O3(P1(Nd2	51.29(10)

O1(P1(Nd2	54.23(9)

C1(P1(Nd2	117.91(12)

O8(P2(O7	116.79(14)

O8(P2(O6	111.64(14)

O7(P2(O6	105.49(14)

O8(P2(C3	106.56(16)

O7(P2(C3	108.64(16)

O6(P2(C3	107.37(16)

O8(P2(Nd2	136.99(11)

O7(P2(Nd2	59.37(10)

O6(P2(Nd2	46.49(9)

C3(P2(Nd2	115.14(12)

O10(C4(O9	119.2(3)

O10(C4(C3	121.2(3)

O9(C4(C3	119.6(3)

O10(C4(Nd1iv	64.33(19)

O9(C4(Nd1iv	55.82(17)

C3(C4(Nd1iv	169.2(3)

P1(O1(Nd1	136.83(14)

P1(O1(Nd2	96.71(11)

Nd1(O1(Nd2	120.48(10)

P1(O3(Nd2	100.08(12)

P2(O6(Nd2iv	136.62(14)

P2(O6(Nd2	106.72(12)

Nd2iv(O6(Nd2	115.45(9)

P2(O7(Nd1ii	138.83(15)

P2(O7(Nd2	92.87(11)

Nd1ii(O7(Nd2	123.78(9)

P1(O2(Nd2ii	123.57(14)

C2(O4(Nd1	144.9(2)

C2(O4(Nd1iii	95.3(2)

Nd1(O4(Nd1iii	114.80(9)

P2(O8(Nd1v	139.56(14)

Nd2(O1W(H1W	118(4)

Nd2(O1W(H2W	112(4)

H1W(O1W(H2W	105(5)

Nd2(O2W(H3W	123(3)

Nd2(O2W(H4W	127(4)

H3W(O2W(H4W	107(5)

C4(C3(P2	114.8(3)

C4(C3(H3A	108.6

P2(C3(H3A	108.6

C4(C3(H3B	108.6

P2(C3(H3B	108.6

H3A(C3(H3B	107.5

C2(C1(P1	114.7(3)

C2(C1(H1A	108.6

P1(C1(H1A	108.6

C2(C1(H1B	108.6

P1(C1(H1B	108.6

H1A(C1(H1B	107.6

O5(C2(O4	120.4(3)

O5(C2(C1	121.3(3)

O4(C2(C1	118.3(3)

O5(C2(Nd1iii	61.36(18)

O4(C2(Nd1iii	59.23(17)

C1(C2(Nd1iii	176.7(2)

C2(O5(Nd1iii	93.5(2)

C4(O9(Nd1iv	99.7(2)

C4(O9(Nd2iv	144.8(2)

Nd1iv(O9(Nd2iv	115.14(9)

C4(O10(Nd1iv	91.4(2)

H5W(O3W(H6W	105(6)

Nd1(O4W(H7W	107(4)

Symmetry transformations used to generate equivalent atoms:

(i) x,y,z(1    (ii) (x+2,(y+1,(z+2    (iii) (x+2,(y+1,(z+1

(iv)  (x+2,(y,(z+2    (v) x,y,z+1

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

Nd1	6(1) 	5(1)	5(1) 	2(1)	2(1) 	1(1)

Nd2	7(1) 	5(1)	6(1) 	2(1)	2(1) 	1(1)

P1	6(1) 	6(1)	6(1) 	3(1)	2(1) 	1(1)

P2	8(1) 	5(1)	6(1) 	2(1)	3(1) 	1(1)

C4	8(2) 	8(2)	7(2) 	1(1)	5(1) 	2(1)

O1	7(1) 	9(1)	8(1) 	4(1)	2(1) 	0(1)

O3	8(1) 	10(1)	6(1) 	4(1)	2(1) 	1(1)

O6	9(1) 	7(1)	6(1) 	2(1)	4(1) 	1(1)

O7	11(1) 	6(1)	11(1) 	3(1)	6(1) 	3(1)

O2	9(1) 	9(1)	10(1) 	3(1)	3(1) 	1(1)

O4	6(1) 	10(1)	8(1) 	4(1)	2(1) 	0(1)

O8	13(1) 	7(1)	8(1) 	1(1)	7(1) 	1(1)

O1W	11(2) 	11(1)	13(1) 	0(1)	6(1) 	0(1)

O2W	12(1) 	11(2)	18(2) 	5(1)	3(1) 	1(1)

C3	11(2) 	7(2)	9(2) 	5(1)	4(1) 	2(1)

C1	8(2) 	13(2)	8(2) 	6(1)	4(1) 	3(1)

C2	6(2) 	6(2)	5(2) 	0(1)	3(1) 	4(1)

O5	8(1) 	12(1)	14(1) 	7(1)	3(1) 	(2(1)

O9	14(1) 	7(1)	9(1) 	4(1)	0(1) 	1(1)

O10	17(1) 	12(1)	11(1) 	6(1)	(2(1) 	0(1)

O3W	11(2) 	18(2)	16(2) 	2(1)	3(1) 	(1(1)

O4W	14(2) 	18(2)	11(2) 	(3(1)	6(1) 	(1(1)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H3A	13423	1434	13820	10	1

H3B	12955	2046	15324	10	1

H1A	14414	5961	9288	11	1

H1B	13707	4124	8326	11	1

H3W	14240(70)	2290(60)	11660(60)	26(14)	1

H1W	13090(80)	1260(70)	8260(70)	40(17)	1

H4W	13710(60)	830(70)	11070(60)	23(15)	1

H2W	11740(60)	420(70)	7290(60)	27(15)	1

H5W	14900(70)	810(70)	7330(80)	44(18)	1

H6W	16210(70)	1630(70)	8540(70)	39(16)	1

H7W	6260(60)	4360(50)	6970(60)	14(13)	1