|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	2009src0837 / ADOLINA4

Empirical formula 	C38H27CrNNaO12S24

Formula weight 	1534.04

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21

Unit cell dimensions	a = 10.4088(4) Å	( = 90°

b = 14.7524(8) Å	( = 94.741(3)°

c = 18.2275(8) Å	(  = 90°

Volume	2789.3(2) Å3

Z	2

Density (calculated)	1.826 Mg / m3

Absorption coefficient	1.171 mm(1

F(000)	1554

Crystal	Plate; Green

Crystal size	0.08 ( 0.06 ( 0.01 mm3

( range for data collection	2.98 ( 25.00°

Index ranges	(12 ( h ( 12, (17 ( k ( 17, (21 ( l ( 21

Reflections collected	21720

Independent reflections	9280 [Rint = 0.0821]

Completeness to ( = 25.00°	99.4 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9884 and 0.9122

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	9280 / 592 / 753

Goodness-of-fit on F2	1.090

Final R indices [F2 > 2((F2)]	R1 = 0.0976, wR2 = 0.1964

R indices (all data)	R1 = 0.1731, wR2 = 0.2397

Absolute structure parameter	0.28(8)

Largest diff. peak and hole	1.113 and (0.604 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP3 for Windows (L. J. Farrugia, J. Appl. Crystallogr. 1997, 30, 565).

Special details:

All hydrogen atoms were fixed using a standard riding model.

There is possible extra pseudo-symmetry observed. Due to the metal atom  positions it can be ignored, but it did cause problems with the displacement parameters for those atoms for wich the additional symmetry did hold. Thus a loose global thermal displacement restraint (SIMU) was used.

There was also some disorder of the BEDT-TTF molecules and some C-S distance restraints were used.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

Na1	(2014(6)	6919(5)	73(3)	17(1)	1

Cr1	3046(3)	5601(3)	42(2)	35(1)	1

C1	(20(20)	7730(30)	2080(20)	38(8)	0.47(3)

C2	(1050(30)	7060(30)	2211(11)	25(7)	0.47(3)

C201	120(18)	7260(20)	1971(13)	19(6)	0.53(3)

C202	(1050(30)	7580(30)	2313(16)	42(8)	0.53(3)

C3	(55(18)	7227(16)	3659(11)	44(5)	1

C4	1128(19)	7407(16)	3424(11)	44(5)	1

C5	1496(18)	7355(15)	4837(10)	41(5)	1

C6	2050(15)	7297(13)	5573(8)	27(4)	1

C7	3648(15)	7318(13)	6686(9)	24(4)	1

C8	2468(15)	7129(14)	6978(10)	33(4)	1

C9	3566(15)	7508(14)	8323(10)	33(4)	1

C10	4816(16)	7115(15)	8110(9)	35(4)	1

S1	1545(5)	7536(4)	2517(3)	45(1)	1

S2	(1523(4)	7056(5)	3133(3)	42(1)	1

S3	(152(5)	7117(5)	4605(3)	44(1)	1

S4	2399(5)	7491(4)	4101(3)	39(1)	1

S5	3666(5)	7452(5)	5756(3)	44(1)	1

S6	1144(4)	7112(4)	6304(3)	42(1)	1

S7	2115(4)	7004(4)	7877(2)	37(1)	1

S8	5148(4)	7395(4)	7184(3)	40(2)	1

C11	5970(20)	520(20)	7792(10)	34(6)	0.68(3)

C12	4960(16)	(160(17)	7949(13)	23(5)	0.68(3)

C211	6040(40)	(90(40)	7720(20)	29(9)	0.32(3)

C212	4870(20)	400(30)	7940(30)	29(9)	0.32(3)

C13	3755(16)	147(14)	6586(9)	30(4)	1

C14	4902(16)	337(14)	6347(9)	33(4)	1

C15	3389(17)	231(15)	5179(10)	38(4)	1

C16	2813(19)	196(16)	4477(11)	46(5)	1

C17	2392(17)	298(14)	3070(10)	34(4)	1

C18	1268(18)	183(15)	3277(11)	38(5)	1

C19	270(30)	490(30)	1896(13)	20(6)	0.48(3)

C20	1434(19)	50(30)	1624(18)	28(7)	0.48(3)

C219	260(20)	(86(19)	1864(10)	24(6)	0.52(3)

C220	1248(17)	592(19)	1677(14)	23(6)	0.52(3)

S11	6395(4)	438(5)	6849(3)	46(2)	1

S12	3355(5)	9(6)	7488(3)	66(2)	1

S13	2449(5)	19(5)	5915(3)	50(2)	1

S14	4997(4)	341(5)	5397(3)	46(2)	1

S15	3728(4)	359(5)	3718(2)	44(2)	1

S16	1198(5)	55(5)	4238(3)	44(2)	1

S17	(224(4)	114(4)	2781(3)	40(1)	1

S18	2848(4)	495(4)	2147(2)	34(1)	1

C21	10192(17)	9181(15)	7986(11)	37(5)	1

C22	9008(19)	8700(16)	8204(12)	49(5)	1

C23	8468(18)	8447(15)	6702(11)	35(5)	1

C24	8969(18)	9212(14)	6600(11)	34(4)	1

C25	7793(18)	8725(15)	5353(11)	36(4)	1

C26	7200(18)	8742(15)	4666(12)	40(5)	1

C27	6516(18)	9148(16)	3275(11)	37(5)	1

C28	5885(18)	8344(15)	3463(11)	37(5)	1

C29	4657(19)	8352(16)	2046(11)	46(5)	1

C30	5800(18)	8862(15)	1814(11)	39(5)	1

S21	9885(5)	9911(4)	7183(3)	45(1)	1

S22	8414(5)	7844(5)	7553(3)	52(2)	1

S23	7501(5)	7894(5)	5977(3)	50(2)	1

S24	8820(6)	9617(5)	5670(3)	50(2)	1

S25	7428(5)	9636(5)	4019(3)	47(2)	1

S26	6121(5)	7903(5)	4330(3)	52(2)	1

S27	4983(6)	7631(5)	2838(3)	62(2)	1

S28	6420(5)	9717(4)	2459(3)	49(2)	1

C31	900(18)	6600(13)	(264(10)	34(4)	1

C32	643(19)	6005(14)	461(10)	38(4)	1

O31	1994(14)	6589(9)	(417(7)	45(4)	1

O32	1627(13)	5604(12)	734(7)	53(4)	1

O33	(442(14)	5986(12)	672(9)	64(4)	1

O34	(36(12)	7052(10)	(516(7)	49(3)	1

C41	2112(13)	3941(11)	(384(7)	17(3)	1

C42	3114(18)	3753(14)	271(10)	39(4)	1

O41	2024(11)	4714(10)	(596(6)	35(3)	1

O42	3726(11)	4489(9)	510(6)	42(3)	1

O43	3239(13)	3001(10)	577(8)	51(4)	1

O44	1539(12)	3269(9)	(655(7)	44(3)	1

C51	5506(15)	5919(12)	(267(8)	28(4)	1

C52	5395(18)	6424(15)	471(11)	41(4)	1

O51	4471(9)	5655(8)	(608(5)	28(3)	1

O52	4220(10)	6392(9)	672(6)	31(3)	1

O53	6352(12)	6753(12)	814(7)	54(4)	1

O54	6618(11)	5901(9)	(524(6)	35(3)	1

C61	2160(20)	8587(19)	377(16)	75(7)	1

C62	2290(30)	9000(20)	(306(15)	92(8)	1

N61	1972(18)	8259(15)	926(10)	92(7)	1

Table 3. Bond lengths [Å] and angles [°].

Na1(O53i	2.272(15)

Na1(O54i	2.282(14)

Na1(O44ii	2.292(14)

Na1(O43ii	2.309(15)

Na1(O33	2.338(17)

Na1(O34	2.406(14)

Cr1(O42	1.955(13)

Cr1(O31	1.968(14)

Cr1(O51	1.975(10)

Cr1(O52	1.984(12)

Cr1(O41	1.998(13)

Cr1(O32	2.020(14)

C1(C2	1.500(17)

C1(S1	1.780(18)

C1(H1A	0.9900

C1(H1B	0.9900

C2(S2	1.789(18)

C2(H2A	0.9900

C2(H2B	0.9900

C201(C202	1.494(17)

C201(S1	1.764(17)

C201(H20A	0.9900

C201(H20B	0.9900

C202(S2	1.788(18)

C202(H20C	0.9900

C202(H20D	0.9900

C3(C4	1.36(3)

C3(S3	1.74(2)

C3(S2	1.75(2)

C4(S4	1.74(2)

C4(S1	1.75(2)

C5(C6	1.42(2)

C5(S4	1.712(19)

C5(S3	1.768(19)

C6(S5	1.702(17)

C6(S6	1.716(16)

C7(C8	1.41(2)

C7(S5	1.708(16)

C7(S8	1.742(17)

C8(S7	1.717(19)

C8(S6	1.770(17)

C9(C10	1.50(2)

C9(S7	1.814(16)

C9(H9A	0.9900

C9(H9B	0.9900

C10(S8	1.800(16)

C10(H10A	0.9900

C10(H10B	0.9900

C11(C12	1.506(16)

C11(S11	1.813(16)

C11(H11A	0.9900

C11(H11B	0.9900

C12(S12	1.824(16)

C12(H12A	0.9900

C12(H12B	0.9900

C211(C212	1.499(18)

C211(S11	1.827(19)

C211(H21A	0.9900

C211(H21B	0.9900

C212(S12	1.812(19)

C212(H21C	0.9900

C212(H21D	0.9900

C13(C14	1.33(2)

C13(S12	1.741(17)

C13(S13	1.763(17)

C14(S11	1.743(17)

C14(S14	1.743(16)

C15(C16	1.37(3)

C15(S14	1.696(18)

C15(S13	1.753(19)

C16(S16	1.71(2)

C16(S15	1.76(2)

C17(C18	1.27(3)

C17(S15	1.750(17)

C17(S18	1.809(18)

C18(S17	1.735(18)

C18(S16	1.77(2)

C19(C20	1.499(18)

C19(S17	1.820(17)

C19(H19A	0.9900

C19(H19B	0.9900

C20(S18	1.808(17)

C20(H20E	0.9900

C20(H20F	0.9900

C219(C220	1.495(17)

C219(S17	1.809(16)

C219(H21E	0.9900

C219(H21F	0.9900

C220(S18	1.814(15)

C220(H22A	0.9900

C220(H22B	0.9900

C21(C22	1.50(3)

C21(S21	1.82(2)

C21(H21G	0.9900

C21(H21H	0.9900

C22(S22	1.81(2)

C22(H22C	0.9900

C22(H22D	0.9900

C23(C24	1.26(3)

C23(S23	1.79(2)

C23(S22	1.79(2)

C24(S21	1.71(2)

C24(S24	1.79(2)

C25(C26	1.349(17)

C25(S23	1.72(2)

C25(S24	1.76(2)

C26(S26	1.75(2)

C26(S25	1.80(2)

C27(C28	1.41(3)

C27(S28	1.70(2)

C27(S25	1.74(2)

C28(S26	1.71(2)

C28(S27	1.76(2)

C29(C30	1.50(3)

C29(S27	1.80(2)

C29(H29A	0.9900

C29(H29B	0.9900

C30(S28	1.81(2)

C30(H30A	0.9900

C30(H30B	0.9900

C31(O31	1.19(2)

C31(O34	1.24(2)

C31(C32	1.63(3)

C32(O33	1.22(2)

C32(O32	1.25(2)

C41(O41	1.205(19)

C41(O44	1.240(19)

C41(C42	1.544(18)

C42(O43	1.24(2)

C42(O42	1.31(2)

O43(Na1iii	2.309(15)

O44(Na1iii	2.292(14)

C51(O51	1.260(18)

C51(O54	1.284(18)

C51(C52	1.55(3)

C52(O53	1.23(2)

C52(O52	1.31(2)

O53(Na1iv	2.272(15)

O54(Na1iv	2.282(14)

C61(N61	1.14(3)

C61(C62	1.40(3)

C62(H62A	0.9800

C62(H62B	0.9800

C62(H62C	0.9800

O53i(Na1(O54i	75.2(5)

O53i(Na1(O44ii	87.8(6)

O54i(Na1(O44ii	153.5(5)

O53i(Na1(O43ii	88.3(6)

O54i(Na1(O43ii	85.1(5)

O44ii(Na1(O43ii	74.1(5)

O53i(Na1(O33	100.9(6)

O54i(Na1(O33	102.7(6)

O44ii(Na1(O33	100.3(6)

O43ii(Na1(O33	169.2(6)

O53i(Na1(O34	169.8(5)

O54i(Na1(O34	111.4(5)

O44ii(Na1(O34	88.6(5)

O43ii(Na1(O34	99.9(6)

O33(Na1(O34	70.4(5)

O42(Cr1(O31	167.4(6)

O42(Cr1(O51	91.9(5)

O31(Cr1(O51	97.7(6)

O42(Cr1(O52	93.3(5)

O31(Cr1(O52	96.0(6)

O51(Cr1(O52	82.3(5)

O42(Cr1(O41	82.0(5)

O31(Cr1(O41	89.2(5)

O51(Cr1(O41	93.8(5)

O52(Cr1(O41	173.8(5)

O42(Cr1(O32	89.3(6)

O31(Cr1(O32	81.6(6)

O51(Cr1(O32	177.0(6)

O52(Cr1(O32	94.9(5)

O41(Cr1(O32	89.0(6)

C2(C1(S1	117(2)

C2(C1(H1A	108.0

S1(C1(H1A	108.0

C2(C1(H1B	108.0

S1(C1(H1B	108.0

H1A(C1(H1B	107.2

C1(C2(S2	114(3)

C1(C2(H2A	108.7

S2(C2(H2A	108.7

C1(C2(H2B	108.7

S2(C2(H2B	108.7

H2A(C2(H2B	107.6

C202(C201(S1	112(2)

C202(C201(H20A	109.3

S1(C201(H20A	109.3

C202(C201(H20B	109.3

S1(C201(H20B	109.3

H20A(C201(H20B	108.0

C201(C202(S2	120(2)

C201(C202(H20C	107.3

S2(C202(H20C	107.3

C201(C202(H20D	107.3

S2(C202(H20D	107.3

H20C(C202(H20D	106.9

C4(C3(S3	117.2(16)

C4(C3(S2	128.7(16)

S3(C3(S2	114.1(11)

C3(C4(S4	116.4(16)

C3(C4(S1	128.1(16)

S4(C4(S1	115.4(11)

C6(C5(S4	122.8(14)

C6(C5(S3	121.6(14)

S4(C5(S3	114.8(10)

C5(C6(S5	119.7(13)

C5(C6(S6	122.5(13)

S5(C6(S6	117.8(9)

C8(C7(S5	118.7(13)

C8(C7(S8	126.1(13)

S5(C7(S8	115.2(9)

C7(C8(S7	130.1(13)

C7(C8(S6	113.2(13)

S7(C8(S6	116.4(10)

C10(C9(S7	115.6(12)

C10(C9(H9A	108.4

S7(C9(H9A	108.4

C10(C9(H9B	108.4

S7(C9(H9B	108.4

H9A(C9(H9B	107.4

C9(C10(S8	113.0(13)

C9(C10(H10A	109.0

S8(C10(H10A	109.0

C9(C10(H10B	109.0

S8(C10(H10B	109.0

H10A(C10(H10B	107.8

C4(S1(C201	104.2(11)

C4(S1(C1	98.9(16)

C201(S1(C1	24.2(14)

C3(S2(C202	96.2(15)

C3(S2(C2	102.7(12)

C202(S2(C2	25.7(15)

C3(S3(C5	94.8(9)

C5(S4(C4	96.6(10)

C6(S5(C7	95.0(8)

C6(S6(C8	95.2(8)

C8(S7(C9	98.5(9)

C7(S8(C10	103.9(8)

C12(C11(S11	111.1(16)

C12(C11(H11A	109.4

S11(C11(H11A	109.4

C12(C11(H11B	109.4

S11(C11(H11B	109.4

H11A(C11(H11B	108.0

C11(C12(S12	116.8(16)

C11(C12(H12A	108.1

S12(C12(H12A	108.1

C11(C12(H12B	108.1

S12(C12(H12B	108.1

H12A(C12(H12B	107.3

C212(C211(S11	105(3)

C212(C211(H21A	110.8

S11(C211(H21A	110.8

C212(C211(H21B	110.8

S11(C211(H21B	110.8

H21A(C211(H21B	108.9

C211(C212(S12	115(3)

C211(C212(H21C	108.5

S12(C212(H21C	108.5

C211(C212(H21D	108.5

S12(C212(H21D	108.5

H21C(C212(H21D	107.5

C14(C13(S12	128.6(13)

C14(C13(S13	117.1(13)

S12(C13(S13	114.3(10)

C13(C14(S11	129.0(13)

C13(C14(S14	116.8(13)

S11(C14(S14	113.6(10)

C16(C15(S14	124.8(15)

C16(C15(S13	118.7(15)

S14(C15(S13	116.1(10)

C15(C16(S16	126.0(16)

C15(C16(S15	120.4(15)

S16(C16(S15	113.6(11)

C18(C17(S15	120.4(15)

C18(C17(S18	128.1(14)

S15(C17(S18	111.4(10)

C17(C18(S17	131.3(16)

C17(C18(S16	115.0(14)

S17(C18(S16	113.7(11)

C20(C19(S17	117(2)

C20(C19(H19A	108.0

S17(C19(H19A	108.0

C20(C19(H19B	108.0

S17(C19(H19B	108.0

H19A(C19(H19B	107.3

C19(C20(S18	108(2)

C19(C20(H20E	110.0

S18(C20(H20E	110.0

C19(C20(H20F	110.0

S18(C20(H20F	110.0

H20E(C20(H20F	108.4

C220(C219(S17	110.5(17)

C220(C219(H21E	109.5

S17(C219(H21E	109.5

C220(C219(H21F	109.5

S17(C219(H21F	109.5

H21E(C219(H21F	108.1

C219(C220(S18	117.5(18)

C219(C220(H22A	107.9

S18(C220(H22A	107.9

C219(C220(H22B	107.9

S18(C220(H22B	107.9

H22A(C220(H22B	107.2

C14(S11(C11	103.3(10)

C14(S11(C211	100.6(18)

C11(S11(C211	29.1(17)

C13(S12(C212	97.0(17)

C13(S12(C12	99.8(10)

C212(S12(C12	26.7(15)

C15(S13(C13	93.7(9)

C15(S14(C14	95.5(9)

C17(S15(C16	94.1(9)

C16(S16(C18	96.8(9)

C18(S17(C219	100.7(11)

C18(S17(C19	98.0(12)

C219(S17(C19	27.3(12)

C20(S18(C17	99.7(13)

C20(S18(C220	26.3(13)

C17(S18(C220	98.7(10)

C22(C21(S21	113.4(14)

C22(C21(H21G	108.9

S21(C21(H21G	108.9

C22(C21(H21H	108.9

S21(C21(H21H	108.9

H21G(C21(H21H	107.7

C21(C22(S22	113.5(15)

C21(C22(H22C	108.9

S22(C22(H22C	108.9

C21(C22(H22D	108.9

S22(C22(H22D	108.9

H22C(C22(H22D	107.7

C24(C23(S23	120.7(16)

C24(C23(S22	127.9(17)

S23(C23(S22	110.9(11)

C23(C24(S21	131.4(17)

C23(C24(S24	115.7(16)

S21(C24(S24	112.7(12)

C26(C25(S23	122.4(12)

C26(C25(S24	120.5(12)

S23(C25(S24	116.8(12)

C25(C26(S26	122.9(12)

C25(C26(S25	123.2(12)

S26(C26(S25	113.9(12)

C28(C27(S28	129.1(16)

C28(C27(S25	113.1(15)

S28(C27(S25	117.7(13)

C27(C28(S26	120.7(16)

C27(C28(S27	125.3(15)

S26(C28(S27	113.5(13)

C30(C29(S27	114.9(15)

C30(C29(H29A	108.5

S27(C29(H29A	108.5

C30(C29(H29B	108.5

S27(C29(H29B	108.5

H29A(C29(H29B	107.5

C29(C30(S28	114.6(14)

C29(C30(H30A	108.6

S28(C30(H30A	108.6

C29(C30(H30B	108.6

S28(C30(H30B	108.6

H30A(C30(H30B	107.6

C24(S21(C21	101.2(10)

C23(S22(C22	100.8(11)

C25(S23(C23	92.6(10)

C25(S24(C24	93.7(10)

C27(S25(C26	96.6(10)

C28(S26(C26	95.4(11)

C28(S27(C29	102.7(11)

C27(S28(C30	102.5(10)

O31(C31(O34	131.1(19)

O31(C31(C32	114.0(16)

O34(C31(C32	114.5(17)

O33(C32(O32	128(2)

O33(C32(C31	119.1(18)

O32(C32(C31	113.3(16)

C31(O31(Cr1	114.7(12)

C32(O32(Cr1	111.7(12)

C32(O33(Na1	117.9(14)

C31(O34(Na1	117.8(13)

O41(C41(O44	127.5(14)

O41(C41(C42	116.5(13)

O44(C41(C42	115.9(14)

O43(C42(O42	123.9(17)

O43(C42(C41	123.2(16)

O42(C42(C41	112.7(15)

C41(O41(Cr1	114.2(10)

C42(O42(Cr1	113.6(11)

C42(O43(Na1iii	110.7(12)

C41(O44(Na1iii	115.6(10)

O51(C51(O54	125.0(15)

O51(C51(C52	117.0(14)

O54(C51(C52	117.4(15)

O53(C52(O52	127.6(19)

O53(C52(C51	121.0(17)

O52(C52(C51	111.3(15)

C51(O51(Cr1	111.7(10)

C52(O52(Cr1	114.0(11)

C52(O53(Na1iv	110.8(13)

C51(O54(Na1iv	111.0(11)

N61(C61(C62	176(3)

C61(C62(H62A	109.5

C61(C62(H62B	109.5

H62A(C62(H62B	109.5

C61(C62(H62C	109.5

H62A(C62(H62C	109.5

H62B(C62(H62C	109.5

Symmetry transformations used to generate equivalent atoms:

(i) x(1,y,z    (ii) (x,y+1/2,(z    (iii) (x,y(1/2,(z

(iv)  x+1,y,z

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

Na1	24(3) 	23(4)	6(3) 	1(3)	1(2) 	5(3)

Cr1	38(2) 	41(2)	25(2) 	(2(2)	(6(1) 	0(2)

C1	46(11) 	37(11)	29(10) 	(4(8)	(13(8) 	9(8)

C2	31(10) 	24(10)	19(9) 	(6(8)	(8(7) 	(1(8)

C201	30(9) 	13(9)	12(8) 	(7(7)	(8(7) 	8(7)

C202	50(10) 	34(10)	39(10) 	3(8)	(11(8) 	9(8)

C3	45(8) 	55(9)	33(8) 	(6(7)	14(6) 	13(7)

C4	44(8) 	51(9)	34(8) 	14(7)	(6(6) 	1(7)

C5	40(7) 	57(9)	25(7) 	0(7)	(1(6) 	7(7)

C6	30(7) 	44(8)	7(6) 	10(6)	(4(5) 	4(6)

C7	23(6) 	37(8)	12(6) 	1(6)	2(5) 	5(6)

C8	24(6) 	41(8)	32(7) 	6(6)	(1(6) 	12(6)

C9	44(7) 	28(7)	28(7) 	(7(6)	3(6) 	0(6)

C10	33(7) 	45(8)	25(7) 	(2(6)	(13(6) 	(10(7)

S1	42(3) 	60(4)	32(3) 	12(3)	(9(2) 	(7(3)

S2	26(2) 	63(4)	35(3) 	(12(3)	(12(2) 	6(3)

S3	36(3) 	72(4)	22(2) 	(4(3)	(8(2) 	9(3)

S4	34(3) 	58(4)	24(3) 	4(3)	(5(2) 	(2(2)

S5	38(3) 	64(4)	29(3) 	6(3)	(2(2) 	4(3)

S6	36(3) 	62(4)	26(3) 	(6(3)	(6(2) 	11(3)

S7	29(2) 	57(4)	24(3) 	(10(3)	0(2) 	1(3)

S8	29(2) 	69(4)	20(2) 	0(3)	(9(2) 	0(3)

C11	42(9) 	30(9)	27(8) 	(5(7)	(7(7) 	7(7)

C12	27(6) 	23(6)	19(6) 	(2(4)	(5(4) 	(1(4)

C211	32(11) 	24(11)	29(11) 	3(8)	(3(8) 	4(8)

C212	34(11) 	26(11)	25(11) 	0(8)	(8(8) 	9(8)

C13	32(7) 	43(8)	15(6) 	(6(6)	0(5) 	11(6)

C14	39(7) 	47(8)	12(6) 	5(6)	(4(5) 	13(6)

C15	35(7) 	51(8)	28(7) 	6(6)	(3(6) 	11(6)

C16	45(8) 	51(9)	41(8) 	(6(7)	(2(6) 	2(7)

C17	39(7) 	37(8)	24(7) 	(6(6)	(10(6) 	(2(6)

C18	36(7) 	41(8)	35(8) 	(4(7)	(6(6) 	3(7)

C19	26(9) 	22(10)	13(9) 	8(8)	2(7) 	(2(8)

C20	31(10) 	27(10)	25(9) 	0(8)	2(7) 	0(8)

C219	28(9) 	26(9)	20(8) 	(1(7)	1(7) 	(8(8)

C220	21(8) 	22(9)	24(8) 	1(8)	(13(7) 	1(7)

S11	33(2) 	78(5)	25(3) 	1(3)	(9(2) 	18(3)

S12	35(3) 	151(7)	11(2) 	8(3)	(3(2) 	12(4)

S13	38(3) 	95(5)	14(2) 	2(3)	(8(2) 	(1(3)

S14	28(2) 	89(5)	20(2) 	4(3)	(2(2) 	12(3)

S15	19(2) 	95(5)	16(2) 	7(3)	(4(2) 	5(3)

S16	28(2) 	89(5)	14(2) 	3(3)	(1(2) 	2(3)

S17	29(2) 	67(4)	24(3) 	1(3)	0(2) 	(1(3)

S18	32(2) 	50(4)	18(2) 	5(2)	(5(2) 	10(3)

C21	37(7) 	44(8)	28(7) 	5(6)	(5(6) 	(5(7)

C22	42(8) 	60(9)	44(8) 	(1(7)	4(7) 	7(7)

C23	30(7) 	36(8)	36(8) 	2(7)	(10(6) 	3(6)

C24	37(7) 	32(8)	33(7) 	(1(6)	(2(6) 	(3(6)

C25	31(7) 	48(8)	32(7) 	(5(6)	15(6) 	(9(6)

C26	29(7) 	53(8)	39(8) 	(3(7)	2(6) 	(2(7)

C27	32(7) 	46(8)	34(7) 	(2(7)	11(6) 	1(7)

C28	36(7) 	43(8)	31(7) 	0(6)	4(6) 	4(7)

C29	50(8) 	47(9)	37(8) 	(5(7)	(8(7) 	(4(7)

C30	39(7) 	43(8)	34(7) 	2(6)	3(6) 	8(7)

S21	51(3) 	42(4)	41(3) 	5(3)	(9(2) 	(17(3)

S22	49(3) 	61(4)	43(3) 	12(3)	(19(3) 	(15(3)

S23	54(3) 	59(4)	38(3) 	(3(3)	6(3) 	(25(3)

S24	60(4) 	70(5)	21(3) 	1(3)	6(2) 	(22(3)

S25	50(3) 	65(4)	27(3) 	(3(3)	3(2) 	(12(3)

S26	49(3) 	69(5)	38(3) 	2(3)	4(3) 	(23(3)

S27	66(4) 	68(5)	47(4) 	11(3)	(24(3) 	(17(4)

S28	44(3) 	52(4)	48(3) 	24(3)	(18(2) 	(15(3)

C31	37(7) 	24(7)	39(7) 	(2(6)	(1(6) 	6(6)

C32	41(7) 	42(8)	31(7) 	(9(6)	4(6) 	(7(6)

O31	64(9) 	29(7)	42(7) 	6(6)	2(6) 	(7(6)

O32	58(8) 	74(10)	23(6) 	14(7)	(15(5) 	(12(8)

O33	62(9) 	71(11)	57(9) 	3(8)	(3(7) 	(9(8)

O34	54(8) 	41(8)	51(8) 	5(6)	0(6) 	4(7)

C41	17(6) 	24(7)	9(5) 	1(5)	3(5) 	(10(5)

C42	40(7) 	46(8)	32(7) 	0(6)	3(6) 	(1(6)

O41	35(6) 	52(9)	17(5) 	(7(6)	(13(5) 	5(6)

O42	39(7) 	60(9)	23(6) 	4(6)	(18(5) 	4(6)

O43	69(9) 	41(8)	37(7) 	14(6)	(26(6) 	(1(7)

O44	51(7) 	41(8)	37(7) 	9(6)	(17(6) 	4(6)

C51	34(7) 	36(7)	14(6) 	10(5)	4(5) 	(6(6)

C52	41(7) 	43(8)	39(7) 	2(6)	1(6) 	4(6)

O51	33(6) 	36(7)	15(5) 	(5(5)	(3(4) 	(10(5)

O52	31(6) 	46(8)	17(5) 	(16(5)	(2(5) 	8(5)

O53	39(7) 	84(11)	37(7) 	(31(7)	(14(6) 	5(7)

O54	40(7) 	49(8)	19(6) 	5(5)	10(5) 	(3(6)

C61	71(10) 	80(10)	76(10) 	4(8)	7(8) 	(12(8)

C62	99(11) 	86(11)	89(11) 	(3(8)	(9(8) 	(2(9)

N61	76(13) 	134(18)	62(12) 	32(12)	(8(10) 	(39(12)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H1A	(313	8335	2232	46	0.47(3)

H1B	56	7762	1539	46	0.47(3)

H2A	(744	6443	2094	30	0.47(3)

H2B	(1822	7187	1870	30	0.47(3)

H20A	146	7535	1478	23	0.53(3)

H20B	71	6591	1907	23	0.53(3)

H20C	(1788	7532	1936	50	0.53(3)

H20D	(928	8236	2421	50	0.53(3)

H9A	3559	8164	8210	40	1

H9B	3539	7443	8862	40	1

H10A	4786	6447	8161	42	1

H10B	5529	7341	8455	42	1

H11A	6754	424	8131	40	0.68(3)

H11B	5650	1143	7881	40	0.68(3)

H12A	4882	(166	8487	28	0.68(3)

H12B	5268	(766	7811	28	0.68(3)

H21A	5861	(741	7651	34	0.32(3)

H21B	6772	(10	8096	34	0.32(3)

H21C	4965	1057	7825	35	0.32(3)

H21D	4836	346	8475	35	0.32(3)

H19A	(467	396	1522	24	0.48(3)

H19B	424	1154	1927	24	0.48(3)

H20E	1478	186	1094	33	0.48(3)

H20F	1387	(612	1686	33	0.48(3)

H21E	619	(705	1836	29	0.52(3)

H21F	(503	(43	1503	29	0.52(3)

H22A	913	1204	1778	28	0.52(3)

H22B	1334	555	1141	28	0.52(3)

H21G	10847	8723	7880	44	1

H21H	10552	9552	8406	44	1

H22C	8319	9153	8256	59	1

H22D	9207	8412	8691	59	1

H29A	4303	7975	1628	55	1

H29B	3984	8795	2156	55	1

H30A	5556	9157	1334	46	1

H30B	6497	8423	1739	46	1

H62A	1741	8692	(689	138	1

H62B	3194	8960	(422	138	1

H62C	2040	9639	(283	138	1