|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	2009src1135 / LeeSnitromethane

Empirical formula 	C37H27CrNNaO14S24

Formula weight 	1554.03

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21

Unit cell dimensions	a = 10.4550(4) Å	( = 90°

b = 14.6532(8) Å	( = 94.095(2)°

c = 18.1135(10) Å	(  = 90°

Volume	2767.9(2) Å3

Z	2

Density (calculated)	1.865 Mg / m3

Absorption coefficient	1.184 mm(1

F(000)	1574

Crystal	Sheet; Dark Orange

Crystal size	0.08 ( 0.05 ( 0.01 mm3

( range for data collection	3.00 ( 27.48°

Index ranges	(13 ( h ( 13, (18 ( k ( 19, (23 ( l ( 23

Reflections collected	25203

Independent reflections	12000 [Rint = 0.0424]

Completeness to ( = 27.48°	99.5 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9883 and 0.9113

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	12000 / 279 / 719

Goodness-of-fit on F2	1.088

Final R indices [F2 > 2((F2)]	R1 = 0.0641, wR2 = 0.1221

R indices (all data)	R1 = 0.0896, wR2 = 0.1360

Absolute structure parameter	0.50(4)

Largest diff. peak and hole	1.503 and (0.516 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP3 for Windows (L. J. Farrugia, J. Appl. Crystallogr. 1997, 30, 565).

Special details:

All hydrogen atoms were fixed using a standard riding model.

There is partial disorder on some of the BEDT-TTF molecules. A few geometrical restraints (SADI) were used alsong with a loose global thermal restraint (SIMU).

There is pseudo-symmetry. Although the BEDT-TTF molecules do obey this, the metal oxalate sheets do not due to the subtle differences in M-O distances.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

Cr1	7983(1)	261(1)	75(1)	23(1)	1

Na1	7038(3)	3980(2)	(83(2)	11(1)	1

C1	6013(8)	2199(7)	1812(5)	29(2)	1

C2	4859(9)	1666(7)	2005(5)	27(2)	1

C3	6016(9)	1664(7)	3410(5)	25(2)	1

C4	6583(8)	2449(7)	3272(5)	28(2)	1

C5	7237(8)	2101(8)	4659(6)	30(2)	1

C6	7805(8)	2098(8)	5344(6)	28(2)	1

C7	9031(7)	2556(6)	6570(5)	22(2)	1

C8	8477(8)	1742(7)	6716(6)	26(2)	1

C9	9127(9)	2034(7)	8227(6)	35(2)	1

C10	10242(8)	2556(7)	7978(5)	26(2)	1

S1	6554(2)	3064(2)	2448(2)	35(1)	1

S2	5151(2)	943(2)	2815(2)	34(1)	1

S3	6202(2)	1239(2)	4332(1)	35(1)	1

S4	7451(2)	2998(2)	4034(2)	34(1)	1

S5	8817(2)	2997(2)	5682(1)	33(1)	1

S6	7566(2)	1222(2)	5991(1)	33(1)	1

S7	8539(2)	1152(2)	7558(2)	36(1)	1

S8	9923(2)	3279(2)	7184(2)	36(1)	1

C11	116(11)	1037(10)	2063(7)	23(3)	0.604(14)

C12	(910(13)	343(11)	2207(6)	25(2)	0.604(14)

C13	139(8)	618(8)	3667(5)	33(2)	1

C14	1308(8)	753(7)	3406(5)	25(2)	1

C15	1651(7)	725(8)	4846(4)	29(2)	1

C16	2179(8)	692(8)	5562(4)	27(2)	1

C17	3745(8)	679(7)	6720(5)	29(2)	1

C18	2550(7)	548(7)	6992(5)	25(2)	1

C19	3579(8)	795(9)	8383(5)	46(3)	1

C20	4771(8)	424(10)	8148(5)	42(3)	1

S11	1717(2)	854(3)	2501(1)	42(1)	1

S12	(1343(2)	480(2)	3155(1)	31(1)	1

S13	35(2)	579(2)	4616(1)	32(1)	1

S14	2586(2)	860(2)	4090(1)	31(1)	1

S15	3823(2)	818(2)	5780(1)	30(1)	1

S16	1267(2)	557(2)	6304(1)	29(1)	1

S17	2132(2)	396(2)	7886(1)	22(1)	1

S18	5213(2)	729(2)	7240(1)	25(1)	1

C111	309(13)	583(17)	1975(10)	23(3)	0.396(14)

C112	(897(18)	925(16)	2264(9)	25(2)	0.396(14)

C21	1442(8)	3353(5)	1655(5)	22(2)	1

C22	201(7)	3781(6)	1869(4)	20(2)	1

C23	1329(8)	3554(6)	3285(4)	17(2)	1

C24	2487(8)	3686(7)	3049(5)	23(2)	1

C25	2888(8)	3543(7)	4457(5)	30(2)	1

C26	3400(8)	3555(7)	5179(5)	27(2)	1

C27	4948(7)	3634(6)	6364(4)	18(2)	1

C28	3766(9)	3490(8)	6590(5)	29(2)	1

C29	4898(10)	3139(10)	7996(8)	28(3)	0.684(15)

C30	5964(11)	3786(11)	7815(6)	29(3)	0.684(15)

S21	2873(2)	3828(2)	2120(1)	24(1)	1

S22	(178(2)	3488(2)	2805(1)	26(1)	1

S23	1268(2)	3423(2)	4246(1)	29(1)	1

S24	3794(2)	3706(2)	3701(1)	29(1)	1

S25	5044(2)	3707(2)	5405(1)	30(1)	1

S26	2505(2)	3384(2)	5919(1)	30(1)	1

S27	3347(2)	3360(2)	7513(1)	36(1)	1

S28	6412(2)	3766(2)	6873(1)	29(1)	1

C129	4821(17)	3620(20)	8001(15)	28(3)	0.316(15)

C130	5990(20)	3209(19)	7712(11)	29(3)	0.316(15)

C31	8066(8)	2111(7)	325(5)	25(2)	1

C32	7065(8)	1959(6)	(358(4)	18(2)	1

O31	8659(5)	1401(4)	564(3)	26(1)	1

O32	6983(5)	1133(4)	(576(3)	24(1)	1

O33	6507(6)	2629(5)	(640(4)	37(2)	1

O34	8214(6)	2883(4)	590(4)	29(1)	1

C41	10312(8)	(531(6)	500(5)	23(2)	1

C42	10480(7)	(44(6)	(258(5)	17(2)	1

O41	9183(6)	(504(4)	713(3)	27(1)	1

O42	9430(5)	239(4)	(583(3)	26(1)	1

O43	11557(5)	38(4)	(489(3)	28(1)	1

O44	11279(6)	(864(6)	847(3)	44(2)	1

C51	5584(8)	(136(6)	481(5)	25(2)	1

C52	5824(8)	(732(6)	(225(4)	20(2)	1

O51	6556(5)	240(5)	760(3)	29(1)	1

O52	6954(6)	(749(4)	(413(3)	27(1)	1

O53	4879(6)	(1145(5)	(531(3)	35(2)	1

O54	4466(6)	(90(5)	693(4)	35(2)	1

C61	3237(12)	1952(8)	232(6)	58(4)	1

N61	2366(9)	2361(7)	(285(5)	54(3)	1

O61	1235(7)	2333(6)	(158(5)	60(2)	1

O62	2748(6)	2710(5)	(854(3)	55(2)	1

Table 3. Bond lengths [Å] and angles [°].

Cr1(O32	1.984(6)

Cr1(O41	1.989(6)

Cr1(O42	1.992(6)

Cr1(O31	1.997(6)

Cr1(O52	1.999(6)

Cr1(O51	2.007(6)

Na1(O33	2.273(8)

Na1(O54i	2.303(7)

Na1(O34	2.317(7)

Na1(O44ii	2.327(7)

Na1(O43ii	2.329(7)

Na1(O53i	2.366(7)

C1(C2	1.500(13)

C1(S1	1.778(11)

C1(H1A	0.9900

C1(H1B	0.9900

C2(S2	1.817(9)

C2(H2A	0.9900

C2(H2B	0.9900

C3(C4	1.327(14)

C3(S2	1.719(10)

C3(S3	1.780(10)

C4(S1	1.741(10)

C4(S4	1.788(10)

C5(C6	1.336(8)

C5(S3	1.740(10)

C5(S4	1.759(11)

C6(S6	1.768(11)

C6(S5	1.771(10)

C7(C8	1.361(13)

C7(S5	1.733(10)

C7(S8	1.755(9)

C8(S6	1.743(10)

C8(S7	1.750(11)

C9(C10	1.491(14)

C9(S7	1.848(11)

C9(H9A	0.9900

C9(H9B	0.9900

C10(S8	1.798(10)

C10(H10A	0.9900

C10(H10B	0.9900

C11(C12	1.514(16)

C11(S11	1.821(11)

C11(H11A	0.9900

C11(H11B	0.9900

C12(S12	1.818(11)

C12(H12A	0.9900

C12(H12B	0.9900

C13(C14	1.355(12)

C13(S13	1.732(10)

C13(S12	1.760(9)

C14(S11	1.730(9)

C14(S14	1.763(9)

C15(C16	1.372(11)

C15(S13	1.724(8)

C15(S14	1.750(8)

C16(S16	1.715(8)

C16(S15	1.746(8)

C17(C18	1.389(11)

C17(S15	1.722(10)

C17(S18	1.745(9)

C18(S17	1.722(9)

C18(S16	1.764(8)

C19(C20	1.451(13)

C19(S17	1.801(9)

C19(H19A	0.9900

C19(H19B	0.9900

C20(S18	1.797(10)

C20(H20A	0.9900

C20(H20B	0.9900

S11(C111	1.742(13)

S12(C112	1.832(13)

C111(C112	1.487(17)

C111(H11C	0.9900

C111(H11D	0.9900

C112(H11E	0.9900

C112(H11F	0.9900

C21(C22	1.516(11)

C21(S21	1.804(8)

C21(H21A	0.9900

C21(H21B	0.9900

C22(S22	1.820(8)

C22(H22A	0.9900

C22(H22B	0.9900

C23(C24	1.327(12)

C23(S22	1.747(8)

C23(S23	1.756(8)

C24(S24	1.741(8)

C24(S21	1.770(9)

C25(C26	1.378(13)

C25(S23	1.718(8)

C25(S24	1.737(10)

C26(S26	1.707(10)

C26(S25	1.753(9)

C27(C28	1.347(12)

C27(S28	1.741(8)

C27(S25	1.750(8)

C28(S26	1.735(8)

C28(S27	1.768(9)

C29(C30	1.517(15)

C29(S27	1.816(9)

C29(H29A	0.9900

C29(H29B	0.9900

C30(S28	1.801(10)

C30(H30A	0.9900

C30(H30B	0.9900

S27(C129	1.761(14)

S28(C130	1.807(15)

C129(C130	1.49(2)

C129(H12C	0.9900

C129(H12D	0.9900

C130(H13A	0.9900

C130(H13B	0.9900

C31(O34	1.234(11)

C31(O31	1.271(11)

C31(C32	1.578(8)

C32(O33	1.234(10)

C32(O32	1.274(10)

C41(O44	1.251(10)

C41(O41	1.268(10)

C41(C42	1.570(12)

C42(O43	1.235(9)

C42(O42	1.277(9)

O43(Na1iii	2.329(7)

O44(Na1iii	2.327(7)

C51(O51	1.233(10)

C51(O54	1.258(9)

C51(C52	1.582(12)

C52(O52	1.253(10)

C52(O53	1.254(10)

O53(Na1iv	2.366(7)

O54(Na1iv	2.303(7)

C61(N61	1.394(12)

C61(H61A	0.9800

C61(H61B	0.9800

C61(H61C	0.9800

N61(O61	1.221(11)

N61(O62	1.243(10)

O32(Cr1(O41	172.4(3)

O32(Cr1(O42	92.6(3)

O41(Cr1(O42	82.2(2)

O32(Cr1(O31	83.1(2)

O41(Cr1(O31	91.4(3)

O42(Cr1(O31	91.1(3)

O32(Cr1(O52	88.3(2)

O41(Cr1(O52	97.9(3)

O42(Cr1(O52	97.5(3)

O31(Cr1(O52	168.1(3)

O32(Cr1(O51	89.6(3)

O41(Cr1(O51	95.6(3)

O42(Cr1(O51	177.7(3)

O31(Cr1(O51	89.7(3)

O52(Cr1(O51	82.0(3)

O33(Na1(O54i	99.6(3)

O33(Na1(O34	74.5(2)

O54i(Na1(O34	169.0(3)

O33(Na1(O44ii	89.5(3)

O54i(Na1(O44ii	100.1(3)

O34(Na1(O44ii	89.2(3)

O33(Na1(O43ii	154.7(2)

O54i(Na1(O43ii	101.9(3)

O34(Na1(O43ii	86.2(2)

O44ii(Na1(O43ii	73.7(2)

O33(Na1(O53i	87.4(3)

O54i(Na1(O53i	72.5(2)

O34(Na1(O53i	97.7(3)

O44ii(Na1(O53i	171.3(3)

O43ii(Na1(O53i	111.8(2)

C2(C1(S1	116.4(7)

C2(C1(H1A	108.2

S1(C1(H1A	108.2

C2(C1(H1B	108.2

S1(C1(H1B	108.2

H1A(C1(H1B	107.4

C1(C2(S2	113.6(6)

C1(C2(H2A	108.8

S2(C2(H2A	108.8

C1(C2(H2B	108.8

S2(C2(H2B	108.8

H2A(C2(H2B	107.7

C4(C3(S2	129.6(8)

C4(C3(S3	117.4(7)

S2(C3(S3	113.0(6)

C3(C4(S1	129.0(8)

C3(C4(S4	117.0(7)

S1(C4(S4	114.0(6)

C6(C5(S3	122.5(6)

C6(C5(S4	122.1(5)

S3(C5(S4	115.3(6)

C5(C6(S6	122.9(5)

C5(C6(S5	122.2(6)

S6(C6(S5	114.9(6)

C8(C7(S5	118.6(7)

C8(C7(S8	128.3(8)

S5(C7(S8	113.0(5)

C7(C8(S6	117.0(8)

C7(C8(S7	127.8(8)

S6(C8(S7	115.2(6)

C10(C9(S7	113.0(8)

C10(C9(H9A	109.0

S7(C9(H9A	109.0

C10(C9(H9B	109.0

S7(C9(H9B	109.0

H9A(C9(H9B	107.8

C9(C10(S8	116.1(7)

C9(C10(H10A	108.3

S8(C10(H10A	108.3

C9(C10(H10B	108.3

S8(C10(H10B	108.3

H10A(C10(H10B	107.4

C4(S1(C1	99.9(5)

C3(S2(C2	101.4(5)

C5(S3(C3	95.1(5)

C5(S4(C4	94.6(5)

C7(S5(C6	94.5(5)

C8(S6(C6	95.0(5)

C8(S7(C9	102.5(5)

C7(S8(C10	102.2(5)

C12(C11(S11	117.8(10)

C12(C11(H11A	107.9

S11(C11(H11A	107.9

C12(C11(H11B	107.9

S11(C11(H11B	107.9

H11A(C11(H11B	107.2

C11(C12(S12	108.4(9)

C11(C12(H12A	110.0

S12(C12(H12A	110.0

C11(C12(H12B	110.0

S12(C12(H12B	110.0

H12A(C12(H12B	108.4

C14(C13(S13	118.2(7)

C14(C13(S12	128.0(8)

S13(C13(S12	113.8(5)

C13(C14(S11	129.3(7)

C13(C14(S14	115.2(7)

S11(C14(S14	115.6(5)

C16(C15(S13	123.0(6)

C16(C15(S14	122.3(6)

S13(C15(S14	114.7(5)

C15(C16(S16	122.5(6)

C15(C16(S15	122.2(6)

S16(C16(S15	115.3(5)

C18(C17(S15	118.4(7)

C18(C17(S18	126.3(7)

S15(C17(S18	115.3(5)

C17(C18(S17	130.3(7)

C17(C18(S16	113.9(7)

S17(C18(S16	115.7(4)

C20(C19(S17	116.1(8)

C20(C19(H19A	108.3

S17(C19(H19A	108.3

C20(C19(H19B	108.3

S17(C19(H19B	108.3

H19A(C19(H19B	107.4

C19(C20(S18	117.2(8)

C19(C20(H20A	108.0

S18(C20(H20A	108.0

C19(C20(H20B	108.0

S18(C20(H20B	108.0

H20A(C20(H20B	107.2

C14(S11(C111	104.0(7)

C14(S11(C11	98.3(5)

C111(S11(C11	23.1(7)

C13(S12(C12	103.9(5)

C13(S12(C112	98.8(8)

C12(S12(C112	27.2(8)

C15(S13(C13	96.1(4)

C15(S14(C14	95.8(4)

C17(S15(C16	95.5(4)

C16(S16(C18	96.8(4)

C18(S17(C19	99.6(4)

C17(S18(C20	102.1(4)

C112(C111(S11	115.8(14)

C112(C111(H11C	108.3

S11(C111(H11C	108.3

C112(C111(H11D	108.3

S11(C111(H11D	108.3

H11C(C111(H11D	107.4

C111(C112(S12	117.8(13)

C111(C112(H11E	107.9

S12(C112(H11E	107.9

C111(C112(H11F	107.9

S12(C112(H11F	107.9

H11E(C112(H11F	107.2

C22(C21(S21	114.7(6)

C22(C21(H21A	108.6

S21(C21(H21A	108.6

C22(C21(H21B	108.6

S21(C21(H21B	108.6

H21A(C21(H21B	107.6

C21(C22(S22	112.8(6)

C21(C22(H22A	109.0

S22(C22(H22A	109.0

C21(C22(H22B	109.0

S22(C22(H22B	109.0

H22A(C22(H22B	107.8

C24(C23(S22	131.2(7)

C24(C23(S23	115.7(6)

S22(C23(S23	113.1(5)

C23(C24(S24	118.2(7)

C23(C24(S21	126.8(6)

S24(C24(S21	114.9(5)

C26(C25(S23	121.6(7)

C26(C25(S24	123.4(7)

S23(C25(S24	115.0(5)

C25(C26(S26	123.1(7)

C25(C26(S25	122.1(7)

S26(C26(S25	114.8(5)

C28(C27(S28	130.4(6)

C28(C27(S25	115.5(6)

S28(C27(S25	114.1(4)

C27(C28(S26	118.0(7)

C27(C28(S27	126.8(6)

S26(C28(S27	115.2(5)

C30(C29(S27	115.4(8)

C30(C29(H29A	108.4

S27(C29(H29A	108.4

C30(C29(H29B	108.4

S27(C29(H29B	108.4

H29A(C29(H29B	107.5

C29(C30(S28	116.0(10)

C29(C30(H30A	108.3

S28(C30(H30A	108.3

C29(C30(H30B	108.3

S28(C30(H30B	108.3

H30A(C30(H30B	107.4

C24(S21(C21	99.2(4)

C23(S22(C22	101.7(4)

C25(S23(C23	96.0(4)

C25(S24(C24	95.0(4)

C27(S25(C26	95.7(4)

C26(S26(C28	96.0(4)

C129(S27(C28	100.6(10)

C129(S27(C29	22.7(9)

C28(S27(C29	101.6(6)

C27(S28(C30	103.0(5)

C27(S28(C130	97.8(9)

C30(S28(C130	27.8(10)

C130(C129(S27	116.7(18)

C130(C129(H12C	108.1

S27(C129(H12C	108.1

C130(C129(H12D	108.1

S27(C129(H12D	108.1

H12C(C129(H12D	107.3

C129(C130(S28	111.7(18)

C129(C130(H13A	109.3

S28(C130(H13A	109.3

C129(C130(H13B	109.3

S28(C130(H13B	109.3

H13A(C130(H13B	107.9

O34(C31(O31	124.9(8)

O34(C31(C32	119.5(8)

O31(C31(C32	115.6(6)

O33(C32(O32	127.5(8)

O33(C32(C31	118.6(7)

O32(C32(C31	113.8(6)

C31(O31(Cr1	112.6(5)

C32(O32(Cr1	114.0(5)

C32(O33(Na1	114.6(6)

C31(O34(Na1	112.6(6)

O44(C41(O41	126.6(9)

O44(C41(C42	118.7(8)

O41(C41(C42	114.6(7)

O43(C42(O42	125.9(8)

O43(C42(C41	120.2(7)

O42(C42(C41	113.9(7)

C41(O41(Cr1	113.8(6)

C42(O42(Cr1	113.2(5)

C42(O43(Na1iii	110.2(5)

C41(O44(Na1iii	111.0(6)

O51(C51(O54	127.5(8)

O51(C51(C52	113.8(7)

O54(C51(C52	118.7(8)

O52(C52(O53	126.8(8)

O52(C52(C51	116.0(7)

O53(C52(C51	117.2(7)

C51(O51(Cr1	112.4(5)

C52(O52(Cr1	110.7(5)

C52(O53(Na1iv	115.0(6)

C51(O54(Na1iv	116.0(6)

N61(C61(H61A	109.5

N61(C61(H61B	109.5

H61A(C61(H61B	109.5

N61(C61(H61C	109.5

H61A(C61(H61C	109.5

H61B(C61(H61C	109.5

O61(N61(O62	122.9(10)

O61(N61(C61	117.0(11)

O62(N61(C61	120.1(10)

Symmetry transformations used to generate equivalent atoms:

(i) (x+1,y+1/2,(z    (ii) (x+2,y+1/2,(z    (iii) (x+2,y(1/2,(z

(iv)  (x+1,y(1/2,(z

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

Cr1	21(1) 	26(1)	22(1) 	0(1)	1(1) 	1(1)

Na1	14(1) 	14(2)	4(1) 	(1(1)	0(1) 	0(1)

C1	26(4) 	38(6)	25(5) 	4(4)	11(4) 	(3(4)

C2	38(5) 	23(5)	16(5) 	5(4)	(9(4) 	0(4)

C3	31(5) 	30(5)	15(5) 	4(4)	1(4) 	2(4)

C4	23(4) 	35(5)	24(5) 	8(4)	(2(4) 	(5(4)

C5	17(4) 	43(6)	32(6) 	(2(5)	7(4) 	(10(4)

C6	26(5) 	35(5)	24(5) 	(7(4)	5(4) 	(1(4)

C7	7(4) 	23(5)	35(5) 	(1(4)	2(3) 	1(3)

C8	8(4) 	24(5)	45(6) 	(9(4)	6(4) 	5(3)

C9	38(5) 	32(5)	34(6) 	(1(5)	(3(4) 	12(4)

C10	25(4) 	30(5)	24(5) 	(3(4)	2(4) 	3(4)

S1	37(1) 	30(1)	37(2) 	11(1)	(13(1) 	(9(1)

S2	43(1) 	26(1)	31(1) 	6(1)	(8(1) 	(11(1)

S3	45(2) 	45(2)	18(1) 	(1(1)	6(1) 	(22(1)

S4	37(1) 	36(2)	28(1) 	(2(1)	7(1) 	(15(1)

S5	36(1) 	40(2)	24(1) 	(1(1)	7(1) 	(14(1)

S6	38(1) 	39(2)	24(1) 	(3(1)	7(1) 	(16(1)

S7	32(1) 	32(1)	41(2) 	17(1)	(12(1) 	(10(1)

S8	39(1) 	36(2)	31(1) 	9(1)	(12(1) 	(12(1)

C11	34(5) 	28(7)	6(5) 	(9(5)	1(4) 	(1(6)

C12	33(5) 	22(5)	20(5) 	6(6)	(3(4) 	6(6)

C13	26(4) 	45(6)	27(5) 	(7(5)	(6(4) 	11(4)

C14	22(4) 	29(5)	24(5) 	(6(4)	6(3) 	7(4)

C15	22(4) 	55(6)	10(4) 	(2(4)	8(3) 	0(4)

C16	26(4) 	46(6)	9(4) 	4(4)	3(3) 	1(4)

C17	22(4) 	34(5)	30(5) 	9(4)	6(3) 	(2(4)

C18	16(4) 	36(6)	22(4) 	0(4)	4(3) 	6(4)

C19	33(5) 	89(8)	17(4) 	(5(5)	11(4) 	(24(5)

C20	25(4) 	79(9)	22(5) 	9(5)	(6(4) 	(6(5)

S11	31(1) 	80(2)	15(1) 	9(1)	2(1) 	14(1)

S12	22(1) 	53(2)	19(1) 	(2(1)	(2(1) 	10(1)

S13	25(1) 	55(2)	16(1) 	1(1)	2(1) 	10(1)

S14	21(1) 	55(2)	17(1) 	6(1)	2(1) 	1(1)

S15	20(1) 	56(2)	13(1) 	3(1)	4(1) 	(1(1)

S16	20(1) 	51(2)	15(1) 	3(1)	0(1) 	5(1)

S17	19(1) 	34(1)	13(1) 	2(1)	2(1) 	5(1)

S18	20(1) 	41(2)	15(1) 	1(1)	2(1) 	1(1)

C111	34(5) 	28(7)	6(5) 	(9(5)	1(4) 	(1(6)

C112	33(5) 	22(5)	20(5) 	6(6)	(3(4) 	6(6)

C21	36(4) 	8(3)	22(4) 	(2(3)	(1(3) 	5(3)

C22	25(4) 	24(4)	12(4) 	(8(4)	3(3) 	(9(4)

C23	23(4) 	22(4)	5(3) 	(7(3)	(4(3) 	4(3)

C24	29(4) 	27(5)	13(4) 	0(4)	(1(3) 	9(4)

C25	22(4) 	40(6)	28(5) 	(4(5)	0(4) 	14(4)

C26	27(4) 	26(5)	26(5) 	2(4)	(7(4) 	3(4)

C27	25(4) 	24(5)	7(4) 	5(3)	3(3) 	9(4)

C28	33(5) 	42(6)	9(4) 	5(4)	(9(4) 	3(4)

C29	31(5) 	22(7)	27(5) 	18(6)	(19(4) 	(15(6)

C30	27(5) 	36(7)	21(5) 	(7(5)	(8(4) 	(8(6)

S21	21(1) 	35(1)	17(1) 	(1(1)	2(1) 	3(1)

S22	19(1) 	40(2)	18(1) 	(1(1)	2(1) 	(2(1)

S23	28(1) 	45(2)	15(1) 	3(1)	2(1) 	2(1)

S24	20(1) 	48(2)	18(1) 	(2(1)	1(1) 	5(1)

S25	21(1) 	50(2)	18(1) 	1(1)	1(1) 	3(1)

S26	27(1) 	48(2)	15(1) 	1(1)	(3(1) 	0(1)

S27	24(1) 	67(2)	16(1) 	8(1)	(1(1) 	0(1)

S28	24(1) 	36(1)	25(1) 	(2(1)	(2(1) 	7(1)

C129	31(5) 	22(7)	27(5) 	18(6)	(19(4) 	(15(6)

C130	27(5) 	36(7)	21(5) 	(7(5)	(8(4) 	(8(6)

C31	20(4) 	28(4)	27(4) 	(15(4)	2(3) 	(8(3)

C32	24(4) 	21(4)	7(3) 	10(3)	4(3) 	5(3)

O31	22(3) 	34(3)	21(3) 	3(2)	(6(2) 	(9(2)

O32	22(3) 	27(3)	22(3) 	(1(2)	(7(2) 	(1(2)

O33	36(3) 	43(4)	30(3) 	6(3)	(14(3) 	4(3)

O34	40(3) 	23(3)	22(3) 	(6(2)	(6(2) 	4(3)

C41	35(4) 	18(4)	15(4) 	(3(3)	(9(3) 	3(3)

C42	14(3) 	18(4)	20(4) 	(1(3)	3(3) 	(3(3)

O41	37(3) 	26(3)	19(3) 	5(2)	2(2) 	(2(2)

O42	43(3) 	22(3)	15(2) 	1(2)	5(2) 	6(3)

O43	35(3) 	29(3)	23(3) 	1(2)	13(2) 	(7(3)

O44	44(4) 	66(5)	20(3) 	20(3)	(4(3) 	(2(3)

C51	31(4) 	29(4)	16(4) 	(2(3)	8(3) 	9(3)

C52	27(4) 	19(4)	14(4) 	4(3)	(1(3) 	2(3)

O51	30(3) 	32(3)	24(3) 	(9(3)	(9(2) 	12(3)

O52	35(3) 	30(3)	18(3) 	(1(2)	8(2) 	2(2)

O53	42(3) 	38(4)	27(3) 	(4(3)	13(3) 	(12(3)

O54	36(3) 	44(4)	26(3) 	(9(3)	13(3) 	2(3)

C61	102(10) 	38(6)	27(6) 	7(5)	(41(6) 	11(7)

N61	67(6) 	40(5)	56(6) 	(13(4)	18(5) 	(7(4)

O61	43(4) 	59(5)	77(5) 	(4(4)	(6(4) 	(10(4)

O62	72(4) 	64(4)	31(3) 	3(3)	13(3) 	1(4)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H1A	5816	2488	1323	35	1

H1B	6727	1766	1760	35	1

H2A	4567	1280	1578	32	1

H2B	4158	2097	2096	32	1

H9A	8421	2465	8308	42	1

H9B	9380	1739	8707	42	1

H10A	10918	2115	7865	32	1

H10B	10591	2940	8395	32	1

H11A	(185	1642	2223	27	0.604(14)

H11B	187	1069	1522	27	0.604(14)

H12A	(583	(282	2133	31	0.604(14)

H12B	(1672	440	1859	31	0.604(14)

H19A	3611	1468	8336	55	1

H19B	3526	651	8914	55	1

H20A	4718	(250	8173	51	1

H20B	5472	618	8511	51	1

H11C	370	829	1470	27	0.396(14)

H11D	251	(90	1932	27	0.396(14)

H11E	(1609	791	1890	31	0.396(14)

H11F	(831	1597	2306	31	0.396(14)

H21A	1494	3423	1115	26	1

H21B	1416	2691	1764	26	1

H22A	(509	3577	1517	24	1

H22B	268	4453	1828	24	1

H29A	4801	3167	8535	33	0.684(15)

H29B	5162	2509	7879	33	0.684(15)

H30A	6733	3641	8145	34	0.684(15)

H30B	5698	4415	7932	34	0.684(15)

H12C	4925	4289	8007	33	0.316(15)

H12D	4774	3416	8520	33	0.316(15)

H13A	5837	2552	7611	34	0.316(15)

H13B	6713	3261	8093	34	0.316(15)

H61A	3697	2426	527	87	1

H61B	3851	1587	(26	87	1

H61C	2775	1557	559	87	1