|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	2009src1086 Sm iBu

Empirical formula 	C36H81N3O12P3Sm

Formula weight 	991.30

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Tetragonal

Space group 	P41212

Unit cell dimensions	a = 15.2470(5) Å	( = 90°

b = 15.2470(5) Å	( = 90°

c = 43.4821(18) Å	(  = 90°

Volume	10108.3(6) Å3

Z	8

Density (calculated)	1.303 Mg / m3

Absorption coefficient	1.309 mm(1

F(000)	4168

Crystal	Cut Block; colourless

Crystal size	0.16 ( 0.13 ( 0.10 mm3

( range for data collection	2.99 ( 27.48°

Index ranges	(17 ( h ( 18, (19 ( k ( 19, (56 ( l ( 56

Reflections collected	97636

Independent reflections	11524 [Rint = 0.0955]

Completeness to ( = 27.48°	99.7 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.8802 and 0.8179

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	11524 / 970 / 745

Goodness-of-fit on F2	1.048

Final R indices [F2 > 2((F2)]	R1 = 0.0823, wR2 = 0.1537

R indices (all data)	R1 = 0.1415, wR2 = 0.1777

Absolute structure parameter	0.07(3)

Largest diff. peak and hole	1.879 and (1.987 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP3 for Windows (L. J. Farrugia, J. Appl. Crystallogr. 1997, 30, 565).

Special details:

All hydrogen atoms were fixed using a standard riding model.

Two of the three phosphorus ligands were disordered. This resulted in all the ligands been restrained to be similar using the SAME compound. Also a loose global thermal restraint (SIMU) was used.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

Sm1	5346(1)	9891(1)	1512(1)	62(1)	1

C1	4562(7)	9367(7)	2420(2)	76(3)	1

C2	4328(7)	9086(8)	2756(2)	73(3)	1

C3	4927(9)	8345(8)	2859(3)	90(4)	1

C4	3398(8)	8792(9)	2767(2)	88(4)	1

C5	5106(7)	11121(7)	2589(2)	68(3)	1

C6	4163(7)	11424(8)	2585(2)	70(3)	1

C7	3882(9)	11735(9)	2271(2)	87(4)	1

C8	4015(8)	12131(8)	2823(3)	77(4)	1

C9	6392(6)	9714(8)	2502(2)	81(4)	1

C10	7235(9)	10103(11)	2370(3)	114(4)	1

C11	7975(10)	9583(14)	2495(5)	181(8)	1

C12	7351(11)	10985(12)	2463(4)	145(7)	1

O1	5461(4)	10414(4)	2021(1)	57(2)	1

P1	5395(2)	10176(2)	2358(1)	64(1)	1

C13	2467(12)	8677(13)	1791(5)	92(5)	0.619(8)

C14	1993(17)	9486(15)	1889(7)	128(5)	0.619(8)

C15	1266(17)	9404(18)	2123(6)	149(9)	0.619(8)

C16	2435(18)	10311(16)	1885(8)	139(8)	0.619(8)

C17	3153(15)	8784(14)	1165(4)	115(6)	0.619(8)

C18	2549(14)	8216(14)	999(4)	103(5)	0.619(8)

C19	1732(14)	8627(16)	882(6)	100(7)	0.619(8)

C20	3011(15)	7698(17)	755(5)	130(9)	0.619(8)

C21	3904(18)	7519(12)	1572(6)	173(9)	0.619(8)

C22	4261(17)	7146(18)	1875(7)	177(9)	0.619(8)

C23	3560(18)	6710(20)	2039(7)	174(11)	0.619(8)

C24	5005(18)	6600(20)	1885(9)	217(14)	0.619(8)

O2	4105(10)	9287(10)	1653(4)	51(3)	0.619(8)

P2	3446(6)	8604(6)	1570(2)	67(2)	0.619(8)

C113	2250(20)	8777(19)	1866(7)	108(6)	0.381(8)

C114	1780(20)	9680(20)	1872(8)	135(6)	0.381(8)

C115	2150(40)	10280(30)	2116(9)	148(10)	0.381(8)

C116	1860(30)	10130(30)	1574(8)	137(9)	0.381(8)

C117	2565(19)	9128(19)	1238(6)	117(7)	0.381(8)

C118	1695(19)	8770(20)	1137(7)	111(6)	0.381(8)

C119	1060(20)	9480(20)	1046(8)	124(12)	0.381(8)

C120	1850(30)	8160(20)	874(9)	96(9)	0.381(8)

C121	3280(20)	7533(14)	1461(8)	170(10)	0.381(8)

C122	3970(20)	7014(17)	1653(9)	168(9)	0.381(8)

C123	3780(30)	7240(30)	1971(9)	176(11)	0.381(8)

C124	4000(20)	6093(15)	1611(10)	120(12)	0.381(8)

O102	3877(14)	9147(19)	1653(7)	51(4)	0.381(8)

P102	3068(7)	8625(10)	1579(3)	57(3)	0.381(8)

C25	5920(20)	12490(20)	1774(9)	78(5)	0.347(10)

C26	6160(20)	13400(20)	1907(7)	85(5)	0.347(10)

C27	6970(20)	13380(30)	2106(10)	110(10)	0.347(10)

C28	5450(30)	13680(30)	2124(8)	83(10)	0.347(10)

C29	7546(14)	11670(20)	1583(7)	79(5)	0.347(10)

C30	8114(19)	11070(20)	1399(7)	89(6)	0.347(10)

C31	8500(20)	11400(30)	1106(7)	84(9)	0.347(10)

C32	8810(20)	10710(30)	1605(8)	97(8)	0.347(10)

C33	6570(20)	12630(30)	1129(8)	76(5)	0.347(10)

C34	5760(20)	12660(20)	911(6)	84(5)	0.347(10)

C35	5520(30)	11740(20)	854(10)	137(11)	0.347(10)

C36	5910(30)	13030(20)	608(6)	89(9)	0.347(10)

O3	5955(14)	11107(16)	1392(6)	49(3)	0.347(10)

P3	6453(11)	11942(13)	1462(4)	48(3)	0.347(10)

C125	6085(13)	12549(13)	1779(5)	77(4)	0.653(10)

C126	6170(13)	13555(13)	1792(5)	85(5)	0.653(10)

C127	7078(14)	13854(18)	1871(7)	128(8)	0.653(10)

C128	5557(16)	14011(16)	1991(6)	114(8)	0.653(10)

C129	7824(10)	11968(13)	1587(5)	89(5)	0.653(10)

C130	8403(11)	11328(15)	1431(5)	87(5)	0.653(10)

C131	8202(17)	10873(18)	1144(5)	117(7)	0.653(10)

C132	9284(10)	11297(11)	1562(4)	64(5)	0.653(10)

C133	6625(13)	12691(15)	1137(5)	74(4)	0.653(10)

C134	5659(13)	12949(10)	1044(4)	77(4)	0.653(10)

C135	5433(19)	12329(13)	804(4)	108(6)	0.653(10)

C136	5670(15)	13809(11)	908(5)	105(7)	0.653(10)

O103	6324(7)	11115(8)	1418(3)	49(3)	0.653(10)

P103	6705(7)	12012(8)	1473(3)	61(2)	0.653(10)

N11	5703(8)	8903(7)	942(2)	77(3)	1

O11	5235(6)	8591(4)	1164(1)	75(2)	1

O12	6064(6)	9617(5)	985(2)	81(2)	1

O13	5773(7)	8492(6)	698(2)	102(3)	1

N21	3972(7)	11001(6)	1221(2)	77(3)	1

O21	4388(5)	10398(5)	1079(1)	71(2)	1

O22	4234(5)	11146(5)	1500(1)	68(2)	1

O23	3381(7)	11400(6)	1103(2)	100(3)	1

N31	6556(8)	8623(7)	1801(2)	76(3)	1

O31	5743(7)	8577(5)	1834(2)	75(2)	1

O32	7057(7)	8138(6)	1940(2)	96(3)	1

O33	6818(6)	9215(5)	1612(2)	70(2)	1

Table 3. Bond lengths [Å] and angles [°].

Sm1(O3	2.14(2)

Sm1(O2	2.194(12)

Sm1(O1	2.359(5)

Sm1(O103	2.422(11)

Sm1(O11	2.499(7)

Sm1(O21	2.504(6)

Sm1(O33	2.508(8)

Sm1(O31	2.519(7)

Sm1(O22	2.558(7)

Sm1(O12	2.570(7)

Sm1(O102	2.59(2)

Sm1(N11	2.949(8)

C1(C2	1.565(11)

C1(P1	1.791(9)

C1(H1A	0.9900

C1(H1B	0.9900

C2(C4	1.488(13)

C2(C3	1.519(14)

C2(H2	1.0000

C3(H3A	0.9800

C3(H3B	0.9800

C3(H3C	0.9800

C4(H4A	0.9800

C4(H4B	0.9800

C4(H4C	0.9800

C5(C6	1.510(13)

C5(P1	1.810(9)

C5(H5A	0.9900

C5(H5B	0.9900

C6(C7	1.508(12)

C6(C8	1.512(12)

C6(H6	1.0000

C7(H7A	0.9800

C7(H7B	0.9800

C7(H7C	0.9800

C8(H8A	0.9800

C8(H8B	0.9800

C8(H8C	0.9800

C9(C10	1.529(15)

C9(P1	1.788(10)

C9(H9A	0.9900

C9(H9B	0.9900

C10(C12	1.415(16)

C10(C11	1.482(16)

C10(H10	1.0000

C11(H11A	0.9800

C11(H11B	0.9800

C11(H11C	0.9800

C12(H12A	0.9800

C12(H12B	0.9800

C12(H12C	0.9800

O1(P1	1.514(5)

C13(C14	1.491(16)

C13(P2	1.780(13)

C13(H13A	0.9900

C13(H13B	0.9900

C14(C16	1.427(18)

C14(C15	1.512(18)

C14(H14	1.0000

C15(H15A	0.9800

C15(H15B	0.9800

C15(H15C	0.9800

C16(H16A	0.9800

C16(H16B	0.9800

C16(H16C	0.9800

C17(C18	1.455(16)

C17(P2	1.836(14)

C17(H17A	0.9900

C17(H17B	0.9900

C18(C19	1.486(17)

C18(C20	1.500(17)

C18(H18	1.0000

C19(H19A	0.9800

C19(H19B	0.9800

C19(H19C	0.9800

C20(H20A	0.9800

C20(H20B	0.9800

C20(H20C	0.9800

C21(C22	1.53(2)

C21(P2	1.797(15)

C21(H21A	0.9900

C21(H21B	0.9900

C22(C24	1.412(19)

C22(C23	1.45(2)

C22(H22	1.0000

C23(H23A	0.9800

C23(H23B	0.9800

C23(H23C	0.9800

C24(H24A	0.9800

C24(H24B	0.9800

C24(H24C	0.9800

O2(P2	1.491(10)

C113(C114	1.553(17)

C113(P102	1.781(15)

C113(H11D	0.9900

C113(H11E	0.9900

C114(C116	1.469(19)

C114(C115	1.51(2)

C114(H114	1.0000

C115(H11F	0.9800

C115(H11G	0.9800

C115(H11H	0.9800

C116(H11I	0.9800

C116(H11J	0.9800

C116(H11K	0.9800

C117(C118	1.499(18)

C117(P102	1.840(15)

C117(H11L	0.9900

C117(H11M	0.9900

C118(C120	1.491(19)

C118(C119	1.506(19)

C118(H118	1.0000

C119(H11N	0.9800

C119(H11O	0.9800

C119(H11P	0.9800

C120(H12D	0.9800

C120(H12E	0.9800

C120(H12F	0.9800

C121(C122	1.56(2)

C121(P102	1.773(15)

C121(H12G	0.9900

C121(H12H	0.9900

C122(C124	1.42(2)

C122(C123	1.45(2)

C122(H122	1.0000

C123(H12I	0.9800

C123(H12J	0.9800

C123(H12K	0.9800

C124(H12L	0.9800

C124(H12M	0.9800

C124(H12N	0.9800

O102(P102	1.501(13)

C25(C26	1.535(17)

C25(P3	1.794(14)

C25(H25A	0.9900

C25(H25B	0.9900

C26(C28	1.496(19)

C26(C27	1.513(19)

C26(H26	1.0000

C27(H27A	0.9800

C27(H27B	0.9800

C27(H27C	0.9800

C28(H28A	0.9800

C28(H28B	0.9800

C28(H28C	0.9800

C29(C30	1.489(17)

C29(P3	1.796(15)

C29(H29A	0.9900

C29(H29B	0.9900

C30(C31	1.488(19)

C30(C32	1.492(19)

C30(H30	1.0000

C31(H31A	0.9800

C31(H31B	0.9800

C31(H31C	0.9800

C32(H32A	0.9800

C32(H32B	0.9800

C32(H32C	0.9800

C33(C34	1.547(19)

C33(P3	1.797(15)

C33(H33A	0.9900

C33(H33B	0.9900

C34(C36	1.45(2)

C34(C35	1.46(2)

C34(H34	1.0000

C35(H35A	0.9800

C35(H35B	0.9800

C35(H35C	0.9800

C36(H36A	0.9800

C36(H36B	0.9800

C36(H36C	0.9800

O3(P3	1.513(13)

C125(C126	1.539(16)

C125(P103	1.828(11)

C125(H12O	0.9900

C125(H12P	0.9900

C126(C128	1.453(16)

C126(C127	1.498(17)

C126(H126	1.0000

C127(H12Q	0.9800

C127(H12R	0.9800

C127(H12S	0.9800

C128(H12T	0.9800

C128(H12U	0.9800

C128(H12V	0.9800

C129(C130	1.479(15)

C129(P103	1.777(13)

C129(H12W	0.9900

C129(H12$	0.9900

C130(C132	1.461(16)

C130(C131	1.462(16)

C130(H130	1.0000

C131(H13C	0.9800

C131(H13D	0.9800

C131(H13E	0.9800

C132(H13F	0.9800

C132(H13G	0.9800

C132(H13H	0.9800

C133(C134	1.575(18)

C133(P103	1.796(12)

C133(H13I	0.9900

C133(H13J	0.9900

C134(C136	1.440(17)

C134(C135	1.453(18)

C134(H134	1.0000

C135(H13K	0.9800

C135(H13L	0.9800

C135(H13M	0.9800

C136(H13N	0.9800

C136(H13O	0.9800

C136(H13P	0.9800

O103(P103	1.504(9)

N11(O12	1.235(13)

N11(O13	1.237(10)

N11(O11	1.290(12)

N21(O23	1.203(11)

N21(O21	1.276(10)

N21(O22	1.294(11)

N31(O32	1.221(11)

N31(O31	1.251(13)

N31(O33	1.285(12)

O3(Sm1(O2	143.8(8)

O3(Sm1(O1	84.5(7)

O2(Sm1(O1	86.7(5)

O3(Sm1(O103	12.6(8)

O2(Sm1(O103	154.4(6)

O1(Sm1(O103	81.5(3)

O3(Sm1(O11	124.8(7)

O2(Sm1(O11	77.2(5)

O1(Sm1(O11	147.2(2)

O103(Sm1(O11	123.5(3)

O3(Sm1(O21	78.6(7)

O2(Sm1(O21	80.6(5)

O1(Sm1(O21	130.1(2)

O103(Sm1(O21	89.8(4)

O11(Sm1(O21	75.6(2)

O3(Sm1(O33	90.6(7)

O2(Sm1(O33	123.4(5)

O1(Sm1(O33	84.8(2)

O103(Sm1(O33	78.2(4)

O11(Sm1(O33	80.8(3)

O21(Sm1(O33	141.2(2)

O3(Sm1(O31	136.2(7)

O2(Sm1(O31	73.5(5)

O1(Sm1(O31	74.2(2)

O103(Sm1(O31	123.9(4)

O11(Sm1(O31	73.9(2)

O21(Sm1(O31	143.5(3)

O33(Sm1(O31	50.3(3)

O3(Sm1(O22	68.5(7)

O2(Sm1(O22	75.4(5)

O1(Sm1(O22	79.4(2)

O103(Sm1(O22	80.1(3)

O11(Sm1(O22	122.4(3)

O21(Sm1(O22	50.7(2)

O33(Sm1(O22	154.8(3)

O31(Sm1(O22	139.9(2)

O3(Sm1(O12	74.9(7)

O2(Sm1(O12	123.3(5)

O1(Sm1(O12	149.2(3)

O103(Sm1(O12	73.4(4)

O11(Sm1(O12	50.3(3)

O21(Sm1(O12	68.3(2)

O33(Sm1(O12	73.0(2)

O31(Sm1(O12	105.3(2)

O22(Sm1(O12	112.7(2)

O3(Sm1(O102	144.6(9)

O2(Sm1(O102	2.7(10)

O1(Sm1(O102	89.4(6)

O103(Sm1(O102	155.7(8)

O11(Sm1(O102	74.7(7)

O21(Sm1(O102	78.9(7)

O33(Sm1(O102	123.6(7)

O31(Sm1(O102	74.1(7)

O22(Sm1(O102	76.0(7)

O12(Sm1(O102	120.6(7)

O3(Sm1(N11	99.1(7)

O2(Sm1(N11	100.3(5)

O1(Sm1(N11	161.2(3)

O103(Sm1(N11	98.0(4)

O11(Sm1(N11	25.7(3)

O21(Sm1(N11	68.6(2)

O33(Sm1(N11	76.7(3)

O31(Sm1(N11	91.0(2)

O22(Sm1(N11	119.2(2)

O12(Sm1(N11	24.6(3)

O102(Sm1(N11	97.7(7)

C2(C1(P1	119.4(7)

C2(C1(H1A	107.5

P1(C1(H1A	107.5

C2(C1(H1B	107.5

P1(C1(H1B	107.5

H1A(C1(H1B	107.0

C4(C2(C3	109.8(10)

C4(C2(C1	109.2(9)

C3(C2(C1	109.9(9)

C4(C2(H2	109.3

C3(C2(H2	109.3

C1(C2(H2	109.3

C2(C3(H3A	109.5

C2(C3(H3B	109.5

H3A(C3(H3B	109.5

C2(C3(H3C	109.5

H3A(C3(H3C	109.5

H3B(C3(H3C	109.5

C2(C4(H4A	109.5

C2(C4(H4B	109.5

H4A(C4(H4B	109.5

C2(C4(H4C	109.5

H4A(C4(H4C	109.5

H4B(C4(H4C	109.5

C6(C5(P1	118.0(8)

C6(C5(H5A	107.8

P1(C5(H5A	107.8

C6(C5(H5B	107.8

P1(C5(H5B	107.8

H5A(C5(H5B	107.1

C7(C6(C5	112.1(9)

C7(C6(C8	110.7(9)

C5(C6(C8	110.7(9)

C7(C6(H6	107.7

C5(C6(H6	107.7

C8(C6(H6	107.7

C6(C7(H7A	109.5

C6(C7(H7B	109.5

H7A(C7(H7B	109.5

C6(C7(H7C	109.5

H7A(C7(H7C	109.5

H7B(C7(H7C	109.5

C6(C8(H8A	109.5

C6(C8(H8B	109.5

H8A(C8(H8B	109.5

C6(C8(H8C	109.5

H8A(C8(H8C	109.5

H8B(C8(H8C	109.5

C10(C9(P1	115.5(8)

C10(C9(H9A	108.4

P1(C9(H9A	108.4

C10(C9(H9B	108.4

P1(C9(H9B	108.4

H9A(C9(H9B	107.5

C12(C10(C11	108.0(15)

C12(C10(C9	111.4(13)

C11(C10(C9	107.1(12)

C12(C10(H10	110.1

C11(C10(H10	110.1

C9(C10(H10	110.1

C10(C11(H11A	109.5

C10(C11(H11B	109.5

H11A(C11(H11B	109.5

C10(C11(H11C	109.5

H11A(C11(H11C	109.5

H11B(C11(H11C	109.5

C10(C12(H12A	109.5

C10(C12(H12B	109.5

H12A(C12(H12B	109.5

C10(C12(H12C	109.5

H12A(C12(H12C	109.5

H12B(C12(H12C	109.5

P1(O1(Sm1	145.4(4)

O1(P1(C9	112.2(4)

O1(P1(C1	111.0(4)

C9(P1(C1	106.2(6)

O1(P1(C5	111.2(4)

C9(P1(C5	109.0(5)

C1(P1(C5	107.0(5)

C14(C13(P2	127.7(13)

C14(C13(H13A	105.4

P2(C13(H13A	105.4

C14(C13(H13B	105.4

P2(C13(H13B	105.4

H13A(C13(H13B	106.0

C16(C14(C13	119.9(18)

C16(C14(C15	115.2(18)

C13(C14(C15	118.6(18)

C16(C14(H14	98.4

C13(C14(H14	98.4

C15(C14(H14	98.4

C14(C15(H15A	109.5

C14(C15(H15B	109.5

H15A(C15(H15B	109.5

C14(C15(H15C	109.5

H15A(C15(H15C	109.5

H15B(C15(H15C	109.5

C14(C16(H16A	109.5

C14(C16(H16B	109.5

H16A(C16(H16B	109.5

C14(C16(H16C	109.5

H16A(C16(H16C	109.5

H16B(C16(H16C	109.5

C18(C17(P2	122.6(14)

C18(C17(H17A	106.7

P2(C17(H17A	106.7

C18(C17(H17B	106.7

P2(C17(H17B	106.7

H17A(C17(H17B	106.6

C17(C18(C19	116.7(17)

C17(C18(C20	111.6(17)

C19(C18(C20	111.8(15)

C17(C18(H18	105.2

C19(C18(H18	105.2

C20(C18(H18	105.2

C18(C19(H19A	109.5

C18(C19(H19B	109.5

H19A(C19(H19B	109.5

C18(C19(H19C	109.5

H19A(C19(H19C	109.5

H19B(C19(H19C	109.5

C18(C20(H20A	109.5

C18(C20(H20B	109.5

H20A(C20(H20B	109.5

C18(C20(H20C	109.5

H20A(C20(H20C	109.5

H20B(C20(H20C	109.5

C22(C21(P2	118.9(17)

C22(C21(H21A	107.6

P2(C21(H21A	107.6

C22(C21(H21B	107.6

P2(C21(H21B	107.6

H21A(C21(H21B	107.0

C24(C22(C23	108(2)

C24(C22(C21	122(2)

C23(C22(C21	109(2)

C24(C22(H22	105.4

C23(C22(H22	105.4

C21(C22(H22	105.4

C22(C23(H23A	109.5

C22(C23(H23B	109.5

H23A(C23(H23B	109.5

C22(C23(H23C	109.5

H23A(C23(H23C	109.5

H23B(C23(H23C	109.5

C22(C24(H24A	109.5

C22(C24(H24B	109.5

H24A(C24(H24B	109.5

C22(C24(H24C	109.5

H24A(C24(H24C	109.5

H24B(C24(H24C	109.5

P2(O2(Sm1	143.8(10)

O2(P2(C13	113.0(9)

O2(P2(C21	112.3(11)

C13(P2(C21	112.4(11)

O2(P2(C17	107.0(9)

C13(P2(C17	107.8(11)

C21(P2(C17	103.7(11)

C114(C113(P102	116.7(16)

C114(C113(H11D	108.1

P102(C113(H11D	108.1

C114(C113(H11E	108.1

P102(C113(H11E	108.1

H11D(C113(H11E	107.3

C116(C114(C115	108(2)

C116(C114(C113	111.0(19)

C115(C114(C113	112(2)

C116(C114(H114	108.5

C115(C114(H114	108.5

C113(C114(H114	108.5

C114(C115(H11F	109.5

C114(C115(H11G	109.5

H11F(C115(H11G	109.5

C114(C115(H11H	109.5

H11F(C115(H11H	109.5

H11G(C115(H11H	109.5

C114(C116(H11I	109.5

C114(C116(H11J	109.5

H11I(C116(H11J	109.5

C114(C116(H11K	109.5

H11I(C116(H11K	109.5

H11J(C116(H11K	109.5

C118(C117(P102	116.9(17)

C118(C117(H11L	108.1

P102(C117(H11L	108.1

C118(C117(H11M	108.1

P102(C117(H11M	108.1

H11L(C117(H11M	107.3

C120(C118(C117	108(2)

C120(C118(C119	110(2)

C117(C118(C119	113(2)

C120(C118(H118	108.5

C117(C118(H118	108.5

C119(C118(H118	108.5

C118(C119(H11N	109.5

C118(C119(H11O	109.5

H11N(C119(H11O	109.5

C118(C119(H11P	109.5

H11N(C119(H11P	109.5

H11O(C119(H11P	109.5

C118(C120(H12D	109.5

C118(C120(H12E	109.5

H12D(C120(H12E	109.5

C118(C120(H12F	109.5

H12D(C120(H12F	109.5

H12E(C120(H12F	109.5

C122(C121(P102	116.4(17)

C122(C121(H12G	108.2

P102(C121(H12G	108.2

C122(C121(H12H	108.2

P102(C121(H12H	108.2

H12G(C121(H12H	107.3

C124(C122(C123	111(3)

C124(C122(C121	117(2)

C123(C122(C121	104(2)

C124(C122(H122	108.0

C123(C122(H122	108.0

C121(C122(H122	108.0

C122(C123(H12I	109.5

C122(C123(H12J	109.5

H12I(C123(H12J	109.5

C122(C123(H12K	109.5

H12I(C123(H12K	109.5

H12J(C123(H12K	109.5

C122(C124(H12L	109.5

C122(C124(H12M	109.5

H12L(C124(H12M	109.5

C122(C124(H12N	109.5

H12L(C124(H12N	109.5

H12M(C124(H12N	109.5

P102(O102(Sm1	153.3(17)

O102(P102(C121	114.1(14)

O102(P102(C113	111.1(14)

C121(P102(C113	117.0(14)

O102(P102(C117	107.1(13)

C121(P102(C117	103.5(13)

C113(P102(C117	102.5(13)

C26(C25(P3	126.6(19)

C26(C25(H25A	105.7

P3(C25(H25A	105.7

C26(C25(H25B	105.7

P3(C25(H25B	105.7

H25A(C25(H25B	106.1

C28(C26(C27	103.2(19)

C28(C26(C25	109.1(19)

C27(C26(C25	113(2)

C28(C26(H26	110.3

C27(C26(H26	110.3

C25(C26(H26	110.3

C26(C27(H27A	109.5

C26(C27(H27B	109.5

H27A(C27(H27B	109.5

C26(C27(H27C	109.5

H27A(C27(H27C	109.5

H27B(C27(H27C	109.5

C26(C28(H28A	109.5

C26(C28(H28B	109.5

H28A(C28(H28B	109.5

C26(C28(H28C	109.5

H28A(C28(H28C	109.5

H28B(C28(H28C	109.5

C30(C29(P3	121.5(17)

C30(C29(H29A	106.9

P3(C29(H29A	106.9

C30(C29(H29B	106.9

P3(C29(H29B	106.9

H29A(C29(H29B	106.7

C29(C30(C31	119(2)

C29(C30(C32	108.5(19)

C31(C30(C32	111(2)

C29(C30(H30	105.8

C31(C30(H30	105.8

C32(C30(H30	105.8

C30(C31(H31A	109.5

C30(C31(H31B	109.5

H31A(C31(H31B	109.5

C30(C31(H31C	109.5

H31A(C31(H31C	109.5

H31B(C31(H31C	109.5

C30(C32(H32A	109.5

C30(C32(H32B	109.5

H32A(C32(H32B	109.5

C30(C32(H32C	109.5

H32A(C32(H32C	109.5

H32B(C32(H32C	109.5

C34(C33(P3	115.5(16)

C34(C33(H33A	108.4

P3(C33(H33A	108.4

C34(C33(H33B	108.4

P3(C33(H33B	108.4

H33A(C33(H33B	107.5

C36(C34(C35	105(2)

C36(C34(C33	116(2)

C35(C34(C33	107(2)

C36(C34(H34	109.7

C35(C34(H34	109.7

C33(C34(H34	109.7

C34(C35(H35A	109.5

C34(C35(H35B	109.5

H35A(C35(H35B	109.5

C34(C35(H35C	109.5

H35A(C35(H35C	109.5

H35B(C35(H35C	109.5

C34(C36(H36A	109.5

C34(C36(H36B	109.5

H36A(C36(H36B	109.5

C34(C36(H36C	109.5

H36A(C36(H36C	109.5

H36B(C36(H36C	109.5

P3(O3(Sm1	154.0(16)

O3(P3(C29	109.4(13)

O3(P3(C25	108.5(12)

C29(P3(C25	107.9(13)

O3(P3(C33	112.3(13)

C29(P3(C33	106.3(13)

C25(P3(C33	112.2(14)

C126(C125(P103	115.4(12)

C126(C125(H12O	108.4

P103(C125(H12O	108.4

C126(C125(H12P	108.4

P103(C125(H12P	108.4

H12O(C125(H12P	107.5

C128(C126(C127	108.1(15)

C128(C126(C125	116.3(15)

C127(C126(C125	112.9(16)

C128(C126(H126	106.3

C127(C126(H126	106.3

C125(C126(H126	106.3

C126(C127(H12Q	109.5

C126(C127(H12R	109.5

H12Q(C127(H12R	109.5

C126(C127(H12S	109.5

H12Q(C127(H12S	109.5

H12R(C127(H12S	109.5

C126(C128(H12T	109.5

C126(C128(H12U	109.5

H12T(C128(H12U	109.5

C126(C128(H12V	109.5

H12T(C128(H12V	109.5

H12U(C128(H12V	109.5

C130(C129(P103	118.1(11)

C130(C129(H12W	107.8

P103(C129(H12W	107.8

C130(C129(H12$	107.8

P103(C129(H12$	107.8

H12W(C129(H12$	107.1

C132(C130(C131	120.6(14)

C132(C130(C129	113.2(12)

C131(C130(C129	125.4(14)

C132(C130(H130	93.0

C131(C130(H130	93.0

C129(C130(H130	93.0

C130(C131(H13C	109.5

C130(C131(H13D	109.5

H13C(C131(H13D	109.5

C130(C131(H13E	109.5

H13C(C131(H13E	109.5

H13D(C131(H13E	109.5

C130(C132(H13F	109.5

C130(C132(H13G	109.5

H13F(C132(H13G	109.5

C130(C132(H13H	109.5

H13F(C132(H13H	109.5

H13G(C132(H13H	109.5

C134(C133(P103	114.5(12)

C134(C133(H13I	108.6

P103(C133(H13I	108.6

C134(C133(H13J	108.6

P103(C133(H13J	108.6

H13I(C133(H13J	107.6

C136(C134(C135	107.3(15)

C136(C134(C133	108.8(15)

C135(C134(C133	104.1(16)

C136(C134(H134	112.1

C135(C134(H134	112.1

C133(C134(H134	112.1

C134(C135(H13K	109.5

C134(C135(H13L	109.5

H13K(C135(H13L	109.5

C134(C135(H13M	109.5

H13K(C135(H13M	109.5

H13L(C135(H13M	109.5

C134(C136(H13N	109.5

C134(C136(H13O	109.5

H13N(C136(H13O	109.5

C134(C136(H13P	109.5

H13N(C136(H13P	109.5

H13O(C136(H13P	109.5

P103(O103(Sm1	155.7(7)

O103(P103(C129	112.4(9)

O103(P103(C133	111.7(9)

C129(P103(C133	108.3(9)

O103(P103(C125	108.8(8)

C129(P103(C125	108.1(9)

C133(P103(C125	107.4(9)

O12(N11(O13	122.6(11)

O12(N11(O11	117.2(8)

O13(N11(O11	120.1(11)

O12(N11(Sm1	60.2(5)

O13(N11(Sm1	174.3(9)

O11(N11(Sm1	57.3(4)

N11(O11(Sm1	97.0(6)

N11(O12(Sm1	95.1(6)

O23(N21(O21	122.0(9)

O23(N21(O22	123.0(9)

O21(N21(O22	115.0(9)

O23(N21(Sm1	175.5(10)

O21(N21(Sm1	56.3(5)

O22(N21(Sm1	58.8(5)

N21(O21(Sm1	98.6(6)

N21(O22(Sm1	95.5(5)

O32(N31(O31	122.1(11)

O32(N31(O33	123.1(12)

O31(N31(O33	114.9(10)

O32(N31(Sm1	175.3(7)

O31(N31(Sm1	57.7(5)

O33(N31(Sm1	57.4(6)

N31(O31(Sm1	97.5(6)

N31(O33(Sm1	97.0(7)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

Sm1	108(1) 	46(1)	31(1) 	2(1)	19(1) 	15(1)

C1	97(8) 	97(8)	36(5) 	2(5)	20(5) 	8(7)

C2	86(8) 	84(7)	48(5) 	12(5)	20(5) 	3(6)

C3	91(9) 	113(10)	65(7) 	27(7)	14(7) 	16(9)

C4	102(10) 	96(10)	65(7) 	22(7)	24(7) 	(6(8)

C5	93(8) 	74(7)	36(4) 	(12(4)	15(5) 	6(6)

C6	86(7) 	79(7)	46(5) 	(4(5)	19(5) 	6(6)

C7	93(10) 	102(10)	66(7) 	8(7)	9(7) 	13(8)

C8	69(8) 	89(9)	73(7) 	(24(7)	15(6) 	14(7)

C9	86(8) 	109(9)	47(6) 	15(6)	22(5) 	5(8)

C10	93(9) 	151(11)	97(8) 	5(9)	2(7) 	13(9)

C11	79(11) 	210(20)	249(19) 	47(18)	37(13) 	28(13)

C12	90(11) 	210(19)	135(13) 	(61(14)	8(10) 	(31(13)

O1	82(4) 	59(4)	30(3) 	2(3)	15(3) 	10(4)

P1	80(2) 	79(2)	34(1) 	1(1)	15(1) 	9(2)

C13	85(10) 	82(9)	110(10) 	(33(9)	19(9) 	(8(9)

C14	126(12) 	106(11)	151(11) 	(35(10)	16(10) 	7(10)

C15	147(19) 	132(18)	167(19) 	(62(16)	21(16) 	(1(16)

C16	134(16) 	121(15)	163(16) 	(33(16)	28(14) 	2(14)

C17	116(15) 	117(14)	112(12) 	(5(11)	(7(12) 	(2(12)

C18	117(13) 	107(12)	86(10) 	(18(10)	(21(10) 	7(10)

C19	116(15) 	86(15)	97(13) 	(44(13)	6(12) 	(25(14)

C20	129(19) 	135(19)	126(17) 	(85(15)	(36(15) 	31(15)

C21	125(16) 	116(15)	280(20) 	(38(16)	82(17) 	(48(14)

C22	128(16) 	119(14)	280(20) 	(20(16)	73(17) 	(39(13)

C23	124(19) 	110(19)	290(30) 	(20(20)	80(20) 	(62(16)

C24	160(30) 	170(30)	330(30) 	0(30)	10(30) 	(10(20)

O2	64(8) 	43(6)	45(5) 	(6(5)	25(6) 	(29(5)

P2	74(6) 	68(3)	59(3) 	(13(3)	(1(4) 	(10(5)

C113	105(13) 	88(12)	130(12) 	(45(11)	26(11) 	14(11)

C114	136(13) 	112(12)	157(13) 	(36(12)	17(12) 	9(11)

C115	155(19) 	122(18)	170(20) 	(19(19)	19(19) 	0(18)

C116	135(18) 	122(18)	153(19) 	(31(18)	23(17) 	6(17)

C117	118(16) 	115(15)	116(14) 	10(13)	(21(14) 	2(14)

C118	117(14) 	111(13)	104(12) 	4(12)	(20(12) 	7(12)

C119	120(20) 	150(30)	100(20) 	40(20)	(40(19) 	30(20)

C120	107(17) 	83(18)	98(16) 	8(17)	(9(15) 	28(17)

C121	116(18) 	116(16)	280(20) 	(42(18)	80(19) 	(32(16)

C122	118(16) 	109(15)	280(20) 	(34(16)	78(17) 	(35(14)

C123	110(20) 	130(20)	280(30) 	(20(20)	90(20) 	(75(18)

C124	80(20) 	30(14)	250(30) 	(10(20)	60(20) 	1(15)

O102	47(9) 	55(8)	50(7) 	(23(7)	3(8) 	(8(8)

P102	34(6) 	78(5)	60(5) 	(31(4)	6(5) 	0(5)

C25	71(10) 	96(11)	66(9) 	(47(9)	20(9) 	(11(10)

C26	77(9) 	98(10)	80(10) 	(46(9)	16(9) 	(17(9)

C27	96(19) 	120(20)	120(20) 	(77(18)	(9(19) 	(15(18)

C28	100(18) 	80(20)	66(18) 	(25(16)	21(17) 	(1(18)

C29	76(10) 	82(10)	80(8) 	(30(9)	8(9) 	9(9)

C30	82(11) 	94(11)	90(9) 	(37(9)	5(9) 	21(10)

C31	77(16) 	97(18)	80(15) 	(27(15)	(4(14) 	0(16)

C32	94(17) 	97(17)	99(16) 	(16(15)	15(15) 	25(15)

C33	105(11) 	52(9)	71(9) 	5(9)	3(9) 	4(9)

C34	116(11) 	61(10)	75(10) 	10(9)	(4(9) 	(4(9)

C35	160(20) 	120(20)	120(20) 	(10(20)	(20(20) 	0(20)

C36	120(20) 	97(19)	55(15) 	18(15)	(11(16) 	(7(17)

O3	45(7) 	50(4)	51(4) 	7(3)	20(6) 	(10(6)

P3	34(7) 	58(6)	50(5) 	(3(4)	18(5) 	8(6)

C125	72(9) 	95(10)	64(8) 	(44(7)	17(7) 	(8(8)

C126	75(8) 	99(10)	80(9) 	(53(8)	16(8) 	(18(8)

C127	104(14) 	126(16)	154(17) 	(62(14)	0(15) 	(13(13)

C128	109(14) 	102(15)	131(17) 	(51(13)	(1(14) 	15(13)

C129	81(10) 	96(11)	90(9) 	(32(9)	1(8) 	25(9)

C130	77(9) 	94(10)	90(8) 	(40(8)	2(8) 	18(8)

C131	120(15) 	128(16)	102(13) 	(42(13)	(3(12) 	56(14)

C132	50(10) 	57(9)	86(11) 	(11(9)	13(9) 	8(8)

C133	100(10) 	49(8)	74(8) 	6(7)	7(8) 	6(7)

C134	121(10) 	56(8)	54(8) 	(1(6)	(11(8) 	(2(8)

C135	155(15) 	72(12)	95(12) 	31(10)	(26(12) 	(29(13)

C136	106(16) 	73(12)	135(18) 	1(13)	(26(14) 	(8(12)

O103	45(7) 	50(4)	51(4) 	7(3)	20(6) 	(10(6)

P103	59(6) 	59(3)	63(3) 	(16(3)	19(4) 	(7(4)

N11	123(7) 	68(5)	40(4) 	(4(4)	16(5) 	18(5)

O11	133(7) 	59(4)	32(3) 	0(3)	20(4) 	21(5)

O12	134(7) 	70(5)	40(3) 	(3(4)	25(4) 	15(5)

O13	160(9) 	106(7)	40(4) 	(24(4)	30(5) 	5(6)

N21	123(7) 	59(5)	50(4) 	(1(4)	11(5) 	30(5)

O21	120(6) 	55(4)	39(3) 	6(3)	17(3) 	28(4)

O22	108(6) 	59(4)	38(3) 	(4(4)	6(4) 	19(4)

O23	141(9) 	91(7)	68(5) 	(4(5)	(15(5) 	60(6)

N31	119(7) 	72(6)	36(4) 	1(4)	17(5) 	28(6)

O31	120(7) 	67(5)	38(4) 	10(3)	15(4) 	13(5)

O32	137(8) 	99(7)	52(4) 	20(4)	10(5) 	59(6)

O33	104(6) 	67(5)	38(4) 	4(3)	16(4) 	20(4)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H1A	4017	9584	2323	92	1

H1B	4739	8831	2307	92	1

H2	4407	9599	2897	87	1

H3A	4704	8093	3051	135	1

H3B	5520	8574	2892	135	1

H3C	4943	7890	2700	135	1

H4A	3325	8274	2636	131	1

H4B	3017	9264	2693	131	1

H4C	3240	8644	2979	131	1

H5A	5266	10991	2805	81	1

H5B	5476	11618	2521	81	1

H6	3787	10911	2641	85	1

H7A	4295	12180	2197	130	1

H7B	3293	11989	2284	130	1

H7C	3876	11238	2128	130	1

H8A	4478	12575	2806	115	1

H8B	4030	11870	3029	115	1

H8C	3443	12406	2789	115	1

H9A	6402	9790	2728	97	1

H9B	6388	9076	2460	97	1

H10	7228	10064	2140	137	1

H11A	8502	9690	2371	271	1

H11B	7827	8958	2488	271	1

H11C	8085	9757	2708	271	1

H12A	7543	11001	2678	217	1

H12B	6794	11301	2442	217	1

H12C	7796	11263	2333	217	1

H13A	2028	8322	1679	111	0.619(8)

H13B	2592	8354	1984	111	0.619(8)

H14	1623	9569	1701	153	0.619(8)

H15A	1520	9297	2327	223	0.619(8)

H15B	883	8913	2067	223	0.619(8)

H15C	924	9948	2128	223	0.619(8)

H16A	2778	10364	1696	209	0.619(8)

H16B	2827	10350	2063	209	0.619(8)

H16C	2002	10786	1895	209	0.619(8)

H17A	2912	9386	1151	138	0.619(8)

H17B	3709	8785	1047	138	0.619(8)

H18	2351	7772	1154	124	0.619(8)

H19A	1432	8930	1051	150	0.619(8)

H19B	1346	8172	798	150	0.619(8)

H19C	1878	9050	720	150	0.619(8)

H20A	2981	7072	805	195	0.619(8)

H20B	3626	7882	744	195	0.619(8)

H20C	2727	7802	556	195	0.619(8)

H21A	3447	7111	1496	207	0.619(8)

H21B	4388	7507	1420	207	0.619(8)

H22	4416	7669	2002	212	0.619(8)

H23A	3385	6181	1927	260	0.619(8)

H23B	3056	7108	2056	260	0.619(8)

H23C	3763	6550	2245	260	0.619(8)

H24A	5535	6956	1901	325	0.619(8)

H24B	5032	6244	1696	325	0.619(8)

H24C	4964	6207	2063	325	0.619(8)

H11D	1794	8319	1837	129	0.381(8)

H11E	2519	8679	2069	129	0.381(8)

H114	1144	9588	1915	162	0.381(8)

H11F	1836	10836	2114	223	0.381(8)

H11G	2775	10380	2075	223	0.381(8)

H11H	2084	9998	2318	223	0.381(8)

H11I	1932	10762	1608	206	0.381(8)

H11J	1338	10022	1450	206	0.381(8)

H11K	2380	9905	1465	206	0.381(8)

H11L	2494	9763	1278	140	0.381(8)

H11M	2981	9067	1064	140	0.381(8)

H118	1437	8428	1311	133	0.381(8)

H11N	693	9635	1224	186	0.381(8)

H11O	678	9263	880	186	0.381(8)

H11P	1378	9996	976	186	0.381(8)

H12D	1294	7872	820	144	0.381(8)

H12E	2282	7721	932	144	0.381(8)

H12F	2061	8497	696	144	0.381(8)

H12G	2722	7203	1467	204	0.381(8)

H12H	3480	7547	1244	204	0.381(8)

H122	4568	7255	1602	201	0.381(8)

H12I	3241	6940	2035	263	0.381(8)

H12J	3699	7875	1988	263	0.381(8)

H12K	4267	7055	2103	263	0.381(8)

H12L	4572	5869	1678	180	0.381(8)

H12M	3917	5956	1393	180	0.381(8)

H12N	3535	5819	1732	180	0.381(8)

H25A	5292	12534	1715	93	0.347(10)

H25B	5941	12081	1950	93	0.347(10)

H26	6225	13834	1737	102	0.347(10)

H27A	7256	13954	2099	165	0.347(10)

H27B	7372	12929	2031	165	0.347(10)

H27C	6801	13247	2319	165	0.347(10)

H28A	4893	13415	2063	125	0.347(10)

H28B	5400	14320	2119	125	0.347(10)

H28C	5602	13490	2333	125	0.347(10)

H29A	7868	12233	1605	95	0.347(10)

H29B	7499	11416	1791	95	0.347(10)

H30	7734	10566	1341	107	0.347(10)

H31A	8113	11245	934	127	0.347(10)

H31B	9076	11134	1075	127	0.347(10)

H31C	8560	12041	1116	127	0.347(10)

H32A	8569	10209	1719	145	0.347(10)

H32B	8995	11164	1751	145	0.347(10)

H32C	9308	10519	1481	145	0.347(10)

H33A	6686	13239	1200	91	0.347(10)

H33B	7082	12434	1011	91	0.347(10)

H34	5267	12969	1014	101	0.347(10)

H35A	5246	11698	650	205	0.347(10)

H35B	5102	11550	1011	205	0.347(10)

H35C	6044	11375	861	205	0.347(10)

H36A	6350	12675	499	134	0.347(10)

H36B	6122	13630	628	134	0.347(10)

H36C	5360	13023	492	134	0.347(10)

H12O	5457	12399	1754	93	0.653(10)

H12P	6280	12307	1979	93	0.653(10)

H126	6052	13771	1578	102	0.653(10)

H12Q	7220	14382	1753	192	0.653(10)

H12R	7498	13389	1821	192	0.653(10)

H12S	7110	13985	2091	192	0.653(10)

H12T	5676	13855	2206	171	0.653(10)

H12U	4956	13841	1938	171	0.653(10)

H12V	5625	14646	1964	171	0.653(10)

H12W	8078	12559	1556	107	0.653(10)

H12$	7841	11843	1810	107	0.653(10)

H130	8191	10829	1561	104	0.653(10)

H13C	7760	10419	1182	176	0.653(10)

H13D	8737	10600	1063	176	0.653(10)

H13E	7975	11294	993	176	0.653(10)

H13F	9634	10858	1452	96	0.653(10)

H13G	9248	11138	1780	96	0.653(10)

H13H	9562	11873	1542	96	0.653(10)

H13I	6964	13235	1172	89	0.653(10)

H13J	6899	12380	962	89	0.653(10)

H134	5247	12914	1223	93	0.653(10)

H13K	4820	12149	827	161	0.653(10)

H13L	5813	11813	819	161	0.653(10)

H13M	5513	12607	602	161	0.653(10)

H13N	6010	13792	716	157	0.653(10)

H13O	5939	14226	1050	157	0.653(10)

H13P	5068	13993	862	157	0.653(10)