|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	2009src1245 / Dy iBu

Empirical formula 	C36H81DyN3O12P3

Formula weight 	1003.45

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Tetragonal

Space group 	P43212

Unit cell dimensions	a = 15.3937(10) Å	( = 90°

b = 15.3937(10) Å	( = 90°

c = 43.421(4) Å	(  = 90°

Volume	10289.2(13) Å3

Z	8

Density (calculated)	1.296 Mg / m3

Absorption coefficient	1.597 mm(1

F(000)	4200

Crystal	Plate; Colourless

Crystal size	0.90 ( 0.66 ( 0.12 mm3

( range for data collection	2.96 ( 25.00°

Index ranges	(18 ( h ( 18, (18 ( k ( 18, (42 ( l ( 51

Reflections collected	35049

Independent reflections	8880 [Rint = 0.0833]

Completeness to ( = 25.00°	98.7 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.8314 and 0.3274

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	8880 / 976 / 751

Goodness-of-fit on F2	1.048

Final R indices [F2 > 2((F2)]	R1 = 0.0801, wR2 = 0.2233

R indices (all data)	R1 = 0.1082, wR2 = 0.2577

Absolute structure parameter	0.16(3)

Largest diff. peak and hole	1.449 and (1.907 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP3 for Windows (L. J. Farrugia, J. Appl. Crystallogr. 1997, 30, 565).

Special details:

All hydrogen atoms were fixed using a standard riding model.

Two of the three phosphorus ligands were disordered. This resulted in all the ligands been restrained to be similar using the SAME compound. Also a loose global thermal restraint (SIMU) was used.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

Dy1	70(1)	5322(1)	984(1)	55(1)	1

C1	586(8)	4527(9)	84(3)	75(4)	1

C2	865(11)	4285(11)	(251(3)	91(4)	1

C3	1111(13)	3356(12)	(266(4)	103(5)	1

C4	1532(11)	4818(13)	(375(3)	101(5)	1

C5	(1137(8)	5135(9)	(86(3)	68(3)	1

C6	(1483(10)	4212(10)	(79(3)	79(3)	1

C7	(2155(11)	4073(11)	(339(4)	93(5)	1

C8	(1875(12)	3972(13)	226(3)	97(5)	1

C9	301(10)	6360(8)	(1(3)	84(4)	1

C10	(48(12)	7175(10)	120(4)	97(4)	1

C11	526(15)	7971(13)	(15(5)	127(6)	1

C12	(920(12)	7334(12)	37(4)	114(6)	1

O1	(417(5)	5449(6)	487(2)	59(2)	1

P1	(188(2)	5378(2)	143(1)	60(1)	1

C13	(2546(14)	6058(19)	780(6)	75(4)	0.488(10)

C14	(3553(15)	6202(18)	784(7)	79(5)	0.488(10)

C15	(4045(19)	5670(20)	568(7)	87(6)	0.488(10)

C16	(3850(20)	7064(19)	792(8)	94(6)	0.488(10)

C17	(2525(16)	6564(14)	1443(4)	59(4)	0.488(10)

C18	(2412(16)	5737(14)	1646(4)	60(4)	0.488(10)

C19	(2942(19)	5917(18)	1949(4)	67(7)	0.488(10)

C20	(2840(20)	4964(17)	1500(6)	78(6)	0.488(10)

C21	(1966(17)	7749(14)	955(6)	83(4)	0.488(10)

C22	(1407(19)	8400(17)	1103(6)	89(4)	0.488(10)

C23	(780(20)	8830(30)	839(7)	101(7)	0.488(10)

C24	(780(20)	8110(20)	1312(7)	96(7)	0.488(10)

O2	(1035(12)	6310(15)	1097(6)	62(3)	0.488(10)

P2	(1943(9)	6631(10)	1080(3)	59(2)	0.488(10)

C113	(2433(14)	6102(18)	662(5)	74(5)	0.512(10)

C114	(3428(16)	6230(17)	606(7)	81(4)	0.512(10)

C115	(3800(20)	5610(20)	382(6)	88(7)	0.512(10)

C116	(3640(20)	7088(18)	524(8)	94(7)	0.512(10)

C117	(2694(15)	6676(14)	1306(5)	60(4)	0.512(10)

C118	(2903(15)	5830(14)	1472(5)	65(4)	0.512(10)

C119	(3857(16)	5860(20)	1596(8)	92(8)	0.512(10)

C120	(2800(20)	4958(17)	1338(8)	102(7)	0.512(10)

C121	(1640(20)	7721(13)	884(6)	86(5)	0.512(10)

C122	(1121(19)	8302(16)	1078(6)	89(4)	0.512(10)

C123	(1290(20)	9288(16)	938(7)	92(6)	0.512(10)

C124	(1320(20)	8470(20)	1389(6)	92(6)	0.512(10)

O102	(1147(12)	6115(13)	1078(6)	60(3)	0.512(10)

P102	(1929(9)	6643(10)	986(3)	67(2)	0.512(10)

C25	1114(19)	3110(20)	1336(5)	117(8)	0.455(12)

C26	1740(20)	2470(20)	1503(7)	120(8)	0.455(12)

C27	1270(30)	1750(20)	1658(11)	122(8)	0.455(12)

C28	2310(20)	2920(20)	1702(10)	126(11)	0.455(12)

C29	1250(20)	2473(18)	691(8)	81(4)	0.455(12)

C30	430(20)	1900(20)	698(8)	92(5)	0.455(12)

C31	550(30)	1220(30)	433(11)	104(7)	0.455(12)

C32	(400(20)	2350(30)	612(12)	106(7)	0.455(12)

C33	2383(14)	3880(20)	920(6)	87(5)	0.455(12)

C34	2710(20)	4220(20)	632(7)	94(5)	0.455(12)

C35	3300(20)	5080(20)	647(9)	122(10)	0.455(12)

C36	3060(30)	3730(30)	396(8)	106(9)	0.455(12)

O3	639(18)	4092(16)	841(7)	60(4)	0.455(12)

P3	1293(9)	3413(9)	940(3)	69(3)	0.455(12)

C125	739(17)	2693(18)	1303(6)	120(8)	0.545(12)

C126	1152(18)	1814(18)	1414(7)	124(8)	0.545(12)

C127	510(20)	1140(20)	1487(10)	133(9)	0.545(12)

C128	1789(19)	1950(20)	1640(8)	121(9)	0.545(12)

C129	1127(18)	2256(18)	651(7)	90(5)	0.545(12)

C130	290(20)	1738(19)	594(7)	98(5)	0.545(12)

C131	470(30)	1050(20)	338(10)	114(8)	0.545(12)

C132	(460(20)	2260(30)	484(9)	107(8)	0.545(12)

C133	2292(11)	3345(18)	1006(5)	80(4)	0.545(12)

C134	2817(14)	3821(19)	781(6)	91(5)	0.545(12)

C135	3790(15)	3940(20)	921(8)	108(8)	0.545(12)

C136	3010(20)	3400(20)	501(6)	99(7)	0.545(12)

O103	664(16)	3906(13)	843(7)	59(3)	0.545(12)

P103	1155(7)	3103(6)	943(3)	60(2)	0.545(12)

N11	1066(8)	5675(9)	1541(3)	72(2)	1

O11	357(7)	6027(7)	1505(2)	78(3)	1

O12	1342(6)	5186(7)	1321(2)	71(2)	1

O13	1479(8)	5753(8)	1773(2)	87(3)	1

N21	1364(7)	6442(9)	713(3)	68(3)	1

O21	749(6)	6748(7)	889(2)	69(2)	1

O22	1373(5)	5651(7)	668(2)	66(2)	1

O23	1885(7)	6949(8)	577(2)	83(3)	1

N31	(1063(8)	4021(9)	1261(3)	75(3)	1

O31	(1194(6)	4306(7)	984(2)	73(2)	1

O32	(464(6)	4410(6)	1407(2)	70(2)	1

O33	(1478(7)	3446(8)	1380(3)	90(3)	1

Table 3. Bond lengths [Å] and angles [°].

Dy1(O3	2.18(2)

Dy1(O102	2.274(18)

Dy1(O1	2.293(8)

Dy1(O2	2.334(19)

Dy1(O103	2.44(2)

Dy1(O12	2.454(9)

Dy1(O32	2.455(9)

Dy1(O21	2.467(10)

Dy1(O22	2.481(9)

Dy1(O31	2.496(9)

Dy1(O11	2.548(10)

Dy1(N21	2.884(11)

C1(C2	1.561(15)

C1(P1	1.790(11)

C1(H1A	0.9900

C1(H1B	0.9900

C2(C4	1.422(19)

C2(C3	1.48(2)

C2(H2	1.0000

C3(H3A	0.9800

C3(H3B	0.9800

C3(H3C	0.9800

C4(H4A	0.9800

C4(H4B	0.9800

C4(H4C	0.9800

C5(C6	1.517(17)

C5(P1	1.806(11)

C5(H5A	0.9900

C5(H5B	0.9900

C6(C8	1.502(17)

C6(C7	1.545(16)

C6(H6	1.0000

C7(H7A	0.9800

C7(H7B	0.9800

C7(H7C	0.9800

C8(H8A	0.9800

C8(H8B	0.9800

C8(H8C	0.9800

C9(C10	1.462(18)

C9(P1	1.801(13)

C9(H9A	0.9900

C9(H9B	0.9900

C10(C12	1.411(19)

C10(C11	1.62(2)

C10(H10	1.0000

C11(H11A	0.9800

C11(H11B	0.9800

C11(H11C	0.9800

C12(H12A	0.9800

C12(H12B	0.9800

C12(H12C	0.9800

O1(P1	1.536(8)

C13(C14	1.566(19)

C13(P2	1.825(15)

C13(H13A	0.9900

C13(H13B	0.9900

C14(C16	1.40(2)

C14(C15	1.46(2)

C14(H14	1.0000

C15(H15A	0.9800

C15(H15B	0.9800

C15(H15C	0.9800

C16(H16A	0.9800

C16(H16B	0.9800

C16(H16C	0.9800

C17(C18	1.56(2)

C17(P2	1.816(15)

C17(H17A	0.9900

C17(H17B	0.9900

C18(C20	1.50(2)

C18(C19	1.572(19)

C18(H18	1.0000

C19(H19A	0.9800

C19(H19B	0.9800

C19(H19C	0.9800

C20(H20A	0.9800

C20(H20B	0.9800

C20(H20C	0.9800

C21(C22	1.47(2)

C21(P2	1.806(17)

C21(H21A	0.9900

C21(H21B	0.9900

C22(C24	1.40(2)

C22(C23	1.64(2)

C22(H22	1.0000

C23(H23A	0.9800

C23(H23B	0.9800

C23(H23C	0.9800

C24(H24A	0.9800

C24(H24B	0.9800

C24(H24C	0.9800

O2(P2	1.485(13)

C113(C114	1.563(19)

C113(P102	1.808(15)

C113(H11D	0.9900

C113(H11E	0.9900

C114(C116	1.40(2)

C114(C115	1.48(2)

C114(H114	1.0000

C115(H11F	0.9800

C115(H11G	0.9800

C115(H11H	0.9800

C116(H11I	0.9800

C116(H11J	0.9800

C116(H11K	0.9800

C117(C118	1.523(19)

C117(P102	1.820(15)

C117(H11L	0.9900

C117(H11M	0.9900

C118(C120	1.47(2)

C118(C119	1.56(2)

C118(H118	1.0000

C119(H11N	0.9800

C119(H11O	0.9800

C119(H11P	0.9800

C120(H12D	0.9800

C120(H12E	0.9800

C120(H12F	0.9800

C121(C122	1.47(2)

C121(P102	1.772(16)

C121(H12G	0.9900

C121(H12H	0.9900

C122(C124	1.41(2)

C122(C123	1.65(2)

C122(H122	1.0000

C123(H12I	0.9800

C123(H12J	0.9800

C123(H12K	0.9800

C124(H12L	0.9800

C124(H12M	0.9800

C124(H12N	0.9800

O102(P102	1.506(12)

C25(C26	1.564(19)

C25(P3	1.803(16)

C25(H25A	0.9900

C25(H25B	0.9900

C26(C28	1.41(2)

C26(C27	1.48(2)

C26(H26	1.0000

C27(H27A	0.9800

C27(H27B	0.9800

C27(H27C	0.9800

C28(H28A	0.9800

C28(H28B	0.9800

C28(H28C	0.9800

C29(C30	1.54(2)

C29(P3	1.806(16)

C29(H29A	0.9900

C29(H29B	0.9900

C30(C32	1.49(2)

C30(C31	1.57(2)

C30(H30	1.0000

C31(H31A	0.9800

C31(H31B	0.9800

C31(H31C	0.9800

C32(H32A	0.9800

C32(H32B	0.9800

C32(H32C	0.9800

C33(C34	1.45(2)

C33(P3	1.825(17)

C33(H33A	0.9900

C33(H33B	0.9900

C34(C36	1.38(2)

C34(C35	1.61(2)

C34(H34	1.0000

C35(H35A	0.9800

C35(H35B	0.9800

C35(H35C	0.9800

C36(H36A	0.9800

C36(H36B	0.9800

C36(H36C	0.9800

O3(P3	1.513(13)

C125(C126	1.571(19)

C125(P103	1.800(16)

C125(H12O	0.9900

C125(H12P	0.9900

C126(C128	1.40(2)

C126(C127	1.47(2)

C126(H126	1.0000

C127(H12Q	0.9800

C127(H12R	0.9800

C127(H12S	0.9800

C128(H12T	0.9800

C128(H12U	0.9800

C128(H12V	0.9800

C129(C130	1.53(2)

C129(P103	1.818(15)

C129(H12W	0.9900

C129(H12$	0.9900

C130(C132	1.49(2)

C130(C131	1.56(2)

C130(H130	1.0000

C131(H13C	0.9800

C131(H13D	0.9800

C131(H13E	0.9800

C132(H13F	0.9800

C132(H13G	0.9800

C132(H13H	0.9800

C133(C134	1.47(2)

C133(P103	1.811(16)

C133(H13I	0.9900

C133(H13J	0.9900

C134(C136	1.41(2)

C134(C135	1.63(2)

C134(H134	1.0000

C135(H13K	0.9800

C135(H13L	0.9800

C135(H13M	0.9800

C136(H13N	0.9800

C136(H13O	0.9800

C136(H13P	0.9800

O103(P103	1.512(12)

N11(O13	1.197(14)

N11(O11	1.229(17)

N11(O12	1.287(15)

N21(O22	1.234(15)

N21(O23	1.265(14)

N21(O21	1.302(15)

N31(O33	1.209(15)

N31(O32	1.270(14)

N31(O31	1.295(15)

O3(Dy1(O102	148.3(10)

O3(Dy1(O1	86.5(8)

O102(Dy1(O1	81.6(7)

O3(Dy1(O2	157.0(10)

O102(Dy1(O2	8.7(9)

O1(Dy1(O2	84.5(7)

O3(Dy1(O103	2.9(14)

O102(Dy1(O103	146.4(8)

O1(Dy1(O103	87.9(6)

O2(Dy1(O103	155.1(9)

O3(Dy1(O12	77.0(8)

O102(Dy1(O12	126.6(6)

O1(Dy1(O12	146.1(3)

O2(Dy1(O12	120.7(6)

O103(Dy1(O12	77.0(6)

O3(Dy1(O32	81.4(9)

O102(Dy1(O32	84.0(7)

O1(Dy1(O32	130.1(3)

O2(Dy1(O32	88.3(7)

O103(Dy1(O32	78.6(7)

O12(Dy1(O32	76.8(3)

O3(Dy1(O21	123.8(9)

O102(Dy1(O21	84.3(6)

O1(Dy1(O21	84.6(3)

O2(Dy1(O21	76.3(6)

O103(Dy1(O21	126.5(7)

O12(Dy1(O21	80.6(3)

O32(Dy1(O21	140.9(3)

O3(Dy1(O22	72.3(9)

O102(Dy1(O22	131.0(7)

O1(Dy1(O22	74.2(3)

O2(Dy1(O22	124.9(7)

O103(Dy1(O22	75.1(7)

O12(Dy1(O22	72.7(3)

O32(Dy1(O22	143.2(3)

O21(Dy1(O22	51.9(3)

O3(Dy1(O31	76.7(9)

O102(Dy1(O31	72.2(6)

O1(Dy1(O31	78.4(3)

O2(Dy1(O31	80.8(6)

O103(Dy1(O31	74.5(7)

O12(Dy1(O31	124.6(4)

O32(Dy1(O31	51.7(3)

O21(Dy1(O31	152.6(4)

O22(Dy1(O31	139.4(3)

O3(Dy1(O11	123.6(8)

O102(Dy1(O11	75.8(6)

O1(Dy1(O11	148.9(3)

O2(Dy1(O11	70.2(7)

O103(Dy1(O11	122.5(6)

O12(Dy1(O11	50.8(3)

O32(Dy1(O11	68.7(3)

O21(Dy1(O11	72.3(3)

O22(Dy1(O11	105.2(3)

O31(Dy1(O11	113.6(3)

O3(Dy1(N21	97.3(9)

O102(Dy1(N21	108.7(7)

O1(Dy1(N21	78.0(3)

O2(Dy1(N21	101.5(7)

O103(Dy1(N21	100.0(7)

O12(Dy1(N21	75.1(3)

O32(Dy1(N21	151.4(3)

O21(Dy1(N21	26.8(3)

O22(Dy1(N21	25.2(3)

O31(Dy1(N21	156.0(3)

O11(Dy1(N21	89.2(3)

C2(C1(P1	119.4(10)

C2(C1(H1A	107.5

P1(C1(H1A	107.5

C2(C1(H1B	107.5

P1(C1(H1B	107.5

H1A(C1(H1B	107.0

C4(C2(C3	110.8(14)

C4(C2(C1	114.6(13)

C3(C2(C1	110.1(13)

C4(C2(H2	107.0

C3(C2(H2	107.0

C1(C2(H2	107.0

C2(C3(H3A	109.5

C2(C3(H3B	109.5

H3A(C3(H3B	109.5

C2(C3(H3C	109.5

H3A(C3(H3C	109.5

H3B(C3(H3C	109.5

C2(C4(H4A	109.5

C2(C4(H4B	109.5

H4A(C4(H4B	109.5

C2(C4(H4C	109.5

H4A(C4(H4C	109.5

H4B(C4(H4C	109.5

C6(C5(P1	117.9(9)

C6(C5(H5A	107.8

P1(C5(H5A	107.8

C6(C5(H5B	107.8

P1(C5(H5B	107.8

H5A(C5(H5B	107.2

C8(C6(C5	112.8(12)

C8(C6(C7	109.9(13)

C5(C6(C7	110.6(11)

C8(C6(H6	107.8

C5(C6(H6	107.8

C7(C6(H6	107.8

C6(C7(H7A	109.5

C6(C7(H7B	109.5

H7A(C7(H7B	109.5

C6(C7(H7C	109.5

H7A(C7(H7C	109.5

H7B(C7(H7C	109.5

C6(C8(H8A	109.5

C6(C8(H8B	109.5

H8A(C8(H8B	109.5

C6(C8(H8C	109.5

H8A(C8(H8C	109.5

H8B(C8(H8C	109.5

C10(C9(P1	116.3(11)

C10(C9(H9A	108.2

P1(C9(H9A	108.2

C10(C9(H9B	108.2

P1(C9(H9B	108.2

H9A(C9(H9B	107.4

C12(C10(C9	114.0(15)

C12(C10(C11	107.2(15)

C9(C10(C11	108.6(14)

C12(C10(H10	109.0

C9(C10(H10	109.0

C11(C10(H10	109.0

C10(C11(H11A	109.5

C10(C11(H11B	109.5

H11A(C11(H11B	109.5

C10(C11(H11C	109.5

H11A(C11(H11C	109.5

H11B(C11(H11C	109.5

C10(C12(H12A	109.5

C10(C12(H12B	109.5

H12A(C12(H12B	109.5

C10(C12(H12C	109.5

H12A(C12(H12C	109.5

H12B(C12(H12C	109.5

P1(O1(Dy1	146.3(5)

O1(P1(C1	110.1(5)

O1(P1(C9	112.0(6)

C1(P1(C9	106.6(7)

O1(P1(C5	111.3(5)

C1(P1(C5	107.9(6)

C9(P1(C5	108.7(7)

C14(C13(P2	115.4(14)

C14(C13(H13A	108.4

P2(C13(H13A	108.4

C14(C13(H13B	108.4

P2(C13(H13B	108.4

H13A(C13(H13B	107.5

C16(C14(C15	112(2)

C16(C14(C13	117(2)

C15(C14(C13	115.4(19)

C16(C14(H14	103.2

C15(C14(H14	103.2

C13(C14(H14	103.2

C14(C15(H15A	109.5

C14(C15(H15B	109.5

H15A(C15(H15B	109.5

C14(C15(H15C	109.5

H15A(C15(H15C	109.5

H15B(C15(H15C	109.5

C14(C16(H16A	109.5

C14(C16(H16B	109.5

H16A(C16(H16B	109.5

C14(C16(H16C	109.5

H16A(C16(H16C	109.5

H16B(C16(H16C	109.5

C18(C17(P2	118.8(13)

C18(C17(H17A	107.6

P2(C17(H17A	107.6

C18(C17(H17B	107.6

P2(C17(H17B	107.6

H17A(C17(H17B	107.0

C20(C18(C17	111.1(18)

C20(C18(C19	105.3(16)

C17(C18(C19	105.7(16)

C20(C18(H18	111.5

C17(C18(H18	111.5

C19(C18(H18	111.5

C18(C19(H19A	109.5

C18(C19(H19B	109.5

H19A(C19(H19B	109.5

C18(C19(H19C	109.5

H19A(C19(H19C	109.5

H19B(C19(H19C	109.5

C18(C20(H20A	109.5

C18(C20(H20B	109.5

H20A(C20(H20B	109.5

C18(C20(H20C	109.5

H20A(C20(H20C	109.5

H20B(C20(H20C	109.5

C22(C21(P2	120.4(16)

C22(C21(H21A	107.2

P2(C21(H21A	107.2

C22(C21(H21B	107.2

P2(C21(H21B	107.2

H21A(C21(H21B	106.8

C24(C22(C21	118(2)

C24(C22(C23	100.1(19)

C21(C22(C23	108.5(19)

C24(C22(H22	109.9

C21(C22(H22	109.9

C23(C22(H22	109.9

C22(C23(H23A	109.5

C22(C23(H23B	109.5

H23A(C23(H23B	109.5

C22(C23(H23C	109.5

H23A(C23(H23C	109.5

H23B(C23(H23C	109.5

C22(C24(H24A	109.5

C22(C24(H24B	109.5

H24A(C24(H24B	109.5

C22(C24(H24C	109.5

H24A(C24(H24C	109.5

H24B(C24(H24C	109.5

P2(O2(Dy1	153.2(14)

O2(P2(C21	110.5(13)

O2(P2(C17	113.8(12)

C21(P2(C17	107.8(11)

O2(P2(C13	110.7(11)

C21(P2(C13	103.6(12)

C17(P2(C13	109.9(11)

C114(C113(P102	119.0(15)

C114(C113(H11D	107.6

P102(C113(H11D	107.6

C114(C113(H11E	107.6

P102(C113(H11E	107.6

H11D(C113(H11E	107.0

C116(C114(C115	111(2)

C116(C114(C113	112(2)

C115(C114(C113	113.4(19)

C116(C114(H114	106.5

C115(C114(H114	106.5

C113(C114(H114	106.5

C114(C115(H11F	109.5

C114(C115(H11G	109.5

H11F(C115(H11G	109.5

C114(C115(H11H	109.5

H11F(C115(H11H	109.5

H11G(C115(H11H	109.5

C114(C116(H11I	109.5

C114(C116(H11J	109.5

H11I(C116(H11J	109.5

C114(C116(H11K	109.5

H11I(C116(H11K	109.5

H11J(C116(H11K	109.5

C118(C117(P102	118.3(13)

C118(C117(H11L	107.7

P102(C117(H11L	107.7

C118(C117(H11M	107.7

P102(C117(H11M	107.7

H11L(C117(H11M	107.1

C120(C118(C117	124.8(19)

C120(C118(C119	105.0(18)

C117(C118(C119	109.7(17)

C120(C118(H118	105.3

C117(C118(H118	105.3

C119(C118(H118	105.3

C118(C119(H11N	109.5

C118(C119(H11O	109.5

H11N(C119(H11O	109.5

C118(C119(H11P	109.5

H11N(C119(H11P	109.5

H11O(C119(H11P	109.5

C118(C120(H12D	109.5

C118(C120(H12E	109.5

H12D(C120(H12E	109.5

C118(C120(H12F	109.5

H12D(C120(H12F	109.5

H12E(C120(H12F	109.5

C122(C121(P102	124.3(16)

C122(C121(H12G	106.3

P102(C121(H12G	106.3

C122(C121(H12H	106.3

P102(C121(H12H	106.3

H12G(C121(H12H	106.4

C124(C122(C121	123(2)

C124(C122(C123	98.4(18)

C121(C122(C123	105.3(17)

C124(C122(H122	109.6

C121(C122(H122	109.6

C123(C122(H122	109.6

C122(C123(H12I	109.5

C122(C123(H12J	109.5

H12I(C123(H12J	109.5

C122(C123(H12K	109.5

H12I(C123(H12K	109.5

H12J(C123(H12K	109.5

C122(C124(H12L	109.5

C122(C124(H12M	109.5

H12L(C124(H12M	109.5

C122(C124(H12N	109.5

H12L(C124(H12N	109.5

H12M(C124(H12N	109.5

P102(O102(Dy1	154.3(16)

O102(P102(C121	111.9(13)

O102(P102(C113	107.5(11)

C121(P102(C113	110.1(12)

O102(P102(C117	109.3(12)

C121(P102(C117	108.9(12)

C113(P102(C117	109.2(11)

C26(C25(P3	120.8(17)

C26(C25(H25A	107.1

P3(C25(H25A	107.1

C26(C25(H25B	107.1

P3(C25(H25B	107.1

H25A(C25(H25B	106.8

C28(C26(C27	113(2)

C28(C26(C25	111(2)

C27(C26(C25	112(2)

C28(C26(H26	106.7

C27(C26(H26	106.7

C25(C26(H26	106.7

C26(C27(H27A	109.5

C26(C27(H27B	109.5

H27A(C27(H27B	109.5

C26(C27(H27C	109.5

H27A(C27(H27C	109.5

H27B(C27(H27C	109.5

C26(C28(H28A	109.5

C26(C28(H28B	109.5

H28A(C28(H28B	109.5

C26(C28(H28C	109.5

H28A(C28(H28C	109.5

H28B(C28(H28C	109.5

C30(C29(P3	118.2(16)

C30(C29(H29A	107.8

P3(C29(H29A	107.8

C30(C29(H29B	107.8

P3(C29(H29B	107.8

H29A(C29(H29B	107.1

C32(C30(C29	116(2)

C32(C30(C31	103(2)

C29(C30(C31	105.4(19)

C32(C30(H30	110.6

C29(C30(H30	110.6

C31(C30(H30	110.6

C30(C31(H31A	109.5

C30(C31(H31B	109.5

H31A(C31(H31B	109.5

C30(C31(H31C	109.5

H31A(C31(H31C	109.5

H31B(C31(H31C	109.5

C30(C32(H32A	109.5

C30(C32(H32B	109.5

H32A(C32(H32B	109.5

C30(C32(H32C	109.5

H32A(C32(H32C	109.5

H32B(C32(H32C	109.5

C34(C33(P3	120.4(18)

C34(C33(H33A	107.2

P3(C33(H33A	107.2

C34(C33(H33B	107.2

P3(C33(H33B	107.2

H33A(C33(H33B	106.9

C36(C34(C33	125(2)

C36(C34(C35	106(2)

C33(C34(C35	118(2)

C36(C34(H34	101.5

C33(C34(H34	101.5

C35(C34(H34	101.5

C34(C35(H35A	109.5

C34(C35(H35B	109.5

H35A(C35(H35B	109.5

C34(C35(H35C	109.5

H35A(C35(H35C	109.5

H35B(C35(H35C	109.5

C34(C36(H36A	109.5

C34(C36(H36B	109.5

H36A(C36(H36B	109.5

C34(C36(H36C	109.5

H36A(C36(H36C	109.5

H36B(C36(H36C	109.5

P3(O3(Dy1	142.1(18)

O3(P3(C25	110.2(13)

O3(P3(C29	111.3(13)

C25(P3(C29	111.0(14)

O3(P3(C33	109.1(14)

C25(P3(C33	106.7(13)

C29(P3(C33	108.4(12)

C126(C125(P103	115.1(16)

C126(C125(H12O	108.5

P103(C125(H12O	108.5

C126(C125(H12P	108.5

P103(C125(H12P	108.5

H12O(C125(H12P	107.5

C128(C126(C127	115(2)

C128(C126(C125	112(2)

C127(C126(C125	114(2)

C128(C126(H126	105.0

C127(C126(H126	105.0

C125(C126(H126	105.0

C126(C127(H12Q	109.5

C126(C127(H12R	109.5

H12Q(C127(H12R	109.5

C126(C127(H12S	109.5

H12Q(C127(H12S	109.5

H12R(C127(H12S	109.5

C126(C128(H12T	109.5

C126(C128(H12U	109.5

H12T(C128(H12U	109.5

C126(C128(H12V	109.5

H12T(C128(H12V	109.5

H12U(C128(H12V	109.5

C130(C129(P103	120.4(16)

C130(C129(H12W	107.2

P103(C129(H12W	107.2

C130(C129(H12$	107.2

P103(C129(H12$	107.2

H12W(C129(H12$	106.9

C132(C130(C129	115(2)

C132(C130(C131	106.0(19)

C129(C130(C131	108.8(19)

C132(C130(H130	109.0

C129(C130(H130	109.0

C131(C130(H130	109.0

C130(C131(H13C	109.5

C130(C131(H13D	109.5

H13C(C131(H13D	109.5

C130(C131(H13E	109.5

H13C(C131(H13E	109.5

H13D(C131(H13E	109.5

C130(C132(H13F	109.5

C130(C132(H13G	109.5

H13F(C132(H13G	109.5

C130(C132(H13H	109.5

H13F(C132(H13H	109.5

H13G(C132(H13H	109.5

C134(C133(P103	122.4(15)

C134(C133(H13I	106.7

P103(C133(H13I	106.7

C134(C133(H13J	106.7

P103(C133(H13J	106.7

H13I(C133(H13J	106.6

C136(C134(C133	117(2)

C136(C134(C135	100.6(18)

C133(C134(C135	108.4(19)

C136(C134(H134	110.0

C133(C134(H134	110.0

C135(C134(H134	110.0

C134(C135(H13K	109.5

C134(C135(H13L	109.5

H13K(C135(H13L	109.5

C134(C135(H13M	109.5

H13K(C135(H13M	109.5

H13L(C135(H13M	109.5

C134(C136(H13N	109.5

C134(C136(H13O	109.5

H13N(C136(H13O	109.5

C134(C136(H13P	109.5

H13N(C136(H13P	109.5

H13O(C136(H13P	109.5

P103(O103(Dy1	147.7(16)

O103(P103(C125	110.9(12)

O103(P103(C133	111.0(12)

C125(P103(C133	106.5(12)

O103(P103(C129	112.0(12)

C125(P103(C129	110.2(12)

C133(P103(C129	106.0(11)

O13(N11(O11	122.4(14)

O13(N11(O12	120.5(14)

O11(N11(O12	117.1(12)

O13(N11(Dy1	175.0(11)

O11(N11(Dy1	60.6(7)

O12(N11(Dy1	56.6(6)

N11(O11(Dy1	94.6(8)

N11(O12(Dy1	97.5(8)

O22(N21(O23	121.7(12)

O22(N21(O21	117.3(11)

O23(N21(O21	120.7(13)

O22(N21(Dy1	58.9(6)

O23(N21(Dy1	175.1(9)

O21(N21(Dy1	58.5(6)

N21(O21(Dy1	94.8(8)

N21(O22(Dy1	96.0(7)

O33(N31(O32	121.0(13)

O33(N31(O31	124.3(12)

O32(N31(O31	114.6(11)

O33(N31(Dy1	175.1(11)

O32(N31(Dy1	56.5(6)

O31(N31(Dy1	58.5(6)

N31(O31(Dy1	95.3(7)

N31(O32(Dy1	97.9(8)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

Dy1	45(1) 	77(1)	43(1) 	(7(1)	1(1) 	(4(1)

C1	62(7) 	106(9)	59(7) 	(25(7)	9(6) 	12(7)

C2	78(7) 	120(9)	75(8) 	(21(7)	12(6) 	13(7)

C3	84(11) 	127(13)	96(11) 	(22(10)	21(9) 	3(10)

C4	111(11) 	155(14)	38(8) 	(19(9)	24(7) 	17(11)

C5	68(7) 	88(8)	47(6) 	(3(6)	(9(5) 	1(6)

C6	80(7) 	89(8)	67(7) 	(7(6)	(19(6) 	(3(6)

C7	81(10) 	88(10)	110(11) 	(27(9)	(38(9) 	3(8)

C8	90(10) 	110(12)	90(10) 	(4(10)	7(9) 	(34(9)

C9	98(10) 	87(8)	66(8) 	2(7)	(8(8) 	2(8)

C10	118(10) 	92(8)	82(8) 	2(7)	(11(8) 	1(8)

C11	151(15) 	111(13)	118(13) 	(3(12)	(8(13) 	(1(12)

C12	152(15) 	97(12)	93(11) 	3(10)	(40(12) 	14(11)

O1	51(4) 	83(5)	43(4) 	(5(4)	6(3) 	4(4)

P1	65(2) 	76(2)	40(2) 	(5(1)	(10(1) 	3(2)

C13	76(7) 	96(7)	53(8) 	(23(8)	(7(7) 	15(6)

C14	85(9) 	102(9)	50(9) 	(23(9)	(13(9) 	18(8)

C15	92(12) 	119(13)	49(11) 	(17(12)	(9(11) 	14(11)

C16	97(13) 	109(13)	75(12) 	(17(13)	(12(12) 	6(12)

C17	58(8) 	77(8)	41(8) 	(29(8)	14(7) 	(12(7)

C18	65(8) 	79(8)	37(8) 	(34(8)	17(7) 	(15(7)

C19	78(14) 	83(15)	38(12) 	(25(11)	0(11) 	6(13)

C20	87(11) 	96(12)	52(12) 	(26(12)	31(11) 	(9(11)

C21	74(8) 	97(7)	78(8) 	(13(7)	0(7) 	(21(7)

C22	81(9) 	102(8)	84(8) 	(13(7)	1(8) 	(25(7)

C23	93(13) 	117(13)	92(13) 	(21(12)	2(12) 	(31(12)

C24	86(13) 	103(13)	97(13) 	0(12)	3(12) 	(25(12)

O2	53(5) 	80(6)	52(6) 	(20(6)	0(5) 	7(5)

P2	52(3) 	75(4)	52(5) 	(23(4)	4(4) 	(4(3)

C113	77(9) 	99(9)	46(9) 	(23(9)	(16(9) 	17(8)

C114	84(8) 	106(8)	53(8) 	(24(8)	(11(8) 	17(7)

C115	102(14) 	128(14)	33(11) 	(39(12)	(6(12) 	13(13)

C116	103(14) 	110(14)	69(13) 	(5(14)	(17(13) 	3(13)

C117	56(7) 	76(7)	48(8) 	(26(7)	10(7) 	(6(6)

C118	66(7) 	80(7)	50(8) 	(23(7)	18(6) 	(9(7)

C119	81(15) 	91(16)	106(17) 	(9(15)	14(14) 	(5(14)

C120	106(13) 	115(14)	84(15) 	(23(15)	15(14) 	(3(13)

C121	76(10) 	101(8)	83(9) 	(15(8)	4(8) 	(19(8)

C122	79(9) 	102(8)	85(8) 	(13(7)	1(8) 	(25(7)

C123	80(12) 	98(12)	97(13) 	(19(12)	(9(11) 	(25(11)

C124	94(13) 	96(12)	86(12) 	4(12)	1(12) 	(32(11)

O102	49(5) 	78(6)	54(6) 	(19(6)	(6(5) 	5(5)

P102	59(3) 	83(4)	58(5) 	(26(4)	(2(4) 	5(3)

C25	88(13) 	127(16)	137(15) 	85(14)	40(12) 	59(12)

C26	88(12) 	133(15)	141(14) 	77(13)	39(12) 	59(11)

C27	87(14) 	134(16)	145(16) 	76(15)	31(15) 	60(13)

C28	87(18) 	140(20)	150(20) 	77(19)	3(17) 	59(17)

C29	81(8) 	70(9)	90(8) 	(14(8)	(29(8) 	(2(7)

C30	91(9) 	86(10)	100(10) 	(21(9)	(35(9) 	(5(8)

C31	103(13) 	104(14)	106(16) 	(20(13)	(48(14) 	(3(13)

C32	105(13) 	99(13)	113(16) 	(37(14)	(33(14) 	(7(12)

C33	82(9) 	90(10)	91(10) 	(13(9)	5(9) 	26(9)

C34	86(9) 	96(11)	100(11) 	(10(9)	5(9) 	27(9)

C35	103(18) 	120(20)	140(20) 	(3(19)	(17(18) 	37(18)

C36	100(14) 	108(17)	111(17) 	(15(15)	(2(15) 	1(15)

O3	73(7) 	51(8)	56(6) 	(21(7)	(11(6) 	16(6)

P3	74(5) 	63(7)	71(4) 	(19(5)	(10(4) 	17(5)

C125	90(13) 	131(16)	139(14) 	87(14)	44(12) 	55(12)

C126	91(12) 	136(15)	144(14) 	77(13)	47(12) 	54(11)

C127	102(15) 	137(18)	160(18) 	73(16)	47(16) 	43(14)

C128	84(14) 	136(17)	142(16) 	67(15)	52(14) 	65(14)

C129	87(9) 	82(10)	99(10) 	(20(9)	(34(9) 	(4(8)

C130	94(9) 	95(10)	107(11) 	(23(9)	(39(10) 	(4(8)

C131	107(15) 	117(16)	118(18) 	(18(14)	(47(15) 	4(14)

C132	109(14) 	101(14)	110(17) 	(38(15)	(24(15) 	5(13)

C133	78(8) 	83(9)	80(8) 	(10(8)	(2(7) 	24(8)

C134	83(8) 	94(10)	95(10) 	(5(9)	4(8) 	23(9)

C135	86(15) 	101(17)	136(18) 	7(16)	(17(16) 	30(14)

C136	90(12) 	97(14)	110(14) 	(6(12)	11(13) 	4(13)

O103	70(5) 	48(7)	59(5) 	(8(6)	(16(5) 	11(5)

P103	68(4) 	38(5)	73(4) 	(1(4)	(21(3) 	(7(3)

N11	64(5) 	95(6)	57(5) 	(2(5)	(1(5) 	(12(5)

O11	75(5) 	96(6)	61(5) 	(9(5)	4(5) 	(12(5)

O12	59(5) 	101(7)	53(5) 	(4(5)	(1(4) 	(3(5)

O13	97(7) 	107(8)	56(6) 	(3(6)	(12(6) 	(20(6)

N21	52(5) 	89(6)	62(5) 	(9(5)	(3(4) 	(24(5)

O21	60(5) 	92(6)	55(5) 	(3(5)	0(4) 	(9(5)

O22	46(4) 	86(6)	66(5) 	(16(5)	(2(4) 	(15(4)

O23	79(7) 	112(8)	57(5) 	(10(5)	3(5) 	(28(6)

N31	59(5) 	95(6)	71(6) 	(5(5)	4(5) 	(21(5)

O31	59(5) 	94(6)	66(5) 	(15(5)	(1(5) 	(18(4)

O32	54(5) 	91(6)	64(5) 	(6(4)	1(4) 	(5(4)

O33	76(7) 	112(8)	83(7) 	15(6)	3(5) 	(37(6)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H1A	1119	4684	199	91	1

H1B	350	3995	181	91	1

H2	342	4361	(384	109	1

H3A	1272	3207	(478	154	1

H3B	618	2997	(202	154	1

H3C	1606	3249	(130	154	1

H4A	2061	4754	(252	152	1

H4B	1345	5427	(372	152	1

H4C	1649	4642	(588	152	1

H5A	(1610	5526	(18	81	1

H5B	(1002	5283	(302	81	1

H6	(984	3811	(118	95	1

H7A	(2639	4480	(312	140	1

H7B	(2375	3476	(330	140	1

H7C	(1878	4175	(539	140	1

H8A	(1428	4001	386	145	1

H8B	(2108	3380	215	145	1

H8C	(2345	4378	275	145	1

H9A	931	6341	46	100	1

H9B	240	6366	(228	100	1

H10	(1	7172	349	117	1

H11A	397	8049	(235	190	1

H11B	1145	7840	10	190	1

H11C	384	8505	96	190	1

H12A	(965	7376	(188	171	1

H12B	(1115	7880	130	171	1

H12C	(1286	6856	110	171	1

H13A	(2319	6244	577	90	0.488(10)

H13B	(2430	5429	801	90	0.488(10)

H14	(3731	5969	989	95	0.488(10)

H15A	(4646	5877	559	130	0.488(10)

H15B	(4038	5063	637	130	0.488(10)

H15C	(3782	5708	363	130	0.488(10)

H16A	(4165	7194	602	140	0.488(10)

H16B	(3350	7457	810	140	0.488(10)

H16C	(4234	7142	969	140	0.488(10)

H17A	(2352	7071	1569	71	0.488(10)

H17B	(3152	6628	1398	71	0.488(10)

H18	(1785	5621	1692	72	0.488(10)

H19A	(3532	6102	1895	100	0.488(10)

H19B	(2655	6376	2067	100	0.488(10)

H19C	(2969	5385	2072	100	0.488(10)

H20A	(2823	4472	1643	118	0.488(10)

H20B	(2531	4810	1310	118	0.488(10)

H20C	(3445	5105	1451	118	0.488(10)

H21A	(1827	7754	732	100	0.488(10)

H21B	(2573	7955	975	100	0.488(10)

H22	(1772	8861	1201	107	0.488(10)

H23A	(195	8582	855	151	0.488(10)

H23B	(746	9462	871	151	0.488(10)

H23C	(1019	8713	635	151	0.488(10)

H24A	(746	8511	1487	143	0.488(10)

H24B	(211	8082	1209	143	0.488(10)

H24C	(936	7529	1386	143	0.488(10)

H11D	(2125	6292	474	89	0.512(10)

H11E	(2326	5471	685	89	0.512(10)

H114	(3722	6115	807	97	0.512(10)

H11F	(4420	5540	420	131	0.512(10)

H11G	(3509	5042	406	131	0.512(10)

H11H	(3703	5822	173	131	0.512(10)

H11I	(3407	7213	318	141	0.512(10)

H11J	(3379	7489	673	141	0.512(10)

H11K	(4269	7159	523	141	0.512(10)

H11L	(2465	7090	1460	72	0.512(10)

H11M	(3246	6919	1228	72	0.512(10)

H118	(2526	5830	1660	78	0.512(10)

H11N	(4262	5875	1423	139	0.512(10)

H11O	(3935	6380	1723	139	0.512(10)

H11P	(3969	5341	1721	139	0.512(10)

H12D	(2827	4999	1113	153	0.512(10)

H12E	(3277	4584	1410	153	0.512(10)

H12F	(2246	4711	1401	153	0.512(10)

H12G	(1340	7682	684	104	0.512(10)

H12H	(2198	8029	844	104	0.512(10)

H122	(492	8148	1058	107	0.512(10)

H12I	(1267	9713	1106	137	0.512(10)

H12J	(1857	9311	839	137	0.512(10)

H12K	(834	9425	787	137	0.512(10)

H12L	(1378	7924	1500	138	0.512(10)

H12M	(1861	8801	1401	138	0.512(10)

H12N	(846	8816	1481	138	0.512(10)

H25A	1108	3656	1458	140	0.455(12)

H25B	523	2862	1349	140	0.455(12)

H26	2110	2194	1340	144	0.455(12)

H27A	1153	1910	1873	183	0.455(12)

H27B	1619	1221	1651	183	0.455(12)

H27C	715	1649	1551	183	0.455(12)

H28A	2046	2967	1907	189	0.455(12)

H28B	2423	3500	1620	189	0.455(12)

H28C	2861	2600	1719	189	0.455(12)

H29A	1340	2674	477	97	0.455(12)

H29B	1754	2097	744	97	0.455(12)

H30	368	1608	902	111	0.455(12)

H31A	187	713	473	156	0.455(12)

H31B	1165	1039	426	156	0.455(12)

H31C	391	1481	236	156	0.455(12)

H32A	(816	2294	780	159	0.455(12)

H32B	(634	2086	425	159	0.455(12)

H32C	(279	2968	574	159	0.455(12)

H33A	2411	4351	1073	105	0.455(12)

H33B	2794	3422	988	105	0.455(12)

H34	2170	4449	534	113	0.455(12)

H35A	3661	5122	461	183	0.455(12)

H35B	3678	5059	829	183	0.455(12)

H35C	2925	5596	660	183	0.455(12)

H36A	3104	3119	463	159	0.455(12)

H36B	3636	3945	342	159	0.455(12)

H36C	2678	3760	215	159	0.455(12)

H12O	836	3138	1464	144	0.545(12)

H12P	104	2611	1282	144	0.545(12)

H126	1475	1587	1231	148	0.545(12)

H12Q	811	597	1538	199	0.545(12)

H12R	134	1042	1308	199	0.545(12)

H12S	156	1325	1662	199	0.545(12)

H12T	1715	2522	1732	181	0.545(12)

H12U	2366	1904	1546	181	0.545(12)

H12V	1731	1501	1800	181	0.545(12)

H12W	1293	2529	453	107	0.545(12)

H12$	1589	1834	703	107	0.545(12)

H130	125	1431	789	118	0.545(12)

H13C	282	1278	138	171	0.545(12)

H13D	147	515	384	171	0.545(12)

H13E	1093	919	330	171	0.545(12)

H13F	(344	2880	519	160	0.545(12)

H13G	(984	2092	598	160	0.545(12)

H13H	(549	2158	264	160	0.545(12)

H13I	2327	3673	1202	96	0.545(12)

H13J	2587	2783	1042	96	0.545(12)

H134	2552	4403	740	109	0.545(12)

H13K	4115	3397	896	162	0.545(12)

H13L	3751	4084	1141	162	0.545(12)

H13M	4089	4409	812	162	0.545(12)

H13N	2994	2770	532	148	0.545(12)

H13O	3585	3577	430	148	0.545(12)

H13P	2572	3563	346	148	0.545(12)