|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	2009src1246 / Er iBu

Empirical formula 	C36H81ErN3O12P3

Formula weight 	1008.21

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Tetragonal

Space group 	P41212

Unit cell dimensions	a = 15.3066(7) Å	( = 90°

b = 15.3066(7) Å	( = 90°

c = 43.170(3) Å	(  = 90°

Volume	10114.3(9) Å3

Z	8

Density (calculated)	1.324 Mg / m3

Absorption coefficient	1.807 mm(1

F(000)	4216

Crystal	Block; Pale Pink

Crystal size	0.46 ( 0.34 ( 0.30 mm3

( range for data collection	2.98 ( 25.00°

Index ranges	(18 ( h ( 17, (18 ( k ( 15, (49 ( l ( 51

Reflections collected	59748

Independent reflections	8906 [Rint = 0.1594]

Completeness to ( = 25.00°	99.7 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.6132 and 0.4903

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	8906 / 982 / 750

Goodness-of-fit on F2	1.042

Final R indices [F2 > 2((F2)]	R1 = 0.0637, wR2 = 0.1138

R indices (all data)	R1 = 0.1423, wR2 = 0.1370

Absolute structure parameter	0.049(16)

Largest diff. peak and hole	0.616 and (0.598 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP3 for Windows (L. J. Farrugia, J. Appl. Crystallogr. 1997, 30, 565).

Special details:

All hydrogen atoms were fixed using a standard riding model.

One of the three phosphorus ligands was disordered. This resulted in all the ligands been restrained to be similar using the SAME compound. Also a loose global thermal restraint (SIMU) was used.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

Er1	5336(1)	9921(1)	1517(1)	55(1)	1

C1	5112(6)	11128(5)	2590(2)	59(3)	1

C2	4161(6)	11453(6)	2593(2)	61(3)	1

C3	3885(8)	11793(8)	2274(2)	91(4)	1

C4	4031(7)	12134(7)	2833(2)	77(4)	1

C5	6367(5)	9711(6)	2500(2)	59(3)	1

C6	7227(7)	10083(9)	2373(3)	109(4)	1

C7	7341(9)	10997(10)	2469(3)	144(7)	1

C8	7979(8)	9525(11)	2505(4)	175(8)	1

C9	4537(6)	9384(6)	2418(2)	64(3)	1

C10	4289(7)	9129(7)	2748(2)	71(3)	1

C11	4865(8)	8361(7)	2863(2)	93(4)	1

C12	3371(7)	8837(8)	2774(2)	89(4)	1

O1	5436(4)	10410(4)	2015(1)	55(2)	1

P1	5374(2)	10188(2)	2355(1)	57(1)	1

C13	6552(13)	12557(19)	1101(5)	60(7)	0.540(10)

C14	5719(13)	12580(16)	904(5)	80(8)	0.540(10)

C15	5904(14)	13061(18)	588(4)	117(10)	0.540(10)

C16	4908(12)	12897(14)	1043(4)	83(7)	0.540(10)

C17	5966(17)	12492(18)	1756(6)	76(7)	0.540(10)

C18	6220(17)	13450(18)	1827(6)	97(7)	0.540(10)

C19	5468(17)	13890(20)	1988(8)	137(12)	0.540(10)

C20	6934(17)	13498(19)	2071(8)	140(11)	0.540(10)

C21	7627(14)	11730(20)	1575(5)	88(7)	0.540(10)

C22	8283(13)	11129(19)	1423(5)	112(7)	0.540(10)

C23	9237(11)	11320(12)	1561(5)	63(7)	0.540(10)

C24	8456(18)	11300(20)	1094(5)	126(11)	0.540(10)

O2	6079(18)	11059(15)	1391(6)	52(6)	0.540(10)

P2	6540(12)	11903(12)	1445(4)	58(4)	0.540(10)

C113	6703(15)	12700(20)	1171(6)	58(8)	0.460(10)

C114	5782(16)	12946(13)	1051(5)	63(7)	0.460(10)

C115	5510(20)	12246(14)	804(6)	73(9)	0.460(10)

C116	5715(16)	13832(11)	931(6)	90(10)	0.460(10)

C117	6090(20)	12555(19)	1814(7)	78(8)	0.460(10)

C118	6140(17)	13560(20)	1828(8)	95(7)	0.460(10)

C119	5700(20)	13880(30)	2114(8)	140(14)	0.460(10)

C120	7074(17)	13880(20)	1827(8)	104(10)	0.460(10)

C121	7805(17)	11870(20)	1617(7)	103(8)	0.460(10)

C122	8414(17)	11350(20)	1410(7)	111(8)	0.460(10)

C123	9000(20)	10750(20)	1620(8)	151(13)	0.460(10)

C124	8074(17)	10700(20)	1197(6)	91(9)	0.460(10)

O102	6300(20)	11133(18)	1444(8)	55(7)	0.460(10)

P102	6691(14)	12000(14)	1506(4)	56(4)	0.460(10)

C25	2460(16)	8739(13)	1808(5)	86(6)	0.655(9)

C26	2001(16)	9592(15)	1882(6)	135(7)	0.655(9)

C27	1162(15)	9414(15)	2087(6)	162(11)	0.655(9)

C28	2366(14)	10417(15)	1959(6)	147(9)	0.655(9)

C29	3102(12)	8900(12)	1154(3)	94(7)	0.655(9)

C30	2480(12)	8231(12)	1007(4)	94(6)	0.655(9)

C31	1713(15)	8658(15)	864(6)	109(9)	0.655(9)

C32	2940(13)	7644(13)	777(5)	142(9)	0.655(9)

C33	3831(15)	7626(10)	1559(5)	115(8)	0.655(9)

C34	4207(14)	7189(16)	1834(6)	128(8)	0.655(9)

C35	3514(16)	6798(15)	2059(5)	126(10)	0.655(9)

C36	4970(16)	6612(17)	1852(6)	194(13)	0.655(9)

O3	4058(15)	9366(13)	1661(6)	55(4)	0.655(9)

P3	3394(9)	8715(8)	1559(2)	71(3)	0.655(9)

C125	2340(40)	8800(30)	1885(9)	109(9)	0.345(9)

C126	1780(30)	9630(20)	1856(9)	150(10)	0.345(9)

C127	1430(30)	9960(30)	2172(9)	188(16)	0.345(9)

C128	2040(30)	10320(30)	1650(11)	166(16)	0.345(9)

C129	2565(17)	9269(18)	1238(7)	92(10)	0.345(9)

C130	1703(18)	8808(19)	1140(7)	92(9)	0.345(9)

C131	1085(18)	9480(20)	1031(8)	105(13)	0.345(9)

C132	1870(30)	8160(20)	880(10)	91(13)	0.345(9)

C133	3280(20)	7645(15)	1462(7)	112(11)	0.345(9)

C134	3870(20)	7068(16)	1649(7)	101(9)	0.345(9)

C135	3750(40)	7180(30)	2004(7)	146(16)	0.345(9)

C136	4044(19)	6163(14)	1577(7)	68(10)	0.345(9)

O103	3920(30)	9230(30)	1643(12)	57(8)	0.345(9)

P103	3106(15)	8752(14)	1569(5)	66(6)	0.345(9)

N11	4008(6)	11009(6)	1240(2)	71(3)	1

O11	4267(5)	11155(4)	1519(2)	67(2)	1

O12	4420(4)	10412(4)	1095(1)	63(2)	1

O13	3438(6)	11430(5)	1119(2)	90(3)	1

N21	5675(7)	8930(7)	960(2)	69(2)	1

O21	5223(5)	8645(4)	1183(2)	65(2)	1

O22	6048(5)	9673(6)	997(2)	74(2)	1

O23	5768(5)	8515(5)	718(2)	87(3)	1

N31	6503(7)	8653(6)	1799(2)	58(2)	1

O31	5686(5)	8626(4)	1838(1)	59(2)	1

O32	6752(5)	9270(5)	1609(1)	67(2)	1

O33	7018(5)	8159(5)	1923(1)	83(3)	1

Table 3. Bond lengths [Å] and angles [°].

Er1(O2	2.15(2)

Er1(O3	2.22(2)

Er1(O1	2.280(5)

Er1(O102	2.39(3)

Er1(O32	2.419(7)

Er1(O12	2.421(6)

Er1(O21	2.434(6)

Er1(O103	2.47(4)

Er1(O31	2.476(6)

Er1(O11	2.498(6)

Er1(O22	2.527(6)

Er1(N11	2.887(9)

C1(C2	1.539(11)

C1(P1	1.805(8)

C1(H1A	0.9900

C1(H1B	0.9900

C2(C4	1.484(10)

C2(C3	1.531(11)

C2(H2	1.0000

C3(H3A	0.9800

C3(H3B	0.9800

C3(H3C	0.9800

C4(H4A	0.9800

C4(H4B	0.9800

C4(H4C	0.9800

C5(C6	1.534(12)

C5(P1	1.799(8)

C5(H5A	0.9900

C5(H5B	0.9900

C6(C7	1.468(14)

C6(C8	1.542(14)

C6(H6	1.0000

C7(H7A	0.9800

C7(H7B	0.9800

C7(H7C	0.9800

C8(H8A	0.9800

C8(H8B	0.9800

C8(H8C	0.9800

C9(C10	1.526(10)

C9(P1	1.797(8)

C9(H9A	0.9900

C9(H9B	0.9900

C10(C12	1.479(13)

C10(C11	1.550(12)

C10(H10	1.0000

C11(H11A	0.9800

C11(H11B	0.9800

C11(H11C	0.9800

C12(H12A	0.9800

C12(H12B	0.9800

C12(H12C	0.9800

O1(P1	1.509(5)

C13(C14	1.534(16)

C13(P2	1.789(12)

C13(H13A	0.9900

C13(H13B	0.9900

C14(C16	1.461(18)

C14(C15	1.576(17)

C14(H14	1.0000

C15(H15A	0.9800

C15(H15B	0.9800

C15(H15C	0.9800

C16(H16A	0.9800

C16(H16B	0.9800

C16(H16C	0.9800

C17(C18	1.548(16)

C17(P2	1.842(12)

C17(H17A	0.9900

C17(H17B	0.9900

C18(C19	1.506(17)

C18(C20	1.522(18)

C18(H18	1.0000

C19(H19A	0.9800

C19(H19B	0.9800

C19(H19C	0.9800

C20(H20A	0.9800

C20(H20B	0.9800

C20(H20C	0.9800

C21(C22	1.513(15)

C21(P2	1.775(13)

C21(H21A	0.9900

C21(H21B	0.9900

C22(C24	1.469(18)

C22(C23	1.604(17)

C22(H22	1.0000

C23(H23A	0.9800

C23(H23B	0.9800

C23(H23C	0.9800

C24(H24A	0.9800

C24(H24B	0.9800

C24(H24C	0.9800

O2(P2	1.491(11)

C113(C114	1.550(17)

C113(P102	1.793(13)

C113(H11D	0.9900

C113(H11E	0.9900

C114(C116	1.453(17)

C114(C115	1.569(17)

C114(H114	1.0000

C115(H11F	0.9800

C115(H11G	0.9800

C115(H11H	0.9800

C116(H11I	0.9800

C116(H11J	0.9800

C116(H11K	0.9800

C117(C118	1.546(17)

C117(P102	1.827(13)

C117(H11L	0.9900

C117(H11M	0.9900

C118(C119	1.492(18)

C118(C120	1.512(18)

C118(H118	1.0000

C119(H11N	0.9800

C119(H11O	0.9800

C119(H11P	0.9800

C120(H12D	0.9800

C120(H12E	0.9800

C120(H12F	0.9800

C121(C122	1.516(16)

C121(P102	1.783(14)

C121(H12G	0.9900

C121(H12H	0.9900

C122(C124	1.456(18)

C122(C123	1.580(18)

C122(H122	1.0000

C123(H12I	0.9800

C123(H12J	0.9800

C123(H12K	0.9800

C124(H12L	0.9800

C124(H12M	0.9800

C124(H12N	0.9800

O102(P102	1.479(13)

C25(C26	1.515(15)

C25(P3	1.787(12)

C25(H25A	0.9900

C25(H25B	0.9900

C26(C28	1.421(17)

C26(C27	1.584(16)

C26(H26	1.0000

C27(H27A	0.9800

C27(H27B	0.9800

C27(H27C	0.9800

C28(H28A	0.9800

C28(H28B	0.9800

C28(H28C	0.9800

C29(C30	1.536(15)

C29(P3	1.828(12)

C29(H29A	0.9900

C29(H29B	0.9900

C30(C31	1.479(17)

C30(C32	1.512(17)

C30(H30	1.0000

C31(H31A	0.9800

C31(H31B	0.9800

C31(H31C	0.9800

C32(H32A	0.9800

C32(H32B	0.9800

C32(H32C	0.9800

C33(C34	1.481(16)

C33(P3	1.796(13)

C33(H33A	0.9900

C33(H33B	0.9900

C34(C36	1.465(17)

C34(C35	1.558(16)

C34(H34	1.0000

C35(H35A	0.9800

C35(H35B	0.9800

C35(H35C	0.9800

C36(H36A	0.9800

C36(H36B	0.9800

C36(H36C	0.9800

O3(P3	1.489(11)

C125(C126	1.540(18)

C125(P103	1.802(15)

C125(H12O	0.9900

C125(H12P	0.9900

C126(C128	1.438(18)

C126(C127	1.547(19)

C126(H126	1.0000

C127(H12Q	0.9800

C127(H12R	0.9800

C127(H12S	0.9800

C128(H12T	0.9800

C128(H12U	0.9800

C128(H12V	0.9800

C129(C130	1.556(17)

C129(P103	1.830(15)

C129(H12W	0.9900

C129(H12$	0.9900

C130(C131	1.477(19)

C130(C132	1.52(2)

C130(H130	1.0000

C131(H13C	0.9800

C131(H13D	0.9800

C131(H13E	0.9800

C132(H13F	0.9800

C132(H13G	0.9800

C132(H13H	0.9800

C133(C134	1.504(18)

C133(P103	1.776(15)

C133(H13I	0.9900

C133(H13J	0.9900

C134(C136	1.444(18)

C134(C135	1.552(18)

C134(H134	1.0000

C135(H13K	0.9800

C135(H13L	0.9800

C135(H13M	0.9800

C136(H13N	0.9800

C136(H13O	0.9800

C136(H13P	0.9800

O103(P103	1.482(14)

N11(O13	1.204(9)

N11(O12	1.274(9)

N11(O11	1.288(9)

N21(O23	1.230(9)

N21(O21	1.265(10)

N21(O22	1.282(12)

N31(O33	1.216(9)

N31(O31	1.262(10)

N31(O32	1.307(10)

O2(Er1(O3	147.8(10)

O2(Er1(O1	86.4(7)

O3(Er1(O1	85.6(6)

O2(Er1(O102	8.8(15)

O3(Er1(O102	151.4(11)

O1(Er1(O102	80.2(8)

O2(Er1(O32	84.3(8)

O3(Er1(O32	125.9(6)

O1(Er1(O32	85.4(2)

O102(Er1(O32	77.7(9)

O2(Er1(O12	82.2(8)

O3(Er1(O12	79.5(6)

O1(Er1(O12	130.3(2)

O102(Er1(O12	90.9(9)

O32(Er1(O12	140.4(2)

O2(Er1(O21	122.5(7)

O3(Er1(O21	78.2(7)

O1(Er1(O21	145.8(2)

O102(Er1(O21	125.9(8)

O32(Er1(O21	80.2(2)

O12(Er1(O21	76.2(2)

O2(Er1(O103	150.1(13)

O3(Er1(O103	4.3(17)

O1(Er1(O103	89.6(11)

O102(Er1(O103	154.6(14)

O32(Er1(O103	124.9(10)

O12(Er1(O103	78.0(10)

O21(Er1(O103	74.0(12)

O2(Er1(O31	132.5(8)

O3(Er1(O31	74.3(6)

O1(Er1(O31	73.87(19)

O102(Er1(O31	124.1(9)

O32(Er1(O31	52.0(2)

O12(Er1(O31	142.7(2)

O21(Er1(O31	72.8(2)

O103(Er1(O31	73.9(10)

O2(Er1(O11	74.6(8)

O3(Er1(O11	73.2(6)

O1(Er1(O11	78.0(2)

O102(Er1(O11	79.5(9)

O32(Er1(O11	153.8(3)

O12(Er1(O11	52.3(2)

O21(Er1(O11	124.2(2)

O103(Er1(O11	75.6(11)

O31(Er1(O11	138.2(2)

O2(Er1(O22	70.6(7)

O3(Er1(O22	124.8(7)

O1(Er1(O22	149.1(2)

O102(Er1(O22	74.4(8)

O32(Er1(O22	72.4(2)

O12(Er1(O22	68.0(2)

O21(Er1(O22	51.9(2)

O103(Er1(O22	120.6(11)

O31(Er1(O22	106.4(2)

O11(Er1(O22	113.5(2)

O2(Er1(N11	78.5(8)

O3(Er1(N11	73.5(6)

O1(Er1(N11	104.4(2)

O102(Er1(N11	86.1(9)

O32(Er1(N11	159.4(3)

O12(Er1(N11	25.9(2)

O21(Er1(N11	99.6(2)

O103(Er1(N11	73.9(10)

O31(Er1(N11	147.8(3)

O11(Er1(N11	26.4(2)

O22(Er1(N11	91.2(2)

C2(C1(P1	118.2(6)

C2(C1(H1A	107.8

P1(C1(H1A	107.8

C2(C1(H1B	107.8

P1(C1(H1B	107.8

H1A(C1(H1B	107.1

C4(C2(C3	110.7(8)

C4(C2(C1	111.1(8)

C3(C2(C1	111.3(8)

C4(C2(H2	107.8

C3(C2(H2	107.8

C1(C2(H2	107.8

C2(C3(H3A	109.5

C2(C3(H3B	109.5

H3A(C3(H3B	109.5

C2(C3(H3C	109.5

H3A(C3(H3C	109.5

H3B(C3(H3C	109.5

C2(C4(H4A	109.5

C2(C4(H4B	109.5

H4A(C4(H4B	109.5

C2(C4(H4C	109.5

H4A(C4(H4C	109.5

H4B(C4(H4C	109.5

C6(C5(P1	116.8(7)

C6(C5(H5A	108.1

P1(C5(H5A	108.1

C6(C5(H5B	108.1

P1(C5(H5B	108.1

H5A(C5(H5B	107.3

C7(C6(C5	110.8(10)

C7(C6(C8	109.6(11)

C5(C6(C8	107.6(10)

C7(C6(H6	109.6

C5(C6(H6	109.6

C8(C6(H6	109.6

C6(C7(H7A	109.5

C6(C7(H7B	109.5

H7A(C7(H7B	109.5

C6(C7(H7C	109.5

H7A(C7(H7C	109.5

H7B(C7(H7C	109.5

C6(C8(H8A	109.5

C6(C8(H8B	109.5

H8A(C8(H8B	109.5

C6(C8(H8C	109.5

H8A(C8(H8C	109.5

H8B(C8(H8C	109.5

C10(C9(P1	119.6(6)

C10(C9(H9A	107.4

P1(C9(H9A	107.4

C10(C9(H9B	107.4

P1(C9(H9B	107.4

H9A(C9(H9B	107.0

C12(C10(C9	112.6(8)

C12(C10(C11	106.7(9)

C9(C10(C11	110.5(8)

C12(C10(H10	109.0

C9(C10(H10	109.0

C11(C10(H10	109.0

C10(C11(H11A	109.5

C10(C11(H11B	109.5

H11A(C11(H11B	109.5

C10(C11(H11C	109.5

H11A(C11(H11C	109.5

H11B(C11(H11C	109.5

C10(C12(H12A	109.5

C10(C12(H12B	109.5

H12A(C12(H12B	109.5

C10(C12(H12C	109.5

H12A(C12(H12C	109.5

H12B(C12(H12C	109.5

P1(O1(Er1	146.9(3)

O1(P1(C9	110.3(3)

O1(P1(C5	112.1(4)

C9(P1(C5	105.8(4)

O1(P1(C1	112.3(4)

C9(P1(C1	107.7(4)

C5(P1(C1	108.4(4)

C14(C13(P2	117.6(13)

C14(C13(H13A	107.9

P2(C13(H13A	107.9

C14(C13(H13B	107.9

P2(C13(H13B	107.9

H13A(C13(H13B	107.2

C16(C14(C13	119.1(19)

C16(C14(C15	110.6(16)

C13(C14(C15	109.9(15)

C16(C14(H14	105.3

C13(C14(H14	105.3

C15(C14(H14	105.3

C14(C15(H15A	109.5

C14(C15(H15B	109.5

H15A(C15(H15B	109.5

C14(C15(H15C	109.5

H15A(C15(H15C	109.5

H15B(C15(H15C	109.5

C14(C16(H16A	109.5

C14(C16(H16B	109.5

H16A(C16(H16B	109.5

C14(C16(H16C	109.5

H16A(C16(H16C	109.5

H16B(C16(H16C	109.5

C18(C17(P2	119.1(14)

C18(C17(H17A	107.5

P2(C17(H17A	107.5

C18(C17(H17B	107.5

P2(C17(H17B	107.5

H17A(C17(H17B	107.0

C19(C18(C20	101.9(16)

C19(C18(C17	109.0(16)

C20(C18(C17	111.2(19)

C19(C18(H18	111.4

C20(C18(H18	111.4

C17(C18(H18	111.4

C18(C19(H19A	109.5

C18(C19(H19B	109.5

H19A(C19(H19B	109.5

C18(C19(H19C	109.5

H19A(C19(H19C	109.5

H19B(C19(H19C	109.5

C18(C20(H20A	109.5

C18(C20(H20B	109.5

H20A(C20(H20B	109.5

C18(C20(H20C	109.5

H20A(C20(H20C	109.5

H20B(C20(H20C	109.5

C22(C21(P2	125.1(13)

C22(C21(H21A	106.0

P2(C21(H21A	106.0

C22(C21(H21B	106.0

P2(C21(H21B	106.0

H21A(C21(H21B	106.3

C24(C22(C21	115.5(19)

C24(C22(C23	99.4(17)

C21(C22(C23	109.4(16)

C24(C22(H22	110.7

C21(C22(H22	110.7

C23(C22(H22	110.7

C22(C23(H23A	109.5

C22(C23(H23B	109.5

H23A(C23(H23B	109.5

C22(C23(H23C	109.5

H23A(C23(H23C	109.5

H23B(C23(H23C	109.5

C22(C24(H24A	109.5

C22(C24(H24B	109.5

H24A(C24(H24B	109.5

C22(C24(H24C	109.5

H24A(C24(H24C	109.5

H24B(C24(H24C	109.5

P2(O2(Er1	155.9(15)

O2(P2(C21	111.4(12)

O2(P2(C13	111.2(11)

C21(P2(C13	109.6(11)

O2(P2(C17	108.2(11)

C21(P2(C17	106.8(11)

C13(P2(C17	109.7(11)

C114(C113(P102	114.1(15)

C114(C113(H11D	108.7

P102(C113(H11D	108.7

C114(C113(H11E	108.7

P102(C113(H11E	108.7

H11D(C113(H11E	107.6

C116(C114(C113	114.4(17)

C116(C114(C115	112.1(17)

C113(C114(C115	107.5(18)

C116(C114(H114	107.5

C113(C114(H114	107.5

C115(C114(H114	107.5

C114(C115(H11F	109.5

C114(C115(H11G	109.5

H11F(C115(H11G	109.5

C114(C115(H11H	109.5

H11F(C115(H11H	109.5

H11G(C115(H11H	109.5

C114(C116(H11I	109.5

C114(C116(H11J	109.5

H11I(C116(H11J	109.5

C114(C116(H11K	109.5

H11I(C116(H11K	109.5

H11J(C116(H11K	109.5

C118(C117(P102	118.0(15)

C118(C117(H11L	107.8

P102(C117(H11L	107.8

C118(C117(H11M	107.8

P102(C117(H11M	107.8

H11L(C117(H11M	107.2

C119(C118(C120	109.1(19)

C119(C118(C117	110(2)

C120(C118(C117	111.6(18)

C119(C118(H118	108.8

C120(C118(H118	108.8

C117(C118(H118	108.8

C118(C119(H11N	109.5

C118(C119(H11O	109.5

H11N(C119(H11O	109.5

C118(C119(H11P	109.5

H11N(C119(H11P	109.5

H11O(C119(H11P	109.5

C118(C120(H12D	109.5

C118(C120(H12E	109.5

H12D(C120(H12E	109.5

C118(C120(H12F	109.5

H12D(C120(H12F	109.5

H12E(C120(H12F	109.5

C122(C121(P102	119.2(15)

C122(C121(H12G	107.5

P102(C121(H12G	107.5

C122(C121(H12H	107.5

P102(C121(H12H	107.5

H12G(C121(H12H	107.0

C124(C122(C121	121(2)

C124(C122(C123	99.5(19)

C121(C122(C123	108.6(18)

C124(C122(H122	109.1

C121(C122(H122	109.1

C123(C122(H122	109.1

C122(C123(H12I	109.5

C122(C123(H12J	109.5

H12I(C123(H12J	109.5

C122(C123(H12K	109.5

H12I(C123(H12K	109.5

H12J(C123(H12K	109.5

C122(C124(H12L	109.5

C122(C124(H12M	109.5

H12L(C124(H12M	109.5

C122(C124(H12N	109.5

H12L(C124(H12N	109.5

H12M(C124(H12N	109.5

P102(O102(Er1	157.0(19)

O102(P102(C121	109.5(13)

O102(P102(C113	113.0(14)

C121(P102(C113	105.9(12)

O102(P102(C117	110.3(13)

C121(P102(C117	109.6(12)

C113(P102(C117	108.4(12)

C26(C25(P3	121.1(13)

C26(C25(H25A	107.1

P3(C25(H25A	107.1

C26(C25(H25B	107.1

P3(C25(H25B	107.1

H25A(C25(H25B	106.8

C28(C26(C25	129(2)

C28(C26(C27	109.9(17)

C25(C26(C27	110.3(16)

C28(C26(H26	100.8

C25(C26(H26	100.8

C27(C26(H26	100.8

C26(C27(H27A	109.5

C26(C27(H27B	109.5

H27A(C27(H27B	109.5

C26(C27(H27C	109.5

H27A(C27(H27C	109.5

H27B(C27(H27C	109.5

C26(C28(H28A	109.5

C26(C28(H28B	109.5

H28A(C28(H28B	109.5

C26(C28(H28C	109.5

H28A(C28(H28C	109.5

H28B(C28(H28C	109.5

C30(C29(P3	116.3(11)

C30(C29(H29A	108.2

P3(C29(H29A	108.2

C30(C29(H29B	108.2

P3(C29(H29B	108.2

H29A(C29(H29B	107.4

C31(C30(C32	111.1(14)

C31(C30(C29	111.6(15)

C32(C30(C29	112.3(15)

C31(C30(H30	107.2

C32(C30(H30	107.2

C29(C30(H30	107.2

C30(C31(H31A	109.5

C30(C31(H31B	109.5

H31A(C31(H31B	109.5

C30(C31(H31C	109.5

H31A(C31(H31C	109.5

H31B(C31(H31C	109.5

C30(C32(H32A	109.5

C30(C32(H32B	109.5

H32A(C32(H32B	109.5

C30(C32(H32C	109.5

H32A(C32(H32C	109.5

H32B(C32(H32C	109.5

C34(C33(P3	124.2(15)

C34(C33(H33A	106.3

P3(C33(H33A	106.3

C34(C33(H33B	106.3

P3(C33(H33B	106.3

H33A(C33(H33B	106.4

C36(C34(C33	129(2)

C36(C34(C35	106.1(15)

C33(C34(C35	114.1(17)

C36(C34(H34	101.1

C33(C34(H34	101.1

C35(C34(H34	101.1

C34(C35(H35A	109.5

C34(C35(H35B	109.5

H35A(C35(H35B	109.5

C34(C35(H35C	109.5

H35A(C35(H35C	109.5

H35B(C35(H35C	109.5

C34(C36(H36A	109.5

C34(C36(H36B	109.5

H36A(C36(H36B	109.5

C34(C36(H36C	109.5

H36A(C36(H36C	109.5

H36B(C36(H36C	109.5

P3(O3(Er1	140.9(16)

O3(P3(C25	110.9(10)

O3(P3(C33	111.6(11)

C25(P3(C33	108.6(10)

O3(P3(C29	110.1(10)

C25(P3(C29	112.0(10)

C33(P3(C29	103.5(9)

C126(C125(P103	109.9(15)

C126(C125(H12O	109.7

P103(C125(H12O	109.7

C126(C125(H12P	109.7

P103(C125(H12P	109.7

H12O(C125(H12P	108.2

C128(C126(C125	119(2)

C128(C126(C127	114(2)

C125(C126(C127	113(2)

C128(C126(H126	102.4

C125(C126(H126	102.4

C127(C126(H126	102.4

C126(C127(H12Q	109.5

C126(C127(H12R	109.5

H12Q(C127(H12R	109.5

C126(C127(H12S	109.5

H12Q(C127(H12S	109.5

H12R(C127(H12S	109.5

C126(C128(H12T	109.5

C126(C128(H12U	109.5

H12T(C128(H12U	109.5

C126(C128(H12V	109.5

H12T(C128(H12V	109.5

H12U(C128(H12V	109.5

C130(C129(P103	113.6(16)

C130(C129(H12W	108.9

P103(C129(H12W	108.9

C130(C129(H12$	108.9

P103(C129(H12$	108.9

H12W(C129(H12$	107.7

C131(C130(C132	109.1(19)

C131(C130(C129	108.2(19)

C132(C130(C129	111(2)

C131(C130(H130	109.5

C132(C130(H130	109.5

C129(C130(H130	109.5

C130(C131(H13C	109.5

C130(C131(H13D	109.5

H13C(C131(H13D	109.5

C130(C131(H13E	109.5

H13C(C131(H13E	109.5

H13D(C131(H13E	109.5

C130(C132(H13F	109.5

C130(C132(H13G	109.5

H13F(C132(H13G	109.5

C130(C132(H13H	109.5

H13F(C132(H13H	109.5

H13G(C132(H13H	109.5

C134(C133(P103	120.6(17)

C134(C133(H13I	107.2

P103(C133(H13I	107.2

C134(C133(H13J	107.2

P103(C133(H13J	107.2

H13I(C133(H13J	106.8

C136(C134(C133	124(2)

C136(C134(C135	110(2)

C133(C134(C135	113(2)

C136(C134(H134	102.1

C133(C134(H134	102.1

C135(C134(H134	102.1

C134(C135(H13K	109.5

C134(C135(H13L	109.5

H13K(C135(H13L	109.5

C134(C135(H13M	109.5

H13K(C135(H13M	109.5

H13L(C135(H13M	109.5

C134(C136(H13N	109.5

C134(C136(H13O	109.5

H13N(C136(H13O	109.5

C134(C136(H13P	109.5

H13N(C136(H13P	109.5

H13O(C136(H13P	109.5

P103(O103(Er1	154(3)

O103(P103(C133	113.7(16)

O103(P103(C125	111.4(16)

C133(P103(C125	109.5(14)

O103(P103(C129	109.8(16)

C133(P103(C129	106.0(13)

C125(P103(C129	106.1(13)

O13(N11(O12	121.9(9)

O13(N11(O11	122.4(9)

O12(N11(O11	115.6(8)

O13(N11(Er1	177.1(9)

O12(N11(Er1	56.1(4)

O11(N11(Er1	59.7(4)

N11(O11(Er1	93.9(5)

N11(O12(Er1	97.9(5)

O23(N21(O21	122.2(11)

O23(N21(O22	120.8(10)

O21(N21(O22	117.0(9)

O23(N21(Er1	176.2(7)

O21(N21(Er1	56.5(5)

O22(N21(Er1	60.8(5)

N21(O21(Er1	97.8(6)

N21(O22(Er1	93.0(6)

O33(N31(O31	124.2(10)

O33(N31(O32	122.4(10)

O31(N31(O32	113.3(8)

O33(N31(Er1	176.5(8)

O31(N31(Er1	57.9(5)

O32(N31(Er1	55.6(5)

N31(O31(Er1	96.6(6)

N31(O32(Er1	98.0(6)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

Er1	83(1) 	49(1)	34(1) 	1(1)	7(1) 	7(1)

C1	90(9) 	50(6)	38(5) 	(2(4)	(5(6) 	(3(6)

C2	64(8) 	62(7)	58(7) 	(14(6)	4(6) 	(1(6)

C3	88(10) 	116(11)	68(8) 	(21(7)	(1(7) 	36(8)

C4	77(9) 	90(9)	66(7) 	(38(7)	9(6) 	0(7)

C5	69(7) 	66(8)	43(6) 	(1(6)	11(5) 	4(6)

C6	72(9) 	144(12)	110(10) 	(42(10)	(23(7) 	36(9)

C7	93(12) 	220(20)	119(12) 	(64(12)	10(10) 	(39(12)

C8	77(11) 	202(19)	247(19) 	67(16)	(4(12) 	15(12)

C9	81(8) 	74(7)	39(5) 	3(5)	10(5) 	(4(6)

C10	94(9) 	63(8)	57(7) 	(4(6)	23(6) 	(2(7)

C11	117(11) 	107(10)	54(7) 	18(7)	8(7) 	(22(9)

C12	95(11) 	105(11)	66(8) 	14(7)	26(7) 	14(8)

O1	69(4) 	57(4)	39(3) 	0(3)	6(3) 	(1(4)

P1	69(2) 	67(2)	34(1) 	(3(1)	6(1) 	1(2)

C13	45(12) 	57(14)	76(13) 	19(12)	(3(11) 	(16(11)

C14	68(14) 	82(17)	89(17) 	42(14)	(16(14) 	(19(14)

C15	87(18) 	180(30)	86(18) 	28(17)	(6(14) 	10(18)

C16	53(15) 	108(16)	87(15) 	25(12)	25(12) 	(8(13)

C17	59(12) 	87(13)	83(14) 	(42(11)	2(11) 	1(11)

C18	76(12) 	97(13)	117(13) 	(47(12)	10(12) 	(22(12)

C19	99(19) 	129(18)	180(30) 	(137(18)	(81(18) 	61(16)

C20	90(20) 	110(20)	220(30) 	(70(20)	(20(20) 	37(17)

C21	78(14) 	116(14)	69(12) 	(31(11)	10(11) 	0(12)

C22	88(14) 	140(15)	107(13) 	(38(13)	3(12) 	37(13)

C23	51(13) 	26(11)	112(17) 	(35(12)	6(13) 	12(10)

C24	100(20) 	190(30)	85(18) 	(33(19)	(2(16) 	50(20)

O2	60(14) 	51(10)	44(12) 	(1(8)	20(10) 	(18(8)

P2	53(7) 	58(7)	65(7) 	(14(6)	(3(5) 	(1(5)

C113	57(15) 	36(14)	81(16) 	(18(12)	(5(12) 	(2(12)

C114	64(13) 	71(14)	53(13) 	(20(11)	(23(11) 	(31(12)

C115	100(20) 	55(17)	67(17) 	10(13)	(14(15) 	(28(15)

C116	73(19) 	46(15)	150(20) 	(11(17)	(49(18) 	(32(13)

C117	64(14) 	86(14)	84(14) 	(53(13)	8(13) 	(16(13)

C118	70(13) 	98(14)	118(14) 	(46(13)	3(12) 	(18(13)

C119	120(30) 	130(20)	170(30) 	(110(20)	(20(20) 	10(20)

C120	64(18) 	80(20)	160(30) 	(30(20)	0(20) 	(18(15)

C121	72(15) 	141(17)	95(15) 	(19(14)	3(13) 	13(15)

C122	87(14) 	141(16)	105(14) 	(39(13)	6(13) 	40(14)

C123	150(30) 	130(30)	170(30) 	10(20)	20(20) 	120(20)

C124	50(17) 	130(20)	100(20) 	(24(18)	8(15) 	(9(16)

O102	72(16) 	45(11)	49(11) 	(14(10)	(3(10) 	1(10)

P102	52(8) 	53(7)	62(8) 	(16(6)	4(6) 	(9(5)

C25	75(14) 	80(12)	103(13) 	(12(11)	11(11) 	(12(11)

C26	107(15) 	127(15)	170(15) 	(20(14)	13(13) 	18(13)

C27	190(20) 	109(19)	190(20) 	(106(17)	(16(19) 	(15(18)

C28	109(18) 	140(20)	190(20) 	0(20)	13(18) 	(16(17)

C29	60(14) 	121(16)	101(13) 	7(12)	(5(11) 	(31(12)

C30	107(14) 	100(14)	76(11) 	(3(11)	(27(11) 	(37(12)

C31	107(19) 	100(20)	116(18) 	(30(18)	(25(15) 	(43(17)

C32	110(20) 	105(19)	210(20) 	(75(18)	(36(18) 	(8(14)

C33	136(19) 	67(13)	143(18) 	1(13)	(3(15) 	(46(15)

C34	140(20) 	93(15)	146(19) 	36(14)	21(16) 	(16(14)

C35	160(20) 	68(16)	150(20) 	20(15)	25(18) 	(24(15)

C36	200(30) 	140(20)	240(30) 	30(20)	20(30) 	40(30)

O3	54(9) 	57(10)	53(8) 	(4(8)	(9(7) 	(10(6)

P3	77(9) 	75(5)	59(4) 	(4(4)	2(4) 	(13(5)

C125	91(18) 	94(18)	142(19) 	(38(17)	24(16) 	10(16)

C126	130(20) 	130(19)	190(20) 	(27(18)	23(18) 	25(18)

C127	190(30) 	170(30)	210(30) 	(70(30)	(30(30) 	30(30)

C128	140(30) 	160(30)	200(30) 	10(30)	50(30) 	40(30)

C129	70(20) 	110(20)	96(19) 	44(17)	(30(17) 	(20(17)

C130	91(18) 	93(18)	91(17) 	18(16)	(32(16) 	(33(16)

C131	80(30) 	140(30)	90(30) 	40(20)	(40(20) 	(50(20)

C132	100(30) 	90(30)	90(20) 	20(20)	(40(20) 	(20(20)

C133	110(30) 	62(18)	160(20) 	18(18)	0(20) 	(30(20)

C134	110(20) 	61(16)	130(20) 	36(17)	0(17) 	(35(17)

C135	120(30) 	140(30)	180(30) 	10(30)	30(30) 	(40(30)

C136	60(20) 	36(18)	110(30) 	(2(18)	(10(19) 	(25(16)

O103	71(17) 	49(14)	50(13) 	(19(12)	(4(13) 	(13(12)

P103	45(11) 	59(8)	92(10) 	(10(7)	(20(8) 	(22(6)

N11	99(8) 	62(7)	52(6) 	2(5)	(8(5) 	32(6)

O11	97(6) 	60(5)	43(4) 	5(4)	3(4) 	13(4)

O12	92(5) 	56(4)	40(3) 	(5(3)	(3(3) 	13(4)

O13	111(8) 	95(7)	62(5) 	(4(4)	(17(5) 	43(6)

N21	96(7) 	67(7)	44(6) 	(7(6)	2(6) 	20(5)

O21	99(6) 	60(4)	36(4) 	(1(3)	4(4) 	13(4)

O22	102(6) 	82(6)	37(4) 	1(4)	12(4) 	15(5)

O23	118(7) 	101(7)	43(4) 	(24(4)	17(4) 	9(5)

N31	81(8) 	54(7)	38(5) 	(5(4)	0(5) 	12(6)

O31	72(5) 	52(5)	51(4) 	6(3)	2(4) 	8(4)

O32	86(6) 	71(6)	43(4) 	0(4)	2(4) 	8(4)

O33	119(8) 	75(6)	56(5) 	8(4)	(2(4) 	47(5)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H1A	5280	10992	2806	71	1

H1B	5487	11617	2520	71	1

H2	3777	10946	2646	73	1

H3A	3300	12050	2288	136	1

H3B	3877	11308	2126	136	1

H3C	4301	12238	2204	136	1

H4A	4417	12631	2791	116	1

H4B	4168	11891	3038	116	1

H4C	3422	12330	2830	116	1

H5A	6372	9775	2728	71	1

H5B	6354	9077	2453	71	1

H6	7229	10046	2142	130	1

H7A	6792	11315	2438	216	1

H7B	7802	11267	2345	216	1

H7C	7503	11017	2689	216	1

H8A	8490	9573	2370	263	1

H8B	7794	8913	2517	263	1

H8C	8130	9734	2713	263	1

H9A	4000	9595	2314	77	1

H9B	4719	8844	2309	77	1

H10	4381	9643	2887	86	1

H11A	4714	8222	3078	139	1

H11B	5482	8528	2851	139	1

H11C	4763	7848	2732	139	1

H12A	3272	8344	2633	133	1

H12B	2981	9319	2718	133	1

H12C	3253	8653	2987	133	1

H13A	6693	13165	1162	71	0.540(10)

H13B	7036	12348	968	71	0.540(10)

H14	5601	11957	847	96	0.540(10)

H15A	5403	12987	449	176	0.540(10)

H15B	6427	12812	492	176	0.540(10)

H15C	5998	13685	627	176	0.540(10)

H16A	5002	13481	1129	124	0.540(10)

H16B	4726	12498	1208	124	0.540(10)

H16C	4451	12923	884	124	0.540(10)

H17A	5334	12482	1707	91	0.540(10)

H17B	6044	12153	1950	91	0.540(10)

H18	6392	13769	1634	116	0.540(10)

H19A	4977	13950	1843	206	0.540(10)

H19B	5650	14475	2057	206	0.540(10)

H19C	5288	13544	2167	206	0.540(10)

H20A	7182	14088	2075	210	0.540(10)

H20B	7394	13076	2022	210	0.540(10)

H20C	6686	13361	2275	210	0.540(10)

H21A	7905	12316	1580	105	0.540(10)

H21B	7579	11537	1793	105	0.540(10)

H22	8117	10504	1456	134	0.540(10)

H23A	9665	10941	1459	95	0.540(10)

H23B	9238	11204	1784	95	0.540(10)

H23C	9391	11933	1524	95	0.540(10)

H24A	7901	11335	981	189	0.540(10)

H24B	8808	10820	1008	189	0.540(10)

H24C	8774	11849	1072	189	0.540(10)

H11D	7025	13237	1223	69	0.460(10)

H11E	7025	12396	1003	69	0.460(10)

H114	5367	12896	1229	75	0.460(10)

H11F	4872	12240	783	110	0.460(10)

H11G	5712	11668	870	110	0.460(10)

H11H	5774	12393	604	110	0.460(10)

H11I	6063	13883	742	135	0.460(10)

H11J	5935	14244	1087	135	0.460(10)

H11K	5103	13965	885	135	0.460(10)

H11L	5470	12388	1796	94	0.460(10)

H11M	6308	12325	2015	94	0.460(10)

H118	5831	13809	1643	114	0.460(10)

H11N	5062	13846	2087	210	0.460(10)

H11O	5863	14490	2153	210	0.460(10)

H11P	5872	13519	2291	210	0.460(10)

H12D	7110	14440	1939	155	0.460(10)

H12E	7268	13969	1612	155	0.460(10)

H12F	7449	13451	1928	155	0.460(10)

H12G	8058	12461	1641	123	0.460(10)

H12H	7812	11591	1824	123	0.460(10)

H122	8797	11765	1293	133	0.460(10)

H12I	8658	10527	1795	226	0.460(10)

H12J	9500	11086	1699	226	0.460(10)

H12K	9221	10254	1498	226	0.460(10)

H12L	7908	10172	1313	137	0.460(10)

H12M	8524	10546	1044	137	0.460(10)

H12N	7560	10930	1090	137	0.460(10)

H25A	2018	8345	1716	103	0.655(9)

H25B	2637	8476	2007	103	0.655(9)

H26	1725	9727	1677	162	0.655(9)

H27A	1315	9470	2307	243	0.655(9)

H27B	946	8823	2047	243	0.655(9)

H27C	707	9840	2035	243	0.655(9)

H28A	2034	10678	2129	220	0.655(9)

H28B	2341	10803	1778	220	0.655(9)

H28C	2976	10340	2022	220	0.655(9)

H29A	2829	9485	1138	113	0.655(9)

H29B	3646	8914	1031	113	0.655(9)

H30	2258	7850	1178	113	0.655(9)

H31A	1372	8955	1025	163	0.655(9)

H31B	1349	8217	763	163	0.655(9)

H31C	1910	9087	711	163	0.655(9)

H32A	2551	7162	719	213	0.655(9)

H32B	3472	7407	872	213	0.655(9)

H32C	3094	7981	592	213	0.655(9)

H33A	3356	7241	1483	139	0.655(9)

H33B	4291	7616	1398	139	0.655(9)

H34	4417	7703	1956	153	0.655(9)

H35A	3330	6223	1983	189	0.655(9)

H35B	3008	7188	2069	189	0.655(9)

H35C	3770	6736	2266	189	0.655(9)

H36A	4795	6014	1799	292	0.655(9)

H36B	5207	6623	2063	292	0.655(9)

H36C	5417	6812	1706	292	0.655(9)

H12O	1959	8279	1881	131	0.345(9)

H12P	2658	8808	2084	131	0.345(9)

H126	1234	9407	1754	180	0.345(9)

H12Q	1554	9522	2332	282	0.345(9)

H12R	793	10045	2159	282	0.345(9)

H12S	1710	10511	2226	282	0.345(9)

H12T	2646	10214	1583	249	0.345(9)

H12U	2011	10881	1758	249	0.345(9)

H12V	1658	10330	1469	249	0.345(9)

H12W	2434	9885	1291	110	0.345(9)

H12$	2972	9272	1060	110	0.345(9)

H130	1447	8495	1322	110	0.345(9)

H13C	930	9868	1204	157	0.345(9)

H13D	556	9201	951	157	0.345(9)

H13E	1359	9826	866	157	0.345(9)

H13F	1957	8478	686	137	0.345(9)

H13G	1362	7772	859	137	0.345(9)

H13H	2389	7815	928	137	0.345(9)

H13I	2696	7359	1457	135	0.345(9)

H13J	3499	7644	1246	135	0.345(9)

H134	4454	7344	1613	122	0.345(9)

H13K	3385	6705	2083	220	0.345(9)

H13L	3478	7741	2047	220	0.345(9)

H13M	4327	7153	2105	220	0.345(9)

H13N	4022	5816	1767	102	0.345(9)

H13O	4625	6111	1483	102	0.345(9)

H13P	3603	5948	1431	102	0.345(9)