|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	2009src1247

Empirical formula 	C36H81HoN3O12P3

Formula weight 	1005.88

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Tetragonal

Space group 	P41212

Unit cell dimensions	a = 15.2959(6) Å	( = 90°

b = 15.2959(6) Å	( = 90°

c = 43.217(2) Å	(  = 90°

Volume	10111.3(7) Å3

Z	8

Density (calculated)	1.322 Mg / m3

Absorption coefficient	1.712 mm(1

F(000)	4208

Crystal	block; colourless

Crystal size	0.22 ( 0.15 ( 0.12 mm3

( range for data collection	2.98 ( 27.48°

Index ranges	(19 ( h ( 19, (19 ( k ( 19, (56 ( l ( 51

Reflections collected	51946

Independent reflections	11537 [Rint = 0.0682]

Completeness to ( = 27.48°	99.6 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.8209 and 0.7045

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	11537 / 946 / 751

Goodness-of-fit on F2	1.048

Final R indices [F2 > 2((F2)]	R1 = 0.0588, wR2 = 0.1385

R indices (all data)	R1 = 0.0857, wR2 = 0.1538

Absolute structure parameter	0.097(16)

Largest diff. peak and hole	0.972 and (1.912 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP3 for Windows (L. J. Farrugia, J. Appl. Crystallogr. 1997, 30, 565).

Special details:

All hydrogen atoms were fixed using a standard riding model.

Two of the three phosphorus ligands were disordered. This resulted in all the ligands been restrained to be similar using the SAME compound. Also a loose global thermal restraint (SIMU) was used.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

Ho1	5335(1)	85(1)	984(1)	48(1)	1

C1	4531(6)	607(5)	80(2)	63(2)	1

C2	4311(6)	893(6)	(254(2)	68(2)	1

C3	3392(7)	1168(8)	(271(2)	87(3)	1

C4	4892(8)	1640(7)	(362(2)	87(3)	1

C5	5115(5)	(1141(5)	(90(2)	56(2)	1

C6	4172(5)	(1453(6)	(84(2)	59(2)	1

C7	4030(7)	(2134(7)	(331(2)	75(3)	1

C8	3905(7)	(1776(7)	222(2)	82(3)	1

C9	6374(5)	286(6)	(2(2)	64(2)	1

C10	7215(6)	(105(8)	125(2)	93(3)	1

C11	7967(8)	479(11)	7(3)	144(6)	1

C12	7349(7)	(946(10)	31(3)	130(6)	1

O1	5449(3)	(413(3)	486(1)	49(1)	1

P1	5376(1)	(186(1)	145(1)	50(1)	1

C13	6010(20)	(2593(15)	760(6)	69(6)	0.405(9)

C14	6180(17)	(3578(16)	762(7)	80(6)	0.405(9)

C15	5619(19)	(4097(17)	568(7)	87(8)	0.405(9)

C16	7085(17)	(3860(20)	702(9)	112(9)	0.405(9)

C17	7609(13)	(1716(19)	939(6)	77(5)	0.405(9)

C18	8201(17)	(1090(20)	1098(7)	96(6)	0.405(9)

C19	8800(19)	(580(20)	894(7)	120(9)	0.405(9)

C20	7900(20)	(600(30)	1349(7)	136(12)	0.405(9)

C21	6503(15)	(2530(17)	1425(5)	54(5)	0.405(9)

C22	5688(12)	(2433(14)	1642(4)	53(5)	0.405(9)

C23	5881(13)	(3004(16)	1922(4)	67(7)	0.405(9)

C24	5320(20)	(1720(20)	1732(8)	176(15)	0.405(9)

O2	6004(12)	(1098(12)	1097(6)	44(5)	0.405(9)

P2	6508(9)	(1929(9)	1065(3)	46(2)	0.405(9)

C113	6038(13)	(2478(11)	695(4)	58(4)	0.595(9)

C114	6156(11)	(3461(11)	628(4)	73(5)	0.595(9)

C115	5493(12)	(3754(12)	401(4)	84(6)	0.595(9)

C116	6987(12)	(3616(17)	461(6)	127(9)	0.595(9)

C117	7787(10)	(1862(16)	886(5)	88(5)	0.595(9)

C118	8426(11)	(1376(17)	1072(4)	95(5)	0.595(9)

C119	9302(8)	(1289(10)	935(4)	68(4)	0.595(9)

C120	8387(13)	(1133(19)	1382(4)	121(8)	0.595(9)

C121	6656(10)	(2685(10)	1336(4)	50(4)	0.595(9)

C122	5776(8)	(2916(10)	1473(4)	63(4)	0.595(9)

C123	5808(13)	(3843(10)	1592(5)	107(7)	0.595(9)

C124	4917(10)	(2857(13)	1432(4)	102(6)	0.595(9)

O102	6305(9)	(1091(9)	1075(4)	45(3)	0.595(9)

P102	6672(7)	(1973(8)	1004(2)	53(2)	0.595(9)

C25	2452(12)	1255(12)	700(4)	73(4)	0.603(8)

C26	1883(14)	440(14)	695(5)	116(5)	0.603(8)

C27	2283(17)	(392(16)	680(7)	148(9)	0.603(8)

C28	1193(16)	469(19)	448(5)	156(9)	0.603(8)

C29	3093(10)	1125(10)	1347(3)	74(4)	0.603(8)

C30	2490(11)	1771(10)	1493(3)	82(4)	0.603(8)

C31	1704(13)	1357(14)	1631(5)	99(7)	0.603(8)

C32	2923(13)	2349(12)	1710(5)	127(8)	0.603(8)

C33	3851(12)	2398(9)	929(4)	90(5)	0.603(8)

C34	4243(12)	2794(13)	643(5)	100(5)	0.603(8)

C35	3527(15)	3205(15)	445(5)	114(7)	0.603(8)

C36	4957(15)	3320(16)	645(6)	152(10)	0.603(8)

O3	4094(12)	659(13)	843(6)	54(4)	0.603(8)

P3	3413(5)	1307(6)	945(2)	63(2)	0.603(8)

C125	2340(20)	1249(18)	606(6)	85(6)	0.397(8)

C126	1816(19)	414(19)	548(6)	107(7)	0.397(8)

C127	2314(19)	(353(19)	472(6)	92(8)	0.397(8)

C128	1162(18)	550(30)	293(5)	130(11)	0.397(8)

C129	2563(14)	746(14)	1248(5)	82(6)	0.397(8)

C130	1737(13)	1174(14)	1366(5)	81(5)	0.397(8)

C131	1085(14)	489(17)	1456(5)	87(8)	0.397(8)

C132	1910(20)	1788(16)	1608(6)	88(8)	0.397(8)

C133	3337(16)	2363(10)	1031(5)	82(6)	0.397(8)

C134	3955(17)	2937(12)	839(6)	85(6)	0.397(8)

C135	3740(30)	2800(20)	501(6)	129(10)	0.397(8)

C136	4032(17)	3804(11)	898(6)	84(8)	0.397(8)

O103	3938(15)	764(19)	849(8)	40(4)	0.397(8)

P103	3112(7)	1263(9)	920(3)	55(3)	0.397(8)

N11	4000(5)	(1007(4)	1264(2)	64(2)	1

O11	4269(4)	(1154(4)	985(1)	60(1)	1

O12	4407(4)	(412(3)	1408(1)	59(1)	1

O13	3434(5)	(1431(4)	1382(1)	83(2)	1

N21	6503(5)	1348(4)	705(1)	56(2)	1

O21	5686(4)	1383(3)	663(1)	56(1)	1

O22	6762(4)	742(4)	892(1)	61(2)	1

O23	7012(5)	1843(5)	575(1)	77(2)	1

N31	5687(5)	1069(5)	1545(1)	60(2)	1

O31	5227(5)	1363(3)	1320(1)	61(2)	1

O32	6047(4)	344(4)	1505(1)	68(2)	1

O33	5766(5)	1481(4)	1783(1)	77(2)	1

Table 3. Bond lengths [Å] and angles [°].

Ho1(O2	2.136(19)

Ho1(O3	2.178(18)

Ho1(O1	2.290(4)

Ho1(O102	2.364(13)

Ho1(O22	2.435(6)

Ho1(O31	2.442(5)

Ho1(O12	2.441(5)

Ho1(O103	2.45(2)

Ho1(O21	2.481(5)

Ho1(O11	2.499(5)

Ho1(O32	2.534(5)

Ho1(N21	2.895(7)

C1(C2	1.545(8)

C1(P1	1.796(7)

C1(H1A	0.9900

C1(H1B	0.9900

C2(C3	1.468(12)

C2(C4	1.520(11)

C2(H2	1.0000

C3(H3A	0.9800

C3(H3B	0.9800

C3(H3C	0.9800

C4(H4A	0.9800

C4(H4B	0.9800

C4(H4C	0.9800

C5(C6	1.519(10)

C5(P1	1.823(7)

C5(H5A	0.9900

C5(H5B	0.9900

C6(C8	1.468(10)

C6(C7	1.509(10)

C6(H6	1.0000

C7(H7A	0.9800

C7(H7B	0.9800

C7(H7C	0.9800

C8(H8A	0.9800

C8(H8B	0.9800

C8(H8C	0.9800

C9(C10	1.523(12)

C9(P1	1.805(7)

C9(H9A	0.9900

C9(H9B	0.9900

C10(C12	1.365(14)

C10(C11	1.544(13)

C10(H10	1.0000

C11(H11A	0.9800

C11(H11B	0.9800

C11(H11C	0.9800

C12(H12A	0.9800

C12(H12B	0.9800

C12(H12C	0.9800

O1(P1	1.516(4)

C13(C14	1.529(16)

C13(P2	1.828(13)

C13(H13A	0.9900

C13(H13B	0.9900

C14(C15	1.437(17)

C14(C16	1.470(17)

C14(H14	1.0000

C15(H15A	0.9800

C15(H15B	0.9800

C15(H15C	0.9800

C16(H16A	0.9800

C16(H16B	0.9800

C16(H16C	0.9800

C17(C18	1.482(15)

C17(P2	1.800(13)

C17(H17A	0.9900

C17(H17B	0.9900

C18(C20	1.398(18)

C18(C19	1.497(17)

C18(H18	1.0000

C19(H19A	0.9800

C19(H19B	0.9800

C19(H19C	0.9800

C20(H20A	0.9800

C20(H20B	0.9800

C20(H20C	0.9800

C21(C22	1.568(16)

C21(P2	1.806(13)

C21(H21A	0.9900

C21(H21B	0.9900

C22(C24	1.291(18)

C22(C23	1.520(15)

C22(H22	1.0000

C23(H23A	0.9800

C23(H23B	0.9800

C23(H23C	0.9800

C24(H24A	0.9800

C24(H24B	0.9800

C24(H24C	0.9800

O2(P2	1.493(12)

C113(C114	1.542(14)

C113(P102	1.823(11)

C113(H11D	0.9900

C113(H11E	0.9900

C114(C115	1.480(15)

C114(C116	1.481(16)

C114(H114	1.0000

C115(H11F	0.9800

C115(H11G	0.9800

C115(H11H	0.9800

C116(H11I	0.9800

C116(H11J	0.9800

C116(H11K	0.9800

C117(C118	1.466(14)

C117(P102	1.788(12)

C117(H11L	0.9900

C117(H11M	0.9900

C118(C120	1.391(15)

C118(C119	1.472(15)

C118(H118	1.0000

C119(H11N	0.9800

C119(H11O	0.9800

C119(H11P	0.9800

C120(H12D	0.9800

C120(H12E	0.9800

C120(H12F	0.9800

C121(C122	1.513(14)

C121(P102	1.801(11)

C121(H12G	0.9900

C121(H12H	0.9900

C122(C124	1.330(16)

C122(C123	1.509(15)

C122(H122	1.0000

C123(H12I	0.9800

C123(H12J	0.9800

C123(H12K	0.9800

C124(H12L	0.9800

C124(H12M	0.9800

C124(H12N	0.9800

O102(P102	1.492(10)

C25(C26	1.521(15)

C25(P3	1.814(12)

C25(H25A	0.9900

C25(H25B	0.9900

C26(C27	1.414(17)

C26(C28	1.502(16)

C26(H26	1.0000

C27(H27A	0.9800

C27(H27B	0.9800

C27(H27C	0.9800

C28(H28A	0.9800

C28(H28B	0.9800

C28(H28C	0.9800

C29(C30	1.492(14)

C29(P3	1.825(11)

C29(H29A	0.9900

C29(H29B	0.9900

C30(C32	1.449(16)

C30(C31	1.482(16)

C30(H30	1.0000

C31(H31A	0.9800

C31(H31B	0.9800

C31(H31C	0.9800

C32(H32A	0.9800

C32(H32B	0.9800

C32(H32C	0.9800

C33(C34	1.504(16)

C33(P3	1.800(13)

C33(H33A	0.9900

C33(H33B	0.9900

C34(C36	1.357(17)

C34(C35	1.526(16)

C34(H34	1.0000

C35(H35A	0.9800

C35(H35B	0.9800

C35(H35C	0.9800

C36(H36A	0.9800

C36(H36B	0.9800

C36(H36C	0.9800

O3(P3	1.505(11)

C125(C126	1.527(16)

C125(P103	1.800(14)

C125(H12O	0.9900

C125(H12P	0.9900

C126(C127	1.438(18)

C126(C128	1.501(17)

C126(H126	1.0000

C127(H12Q	0.9800

C127(H12R	0.9800

C127(H12S	0.9800

C128(H12T	0.9800

C128(H12U	0.9800

C128(H12V	0.9800

C129(C130	1.512(16)

C129(P103	1.828(13)

C129(H12W	0.9900

C129(H12$	0.9900

C130(C132	1.431(17)

C130(C131	1.497(17)

C130(H130	1.0000

C131(H13C	0.9800

C131(H13D	0.9800

C131(H13E	0.9800

C132(H13F	0.9800

C132(H13G	0.9800

C132(H13H	0.9800

C133(C134	1.533(17)

C133(P103	1.784(14)

C133(H13I	0.9900

C133(H13J	0.9900

C134(C136	1.355(17)

C134(C135	1.514(18)

C134(H134	1.0000

C135(H13K	0.9800

C135(H13L	0.9800

C135(H13M	0.9800

C136(H13N	0.9800

C136(H13O	0.9800

C136(H13P	0.9800

O103(P103	1.508(12)

N11(O13	1.196(9)

N11(O12	1.266(8)

N11(O11	1.295(8)

N21(O23	1.221(8)

N21(O21	1.264(9)

N21(O22	1.293(9)

N31(O33	1.210(7)

N31(O32	1.251(10)

N31(O31	1.281(9)

O2(Ho1(O3	145.4(8)

O2(Ho1(O1	84.1(7)

O3(Ho1(O1	86.4(6)

O2(Ho1(O102	10.5(8)

O3(Ho1(O102	154.2(7)

O1(Ho1(O102	81.7(4)

O2(Ho1(O22	87.6(6)

O3(Ho1(O22	124.7(6)

O1(Ho1(O22	85.16(17)

O102(Ho1(O22	77.2(4)

O2(Ho1(O31	125.1(7)

O3(Ho1(O31	77.6(6)

O1(Ho1(O31	146.19(16)

O102(Ho1(O31	123.5(4)

O22(Ho1(O31	80.1(2)

O2(Ho1(O12	81.0(7)

O3(Ho1(O12	80.1(6)

O1(Ho1(O12	130.33(16)

O102(Ho1(O12	90.1(4)

O22(Ho1(O12	140.56(16)

O31(Ho1(O12	76.26(18)

O2(Ho1(O103	146.4(9)

O3(Ho1(O103	2.7(13)

O1(Ho1(O103	89.1(8)

O102(Ho1(O103	155.6(8)

O22(Ho1(O103	124.7(8)

O31(Ho1(O103	75.1(8)

O12(Ho1(O103	78.6(8)

O2(Ho1(O21	134.6(6)

O3(Ho1(O21	73.1(6)

O1(Ho1(O21	73.99(16)

O102(Ho1(O21	124.5(4)

O22(Ho1(O21	52.0(2)

O31(Ho1(O21	72.93(16)

O12(Ho1(O21	142.66(19)

O103(Ho1(O21	73.5(8)

O2(Ho1(O11	70.8(5)

O3(Ho1(O11	74.8(6)

O1(Ho1(O11	78.42(16)

O102(Ho1(O11	80.4(4)

O22(Ho1(O11	153.9(2)

O31(Ho1(O11	124.2(2)

O12(Ho1(O11	51.92(16)

O103(Ho1(O11	75.6(8)

O21(Ho1(O11	138.47(17)

O2(Ho1(O32	73.9(7)

O3(Ho1(O32	124.0(6)

O1(Ho1(O32	148.81(19)

O102(Ho1(O32	72.6(4)

O22(Ho1(O32	72.28(18)

O31(Ho1(O32	51.3(2)

O12(Ho1(O32	68.29(19)

O103(Ho1(O32	121.3(8)

O21(Ho1(O32	106.21(18)

O11(Ho1(O32	113.41(17)

O2(Ho1(N21	111.4(6)

O3(Ho1(N21	98.7(6)

O1(Ho1(N21	77.49(16)

O102(Ho1(N21	101.0(4)

O22(Ho1(N21	26.3(2)

O31(Ho1(N21	75.83(18)

O12(Ho1(N21	151.62(16)

O103(Ho1(N21	99.0(8)

O21(Ho1(N21	25.74(19)

O11(Ho1(N21	155.40(15)

O32(Ho1(N21	90.06(18)

C2(C1(P1	119.7(6)

C2(C1(H1A	107.4

P1(C1(H1A	107.4

C2(C1(H1B	107.4

P1(C1(H1B	107.4

H1A(C1(H1B	106.9

C3(C2(C4	109.2(8)

C3(C2(C1	109.6(7)

C4(C2(C1	111.8(7)

C3(C2(H2	108.7

C4(C2(H2	108.7

C1(C2(H2	108.7

C2(C3(H3A	109.5

C2(C3(H3B	109.5

H3A(C3(H3B	109.5

C2(C3(H3C	109.5

H3A(C3(H3C	109.5

H3B(C3(H3C	109.5

C2(C4(H4A	109.5

C2(C4(H4B	109.5

H4A(C4(H4B	109.5

C2(C4(H4C	109.5

H4A(C4(H4C	109.5

H4B(C4(H4C	109.5

C6(C5(P1	116.7(5)

C6(C5(H5A	108.1

P1(C5(H5A	108.1

C6(C5(H5B	108.1

P1(C5(H5B	108.1

H5A(C5(H5B	107.3

C8(C6(C7	111.4(8)

C8(C6(C5	112.7(7)

C7(C6(C5	110.0(7)

C8(C6(H6	107.5

C7(C6(H6	107.5

C5(C6(H6	107.5

C6(C7(H7A	109.5

C6(C7(H7B	109.5

H7A(C7(H7B	109.5

C6(C7(H7C	109.5

H7A(C7(H7C	109.5

H7B(C7(H7C	109.5

C6(C8(H8A	109.5

C6(C8(H8B	109.5

H8A(C8(H8B	109.5

C6(C8(H8C	109.5

H8A(C8(H8C	109.5

H8B(C8(H8C	109.5

C10(C9(P1	115.4(6)

C10(C9(H9A	108.4

P1(C9(H9A	108.4

C10(C9(H9B	108.4

P1(C9(H9B	108.4

H9A(C9(H9B	107.5

C12(C10(C9	112.9(9)

C12(C10(C11	109.6(11)

C9(C10(C11	106.3(9)

C12(C10(H10	109.3

C9(C10(H10	109.3

C11(C10(H10	109.3

C10(C11(H11A	109.5

C10(C11(H11B	109.5

H11A(C11(H11B	109.5

C10(C11(H11C	109.5

H11A(C11(H11C	109.5

H11B(C11(H11C	109.5

C10(C12(H12A	109.5

C10(C12(H12B	109.5

H12A(C12(H12B	109.5

C10(C12(H12C	109.5

H12A(C12(H12C	109.5

H12B(C12(H12C	109.5

P1(O1(Ho1	146.2(3)

O1(P1(C1	111.1(3)

O1(P1(C9	111.9(3)

C1(P1(C9	106.4(4)

O1(P1(C5	111.9(3)

C1(P1(C5	107.2(4)

C9(P1(C5	108.0(4)

C14(C13(P2	118.3(15)

C14(C13(H13A	107.7

P2(C13(H13A	107.7

C14(C13(H13B	107.7

P2(C13(H13B	107.7

H13A(C13(H13B	107.1

C15(C14(C16	107.5(18)

C15(C14(C13	116.2(18)

C16(C14(C13	116.3(19)

C15(C14(H14	105.2

C16(C14(H14	105.2

C13(C14(H14	105.2

C14(C15(H15A	109.5

C14(C15(H15B	109.5

H15A(C15(H15B	109.5

C14(C15(H15C	109.5

H15A(C15(H15C	109.5

H15B(C15(H15C	109.5

C14(C16(H16A	109.5

C14(C16(H16B	109.5

H16A(C16(H16B	109.5

C14(C16(H16C	109.5

H16A(C16(H16C	109.5

H16B(C16(H16C	109.5

C18(C17(P2	123.1(14)

C18(C17(H17A	106.6

P2(C17(H17A	106.6

C18(C17(H17B	106.6

P2(C17(H17B	106.6

H17A(C17(H17B	106.5

C20(C18(C17	120.6(18)

C20(C18(C19	112(2)

C17(C18(C19	115.8(18)

C20(C18(H18	101.5

C17(C18(H18	101.5

C19(C18(H18	101.5

C18(C19(H19A	109.5

C18(C19(H19B	109.5

H19A(C19(H19B	109.5

C18(C19(H19C	109.5

H19A(C19(H19C	109.5

H19B(C19(H19C	109.5

C18(C20(H20A	109.5

C18(C20(H20B	109.5

H20A(C20(H20B	109.5

C18(C20(H20C	109.5

H20A(C20(H20C	109.5

H20B(C20(H20C	109.5

C22(C21(P2	118.1(12)

C22(C21(H21A	107.8

P2(C21(H21A	107.8

C22(C21(H21B	107.8

P2(C21(H21B	107.8

H21A(C21(H21B	107.1

C24(C22(C23	109.4(19)

C24(C22(C21	127(2)

C23(C22(C21	105.5(13)

C24(C22(H22	104.1

C23(C22(H22	104.1

C21(C22(H22	104.1

C22(C23(H23A	109.5

C22(C23(H23B	109.5

H23A(C23(H23B	109.5

C22(C23(H23C	109.5

H23A(C23(H23C	109.5

H23B(C23(H23C	109.5

C22(C24(H24A	109.5

C22(C24(H24B	109.5

H24A(C24(H24B	109.5

C22(C24(H24C	109.5

H24A(C24(H24C	109.5

H24B(C24(H24C	109.5

P2(O2(Ho1	161.4(17)

O2(P2(C17	110.9(12)

O2(P2(C21	110.6(12)

C17(P2(C21	110.9(12)

O2(P2(C13	108.9(11)

C17(P2(C13	105.7(12)

C21(P2(C13	109.7(12)

C114(C113(P102	119.3(11)

C114(C113(H11D	107.5

P102(C113(H11D	107.5

C114(C113(H11E	107.5

P102(C113(H11E	107.5

H11D(C113(H11E	107.0

C115(C114(C116	102.6(13)

C115(C114(C113	109.9(12)

C116(C114(C113	110.3(15)

C115(C114(H114	111.3

C116(C114(H114	111.3

C113(C114(H114	111.3

C114(C115(H11F	109.5

C114(C115(H11G	109.5

H11F(C115(H11G	109.5

C114(C115(H11H	109.5

H11F(C115(H11H	109.5

H11G(C115(H11H	109.5

C114(C116(H11I	109.5

C114(C116(H11J	109.5

H11I(C116(H11J	109.5

C114(C116(H11K	109.5

H11I(C116(H11K	109.5

H11J(C116(H11K	109.5

C118(C117(P102	121.9(12)

C118(C117(H11L	106.9

P102(C117(H11L	106.9

C118(C117(H11M	106.9

P102(C117(H11M	106.9

H11L(C117(H11M	106.7

C120(C118(C117	129.3(14)

C120(C118(C119	113.7(13)

C117(C118(C119	115.7(12)

C120(C118(H118	93.8

C117(C118(H118	93.8

C119(C118(H118	93.8

C118(C119(H11N	109.5

C118(C119(H11O	109.5

H11N(C119(H11O	109.5

C118(C119(H11P	109.5

H11N(C119(H11P	109.5

H11O(C119(H11P	109.5

C118(C120(H12D	109.5

C118(C120(H12E	109.5

H12D(C120(H12E	109.5

C118(C120(H12F	109.5

H12D(C120(H12F	109.5

H12E(C120(H12F	109.5

C122(C121(P102	117.7(10)

C122(C121(H12G	107.9

P102(C121(H12G	107.9

C122(C121(H12H	107.9

P102(C121(H12H	107.9

H12G(C121(H12H	107.2

C124(C122(C123	98.1(13)

C124(C122(C121	144.3(14)

C123(C122(C121	109.0(12)

C124(C122(H122	99.1

C123(C122(H122	99.1

C121(C122(H122	99.1

C122(C123(H12I	109.5

C122(C123(H12J	109.5

H12I(C123(H12J	109.5

C122(C123(H12K	109.5

H12I(C123(H12K	109.5

H12J(C123(H12K	109.5

C122(C124(H12L	109.5

C122(C124(H12M	109.5

H12L(C124(H12M	109.5

C122(C124(H12N	109.5

H12L(C124(H12N	109.5

H12M(C124(H12N	109.5

P102(O102(Ho1	152.7(10)

O102(P102(C117	109.4(9)

O102(P102(C121	112.2(8)

C117(P102(C121	107.2(10)

O102(P102(C113	109.5(9)

C117(P102(C113	109.8(9)

C121(P102(C113	108.6(8)

C26(C25(P3	120.5(11)

C26(C25(H25A	107.2

P3(C25(H25A	107.2

C26(C25(H25B	107.2

P3(C25(H25B	107.2

H25A(C25(H25B	106.8

C27(C26(C28	107.4(17)

C27(C26(C25	119.5(17)

C28(C26(C25	112.8(17)

C27(C26(H26	105.3

C28(C26(H26	105.3

C25(C26(H26	105.3

C26(C27(H27A	109.5

C26(C27(H27B	109.5

H27A(C27(H27B	109.5

C26(C27(H27C	109.5

H27A(C27(H27C	109.5

H27B(C27(H27C	109.5

C26(C28(H28A	109.5

C26(C28(H28B	109.5

H28A(C28(H28B	109.5

C26(C28(H28C	109.5

H28A(C28(H28C	109.5

H28B(C28(H28C	109.5

C30(C29(P3	117.9(10)

C30(C29(H29A	107.8

P3(C29(H29A	107.8

C30(C29(H29B	107.8

P3(C29(H29B	107.8

H29A(C29(H29B	107.2

C32(C30(C31	111.9(13)

C32(C30(C29	113.2(14)

C31(C30(C29	112.9(13)

C32(C30(H30	106.1

C31(C30(H30	106.1

C29(C30(H30	106.1

C30(C31(H31A	109.5

C30(C31(H31B	109.5

H31A(C31(H31B	109.5

C30(C31(H31C	109.5

H31A(C31(H31C	109.5

H31B(C31(H31C	109.5

C30(C32(H32A	109.5

C30(C32(H32B	109.5

H32A(C32(H32B	109.5

C30(C32(H32C	109.5

H32A(C32(H32C	109.5

H32B(C32(H32C	109.5

C34(C33(P3	123.6(13)

C34(C33(H33A	106.4

P3(C33(H33A	106.4

C34(C33(H33B	106.4

P3(C33(H33B	106.4

H33A(C33(H33B	106.5

C36(C34(C33	123.6(19)

C36(C34(C35	109.7(16)

C33(C34(C35	110.0(15)

C36(C34(H34	103.8

C33(C34(H34	103.8

C35(C34(H34	103.8

C34(C35(H35A	109.5

C34(C35(H35B	109.5

H35A(C35(H35B	109.5

C34(C35(H35C	109.5

H35A(C35(H35C	109.5

H35B(C35(H35C	109.5

C34(C36(H36A	109.5

C34(C36(H36B	109.5

H36A(C36(H36B	109.5

C34(C36(H36C	109.5

H36A(C36(H36C	109.5

H36B(C36(H36C	109.5

P3(O3(Ho1	141.9(15)

O3(P3(C33	110.0(10)

O3(P3(C25	111.2(10)

C33(P3(C25	108.6(8)

O3(P3(C29	111.4(10)

C33(P3(C29	106.1(8)

C25(P3(C29	109.4(9)

C126(C125(P103	118.6(15)

C126(C125(H12O	107.7

P103(C125(H12O	107.7

C126(C125(H12P	107.7

P103(C125(H12P	107.7

H12O(C125(H12P	107.1

C127(C126(C128	107.0(19)

C127(C126(C125	116(2)

C128(C126(C125	111.0(19)

C127(C126(H126	107.4

C128(C126(H126	107.4

C125(C126(H126	107.4

C126(C127(H12Q	109.5

C126(C127(H12R	109.5

H12Q(C127(H12R	109.5

C126(C127(H12S	109.5

H12Q(C127(H12S	109.5

H12R(C127(H12S	109.5

C126(C128(H12T	109.5

C126(C128(H12U	109.5

H12T(C128(H12U	109.5

C126(C128(H12V	109.5

H12T(C128(H12V	109.5

H12U(C128(H12V	109.5

C130(C129(P103	117.3(13)

C130(C129(H12W	108.0

P103(C129(H12W	108.0

C130(C129(H12$	108.0

P103(C129(H12$	108.0

H12W(C129(H12$	107.2

C132(C130(C131	113.3(16)

C132(C130(C129	111.9(19)

C131(C130(C129	110.0(16)

C132(C130(H130	107.1

C131(C130(H130	107.1

C129(C130(H130	107.1

C130(C131(H13C	109.5

C130(C131(H13D	109.5

H13C(C131(H13D	109.5

C130(C131(H13E	109.5

H13C(C131(H13E	109.5

H13D(C131(H13E	109.5

C130(C132(H13F	109.5

C130(C132(H13G	109.5

H13F(C132(H13G	109.5

C130(C132(H13H	109.5

H13F(C132(H13H	109.5

H13G(C132(H13H	109.5

C134(C133(P103	120.9(13)

C134(C133(H13I	107.1

P103(C133(H13I	107.1

C134(C133(H13J	107.1

P103(C133(H13J	107.1

H13I(C133(H13J	106.8

C136(C134(C135	109.7(19)

C136(C134(C133	120.9(19)

C135(C134(C133	107.8(18)

C136(C134(H134	105.8

C135(C134(H134	105.8

C133(C134(H134	105.8

C134(C135(H13K	109.5

C134(C135(H13L	109.5

H13K(C135(H13L	109.5

C134(C135(H13M	109.5

H13K(C135(H13M	109.5

H13L(C135(H13M	109.5

C134(C136(H13N	109.5

C134(C136(H13O	109.5

H13N(C136(H13O	109.5

C134(C136(H13P	109.5

H13N(C136(H13P	109.5

H13O(C136(H13P	109.5

P103(O103(Ho1	154(2)

O103(P103(C133	111.8(13)

O103(P103(C125	113.0(14)

C133(P103(C125	110.0(11)

O103(P103(C129	108.8(13)

C133(P103(C129	106.7(11)

C125(P103(C129	106.2(12)

O13(N11(O12	122.4(7)

O13(N11(O11	122.2(7)

O12(N11(O11	115.3(7)

O13(N11(Ho1	177.8(7)

O12(N11(Ho1	56.4(4)

O11(N11(Ho1	59.1(4)

N11(O11(Ho1	94.5(4)

N11(O12(Ho1	98.0(4)

O23(N21(O21	122.7(7)

O23(N21(O22	122.4(8)

O21(N21(O22	114.9(6)

O23(N21(Ho1	176.2(6)

O21(N21(Ho1	58.5(3)

O22(N21(Ho1	56.6(4)

N21(O21(Ho1	95.8(4)

N21(O22(Ho1	97.1(5)

O33(N31(O32	122.3(7)

O33(N31(O31	121.1(8)

O32(N31(O31	116.6(6)

O33(N31(Ho1	175.1(6)

O32(N31(Ho1	60.4(3)

O31(N31(Ho1	56.4(3)

N31(O31(Ho1	97.7(4)

N31(O32(Ho1	94.1(4)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

Ho1	77(1) 	40(1)	26(1) 	1(1)	(8(1) 	(9(1)

C1	86(6) 	66(5)	36(3) 	(1(3)	(6(4) 	6(5)

C2	88(6) 	79(6)	36(4) 	8(4)	(15(4) 	12(5)

C3	104(9) 	87(8)	69(6) 	17(5)	(20(6) 	(10(6)

C4	113(9) 	95(7)	52(5) 	27(5)	(6(6) 	(9(7)

C5	70(5) 	64(5)	34(3) 	(12(3)	(9(4) 	4(4)

C6	69(5) 	62(5)	46(4) 	(11(4)	(12(4) 	(1(4)

C7	72(6) 	85(7)	68(5) 	(32(5)	(13(5) 	(10(5)

C8	85(7) 	97(8)	62(5) 	(4(5)	(10(5) 	(30(6)

C9	69(5) 	80(6)	44(4) 	(3(4)	(3(4) 	(8(5)

C10	62(6) 	141(10)	77(6) 	(14(7)	(2(5) 	(13(6)

C11	85(9) 	180(16)	168(13) 	2(12)	(18(9) 	(17(10)

C12	56(6) 	248(17)	85(7) 	(87(9)	(13(5) 	45(9)

O1	68(3) 	47(3)	32(2) 	(5(2)	(8(2) 	(3(2)

P1	65(1) 	59(1)	28(1) 	(5(1)	(8(1) 	(1(1)

C13	75(10) 	68(11)	63(12) 	(12(10)	(7(10) 	(4(10)

C14	82(11) 	84(12)	75(13) 	(30(12)	(10(12) 	8(10)

C15	103(17) 	79(16)	80(16) 	(15(13)	(6(15) 	0(14)

C16	90(16) 	100(17)	150(20) 	(53(19)	(4(18) 	19(14)

C17	66(10) 	90(11)	74(10) 	(31(9)	(4(9) 	(13(9)

C18	72(11) 	114(13)	101(11) 	(32(10)	(20(10) 	(28(10)

C19	93(16) 	127(19)	139(18) 	(18(17)	(46(15) 	(45(15)

C20	120(20) 	140(20)	150(20) 	(41(19)	(71(18) 	(34(19)

C21	45(9) 	56(10)	59(10) 	14(9)	(1(9) 	(3(9)

C22	49(9) 	60(10)	51(9) 	43(8)	(16(8) 	(20(8)

C23	45(11) 	125(19)	30(9) 	18(10)	(4(8) 	(7(12)

C24	150(30) 	240(30)	130(30) 	40(30)	(20(20) 	(80(30)

O2	37(11) 	35(7)	60(8) 	(11(6)	(18(8) 	3(7)

P2	47(5) 	42(4)	49(5) 	0(4)	(6(4) 	2(3)

C113	66(8) 	57(8)	52(9) 	(19(7)	(18(7) 	(20(7)

C114	82(8) 	78(9)	59(9) 	(25(8)	(2(8) 	9(7)

C115	89(12) 	69(11)	94(13) 	(58(10)	(8(11) 	(10(10)

C116	90(14) 	139(18)	154(19) 	(90(17)	10(15) 	(19(13)

C117	69(9) 	102(11)	92(10) 	(36(9)	9(8) 	(26(9)

C118	70(9) 	120(11)	96(9) 	(44(9)	(5(8) 	(12(9)

C119	42(8) 	63(9)	98(11) 	(18(8)	(16(8) 	(13(7)

C120	67(11) 	200(20)	99(12) 	(58(13)	43(10) 	(76(12)

C121	41(7) 	45(7)	63(8) 	(6(6)	(9(6) 	2(6)

C122	48(7) 	74(8)	67(8) 	14(7)	7(7) 	0(7)

C123	88(13) 	63(10)	170(19) 	(4(12)	37(14) 	7(9)

C124	90(13) 	110(13)	107(13) 	27(11)	(19(11) 	(19(12)

O102	43(8) 	45(5)	47(5) 	3(4)	(11(6) 	7(5)

P102	48(4) 	56(3)	56(4) 	(17(3)	(1(3) 	(1(2)

C25	84(9) 	73(8)	61(10) 	(8(8)	(9(8) 	19(8)

C26	126(11) 	117(10)	105(12) 	(33(11)	(37(10) 	(9(9)

C27	115(15) 	168(19)	163(18) 	(7(19)	(69(16) 	7(15)

C28	200(20) 	171(18)	101(17) 	(50(17)	(18(17) 	(20(18)

C29	67(9) 	89(10)	65(8) 	8(8)	6(7) 	28(8)

C30	103(10) 	90(9)	52(7) 	6(7)	33(7) 	9(9)

C31	107(15) 	104(15)	87(12) 	(24(12)	45(10) 	30(13)

C32	133(18) 	80(13)	168(19) 	(57(13)	12(16) 	24(12)

C33	100(11) 	72(9)	98(11) 	(9(9)	(15(9) 	39(10)

C34	110(12) 	87(10)	104(12) 	(4(10)	(24(10) 	30(10)

C35	132(18) 	86(14)	124(15) 	(4(12)	(20(14) 	49(13)

C36	150(20) 	127(19)	180(20) 	(12(18)	0(20) 	21(19)

O3	71(9) 	48(7)	44(6) 	(3(5)	(7(7) 	3(6)

P3	75(5) 	60(3)	53(3) 	(7(2)	(15(3) 	20(4)

C125	99(12) 	92(11)	63(13) 	(31(11)	(23(11) 	(3(11)

C126	131(13) 	116(12)	74(13) 	(40(13)	(27(12) 	(16(12)

C127	85(15) 	125(18)	66(14) 	8(16)	(22(14) 	(8(15)

C128	190(20) 	170(20)	26(12) 	(11(16)	39(15) 	(20(20)

C129	86(13) 	85(13)	75(12) 	11(11)	19(11) 	15(11)

C130	94(12) 	92(12)	56(10) 	27(9)	24(10) 	8(10)

C131	73(15) 	120(20)	71(14) 	41(14)	(1(12) 	9(15)

C132	109(18) 	82(17)	73(14) 	35(14)	18(14) 	(8(16)

C133	83(12) 	67(10)	95(11) 	(13(9)	(3(10) 	42(10)

C134	85(11) 	71(11)	99(12) 	(1(11)	0(10) 	27(11)

C135	100(20) 	120(20)	160(20) 	(30(20)	(12(19) 	29(19)

C136	66(15) 	39(11)	150(20) 	(9(14)	(1(15) 	6(10)

O103	31(7) 	46(8)	41(7) 	0(7)	(3(6) 	10(6)

P103	43(5) 	67(4)	53(5) 	(15(3)	3(4) 	12(4)

N11	94(5) 	48(4)	49(4) 	5(3)	(10(4) 	(13(4)

O11	94(4) 	55(3)	31(2) 	(2(2)	(10(3) 	(11(3)

O12	90(4) 	51(3)	34(2) 	(1(2)	(2(2) 	(19(3)

O13	119(6) 	73(4)	56(3) 	(5(3)	17(4) 	(46(4)

N21	82(5) 	55(4)	30(3) 	(7(3)	(2(3) 	(16(4)

O21	76(4) 	52(3)	39(3) 	0(2)	(6(3) 	(6(3)

O22	81(4) 	67(4)	35(3) 	1(3)	(13(3) 	(12(3)

O23	100(5) 	87(5)	45(3) 	15(3)	(5(3) 	(46(4)

N31	94(5) 	57(4)	29(3) 	(2(3)	0(3) 	(20(3)

O31	110(5) 	45(3)	29(2) 	(3(2)	(1(3) 	(9(3)

O32	102(4) 	64(3)	36(3) 	(7(3)	(20(3) 	(12(3)

O33	110(5) 	83(4)	37(3) 	(17(3)	(9(3) 	(10(4)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H1A	3987	376	173	75	1

H1B	4689	1140	197	75	1

H2	4398	383	(396	81	1

H3A	3315	1712	(154	130	1

H3B	3020	711	(182	130	1

H3C	3230	1265	(488	130	1

H4A	4655	1888	(553	130	1

H4B	5484	1420	(400	130	1

H4C	4911	2093	(201	130	1

H5A	5272	(1009	(307	67	1

H5B	5492	(1630	(21	67	1

H6	3793	(941	(135	71	1

H7A	4397	(2645	(288	112	1

H7B	4186	(1890	(533	112	1

H7C	3414	(2310	(333	112	1

H8A	3293	(1966	214	123	1

H8B	3966	(1307	375	123	1

H8C	4275	(2271	281	123	1

H9A	6378	221	(230	77	1

H9B	6370	920	44	77	1

H10	7200	(85	357	112	1

H11A	8505	337	119	216	1

H11B	7818	1095	41	216	1

H11C	8054	376	(215	216	1

H12A	6791	(1261	30	195	1

H12B	7756	(1236	173	195	1

H12C	7596	(946	(178	195	1

H13A	5371	(2502	769	83	0.405(9)

H13B	6214	(2360	559	83	0.405(9)

H14	6051	(3772	978	97	0.405(9)

H15A	5704	(4717	616	131	0.405(9)

H15B	5764	(3991	350	131	0.405(9)

H15C	5009	(3936	606	131	0.405(9)

H16A	7082	(4429	601	168	0.405(9)

H16B	7402	(3896	899	168	0.405(9)

H16C	7372	(3429	568	168	0.405(9)

H17A	7914	(2287	936	92	0.405(9)

H17B	7569	(1518	721	92	0.405(9)

H18	8620	(1502	1202	115	0.405(9)

H19A	8455	(188	763	180	0.405(9)

H19B	9137	(982	763	180	0.405(9)

H19C	9201	(235	1022	180	0.405(9)

H20A	8398	(447	1483	203	0.405(9)

H20B	7476	(939	1468	203	0.405(9)

H20C	7627	(62	1273	203	0.405(9)

H21A	6570	(3158	1375	64	0.405(9)

H21B	7026	(2353	1544	64	0.405(9)

H22	5212	(2752	1530	64	0.405(9)

H23A	6326	(2721	2051	100	0.405(9)

H23B	6096	(3574	1852	100	0.405(9)

H23C	5345	(3084	2043	100	0.405(9)

H24A	5557	(1224	1614	264	0.405(9)

H24B	5436	(1627	1953	264	0.405(9)

H24C	4688	(1755	1698	264	0.405(9)

H11D	5412	(2379	741	70	0.595(9)

H11E	6170	(2158	502	70	0.595(9)

H114	6127	(3814	823	88	0.595(9)

H11F	5622	(3499	198	126	0.595(9)

H11G	4912	(3564	469	126	0.595(9)

H11H	5505	(4393	386	126	0.595(9)

H11I	7165	(4227	487	191	0.595(9)

H11J	7442	(3232	545	191	0.595(9)

H11K	6906	(3491	240	191	0.595(9)

H11L	8021	(2461	860	105	0.595(9)

H11M	7782	(1591	678	105	0.595(9)

H118	8225	(793	995	114	0.595(9)

H11N	9616	(810	1037	102	0.595(9)

H11O	9248	(1165	713	102	0.595(9)

H11P	9627	(1836	964	102	0.595(9)

H12D	7934	(1475	1487	181	0.595(9)

H12E	8247	(509	1397	181	0.595(9)

H12F	8954	(1243	1480	181	0.595(9)

H12G	6952	(3237	1277	59	0.595(9)

H12H	7012	(2409	1500	59	0.595(9)

H122	5827	(2598	1674	76	0.595(9)

H12I	6011	(3843	1807	161	0.595(9)

H12J	6212	(4187	1465	161	0.595(9)

H12K	5222	(4101	1581	161	0.595(9)

H12L	4682	(3433	1378	153	0.595(9)

H12M	4792	(2443	1265	153	0.595(9)

H12N	4642	(2652	1624	153	0.595(9)

H25A	2070	1751	759	88	0.603(8)

H25B	2647	1364	485	88	0.603(8)

H26	1557	446	895	139	0.603(8)

H27A	2909	(323	639	223	0.603(8)

H27B	2016	(734	512	223	0.603(8)

H27C	2200	(698	877	223	0.603(8)

H28A	1457	649	251	234	0.603(8)

H28B	739	890	507	234	0.603(8)

H28C	931	(112	424	234	0.603(8)

H29A	2815	542	1360	89	0.603(8)

H29B	3633	1103	1473	89	0.603(8)

H30	2272	2151	1321	98	0.603(8)

H31A	1880	986	1805	149	0.603(8)

H31B	1410	999	1474	149	0.603(8)

H31C	1304	1812	1704	149	0.603(8)

H32A	2495	2759	1797	190	0.603(8)

H32B	3382	2677	1602	190	0.603(8)

H32C	3183	2004	1877	190	0.603(8)

H33A	3374	2794	995	108	0.603(8)

H33B	4306	2431	1092	108	0.603(8)

H34	4435	2275	519	120	0.603(8)

H35A	3793	3566	283	171	0.603(8)

H35B	3151	3571	575	171	0.603(8)

H35C	3175	2743	349	171	0.603(8)

H36A	4927	3714	823	228	0.603(8)

H36B	4973	3665	454	228	0.603(8)

H36C	5486	2962	659	228	0.603(8)

H12O	1917	1729	641	102	0.397(8)

H12P	2662	1388	414	102	0.397(8)

H126	1481	283	741	129	0.397(8)

H12Q	1952	(874	504	138	0.397(8)

H12R	2832	(384	604	138	0.397(8)

H12S	2496	(324	254	138	0.397(8)

H12T	1412	343	97	195	0.397(8)

H12U	1017	1168	277	195	0.397(8)

H12V	631	211	339	195	0.397(8)

H12W	2420	137	1189	98	0.397(8)

H12$	2985	716	1422	98	0.397(8)

H130	1480	1509	1190	97	0.397(8)

H13C	1292	179	1640	131	0.397(8)

H13D	1014	73	1285	131	0.397(8)

H13E	522	767	1501	131	0.397(8)

H13F	1469	2249	1606	132	0.397(8)

H13G	2492	2049	1576	132	0.397(8)

H13H	1901	1488	1808	132	0.397(8)

H13I	2769	2672	1043	98	0.397(8)

H13J	3574	2344	1244	98	0.397(8)

H134	4552	2686	869	102	0.397(8)

H13K	3700	3365	397	193	0.397(8)

H13L	3174	2495	484	193	0.397(8)

H13M	4194	2443	404	193	0.397(8)

H13N	3513	4110	821	127	0.397(8)

H13O	4554	4032	793	127	0.397(8)

H13P	4086	3898	1121	127	0.397(8)