|  | Single Crystal X-Ray Diffraction Service School of Chemistry - University of Southampton Contact: Dr Mark E Light, light@soton.ac.uk, ex 29429 |
| --- | --- |

Table 1. Crystal data and structure refinement details.

Identification code 	2009src0664

Empirical formula 	C17H14O

Formula weight 	234.28

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	C2/c

Unit cell dimensions	a = 13.3991(5) Å	( = 90°

b = 8.2341(3) Å	( = 96.356(2)°

c = 22.8014(8) Å	(  = 90°

Volume	2500.20(16) Å3

Z	8

Density (calculated)	1.245 Mg / m3

Absorption coefficient	0.076 mm(1

F(000)	992

Crystal	block; colourless

Crystal size	0.30 ( 0.30 ( 0.10 mm3

( range for data collection	2.99 ( 27.47°

Index ranges	(17 ( h ( 17, (10 ( k ( 10, (29 ( l ( 29

Reflections collected	17562

Independent reflections	2874 [Rint = 0.0602]

Completeness to ( = 27.47°	99.9 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9925 and 0.9776

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	2874 / 0 / 165

Goodness-of-fit on F2	1.046

Final R indices [F2 > 2((F2)]	R1 = 0.0553, wR2 = 0.1463

R indices (all data)	R1 = 0.0821, wR2 = 0.1638

Largest diff. peak and hole	0.270 and (0.284 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit ). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: Sheldrick, G. M. SADABS - Bruker Nonius area detector scaling and absorption correction - V2.10 Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	6312(1)	3436(2)	6611(1)	25(1)	1

C2	5913(1)	4631(2)	6933(1)	30(1)	1

C3	6520(1)	5838(2)	7221(1)	33(1)	1

C4	7528(1)	5845(2)	7183(1)	32(1)	1

C5	9022(1)	4677(2)	6810(1)	30(1)	1

C6	9469(1)	3510(2)	6507(1)	31(1)	1

C7	8881(1)	2258(2)	6219(1)	28(1)	1

C8	7857(1)	2191(2)	6228(1)	23(1)	1

C9	7371(1)	3397(2)	6547(1)	22(1)	1

C10	7969(1)	4651(2)	6846(1)	26(1)	1

C11	7318(1)	805(2)	5907(1)	24(1)	1

C12	7393(1)	(760(2)	6144(1)	28(1)	1

C13	6936(1)	(2067(2)	5841(1)	29(1)	1

C14	6391(1)	(1873(2)	5288(1)	27(1)	1

C15	6319(1)	(315(2)	5048(1)	29(1)	1

C16	6772(1)	998(2)	5351(1)	28(1)	1

C17	5891(1)	(3307(2)	4971(1)	36(1)	1

O1	5648(1)	2296(2)	6376(1)	35(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(O1	1.362(2)

C1(C2	1.371(2)

C1(C9	1.443(2)

C2(C3	1.400(3)

C2(H2	0.9500

C3(C4	1.364(3)

C3(H3	0.9500

C4(C10	1.415(2)

C4(H4	0.9500

C5(C6	1.361(3)

C5(C10	1.423(2)

C5(H5	0.9500

C6(C7	1.414(2)

C6(H6	0.9500

C7(C8	1.376(2)

C7(H7	0.9500

C8(C9	1.429(2)

C8(C11	1.498(2)

C9(C10	1.432(2)

C11(C12	1.396(2)

C11(C16	1.402(2)

C12(C13	1.385(2)

C12(H12	0.9500

C13(C14	1.396(2)

C13(H13	0.9500

C14(C15	1.393(2)

C14(C17	1.503(2)

C15(C16	1.386(2)

C15(H15	0.9500

C16(H16	0.9500

C17(H17A	0.9800

C17(H17B	0.9800

C17(H17C	0.9800

O1(H1	0.8400

O1(C1(C2	115.46(15)

O1(C1(C9	123.42(14)

C2(C1(C9	121.10(16)

C1(C2(C3	121.31(16)

C1(C2(H2	119.3

C3(C2(H2	119.3

C4(C3(C2	120.06(16)

C4(C3(H3	120.0

C2(C3(H3	120.0

C3(C4(C10	120.49(16)

C3(C4(H4	119.8

C10(C4(H4	119.8

C6(C5(C10	120.92(16)

C6(C5(H5	119.5

C10(C5(H5	119.5

C5(C6(C7	119.77(16)

C5(C6(H6	120.1

C7(C6(H6	120.1

C8(C7(C6	121.87(16)

C8(C7(H7	119.1

C6(C7(H7	119.1

C7(C8(C9	119.41(15)

C7(C8(C11	116.79(14)

C9(C8(C11	123.79(14)

C8(C9(C10	118.75(14)

C8(C9(C1	125.15(15)

C10(C9(C1	116.07(14)

C4(C10(C5	119.79(16)

C4(C10(C9	120.95(15)

C5(C10(C9	119.26(15)

C12(C11(C16	117.60(15)

C12(C11(C8	120.24(14)

C16(C11(C8	122.07(14)

C13(C12(C11	120.98(15)

C13(C12(H12	119.5

C11(C12(H12	119.5

C12(C13(C14	121.34(15)

C12(C13(H13	119.3

C14(C13(H13	119.3

C15(C14(C13	117.88(15)

C15(C14(C17	121.80(16)

C13(C14(C17	120.32(16)

C16(C15(C14	120.96(15)

C16(C15(H15	119.5

C14(C15(H15	119.5

C15(C16(C11	121.23(16)

C15(C16(H16	119.4

C11(C16(H16	119.4

C14(C17(H17A	109.5

C14(C17(H17B	109.5

H17A(C17(H17B	109.5

C14(C17(H17C	109.5

H17A(C17(H17C	109.5

H17B(C17(H17C	109.5

C1(O1(H1	109.5

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	29(1) 	25(1)	22(1) 	4(1)	4(1) 	0(1)

C2	34(1) 	33(1)	25(1) 	4(1)	9(1) 	7(1)

C3	46(1) 	30(1)	24(1) 	(2(1)	8(1) 	7(1)

C4	46(1) 	27(1)	23(1) 	(2(1)	2(1) 	(2(1)

C5	33(1) 	30(1)	27(1) 	4(1)	0(1) 	(9(1)

C6	23(1) 	40(1)	31(1) 	6(1)	3(1) 	(5(1)

C7	26(1) 	30(1)	30(1) 	4(1)	7(1) 	3(1)

C8	26(1) 	22(1)	22(1) 	3(1)	4(1) 	0(1)

C9	27(1) 	19(1)	19(1) 	3(1)	3(1) 	0(1)

C10	34(1) 	23(1)	19(1) 	4(1)	1(1) 	(3(1)

C11	25(1) 	23(1)	24(1) 	(1(1)	6(1) 	1(1)

C12	36(1) 	26(1)	23(1) 	2(1)	3(1) 	(1(1)

C13	37(1) 	21(1)	29(1) 	0(1)	7(1) 	0(1)

C14	25(1) 	27(1)	29(1) 	(6(1)	9(1) 	(1(1)

C15	28(1) 	34(1)	25(1) 	(1(1)	2(1) 	(1(1)

C16	31(1) 	25(1)	27(1) 	4(1)	4(1) 	3(1)

C17	36(1) 	33(1)	40(1) 	(10(1)	7(1) 	(8(1)

O1	27(1) 	36(1)	43(1) 	(9(1)	10(1) 	(4(1)

Thermal ellipsoids drawn at the 50% probability level.

# Text boxes

# Single Crystal X-Ray Diffraction Service

School of Chemistry - University of Southampton

Contact: Dr Mark E Light, light@soton.ac.uk, ex 29429