|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	2005slh0408    (CAG 137a)

Empirical formula 	C36H48Hg2O8P4S8

Formula weight 	1390.28

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/c

Unit cell dimensions	a = 15.2671(3) Å	( = 90°

b = 14.7379(2) Å	( = 95.0040(10)°

c = 10.5379(3) Å	(  = 90°

Volume	2362.04(9) Å3

Z	2

Density (calculated)	1.955 Mg / m3

Absorption coefficient	7.028 mm(1

F(000)	1352

Crystal	block; colourless

Crystal size	0.25 ( 0.15 ( 0.09 mm3

( range for data collection	3.70 ( 27.50°

Index ranges	(19 ( h ( 19, (17 ( k ( 19, (13 ( l ( 13

Reflections collected	26117

Independent reflections	5402 [Rint = 0.0347]

Completeness to ( = 27.50°	99.7 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.5704 and 0.2725

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	5402 / 0 / 267

Goodness-of-fit on F2	1.054

Final R indices [F2 > 2((F2)]	R1 = 0.0207, wR2 = 0.0437

R indices (all data)	R1 = 0.0231, wR2 = 0.0446

Extinction coefficient	0.00100(8)

Largest diff. peak and hole	0.933 and (1.337 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	8114(2)	3463(2)	5232(3)	17(1)	1

C2	7802(2)	4419(2)	5401(3)	24(1)	1

C3	6340(2)	1617(2)	4036(2)	15(1)	1

C4	6173(2)	1883(2)	2763(2)	18(1)	1

C5	5333(2)	1820(2)	2158(2)	19(1)	1

C6	4649(2)	1490(2)	2821(3)	16(1)	1

C7	4809(2)	1202(2)	4068(3)	19(1)	1

C8	5655(2)	1269(2)	4677(3)	19(1)	1

C9	3123(2)	1108(2)	2743(3)	27(1)	1

C10	10305(2)	2933(2)	6039(3)	28(1)	1

C11	10478(2)	3919(2)	5894(3)	24(1)	1

C12	12299(2)	1279(2)	7122(2)	14(1)	1

C13	12975(2)	793(2)	6639(3)	16(1)	1

C14	13793(2)	729(2)	7330(3)	17(1)	1

C15	13929(2)	1154(2)	8504(2)	17(1)	1

C16	13243(2)	1622(2)	9013(3)	19(1)	1

C17	12436(2)	1681(2)	8325(3)	18(1)	1

C18	15454(2)	752(2)	8754(3)	26(1)	1

O1	7349(1)	2913(1)	4836(2)	15(1)	1

O2	3852(1)	1475(1)	2137(2)	22(1)	1

O3	11143(1)	2487(1)	6375(2)	18(1)	1

O4	14704(1)	1169(1)	9240(2)	23(1)	1

P1	7405(1)	1832(1)	4827(1)	13(1)	1

P2	11249(1)	1419(1)	6253(1)	13(1)	1

S1	8381(1)	1442(1)	3742(1)	17(1)	1

S2	7579(1)	1300(1)	6563(1)	17(1)	1

S3	8789(1)	(1100(1)	5590(1)	16(1)	1

S4	10350(1)	763(1)	7231(1)	17(1)	1

Hg1	9099(1)	647(1)	5613(1)	17(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(O1	1.453(3)

C1(C2	1.502(4)

C1(H1A	0.9900

C1(H1B	0.9900

C2(H2A	0.9800

C2(H2B	0.9800

C2(H2C	0.9800

C3(C8	1.392(4)

C3(C4	1.400(4)

C3(P1	1.789(2)

C4(C5	1.384(3)

C4(H4	0.9500

C5(C6	1.395(4)

C5(H5	0.9500

C6(O2	1.358(3)

C6(C7	1.382(4)

C7(C8	1.395(4)

C7(H7	0.9500

C8(H8	0.9500

C9(O2	1.436(3)

C9(H9A	0.9800

C9(H9B	0.9800

C9(H9C	0.9800

C10(O3	1.454(3)

C10(C11	1.487(4)

C10(H10A	0.9900

C10(H10B	0.9900

C11(H11A	0.9800

C11(H11B	0.9800

C11(H11C	0.9800

C12(C13	1.389(4)

C12(C17	1.399(4)

C12(P2	1.787(2)

C13(C14	1.393(4)

C13(H13	0.9500

C14(C15	1.386(4)

C14(H14	0.9500

C15(O4	1.357(3)

C15(C16	1.400(4)

C16(C17	1.376(4)

C16(H16	0.9500

C17(H17	0.9500

C18(O4	1.433(3)

C18(H18A	0.9800

C18(H18B	0.9800

C18(H18C	0.9800

O1(P1	1.5954(18)

O3(P2	1.5883(18)

P1(S2	1.9866(9)

P1(S1	2.0388(9)

P2(S3i	1.9940(9)

P2(S4	2.0314(9)

S1(Hg1	2.4669(6)

S2(Hg1	2.7777(6)

S3(P2i	1.9940(9)

S3(Hg1	2.6174(6)

S4(Hg1	2.4524(6)

O1(C1(C2	107.6(2)

O1(C1(H1A	110.2

C2(C1(H1A	110.2

O1(C1(H1B	110.2

C2(C1(H1B	110.2

H1A(C1(H1B	108.5

C1(C2(H2A	109.5

C1(C2(H2B	109.5

H2A(C2(H2B	109.5

C1(C2(H2C	109.5

H2A(C2(H2C	109.5

H2B(C2(H2C	109.5

C8(C3(C4	119.1(2)

C8(C3(P1	122.0(2)

C4(C3(P1	118.63(19)

C5(C4(C3	120.4(2)

C5(C4(H4	119.8

C3(C4(H4	119.8

C4(C5(C6	119.8(2)

C4(C5(H5	120.1

C6(C5(H5	120.1

O2(C6(C7	125.1(2)

O2(C6(C5	114.5(2)

C7(C6(C5	120.3(2)

C6(C7(C8	119.8(2)

C6(C7(H7	120.1

C8(C7(H7	120.1

C3(C8(C7	120.5(2)

C3(C8(H8	119.8

C7(C8(H8	119.8

O2(C9(H9A	109.5

O2(C9(H9B	109.5

H9A(C9(H9B	109.5

O2(C9(H9C	109.5

H9A(C9(H9C	109.5

H9B(C9(H9C	109.5

O3(C10(C11	107.9(2)

O3(C10(H10A	110.1

C11(C10(H10A	110.1

O3(C10(H10B	110.1

C11(C10(H10B	110.1

H10A(C10(H10B	108.4

C10(C11(H11A	109.5

C10(C11(H11B	109.5

H11A(C11(H11B	109.5

C10(C11(H11C	109.5

H11A(C11(H11C	109.5

H11B(C11(H11C	109.5

C13(C12(C17	119.6(2)

C13(C12(P2	122.25(19)

C17(C12(P2	118.18(19)

C12(C13(C14	120.2(2)

C12(C13(H13	119.9

C14(C13(H13	119.9

C15(C14(C13	119.7(2)

C15(C14(H14	120.2

C13(C14(H14	120.2

O4(C15(C14	124.9(2)

O4(C15(C16	114.7(2)

C14(C15(C16	120.4(2)

C17(C16(C15	119.6(2)

C17(C16(H16	120.2

C15(C16(H16	120.2

C16(C17(C12	120.5(2)

C16(C17(H17	119.8

C12(C17(H17	119.8

O4(C18(H18A	109.5

O4(C18(H18B	109.5

H18A(C18(H18B	109.5

O4(C18(H18C	109.5

H18A(C18(H18C	109.5

H18B(C18(H18C	109.5

C1(O1(P1	121.14(15)

C6(O2(C9	117.6(2)

C10(O3(P2	121.48(16)

C15(O4(C18	118.2(2)

O1(P1(C3	97.63(10)

O1(P1(S2	113.06(7)

C3(P1(S2	113.74(9)

O1(P1(S1	109.07(7)

C3(P1(S1	111.55(9)

S2(P1(S1	111.07(4)

O3(P2(C12	99.55(10)

O3(P2(S3i	108.55(8)

C12(P2(S3i	114.87(9)

O3(P2(S4	110.62(8)

C12(P2(S4	107.49(9)

S3i(P2(S4	114.71(4)

P1(S1(Hg1	88.91(3)

P1(S2(Hg1	81.60(3)

P2i(S3(Hg1	103.36(3)

P2(S4(Hg1	101.56(3)

S4(Hg1(S1	141.95(2)

S4(Hg1(S3	101.77(2)

S1(Hg1(S3	113.10(2)

S4(Hg1(S2	110.48(2)

S1(Hg1(S2	78.271(19)

S3(Hg1(S2	100.83(2)

Symmetry transformations used to generate equivalent atoms:

(i) (x+2,(y,(z+1

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	14(1) 	18(1)	20(1) 	0(1)	(2(1) 	(3(1)

C2	20(1) 	17(1)	34(2) 	(3(1)	(4(1) 	(3(1)

C3	14(1) 	13(1)	17(1) 	(2(1)	(2(1) 	(1(1)

C4	14(1) 	23(1)	16(1) 	1(1)	1(1) 	(6(1)

C5	18(1) 	24(1)	14(1) 	3(1)	(2(1) 	(4(1)

C6	14(1) 	15(1)	21(1) 	(4(1)	(2(1) 	(1(1)

C7	16(1) 	23(1)	19(1) 	1(1)	3(1) 	(4(1)

C8	17(1) 	22(1)	16(1) 	4(1)	2(1) 	(2(1)

C9	14(1) 	27(2)	38(2) 	3(1)	(1(1) 	(7(1)

C10	16(1) 	18(1)	48(2) 	3(1)	(7(1) 	5(1)

C11	30(2) 	16(1)	24(2) 	0(1)	(6(1) 	6(1)

C12	12(1) 	13(1)	16(1) 	2(1)	(4(1) 	(1(1)

C13	15(1) 	19(1)	15(1) 	(2(1)	(1(1) 	(1(1)

C14	13(1) 	21(1)	18(1) 	(2(1)	0(1) 	3(1)

C15	12(1) 	18(1)	19(1) 	3(1)	(5(1) 	(2(1)

C16	19(1) 	18(1)	18(1) 	(5(1)	(3(1) 	0(1)

C17	16(1) 	16(1)	21(1) 	(1(1)	0(1) 	2(1)

C18	14(1) 	31(2)	33(2) 	(6(1)	(6(1) 	4(1)

O1	12(1) 	13(1)	19(1) 	(2(1)	(4(1) 	(1(1)

O2	13(1) 	31(1)	23(1) 	1(1)	(3(1) 	(6(1)

O3	12(1) 	13(1)	29(1) 	(2(1)	(5(1) 	1(1)

O4	13(1) 	30(1)	24(1) 	(6(1)	(7(1) 	4(1)

P1	12(1) 	13(1)	13(1) 	(1(1)	(2(1) 	1(1)

P2	10(1) 	12(1)	16(1) 	0(1)	(3(1) 	0(1)

S1	16(1) 	22(1)	13(1) 	1(1)	2(1) 	5(1)

S2	17(1) 	20(1)	13(1) 	2(1)	2(1) 	5(1)

S3	18(1) 	17(1)	14(1) 	1(1)	(2(1) 	(2(1)

S4	13(1) 	23(1)	15(1) 	3(1)	(2(1) 	(4(1)

Hg1	13(1) 	19(1)	19(1) 	0(1)	(3(1) 	2(1)