|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	2006src1540 / MAB/SD03

Empirical formula 	C19H18BNO

Formula weight 	287.15

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/c

Unit cell dimensions	a = 14.2194(3) Å	( = 90°

b = 10.2937(2) Å	( = 95.2720(10)°

c = 20.6731(5) Å	(  = 90°

Volume	3013.13(11) Å3

Z	8

Density (calculated)	1.266 Mg / m3

Absorption coefficient	0.077 mm(1

F(000)	1216

Crystal	Blade; Colourless

Crystal size	0.38 ( 0.15 ( 0.08 mm3

( range for data collection	3.34 ( 27.48°

Index ranges	(18 ( h ( 18, (13 ( k ( 13, (26 ( l ( 26

Reflections collected	30176

Independent reflections	6886 [Rint = 0.0437]

Completeness to ( = 27.48°	99.7 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9939 and 0.9715

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	6886 / 0 / 398

Goodness-of-fit on F2	1.097

Final R indices [F2 > 2((F2)]	R1 = 0.0518, wR2 = 0.1016

R indices (all data)	R1 = 0.0678, wR2 = 0.1113

Extinction coefficient	0.0023(5)

Largest diff. peak and hole	0.359 and (0.208 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SADABS Version 2.10. (G. M. Sheldrick (2003)) Bruker AXS Inc., Madison, Wisconsin, USA. Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP3 for Windows (L. J. Farrugia, J. Appl. Crystallogr. 1997, 30, 565).

Special details:

All hydrogen atoms were fixed using a standard riding model

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	4925(1)	6300(2)	1425(1)	25(1)	1

C2	5986(1)	6162(2)	1422(1)	30(1)	1

C3	6356(1)	4960(2)	1765(1)	23(1)	1

C4	7290(1)	4866(2)	2031(1)	31(1)	1

C5	7616(1)	3747(2)	2341(1)	31(1)	1

C6	7002(1)	2714(2)	2381(1)	26(1)	1

C7	6086(1)	2852(2)	2113(1)	22(1)	1

C8	4069(1)	4124(2)	2226(1)	20(1)	1

C9	3086(1)	3934(2)	2178(1)	24(1)	1

C10	2562(1)	4052(2)	2710(1)	27(1)	1

C11	2997(1)	4412(2)	3311(1)	26(1)	1

C12	3962(1)	4631(2)	3375(1)	23(1)	1

C13	4486(1)	4463(2)	2841(1)	21(1)	1

C14	4351(1)	2755(2)	1128(1)	19(1)	1

C15	3929(1)	1635(2)	1351(1)	21(1)	1

C16	3733(1)	558(2)	955(1)	24(1)	1

C17	3950(1)	577(2)	316(1)	26(1)	1

C18	4367(1)	1674(2)	79(1)	27(1)	1

C19	4566(1)	2743(2)	479(1)	23(1)	1

B1	4612(1)	4030(2)	1567(1)	19(1)	1

N1	5762(1)	3948(1)	1814(1)	19(1)	1

O1	4478(1)	5171(1)	1157(1)	22(1)	1

C21	(904(1)	391(2)	3690(1)	26(1)	1

C22	120(1)	(10(2)	3816(1)	29(1)	1

C23	701(1)	921(2)	4248(1)	23(1)	1

C24	1575(1)	536(2)	4541(1)	28(1)	1

C25	2131(1)	1399(2)	4911(1)	31(1)	1

C26	1813(1)	2657(2)	4978(1)	30(1)	1

C27	939(1)	2993(2)	4683(1)	26(1)	1

C28	(1393(1)	2590(2)	4596(1)	22(1)	1

C29	(1168(1)	3026(2)	5233(1)	24(1)	1

C30	(1831(1)	3051(2)	5690(1)	27(1)	1

C31	(2744(1)	2624(2)	5522(1)	28(1)	1

C32	(2992(1)	2182(2)	4896(1)	27(1)	1

C33	(2328(1)	2178(2)	4443(1)	26(1)	1

C34	(572(1)	4046(2)	3707(1)	22(1)	1

C35	(1190(1)	5061(2)	3805(1)	27(1)	1

C36	(1138(1)	6256(2)	3497(1)	32(1)	1

C37	(445(1)	6473(2)	3082(1)	31(1)	1

C38	191(1)	5493(2)	2977(1)	30(1)	1

C39	122(1)	4302(2)	3282(1)	28(1)	1

B21	(686(1)	2617(2)	4017(1)	22(1)	1

N21	382(1)	2143(1)	4328(1)	21(1)	1

O21	(963(1)	1708(1)	3494(1)	23(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(O1	1.4133(19)

C1(C2	1.516(2)

C1(H1A	0.9900

C1(H1B	0.9900

C2(C3	1.498(2)

C2(H2A	0.9900

C2(H2B	0.9900

C3(N1	1.350(2)

C3(C4	1.393(2)

C4(C5	1.378(3)

C4(H4	0.9500

C5(C6	1.382(3)

C5(H5	0.9500

C6(C7	1.376(2)

C6(H6	0.9500

C7(N1	1.347(2)

C7(H7	0.9500

C8(C13	1.396(2)

C8(C9	1.406(2)

C8(B1	1.630(2)

C9(C10	1.390(2)

C9(H9	0.9500

C10(C11	1.386(2)

C10(H10	0.9500

C11(C12	1.385(2)

C11(H11	0.9500

C12(C13	1.398(2)

C12(H12	0.9500

C13(H13	0.9500

C14(C15	1.399(2)

C14(C19	1.403(2)

C14(B1	1.619(2)

C15(C16	1.392(2)

C15(H15	0.9500

C16(C17	1.383(2)

C16(H16	0.9500

C17(C18	1.386(3)

C17(H17	0.9500

C18(C19	1.388(2)

C18(H18	0.9500

C19(H19	0.9500

B1(O1	1.450(2)

B1(N1	1.670(2)

C21(O21	1.416(2)

C21(C22	1.512(2)

C21(H21A	0.9900

C21(H21B	0.9900

C22(C23	1.504(2)

C22(H22A	0.9900

C22(H22B	0.9900

C23(N21	1.353(2)

C23(C24	1.390(2)

C24(C25	1.374(3)

C24(H24	0.9500

C25(C26	1.383(3)

C25(H25	0.9500

C26(C27	1.376(2)

C26(H26	0.9500

C27(N21	1.350(2)

C27(H27	0.9500

C28(C29	1.401(2)

C28(C33	1.404(2)

C28(B21	1.632(2)

C29(C30	1.394(2)

C29(H29	0.9500

C30(C31	1.385(2)

C30(H30	0.9500

C31(C32	1.386(2)

C31(H31	0.9500

C32(C33	1.390(2)

C32(H32	0.9500

C33(H33	0.9500

C34(C35	1.392(2)

C34(C39	1.404(2)

C34(B21	1.619(3)

C35(C36	1.391(3)

C35(H35	0.9500

C36(C37	1.383(3)

C36(H36	0.9500

C37(C38	1.385(3)

C37(H37	0.9500

C38(C39	1.387(3)

C38(H38	0.9500

C39(H39	0.9500

B21(O21	1.455(2)

B21(N21	1.667(2)

O1(C1(C2	109.48(13)

O1(C1(H1A	109.8

C2(C1(H1A	109.8

O1(C1(H1B	109.8

C2(C1(H1B	109.8

H1A(C1(H1B	108.2

C3(C2(C1	112.41(14)

C3(C2(H2A	109.1

C1(C2(H2A	109.1

C3(C2(H2B	109.1

C1(C2(H2B	109.1

H2A(C2(H2B	107.9

N1(C3(C4	119.79(16)

N1(C3(C2	118.60(14)

C4(C3(C2	121.61(16)

C5(C4(C3	120.65(17)

C5(C4(H4	119.7

C3(C4(H4	119.7

C4(C5(C6	118.87(16)

C4(C5(H5	120.6

C6(C5(H5	120.6

C7(C6(C5	118.48(16)

C7(C6(H6	120.8

C5(C6(H6	120.8

N1(C7(C6	122.82(16)

N1(C7(H7	118.6

C6(C7(H7	118.6

C13(C8(C9	115.79(14)

C13(C8(B1	125.62(14)

C9(C8(B1	118.46(14)

C10(C9(C8	122.27(16)

C10(C9(H9	118.9

C8(C9(H9	118.9

C11(C10(C9	120.34(16)

C11(C10(H10	119.8

C9(C10(H10	119.8

C12(C11(C10	119.04(15)

C12(C11(H11	120.5

C10(C11(H11	120.5

C11(C12(C13	119.99(15)

C11(C12(H12	120.0

C13(C12(H12	120.0

C8(C13(C12	122.51(15)

C8(C13(H13	118.7

C12(C13(H13	118.7

C15(C14(C19	116.49(15)

C15(C14(B1	124.48(14)

C19(C14(B1	119.03(14)

C16(C15(C14	122.07(15)

C16(C15(H15	119.0

C14(C15(H15	119.0

C17(C16(C15	120.03(16)

C17(C16(H16	120.0

C15(C16(H16	120.0

C16(C17(C18	119.31(16)

C16(C17(H17	120.3

C18(C17(H17	120.3

C17(C18(C19	120.37(16)

C17(C18(H18	119.8

C19(C18(H18	119.8

C18(C19(C14	121.73(16)

C18(C19(H19	119.1

C14(C19(H19	119.1

O1(B1(C14	108.54(13)

O1(B1(C8	113.18(13)

C14(B1(C8	114.56(13)

O1(B1(N1	106.97(12)

C14(B1(N1	107.30(12)

C8(B1(N1	105.83(12)

C7(N1(C3	119.38(14)

C7(N1(B1	117.81(13)

C3(N1(B1	122.64(13)

C1(O1(B1	114.06(12)

O21(C21(C22	110.01(14)

O21(C21(H21A	109.7

C22(C21(H21A	109.7

O21(C21(H21B	109.7

C22(C21(H21B	109.7

H21A(C21(H21B	108.2

C23(C22(C21	113.28(14)

C23(C22(H22A	108.9

C21(C22(H22A	108.9

C23(C22(H22B	108.9

C21(C22(H22B	108.9

H22A(C22(H22B	107.7

N21(C23(C24	120.47(15)

N21(C23(C22	119.63(14)

C24(C23(C22	119.85(16)

C25(C24(C23	120.34(17)

C25(C24(H24	119.8

C23(C24(H24	119.8

C24(C25(C26	118.89(16)

C24(C25(H25	120.6

C26(C25(H25	120.6

C27(C26(C25	118.80(16)

C27(C26(H26	120.6

C25(C26(H26	120.6

N21(C27(C26	122.58(17)

N21(C27(H27	118.7

C26(C27(H27	118.7

C29(C28(C33	115.98(15)

C29(C28(B21	125.60(14)

C33(C28(B21	118.29(14)

C30(C29(C28	122.22(16)

C30(C29(H29	118.9

C28(C29(H29	118.9

C31(C30(C29	120.07(16)

C31(C30(H30	120.0

C29(C30(H30	120.0

C30(C31(C32	119.34(15)

C30(C31(H31	120.3

C32(C31(H31	120.3

C31(C32(C33	120.05(16)

C31(C32(H32	120.0

C33(C32(H32	120.0

C32(C33(C28	122.33(16)

C32(C33(H33	118.8

C28(C33(H33	118.8

C35(C34(C39	116.12(16)

C35(C34(B21	122.44(14)

C39(C34(B21	121.29(15)

C36(C35(C34	122.38(16)

C36(C35(H35	118.8

C34(C35(H35	118.8

C37(C36(C35	119.88(17)

C37(C36(H36	120.1

C35(C36(H36	120.1

C36(C37(C38	119.46(17)

C36(C37(H37	120.3

C38(C37(H37	120.3

C37(C38(C39	119.94(16)

C37(C38(H38	120.0

C39(C38(H38	120.0

C38(C39(C34	122.20(16)

C38(C39(H39	118.9

C34(C39(H39	118.9

O21(B21(C34	108.64(13)

O21(B21(C28	112.99(14)

C34(B21(C28	113.35(14)

O21(B21(N21	105.91(13)

C34(B21(N21	107.33(13)

C28(B21(N21	108.21(13)

C27(N21(C23	118.88(14)

C27(N21(B21	119.27(14)

C23(N21(B21	121.83(13)

C21(O21(B21	113.46(13)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	32(1) 	16(1)	27(1) 	1(1)	3(1) 	1(1)

C2	31(1) 	22(1)	37(1) 	3(1)	5(1) 	(5(1)

C3	25(1) 	22(1)	23(1) 	(4(1)	5(1) 	(2(1)

C4	25(1) 	33(1)	34(1) 	(5(1)	2(1) 	(6(1)

C5	21(1) 	42(1)	30(1) 	(6(1)	(3(1) 	2(1)

C6	29(1) 	27(1)	23(1) 	(1(1)	0(1) 	6(1)

C7	25(1) 	21(1)	20(1) 	(1(1)	3(1) 	1(1)

C8	23(1) 	15(1)	23(1) 	0(1)	4(1) 	2(1)

C9	22(1) 	28(1)	24(1) 	(1(1)	2(1) 	3(1)

C10	21(1) 	29(1)	33(1) 	1(1)	7(1) 	3(1)

C11	32(1) 	22(1)	24(1) 	3(1)	12(1) 	7(1)

C12	32(1) 	19(1)	20(1) 	1(1)	4(1) 	2(1)

C13	23(1) 	17(1)	22(1) 	1(1)	3(1) 	(1(1)

C14	15(1) 	21(1)	22(1) 	(1(1)	1(1) 	3(1)

C15	19(1) 	23(1)	21(1) 	0(1)	2(1) 	2(1)

C16	19(1) 	20(1)	31(1) 	1(1)	(2(1) 	1(1)

C17	24(1) 	23(1)	30(1) 	(8(1)	(2(1) 	4(1)

C18	29(1) 	30(1)	23(1) 	(5(1)	3(1) 	3(1)

C19	23(1) 	23(1)	23(1) 	(1(1)	4(1) 	1(1)

B1	18(1) 	19(1)	20(1) 	(1(1)	1(1) 	0(1)

N1	21(1) 	19(1)	17(1) 	(2(1)	4(1) 	1(1)

O1	26(1) 	19(1)	21(1) 	1(1)	1(1) 	1(1)

C21	26(1) 	26(1)	26(1) 	(5(1)	3(1) 	(6(1)

C22	31(1) 	24(1)	31(1) 	(5(1)	1(1) 	0(1)

C23	21(1) 	26(1)	22(1) 	(1(1)	4(1) 	(1(1)

C24	24(1) 	29(1)	30(1) 	1(1)	4(1) 	4(1)

C25	20(1) 	44(1)	28(1) 	0(1)	1(1) 	2(1)

C26	22(1) 	39(1)	30(1) 	(8(1)	1(1) 	(6(1)

C27	24(1) 	29(1)	26(1) 	(5(1)	4(1) 	(2(1)

C28	22(1) 	23(1)	22(1) 	1(1)	3(1) 	3(1)

C29	23(1) 	24(1)	25(1) 	0(1)	2(1) 	0(1)

C30	33(1) 	27(1)	21(1) 	(1(1)	5(1) 	4(1)

C31	28(1) 	30(1)	26(1) 	4(1)	11(1) 	9(1)

C32	20(1) 	35(1)	28(1) 	5(1)	4(1) 	4(1)

C33	23(1) 	32(1)	22(1) 	1(1)	2(1) 	2(1)

C34	19(1) 	28(1)	20(1) 	(3(1)	2(1) 	0(1)

C35	24(1) 	32(1)	25(1) 	0(1)	6(1) 	4(1)

C36	35(1) 	29(1)	33(1) 	2(1)	5(1) 	10(1)

C37	38(1) 	28(1)	27(1) 	4(1)	1(1) 	1(1)

C38	31(1) 	35(1)	25(1) 	1(1)	9(1) 	0(1)

C39	28(1) 	28(1)	28(1) 	(2(1)	9(1) 	4(1)

B21	17(1) 	25(1)	22(1) 	(2(1)	1(1) 	2(1)

N21	18(1) 	24(1)	21(1) 	(2(1)	3(1) 	(1(1)

O21	21(1) 	26(1)	22(1) 	(2(1)	2(1) 	(1(1)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H1A	4760	6426	1875	30	1

H1B	4705	7070	1166	30	1

H2A	6150	6139	967	36	1

H2B	6297	6931	1635	36	1

H4	7705	5580	1998	37	1

H5	8252	3686	2524	38	1

H6	7209	1928	2588	32	1

H7	5663	2143	2140	26	1

H9	2769	3717	1768	29	1

H10	1902	3886	2662	33	1

H11	2638	4506	3674	31	1

H12	4268	4895	3781	28	1

H13	5150	4585	2899	25	1

H15	3771	1608	1788	26	1

H16	3449	(191	1122	28	1

H17	3816	(154	43	31	1

H18	4518	1696	(359	32	1

H19	4854	3485	308	27	1

H21A	(1223	(165	3346	31	1

H21B	(1227	272	4090	31	1

H22A	150	(881	4020	34	1

H22B	398	(78	3396	34	1

H24	1789	(327	4486	33	1

H25	2725	1135	5119	37	1

H26	2190	3279	5222	37	1

H27	719	3855	4732	31	1

H29	(543	3314	5359	29	1

H30	(1655	3362	6117	32	1

H31	(3197	2634	5833	33	1

H32	(3615	1883	4777	33	1

H33	(2513	1885	4014	31	1

H35	(1665	4932	4094	32	1

H36	(1578	6922	3571	39	1

H37	(404	7289	2871	37	1

H38	673	5636	2697	36	1

H39	559	3636	3202	33	1