|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	2007src0193  (306-310-3B)

Empirical formula 	C24H16Cl16F32N12O8P12

Formula weight 	2147.33

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	C2/m

Unit cell dimensions	a = 20.9041(7) Å	( = 90°

b = 14.5008(5) Å	( = 102.021(2)°

c = 5.9078(2) Å	(  = 90°

Volume	1751.54(10) Å3

Z	1

Density (calculated)	2.036 Mg / m3

Absorption coefficient	1.039 mm(1

F(000)	1048

Crystal	rod; colourless

Crystal size	0.45 ( 0.10 ( 0.10 mm3

( range for data collection	3.30 ( 27.49°

Index ranges	(27 ( h ( 27, (18 ( k ( 18, (7 ( l ( 7

Reflections collected	9086

Independent reflections	2099 [Rint = 0.0447]

Completeness to ( = 27.49°	99.7 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9032 and 0.6521

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	2099 / 0 / 124

Goodness-of-fit on F2	1.156

Final R indices [F2 > 2((F2)]	R1 = 0.0840, wR2 = 0.2468

R indices (all data)	R1 = 0.0870, wR2 = 0.2484

Largest diff. peak and hole	1.745 and (0.841 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SADABS Version 2.10. (G. M. Sheldrick (2003)) Bruker AXS Inc., Madison, Wisconsin, USA. Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: PLATON  (A.L. Spek, J. Appl. Crystallogr. 2003, 36, 7).

Special details:

P1-P2 = 2.747, P2 - P2 = 2.733, Max deviation from mean plane = 0.141 (N2).

P2 = R, P2a = R, P2b = S, P2c = S.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	1334(3)	1862(5)	(1100(14)	24(2)	1

C2	952(4)	1773(5)	(3575(13)	22(1)	1

C3	214(3)	1886(5)	(3751(12)	22(2)	1

N1	3121(3)	939(4)	(70(11)	21(1)	1

N2	2022(4)	0	244(16)	20(2)	1

O1	2009(2)	1690(4)	(1157(9)	22(1)	1

F1	1069(2)	947(3)	(4445(9)	34(1)	1

F2	1145(2)	2421(4)	(4951(9)	35(1)	1

F3	17(2)	1193(4)	(2546(9)	36(1)	1

F4	109(2)	2679(4)	(2719(10)	42(1)	1

P1	3482(1)	0	(310(4)	18(1)	1

P2	2408(1)	942(1)	472(3)	17(1)	1

Cl1	3783(1)	0	(3303(4)	29(1)	1

Cl2	4349(1)	0	1903(4)	26(1)	1

Cl3	2448(1)	1455(1)	3635(3)	25(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(O1	1.439(8)

C1(C2	1.519(10)

C2(F1	1.345(9)

C2(F2	1.358(9)

C2(C3	1.534(10)

C3(F4	1.340(9)

C3(F3	1.345(9)

C3(C3i	1.558(14)

N1(P1	1.577(6)

N1(P2	1.587(6)

N2(P2	1.578(4)

N2(P2ii	1.578(4)

O1(P2	1.570(5)

P1(N1ii	1.577(6)

P1(Cl1	1.997(4)

P1(Cl2	2.002(3)

P2(Cl3	1.996(2)

O1(C1(C2	106.5(6)

F1(C2(F2	106.6(6)

F1(C2(C1	110.0(6)

F2(C2(C1	110.8(6)

F1(C2(C3	109.3(6)

F2(C2(C3	107.8(6)

C1(C2(C3	112.1(6)

F4(C3(F3	107.7(6)

F4(C3(C2	108.6(6)

F3(C3(C2	107.3(6)

F4(C3(C3i	108.4(5)

F3(C3(C3i	108.8(5)

C2(C3(C3i	115.8(8)

P1(N1(P2	120.5(4)

P2(N2(P2ii	120.0(5)

C1(O1(P2	120.3(5)

N1ii(P1(N1	119.4(4)

N1ii(P1(Cl1	109.0(2)

N1(P1(Cl1	109.0(2)

N1ii(P1(Cl2	109.0(2)

N1(P1(Cl2	109.0(2)

Cl1(P1(Cl2	99.69(15)

O1(P2(N2	110.4(4)

O1(P2(N1	106.3(3)

N2(P2(N1	117.7(4)

O1(P2(Cl3	103.3(2)

N2(P2(Cl3	108.8(3)

N1(P2(Cl3	109.4(3)

Symmetry transformations used to generate equivalent atoms:

(i) (x,y,(z(1    (ii) x,(y,z

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	15(3) 	22(3)	31(4) 	(1(3)	(2(3) 	4(3)

C2	19(3) 	21(3)	28(4) 	3(3)	7(3) 	1(3)

C3	18(3) 	25(4)	24(4) 	(3(3)	3(3) 	(3(3)

N1	15(3) 	21(3)	28(3) 	1(2)	7(2) 	(2(2)

N2	12(4) 	21(4)	27(4) 	0	7(3) 	0

O1	14(2) 	23(3)	27(3) 	5(2)	1(2) 	0(2)

F1	26(2) 	33(3)	38(3) 	(14(2)	(4(2) 	8(2)

F2	21(2) 	48(3)	34(3) 	19(2)	2(2) 	(4(2)

F3	22(2) 	53(3)	30(3) 	16(2)	(3(2) 	(11(2)

F4	26(2) 	43(3)	50(3) 	(23(3)	(6(2) 	12(2)

P1	13(1) 	23(1)	17(1) 	0	4(1) 	0

P2	14(1) 	18(1)	19(1) 	0(1)	3(1) 	0(1)

Cl1	24(1) 	44(2)	19(1) 	0	8(1) 	0

Cl2	14(1) 	41(2)	21(1) 	0	1(1) 	0

Cl3	26(1) 	26(1)	22(1) 	(4(1)	6(1) 	0(1)