|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	2007src0325  (DbSN11)

Empirical formula 	C13H12N2O4

Formula weight 	260.25

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/n

Unit cell dimensions	a = 11.0751(2) Å	( = 90°

b = 4.94410(10) Å	( = 97.5560(10)°

c = 22.8470(5) Å	(  = 90°

Volume	1240.16(4) Å3

Z	4

Density (calculated)	1.394 Mg / m3

Absorption coefficient	0.105 mm(1

F(000)	544

Crystal	blade; colourless

Crystal size	0.45 ( 0.03 ( 0.01 mm3

( range for data collection	3.07 ( 27.50°

Index ranges	(14 ( h ( 14, (5 ( k ( 6, (27 ( l ( 29

Reflections collected	18385

Independent reflections	2853 [Rint = 0.0560]

Completeness to ( = 27.50°	99.6 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9989 and 0.9542

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	2853 / 0 / 182

Goodness-of-fit on F2	1.030

Final R indices [F2 > 2((F2)]	R1 = 0.0461, wR2 = 0.1109

R indices (all data)	R1 = 0.0652, wR2 = 0.1226

Largest diff. peak and hole	0.277 and (0.338 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SADABS Version 2.10. (G. M. Sheldrick (2003)) Bruker AXS Inc., Madison, Wisconsin, USA. Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: PLATON  (A.L. Spek, J. Appl. Crystallogr. 2003, 36, 7).

Special details:

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	10083(1)	10462(3)	2829(1)	20(1)	1

C2	9775(1)	12578(3)	3244(1)	20(1)	1

C3	10621(1)	13245(3)	3738(1)	23(1)	1

C4	10336(2)	15208(4)	4135(1)	29(1)	1

C5	9226(2)	16515(4)	4039(1)	33(1)	1

C6	8381(2)	15891(4)	3549(1)	31(1)	1

C7	8659(1)	13929(3)	3157(1)	25(1)	1

O1	9247(1)	9936(2)	2387(1)	23(1)	1

O2	11087(1)	9304(2)	2899(1)	26(1)	1

O3	11729(1)	12023(3)	3839(1)	30(1)	1

C8	8625(1)	2510(3)	324(1)	21(1)	1

C9	9455(1)	3305(3)	870(1)	20(1)	1

C10	9189(1)	5446(3)	1225(1)	21(1)	1

C11	10932(1)	4703(3)	1877(1)	23(1)	1

C12	11263(1)	2530(3)	1548(1)	25(1)	1

C13	10506(1)	1810(3)	1039(1)	22(1)	1

N1	9909(1)	6117(3)	1725(1)	22(1)	1

N2	8026(1)	4487(3)	13(1)	27(1)	1

O4	8517(1)	98(2)	184(1)	27(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(O2	1.2424(18)

C1(O1	1.3037(17)

C1(C2	1.480(2)

C2(C7	1.397(2)

C2(C3	1.408(2)

C3(O3	1.3597(19)

C3(C4	1.394(2)

C4(C5	1.380(2)

C5(C6	1.395(3)

C6(C7	1.383(2)

C8(O4	1.2362(19)

C8(N2	1.333(2)

C8(C9	1.501(2)

C9(C10	1.389(2)

C9(C13	1.390(2)

C10(N1	1.3465(19)

C11(N1	1.338(2)

C11(C12	1.388(2)

C12(C13	1.387(2)

O2(C1(O1	122.71(14)

O2(C1(C2	121.38(13)

O1(C1(C2	115.91(13)

C7(C2(C3	118.98(14)

C7(C2(C1	121.44(13)

C3(C2(C1	119.58(13)

O3(C3(C4	118.31(14)

O3(C3(C2	121.55(14)

C4(C3(C2	120.15(14)

C5(C4(C3	119.68(15)

C4(C5(C6	120.92(15)

C7(C6(C5	119.45(16)

C6(C7(C2	120.82(15)

O4(C8(N2	123.03(14)

O4(C8(C9	119.66(14)

N2(C8(C9	117.31(13)

C10(C9(C13	118.52(14)

C10(C9(C8	122.03(14)

C13(C9(C8	119.41(14)

N1(C10(C9	122.38(14)

N1(C11(C12	122.61(14)

C13(C12(C11	118.60(15)

C12(C13(C9	119.26(15)

C11(N1(C10	118.60(13)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	20(1) 	21(1)	18(1) 	1(1)	2(1) 	(1(1)

C2	22(1) 	19(1)	18(1) 	0(1)	3(1) 	(1(1)

C3	25(1) 	23(1)	20(1) 	1(1)	1(1) 	2(1)

C4	36(1) 	29(1)	22(1) 	(5(1)	2(1) 	0(1)

C5	40(1) 	30(1)	30(1) 	(7(1)	13(1) 	3(1)

C6	27(1) 	31(1)	36(1) 	(3(1)	10(1) 	6(1)

C7	22(1) 	26(1)	27(1) 	0(1)	3(1) 	1(1)

O1	21(1) 	26(1)	21(1) 	(7(1)	0(1) 	0(1)

O2	22(1) 	30(1)	24(1) 	(5(1)	(2(1) 	7(1)

O3	29(1) 	35(1)	25(1) 	(8(1)	(6(1) 	9(1)

C8	26(1) 	19(1)	19(1) 	(2(1)	6(1) 	(6(1)

C9	25(1) 	17(1)	18(1) 	1(1)	4(1) 	(5(1)

C10	24(1) 	19(1)	19(1) 	1(1)	3(1) 	(4(1)

C11	23(1) 	24(1)	21(1) 	(1(1)	2(1) 	(5(1)

C12	22(1) 	24(1)	28(1) 	1(1)	4(1) 	(3(1)

C13	27(1) 	19(1)	22(1) 	(1(1)	7(1) 	(4(1)

N1	25(1) 	21(1)	19(1) 	(1(1)	2(1) 	(4(1)

N2	38(1) 	19(1)	22(1) 	0(1)	(5(1) 	(5(1)

O4	38(1) 	18(1)	25(1) 	(4(1)	1(1) 	(5(1)