|  | University of Southampton · Department of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	02src273    (300-166-1)

Empirical formula 	C3H6Cl4N3O2P3

Formula weight 	350.82

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Orthorhombic

Space group 	Pna21

Unit cell dimensions	a = 13.3686(5) Å	( = 90°

b = 10.4704(4) Å	( = 90°

c = 8.7799(3) Å	(  = 90°

Volume	1228.96(8) Å3

Z	4

Density (calculated)	1.896 Mg / m3

Absorption coefficient	1.336 mm(1

F(000)	696

Crystal	needle; colourless

Crystal size	0.30 ( 0.04 ( 0.04 mm3

( range for data collection	3.03 ( 27.47°

Index ranges	(17 ( h ( 14, (11 ( k ( 13, (9 ( l ( 11

Reflections collected	5145

Independent reflections	2403 [Rint = 0.0369]

Completeness to ( = 27.47°	99.3 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9485 and 0.6900

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	2403 / 1 / 137

Goodness-of-fit on F2	0.922

Final R indices [F2 > 2((F2)]	R1 = 0.0253, wR2 = 0.0615

R indices (all data)	R1 = 0.0286, wR2 = 0.0631

Absolute structure parameter	0.02(8)

Extinction coefficient	0.0017(6)

Largest diff. peak and hole	0.296 and (0.348 e Å(3

Diffractometer: Enraf Nonius KappaCCD area detector (( scans and ( scans to fill Ewald sphere). Data collection and cell

refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography,

part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing,

Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Program used to solve structure:

SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Program used to refine structure: SHELXL97 (G. M. Sheldrick

(1997), University of Göttingen, Germany).

Further information:  http://www.soton.ac.uk/~xservice/strat.htm

Special details:

P1-P2 = 2.763, P2-P3 = .745, P1-P3 = 2.758, max deviation from mean plane = -0.08 (P1).

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	5215(2)	1439(3)	1947(3)	33(1)	1

C2	5875(2)	351(2)	2426(4)	34(1)	1

C3	5364(2)	(920(3)	2151(3)	35(1)	1

N1	3129(2)	45(2)	1101(3)	29(1)	1

N2	1285(2)	370(2)	2326(3)	32(1)	1

N3	2912(2)	153(2)	4156(3)	32(1)	1

O1	4288(1)	1406(2)	2831(2)	29(1)	1

O2	4405(1)	(964(2)	2961(2)	31(1)	1

P1	3640(1)	159(1)	2741(1)	24(1)	1

P2	1980(1)	199(1)	868(1)	26(1)	1

P3	1745(1)	281(1)	3972(1)	27(1)	1

Cl1	1708(1)	1657(1)	(539(1)	38(1)	1

Cl2	1466(1)	(1260(1)	(362(1)	37(1)	1

Cl3	1091(1)	(1146(1)	5104(1)	43(1)	1

Cl4	1276(1)	1781(1)	5181(1)	37(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(O1	1.463(3)

C1(C2	1.501(4)

C1(H1A	0.9900

C1(H1B	0.9900

C2(C3	1.515(4)

C2(H2A	0.9900

C2(H2B	0.9900

C3(O2	1.467(3)

C3(H3A	0.9900

C3(H3B	0.9900

N1(P2	1.558(2)

N1(P1	1.599(2)

N2(P3	1.573(3)

N2(P2	1.591(3)

N3(P3	1.574(2)

N3(P1	1.579(2)

O1(P1	1.5685(18)

O2(P1	1.5701(18)

P2(Cl2	1.9927(9)

P2(Cl1	1.9977(9)

P3(Cl3	1.9951(10)

P3(Cl4	1.9965(9)

O1(C1(C2	109.3(2)

O1(C1(H1A	109.8

C2(C1(H1A	109.8

O1(C1(H1B	109.8

C2(C1(H1B	109.8

H1A(C1(H1B	108.3

C1(C2(C3	111.0(2)

C1(C2(H2A	109.4

C3(C2(H2A	109.4

C1(C2(H2B	109.4

C3(C2(H2B	109.4

H2A(C2(H2B	108.0

O2(C3(C2	110.1(2)

O2(C3(H3A	109.6

C2(C3(H3A	109.6

O2(C3(H3B	109.6

C2(C3(H3B	109.6

H3A(C3(H3B	108.1

P2(N1(P1	122.15(15)

P3(N2(P2	120.27(14)

P3(N3(P1	122.04(16)

C1(O1(P1	117.47(16)

C3(O2(P1	119.06(16)

O1(P1(O2	104.92(10)

O1(P1(N3	107.76(11)

O2(P1(N3	107.57(11)

O1(P1(N1	110.11(11)

O2(P1(N1	109.46(11)

N3(P1(N1	116.39(12)

N1(P2(N2	118.79(13)

N1(P2(Cl2	109.35(9)

N2(P2(Cl2	108.72(9)

N1(P2(Cl1	109.86(9)

N2(P2(Cl1	107.77(9)

Cl2(P2(Cl1	100.84(4)

N2(P3(N3	119.11(13)

N2(P3(Cl3	109.35(9)

N3(P3(Cl3	108.59(9)

N2(P3(Cl4	108.60(9)

N3(P3(Cl4	108.88(10)

Cl3(P3(Cl4	100.75(4)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	33(1) 	41(1)	25(1) 	(1(1)	4(1) 	(10(1)

C2	25(1) 	54(2)	24(1) 	(1(1)	0(1) 	(1(1)

C3	30(2) 	40(1)	33(1) 	1(1)	5(1) 	10(1)

N1	25(1) 	37(1)	24(1) 	(4(1)	(1(1) 	0(1)

N2	26(1) 	40(1)	29(1) 	(2(1)	(1(1) 	2(1)

N3	26(1) 	46(1)	24(1) 	4(1)	(2(1) 	2(1)

O1	29(1) 	28(1)	31(1) 	(2(1)	1(1) 	(3(1)

O2	26(1) 	31(1)	36(1) 	6(1)	2(1) 	4(1)

P1	24(1) 	27(1)	23(1) 	1(1)	0(1) 	0(1)

P2	25(1) 	28(1)	24(1) 	(2(1)	(2(1) 	0(1)

P3	25(1) 	32(1)	26(1) 	1(1)	3(1) 	0(1)

Cl1	41(1) 	36(1)	36(1) 	8(1)	0(1) 	5(1)

Cl2	35(1) 	35(1)	41(1) 	(12(1)	(4(1) 	(3(1)

Cl3	41(1) 	41(1)	47(1) 	10(1)	11(1) 	(5(1)

Cl4	38(1) 	40(1)	33(1) 	(7(1)	1(1) 	5(1)

Table 5. Torsion angles [°].

O1(C1(C2(C3	60.3(3)

C1(C2(C3(O2	(57.0(3)

C2(C1(O1(P1	(57.8(3)

C2(C3(O2(P1	51.4(3)

C1(O1(P1(O2	46.8(2)

C1(O1(P1(N3	161.18(18)

C1(O1(P1(N1	(70.9(2)

C3(O2(P1(O1	(43.8(2)

C3(O2(P1(N3	(158.34(19)

C3(O2(P1(N1	74.3(2)

P3(N3(P1(O1	113.34(17)

P3(N3(P1(O2	(134.03(15)

P3(N3(P1(N1	(10.8(2)

P2(N1(P1(O1	(110.76(16)

P2(N1(P1(O2	134.40(15)

P2(N1(P1(N3	12.2(2)

P1(N1(P2(N2	(4.8(2)

P1(N1(P2(Cl2	(130.31(13)

P1(N1(P2(Cl1	119.89(14)

P3(N2(P2(N1	(4.5(2)

P3(N2(P2(Cl2	121.32(13)

P3(N2(P2(Cl1	(130.20(13)

P2(N2(P3(N3	5.8(2)

P2(N2(P3(Cl3	(119.79(13)

P2(N2(P3(Cl4	131.13(12)

P1(N3(P3(N2	2.2(2)

P1(N3(P3(Cl3	128.15(14)

P1(N3(P3(Cl4	(123.01(15)

Symmetry transformations used to generate equivalent atoms: