|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	2006sjc0030  (P3)

Empirical formula 	C8H4Cl2N2

Formula weight 	199.03

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	C2/c

Unit cell dimensions	a = 3.8278(2) Å	( = 90°

b = 18.9050(12) Å	( = 95.649(4)°

c = 10.8874(6) Å	(  = 90°

Volume	784.04(8) Å3

Z	4

Density (calculated)	1.686 Mg / m3

Absorption coefficient	0.760 mm(1

F(000)	400

Crystal	block; colourless

Crystal size	0.12 ( 0.05 ( 0.02 mm3

( range for data collection	3.76 ( 27.50°

Index ranges	(4 ( h ( 4, (24 ( k ( 24, (14 ( l ( 14

Reflections collected	5765

Independent reflections	899 [Rint = 0.0366]

Completeness to ( = 27.50°	99.2 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9850 and 0.9143

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	899 / 0 / 55

Goodness-of-fit on F2	1.098

Final R indices [F2 > 2((F2)]	R1 = 0.0279, wR2 = 0.0693

R indices (all data)	R1 = 0.0311, wR2 = 0.0717

Largest diff. peak and hole	0.277 and (0.207 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

Cl1	2727(1)	3085(1)	1194(1)	26(1)	1

N1	2965(3)	4456(1)	1353(1)	18(1)	1

C3	2949(4)	5728(1)	1345(1)	20(1)	1

C1	3969(4)	3877(1)	1914(1)	18(1)	1

C2	3970(4)	5081(1)	1919(1)	16(1)	1

C4	3965(4)	6349(1)	1924(1)	22(1)	1

Table 3. Bond lengths [Å] and angles [°].

Cl1(C1	1.7340(14)

N1(C1	1.2942(19)

N1(C2	1.3697(18)

C3(C4	1.370(2)

C3(C2	1.4114(19)

C1(C1i	1.432(3)

C2(C2i	1.423(3)

C4(C4i	1.416(3)

C1(N1(C2	117.42(12)

C4(C3(C2	119.05(13)

N1(C1(C1i	122.16(8)

N1(C1(Cl1	117.49(11)

C1i(C1(Cl1	120.34(5)

N1(C2(C3	119.69(13)

N1(C2(C2i	120.41(8)

C3(C2(C2i	119.89(8)

C3(C4(C4i	121.06(9)

Symmetry transformations used to generate equivalent atoms:

(i) (x+1,y,(z+1/2

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

Cl1	33(1) 	18(1)	25(1) 	(5(1)	(2(1) 	(4(1)

N1	17(1) 	20(1)	16(1) 	(1(1)	0(1) 	(1(1)

C3	18(1) 	23(1)	18(1) 	3(1)	1(1) 	2(1)

C1	19(1) 	18(1)	17(1) 	(3(1)	2(1) 	(2(1)

C2	15(1) 	18(1)	15(1) 	(1(1)	1(1) 	0(1)

C4	23(1) 	17(1)	26(1) 	4(1)	3(1) 	2(1)