|  | University of Southampton · School of Chemistry # EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement details.

Identification code 	2007src0237

Empirical formula 	C21H28N2O2Si2

Formula weight 	396.63

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/c

Unit cell dimensions	a = 10.72290(10) Å	a = 90°

b = 10.23950(10) Å	b = 92.7121(7)°

c = 20.1530(2) Å	g  = 90°

Volume	2210.26(4) Å3

Z	4

Density (calculated)	1.192 Mg / m3

Absorption coefficient	0.178 mm-1

F(000)	848

Crystal	Block; Colourless

Crystal size	0.16 ´ 0.10 ´ 0.06 mm3

q range for data collection	3.36 - 27.48°

Index ranges	-13 £ h £ 13, -13 £ k £ 13, -26 £ l £ 26

Reflections collected	38821

Independent reflections	5047 [Rint = 0.0341]

Completeness to q = 27.48°	99.7 %

Absorption correction	Semi-empirical from equivalents

Max. and min. transmission	0.9894 and 0.9721

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	5047 / 0 / 250

Goodness-of-fit on F2	1.063

Final R indices [F2 > 2s(F2)]	R1 = 0.0338, wR2 = 0.0839

R indices (all data)	R1 = 0.0380, wR2 = 0.0874

Largest diff. peak and hole	0.349 and -0.245 e Å-3

Diffractometer: Bruker-Nonius APEX II CCD camera (f scans and w scans to fill asymmetric unit). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307-326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: Sheldrick, G. M. SADABS 2007/2 - Bruker Nonius area detector scaling and absorption correction. Structure solution: Sir2004 (Burla, M.C., Caliandro, R., Carrozzini, B., Cascarano, G., De Caro, L., Giacovazzo, C. & Polidori, G. (2004). J. Appl. Cryst. 37, 258).  Structure refinement: SHELXL97 (Sheldrick, G. M. (1997). University of Göttingen, Germany). Graphics: PLATON/PLUTON  (Spek, A. L. (1990). Acta Cryst. A46, C34).

Special details:

The hydrogen atoms were fixed as riding models.

Table 2. Atomic coordinates [´ 104], equivalent isotropic displacement parameters [Å2 ´ 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	6715(1)	-2004(1)	1398(1)	17(1)	1

C2	7876(1)	-230(1)	1027(1)	18(1)	1

C3	8235(1)	-1520(1)	687(1)	19(1)	1

C4	7355(1)	678(1)	475(1)	19(1)	1

C5	6101(1)	1023(1)	419(1)	21(1)	1

C6	5654(1)	1805(1)	-106(1)	25(1)	1

C7	6444(1)	2237(1)	-581(1)	29(1)	1

C8	7695(1)	1884(2)	-532(1)	31(1)	1

C9	8148(1)	1106(1)	-12(1)	27(1)	1

C10	9036(1)	291(1)	1418(1)	20(1)	1

C11	9440(1)	1574(1)	1377(1)	28(1)	1

C12	10491(1)	1996(2)	1749(1)	32(1)	1

C13	11152(1)	1143(2)	2162(1)	31(1)	1

C14	10757(1)	-144(2)	2208(1)	31(1)	1

C15	9703(1)	-564(1)	1840(1)	25(1)	1

C16	6456(2)	-5187(1)	962(1)	39(1)	1

C17	7409(1)	-4052(2)	-318(1)	31(1)	1

C18	9260(1)	-4676(2)	847(1)	34(1)	1

C19	6743(2)	1842(1)	2180(1)	36(1)	1

C20	6597(2)	-703(2)	2931(1)	34(1)	1

C21	4452(1)	131(1)	1970(1)	26(1)	1

N1	7488(1)	-2506(1)	909(1)	18(1)	1

N2	6921(1)	-691(1)	1478(1)	17(1)	1

O1	5989(1)	-2655(1)	1706(1)	22(1)	1

O2	9037(1)	-1652(1)	288(1)	27(1)	1

Si1	7653(1)	-4144(1)	597(1)	21(1)	1

Si2	6170(1)	135(1)	2135(1)	20(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1-O1	1.2179(14)

C1-N2	1.3701(15)

C1-N1	1.4146(14)

C2-N2	1.4785(14)

C2-C4	1.5343(17)

C2-C10	1.5360(16)

C2-C3	1.5451(16)

C3-O2	1.2115(15)

C3-N1	1.3767(15)

C4-C5	1.3899(17)

C4-C9	1.3990(17)

C5-C6	1.3935(18)

C5-H5	0.9500

C6-C7	1.3808(19)

C6-H6	0.9500

C7-C8	1.389(2)

C7-H7	0.9500

C8-C9	1.3867(19)

C8-H8	0.9500

C9-H9	0.9500

C10-C11	1.3867(18)

C10-C15	1.3939(18)

C11-C12	1.3928(19)

C11-H11	0.9500

C12-C13	1.379(2)

C12-H12	0.9500

C13-C14	1.388(2)

C13-H13	0.9500

C14-C15	1.3909(19)

C14-H14	0.9500

C15-H15	0.9500

C16-Si1	1.8490(15)

C16-H16A	0.9800

C16-H16B	0.9800

C16-H16C	0.9800

C17-Si1	1.8536(14)

C17-H17A	0.9800

C17-H17B	0.9800

C17-H17C	0.9800

C18-Si1	1.8544(15)

C18-H18A	0.9800

C18-H18B	0.9800

C18-H18C	0.9800

C19-Si2	1.8531(15)

C19-H19A	0.9800

C19-H19B	0.9800

C19-H19C	0.9800

C20-Si2	1.8562(15)

C20-H20A	0.9800

C20-H20B	0.9800

C20-H20C	0.9800

C21-Si2	1.8567(13)

C21-H21A	0.9800

C21-H21B	0.9800

C21-H21C	0.9800

N1-Si1	1.8018(11)

N2-Si2	1.7935(10)

O1-C1-N2	125.49(11)

O1-C1-N1	124.49(11)

N2-C1-N1	110.01(10)

N2-C2-C4	113.56(9)

N2-C2-C10	111.29(10)

C4-C2-C10	114.82(10)

N2-C2-C3	101.19(9)

C4-C2-C3	106.57(10)

C10-C2-C3	108.23(9)

O2-C3-N1	125.13(11)

O2-C3-C2	126.10(11)

N1-C3-C2	108.78(10)

C5-C4-C9	118.69(12)

C5-C4-C2	122.09(11)

C9-C4-C2	119.09(11)

C4-C5-C6	120.36(12)

C4-C5-H5	119.8

C6-C5-H5	119.8

C7-C6-C5	120.69(12)

C7-C6-H6	119.7

C5-C6-H6	119.7

C6-C7-C8	119.29(12)

C6-C7-H7	120.4

C8-C7-H7	120.4

C9-C8-C7	120.41(13)

C9-C8-H8	119.8

C7-C8-H8	119.8

C8-C9-C4	120.55(12)

C8-C9-H9	119.7

C4-C9-H9	119.7

C11-C10-C15	118.64(12)

C11-C10-C2	123.04(11)

C15-C10-C2	118.31(11)

C10-C11-C12	120.54(13)

C10-C11-H11	119.7

C12-C11-H11	119.7

C13-C12-C11	120.54(13)

C13-C12-H12	119.7

C11-C12-H12	119.7

C12-C13-C14	119.49(13)

C12-C13-H13	120.3

C14-C13-H13	120.3

C13-C14-C15	120.01(13)

C13-C14-H14	120.0

C15-C14-H14	120.0

C14-C15-C10	120.77(13)

C14-C15-H15	119.6

C10-C15-H15	119.6

Si1-C16-H16A	109.5

Si1-C16-H16B	109.5

H16A-C16-H16B	109.5

Si1-C16-H16C	109.5

H16A-C16-H16C	109.5

H16B-C16-H16C	109.5

Si1-C17-H17A	109.5

Si1-C17-H17B	109.5

H17A-C17-H17B	109.5

Si1-C17-H17C	109.5

H17A-C17-H17C	109.5

H17B-C17-H17C	109.5

Si1-C18-H18A	109.5

Si1-C18-H18B	109.5

H18A-C18-H18B	109.5

Si1-C18-H18C	109.5

H18A-C18-H18C	109.5

H18B-C18-H18C	109.5

Si2-C19-H19A	109.5

Si2-C19-H19B	109.5

H19A-C19-H19B	109.5

Si2-C19-H19C	109.5

H19A-C19-H19C	109.5

H19B-C19-H19C	109.5

Si2-C20-H20A	109.5

Si2-C20-H20B	109.5

H20A-C20-H20B	109.5

Si2-C20-H20C	109.5

H20A-C20-H20C	109.5

H20B-C20-H20C	109.5

Si2-C21-H21A	109.5

Si2-C21-H21B	109.5

H21A-C21-H21B	109.5

Si2-C21-H21C	109.5

H21A-C21-H21C	109.5

H21B-C21-H21C	109.5

C3-N1-C1	109.20(10)

C3-N1-Si1	120.09(8)

C1-N1-Si1	130.64(8)

C1-N2-C2	110.70(9)

C1-N2-Si2	118.30(8)

C2-N2-Si2	130.63(8)

N1-Si1-C16	108.52(6)

N1-Si1-C17	106.72(6)

C16-Si1-C17	110.92(8)

N1-Si1-C18	106.54(6)

C16-Si1-C18	112.12(8)

C17-Si1-C18	111.72(7)

N2-Si2-C19	108.75(6)

N2-Si2-C20	108.59(6)

C19-Si2-C20	109.02(8)

N2-Si2-C21	110.04(6)

C19-Si2-C21	109.52(7)

C20-Si2-C21	110.87(7)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2´ 103]. The anisotropic displacement

factor exponent takes the form: -2p 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	16(1) 	17(1)	17(1) 	1(1)	-1(1) 	2(1)

C2	16(1) 	17(1)	21(1) 	0(1)	2(1) 	-1(1)

C3	16(1) 	18(1)	22(1) 	1(1)	0(1) 	-1(1)

C4	20(1) 	16(1)	23(1) 	1(1)	-1(1) 	-2(1)

C5	20(1) 	20(1)	23(1) 	-1(1)	0(1) 	-2(1)

C6	24(1) 	23(1)	29(1) 	-1(1)	-7(1) 	1(1)

C7	36(1) 	23(1)	26(1) 	5(1)	-8(1) 	-4(1)

C8	33(1) 	32(1)	28(1) 	9(1)	2(1) 	-8(1)

C9	22(1) 	29(1)	31(1) 	7(1)	2(1) 	-2(1)

C10	16(1) 	20(1)	24(1) 	-1(1)	1(1) 	-1(1)

C11	24(1) 	23(1)	36(1) 	4(1)	-6(1) 	-5(1)

C12	28(1) 	27(1)	42(1) 	-1(1)	-5(1) 	-9(1)

C13	20(1) 	37(1)	35(1) 	-7(1)	-5(1) 	-2(1)

C14	28(1) 	32(1)	33(1) 	-1(1)	-8(1) 	6(1)

C15	25(1) 	21(1)	29(1) 	0(1)	-3(1) 	2(1)

C16	55(1) 	21(1)	43(1) 	-8(1)	21(1) 	-12(1)

C17	36(1) 	33(1)	22(1) 	-7(1)	1(1) 	0(1)

C18	39(1) 	31(1)	32(1) 	1(1)	2(1) 	15(1)

C19	42(1) 	23(1)	43(1) 	-12(1)	9(1) 	-3(1)

C20	40(1) 	41(1)	20(1) 	-1(1)	0(1) 	12(1)

C21	23(1) 	29(1)	27(1) 	-1(1)	5(1) 	5(1)

N1	18(1) 	16(1)	19(1) 	-1(1)	3(1) 	0(1)

N2	17(1) 	16(1)	19(1) 	0(1)	3(1) 	0(1)

O1	24(1) 	19(1)	23(1) 	2(1)	6(1) 	-2(1)

O2	23(1) 	26(1)	33(1) 	-2(1)	12(1) 	-2(1)

Si1	26(1) 	16(1)	20(1) 	-2(1)	4(1) 	0(1)

Si2	21(1) 	19(1)	19(1) 	-2(1)	2(1) 	3(1)

Table 5. Hydrogen coordinates [´ 104] and isotropic displacement parameters [Å2 ´ 103].

Atom 	x	y	z	Ueq	S.o.f.

H5	5546	724	740	25	1

H6	4797	2043	-137	30	1

H7	6134	2771	-938	34	1

H8	8244	2176	-858	37	1

H9	9003	862	14	32	1

H11	8995	2170	1092	34	1

H12	10755	2878	1718	39	1

H13	11872	1434	2412	37	1

H14	11208	-738	2491	37	1

H15	9433	-1444	1877	30	1

H16A	6596	-5210	1446	59	1

H16B	6512	-6074	784	59	1

H16C	5624	-4828	850	59	1

H17A	6552	-3768	-431	46	1

H17B	7548	-4915	-511	46	1

H17C	7998	-3424	-495	46	1

H18A	9863	-4062	671	51	1

H18B	9408	-5550	669	51	1

H18C	9360	-4698	1332	51	1

H19A	7623	1847	2334	54	1

H19B	6251	2338	2491	54	1

H19C	6657	2242	1738	54	1

H20A	6351	-1623	2899	51	1

H20B	6165	-284	3292	51	1

H20C	7502	-643	3021	51	1

H21A	4235	722	1600	39	1

H21B	4041	425	2367	39	1

H21C	4173	-755	1855	39	1