|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement details.

Identification code 	2007src0831

Empirical formula 	C17H20ClFeNO3

Formula weight 	377.64

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/n

Unit cell dimensions	a = 7.8204(2) Å	( = 90°

b = 19.1689(6) Å	( = 100.727(2)°

c = 11.3839(3) Å	(  = 90°

Volume	1676.72(8) Å3

Z	4

Density (calculated)	1.496 Mg / m3

Absorption coefficient	1.072 mm(1

F(000)	784

Crystal	Block; Orange

Crystal size	0.28 ( 0.18 ( 0.08 mm3

( range for data collection	2.92 ( 27.48°

Index ranges	(10 ( h ( 9, (24 ( k ( 22, (14 ( l ( 14

Reflections collected	21767

Independent reflections	3834 [Rint = 0.0629]

Completeness to ( = 27.48°	99.8 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.7456 and 0.6151

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	3834 / 0 / 211

Goodness-of-fit on F2	1.061

Final R indices [F2 > 2((F2)]	R1 = 0.0437, wR2 = 0.1034

R indices (all data)	R1 = 0.0630, wR2 = 0.1133

Largest diff. peak and hole	0.524 and (0.560 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit ). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: Sheldrick, G. M. SADABS 2007/2 - Bruker Nonius area detector scaling and absorption correction. Structure solution: Sir2004 (Burla, M.C., Caliandro, R., Carrozzini, B., Cascarano, G., De Caro, L., Giacovazzo, C. & Polidori, G. (2004). J. Appl. Cryst. 37, 258).  Structure refinement: SHELXL97 (Sheldrick, G. M. (1997). University of Göttingen, Germany). Graphics: PLATON/PLUTON  (Spek, A. L. (1990). Acta Cryst. A46, C34).

Special details:

The hydrogen atoms were fixed as riding models.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	2802(3)	2750(1)	4028(2)	18(1)	1

C2	2640(3)	2357(1)	2938(2)	21(1)	1

C3	1501(4)	1791(1)	2990(2)	25(1)	1

C4	936(3)	1804(1)	4105(2)	24(1)	1

C5	1727(3)	2395(1)	4768(2)	20(1)	1

C6	6194(3)	1758(2)	5186(2)	26(1)	1

C7	5932(4)	1356(2)	4119(2)	27(1)	1

C8	4756(4)	811(2)	4238(3)	29(1)	1

C9	4268(4)	878(1)	5378(2)	26(1)	1

C10	5156(3)	1462(2)	5963(2)	25(1)	1

C11	3807(3)	3399(1)	4302(2)	19(1)	1

C12	5713(3)	4281(1)	3655(2)	22(1)	1

C13	4606(4)	4856(2)	2968(3)	31(1)	1

C14	7509(4)	4186(1)	3336(3)	27(1)	1

C15	8483(4)	4883(2)	3383(3)	36(1)	1

C16	8567(4)	3659(2)	4175(3)	44(1)	1

C17	1441(4)	2528(1)	6001(3)	26(1)	1

N1	4750(3)	3618(1)	3514(2)	22(1)	1

O1	3738(3)	3751(1)	5223(2)	28(1)	1

O2	2133(3)	3084(1)	6571(2)	33(1)	1

O3	544(3)	2125(1)	6461(2)	33(1)	1

Fe1	3608(1)	1756(1)	4389(1)	17(1)	1

Cl1	4337(1)	4753(1)	1382(1)	44(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(C2	1.437(3)

C1(C5	1.464(3)

C1(C11	1.474(3)

C1(Fe1	2.023(2)

C2(C3	1.412(4)

C2(Fe1	2.040(2)

C2(H2	0.9500

C3(C4	1.419(4)

C3(Fe1	2.068(3)

C3(H3	0.9500

C4(C5	1.436(4)

C4(Fe1	2.056(3)

C4(H4	0.9500

C5(C17	1.483(4)

C5(Fe1	2.021(3)

C6(C7	1.420(4)

C6(C10	1.426(4)

C6(Fe1	2.056(3)

C6(H6	0.9500

C7(C8	1.415(4)

C7(Fe1	2.048(3)

C7(H7	0.9500

C8(C9	1.425(4)

C8(Fe1	2.043(3)

C8(H8	0.9500

C9(C10	1.416(4)

C9(Fe1	2.038(3)

C9(H9	0.9500

C10(Fe1	2.047(3)

C10(H10	0.9500

C11(O1	1.255(3)

C11(N1	1.331(3)

C12(N1	1.470(3)

C12(C13	1.524(4)

C12(C14	1.526(4)

C12(H12	1.0000

C13(Cl1	1.789(3)

C13(H13A	0.9900

C13(H13B	0.9900

C14(C16	1.524(4)

C14(C15	1.534(4)

C14(H14	1.0000

C15(H15A	0.9800

C15(H15B	0.9800

C15(H15C	0.9800

C16(H16A	0.9800

C16(H16B	0.9800

C16(H16C	0.9800

C17(O3	1.226(3)

C17(O2	1.310(4)

N1(H1	0.8800

O2(H2A	0.8400

C2(C1(C5	106.6(2)

C2(C1(C11	125.7(2)

C5(C1(C11	127.7(2)

C2(C1(Fe1	69.90(14)

C5(C1(Fe1	68.70(14)

C11(C1(Fe1	128.20(18)

C3(C2(C1	108.7(2)

C3(C2(Fe1	70.96(15)

C1(C2(Fe1	68.68(14)

C3(C2(H2	125.6

C1(C2(H2	125.6

Fe1(C2(H2	126.3

C2(C3(C4	109.1(2)

C2(C3(Fe1	68.82(15)

C4(C3(Fe1	69.42(15)

C2(C3(H3	125.4

C4(C3(H3	125.4

Fe1(C3(H3	127.9

C3(C4(C5	108.0(2)

C3(C4(Fe1	70.32(15)

C5(C4(Fe1	68.08(14)

C3(C4(H4	126.0

C5(C4(H4	126.0

Fe1(C4(H4	127.2

C4(C5(C1	107.5(2)

C4(C5(C17	120.5(2)

C1(C5(C17	131.9(2)

C4(C5(Fe1	70.68(15)

C1(C5(Fe1	68.87(14)

C17(C5(Fe1	123.36(18)

C7(C6(C10	107.8(2)

C7(C6(Fe1	69.43(15)

C10(C6(Fe1	69.30(15)

C7(C6(H6	126.1

C10(C6(H6	126.1

Fe1(C6(H6	126.8

C8(C7(C6	108.1(2)

C8(C7(Fe1	69.57(15)

C6(C7(Fe1	70.08(15)

C8(C7(H7	125.9

C6(C7(H7	125.9

Fe1(C7(H7	126.0

C7(C8(C9	108.1(2)

C7(C8(Fe1	69.95(15)

C9(C8(Fe1	69.35(15)

C7(C8(H8	126.0

C9(C8(H8	126.0

Fe1(C8(H8	126.3

C10(C9(C8	107.9(2)

C10(C9(Fe1	70.07(15)

C8(C9(Fe1	69.76(15)

C10(C9(H9	126.0

C8(C9(H9	126.0

Fe1(C9(H9	125.7

C9(C10(C6	108.0(2)

C9(C10(Fe1	69.37(15)

C6(C10(Fe1	70.03(15)

C9(C10(H10	126.0

C6(C10(H10	126.0

Fe1(C10(H10	126.2

O1(C11(N1	120.6(2)

O1(C11(C1	121.7(2)

N1(C11(C1	117.6(2)

N1(C12(C13	109.7(2)

N1(C12(C14	110.2(2)

C13(C12(C14	115.1(2)

N1(C12(H12	107.1

C13(C12(H12	107.1

C14(C12(H12	107.1

C12(C13(Cl1	112.83(19)

C12(C13(H13A	109.0

Cl1(C13(H13A	109.0

C12(C13(H13B	109.0

Cl1(C13(H13B	109.0

H13A(C13(H13B	107.8

C16(C14(C12	110.2(2)

C16(C14(C15	110.3(3)

C12(C14(C15	111.2(2)

C16(C14(H14	108.3

C12(C14(H14	108.3

C15(C14(H14	108.3

C14(C15(H15A	109.5

C14(C15(H15B	109.5

H15A(C15(H15B	109.5

C14(C15(H15C	109.5

H15A(C15(H15C	109.5

H15B(C15(H15C	109.5

C14(C16(H16A	109.5

C14(C16(H16B	109.5

H16A(C16(H16B	109.5

C14(C16(H16C	109.5

H16A(C16(H16C	109.5

H16B(C16(H16C	109.5

O3(C17(O2	121.2(3)

O3(C17(C5	119.7(3)

O2(C17(C5	119.1(2)

C11(N1(C12	122.4(2)

C11(N1(H1	118.8

C12(N1(H1	118.8

C17(O2(H2A	109.5

C5(Fe1(C1	42.43(10)

C5(Fe1(C9	120.13(11)

C1(Fe1(C9	157.93(11)

C5(Fe1(C2	69.89(10)

C1(Fe1(C2	41.42(10)

C9(Fe1(C2	158.66(11)

C5(Fe1(C8	154.65(11)

C1(Fe1(C8	160.44(11)

C9(Fe1(C8	40.89(11)

C2(Fe1(C8	122.33(11)

C5(Fe1(C10	108.40(11)

C1(Fe1(C10	123.26(11)

C9(Fe1(C10	40.56(11)

C2(Fe1(C10	159.17(11)

C8(Fe1(C10	68.36(11)

C5(Fe1(C7	163.80(11)

C1(Fe1(C7	124.97(11)

C9(Fe1(C7	68.48(11)

C2(Fe1(C7	107.18(11)

C8(Fe1(C7	40.47(12)

C10(Fe1(C7	68.36(11)

C5(Fe1(C4	41.24(10)

C1(Fe1(C4	69.96(10)

C9(Fe1(C4	105.62(11)

C2(Fe1(C4	68.57(11)

C8(Fe1(C4	118.42(11)

C10(Fe1(C4	124.63(11)

C7(Fe1(C4	153.83(12)

C5(Fe1(C6	126.84(11)

C1(Fe1(C6	109.34(11)

C9(Fe1(C6	68.32(11)

C2(Fe1(C6	122.83(11)

C8(Fe1(C6	68.11(12)

C10(Fe1(C6	40.67(11)

C7(Fe1(C6	40.49(11)

C4(Fe1(C6	163.03(11)

C5(Fe1(C3	68.79(11)

C1(Fe1(C3	68.94(10)

C9(Fe1(C3	122.37(11)

C2(Fe1(C3	40.21(10)

C8(Fe1(C3	105.25(11)

C10(Fe1(C3	159.97(11)

C7(Fe1(C3	119.90(11)

C4(Fe1(C3	40.26(11)

C6(Fe1(C3	156.41(12)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	19(1) 	17(1)	19(1) 	2(1)	4(1) 	1(1)

C2	23(1) 	20(1)	18(1) 	2(1)	1(1) 	0(1)

C3	24(1) 	23(1)	26(1) 	(1(1)	(3(1) 	(2(1)

C4	20(1) 	22(1)	31(1) 	5(1)	4(1) 	(1(1)

C5	18(1) 	20(1)	23(1) 	4(1)	6(1) 	2(1)

C6	20(1) 	31(2)	26(1) 	6(1)	(1(1) 	1(1)

C7	26(1) 	32(2)	26(1) 	6(1)	10(1) 	11(1)

C8	35(2) 	22(1)	29(2) 	1(1)	7(1) 	10(1)

C9	29(2) 	22(1)	30(1) 	8(1)	10(1) 	5(1)

C10	26(1) 	29(2)	20(1) 	4(1)	2(1) 	6(1)

C11	22(1) 	16(1)	20(1) 	0(1)	6(1) 	2(1)

C12	26(1) 	16(1)	24(1) 	0(1)	7(1) 	(1(1)

C13	34(2) 	21(1)	39(2) 	(1(1)	9(1) 	3(1)

C14	28(2) 	24(1)	31(1) 	1(1)	10(1) 	1(1)

C15	30(2) 	37(2)	41(2) 	0(1)	9(1) 	(12(1)

C16	31(2) 	42(2)	59(2) 	15(2)	7(2) 	10(1)

C17	25(1) 	26(2)	29(1) 	6(1)	11(1) 	8(1)

N1	28(1) 	16(1)	23(1) 	(4(1)	11(1) 	(4(1)

O1	38(1) 	26(1)	26(1) 	(9(1)	16(1) 	(7(1)

O2	41(1) 	38(1)	26(1) 	(3(1)	19(1) 	(5(1)

O3	37(1) 	33(1)	37(1) 	11(1)	24(1) 	4(1)

Fe1	19(1) 	15(1)	18(1) 	1(1)	4(1) 	1(1)

Cl1	51(1) 	37(1)	39(1) 	7(1)	(5(1) 	4(1)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H2	3206	2461	2289	25	1

H3	1167	1454	2377	30	1

H4	169	1479	4366	29	1

H6	6929	2154	5351	31	1

H7	6456	1439	3443	33	1

H8	4361	462	3659	35	1

H9	3484	583	5691	31	1

H10	5075	1626	6738	30	1

H12	5897	4408	4522	26	1

H13A	5159	5313	3196	37	1

H13B	3447	4857	3198	37	1

H14	7354	4000	2502	32	1

H15A	7882	5192	2752	53	1

H15B	9675	4800	3261	53	1

H15C	8515	5102	4164	53	1

H16A	8596	3800	5005	66	1

H16B	9756	3640	4018	66	1

H16C	8028	3197	4040	66	1

H1	4800	3357	2886	26	1

H2A	2689	3308	6131	50	1

Table 6. Hydrogen bonds [Å and °].

D(H···A	d(D(H)	d(H···A)	d(D···A)	((DHA)

N1(H1...O3i	0.88	2.04	2.900(3)	164.7

O2(H2A...O1	0.84	1.67	2.507(3)	178.2

Symmetry transformations used to generate equivalent atoms:

(i) x+1/2,(y+1/2,z(1/2