|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	2007src0927    (307-475-A)

Empirical formula 	C10H15Cl3N5OP3

Formula weight 	420.53

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21

Unit cell dimensions	a = 9.68270(10) Å	( = 90°

b = 22.3776(2) Å	( = 91.8460(10)°

c = 16.0124(2) Å	(  = 90°

Volume	3467.70(6) Å3

Z	8

Density (calculated)	1.611 Mg / m3

Absorption coefficient	0.812 mm(1

F(000)	1712

Crystal	prism; colourless

Crystal size	0.20 ( 0.06 ( 0.04 mm3

( range for data collection	3.01 ( 27.50°

Index ranges	(12 ( h ( 12, (29 ( k ( 28, (20 ( l ( 20

Reflections collected	35212

Independent reflections	15188 [Rint = 0.0323]

Completeness to ( = 27.50°	99.6 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9683 and 0.8545

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	15188 / 1 / 814

Goodness-of-fit on F2	1.034

Final R indices [F2 > 2((F2)]	R1 = 0.0316, wR2 = 0.0696

R indices (all data)	R1 = 0.0345, wR2 = 0.0714

Absolute structure parameter	0.44(3)

Largest diff. peak and hole	0.325 and (0.336 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SADABS Version 2.10. (G. M. Sheldrick (2003)) Bruker AXS Inc., Madison, Wisconsin, USA. Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: PLATON  (A.L. Spek, J. Appl. Crystallogr. 2003, 36, 7).

Special details:

Four independent molecules:

P1-P2 = 2.798, P2-P3 = 2.697, P1-P3 = 2.881, max dev = 0.127 (N2)

P4-P5 = 2.795, P5-P6 = 2.712, P4–P6 = 2.779, max dev = 0.133 (N7)

P7-P8 = 2.778, P8-P9 = 2.729, P7-P9 = 2.776, max dev =  0.109 (N12)

P10-P11 = 2.787, P11-P12 = 2.701, P10-P12 = 2.796, max dev = 0.144 (N17)

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	10396(4)	2380(1)	2323(2)	34(1)	1

C2	9763(3)	1759(1)	3520(2)	28(1)	1

C3	10038(3)	1175(1)	3957(2)	27(1)	1

C4	9475(3)	655(1)	3461(2)	28(1)	1

C5	6586(3)	1244(1)	(634(2)	24(1)	1

C6	7269(3)	1061(1)	(1320(2)	30(1)	1

C7	6637(3)	1151(2)	(2110(2)	34(1)	1

C8	5362(3)	1410(2)	(2187(2)	31(1)	1

C9	4704(3)	1592(2)	(1484(2)	47(1)	1

C10	5310(3)	1512(2)	(688(2)	47(1)	1

C11	5927(3)	2877(1)	3817(2)	32(1)	1

C12	5790(3)	2447(1)	2411(2)	25(1)	1

C13	4907(3)	2095(1)	1785(2)	24(1)	1

C14	4632(3)	1470(1)	2103(2)	24(1)	1

C15	1578(3)	1569(1)	6323(2)	20(1)	1

C16	1830(3)	1004(1)	6634(2)	26(1)	1

C17	1430(3)	873(2)	7437(2)	34(1)	1

C18	779(3)	1300(2)	7899(2)	32(1)	1

C19	521(3)	1863(2)	7571(2)	32(1)	1

C20	930(3)	2007(1)	6773(2)	27(1)	1

C21	(2579(3)	2789(2)	7235(2)	38(1)	1

C22	(2659(3)	3402(2)	8494(2)	31(1)	1

C23	(1885(3)	3836(2)	9067(2)	35(1)	1

C24	(1540(3)	4411(2)	8630(2)	32(1)	1

C25	1501(3)	4084(1)	4511(2)	23(1)	1

C26	2339(3)	3670(2)	4137(2)	30(1)	1

C27	2725(3)	3774(2)	3318(2)	39(1)	1

C28	2272(3)	4282(2)	2904(2)	40(1)	1

C29	1422(3)	4684(2)	3292(2)	37(1)	1

C30	1025(3)	4588(1)	4103(2)	29(1)	1

C31	(7287(4)	3253(1)	8418(2)	37(1)	1

C32	(6628(3)	3919(1)	7291(2)	27(1)	1

C33	(6796(3)	4538(1)	6908(2)	27(1)	1

C34	(6247(3)	5023(1)	7492(2)	28(1)	1

C35	(3684(3)	4454(1)	11495(2)	21(1)	1

C36	(4378(3)	4741(2)	12117(2)	29(1)	1

C37	(3850(3)	4680(2)	12934(2)	37(1)	1

C38	(2673(3)	4359(2)	13111(2)	36(1)	1

C39	(1986(3)	4079(2)	12469(2)	33(1)	1

C40	(2490(3)	4123(1)	11649(2)	27(1)	1

N1	11364(2)	1184(1)	1416(1)	22(1)	1

N2	9772(2)	1292(1)	(6(1)	23(1)	1

N3	8601(2)	1306(1)	1512(1)	23(1)	1

N4	10380(3)	1780(1)	2688(2)	23(1)	1

N5	10084(3)	646(1)	2631(2)	24(1)	1

N6	5810(2)	1496(1)	4077(1)	22(1)	1

N7	4544(2)	1407(1)	5564(1)	20(1)	1

N8	3345(2)	2044(1)	4289(1)	20(1)	1

N9	5139(2)	2488(1)	3233(1)	21(1)	1

N10	3855(3)	1484(1)	2879(2)	21(1)	1

N11	(2698(2)	4156(1)	6758(2)	24(1)	1

N12	(1439(2)	4225(1)	5278(2)	29(1)	1

N13	(193(2)	3631(1)	6583(1)	20(1)	1

N14	(1886(2)	3256(1)	7738(2)	23(1)	1

N15	(679(2)	4304(1)	7893(2)	21(1)	1

N16	(8340(2)	4396(1)	9406(2)	24(1)	1

N17	(6751(2)	4295(1)	10832(1)	23(1)	1

N18	(5563(2)	4295(1)	9321(1)	21(1)	1

N19	(7296(2)	3874(1)	8103(2)	23(1)	1

N20	(7029(3)	5004(1)	8262(2)	24(1)	1

O1	7145(2)	1133(1)	185(1)	30(1)	1

O2	1938(2)	1700(1)	5493(1)	21(1)	1

O3	1175(2)	3985(1)	5355(1)	22(1)	1

O4	(4146(2)	4518(1)	10647(1)	22(1)	1

P1	10073(1)	1225(1)	2023(1)	18(1)	1

P2	11240(1)	1275(1)	448(1)	19(1)	1

P3	8493(1)	1446(1)	551(1)	20(1)	1

P4	4533(1)	1871(1)	3654(1)	17(1)	1

P5	5860(1)	1305(1)	5014(1)	18(1)	1

P6	3439(1)	1884(1)	5238(1)	17(1)	1

P7	(1361(1)	3837(1)	7200(1)	17(1)	1

P8	(2717(1)	4365(1)	5834(1)	20(1)	1

P9	(290(1)	3772(1)	5622(1)	19(1)	1

P10	(7022(1)	4395(1)	8816(1)	19(1)	1

P11	(8216(1)	4275(1)	10368(1)	20(1)	1

P12	(5446(1)	4173(1)	10276(1)	18(1)	1

Cl1	12237(1)	2035(1)	139(1)	26(1)	1

Cl2	12395(1)	661(1)	(104(1)	29(1)	1

Cl3	8057(1)	2326(1)	353(1)	31(1)	1

Cl4	6410(1)	446(1)	5135(1)	28(1)	1

Cl5	7513(1)	1691(1)	5607(1)	31(1)	1

Cl6	3776(1)	2638(1)	5919(1)	29(1)	1

Cl7	(3068(1)	5245(1)	5762(1)	45(1)	1

Cl8	(4434(1)	4052(1)	5240(1)	26(1)	1

Cl9	(531(1)	3001(1)	4978(1)	35(1)	1

Cl10	(9105(1)	3480(1)	10639(1)	29(1)	1

Cl11	(9497(1)	4822(1)	10945(1)	29(1)	1

Cl12	(4890(1)	3306(1)	10469(1)	28(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(N4	1.465(4)

C2(N4	1.477(4)

C2(C3	1.503(4)

C3(C4	1.501(4)

C4(N5	1.471(4)

C5(C6	1.363(4)

C5(C10	1.373(4)

C5(O1	1.425(3)

C6(C7	1.403(4)

C7(C8	1.365(4)

C8(C9	1.373(5)

C9(C10	1.396(4)

C11(N9	1.474(3)

C12(N9	1.480(4)

C12(C13	1.517(4)

C13(C14	1.513(4)

C14(N10	1.474(4)

C15(C16	1.379(4)

C15(C20	1.379(4)

C15(O2	1.416(3)

C16(C17	1.385(4)

C17(C18	1.375(5)

C18(C19	1.384(5)

C19(C20	1.387(4)

C21(N14	1.468(4)

C22(N14	1.481(4)

C22(C23	1.517(4)

C23(C24	1.507(5)

C24(N15	1.486(4)

C25(C30	1.377(4)

C25(C26	1.380(4)

C25(O3	1.415(3)

C26(C27	1.394(4)

C27(C28	1.382(5)

C28(C29	1.380(5)

C29(C30	1.382(4)

C31(N19	1.479(4)

C32(N19	1.474(4)

C32(C33	1.521(4)

C33(C34	1.517(4)

C34(N20	1.467(4)

C35(C36	1.378(4)

C35(C40	1.389(4)

C35(O4	1.423(3)

C36(C37	1.395(4)

C37(C38	1.369(5)

C38(C39	1.390(5)

C39(C40	1.389(4)

N1(P2	1.565(2)

N1(P1	1.610(2)

N2(P2	1.576(2)

N2(P3	1.587(2)

N3(P3	1.570(2)

N3(P1	1.630(2)

N4(P1	1.658(2)

N5(P1	1.621(3)

N6(P5	1.560(2)

N6(P4	1.623(2)

N7(P6	1.588(2)

N7(P5	1.589(2)

N8(P6	1.561(2)

N8(P4	1.606(2)

N9(P4	1.653(2)

N10(P4	1.634(2)

N11(P8	1.552(2)

N11(P7	1.620(2)

N12(P8	1.578(3)

N12(P9	1.589(2)

N13(P9	1.571(2)

N13(P7	1.594(2)

N14(P7	1.650(2)

N15(P7	1.646(2)

N16(P11	1.564(2)

N16(P10	1.612(2)

N17(P11	1.580(2)

N17(P12	1.593(2)

N18(P12	1.555(2)

N18(P10	1.621(2)

N19(P10	1.648(2)

N20(P10	1.626(2)

O1(P3	1.578(2)

O2(P6	1.5768(19)

O3(P9	1.569(2)

O4(P12	1.5766(19)

P2(Cl2	1.9950(10)

P2(Cl1	2.0263(10)

P2(P3	2.6974(10)

P3(Cl3	2.0355(10)

P5(Cl4	2.0021(10)

P5(Cl5	2.0275(9)

P6(Cl6	2.0315(10)

P8(Cl7	1.9993(10)

P8(Cl8	2.0142(9)

P9(Cl9	2.0198(10)

P11(Cl11	1.9922(10)

P11(Cl10	2.0292(10)

P12(Cl12	2.0336(10)

N4(C2(C3	112.1(2)

C4(C3(C2	111.8(2)

N5(C4(C3	109.9(2)

C6(C5(C10	122.6(3)

C6(C5(O1	120.6(3)

C10(C5(O1	116.7(3)

C5(C6(C7	118.3(3)

C8(C7(C6	120.6(3)

C7(C8(C9	119.7(3)

C8(C9(C10	121.1(3)

C5(C10(C9	117.7(3)

N9(C12(C13	111.8(2)

C14(C13(C12	111.1(2)

N10(C14(C13	111.3(2)

C16(C15(C20	122.7(3)

C16(C15(O2	118.9(3)

C20(C15(O2	118.3(2)

C15(C16(C17	118.6(3)

C18(C17(C16	120.0(3)

C17(C18(C19	120.6(3)

C18(C19(C20	120.5(3)

C15(C20(C19	117.7(3)

N14(C22(C23	112.5(2)

C24(C23(C22	112.3(2)

N15(C24(C23	111.7(3)

C30(C25(C26	122.5(3)

C30(C25(O3	120.0(3)

C26(C25(O3	117.5(3)

C25(C26(C27	118.4(3)

C28(C27(C26	119.8(3)

C29(C28(C27	120.4(3)

C28(C29(C30	120.7(3)

C25(C30(C29	118.3(3)

N19(C32(C33	112.0(2)

C34(C33(C32	111.8(2)

N20(C34(C33	108.5(2)

C36(C35(C40	122.9(3)

C36(C35(O4	119.8(3)

C40(C35(O4	117.2(3)

C35(C36(C37	117.3(3)

C38(C37(C36	121.6(3)

C37(C38(C39	119.8(3)

C40(C39(C38	120.3(3)

C39(C40(C35	118.1(3)

P2(N1(P1	123.63(14)

P2(N2(P3	117.05(15)

P3(N3(P1	122.89(15)

C1(N4(C2	113.5(2)

C1(N4(P1	115.7(2)

C2(N4(P1	119.09(19)

C4(N5(P1	122.4(2)

P5(N6(P4	122.84(15)

P6(N7(P5	117.25(14)

P6(N8(P4	122.64(14)

C11(N9(C12	112.0(2)

C11(N9(P4	114.71(19)

C12(N9(P4	118.58(19)

C14(N10(P4	116.66(19)

P8(N11(P7	122.32(15)

P8(N12(P9	119.02(15)

P9(N13(P7	121.85(14)

C21(N14(C22	111.8(2)

C21(N14(P7	114.7(2)

C22(N14(P7	115.2(2)

C24(N15(P7	114.50(19)

P11(N16(P10	122.69(14)

P11(N17(P12	116.68(14)

P12(N18(P10	123.40(14)

C32(N19(C31	111.6(2)

C32(N19(P10	119.8(2)

C31(N19(P10	115.5(2)

C34(N20(P10	119.3(2)

C5(O1(P3	123.32(17)

C15(O2(P6	123.69(16)

C25(O3(P9	122.62(16)

C35(O4(P12	122.19(16)

N1(P1(N5	109.04(13)

N1(P1(N3	112.78(12)

N5(P1(N3	112.27(13)

N1(P1(N4	107.67(13)

N5(P1(N4	102.43(13)

N3(P1(N4	112.05(13)

N1(P2(N2	119.95(12)

N1(P2(Cl2	108.86(10)

N2(P2(Cl2	108.82(10)

N1(P2(Cl1	109.22(9)

N2(P2(Cl1	107.28(10)

Cl2(P2(Cl1	101.06(4)

N1(P2(P3	90.12(9)

N2(P2(P3	31.60(9)

Cl2(P2(P3	133.85(4)

Cl1(P2(P3	111.96(4)

N3(P3(O1	107.62(12)

N3(P3(N2	118.59(12)

O1(P3(N2	110.22(12)

N3(P3(Cl3	110.64(10)

O1(P3(Cl3	101.95(9)

N2(P3(Cl3	106.57(10)

N3(P3(P2	89.83(9)

O1(P3(P2	136.02(10)

N2(P3(P2	31.36(8)

Cl3(P3(P2	109.16(4)

N8(P4(N6	114.37(12)

N8(P4(N10	109.26(12)

N6(P4(N10	108.94(13)

N8(P4(N9	109.11(12)

N6(P4(N9	109.06(12)

N10(P4(N9	105.75(12)

N6(P5(N7	119.57(12)

N6(P5(Cl4	110.90(10)

N7(P5(Cl4	107.43(9)

N6(P5(Cl5	109.47(10)

N7(P5(Cl5	108.31(9)

Cl4(P5(Cl5	99.21(4)

N8(P6(O2	106.66(11)

N8(P6(N7	119.51(12)

O2(P6(N7	110.88(12)

N8(P6(Cl6	109.58(9)

O2(P6(Cl6	102.18(8)

N7(P6(Cl6	106.69(9)

N13(P7(N11	115.43(12)

N13(P7(N15	108.92(12)

N11(P7(N15	108.27(13)

N13(P7(N14	109.39(12)

N11(P7(N14	108.66(13)

N15(P7(N14	105.74(12)

N11(P8(N12	119.41(13)

N11(P8(Cl7	110.41(10)

N12(P8(Cl7	107.41(11)

N11(P8(Cl8	109.23(10)

N12(P8(Cl8	108.37(10)

Cl7(P8(Cl8	100.31(4)

O3(P9(N13	107.57(11)

O3(P9(N12	109.96(12)

N13(P9(N12	119.10(13)

O3(P9(Cl9	102.16(8)

N13(P9(Cl9	109.30(10)

N12(P9(Cl9	107.43(11)

N16(P10(N18	113.64(12)

N16(P10(N20	109.26(13)

N18(P10(N20	112.11(13)

N16(P10(N19	107.15(13)

N18(P10(N19	111.43(12)

N20(P10(N19	102.58(13)

N16(P11(N17	119.80(13)

N16(P11(Cl11	108.70(10)

N17(P11(Cl11	109.10(10)

N16(P11(Cl10	110.11(10)

N17(P11(Cl10	107.73(10)

Cl11(P11(Cl10	99.49(4)

N18(P12(O4	108.45(12)

N18(P12(N17	119.01(12)

O4(P12(N17	110.11(12)

N18(P12(Cl12	109.14(10)

O4(P12(Cl12	101.94(8)

N17(P12(Cl12	106.84(10)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	45(2) 	19(2)	38(2) 	1(1)	1(2) 	(2(1)

C2	28(1) 	34(2)	21(2) 	(7(1)	1(1) 	3(1)

C3	29(1) 	38(2)	14(1) 	(1(1)	2(1) 	3(1)

C4	32(2) 	31(2)	20(2) 	2(1)	3(1) 	(6(1)

C5	19(1) 	36(2)	18(1) 	6(1)	(4(1) 	(10(1)

C6	28(2) 	31(2)	31(2) 	(3(1)	(4(1) 	5(1)

C7	38(2) 	42(2)	23(2) 	(5(1)	2(1) 	1(1)

C8	31(2) 	41(2)	19(2) 	3(1)	(7(1) 	(4(1)

C9	24(2) 	82(3)	33(2) 	(5(2)	(7(1) 	13(2)

C10	24(2) 	95(3)	23(2) 	(3(2)	1(1) 	5(2)

C11	40(2) 	28(2)	28(2) 	(2(1)	2(1) 	(16(1)

C12	23(1) 	32(2)	19(1) 	4(1)	5(1) 	(4(1)

C13	23(1) 	38(2)	11(1) 	5(1)	1(1) 	(1(1)

C14	28(1) 	31(2)	14(1) 	(6(1)	1(1) 	2(1)

C15	14(1) 	30(2)	14(1) 	1(1)	1(1) 	(3(1)

C16	29(2) 	27(2)	23(2) 	2(1)	6(1) 	0(1)

C17	33(2) 	38(2)	32(2) 	11(1)	9(1) 	(1(1)

C18	28(2) 	49(2)	19(2) 	5(1)	5(1) 	(4(1)

C19	26(2) 	46(2)	24(2) 	(9(1)	7(1) 	2(1)

C20	20(1) 	31(2)	29(2) 	0(1)	3(1) 	4(1)

C21	33(2) 	32(2)	49(2) 	(4(2)	0(2) 	(9(1)

C22	26(1) 	47(2)	21(2) 	9(1)	2(1) 	(5(1)

C23	26(2) 	65(2)	15(1) 	(1(2)	2(1) 	1(2)

C24	26(1) 	47(2)	23(2) 	(13(1)	(4(1) 	7(1)

C25	18(1) 	38(2)	15(1) 	(2(1)	(1(1) 	(7(1)

C26	26(1) 	39(2)	24(2) 	0(1)	3(1) 	2(1)

C27	26(2) 	62(2)	29(2) 	(7(2)	9(1) 	(4(2)

C28	26(2) 	71(3)	22(2) 	4(2)	4(1) 	(10(2)

C29	31(2) 	52(2)	28(2) 	11(2)	(4(1) 	(11(2)

C30	23(1) 	35(2)	29(2) 	(1(1)	2(1) 	(5(1)

C31	58(2) 	21(2)	32(2) 	0(1)	(5(2) 	(4(1)

C32	28(2) 	32(2)	20(2) 	(5(1)	(1(1) 	5(1)

C33	34(2) 	30(2)	19(2) 	0(1)	1(1) 	1(1)

C34	34(2) 	25(2)	24(2) 	2(1)	1(1) 	(3(1)

C35	18(1) 	24(1)	21(1) 	3(1)	0(1) 	(9(1)

C36	20(1) 	40(2)	27(2) 	(8(1)	2(1) 	(4(1)

C37	34(2) 	53(2)	24(2) 	(11(2)	6(1) 	(18(2)

C38	42(2) 	47(2)	19(2) 	6(1)	(6(1) 	(22(2)

C39	29(2) 	36(2)	34(2) 	7(1)	(11(1) 	(9(1)

C40	19(1) 	34(2)	27(2) 	(1(1)	0(1) 	(3(1)

N1	20(1) 	27(1)	19(1) 	(2(1)	0(1) 	0(1)

N2	21(1) 	31(1)	16(1) 	0(1)	2(1) 	(4(1)

N3	17(1) 	33(1)	18(1) 	4(1)	0(1) 	(2(1)

N4	29(1) 	19(1)	20(1) 	(2(1)	1(1) 	(1(1)

N5	38(1) 	16(1)	19(1) 	(3(1)	2(1) 	(2(1)

N6	23(1) 	27(1)	16(1) 	1(1)	3(1) 	4(1)

N7	20(1) 	26(1)	16(1) 	4(1)	1(1) 	(1(1)

N8	20(1) 	25(1)	17(1) 	3(1)	1(1) 	3(1)

N9	26(1) 	21(1)	16(1) 	2(1)	2(1) 	(4(1)

N10	21(1) 	24(1)	17(1) 	0(1)	0(1) 	(3(1)

N11	22(1) 	33(1)	19(1) 	(1(1)	1(1) 	7(1)

N12	23(1) 	48(2)	17(1) 	12(1)	1(1) 	4(1)

N13	20(1) 	25(1)	15(1) 	2(1)	1(1) 	5(1)

N14	23(1) 	25(1)	21(1) 	1(1)	1(1) 	(3(1)

N15	21(1) 	23(1)	20(1) 	(3(1)	0(1) 	3(1)

N16	16(1) 	32(1)	23(1) 	2(1)	(1(1) 	(1(1)

N17	17(1) 	35(1)	16(1) 	(2(1)	0(1) 	(1(1)

N18	16(1) 	29(1)	16(1) 	1(1)	3(1) 	2(1)

N19	30(1) 	18(1)	21(1) 	0(1)	(4(1) 	(1(1)

N20	33(1) 	16(1)	21(1) 	(1(1)	0(1) 	2(1)

O1	24(1) 	42(1)	22(1) 	11(1)	(6(1) 	(13(1)

O2	18(1) 	30(1)	14(1) 	2(1)	2(1) 	(3(1)

O3	20(1) 	32(1)	15(1) 	(2(1)	1(1) 	(4(1)

O4	18(1) 	32(1)	16(1) 	3(1)	(1(1) 	(5(1)

P1	20(1) 	20(1)	15(1) 	(1(1)	0(1) 	(2(1)

P2	18(1) 	23(1)	17(1) 	(1(1)	2(1) 	0(1)

P3	16(1) 	27(1)	17(1) 	5(1)	0(1) 	(3(1)

P4	19(1) 	18(1)	13(1) 	1(1)	0(1) 	(1(1)

P5	17(1) 	20(1)	16(1) 	0(1)	(1(1) 	(1(1)

P6	18(1) 	20(1)	14(1) 	1(1)	1(1) 	(1(1)

P7	18(1) 	20(1)	14(1) 	(1(1)	0(1) 	2(1)

P8	18(1) 	21(1)	21(1) 	2(1)	(4(1) 	1(1)

P9	18(1) 	24(1)	14(1) 	(1(1)	0(1) 	(2(1)

P10	19(1) 	19(1)	17(1) 	1(1)	(2(1) 	1(1)

P11	16(1) 	24(1)	21(1) 	(1(1)	1(1) 	0(1)

P12	16(1) 	23(1)	16(1) 	2(1)	(1(1) 	(1(1)

Cl1	23(1) 	25(1)	32(1) 	1(1)	4(1) 	(3(1)

Cl2	33(1) 	26(1)	28(1) 	(3(1)	8(1) 	7(1)

Cl3	29(1) 	30(1)	33(1) 	7(1)	0(1) 	5(1)

Cl4	31(1) 	22(1)	32(1) 	2(1)	(3(1) 	5(1)

Cl5	24(1) 	41(1)	27(1) 	(9(1)	(3(1) 	(9(1)

Cl6	36(1) 	24(1)	26(1) 	(7(1)	4(1) 	(5(1)

Cl7	38(1) 	19(1)	78(1) 	5(1)	(23(1) 	(1(1)

Cl8	22(1) 	30(1)	25(1) 	(6(1)	(5(1) 	(3(1)

Cl9	44(1) 	36(1)	26(1) 	(13(1)	7(1) 	(15(1)

Cl10	28(1) 	25(1)	35(1) 	5(1)	(1(1) 	(5(1)

Cl11	26(1) 	29(1)	34(1) 	(1(1)	9(1) 	5(1)

Cl12	31(1) 	24(1)	29(1) 	5(1)	(4(1) 	2(1)