|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement details.

Identification code 	2007src0902r

Empirical formula 	C18H11ClFeN2

Formula weight 	346.59

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/c

Unit cell dimensions	a = 7.3730(5) Å	( = 90°

b = 13.2476(10) Å	( = 93.123(4)°

c = 30.324(2) Å	(  = 90°

Volume	2957.5(4) Å3

Z	8

Density (calculated)	1.557 Mg / m3

Absorption coefficient	1.196 mm(1

F(000)	1408

Crystal	Plate; Orange

Crystal size	0.27 ( 0.14 ( 0.01 mm3

( range for data collection	3.01 ( 25.03°

Index ranges	(8 ( h ( 8, (15 ( k ( 15, (36 ( l ( 35

Reflections collected	23330

Independent reflections	5192 [Rint = 0.0925]

Completeness to ( = 25.03°	99.3 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.7456 and 0.6272

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	5192 / 0 / 397

Goodness-of-fit on F2	1.063

Final R indices [F2 > 2((F2)]	R1 = 0.0617, wR2 = 0.1066

R indices (all data)	R1 = 0.1121, wR2 = 0.1245

Largest diff. peak and hole	0.470 and (0.507 e Å(3

Diffractometer: Bruker-Nonius APEX II CCD camera (( scans and ( scans to fill asymmetric unit). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: Sheldrick, G. M. SADABS 2007/2 - Bruker Nonius area detector scaling and absorption correction. Structure solution: Sir2004 (Burla, M.C., Caliandro, R., Carrozzini, B., Cascarano, G., De Caro, L., Giacovazzo, C. & Polidori, G. (2004). J. Appl. Cryst. 37, 258).  Structure refinement: SHELXL97 (Sheldrick, G. M. (1997). University of Göttingen, Germany). Graphics: PLATON/PLUTON  (Spek, A. L. (1990). Acta Cryst. A46, C34).

Special details:

The hydrogen atoms were fixed as riding models.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	1488(6)	2266(4)	6094(2)	20(1)	1

C2	1053(7)	2364(4)	5630(2)	23(1)	1

C3	2053(7)	1629(4)	5406(2)	25(1)	1

C4	3070(6)	1051(4)	5726(2)	31(1)	1

C5	2730(6)	1433(4)	6150(2)	24(1)	1

C6	(2368(7)	768(4)	5789(2)	29(1)	1

C7	(1555(6)	197(4)	5459(2)	20(1)	1

C8	(334(7)	(509(4)	5673(2)	24(1)	1

C9	(402(7)	(366(4)	6133(2)	28(1)	1

C10	(1672(7)	414(4)	6206(2)	34(2)	1

C11	845(6)	2876(4)	6459(2)	20(1)	1

C12	630(6)	3942(4)	6439(2)	21(1)	1

C13	82(6)	4498(4)	6792(2)	22(1)	1

C14	(260(6)	4011(4)	7181(2)	23(1)	1

C15	(29(7)	2953(4)	7219(2)	26(1)	1

C16	501(7)	2415(4)	6859(2)	23(1)	1

C17	(873(7)	4586(4)	7551(2)	27(1)	1

C18	(369(7)	2439(4)	7628(2)	29(1)	1

N1	(1409(6)	5038(3)	7841(2)	33(1)	1

N2	(624(7)	2030(4)	7951(2)	40(1)	1

Cl1	1119(2)	4611(1)	5965(1)	28(1)	1

Fe1	381(1)	946(1)	5833(1)	20(1)	1

C101	6395(6)	5672(4)	6019(2)	20(1)	1

C102	7546(6)	6552(4)	6060(2)	21(1)	1

C103	7989(6)	6844(4)	5631(2)	28(1)	1

C104	7121(7)	6185(4)	5317(2)	28(1)	1

C105	6127(7)	5469(4)	5558(2)	27(1)	1

C106	2799(7)	7245(4)	5928(2)	31(1)	1

C107	3993(7)	8083(4)	5978(2)	29(1)	1

C108	4521(7)	8349(4)	5548(2)	32(1)	1

C109	3638(8)	7689(5)	5241(2)	38(2)	1

C110	2590(7)	7009(4)	5477(2)	33(2)	1

C111	5722(6)	5131(4)	6398(2)	21(1)	1

C112	5619(6)	4081(4)	6426(2)	19(1)	1

C113	5151(6)	3592(4)	6804(2)	22(1)	1

C114	4737(6)	4121(4)	7176(2)	22(1)	1

C115	4783(6)	5194(4)	7158(2)	22(1)	1

C116	5272(6)	5669(4)	6775(2)	22(1)	1

C117	4302(7)	3618(4)	7575(2)	26(1)	1

C118	4350(7)	5777(4)	7543(2)	27(1)	1

N101	3969(6)	3186(4)	7892(2)	37(1)	1

N102	4014(7)	6219(4)	7850(2)	39(1)	1

Cl11	6215(2)	3321(1)	5988(1)	29(1)	1

Fe11	5253(1)	6895(1)	5684(1)	21(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(C5	1.437(7)

C1(C2	1.435(7)

C1(C11	1.468(7)

C1(Fe1	2.069(5)

C2(C3	1.416(7)

C2(Fe1	2.046(5)

C2(H2	0.9500

C3(C4	1.416(7)

C3(Fe1	2.045(5)

C3(H3	0.9500

C4(C5	1.417(7)

C4(Fe1	2.031(5)

C4(H4	0.9500

C5(Fe1	2.039(5)

C5(H5	0.9500

C6(C7	1.416(7)

C6(C10	1.418(8)

C6(Fe1	2.038(5)

C6(H6	0.9500

C7(C8	1.429(7)

C7(Fe1	2.033(5)

C7(H7	0.9500

C8(C9	1.412(7)

C8(Fe1	2.050(5)

C8(H8	0.9500

C9(C10	1.420(8)

C9(Fe1	2.059(5)

C9(H9	0.9500

C10(Fe1	2.064(5)

C10(H10	0.9500

C11(C16	1.393(7)

C11(C12	1.423(7)

C12(C13	1.376(7)

C12(Cl1	1.743(5)

C13(C14	1.381(7)

C13(H13	0.9500

C14(C15	1.415(7)

C14(C17	1.448(7)

C15(C16	1.377(7)

C15(C18	1.452(8)

C16(H16	0.9500

C17(N1	1.152(6)

C18(N2	1.143(7)

C101(C105	1.426(7)

C101(C102	1.444(7)

C101(C111	1.465(7)

C101(Fe11	2.067(5)

C102(C103	1.409(7)

C102(Fe11	2.037(5)

C102(H102	0.9500

C103(C104	1.419(7)

C103(Fe11	2.033(5)

C103(H103	0.9500

C104(C105	1.424(7)

C104(Fe11	2.046(5)

C104(H104	0.9500

C105(Fe11	2.039(5)

C105(H105	0.9500

C106(C110	1.403(7)

C106(C107	1.420(7)

C106(Fe11	2.045(5)

C106(H106	0.9500

C107(C108	1.425(7)

C107(Fe11	2.056(5)

C107(H107	0.9500

C108(C109	1.413(8)

C108(Fe11	2.036(5)

C108(H108	0.9500

C109(C110	1.408(8)

C109(Fe11	2.039(6)

C109(H109	0.9500

C110(Fe11	2.034(5)

C110(H110	0.9500

C111(C112	1.395(7)

C111(C116	1.402(7)

C112(C113	1.378(7)

C112(Cl11	1.743(5)

C113(C114	1.375(7)

C113(H113	0.9500

C114(C115	1.423(7)

C114(C117	1.434(7)

C115(C116	1.384(7)

C115(C118	1.452(7)

C116(H116	0.9500

C117(N101	1.155(6)

C118(N102	1.138(6)

C5(C1(C2	106.9(4)

C5(C1(C11	124.3(5)

C2(C1(C11	128.7(5)

C5(C1(Fe1	68.4(3)

C2(C1(Fe1	68.7(3)

C11(C1(Fe1	128.1(3)

C3(C2(C1	108.2(5)

C3(C2(Fe1	69.7(3)

C1(C2(Fe1	70.5(3)

C3(C2(H2	125.9

C1(C2(H2	125.9

Fe1(C2(H2	125.5

C4(C3(C2	108.4(5)

C4(C3(Fe1	69.1(3)

C2(C3(Fe1	69.8(3)

C4(C3(H3	125.8

C2(C3(H3	125.8

Fe1(C3(H3	126.8

C3(C4(C5	108.3(5)

C3(C4(Fe1	70.2(3)

C5(C4(Fe1	69.9(3)

C3(C4(H4	125.8

C5(C4(H4	125.8

Fe1(C4(H4	125.6

C4(C5(C1	108.1(5)

C4(C5(Fe1	69.3(3)

C1(C5(Fe1	70.6(3)

C4(C5(H5	125.9

C1(C5(H5	125.9

Fe1(C5(H5	125.7

C7(C6(C10	108.0(5)

C7(C6(Fe1	69.5(3)

C10(C6(Fe1	70.8(3)

C7(C6(H6	126.0

C10(C6(H6	126.0

Fe1(C6(H6	125.3

C6(C7(C8	107.9(5)

C6(C7(Fe1	69.8(3)

C8(C7(Fe1	70.1(3)

C6(C7(H7	126.0

C8(C7(H7	126.0

Fe1(C7(H7	125.6

C9(C8(C7	107.8(5)

C9(C8(Fe1	70.3(3)

C7(C8(Fe1	68.9(3)

C9(C8(H8	126.1

C7(C8(H8	126.1

Fe1(C8(H8	126.3

C8(C9(C10	108.1(5)

C8(C9(Fe1	69.5(3)

C10(C9(Fe1	70.0(3)

C8(C9(H9	125.9

C10(C9(H9	125.9

Fe1(C9(H9	126.1

C9(C10(C6	108.1(5)

C9(C10(Fe1	69.7(3)

C6(C10(Fe1	68.8(3)

C9(C10(H10	125.9

C6(C10(H10	125.9

Fe1(C10(H10	127.1

C16(C11(C12	116.5(5)

C16(C11(C1	119.7(4)

C12(C11(C1	123.7(5)

C13(C12(C11	122.4(5)

C13(C12(Cl1	116.9(4)

C11(C12(Cl1	120.8(4)

C12(C13(C14	119.3(5)

C12(C13(H13	120.4

C14(C13(H13	120.4

C13(C14(C15	120.3(5)

C13(C14(C17	119.8(5)

C15(C14(C17	120.0(5)

C16(C15(C14	119.2(5)

C16(C15(C18	120.3(5)

C14(C15(C18	120.5(5)

C15(C16(C11	122.4(5)

C15(C16(H16	118.8

C11(C16(H16	118.8

N1(C17(C14	178.2(6)

N2(C18(C15	179.5(6)

C4(Fe1(C7	127.3(2)

C4(Fe1(C6	166.8(2)

C7(Fe1(C6	40.70(19)

C4(Fe1(C5	40.7(2)

C7(Fe1(C5	165.9(2)

C6(Fe1(C5	152.1(2)

C4(Fe1(C3	40.6(2)

C7(Fe1(C3	107.0(2)

C6(Fe1(C3	129.9(2)

C5(Fe1(C3	68.4(2)

C4(Fe1(C2	68.5(2)

C7(Fe1(C2	117.0(2)

C6(Fe1(C2	110.1(2)

C5(Fe1(C2	68.8(2)

C3(Fe1(C2	40.49(19)

C4(Fe1(C8	105.5(2)

C7(Fe1(C8	40.98(19)

C6(Fe1(C8	68.5(2)

C5(Fe1(C8	127.6(2)

C3(Fe1(C8	115.0(2)

C2(Fe1(C8	148.8(2)

C4(Fe1(C9	115.3(2)

C7(Fe1(C9	68.3(2)

C6(Fe1(C9	68.2(2)

C5(Fe1(C9	108.1(2)

C3(Fe1(C9	147.7(2)

C2(Fe1(C9	170.5(2)

C8(Fe1(C9	40.2(2)

C4(Fe1(C10	149.6(3)

C7(Fe1(C10	68.0(2)

C6(Fe1(C10	40.5(2)

C5(Fe1(C10	118.6(2)

C3(Fe1(C10	169.6(2)

C2(Fe1(C10	132.5(2)

C8(Fe1(C10	67.8(2)

C9(Fe1(C10	40.3(2)

C4(Fe1(C1	68.6(2)

C7(Fe1(C1	151.2(2)

C6(Fe1(C1	119.5(2)

C5(Fe1(C1	40.95(19)

C3(Fe1(C1	68.3(2)

C2(Fe1(C1	40.80(19)

C8(Fe1(C1	167.5(2)

C9(Fe1(C1	131.2(2)

C10(Fe1(C1	111.4(2)

C105(C101(C102	106.6(4)

C105(C101(C111	130.0(5)

C102(C101(C111	123.4(5)

C105(C101(Fe11	68.6(3)

C102(C101(Fe11	68.3(3)

C111(C101(Fe11	128.5(3)

C103(C102(C101	107.9(5)

C103(C102(Fe11	69.6(3)

C101(C102(Fe11	70.5(3)

C103(C102(H102	126.1

C101(C102(H102	126.1

Fe11(C102(H102	125.4

C102(C103(C104	109.4(5)

C102(C103(Fe11	69.9(3)

C104(C103(Fe11	70.1(3)

C102(C103(H103	125.3

C104(C103(H103	125.3

Fe11(C103(H103	126.2

C103(C104(C105	106.9(5)

C103(C104(Fe11	69.2(3)

C105(C104(Fe11	69.3(3)

C103(C104(H104	126.5

C105(C104(H104	126.5

Fe11(C104(H104	126.5

C104(C105(C101	109.2(5)

C104(C105(Fe11	69.8(3)

C101(C105(Fe11	70.7(3)

C104(C105(H105	125.4

C101(C105(H105	125.4

Fe11(C105(H105	125.6

C110(C106(C107	108.2(5)

C110(C106(Fe11	69.5(3)

C107(C106(Fe11	70.1(3)

C110(C106(H106	125.9

C107(C106(H106	125.9

Fe11(C106(H106	126.1

C106(C107(C108	107.1(5)

C106(C107(Fe11	69.3(3)

C108(C107(Fe11	68.9(3)

C106(C107(H107	126.4

C108(C107(H107	126.4

Fe11(C107(H107	126.9

C109(C108(C107	108.2(5)

C109(C108(Fe11	69.8(3)

C107(C108(Fe11	70.4(3)

C109(C108(H108	125.9

C107(C108(H108	125.9

Fe11(C108(H108	125.5

C110(C109(C108	107.8(5)

C110(C109(Fe11	69.6(3)

C108(C109(Fe11	69.6(3)

C110(C109(H109	126.1

C108(C109(H109	126.1

Fe11(C109(H109	126.2

C106(C110(C109	108.7(5)

C106(C110(Fe11	70.3(3)

C109(C110(Fe11	70.0(3)

C106(C110(H110	125.7

C109(C110(H110	125.7

Fe11(C110(H110	125.7

C112(C111(C116	116.2(5)

C112(C111(C101	123.9(5)

C116(C111(C101	119.8(5)

C113(C112(C111	122.4(5)

C113(C112(Cl11	116.6(4)

C111(C112(Cl11	120.8(4)

C114(C113(C112	121.3(5)

C114(C113(H113	119.4

C112(C113(H113	119.4

C113(C114(C115	118.0(5)

C113(C114(C117	121.7(5)

C115(C114(C117	120.3(5)

C116(C115(C114	119.7(5)

C116(C115(C118	120.8(5)

C114(C115(C118	119.5(5)

C115(C116(C111	122.4(5)

C115(C116(H116	118.8

C111(C116(H116	118.8

N101(C117(C114	177.9(6)

N102(C118(C115	178.8(6)

C103(Fe11(C110	157.4(2)

C103(Fe11(C108	105.6(2)

C110(Fe11(C108	68.1(2)

C103(Fe11(C109	120.8(2)

C110(Fe11(C109	40.5(2)

C108(Fe11(C109	40.6(2)

C103(Fe11(C102	40.5(2)

C110(Fe11(C102	161.2(2)

C108(Fe11(C102	121.8(2)

C109(Fe11(C102	157.0(2)

C103(Fe11(C105	68.2(2)

C110(Fe11(C105	108.7(2)

C108(Fe11(C105	157.1(2)

C109(Fe11(C105	122.2(2)

C102(Fe11(C105	68.7(2)

C103(Fe11(C104	40.7(2)

C110(Fe11(C104	122.2(2)

C108(Fe11(C104	120.2(2)

C109(Fe11(C104	105.3(2)

C102(Fe11(C104	68.8(2)

C105(Fe11(C104	40.8(2)

C103(Fe11(C106	159.6(2)

C110(Fe11(C106	40.2(2)

C108(Fe11(C106	68.2(2)

C109(Fe11(C106	68.0(2)

C102(Fe11(C106	124.9(2)

C105(Fe11(C106	124.9(2)

C104(Fe11(C106	159.4(2)

C103(Fe11(C107	122.2(2)

C110(Fe11(C107	68.0(2)

C108(Fe11(C107	40.8(2)

C109(Fe11(C107	68.3(2)

C102(Fe11(C107	108.0(2)

C105(Fe11(C107	161.0(2)

C104(Fe11(C107	157.1(2)

C106(Fe11(C107	40.5(2)

C103(Fe11(C101	68.5(2)

C110(Fe11(C101	124.8(2)

C108(Fe11(C101	159.6(2)

C109(Fe11(C101	159.3(2)

C102(Fe11(C101	41.18(19)

C105(Fe11(C101	40.64(19)

C104(Fe11(C101	68.8(2)

C106(Fe11(C101	110.2(2)

C107(Fe11(C101	124.7(2)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	20(3) 	21(3)	19(3) 	0(2)	(4(2) 	(8(2)

C2	25(3) 	10(3)	33(3) 	(3(2)	1(2) 	(5(2)

C3	29(3) 	21(3)	26(3) 	(6(2)	9(2) 	(12(3)

C4	11(3) 	27(3)	56(4) 	(13(3)	11(3) 	(8(2)

C5	18(3) 	21(3)	33(4) 	(2(3)	(5(2) 	(1(2)

C6	13(3) 	25(3)	51(4) 	(7(3)	10(3) 	(9(2)

C7	20(3) 	16(3)	24(3) 	0(2)	(2(2) 	(5(2)

C8	21(3) 	16(3)	34(4) 	(9(3)	2(2) 	(8(2)

C9	38(3) 	22(3)	25(3) 	7(3)	0(3) 	(15(3)

C10	35(3) 	37(4)	31(4) 	(16(3)	19(3) 	(23(3)

C11	14(3) 	24(3)	22(3) 	(1(2)	(3(2) 	1(2)

C12	15(3) 	22(3)	25(3) 	0(2)	(1(2) 	(1(2)

C13	22(3) 	15(3)	29(3) 	(4(2)	(5(2) 	2(2)

C14	21(3) 	29(3)	19(3) 	(10(3)	0(2) 	0(2)

C15	31(3) 	22(3)	23(3) 	1(3)	(5(2) 	(8(3)

C16	30(3) 	17(3)	23(3) 	(4(2)	(5(2) 	1(2)

C17	28(3) 	24(3)	26(4) 	1(3)	(8(3) 	(8(3)

C18	33(3) 	21(3)	34(4) 	(6(3)	(4(3) 	1(3)

N1	40(3) 	29(3)	31(3) 	(9(2)	(1(2) 	2(2)

N2	55(3) 	35(3)	30(3) 	2(3)	2(3) 	(2(3)

Cl1	32(1) 	22(1)	30(1) 	3(1)	2(1) 	0(1)

Fe1	17(1) 	20(1)	23(1) 	(2(1)	2(1) 	(3(1)

C101	17(3) 	16(3)	27(3) 	0(2)	(2(2) 	4(2)

C102	17(3) 	17(3)	29(3) 	(1(2)	(5(2) 	0(2)

C103	15(3) 	26(3)	43(4) 	7(3)	5(2) 	2(2)

C104	28(3) 	33(3)	26(3) 	5(3)	12(3) 	7(3)

C105	23(3) 	27(3)	31(4) 	1(3)	4(2) 	2(3)

C106	21(3) 	34(4)	38(4) 	17(3)	14(3) 	10(3)

C107	27(3) 	22(3)	39(4) 	(10(3)	(3(3) 	12(3)

C108	25(3) 	22(3)	50(4) 	7(3)	11(3) 	7(3)

C109	38(4) 	44(4)	32(4) 	12(3)	7(3) 	16(3)

C110	16(3) 	39(4)	43(4) 	(4(3)	(9(3) 	6(3)

C111	15(3) 	25(3)	22(3) 	0(2)	(3(2) 	0(2)

C112	15(3) 	21(3)	21(3) 	0(2)	(3(2) 	(1(2)

C113	21(3) 	19(3)	25(3) 	7(3)	(8(2) 	(2(2)

C114	20(3) 	26(3)	21(3) 	0(3)	(1(2) 	(1(2)

C115	22(3) 	24(3)	20(3) 	(2(2)	(3(2) 	4(2)

C116	23(3) 	17(3)	26(3) 	0(2)	(5(2) 	(2(2)

C117	26(3) 	20(3)	32(4) 	(1(3)	(2(3) 	(5(3)

C118	30(3) 	28(3)	22(3) 	6(3)	0(3) 	(1(3)

N101	45(3) 	32(3)	34(3) 	10(3)	1(2) 	(5(2)

N102	52(3) 	36(3)	29(3) 	(1(3)	8(3) 	(2(3)

Cl11	35(1) 	20(1)	33(1) 	(6(1)	5(1) 	(1(1)

Fe11	17(1) 	20(1)	25(1) 	2(1)	1(1) 	1(1)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H2	234	2840	5495	27	1

H3	2044	1538	5096	30	1

H4	3847	502	5666	37	1

H5	3236	1183	6423	29	1

H6	(3229	1295	5741	35	1

H7	(1780	270	5149	24	1

H8	394	(989	5531	29	1

H9	284	(729	6355	34	1

H10	(1999	656	6486	40	1

H13	(58	5209	6767	27	1

H16	636	1704	6885	28	1

H102	7936	6878	6327	26	1

H103	8749	7395	5564	33	1

H104	7189	6216	5006	34	1

H105	5401	4940	5432	33	1

H106	2238	6903	6160	37	1

H107	4369	8406	6248	35	1

H108	5327	8879	5481	38	1

H109	3733	7700	4930	45	1

H110	1862	6479	5353	40	1

H113	5113	2875	6809	26	1

H116	5304	6385	6768	26	1