|  | University of Southampton · Department of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	02src141

Empirical formula 	C14H24N3O5

Formula weight 	314.36

Temperature 	293(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/c

Unit cell dimensions	a = 19.380(2) Å

b = 13.2761(11) Å	( = 91.600(3)°

c = 13.0097(11) Å

Volume	3346.0(5) Å3

Z	8

Density (calculated)	1.248 Mg / m3

Absorption coefficient	0.095 mm(1

F(000)	1352

Crystal	Colourless Block

Crystal size	0.20 ( 0.20 ( 0.15 mm3

( range for data collection	3.15 ( 25.03°

Index ranges	(23 ( h ( 20, (15 ( k ( 15, (15 ( l ( 15

Reflections collected	15984

Independent reflections	5259 [Rint = 0.1193]

Completeness to ( = 25.03°	89.0 %

Max. and min. transmission	0.9859 and 0.9813

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	5259 / 0 / 411

Goodness-of-fit on F2	1.013

Final R indices [F2 > 2((F2)]	R1 = 0.0849, wR2 = 0.2158

R indices (all data)	R1 = 0.1774, wR2 = 0.2612

Largest diff. peak and hole	0.601 and (0.501 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:  All hydrogen atoms were placed in idealised positions and refined using a riding model.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

N1	354(2)	4269(3)	3389(3)	36(1)	1

N2	343(2)	5733(3)	2578(3)	37(1)	1

N3	969(2)	5628(3)	4183(3)	33(1)	1

O1	(1010(2)	5016(3)	3683(3)	45(1)	1

O2	260(2)	2621(3)	3795(3)	41(1)	1

O3	1122(2)	3564(3)	4511(3)	36(1)	1

O4	1042(2)	7196(3)	3376(3)	39(1)	1

O5	1561(2)	6868(2)	4917(3)	37(1)	1

C1	(905(3)	4139(4)	3100(4)	36(1)	1

C2	(215(3)	4170(4)	2605(4)	34(1)	1

C3	(115(3)	5105(4)	1944(4)	42(1)	1

C4	585(2)	5265(4)	3416(4)	30(1)	1

C5	564(3)	3411(4)	3926(4)	36(1)	1

C6	1405(3)	2736(4)	5163(4)	35(1)	1

C7	892(3)	2453(5)	5955(5)	49(2)	1

C8	1612(3)	1856(4)	4507(5)	47(2)	1

C9	2042(3)	3206(4)	5652(4)	45(2)	1

C10	1172(3)	6616(4)	4081(4)	33(1)	1

C11	1832(3)	7908(4)	5039(4)	38(1)	1

C12	1232(3)	8649(4)	5050(5)	48(2)	1

C13	2341(3)	8129(5)	4218(5)	54(2)	1

C14	2187(4)	7879(5)	6079(5)	55(2)	1

N4	4490(2)	6604(3)	9353(3)	33(1)	1

N5	4492(2)	7290(3)	10891(4)	40(1)	1

N6	3920(2)	5716(3)	10676(3)	35(1)	1

O6	5861(2)	6284(3)	10140(3)	48(1)	1

O7	4585(2)	6309(3)	7654(3)	41(1)	1

O8	3781(2)	5482(3)	8554(3)	34(1)	1

O9	3858(3)	6360(4)	12336(3)	77(2)	1

O10	3383(2)	4901(3)	11899(3)	54(1)	1

C15	5738(3)	6904(4)	9273(4)	41(1)	1

C16	5033(3)	7382(4)	9312(4)	37(1)	1

C17	4916(3)	7966(4)	10297(4)	42(1)	1

C18	4269(3)	6496(4)	10359(4)	34(1)	1

C19	4297(3)	6115(4)	8446(4)	35(1)	1

C20	3524(3)	4887(4)	7657(4)	39(1)	1

C21	3227(3)	5581(5)	6840(4)	48(2)	1

C22	2953(3)	4262(4)	8126(4)	46(2)	1

C23	4084(3)	4220(5)	7276(5)	52(2)	1

C24	3737(3)	5720(4)	11688(4)	37(1)	1

C25	3158(4)	4682(5)	12953(5)	56(2)	1

C26	2632(4)	5367(9)	13259(6)	118(4)	1

C27	2885(13)	3650(11)	12819(10)	331(17)	1

C28	3741(5)	4685(12)	13678(7)	177(7)	1

Table 3. Bond lengths [Å] and angles [°].

N1(C5	1.391(7)

N1(C4	1.396(7)

N1(C2	1.487(7)

N2(C4	1.329(6)

N2(C3	1.457(7)

N3(C4	1.319(6)

N3(C10	1.377(7)

O1(C1	1.407(6)

O2(C5	1.213(6)

O3(C5	1.320(6)

O3(C6	1.483(6)

O4(C10	1.219(6)

O5(C10	1.348(6)

O5(C11	1.484(6)

C1(C2	1.501(8)

C2(C3	1.526(8)

C6(C7	1.499(8)

C6(C8	1.508(8)

C6(C9	1.508(8)

C11(C14	1.500(8)

C11(C13	1.502(8)

C11(C12	1.524(8)

N4(C19	1.388(7)

N4(C18	1.396(7)

N4(C16	1.477(7)

N5(C18	1.327(7)

N5(C17	1.453(7)

N6(C18	1.310(7)

N6(C24	1.372(7)

O6(C15	1.410(6)

O7(C19	1.213(6)

O8(C19	1.317(6)

O8(C20	1.483(6)

O9(C24	1.216(7)

O10(C24	1.319(6)

O10(C25	1.480(7)

C15(C16	1.510(8)

C16(C17	1.519(8)

C20(C23	1.496(8)

C20(C21	1.508(8)

C20(C22	1.523(8)

C25(C26	1.432(10)

C25(C28	1.452(12)

C25(C27	1.478(12)

C5(N1(C4	132.3(4)

C5(N1(C2	118.2(4)

C4(N1(C2	109.4(4)

C4(N2(C3	113.1(4)

C4(N3(C10	115.6(4)

C5(O3(C6	120.0(4)

C10(O5(C11	120.4(4)

O1(C1(C2	110.6(4)

N1(C2(C1	111.2(4)

N1(C2(C3	102.2(4)

C1(C2(C3	113.2(5)

N2(C3(C2	103.4(4)

N3(C4(N2	128.9(5)

N3(C4(N1	122.6(5)

N2(C4(N1	108.5(4)

O2(C5(O3	126.9(5)

O2(C5(N1	120.3(5)

O3(C5(N1	112.8(5)

O3(C6(C7	109.7(4)

O3(C6(C8	110.5(4)

C7(C6(C8	112.7(5)

O3(C6(C9	102.7(4)

C7(C6(C9	111.4(5)

C8(C6(C9	109.4(5)

O4(C10(O5	123.4(5)

O4(C10(N3	128.3(5)

O5(C10(N3	108.3(4)

O5(C11(C14	103.0(4)

O5(C11(C13	110.1(5)

C14(C11(C13	110.7(5)

O5(C11(C12	109.5(4)

C14(C11(C12	109.8(5)

C13(C11(C12	113.3(5)

C19(N4(C18	131.8(4)

C19(N4(C16	118.1(4)

C18(N4(C16	110.1(4)

C18(N5(C17	113.3(4)

C18(N6(C24	116.6(5)

C19(O8(C20	119.7(4)

C24(O10(C25	121.6(5)

O6(C15(C16	110.6(5)

N4(C16(C15	110.7(4)

N4(C16(C17	101.8(4)

C15(C16(C17	113.5(5)

N5(C17(C16	103.5(4)

N6(C18(N5	128.9(5)

N6(C18(N4	123.4(5)

N5(C18(N4	107.6(5)

O7(C19(O8	126.4(5)

O7(C19(N4	120.2(5)

O8(C19(N4	113.3(5)

O8(C20(C23	110.2(4)

O8(C20(C21	110.0(4)

C23(C20(C21	113.2(5)

O8(C20(C22	101.9(4)

C23(C20(C22	110.6(5)

C21(C20(C22	110.4(5)

O9(C24(O10	121.5(5)

O9(C24(N6	128.2(5)

O10(C24(N6	110.2(5)

C26(C25(C28	111.5(8)

C26(C25(C27	111.5(12)

C28(C25(C27	110.4(13)

C26(C25(O10	111.3(6)

C28(C25(O10	111.0(6)

C27(C25(O10	100.7(6)

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

N1	40(3) 	31(3)	37(3) 	2(2)	(3(2) 	(2(2)

N2	46(3) 	38(3)	26(2) 	2(2)	(3(2) 	(3(2)

N3	38(3) 	27(2)	34(3) 	1(2)	0(2) 	(5(2)

O1	62(3) 	35(2)	37(2) 	(3(2)	7(2) 	5(2)

O2	44(2) 	34(2)	42(2) 	0(2)	(4(2) 	(6(2)

O3	39(2) 	31(2)	36(2) 	(1(2)	(1(2) 	1(2)

O4	50(2) 	34(2)	34(2) 	6(2)	(4(2) 	(6(2)

O5	45(2) 	27(2)	37(2) 	0(2)	(2(2) 	(8(2)

C1	43(4) 	30(3)	36(3) 	(3(3)	1(3) 	(4(2)

C2	44(4) 	28(3)	31(3) 	(1(3)	0(3) 	(1(2)

C3	56(4) 	38(3)	33(3) 	(2(3)	(1(3) 	(5(3)

C4	28(3) 	32(3)	30(3) 	2(3)	7(2) 	(2(2)

C5	38(3) 	33(3)	37(3) 	(7(3)	4(3) 	2(3)

C6	41(3) 	30(3)	33(3) 	8(3)	(3(3) 	3(2)

C7	54(4) 	48(4)	45(3) 	9(3)	6(3) 	2(3)

C8	49(4) 	36(3)	55(4) 	(8(3)	(2(3) 	7(3)

C9	56(4) 	41(3)	39(3) 	(6(3)	(6(3) 	10(3)

C10	32(3) 	30(3)	36(3) 	(2(3)	(1(3) 	4(2)

C11	51(4) 	28(3)	34(3) 	1(3)	(2(3) 	(6(3)

C12	65(4) 	33(3)	44(3) 	(8(3)	2(3) 	1(3)

C13	56(4) 	55(4)	51(4) 	2(3)	5(3) 	(16(3)

C14	76(5) 	43(4)	43(4) 	4(3)	(15(3) 	(13(3)

N4	42(3) 	29(2)	28(3) 	1(2)	6(2) 	(4(2)

N5	47(3) 	28(3)	44(3) 	(8(2)	1(2) 	(5(2)

N6	44(3) 	33(3)	29(3) 	7(2)	3(2) 	0(2)

O6	66(3) 	37(2)	40(2) 	1(2)	(2(2) 	7(2)

O7	52(2) 	39(2)	32(2) 	6(2)	10(2) 	(1(2)

O8	41(2) 	30(2)	32(2) 	0(2)	4(2) 	(6(2)

O9	115(4) 	74(3)	43(3) 	(12(3)	29(3) 	(52(3)

O10	87(3) 	44(2)	34(2) 	(3(2)	25(2) 	(22(2)

C15	44(4) 	45(3)	35(3) 	8(3)	(2(3) 	(5(3)

C16	43(4) 	32(3)	34(3) 	3(3)	3(2) 	(7(3)

C17	51(4) 	33(3)	41(3) 	(1(3)	5(3) 	(9(3)

C18	37(3) 	32(3)	32(3) 	2(3)	(1(2) 	3(3)

C19	41(3) 	34(3)	30(3) 	0(3)	(2(3) 	3(3)

C20	53(4) 	37(3)	27(3) 	(9(3)	(4(3) 	(5(3)

C21	59(4) 	51(4)	34(3) 	2(3)	0(3) 	(5(3)

C22	60(4) 	39(3)	37(3) 	(7(3)	(9(3) 	(9(3)

C23	71(4) 	40(4)	47(4) 	(10(3)	10(3) 	(1(3)

C24	41(3) 	32(3)	38(4) 	(2(3)	6(3) 	(1(3)

C25	90(5) 	39(4)	40(4) 	(4(3)	24(4) 	(15(3)

C26	77(6) 	199(11)	80(6) 	69(7)	48(5) 	73(7)

C27	700(40) 	186(14)	122(10) 	(92(10)	245(18) 	(300(20)

C28	99(7) 	348(19)	87(6) 	138(10)	51(6) 	113(10)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H1	(967	4881	4297	67	1

H1A	(1267	4082	2573	43	1

H1B	(929	3553	3542	43	1

H2	(150	3561	2193	41	1

H3A	96	4933	1299	51	1

H3B	(551	5442	1799	51	1

H7A	784	3034	6359	73	1

H7B	1085	1938	6395	73	1

H7C	479	2205	5619	73	1

H8A	1205	1513	4254	70	1

H8B	1891	1400	4912	70	1

H8C	1870	2096	3937	70	1

H9A	2339	3442	5125	68	1

H9B	2282	2713	6066	68	1

H9C	1911	3762	6076	68	1

H1C	1025	8696	4373	71	1

H1D	1399	9300	5261	71	1

H1E	895	8418	5522	71	1

H1F	2686	7610	4215	81	1

H1G	2557	8767	4354	81	1

H1H	2104	8150	3560	81	1

H1I	1858	7705	6589	82	1

H1J	2381	8528	6234	82	1

H1K	2548	7383	6079	82	1

H6	5943	5708	9950	72	1

H1L	5769	6505	8652	50	1

H1M	6088	7426	9254	50	1

H16	4953	7818	8713	44	1

H1N	5350	8108	10657	50	1

H1O	4678	8595	10155	50	1

H2A	2916	6048	7147	72	1

H2B	2983	5191	6326	72	1

H2C	3595	5945	6528	72	1

H2D	3138	3895	8707	69	1

H2E	2771	3798	7622	69	1

H2F	2591	4700	8344	69	1

H2G	4437	4626	6978	79	1

H2H	3896	3768	6765	79	1

H2I	4280	3839	7839	79	1

H2J	2822	6032	13325	176	1

H2K	2456	5158	13908	176	1

H2L	2264	5372	12750	176	1

H2M	3019	3248	13405	497	1

H2N	3068	3358	12209	497	1

H2O	2391	3673	12755	497	1

H2P	3877	5367	13822	266	1

H2Q	4120	4328	13388	266	1

H2R	3612	4361	14304	266	1

Table 6. Hydrogen bonds [Å and °].

D(H···A	d(D(H)	d(H···A)	d(D···A)	((DHA)

O1(H1...N3i	0.82	2.09	2.904(5)	171.4

O1(H1...O3i	0.82	2.60	3.025(5)	113.4

O6(H6...N6ii	0.82	2.08	2.895(6)	173.5

O6(H6...O8ii	0.82	2.55	2.967(5)	112.7

Symmetry transformations used to generate equivalent atoms:

(i) (x,(y+1,(z+1    (ii) (x+1,(y+1,(z+2